Supporting Information

for

A-site order-disorder in the NdBaMn2O5+δ SOFC electrode material monitored in-situ by neutron diffraction under hydrogen flow

## Florent Tonus1, Mona Bahout2*, Vincent Dorcet2, Rakesh K. Sharma3, Elisabeth Djurado3

Serge Paofai2, Ronald I. Smith4, and Stephen J. Skinner1*

1 Department of Materials, Imperial College London, Exhibition Road, London SW7 2AZ, United Kingdom.

2Institut des Sciences Chimiques de Rennes, UMR CNRS 6226, Université de Rennes 1, 263 Avenue du Général Leclerc, 35042 Rennes, France.

3 Univ. Grenoble Alpes, CNRS, G-INP, LEPMI, F-38000, Grenoble, France.

4The ISIS Facility, STFC Rutherford Appleton Laboratory, Harwell Campus, Didcot, OX11 0QX, UK.

Fig. S.I. 1. Fitted room temperature X-ray diffraction pattern of Nd0.5Ba0.5MnO3- phase indexed in Imma (upper markers); lower markers correspond to BaMnO3 secondary phase (~ 8 wt %) indexed in P63/mmc.

.Fig. S.I. 2. Rietveld fits to data collected at 900 °C for 2 hours from the (left) 90 ° detector bank and (right) backscattering-bank. Bragg peaks correspond to NdBaMn2O5 P4/mmm (upper markers) and MnO Fdm (lower markers). The unindexed peak at d ~ 2.5 Å is labelled (*).

Fig. S.I. 3. Rietveld fit to the data collected for 2 h in the 90° detectors after cooling to 65 °C. Bragg peaks correspond to NdBaMn2O5, S.G. P4/nmm (upper markers) and MnO, S.G. Fdm (lower markers). The additional peak likely to arise from crystallization of SiO2 from the quartz tube is labelled (*).

Table S.I. 1. Refined lattice parameters and isotropic atomic displacement parameter (Biso) for Nd0.5Ba0.5MnO3.00 (S.G. Imma) at 20 °C with atoms in the following positions: (Nd,Ba), 4e (0, 1/4, z); Mn, 4b(0, 0, 1/2); O1, 4e(0, 1/4, z); O2, 8g (1/4, y, 01/4), a = 5.503(1) Å, b = 7.7962(4) Å, c = 5.502(1) Å, Vp = 59.01(2) Å3, χ2 ~ 1.92, RB ~ 1.98 %, Rf ~ 4.45%.

| Atom | z or y | Biso (Å2) |
| --- | --- | --- |
| Nd, Ba | 0.0 | 0.56(2) |
| Mn |  | 0.62(3) |
| O1 | 0.470(2) | 2.1(2) |
| O2 | 0.512(1) | 2.5(1) |

Table S.I. 2. Refined structural parameters and anisotropic thermal vibration parameters Bii for Nd0.5Ba0.5MnO2.5 (S.G. Pmm) at T ~ 700 °C 700 °C with atoms in the following positions: Nd,Ba, 1a (0, 0, 0); Mn, 1b (1/2, 1/2, 1/2); O, 3c (0, 1/2, 1/2).

| Atom | B11, B22, B33 (× 103) |
| --- | --- |
| Nd, Ba | 44(1), 44(1) 44(1) |
| Mn | 29(1), 29(1), 29(1) |
| O | 39(2), 154(2), 154(2) |

Table S.I. 3. Refined structural parameters ~and anisotropic thermal vibration parameters Bii at 800 °C for NdBaMn2O5 in space group P4/mmm with atoms in the following positions: Nd, 1a (0, 0, 0); Ba, 1b (0, 0, 1/2); Mn, 2h (1/2, 1/2, z); O1, 1d (1/2, 1/2, 1/2); O2, 4i (1/2, 0, z); a ~ 4.0066(5) Å,  c ~ 7.889(1) Å, χ2 ~ 1.0, RB ~ 4 %, RF ~ 8 %.

| Atom | B11, B22, B33 (× 103) |
| --- | --- |
| Nd | 22(2), 22(2) 5(1) |
| Ba | 27(3), 27(2), 4(1) |
| Mn | 25(2), 25(2), 8(1) |
| O1 | 106(6), 106(6), 4(1) |
| O2 | 41(3), 31(2), 27(1) |

Table S.I. 4. Refined structural parameters and isotropic thermal vibration parameters Biso at 65 °C for NdBaMn2O5 in space group P4/nmm with atoms in the following positions: Nd, 2b (3/4, 1/4, 1/2); Ba, 2a (3/4, 1/4, 0); Mn1(Mn2+), 2c (1/4, 1/4, z); Mn2(Mn3+), 2c (1/4, 1/4, z); O1, 2c (1/4, 1/4, z); O3, 8j (x, x, z); O3, 2c (1/4, 1/4, 1/2). Biso for Mn1 and Mn2 were constrained to be equal.

| Atom | a (Å) | 5.6251(4) |
| --- | --- | --- |
|  | c (Å) | 7.7717(7) |
| Nd | Biso (Å2) | 0.47(4) |
| Ba | Biso (Å2) | 0.56(7) |
| Mn1 | z | 0.258(2) |
|  | Biso (Å2) | 0.31(6) |
| Mn2 | z | 0.756(1) |
| O1 | z | 0.002(3) |
| O2 | x | 0.500(2) |
|  | z | 0.3077(2) |
|  | Biso (Å2) | 1.38(4) |
|  | χ2 | 2.11 |
|  | RB % | 5.42 |