Evolution of structure in the incommensurate modulated LaNb1-xWxO4+x/2 (x = 0.04–0.16) oxide ion conductors

Cheng Li,1,2* Stevin Pramana,1,3 Ryan D. Bayliss,1 Clare P. Grey,4 Frédéric Blanc,4,5 and Stephen J. Skinner1*

1Department of Materials, Imperial College London, Exhibition Road, London, SW7 2AZ, UK

2Jülich Centre for Neutron Science JCNS, Forschungszentrum Jülich GmbH, Outstation at SNS, Oak Ridge, TN 37831-6473, USA

3School of Engineering, Newcastle University, Newcastle upon Tyne, NE1 7RU, UK

4Department of Chemistry, University of Cambridge, Lensfield Road, Cambridge, CB2 1EW

5Department of Chemistry, Stephenson Institute for Renewable Energy, Crown Street, University of Liverpool, Liverpool, L69 3BX

*corresponding authors:

lic1@ornl.gov, tel +1 865 232 8422, address: 8600 Oak Ridge National Laboratory, 1 Bethel Valley Rd, Oak Ridge, TN 37830

s.skinner@imperial.ac.uk, tel +44 (0)20 7594 6782, address: Imperial College London, South Kensington Campus, London SW7 2AZ

# Abstract

Hyper-stoichiometric CeNbO4+d phases demonstrate remarkable oxygen diffusivity and provide an interesting structural template for oxygen ion conductors. Previously, we have reported the room temperature structure of the incommensurate modulated LaNb0.88W0.12O4.06, a structural analogue of CeNbO4+d, and suggested that it is a pure oxygen ion conductor, the anions moving via an interstitialcy mechanism. However, the high temperature structural information for the LaNb1-xWxO4+d (x = 0.04 - 0.16) family, which is key to understanding the structure-property relationship in oxygen ionic conductors with complex structures at operating conditions, is unreported. In this contribution, we address this question by investigating the high temperature structural evolution of the LaNb1-xWxO4+2/x phases using a combination of thermal analysis, scattering techniques and 17O and 93Nb nuclear magnetic resonance spectroscopy. We reveal a series of phase transitions between a modulated monoclinic phase, a high temperature unmodulated tetragonal phase and a high temperature modulated tetragonal phase. These findings are correlated with the ion transport and offer insights into the design of new materials for solid state electrochemical devices.

# Introduction

Discovery and optimization of ionic conducting electrolyte materials is crucial in obtaining solid oxide fuel cells (SOFCs) with lower operation temperature.1–5 The established electrolyte materials are limited to fluorite and perovskite-based systems, which rely on an isotropic, vacancy hopping mechanism facilitated by the cubic or near cubic crystal lattice.1–3

Recent years however have witnessed a growing interest towards complex structures with anisotropic conducting pathways for electrolyte applications. The apatite4,6 and the melilite5,7 family for instance have shown high oxide ion conductivity (~0.001-0.01 S cm-1) in the intermediate temperature range (500-700 °C).

Another family of particular interest is the hyper-stoichiometric fergusonite/scheelite structure which find application in a wide range of electrochemical devices including fuel cells, electrolysers and permeation membranes.8–11 Their unity oxide ionic transfer number, good thermal stability and high total electrical conductivity make them attractive alternatives to conventional materials (for instance, conductivity of σ = 0.042 S cm-1 at 800 °C was reported for the scheelite Pb0.8La0.2WO4+d, comparable to that of the yttria stabilised zirconia, or YSZ, benchmark10,12). One member of the fergusonite/scheelite family, the hyper-stoichiometric CeNbO4+d phases have shown remarkable oxygen diffusivity, D*, in the range of 10-6 cm2 s-1 below 800 °C, about an order of magnitude higher than the YSZ.9,12  Interestingly, a sharp drop in diffusivity was observed on transition from the low temperature monoclinic phase to the high temperature tetragonal phase, highlighting the link between the unique modulated crystal structure and the remarkable oxygen diffusivity in CeNbO4+d phases. Indeed, CeNbO4+d provides an interesting structural template, in which the modulation induced polyhedron distortion is correlated with enhanced oxygen diffusivity.13

We have recently developed materials based on the CeNbO4+d structural template and reported the room temperature structure and transport properties of the hyper-stoichiometric LaNb0.88W0.12O4.06.14 Its room temperature structure has distorted BOx (B = Nb,W) polyhedra, a result of the B site cation ordering, that facilitates the difference in the charge and size between W and Nb. The distorted polyhedra form interconnected slabs along the ac plane,14 while the undoped LaNbO4 parent phase features isolated polyhedra.13

Despite great interest in the conductivity and the diffusion mechanism in LaNb1-xWxO4+x/2 and related compounds,9–18 their high temperature structures have been scarcely investigated. The interplay between phase transition, crystal structure and the ionic conductivity in LaNb1-xWxO4+x/2 has not been established, which is crucial in realizing the potential of the interstitial containing structural template. The discrepancy is likely due to the complex modulated structure, and literature reports often treated the high temperature structure as an unmodulated structure,15,16 and thus risks oversimplifying the structure and missing subtle mechanistic details relating to the oxygen diffusion process.

In this current study, the structural evolution of the LaNb1-xWxO4+x/2 phases were investigated using high temperature diffraction-based techniques and 17O and 93Nb Magic Angle Spinning (MAS) Nuclear Magnetic Resonance (NMR) spectroscopy. Investigation of the high temperature crystal structure allow us to verify temperature stability of the highly defective local structure. Key structural features, including the complex phase transition behaviour of the LaNb1-xWxO4+x/2 series, the distribution of the interstitial oxygen ions and the change in Nb coordination environment, were addressed using thermal analysis, in situ X-ray and neutron diffraction, 17O and 93Nb MAS NMR. The nature of the phase transitions in the LaNb1-xWxO4+x/2 family (x = 0.04 – 0.16), and their relationship to the oxygen ion diffusion process is discussed.

# Experimental

The materials investigated in this work were prepared using solid state synthesis from a stoichiometric mix of La2O3 (99.9%), Nb2O5 (99.9%) and WO3 (99.9%) powders (all from Sigma-Aldrich). Before the synthesis, La2O3 powder was treated at 1000 °C for 10 h to remove moisture and the presence of La(OH)3. All the starting powders were examined with X-ray diffraction (XRD, PANalytical X’Pert Pro MPD, Cu Kα radiation, λ = 1.54056 Å) to confirm phase purity. The powder mixtures were ball milled for 24 h in acetone with zirconia balls to achieve a homogeneous mix. The mixed powders were first calcined under an ambient atmosphere at 1200 °C for 10 h, then crushed, milled and calcined again at 1400 °C for 10 h under ambient air (all heating rate 10 °C/h). Phase purity was verified with XRD after each calcination step which was repeated for 2 to 3 times until no change in phase composition was confirmed. 17O enriched LaNbO4 and LaNb0.86W0.14O4+d samples were prepared by heating the as-synthesised LaNbO4 and LaNb0.86W0.14O4+d in a quartz tube under 60 % 17O enriched O2 gas (Isotec, used as received) at 1000 °C in a tube furnace for 24 hours.

Thermogravimetric analysis (TGA) measurements were conducted using a Netzsch STA 449C Jupiter heat flux instrument. Approximately 50 mg of sample was loaded into a Pt crucible and the TGA measurements were performed under static laboratory air over the temperature range of room temperature to 950 °C with a heating rate of 10 °C/min. The instrument was calibrated by measuring the empty sample environment under the same experimental conditions. Sintered, rectangular-bars with the approximate dimension 4 mm × 4 mm × 25 mm were used for dilatometry measurements, to determine the thermal expansion of the materials (Netzsch DIL 402 E dilatometer). The samples were prepared using a uniaxial press at 150 MPa followed by an isostatic press at 300 MPa for 1 min. Samples were sintered at 1400 °C for 10 h, with 10 °C/h ramp rate, and reached more than 95% density. An alumina rod reference was used to calibrate the instrument prior to sample measurement. Measurement were carried out from room temperature to 800 °C with a heating rate of 10 °C/min.

In situ neutron scattering measurements were performed at the High Resolution Powder Diffractometer (HRPD, ISIS, Rutherford Appleton Laboratories, UK). Approximately 10 g of sample was placed inside a quartz ampoule heated in a vanadium furnace. Diffraction patterns were gathered from 500 °C to 800 °C with 50 °C interval, under static air. Datasets from the high-resolution backscattered bank (2θ ≈ 145°) in the range of 2.6 Å ≥ d-spacing ≥ 0.9 Å were used for the structure refinement. In-situ high temperature XRD (HTXRD) data were measured using a PANalytical X'Pert diffractometer (Cu Kα1 radiation with λ = 1.54056 Å) fitted with Bühler HDK 2.4 high-temperature chamber. Samples were placed on a Pt heating strip whose temperature was controlled with joule heating. Diffraction patterns were collected from room temperature up to 800 °C with the heating rate set to 60 °C/min and a hold time of 1 min. The actual temperature of the Pt strip was calibrated by refining the lattice parameter of the Pt. All the crystal structures were refined using JANA2006.19

17O NMR experiments on 17O enriched samples were carried out on a 16.4 T Bruker Avance III spectrometer. All one-dimensional spectra were obtained with a rotor synchronized Hahn echo pulse sequence experiment with one rotor period as a dephasing delay. All isotropic resonances have been identified by recording the 17O NMR spectra at two different magic angle spinning (MAS) rates minimum. Experiments in the 22 – 140 °C temperature range were performed with a Bruker 3.2 mm HXY triple-resonance MAS probe (in double resonance mode) tuned to 17O at 0(17O) = 94.96 MHz. 1D spectra were obtained with π/2 pulse length of 1.7 μs at a radio frequency field (rf) amplitude of 1(17O) = 50 kHz. Two-dimensional triple-quantum (TQ) MAS experiments were performed with a z-filter pulse sequence.20,21 120 and 720 scans were averaged for each of 38 and 25 t1 points, incremented by 70.83 s, for 17O enriched LaNbO4 and LaNb0.84W0.16O4.08 respectively. Hard and soft pulses were performed at rf fields of ~ 80 kHz and ~ 8 kHz, respectively. All the samples were packed in ZrO2 rotors and spun at a spinning frequency of r = 20 kHz. Temperature calibration of the probe was performed in separate MAS experiments using the 207Pb resonance of Pb(NO3)2.22 The sample temperatures quoted subsequently have all been corrected according to this calibration and have an accuracy of ± 5 °C. Experiments at 270 °C were performed with a Bruker 4 mm X single-channel MAS probe tuned to 17O at 0(17O) = 94.96 MHz. 1D spectra were obtained with π/2 pulse length of 1.7 μs at a rf field of 1(17O) = 50 kHz. All the samples were packed in ZrO2 rotors and spun at a spinning frequency of r = 14 kHz. Temperature calibration of the probe was performed in separate MAS experiments using the 79Br resonance of KBr.23 The sample temperatures quoted subsequently have all been corrected according to this calibration, and have an accuracy of ± 5 °C. Experiments above 270 °C were performed with a Bruker 7 mm HX laser heated24.  MAS probe tuned to 17O at 0(17O) = 94.96 MHz. 1D spectra were obtained with π/2 pulse length of 3.3 μs at a rf field of 1(17O) = 25 kHz. All the samples were packed in BN containers and spun at a spinning frequency of r = 14 kHz in ZrO2 rotors. Temperature calibration of the probe was performed in separate MAS experiments using the 79Br resonance of KBr. The sample temperatures quoted subsequently have all been corrected according to this calibration, and have an accuracy of ± 10 °C with a temperature gradient across the BN sample holder of ~ 30 °C.

93Nb NMR experiments were performed on a 20 T Bruker Avance II spectrometer using a Jeol double resonance 1 mm HX probe tuned to 0(93Nb) = 207.90 MHz and under MAS at a spinning frequency of r = 78 kHz with recycle delays of 0.1 s. One-dimensional spectra were obtained with a pulse acquire sequence experiment using selective π/2 pulse length of 2.5 μs at a rf field of 1(93Nb) ~ 20 kHz and satisfying the weak rf regime irradiation condition. All the samples were packed in ZrO2 rotors. TQ MAS experiments were performed with a z-filter pulse sequence and 20480 scans were averaged for each of 32 t1 points. Hard and soft pulses were performed at rf fields of ~ 100 kHz and ~ 20 kHz, respectively. The 93Nb isotropic chemical shifts and quadrupolar products were obtained from the center of gravity of the NMR lines in the TQ MAS data according to the literature.25,26 Previous work identifying links between 93Nb parameters and local structure was used for tentative spectral assignments.27–30

All 17O shifts were externally referenced to water at 0.0 ppm. All 93Nb shifts were externally referenced to LiNbO3 at the center of gravity of the line at – 1003 ppm (from the known isotropic shift of this phase of – 988 ppm30 and a quadrupolar-induced shift31 calculated to be 15 ppm at the 20 T magnetic field used for 93Nb) which corresponds to the primary reference of saturated K[NbCl6] in CH3CN at 0 ppm. NMR data were processed using the MatNMR package implemented within MatLab.

# Results and discussion

## Thermal analysis

### Thermogravimetric Analysis (TGA)

The mass change of the LaNb1-xWxO4+x/2 (x = 0.04 – 0.16) series, measured from room temperature to 900 °C, is plotted in Figure 1 and shows no significant weight change from room temperature up to 900 °C. A small drift of about 0.1% weight change up to 900 °C is seen in all measurements, which is mostly likely associated with instrumental effects. A weight loss of about 0.15% was observed for LaNb0.96W0.04O4.02 upon heating (<50 °C) which is likely due to the loss of adsorbed water. The observation is in direct contrast to the CeNbO4+d system which sees a wide range of oxygen stoichiometry during heating.32 Overall the TGA measurements suggest no detectable change in sample mass from room temperature to 900 °C, indicating good thermal stability and a stable valence state of W6+.

Figure 1: TGA measurement of various LaNb1-xWxO4+x/2 (x = 0.04 – 0.16) samples from room temperature to 800°C under laboratory air. The data for CeNbO4 from Skinner and Kang is listed for comparison32.

### Dilatometry

Dilatometry curves of the LaNbO4 reference, as well as the W doped LaNb1-xWxO4+x/2 compositions, recorded in the temperature range from 200 °C to 900 °C, are shown in Figure 2. For the undoped LaNbO4, two distinct regions, corresponding to the low temperature monoclinic phase and the high temperature tetragonal phases respectively, are well separated. A sharp decrease in the thermal expansion rate was observed and is attributed to the monoclinic (m) to tetragonal (t) phase transition.33 The phase transition temperature was determined by first extrapolating the linear part of the expansion curve (the red lines in Figure 2a), and then finding the intersection between the low and high temperature regions. The phase transition temperature (Ttr, reported in Table 1) was estimated to be 490 ± 10 °C for the undoped LaNbO4 which is in good agreement with the literature.33,34

Figure 2: Dilatometry curves show the length change and the linear expansion rate as a function of temperature for (a) LaNbO4 and various LaNb1-xWxO4+x/2 compounds with (b) x = 0.08 (c) x = 0.12 and (d) x = 0.16. The phase transition in LaNbO4 was determined from the intercept of the linear part of the expansion curve, highlighted by the red lines in (a).

The thermomechanical behaviour of LaNb1-xWxO4+x/2 compositions, however, is more complicated; instead of a sudden decrease of the thermal expansion rate approaching the phase transition, the change in LaNb0.92W0.08O4.04 and LaNb0.88W0.12O4.06 was less abrupt (Figure 2b and c). For samples with 8 at% to 12 at% W dopant, the thermal expansion rate increased gradually before reaching a transition point, after which a slow decrease in the expansion rate was observed. Such a transition was absent in LaNb0.84W0.16O4.08 (Figure 2d). The thermal expansion coefficients (TECs, reported in Table 1), before and after the transition, were obtained by averaging the length change of the samples over the respective temperature regions. Comparing with the LaNbO4 parent phase, the W dopant reduces the discrepancy in TEC between the low and high temperature regions (reported in Table 1). For fuel cell applications, a sudden change in TEC promotes mismatch between the electrolyte and electrode during the start-up stage and thus often leads to mechanical failure;35 dilatometry results therefore suggest improved mechanical stability of the LaNb1-xWxO4+x/2 electrolyte with W substitution. In addition, the TEC of the LaNb1-xWxO4+x/2 phases are higher than the conventional electrolyte (i.e. the TEC of Ce0.9G0.1O2-d is ~12 × 10-6/K from room temperature to 800°C36) and has a closer match with conventional electrodes such as La0.6Sr0.4Co0.2Fe0.8O3-d (LSCF) of 16.6 × 10-6/K from room temperature to 650 °C37 indicating that the LaNb1-xWxO4+x/2 phases have suitable mechanical properties to function in fuel cells.

Table 1: Thermal expansion coefficients of the LaNbO4 and various LaNb1-xWxO4+x/2 compositions determined from dilatometry measurements shown in Figure 2.

| Composition | TEC high temperature (10-6/K) | TEC low temperature (10-6/K) | Ttr (°C) | references |
| --- | --- | --- | --- | --- |
| LaNbO4 | 17.3 | 9.3 | 490 ± 10 | this work |
|  | 17.3 | 7.1 | 510 ± 10 | 11 |
|  | 14.0 | 8.4 | 504 ± 10 | 12 |
| LaNb0.92W0.08O4.04 | 17.5 | 12.7 | 468 ± 5 | this work |
| LaNb0.88W0.12O4.06 | 16.2 | 13.1 | 669 ± 5 | this work |
| LaNb0.84W0.16O4.08 | 14.5 |  | - | this work |

## High Temperature XRD of the LaNb1-xWxO4+x/2 (x = 0.04 – 0.16) series

The evolution of the structure and the phase transition of LaNb1-xWxO4+x/2 (x = 0.04–0.16) materials from room temperature to 850 °C was investigated using in situ high temperature X-ray diffraction. The complexity of the phase transition behaviour is well illustrated by the LaNb0.88W0.12O4.06 composition (Figure 3): at room temperature, this composition has a (3 + 2)D modulated structure, with a monoclinic parent phase, indicated by the satellite peaks in the diffraction pattern. Increasing the temperature lowers the intensity of these satellite peaks. At 500 °C, the modulation reflections (the position of the modulation peak with the highest intensity is marked with an arrow in Figure 3) were still observable, whereas the parent structure seems to have transformed to tetragonal symmetry. In situ neutron diffraction data indicate that the satellite peaks become indistinguishable from the background between 650 °C and 800 °C (Figure S1 & S2 in the supporting information). At 800 °C an unmodulated high temperature tetragonal phase formed, similar to the high temperature parent structure of LaNbO4.

Figure 3: Selected high temperature XRD patterns for the LaNb0.88W0.12O4.06 phase; the position of the satellite reflection with highest intensity is highlighted by the arrow.

The lattice parameters of the LaNb0.88W0.12O4.06 composition, obtained using the Le Bail method, are plotted in Figure 4. The subscript “m” and “t” indicate the monoclinic and tetragonal structure respectively. The bm axis was chosen as the unique axis for the monoclinic phase which coincides with the ct axis in the tetragonal unit cell. This choice of unique axes is consistent with the previous report, and aims to avert confusion.38 Approaching the phase transition temperature, Ttr, am decreases while cm increases, resulting in the merging of the monoclinic symmetry-related peaks in the XRD pattern consistent with a transformation to tetragonal symmetry. The bm increases almost linearly with temperature, while the β angle decreases gradually and becomes 90° above the transition temperature.

Figure 4: Refined lattice parameters (a) and cell volume (b) of the LaNb0.88W0.12O4.06 composition as a function of temperature from the X-ray data shown in Figure 3. Error bars are smaller than the symbols. The subscripts “m” and “t” refer to the monoclinic and tetragonal structures respectively.

The m to t transition temperature of the parent phase varies with the W dopant concentration. For instance, neutron scattering data indicates that increasing the dopant level (W = 16 at%) sees a tetragonal-monoclinic mix at room temperature, where the tetragonal phase dominates (Figure S3&S4), whereas the x = 0.04 composition has a phase transition temperature closer to the undoped LaNbO4 phase (Figure S5). Based on the HTXRD data at least three phases, namely a modulated monoclinic phase, a modulated tetragonal structure and an unmodulated tetragonal phase, have been identified.

## In situ neutron scattering of LaNb1-xWxO4+x/2

### In situ neutron scattering of LaNb0.88W0.12O4.06

The HTXRD study clearly identified various structural polymorphs, although detailed structural information, such as atomic position, especially the interstitial position, could not be obtained due to the limitations of instrument resolution and insensitivity to oxygen scattering. The structure of LaNb0.88W0.12O4.06 was therefore examined using in situ high-resolution neutron scattering, in the temperature range 500 °C to 800 °C. This temperature range is of interest as the HTXRD result hinted at a phase transition between a modulated and an unmodulated tetragonal phase.

The neutron scattering pattern of LaNb0.88W0.12O4.06 recorded at 500 °C in static air was first refined with only the unmodulated scheelite phase (I41/a, space group 88). Site occupancy of all the elements were fixed according to the nominal composition when refining the lattice parameter, atomic position and atomic displacement parameters (ADP). Constraints on the occupancy were released in the final refinement, although the Nb/W ratio was still fixed at 88 at%/12 at% at the B site. No significant deviation from ideal stoichiometry was observed and therefore nominal stoichiometry was used for the subsequent data analysis. The refinement of the parent structure finally converged to Rp = 0.028 and Rwp = 0.032. Visual inspection of the refined pattern however revealed additional peaks (insert in Figure S6), whose position coincides with the satellite reflections, therefore confirming the presence of superstructure at elevated temperature. These peaks were not observed by the in-house HTXRD and are possibly related to long-range oxygen ordering. The structural modulation had to be addressed before the interstitials could be investigated as both superstructure and the interstitial content contribute to the observed intensity at the peak position in the parent phase.39

To refine the modulated structure, the superspace group (SSG) I41/a(α, β, 0)00(-β, α, 0)00 was used, based on the space group of the parent structure. There were other SSGs available which are derived from same parent group however the other choices all have a modulation component along the unique axis (ct), which is inconsistent with the modulation waves in the low temperature structure.40 The chosen SSG was also used in the literature to refine the (3 + 2)D modulated Na2/7Gd4/7MoO4 scheelite41 and CaEu(MoO4)4.42

Figure 5: Rietveld refinement of neutron powder scattering data of the LaNb0.88W0.12O4.06 composition recorded at 500 °C using the SSG I41/a(α, β, 0)00(-β, α, 0)00. Improved fitting with Rp = 0.022 and Rwp = 0.023 were obtained, by including the structural modulation in the model. Black, red and blue lines show the experimental data, modelled data and the difference plot respectively. The black ticks mark the theoretical Bragg peak position. The inset shows the enlarged pattern in the d-spacing of 0.84 Å to 1.40 Å range.

Table 2: Summary of the experimental conditions for the in situ neutron data of LaNb0.88W0.12O4.06 at 500 °C

Composition; LaNb0.88W0.12O4.06. Space group; I41/a(α, β, 0)00(-β, α, 0)00. Temperature; 500 °C. a b c (Å); 5.37466(8) 5.37466(8) 11.72917(18). V (Å3); 338.821(9). modulation waves; q1 = 0.3033(3)a* + 0.1177(4)b*. q2 = -0.1177(4)a* + 0.3033(3)b*. data collection. instrument; HRPD at ISIS. data range; d = 2.5889 Å to 0.8696 Å. resolution; Δd/d = 4x 10-4. Reflections (all/observed); 1173/758. among them,. Main Reflections (all/observed); 119/9. 1st order (all/observed); 1045/639. R, Rw for Bragg reflections (Rall); 7.2%, 5.9%. among them,. Main Reflections (R, Rw); 3.7%, 4.1%. q1 1st order (R, Rw); 12.3%, 6.5%. q2 1st order (R, Rw); 11.7%, 6.6%. Rp, Rwp; 2.2%, 2.3%.

To refine the modulated phase, the q modulation vectors and the Fourier magnitudes of the low temperature LaNb0.88W0.12O4.06 structure was used as the input for the subsequent refinement. Only first order modulation waves were refined as most higher order reflections had intensity lower than the 3σ detection limit. Nb and W were set to have identical fractional coordinates, ADP and displacive modulation amplitude were refined based on the site and geometry constraints. The magnitude of the modulation waves was initially fixed at 0.2, which was later released during the final stage of the refinement. The 748 observed peaks allowed the refinement of 33 independent parameters, including the anisotropic displacement parameters. The refinement finally converged with Rp = 0.022 and Rwp = 0.023. The refined pattern is shown in Figure 5, and the experimental parameters, the refined atomic positions and the modulation magnitude are summarized in Tables 2-4 respectively.

Table 3: Summary of the refined atomic parameters of the average structure reported in Figure 5. Occ.; x; y; z; U11; U22; U33; U12; U13; U23. La; 0.997(12); 0; 0.25; 0.625; 0.0397(12); 0.0397(12); 0.0176(13); 0; 0; 0. Nb/W; 0.88/0.12; 0; 0.25; 0.125; 0.0356(14); 0.0356(14); 0.0390(01); 0; 0; 0. O; 1.005(8); 0.2407(4); 0.0910(3); 0.0414(2); 0.0544(14); 0.0690(01); 0.0382(10); 0.0150(1); 0.0088(11); 0.0230(13). Cation site; Bond length (Å); Bond valence sum (BVS). La; 2.503(2) Å × 4, 2.546(2) Å × 4; 3.1(1). Nb/W; 1.835(2) Å × 4, 2.973(2) Å × 4; 5.0(1). Table 4: Refined Fourier magnitudes for the LaNb0.88W0.12O4.06 phase at 500 °C. site; x; y; z. La; position; 0; 0.25; 0.625. s,1a; 0; 0; -0.0030(7). c,1; -0.0123(15); 0.0220(11); 0. s,2; 0; 0; 0.0032(6). c,2; 0.0220(11); -0.0123(15); 0. Nb/W; position; 0; 0.25; 0.125. s,1; 0; 0; 0.0088(8). c,1; -0.0076(16); 0.0218(13); 0. s,2; 0; 0; -0.0088(8). c,2; -0.0218(13); -0.0076(16); 0. pc1, pc2b; -0.25(6), -0.25(6). O; position; 0.240(1); 0.092(3); 0.042 (1). s,1; -0.0008(18); 0.0043(16); 0.0031(7). c,1; -0.0022(19); 0.0334(15); 0.0036(7). s,2; -0.0001(15); -0.0040(2); -0.0034(7). c,2; -0.0289(13); -0.0143(19); 0.0021(8). Distance (Å); average; min; max. La-O; 2.533; 2.462; 2.572. Nb-O; 1.832; 1.772; 1.902. a s, c stands for Fourier magnitude of sin and cos wave respectively; the number describes the wave vectors: the 1st wave is along q1 direction and the 2nd wave is along q2 direction. b p = p0+pc1cos2πt+pc2cos2πu, in which po is the site occupancy of the parent structure. pc1, pc2 are the Fourier magnitude for the occupational waves; t,u are the coordinates in the internal axes; both the Fourier magnitude of the displacive and the occupational waves. The slightly negative occupancy might be related to the choice of wavefunction, similar to that reported in ref14,41

The nuclear density and the residual density maps, in the vicinity of the Nb and La sites, were examined (Figure 6). Overall, the residual density is about 1–2% of the observed density, indicating good fitting quality.

Figure 6: Observed nuclear density maps in the vicinity of (a) La and (b) Nb; and the corresponding difference nuclear density maps in (c) and (d), as a function of the internal coordinates. The contour in (a) and (b) is 2 fm Å-3 whereas in (c) and (d) is 0.2 fm Å-3. Overall a residual level approximately 1-2% of the observed nuclear density was registered.

When refining the structural model with data gathered at 650 °C, the fitting parameters improved little with the inclusion of structural modulation (Rwp from 0.024 to 0.023, Figure S1). Unresolved intensity, such as the features between 1.19 Å and 1.27 Å, was observed. These modulation peaks become quite broad with increasing temperature (Figure S2) and potentially correspond to a partially ordered local structure and mark the transition between the modulated structure and disordered tetragonal parent phase. Closer examination of the local structure however is necessary to verify the existence of any intermediate phase. The degradation in the signal to noise ratio makes fitting with the modulated structural model less reliable; the refinement was nevertheless attempted using a (3 + 2)D structural model for the 650 °C pattern and the fitting is reported in the supplemental information (Figure S1). Increasing the temperature sees further reduction of the peak intensity, and no satellite reflections were observed at 800 °C. The high resolution neutron scattering data is in good agreement with the HTXRD (Figure 3), and confirmed a modulated phase at 500 °C, which gradually transforms into the disordered high temperature tetragonal parent phase.

### In situ neutron scattering of LaNb0.84W0.16O4.08

The same procedures as described in the previous section were used to refine the structure of LaNb0.84W0.16O4.08. Unlike the LaNb0.88W0.12O4.06 composition, which goes through a phase transition from a modulated structure to an unmodulated structure between 650 °C to 800 °C, neutron scattering data confirmed that the LaNb0.84W0.16O4.08 composition maintains its modulated structure up to 800 °C. All the diffraction patterns could be refined using the same I41/a(α, β, 0)00(-β, α, 0)00 SSG. In Figure 7, the data recorded for the LaNb0.84W0.16O4.08 phase at 800 °C is shown with the fit to the model, highlighting the stability of the structural modulation.

Figure 7: Rietveld refinement of neutron powder diffraction data for LaNb0.84W0.16O4.08 recorded at 800 °C, using the SSG I41/a(α, β, 0)00(-β, α, 0)00. Good fitting with Rp = 0.022 and Rwp = 0.023 were obtained. Black, red and blue lines show the experimental data, modelled data and the difference plot respectively. The black and red vertical lines mark the theoretical peak position of the parent structure and the modulated peaks respectively. The inset shows the enlarged pattern in the 0.84 Å to 1.40 Å range.

When refining the occupational magnitude of W/Nb, the occupational wave magnitude used that of the x = 0.12 composition as an input. The refinement showed little improvement of the fitting (Rp changed from 0.022 to 0.0217), while a large negative occupancy (<-0.8) in the t-u section was observed, making the model physically unrealistic. The occupational modulation therefore was fixed at 0.2 and -0.2 respectively for Nb and W for the refinement of the entire neutron scattering dataset for the x = 0.16 composition. Data with higher quality (preferably single crystal diffraction data), is required to allow for higher order modulation waves to provide an accurate description of the cation ordering.

### Interstitial position in LaNb0.84W0.16O4.08

The role of the interstitial oxygen ion in the conduction process in the hyper-stoichiometric scheelite related compositions has been highlighted with previous experimental10,43 and DFT atomic simulation.15 While the correlated interstitialcy diffusion is said to be responsible for the long-range oxygen transport in the hyper-stoichiometric scheelite compounds,15 the interstitial oxygen position in these compounds has been elusive. Indeed, no specific site was identified when examining the difference density map of the LaNb0.84W0.16O4.08 at 500 °C in our study: the observed residual density is at the same level as the negative density, and was therefore ascribed to noise (Figure S8).

In fact, the reported interstitial positions in the hyper-stoichiometric scheelite structures are scattered due to high oxygen mobility coupled with the low interstitial concentration.43 For instance, when studying the modulated CeNbO4+d phases, Thompson et al. suggested that the interstitial occupied the empty eight-coordinate site, at (0, 0.25, 0.375), which leads to minimal disturbance to the neighbouring ions.44 (marked by red spheres in Figure 8). A different Wyckoff  8e position  in I41/a space group at (0, 0.25, 0.325) was predicted in La doped PbWO4 by Takai et al.43 The authors pointed out that the refined occupancy is only 1/3 of the expected value, and suggested that the interstitial could occupy other 8e positions with varied z coordinate (along the arrow direction shown in Figure 8). Most recently, Pramana et al.13 proposed the location of oxygen interstitial not at a specific crystallographic position in the parent structure, but at normal lattice oxygen site in an expanded unit cell. Both the “interstitial” and lattice oxygen cooperatively contribute to diffusion. The structure is therefore better described as Ce12Nb12O51, indicating little difference between the lattice and the “interstitial” oxygen.13

Refinement of the interstitial position in LaNb0.84W0.16O4.08 was attempted following the methodology proposed in ref,43 which assumed an interstitial locating at (0, 0.25, z), however no satisfactory result was obtained. The constraints on the interstitial position were later released, and the refinement converged with the interstitial oxygen ion occupying the (0.274, 0.104, 0.223) general position. However, the refinement returned a large negative occupancy which indicates a false local minimum and was therefore discarded.

Figure 8: Proposed interstitial (shown as red spheres) positions in LaNb0.84W0.16O4.08 based on ref.30 and 28. The green sphere represents La3+ ion whereas the Nb/W atoms are shown in the polyhedral form. The interstitial is assumed to be located along (0, 0.25, z), shown by the black arrow.

It is possible that the interstitial oxygen assumes a rather diffuse distribution in the LaNb0.84W0.16O4.08 system at 500 °C and the oxygen ions are delocalized along the conducting pathway leading to a reduced occupancy at any particular crystallographic site, and thus minimal residual density. Alternatively, the interstitial might be modulated due to the cation ordering, as the ordering of the anion network is expected from the cation ordering.5,13,45,46

In both cases, a diffuse distribution of the interstitial oxygen is predicted. Such prediction is consistent with most recent reports on apatite-type germanates,6,47,48 which showcased the oxygen interstitial delocalised along the diffusion migration pathway. There have been earlier reports on the apatite,4 melilite49 and fergusonite/scheelte15,43,50 which predicts localized interstitial sites. Although these reports focus on the structure at room temperature whereas the mobility of oxygen is expected to increase with increasing sample temperature as suggested by the high temperature 17O NMR data of LaNb0.84W0.16O4.08 (see below). It should also be recognized that charge compensation with A and B site vacancies is possible which would further reduce the interstitial content in LaNb1-xWxO4+x/2.51 Further experimental and simulation studies however are required to thoroughly investigate the “interstitial” oxygen distribution in the LaNb1-xWxO4+x/2 structure.

## Observation of Nb environment with coordination larger than four

A number of 93Nb solid state NMR studies have identified trends linking the 93Nb parameters with niobium coordination number and other structural parameters,27–30 as for many other nuclei and cations (for example, 27Al),52 and is exploited here to probe the local structure of Nb in LaNb0.92W0.08O4.04. Although the 93Nb nucleus is very receptive owning to its large gyromagnetic ratio and 100% natural abundance, its large quadrupolar moment introduces a dominant 2nd-order quadrupolar broadening of the central transition. This can be reduced to provide improved resolution by using very high magnetic fields and applying very fast MAS rates and all 93Nb spectra in this work were obtained at 20 T under MAS at 78 kHz.

The one dimensional 93Nb spectrum of LaNbO4 is given in Figure S9a, and displays the expected broad and complex pattern which is in fair agreement with the simulated spectrum obtained by using known NMR parameters obtained from a comprehensive multi magnetic field strengths study under non spinning conditions.30  The TQMAS spectrum of this phase (Figure S9a) reveals a single niobium crystallographic site at a shift of ~ -1200 ppm and a TQMAS shift of ~ -640 ppm (Figure 10) that yields an isotropic chemical shift of ~ -850 ppm, in agreement with the literature value of  -853 ppm30 and a coordination number of 4 for Nb.

Figure 10: Projection of the isotropic dimension of the 93Nb TQ MAS NMR spectrum of LaNbO4 and LaNb0.92W0.08O4.04 (Figure S9) obtained at room temperature at 20 T and under a MAS rate of 78 kHz. The position of the Nb site in tetrahedral symmetry (NbO4) and tentatively attributed to niobium environment (NbO4+y, y > 1) with coordination larger than four are also show.

The 93Nb very fast MAS NMR spectrum of LaNb0.92W0.08O4.04 (Figure S9b) shows multiple overlapping peaks in the -500 -1600 ppm region with fewer spinning sidebands than LaNbO4. Interestingly, the 93Nb TQMAS spectrum demonstrates that in addition to the 4-coordinated niobium site present in LaNbO4 (observed here at an isotropic chemical shift of ~ -780 ppm in agreement with the -714 and -853 ppm range expected for NbO4 polyhedral found in the literature27–30), a second site with a highly distorted lineshape close to axial symmetry can be observed with a TQMAS shift of ~ -1100 ppm (Figure 10) at an isotropic chemical shift of ~ -1100 ppm. Importantly, the lower shift of this resonance than for the 4-coordinated niobium site, supported by the known general trend for the 93Nb shifts to decrease with increasing niobium coordination numbers27–30, would suggest that this signal corresponds to a coordination number larger than 4 and may therefore be tentatively ascribed to niobium environments near interstitial oxygen ions, possibly in five- or six-coordinated niobium polyhedra.

## Phase diagram of the LaNb1-xWxO4+x/2

Based on the analysis presented so far, the Nb rich corner of the LaNbO4-LaWO4.5 phase diagram is tentatively proposed in Figure 11. The solid lines in the phase diagram indicate the single-phase boundary; the dotted line separates the monoclinic and tetragonal parent phase, whereas the dashed line is the boundary between the modulated structure and the unmodulated structure. The peak temperatures of the thermal expansion rate from the dilatometry measurements (Figure 2) are also marked on the phase diagram.

Figure 11: Proposed phase diagram of the LaNb1-xWxO4+x/2 system, highlighting the complexity of the system. The solid lines signify the boundaries between a biphasic region and the single-phase region. The dotted line is based upon the transition temperature reported in Table S1 and separates the phases with monoclinic and tetragonal parent structures; the dashed line marks the separation between the modulated phases and the unmodulated structure. All lines are guides for the eye. The “peak” temperatures from the expansion rate reported in Figure 2 are marked as “x” on the proposed phase diagram.

The first interesting observation in this phase diagram is the correlation between the “peak” temperature during dilatometry and the phase transition temperature obtained from diffraction. For instance, the expansion rate of the LaNb0.88W0.12O4.06 composition first peaked at ~390 °C and later at ~670 °C (Figure 2c), which corresponds well with two-phase transition of the x = 0.12 composition. In addition, no abrupt change of shrinkage rate was observed in the LaNb0.84W0.16O4.08 composition (Figure 2d), which coincides with the absence of a phase transition in this composition. Such correlation however is missing in LaNb0.92W0.08O4+d, as the dilatometry peak temperature is about 50-70 °C below the modulated to disordered transition. Still, it is not unreasonable to assume that the modulated to disordered phase transition would affect the thermal expansion of the material. As demonstrated earlier14, the Nb/W-O local environment of the modulated LaNb0.88W0.12O4.06 phase differs significantly from its parent structure.

When varying the temperature, both the magnitude and the direction of the q vectors are expected to change,53 leading to variations of bond lengths and bond angles in addition to the thermal effect. The accumulation of the change would, on a macroscopic scale, perturb the expansion rate. In analogy to the ferroelastic to paraelastic transition of the parent LaNbO4 structure, it is logical to assume that the impact of modulation on the linear expansion rate will be at an extremum when the order-disorder transition occurs. Indeed, the peak temperatures of the dilatometry seem to coincide with the transition temperatures between the modulated structure and unmodulated structure in LaNb1-xWxO4+x/2 (Figure 11); it is therefore speculated that the removal of the structural modulation would introduce a subtle change in the expansion behaviour; however further experiments are required to verify this conjecture.

Theories of the modulated phase transition have been devised to explain the transition between the high temperature incommensurate phase and the low temperature commensurate structure (normally referred to as the “lock-in phase”, often observed below room temperature)54–56 and have provided great assistance in understanding the phase transition in structures with charge density wave ordering and magnetic ordering.57–59 However, the phase transition in modulated structures at elevated temperature has been overlooked. The proposed phase diagram highlights the complexity of structural variation in the modulated system and calls for future investigation.

## Capturing the local oxygen structure with 17O MAS NMR spectroscopy

17O solid state NMR was used to provide further insights into the local oxygen environment and the oxide ion mobilities of these complex crystal structures. Due to the very low natural abundance of 17O (0.037 %), the only NMR active isotope of oxygen, both LaNbO4 and LaNb0.84W0.16O4.08 samples were enriched in 17O by a gas solid exchange reaction with 17O enriched O2 gas at 1000 °C prior to acquisition of the 17O NMR data. The XRD powder patterns (Figure S10) are similar to the ones obtained for the parent LaNbO4 and LaNb0.84W0.16O4.08 materials showing that the additional heat treatment in the 17O gas at 1000 °C did not affect the crystal structures.

The 17O MAS NMR spectrum of 17O enriched LaNbO4 is shown in Figure 12 (and Figure S11 for full spectral width) and displays two well separated resonances at 442 (~1.5 kHz broad) and 564 (~1.3 kHz) ppm with an approximately 1:1 intensity ratio (along with a number of spinning sidebands arising from the satellite transitions of this spin 5/2 nucleus), in agreement with the two oxygen crystallographic sites O1 and O2 in monoclinic LaNbO4. The shorter bond distance between Nb and O2 (1.844 Å) than between Nb and O1 (1.903 Å) yields a larger chemical shielding surrounding the O2 sites than for the O1 sites and therefore a smaller shift of the O2 site (442 ppm) than for the O1 sites (564 ppm). The 17O TQMAS experiment21  (which enables isotropic spectra, i.e. free of anisotropic broadening, of quadrupolar nuclei such as 17O to be obtained) is given in Figure 13 and allows isotropic chemical shift values of 442 and 564 ppm for the O2 and O1 oxygen sites to be determined. These values are identical to the resonance peak positions given above, implying that virtually no quadrupolar couplings are present and demonstrating that the NMR lines are dominated by chemical shift interactions and not second-order quadrupolar broadenings as anticipated for ionic solids. In this case, the spinning sideband envelope spreads over approximately 3000 ppm (or 270 kHz at 16.7 T) at room temperature and reflects the large 17O chemical shift anisotropy (and estimated to be ~ - 1300 ppm).

The high temperature MAS 17O NMR spectra are presented in Figure 12 and were obtained under different MAS rates as different NMR probes were used depending on the required temperature and the MAS NMR probe capabilities (see experimental section for further details). Upon increasing the temperature to about 500 °C under MAS, both Nb-O1 and Nb-O2 resonances of monoclinic LaNbO4 phase converge almost linearly (at a rate of ~0.07 ppm/°C for Nb-O1 and ~0.14 ppm/°C for Nb-O2) towards a value of ~520 ppm (close to the average shift value for the Nb-O1 and Nb-O2 peaks at 503 ppm). Extrapolation of the data between room temperature and 500 °C yields an anticipated convergence to occur at ~560 °C which is in agreement with the 17O MAS NMR spectrum collected at 605 °C that reveals a single broad resonance at ~515 ppm (with a spinning sideband manifold covering ~1200 ppm). This temperature-dependent gradual change of the NMR shifts in monoclinic LaNbO4 is induced by the second-order phase transition between the low temperature monoclinic and high temperature tetragonal phase in rare earth niobates (about 495-520 °C in LaNbO4).60 The observation of a single 17O resonance at 605 °C is in agreement with the unique crystallographic oxygen site of the tetragonal phase.

Figure 12: Variable temperature 17O MAS NMR spectrum of (a) 17O enriched LaNbO4 and (b) 17O enriched LaNb0.84W0.16O4.08 obtained at 16.4 T. The samples temperatures are given next to each spectrum. The MAS rate r was 22, 14 and 4 kHz in the 22-140 °C, 270 °C and 398-605 °C temperature range, respectively (see the experimental section for further details). In (b), the lower MAS rate used to record the spectra above 300 °C explains the broadening of the spectra above its temperature due to the overlapping of the central transition with the spinning sidebands. The isotropic resonances are marked with # and + in monoclinic LaNbO4 (for O2 and O1, respectively), § in tetragonal LaNbO4 and | in LaNb0.84W0.16O4.08. Symbol ‘ indicates natural abundance 17O signal from the ZrO2 rotor (around 380 ppm).52 All other peaks are spinning sidebands.

Figure 13: 17O Triple Quantum MAS NMR spectrum of (a) 17O enriched LaNbO4 and (b) 17O enriched LaNb0.84W0.16O4.08 obtained at room temperature at 16.4 T and under a MAS rate of 20 kHz. The dashed line in (b) indicates the + 1 diagonal. Asterisk (*) denote spinning sidebands.

The room temperature 17O NMR spectrum of 17O enriched LaNb0.84W0.16O4.08 obtained under MAS rate of 22 kHz (Figure 12b) is dramatically different from the one obtained for LaNbO4 revealing a very broad resonance (~13 kHz) centred at ~500 ppm (along with a range of broad spinning sidebands, see Figure S11). This resonance spreads from 420 to 570 ppm covering the positions of the two 17O resonances of Nb-O1 and Nb-O2 in LaNbO4 and therefore consistent with a large range of Nb-O/W-O bond lengths ranging from ~1.844 to 1.903 Å in LaNb0.84W0.16O4.08 (corresponding to Nb-O2 to Nb-O1 in LaNbO4). The broad centerband at ~500 ppm therefore reflects a distribution of chemical shifts rather than second-order quadrupolar broadening. This is in agreement with both the 17O TQMAS spectrum of this material (Figure 13b) which shows that the signal at ~500 ppm is clearly spread along the +1 diagonal and with the presence of broad spinning sidebands that should be narrowed by MAS if no distribution of chemical shift was present. There is no clear 17O NMR signal for the interstitial oxygen, and the data above suggest that a range of oxygen environments are observed instead and correspond to different Nb-O and W-O bond lengths and local environments. Upon sample heating, disappearance of the spinning sidebands starting at 270 °C indicates the onset of slow motion in LaNb0.84W0.16O4.08 (see supporting information for further details) and is in sharp contrast with the large number of sidebands in the LaNbO4 data (Figures 11 and S12), likely indicating enhanced oxygen ion mobility in the former phase. Above 300 °C, restriction of the maximum MAS rate available on the 7 mm laser heated MAS probe (4 kHz) does not allow the central transition to be clearly observed due to overlapping spinning sidebands and resulting in a broad pattern (≈ 63 kHz at 605 °C).

# Conclusion

In this contribution, the structure evolution of the LaNb1-xWxO4+x/2 series from room temperature up to 800 °C is investigated. Using high temperature thermal analysis, in situ diffraction techniques and 17O and 93Nb MAS NMR, a sequence of transformation in LaNb1-xWxO4+x/2 between a modulated monoclinic phase, a modulated tetragonal phase and an unmodulated tetragonal phase, which was overlooked in the literature, has been revealed. In situ scattering experiments shed light on the structural evolution of the LaNb0.88W0.12O4.06 and LaNb0.84W0.16O4.08 compositions: modulation peaks were observed and the structure of the LaNb0.88W0.12O4.06 composition between 500 °C  and 650 °C was successfully refined using the I41/a(α,β,0)00(-β,α,0)00 superspace group. The LaNb0.84W0.16O4.08 composition, on the other hand, maintains its modulated structure till 800 °C. Attempts were made to pinpoint the position of the interstitial oxygen in the LaNb0.84W0.16O4.08 composition at 500 °C, and 93Nb MAS NMR data suggests the presence of a distorted site tentatively ascribed to Nb near an interstitial ion. The refinement suggests a non-localized distribution of the interstitial oxygen that agrees with the distribution of 17O shifts observed in the MAS NMR spectra. It is possible that an extended structural model that incorporates interstitials as lattice ions is required to fully describe the structure. Based on the diffraction and thermal analysis data, the phase diagram of the LaNb1-xWxO4+x/2 is drawn, which highlights the complex transitions between a modulated monoclinic phase, a modulated tetragonal phase and a disordered tetragonal.

# Acknowledgements

﻿The authors acknowledge funding from the EPSRC for a studentship to R.D.B., the EU Marie Curie actions for an International Incoming Fellowship 2011-2013 (grant 275212) to F.B., Clare Hall at the University of Cambridge for a Research Fellowship to F.B., the EU ERC for an Advanced Fellowship (LIBNMR) to C.P.G. We thank Matthew T. Dunstan for recording the XRD patterns of 17O enriched LaNbO4 and LaNb0.84W0.16O4.08. We gratefully acknowledge the Science and Technology Facilities Council (STFC) for access to neutron beamtime at HRPD, ISIS (RB1410098). The UK 850 MHz solid-state NMR Facility used in this research was funded by EPSRC and BBSRC, as well as the University of Warwick including via part funding through Birmingham Science City Advanced Materials Projects 1 and 2 supported by Advantage West Midlands (AWM) and the European Regional Development Fund (ERDF). Collaborative assistance from the 850 MHz Facility Manager (Dr. Dinu Iuga, University of Warwick) is acknowledged.

# Supporting Information

Figures S1-S11 and additional text are included in the supporting information document.

# References

(1) 	Huang, K.; Feng, M.; Goodenough, J. B. Synthesis and Electrical Properties of Dense Ce0.9Gd0.1O1.95 Ceramics. J. Am. Ceram. Soc. 2005, 81, 357–362.

(2) 	Huang, K.; Tichy, R. S.; Goodenough, J. B. Superior Perovskite Oxide-Ion Conductor; Strontium- and Magnesium-Doped LaGaO3: I, Phase Relationships and Electrical Properties. J. Am. Ceram. Soc. 2005, 81, 2565–2575.

(3) 	Lacorre, P.; Goutenoire, F.; Bohnke, O.; Retoux, R.; Lallgant, Y. Designing Fast Oxide-Ion Conductors Based on La2Mo2O9. Nature 2000, 404, 856–858.

(4) 	Pramana, S. S.; Klooster, W. T.; White, T. J. Framework Interstitial Oxygen in La10(GeO4)5-(GeO5)O2 Apatite Electrolyte. Acta Crystallogr. Sect. B Struct. Sci. 2007, 63, 597–602.

(5) 	Wei, F.; Gasparyan, H.; Keenan, P. J.; Gutmann, M.; Fang, Y.; Baikie, T.; Claridge, J. B.; Slater, P. R.; Kloc, C. L.; White, T. J. Anisotropic Oxide Ion Conduction in Melilite Intermediate Temperature Electrolytes. J. Mater. Chem. A 2015, 3, 3091–3096.

(6) 	Tate, M. L.; Blom, D. A.; Avdeev, M.; Brand, H. E. A.; McIntyre, G. J.; Vogt, T.; Evans, I. R. New Apatite-Type Oxide Ion Conductor, Bi2La8[(GeO4)6]O3: Structure, Properties, and Direct Imaging of Low-Level Interstitial Oxygen Atoms Using Aberration-Corrected Scanning Transmission Electron Micr. Adv. Funct. Mater. 2017, 27, 1605625.

(7) 	Kuang, X.; Green, M. A.; Niu, H.; Zajdel, P.; Dickinson, C.; Claridge, J. B.; Jantsky, L.; Rosseinsky, M. J. Interstitial Oxide Ion Conductivity in the Layered Tetrahedral Network Melilite Structure. Nat. Mater. 2008, 7, 498–504.

(8) 	Magrasó, A.; Fontaine, M. L.; Larring, Y.; Bredesen, R.; Syvertsen, G. E.; Lein, H. L.; Grande, T.; Huse, M.; Strandbakke, R.; Haugsrud, R.; et al. Development of Proton Conducting SOFCs Based on LaNbO4 Electrolyte - Status in Norway. Fuel Cells 2011, 11, 17–25.

(9) 	Packer, R. J.; Tsipis, E. V.; Munnings, C. N.; Kharton, V. V.; Skinner, S. J.; Frade, J. R. Diffusion and Conductivity Properties of Cerium Niobate. Solid State Ionics 2006, 177, 2059–2064.

(10) 	Esaka, T. Ionic Conduction in Substituted Scheelite-Type Oxides. Solid State Ionics 2000, 136–137, 1–9.

(11) 	Wachowski, S.; Mielewczyk-Gryń, A.; Zagórski, K.; Li, C.; Jasiński, P.; Skinner, S. J.; Haugsrud, R.; Gazda, M. Influence of Sb-Substitution on Ionic Transport in Lanthanum Orthoniobates. J. Mater. Chem. A 2016, 4, 11696–11707.

(12) 	Packer, R. J.; Skinner, S. J. Remarkable Oxide Ion Conductivity Observed at Low Temperatures in a Complex Superstructured Oxide. Adv. Mater. 2010, 22, 1613–1616.

(13) 	Pramana, S. S.; Baikie, T.; An, T.; Tucker, M. G.; Wu, J.; Schreyer, M. K.; Wei, F.; Bayliss, R. D.; Kloc, C. L.; White, T. J.; et al. Correlation of Local Structure and Diffusion Pathways in the Modulated Anisotropic Oxide Ion Conductor CeNbO4.25. J. Am. Chem. Soc. 2016, 138, 1273–1279.

(14) 	Li, C.; Pramana, S. S.; Skinner, S. J. Room Temperature Structure and Transport Properties of the Incommensurate Modulated LaNb0.88 W0.12O4.06. Dalt. Trans. 2019, 48, 1633–1646.

(15) 	Ferrara, C.; Mancini, A.; Ritter, C.; Malavasi, L.; Tealdi, C. Interstitial Oxide Ion Migration in Scheelite-Type Electrolytes: A Combined Neutron Diffraction and Computational Study. J. Mater. Chem. A 2015, 3, 22258–22265.

(16) 	Laguna-Bercero, M. A.; Bayliss, R. D.; Skinner, S. J. LaNb0.84W0.16O4.08 as a Novel Electrolyte for High Temperature Fuel Cell and Solid Oxide Electrolysis Applications. Solid State Ionics 2014, 262, 298–302.

(17) 	Yang, X.; Fernández-Carrión, A. J.; Wang, J.; Porcher, F.; Fayon, F.; Allix, M.; Kuang, X. Cooperative Mechanisms of Oxygen Vacancy Stabilization and Migration in the Isolated Tetrahedral Anion Scheelite Structure. Nat. Commun. 2018, 9, 4484.

(18) 	Li, C.; Bayliss, R. D.; Skinner, S. J. Crystal Structure and Potential Interstitial Oxide Ion Conductivity of LnNbO4 and LnNb0.92W0.08O4.04 (Ln = La, Pr, Nd). Solid State Ionics 2014, 262, 530–535.

(19) 	Petříček, V.; Dušek, M.; Petricek, V.; Dusek, M. Jana2000 - Crystallographic Computing System. Karla Fejfarová & Lukáš Palatinus Praha 2003, 137.

(20) 	Frydman, L.; Harwood, J. S. Isotropic Spectra of Half-Integer Quadrupolar Spins from Bidimensional Magic-Angle-Spinning Nmr. J. Am. Chem. Soc. 1995, 117, 5367–5368.

(21) 	Amoureux, J.-P.; Fernandez, C.; Steuernagel, S. ZFiltering in MQMAS NMR. J. Magn. Reson. Ser. A 1996, 123, 116–118.

(22) 	Bielecki, A.; Burum, D. P. Temperature Dependence of 207Pb MAS Spectra of Solid Lead Nitrate. An Accurate, Sensitive Thermometer for Variable-Temperature MAS. J. Magn. Reson. Ser. A 1995, 116, 215–220.

(23) 	Thurber, K. R.; Tycko, R. Measurement of Sample Temperatures under Magic-Angle Spinning from the Chemical Shift and Spin-Lattice Relaxation Rate of 79Br in KBr Powder. J. Magn. Reson. 2009, 196, 84–87.

(24) 	Ernst, H.; Freude, D.; Mildner, T.; Wolf, I. Laser-Supported High-Temperature MAS NMR for Time-Resolved in Situ Studies of Reaction Steps in Heterogeneous Catalysis. Solid State Nucl. Magn. Reson. 1996, 6, 147–156.

(25) 	Millot, Y.; Man, P. P. Procedures for Labeling the High-Resolution Axis of Two-Dimensional MQ-MAS NMR Spectra of Half-Integer Quadrupole Spins. Solid State Nucl. Magn. Reson. 2002, 21, 21–43.

(26) 	Ashbrook, S. E. Recent Advances in Solid-State NMR Spectroscopy of Quadrupolar Nuclei. Phys. Chem. Chem. Phys. 2009, 11, 6876–6891.

(27) 	Du, L. S.; Schurko, R. W.; Kim, N.; Grey, C. P. Solid-State 93Nb, 19F, and 113Cd Nuclear Magnetic Resonance Study of Niobium Oxyfluorides: Characterization of Local Distortions and Oxygen/Fluorine Ordering. J. Phys. Chem. A 2002, 106, 7876–7886.

(28) 	Papulovskiy, E.; Shubin, A. A.; Terskikh, V. V.; Pickard, C. J.; Lapina, O. B. Theoretical and Experimental Insights into Applicability of Solid-State 93Nb NMR in Catalysis. Phys. Chem. Chem. Phys. 2013, 15, 5115–5131.

(29) 	Dunstan, M. T.; Blanc, F.; Avdeev, M.; McIntyre, G. J.; Grey, C. P.; Ling, C. D. Long-Range-Ordered Coexistence of 4-, 5-, and 6-Coordinate Niobium in the Mixed Ionic-Electronic Conductor γ-Ba4Nb2O9. Chem. Mater. 2013, 25, 3154–3161.

(30) 	Hanna, J. V.; Pike, K. J.; Charpentier, T.; Kemp, T. F.; Smith, M. E.; Lucier, B. E. G.; Schurko, R. W.; Cahill, L. S. A 93Nb Solid-State NMR and Density Functional Theory Study of Four- and Six-Coordinate Niobate Systems. Chem. - A Eur. J. 2010, 16, 3222–3239.

(31) 	Baltisberger, J. H.; Gann, S. L.; Pines, A.; Wooten, E. W.; Chang, T. H.; Mueller, K. T. 87Rb Dynamic-Angle Spinning NMR Spectroscopy of Inorganic Rubidium Salts. J. Am. Chem. Soc. 1992, 114, 7489–7493.

(32) 	Skinner, S. J.; Kang, Y. X-Ray Diffraction Studies and Phase Transformations of CeNbO4+δ Using in Situ Techniques. Solid State Sci. 2003, 5, 1475–1479.

(33) 	Vullum, F.; Nitsche, F.; Selbach, S. M.; Grande, T. Solid Solubility and Phase Transitions in the System LaNb1-xTaxO4. J. Solid State Chem. 2008, 181, 2580–2585.

(34) 	Mokkelbost, T.; Lein, H. L.; Vullum, P. E.; Holmestad, R.; Grande, T.; Einarsrud, M. A. Thermal and Mechanical Properties of LaNbO4-Based Ceramics. Ceram. Int. 2009, 35, 2877–2883.

(35) 	Singhal, S. C.; Kendall, K. High-Temperature Solid Oxide Fuel Cells: Fundamentals, Design, and Applicatons, 1st ed.; Elsevier B.V., 2003.

(36) 	Corbel, G.; Mestiri, S.; Lacorre, P. Physicochemical Compatibility of CGO Fluorite, LSM and LSCF Perovskite Electrode Materials with La2Mo2O9 Fast Oxide-Ion Conductor. Solid State Sci. 2005, 7, 1216–1224.

(37) 	Xu, Q.; Huang, D.; Zhang, F.; Chen, W.; Chen, M.; Liu, H. xing. Structure, Electrical Conducting and Thermal Expansion Properties of La0.6Sr0.4Co0.8Fe0.2O3-d-Ce0.8Sm0.2O2-d Composite Cathodes. J. Alloys Compd. 2008, 454, 460–465.

(38) 	Bayliss, R. D. Synthetic, Structural and Electrochemical Studies of Superstructured Rare-Earth Niobates, Ph.D. Thesis, Imperial College London, 2014.

(39) 	van Smaalen, S. Incommensurate Crystallography; Oxford Scholarship, 2008.

(40) 	Stokes, H. T.; Campbell, B. J.; Van Smaalen, S. Generation of (3 + d)-Dimensional Superspace Groups for Describing the Symmetry of Modulated Crystalline Structures. Acta Crystallogr. Sect. A Found. Crystallogr. 2011, 67, 45–55.

(41) 	Morozov, V.; Arakcheeva, A.; Redkin, B.; Sinitsyn, V.; Khasanov, S.; Kudrenko, E.; Raskina, M.; Lebedev, O.; Van Tendeloo, G. Na2/7Gd4/7MoO4: A Modulated Scheelite-Type Structure and Conductivity Properties. Inorg. Chem. 2012, 51, 5313–5324.

(42) 	Abakumov, A. M.; Morozov, V. A.; Tsirlin, A. A.; Verbeeck, J.; Hadermann, J. Cation Ordering and Flexibility of the BO42- Tetrahedra in Incommensurately Modulated CaEu2(BO4)4 (B = Mo, W) Scheelites. Inorg. Chem. 2014, 53, 9407–9415.

(43) 	Takai, S.; Touda, S.; Oikawa, K.; Mori, K.; Torii, S. Powder Neutron Diffraction Study of Ln-Substituted PbWO4 Oxide Ion Conductors. Solid State Ionics 2002, 148, 123–133.

(44) 	Thompson, J. G.; Withers, R. L.; Brink, F. J. Modulated Structures in Oxidized Cerium Niobates. J. Solid State Chem. 1999, 143, 122–131.

(45) 	Brizé, V.; Georges, S.; Kodjikian, S.; Suard, E.; Goutenoire, F. La6Mo8O33: A New Ordered Defect Scheelite Superstructure. J. Solid State Chem. 2004, 177, 2617–2627.

(46) 	Hadermann, J.; Perez, O.; Creon, N.; Michel, C.; Hervieu, M. The (3 + 2)D Structure of Oxygen Deficient LaSrCuO3.52. J. Mater. Chem. 2007, 17, 2344–2350.

(47) 	Peet, J. R.; Chambers, M. S.; Piovano, A.; Johnson, M. R.; Evans, I. R. Dynamics in Bi(III)-Containing Apatite-Type Oxide Ion Conductors: A Combined Computational and Experimental Study. J. Mater. Chem. A 2018, 6, 5129–5135.

(48) 	Chambers, M. S.; Chater, P. A.; Evans, I. R.; Evans, J. S. O. Average and Local Structure of Apatite-Type Germanates and Implications for Oxide Ion Conductivity. Inorg. Chem. 2019, 58, 14853–14862.

(49) 	Wei, F.; Baikie, T.; An, T.; Schreyer, M.; Kloc, C.; White, T. J. Five-Dimensional Incommensurate Structure of the Melilite Electrolyte [CaNd]2[Ga]2[Ga2O7]2. J. Am. Chem. Soc. 2011, 133, 15200–15211.

(50) 	Takai, S.; Nakanishi, T.; Oikawa, K.; Torii, S.; Hoshikawa, A.; Kamiyama, T.; Esaka, T. Neutron Diffraction and IR Spectroscopy on Mechanically Alloyed La-Substituted PbWO4. Solid State Ionics 2004, 170, 297–304.

(51) 	Takai, S.; Sugiura, K.; Esaka, T. Ionic Conduction Properties of Pb1−xMxWO4+δ (M = Pr, Tb). Mater. Res. Bull. 1999, 34, 193–202.

(52) 	Kenneth J.D. MacKenzie, M. E. S.; MacKenzie, K. J. D.; Smith, M. E. Multinuclear Solid-State NMR of Inorganic Materials, 1st ed.; MacKenzie, K. J. D., Smith, M. E., Eds.; Oxford, 2002.

(53) 	Bak, P. Commensurate Phases , Incommensurate Phases and the Devil ’ s Staircase. Rep. Prog. Phys. 1982, 45, 587.

(54) 	McMillan, W. L. Theory of Discommensurations and the Commensurate-Incommensurate Charge-Density-Wave Phase Transition. Phys. Rev. B 1976, 14, 1496–1502.

(55) 	Grabowski, M.; Subbaswamy, K. R. Phase-Amplitude Soliton Lattice and the Lock-in Transition. Phys. D Nonlinear Phenom. 1982, 5, 348–358.

(56) 	Chattopadhyay, T.; Liss, K. D.; Brückel, T. Incommensurate-Commensurate Lock-in Phase Transition in EuAs3. J. Magn. Magn. Mater. 1998, 177–181, 1058–1060.

(57) 	Chen, C.; Cheong, S.-W. Commensurate to Incommensurate Charge Ordering and Its Real-Space Images in La0.5Ca0.5MnO3. Phys. Rev. Lett. 1996, 76, 4042–4045.

(58) 	Nakanishi, K.; Shiba, H. Domain-like Incommensurate Charge-Density-Wave States and the First-Order Incommensurate-Commensurate Transitions in Layered Tantalum Dichalcogenides. I. 1T-Polytype. J. Phys. Soc. Japan 1977, 43, 1839–1847.

(59) 	Ghiringhelli, G.; Le Tacon, M.; Minola, M.; Blanco-Canosa, S.; Mazzoli, C.; Brookes, N. B.; De Luca, G. M.; Frano, A.; Hawthorn, D. G.; He, F.; et al. Long-Range Incommensurate Charge Fluctuations in (Y,Nd)Ba2Cu3O6+x. Science 2012, 337, 821–825.

(60) 	Sarin, P.; Hughes, R. W.; Lowry, D. R.; Apostolov, Z. D.; Kriven, W. M. High-Temperature Properties and Ferroelastic Phase Transitions in Rare-Earth Niobates (LnNbO4). J. Am. Ceram. Soc. 2014, 97, 3307–3319.

# Table of Contents

Synopsis

High temperature thermal analysis, scattering techniques and 17O nuclear magnetic resonance spectroscopy reveal the structural evolution of the LaNb1-xWxO4+x/2 (x = 0.04 - 0.16) phases to be a series of phase transitions between a modulated monoclinic phase, a high temperature unmodulated tetragonal phase and a high temperature modulated tetragonal phase.