Supplementary Information

Ethyl Methacrylate Diblock Copolymers as Polymeric Surfactants: Effect of Molar Mass and Composition

Birsen Somuncuoğlu, Yu Lin Lee, Anna P. Constantinou, David L. M. Poussin

and Theoni K. Georgiou*

Department of Materials, Imperial College London, South Kensington Campus, Royal School of Mines, Exhibition Road, SW7 2AZ, London, United Kingdom

Figure S1. Method of visual observations to study emulsion stability.

Figure S2. GPC chromatograms of PEGMA-EtMA based copolymers of Polymer series 1. The blue and orange lines represent the PEGMA homopolymers and the diblock copolymers, respectively. The grey lines represent statistical copolymers.

Figure S3. GPC chromatogram of EtMA-DMAEMA based copolymers of Polymer series 2. The orange and green lines represent the EtMA homopolymers and the diblock copolymers, respectively. The grey lines represent statistical copolymers.

Figure S4. The 1H NMR spectra of (a) PEGMA homopolymer and (b) diblock copolymer, P-A2: PEGMA15-b-EtMA13 shown in blue and orange, respectively. The chemical structures of PEGMA and EtMA are also coloured in blue and orange, respectively.

Figure S5. The 1H NMR spectra of (a) EtMA homopolymer and (b) diblock copolymer, P-B1: EtMA7-b-DMAEMA14 shown in orange and green, respectively. The chemical structures of EtMA and DMAEMA are also coloured in orange and green, respectively.

Figure S6. DLS histograms of PEGMA-b-EtMA based diblock copolymers of Polymer series 1, obtained by analysing 1 w/w% solution in deionised water.

Figure S7. DLS histograms of EtMA-b-DMAEMA based diblock copolymers of Polymer series 2, obtained by analysing 1 w/w% solution in deionised water.

Figure S8. Graph shows the kilo counts per second versus polymer concentration.  The targeted compositions of diblock copolymers; 75-25, 60-40 and 50-50 w/w% are represented in blue, green and red, respectively. The circle (), square () and triangle () polymers of different MMs; 9000, 6000 and 3000 g mol-1 are represented, respectively.

Figure S9. Graph shows the kilo counts per second versus polymer concentration.  The targeted compositions of diblock copolymers; 75-25, 60-40 and 50-50 w/w% are represented in blue, green and red, respectively. The circle (), square () and triangle () polymers of different MMs; 9000, 6000 and 3000 g mol-1 are represented, respectively.

Figure S10. CMC (in mol L-1) versus Mn of all water soluble PEGMA-EtMA copolymers. The circle (), square () and triangle () polymers of 30, 40 and 50 wt% are represented, respectively.

Figure S11. CMC (in mol L-1) versus Mn of all water soluble DMAEMA-EtMA copolymers. The circle (), square () and triangle () polymers of 30, 40 and 50 wt% are represented, respectively.

Figure S12. Images of emulsions taken at different time scales. Polymeric surfactants from Polymer series 1 were used as emulsifiers.  1 w/w % of each copolymer was mixed with equal weights of methyl laurate and water.

Figure S13. Images of emulsions taken at different time scales. Polymeric surfactants from Polymer series 2 were used as emulsifiers. 1 w/w % of each copolymer was mixed with equal weights of methyl laurate and water.

Table S1. The fraction of the cream phase-resolved for Polymer series 1 at different times.

|  | ɸ cream |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| time (min) | P-A1 | P-A2 | P-A3 | P-A4 | P-A5 | P-A6 | P-A7 | P-A8 | P-A9 | P-A10 | P-A11 |
| 1 | 0.831 | 0.845 | 0.86 | 0.922 | 0.879 | 0.926 | 0.820 | 0.941 | 0.924 | 0.903 | 0.934 |
| 120 | 0.817 | 0.835 | 0.851 | 0.880 | 0.874 | 0.924 | 0.816 | 0.915 | 0.901 | 0.903 | 0.921 |
| 240 | 0.811 | 0.817 | 0.840 | 0.865 | 0.852 | 0.914 | 0.812 | 0.895 | 0.897 | 0.893 | 0.915 |
| 1440 | 0.787 | 0.749 | 0.769 | 0.803 | 0.822 | 0.876 | 0.796 | 0.813 | 0.861 | 0.878 | 0.853 |
| 2880 | 0.758 | 0.713 | 0.699 | 0.751 | 0.788 | 0.865 | 0.742 | 0.783 | 0.833 | 0.838 | 0.833 |
| 4320 | 0.701 | 0.673 | 0.626 | 0.686 | 0.757 | 0.836 | 0.674 | 0.776 | 0.786 | 0.813 | 0.754 |
| 10080 | 0.616 | 0.612 | 0.601 | 0.637 | 0.641 | 0.761 | 0.634 | 0.694 | 0.700 | 0.794 | 0.713 |
| 20160 | 0.595 | 0.600 | 0.58 | 0.623 | 0.621 | 0.668 | 0.622 | 0.661 | 0.656 | 0.694 | 0.670 |
| 30240 | 0.579 | 0.597 | 0.576 | 0.611 | 0.615 | 0.648 | 0.621 | 0.657 | 0.644 | 0.676 | 0.670 |
| 40320 | 0.570 | 0.576 | 0.575 | 0.605 | 0.613 | 0.640 | 0.620 | 0.644 | 0.632 | 0.672 | 0.630 |

Figure S14. Graph shows the fraction of cream phase resolved for Polymer series 1 over time.  The targeted composition of diblock copolymers; 75-25, 60-40 and 50-50 w/w % are represented in blue, green and red, respectively. The random copolymers with composition 75 -25 and 60-40 w/w % are represented in dark yellow.  The circle (), square () and triangle () polymers of different MMs; 9000, 6000 and 3000 g mol-1 are represented, respectively.

Table S2. The fraction of the cream phase-resolved for Polymer series 2 at different times.

|  | ɸ cream |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| time (min) | P-B1 | P-B4 | P-B7 | P-B6 | P-B8 | P-B2 | P-B3 | P-B5 | P-B9 | P-B10 |
| 1 | 1.002 | 1.000 | 0.953 | 0.943 | 0.925 | 0.907 | 0.948 | 0.941 | 0.919 | 0.980 |
| 120 | 0.961 | 0.960 | 0.927 | 0.939 | 0.869 | 0.907 | 0.946 | 0.932 | 0.883 | 0.960 |
| 240 | 0.950 | 0.953 | 0.907 | 0.922 | 0.858 | 0.897 | 0.950 | 0.896 | 0.867 | 0.917 |
| 1440 | 0.895 | 0.885 | 0.900 | 0.823 | 0.848 | 0.878 | 0.890 | 0.865 | 0.779 | 0.888 |
| 2880 | 0.856 | 0.833 | 0.898 | 0.801 | 0.763 | 0.873 | 0.865 | 0.836 | 0.734 | 0.815 |
| 7200 | 0.700 | 0.726 | 0.763 | 0.686 | 0.639 | 0.731 | 0.821 | 0.694 | 0.645 | 0.811 |
| 10080 | 0.679 | 0.715 | 0.734 | 0.682 | 0.634 | 0.697 | 0.734 | 0.684 | 0.638 | 0.737 |
| 20160 | 0.676 | 0.712 | 0.700 | 0.675 | 0.634 | 0.677 | 0.644 | 0.680 | 0.636 | 0.672 |
| 30240 | 0.666 | 0.708 | 0.686 | 0.670 | 0.628 | 0.663 | 0.632 | 0.672 | 0.626 | 0.668 |
| 40320 | 0.653 | 0.702 | 0.684 | 0.658 | 0.623 | 0.635 | 0.615 | 0.658 | 0.623 | 0.651 |

Figure S15. Graph shows the fraction of cream phase resolved for Polymer series 2 over time.  The targeted composition of diblock copolymers; 75-25, 60-40 and 50-50 w/w % are represented in blue, green and red, respectively. The random copolymer is represented in dark yellow.  The circle (), square () and triangle () polymers of different MMs; 9000, 6000 and 3000 g mol-1 are represented, respectively.