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Abstract

The electrochemistry of several vanadium oxides and oxyhalides has been examined in room temperature ionic liquids made by mixing 1-ethyl-3-methylimidazolium chloride (EMIC) and aluminum chloride.  By varying the mole ratio of the two components, Lewis basic, neutral and acidic ionic liquids were made, while the addition of NaCl to an acidic ionic liquid resulted in a Lewis buffered, neutral solvent.  Because of the ionic nature of these liquids, most oxides have very low solubility: V2O3, V2O4 and VOSO4 are insoluble, while V2O5 and Na3VO4 are slightly soluble with solubility limits of less than 5 mM.  The solubilities of the salts NaVO3 and NH4VO3 and the oxyhalides VOCl3 and VOF3 are significantly higher.   In acidic ionic liquids V2O5, NaVO3, Na3VO4 and NH4VO3 all exhibit three irreversible reduction waves between 1.7 and 0.5V vs. a reference electrode consisting of an aluminum wire in a 0.6 mole fraction AlCl3 ionic liquid.  VOCl3 and VOF3 gave similar reduction peaks suggesting that the oxides may have reacted with the ionic liquid to form oxychlorides.  A new ionic liquid was formed by using VOCl3 as the Lewis acid instead of AlCl3:  

EMIC   +   VOCl3   (   [EMI]+   +   [VOCl4]-
In acetonitrile [VOCl4]- was found to undergo a one electron reversible reduction to [VOCl4]2-:

[VOCl4] -    +    e-    (    [VOCl4]2-
Introduction

Room temperature ionic liquids made by mixing 1-ethyl-3-methylimidazolium chloride and AlCl3 (EMIC/AlCl3) are being investigated by several groups as possible battery electrolytes for use in cells with alkali metal anodes. 
,
,
,
  By varying the ratio of the organic salt (EMIC) to the inorganic salt (AlCl3), Lewis basic, neutral, and acidic liquids can be formed.  The composition of such ionic liquids is represented by the value of N, the mole fraction of AlCl3.  Because these ionic liquids are formed when two solids are mixed, no solvent is used to dissolve the salts.  When N=0.5, a neutral liquid is formed with [EMI]+ and [AlCl4]- in a one to one mole ratio.  If N < 0.5, excess chloride from the EMIC will be present and a Lewis basic liquid is formed.  If N > 0.5, polymeric forms of [AlCl4]- occur and a Lewis acidic liquid results.  Such liquids have several advantages including wide voltage windows, wide liquid temperature ranges, and high conductivities when compared to other solvents and electrolytes or conducting polymers.  The values of these parameters depend on the composition.  For example, compositions between about N=0.35 and 0.65 all yield liquids at, or somewhat below, room temperature (25oC).  The properties of these liquids and their use as solvents for the study of transition metal compounds have been summarized in recent reviews. 
,
,


Since the nonaqueous nature of these liquids allows the use of alkali metals, lithium and sodium have been investigated as possible anodes for cells using them as electrolytes.  Most work has focused on the neutral ionic liquids because these provide the widest voltage window, slightly greater than 4V.  This means that if reversible couples for the anode and cathode can be found to operate near the voltage limits, a cell of about 4V would be possible.  Lipsztajn and Osteryoung 
 were the first workers to report the plating and stripping of Li on tungsten in a neutral ionic liquid.  Yu, Winnick and Kohl 
 reported the reversible plating and stripping of sodium at a mercury drop attached to a gold disk.  Scordilis-Kelley, Fuller, Carlin and Wilkes 
 studied the alkali metals in ionic liquids buffered with NaCl in order to maintain the wide voltage window during charge and discharge cycles.  They found that only lithium could be deposited on a bare tungsten electrode, as the reduction potentials for sodium and potassium fell outside the voltage window.  By adding protons to the buffered ionic liquid, Riechel and Wilkes
 found that the voltage window could be widened by about 300mV, allowing the reversible plating and stripping of sodium at Pt and W electrodes.  


Because of instability of the proton concentration in the ionic liquid studied by Riechel and Wilkes, other reagents for widening the voltage window were sought.  Piersma, Ryan, Schumacher and Riechel 1 found that addition of triethanolamineHCl produced liquids that were stable for months.  Gray, Kohl and Winnick 2 produced stable liquids by pressurizing cells with HCl(g) .   Fuller, Carlin and Osteryoung 3,4 have successfully modified these liquids by the addition of SOCl2.  Whereas lithium has been shown to form dendrites when plated in these electrolytes, sodium forms smooth layers3.  Since sodium is more stable than lithium, provides a higher potential, and does not exhibit the problem of dendrite formation, it may be a better candidate for an anode in this electrolyte.


In contrast to the issue of a suitable anode, little work has been done to identify suitable cathode materials.  There are only a few reports in the literature of vanadium compounds studied in EMIC/AlCl3 ionic liquids
,
,
.  We present here a study of the electrochemistry of several vanadium oxides and oxyhalides in EMIC/AlCl3 electrolytes in order to evaluate their feasibility as cathode materials.  We also report the formation of new room temperature ionic liquids made by mixing EMIC with VOCl3 or VOF3, and describe the reversible electrochemistry of a vanadium (V)/(IV) couple.    

Experimental

   Instrumentation.-  All electrochemical experiments were carried out using a three electrode cell set up in a Vacuum Atmospheres glove box under a dry nitrogen atmosphere.  The electrochemical measurements were made with either an EG&G Princeton Applied Research (PAR) Model 263A potentiostat/galvanostat interfaced to a personal computer running PAR Model 270 software, or a Bioanalytical Systems (BAS) Model 100A electrochemical analyzer.  A BAS platinum disk working electrode (Model MF 2013, 2.01 mm2) was used for voltammetry, while a Pt mesh working electrode was used for coulometry.  A Pt foil auxiliary electrode was used for voltammetry and a Pt foil, isolated from the test solution by means of a fine porosity fritted tube, was used as an auxiliary electrode for coulometry.  The reference electrode for both voltammetry and coulometry in the ionic liquids consisted of an Al wire in an N=0.60 EMIC/AlCl3 ionic liquid, contained in a Pyrex tube with a porous tip to provide solution contact. The reference electrode for work done in acetonitrile was a silver wire in 0.1M tetrabutlyammonium percholrate (TBAP).  The scan rate for all voltammograms was 100mV/s, unless otherwise indicated.  UV-Visible spectra were recorded using a Hewlett Packard Model 8452A diode array spectrometer and quartz cuvettes. Slightly soluble samples were decanted or filtered before recording spectra.  Conductivity measurements were made with an Extech Instruments Oyster conductivity meter kit.  The instrument was calibrated with a KCl solution outside of the glove box in order to determine the cell constant.  Then the clean, dry cell was taken inside the glove box for the ionic liquid measurements.

    Reagents and Synthesis.- The components for the ionic liquids were synthesized and purified using published methods.  1-Ethyl-3-methylimidazolium chloride (EMIC) was synthesized from 1-methylimidazole and chloroethane (Aldrich)
.  Purification of AlCl3 (Fluka) was carried out by recrystallization in a tube furnace.  Neutral ionic liquids  were made in a glove box by mixing carefully weighed amounts of EMIC and AlCl3.  Traces of moisture arising from the synthesis of EMIC were reduced by the addition of ethylaluminum dichloride (Aldrich)
.  Sometimes the ionic liquids were further purified by electrolyzing at ‑1.0V overnight using a Pt mesh working electrode and a large Pt flag auxiliary electrode.  It was concluded that the residual moisture had been removed when reduction peaks normally observed at – 0.5V and –1.2V in the voltammograms were decreased to a few microamps.  Acidic ionic liquids were made by adding excess AlCl3 to a neutral liquid, while basic liquids were made by adding excess EMIC.  The vanadium reagents V2O3, V2O4, V2O5, VOSO4, Na3VO4, VOCl3 and VOF3 (Aldrich), NH4VO3 (Alfa Aesar), and NaVO3 (GFS Chemicals) were used as received.


EMIC/VOCl3 ionic liquids were prepared by mixing 1:1 stoichiometric amounts of VOCl3 and EMIC in a small glass flask and stirring with a Teflon covered magnetic stir bar in the glove box.  


The preparation of [EMI]2[VOCl4] has been previously published 12,
.

Results and Discussion
   Oxides.- The solubilities of seven vanadium oxides (V2O5, V2O4, V2O3, NaVO3, Na3VO4, NH4VO3 , and VOSO4) were evaluated in various EMIC/AlCl3 ionic liquids.  The compositions were basic (N=0.45), neutral (N=0.50), neutral buffered (N=0.50, resulting from the addition of excess NaCl to an N=0.55 ionic liquid), and acidic (N=0.55).  

Solubility at room temperature was determined by trying to dissolve enough of each sample in 11 g of an ionic liquid to create a 5 mM solution.  Table 1 shows the solubilities of the materials surveyed.  In this paper, a material is defined as soluble when a solution greater than or equal to 5 mM can be made.  It is considered slightly soluble if it will form a solution of less than 5 mM that displays significant color or electrochemical activity.  Solution formation was aided by vigorous stirring with a magnetic stirrer.  Some solids were difficult to dissolve, requiring several days of continuous stirring.  In some cases stirring only reduced the particle size of the material resulting in a suspension.  Since the particles settled out when stirring was stopped, these materials were judged insoluble. Sometimes the sample/solvent suspension was also subjected to mild heating (81oC) or prolonged sonication (about three hours) in an effort to make the sample dissolve.  The most soluble compounds were NaVO3 and NH4VO3.  V2O5 and Na3VO4 were slightly soluble, while the other compounds were insoluble.  

 Because of its reported use in xerogel cathodes, 
,
,
,
,
,
 V2O5 was of greatest interest.  In spite of its low solubility, characteristic redox peaks were observed.  Figure 1A shows the cyclic voltammogram of V2O5 in a basic ionic liquid (N=0.45).  The only significant feature is an irreversible reduction peak at about 0.3V.  In a neutral (N=0.50) ionic liquid, (Figure 1B) a similar reduction peak appears near 0.5V and is accompanied by an oxidation peak at 1.3V.  The voltammogram in a neutral, NaCl buffered liquid (not shown) exhibits the same reduction and oxidation peaks as in the neutral solvent.  The voltammogram of V2O5 in an acidic liquid (N=0.55) (Figure 1C) is different in that two distinct reduction peaks are observed, one at 0.5V as in the other solvents, and a second peak at a much more positive potential of 1.7V. A third, less distinct reduction peak was observed at about 1.4V. Note also that the open circuit potential for this solvent is almost 2V.  

The anodic and cathodic scan limits were chosen for several reasons.  The negative limit of the electrochemical window for acidic liquids is at 0V and is determined by the plating of aluminum.  Therefore, acidic liquids were not scanned more negative than 0V.  For neutral or basic liquids the cathodic limit is about –2V.  However, there is no electrochemistry for any of the oxides observed more negative than 0V.  In the range of 0V to –2V only small moisture reduction peaks are observed.  Basic liquids have an electrochemical window with an anodic limit of about 1.2V, which is determined by the oxidation of chloride to chlorine.  Therefore, basic ionic liquids were not scanned more positive than 1.2V.  Neutral and acidic liquids have a limit of about 2V and the positive potential region is where most of the electrochemistry of the vanadium oxides was observed.

 Controlled potential coulometry was carried out on V2O5 in the acidic ionic liquid, as the solubility of V2O5 appeared to be highest in this solvent (compare the current scales in Figure 1). Because the concentration of the oxide was uncertain, no quantitative data can be reported, but upon electrolysis at 1.55V the solution color changed from an intense yellow to green, which is often associated with vanadium(IV) species.  Subsequent voltammograms no longer showed the reduction peak at 1.7V.  This suggests a 1e- reduction to vanadium(IV).  

A subsequent controlled potential coulometry experiment performed at 0.3V resulted in no further color change and the reduction peak at 0.5V was absent from the resulting voltammogram. Thus, the two reduction peaks observed in the acidic liquid appear to correspond to two different vanadium(V) species each undergoing a 1e-  reduction, rather than the sequential reduction of vanadium(V) to vanadium(IV)  and vanadium(III).  This is consistent with the fact that only the second peak (reduction near 0.5V) is observed in basic and neutral ionic liquids.

Sodium metavanadate, NaVO3, dissolved at 5mM concentration in neutral ionic liquid after stirring overnight and resulted in an orange solution.  NaVO3 is soluble in neutral, neutral buffered and acidic liquids, but is only slightly soluble in basic liquids.  The voltammogram of NaVO3 in neutral liquids is similar to that for V2O5 as shown in Figure 1B.  There is a reduction peak at 0.5V and an oxidation peak at about 1.3V.  The voltammogram of NaVO3 in an acidic ionic liquid is shown in Figure 2A.  Like V2O5 (Figure 1C), three reduction peaks are observed, shifted slightly to 1.2, 1.0, and 0.6V.  Comparison of the two voltammograms suggests that these peaks correspond to the same species.  Sodium orthovanadate, Na3VO4, is less soluble than NaVO3, but most of the same features can be seen in the corresponding voltammograms.  In the neutral ionic liquid the reduction peak is at 0.5V and the oxidation peak is at 1.2V.  The voltammogram of Na3VO4 in the acidic solvent is shown in Figure 2B, with only small shifts in the peaks observed.  (Because of the small currents in these figures, a voltammogram of a blank acidic ionic liquid recorded at the same current sensitivity is displayed in Figure 2C for comparison.)

Ammonium vanadate, NH4VO3, was soluble in all of the liquids surveyed.  The voltammograms of the bright yellow solution that resulted from addition to an acidic solvent (N=0.55) yielded three reduction peaks as shown in Figure 3.  The data summarized in Table 2 shows the similarity of the reduction potentials for V2O5, NaVO3, Na3VO4 and NH4VO3 in acidic ionic liquids (Figures 1C, 2A, 2B and 3, respectively).  All exhibit three irreversible reductions in the range 1.7 to 0.5V.

   VOCl3 and VOF3  in EMIC/AlCl3 Ionic Liquids.- Figure 4 shows a voltammogram of VOCl3 in a neutral ionic liquid.  The voltammogram of VOCl3 in basic ionic liquid is not shown but is similar to the voltammogram of VOCl3 in the neutral liquid.  The main feature of these voltammograms is the reduction peak at about 0.4V.  The reduction peaks at about 0.0 and –0.5V in Figure 4 are due to residual moisture in the solvent.


Controlled potential coulometry (CPC) was done to determine what species were responsible for the reduction peak at 0.4V.  A 7mM VOCl3 neutral ionic liquid was electrolyzed for 22 hours at 0.25V.  A voltammogram recorded before electrolysis was like that shown in Figure 4.  After electrolysis the 0.4V peak was gone (Figure 5) and the rest potential, as well as the remaining proton peaks, had moved more negative.  The color of the initial solution was dark brown but after electrolysis for nearly three hours it turned to a light green and after overnight electrolysis it was a light blue.  These color changes corresponded to a total of 1.2 equivalents of electrons per vanadium.  Spectra recorded before and after electrolysis are shown in Figure 6.  These demonstrate the loss of the 470nm peak.  The appearance of the low absorbance spectrum after electrolysis is consistent with the reduction of a V(V) (d0) species to a lower oxidation state V(IV) (d1) species.  Thus, it is believed that the reduction observed in the various ionic liquids at 0.4V is the reduction of V(V) to V(IV).


Figure 7A shows a voltammogram of 7mM VOCl3 in acidic ionic liquid (N=0.55) which exhibits three characteristic reduction peaks at 1.3, 0.8, and 0.4V.  After electrolysis for 20 hours at 1.0V no reduction peaks remain (Figure 7B).  Note in particular the absence of the reduction peak expected at 0.4V.  This suggests that all of the V(V) was reduced as a result of the electrolysis at 1.0V and thus, there was no V(V) left to generate the peak expected at 0.4V.  The solution changed from dark brown to dark purple after electrolysis.  These results demonstrate that there are two or three V(V) species that can be reduced, as was shown for V2O5 in acidic ionic liquids. 


Similar experiments were performed with VOF3.   VOF3 was much easier to work with because it was a stable solid.  The solid was yellow-orange, very similar in appearance to V2O5, and was soluble in neutral and acidic EMIC/AlCl3 ionic liquids.  A voltammogram of 7mM VOF3 in neutral ionic liquid looks much like that of VOCl3 in the same solvent (Figure 4).  The most important feature is the characteristic reduction peak at 0.4V.   A spectrum of this liquid exhibited a peak at 480nm that is similar to that in the spectrum for VOCl3 (Figure 6) at 470nm.


 CPC was performed on the neutral VOF3 solution and the results were similar to those observed for VOCl3, except that two new weak peaks in the visible spectrum appeared.    A spectrum of VOF3 after overnight electrolysis at 0.0V exhibited a new peak at 560nm, while the peak at 480nm was gone.  There was also a new small peak at 720nm, similar to one previously reported as due to the presence of V(IV)
.  The electrolyzed solution was deep purple.  The purple color could also be due to VCl3 or [VCl6]3-, if the reduction of VOCl3 or VOF3 led to vanadium(III) products.13, 24  



A VOF3 solution in acidic ionic liquid was also examined.  The voltammogram for this solvent was like that for VOCl3 (Figure 7A) with three reduction peaks at 1.6, 1.2, and 0.6V. 

   EMIC/VOX3 Ionic Liquids.-When an equimolar mixture of EMIC and VOCl3 was stirred in a small Erlenmeyer flask under a dry nitrogen atmosphere, a homogeneous, dark red, almost black, liquid resulted.  It is proposed that VOCl3 and EMIC react in a manner analogous to the reaction of EMIC and AlCl3:





EMIC + VOCl3   [EMI]+ + [VOCl4]-
It is also proposed that [VOCl4]- undergoes dissociation:






[VOCl4]-  VOCl3 + Cl-
This reaction is analogous to:






[AlCl4]-  AlCl3 + Cl-
in EMIC/AlCl3 ionic liquids, and






H2O  H+ + OH-
in aqueous solutions.  In each of these cases, the equilibrium lies far to the left.  This suggests that a new room temperature ionic liquid, EMIC/VOCl3, is formed.  The conductivity of the new liquid was 2mS (n=3) at 20oC.   This value can be compared to 4 mS for a sample of neutral EMIC/AlCl3 liquid that was measured as a control.  Figure 8 shows a cyclic voltammogram of a slightly basic (Nvthemole fraction VOCl3) EMIC/VOCl3 ionic liquid.  The main features observed during the negative scan were large reductions at 0.5V and –0.6V.  The current then forms a plateau.  During the positive scan, an oxidation peak was observed at 1.6V, which indicates the presence of chloride.  The anodic limit is about 2.0V.  After the experiment, when the Pt working and the Pt auxiliary electrodes were being washed, it was observed that both Pt surfaces were coated with a thick, dark film that turned brick red briefly when being washed off with tap water.  This film could account for the passivation of the electrodes during cyclic voltammetry.


As it was noticed that there was some undissolved EMIC still present, additional VOCl3 was added to make the liquid acidic (Nv > 0.5).  This led to a completely liquid sample.  A voltammogram for this liquid is shown in Figure 9.  In contrast to the basic case, the acidic liquid showed more peaks, but their resolution was poor.  The positive limit of this liquid was about 0.5V.  The currents were very high (milliamps instead of microamps) indicating that the solvent itself was being reduced.  The Pt working electrode was passivated at potentials beyond –2.0V.


The neat EMIC/VOCl3 ionic liquid was so intensely colored that a visible spectrum could not be recorded directly.  Instead, a solution was prepared by dissolving 0.4 grams of the liquid in 100 grams of CH3CN.  The spectrum (Figure 10) showed a strong absorption peak at 475nm and a very weak peak at about 660nm, and is very similar to the spectra of VOCl3 (Figure 6) and VOF3 recorded in EMIC/AlCl3 ionic liquids.  These spectra match closely the spectrum for [VOCl4]- in acetonitrile reported by Zhang and Holm
.  These workers reported a high absorbance peak at 487nm and a weak absorbance at 650nm.  Thus, we believe that [VOCl4]- is the dominant vanadium species in the EMIC/VOCl3 ionic liquid.


For comparison to VOCl3, VOF3 was mixed with EMIC under dry nitrogen in the glove box.  Since the mixtures were made from two solids, they were easy to weigh accurately and were made in three ratios: 1:1 VOF3:EMIC (NF=0.5, NF=mole fraction of VOF3, (neutral)), 2:3 VOF3:EMIC (NF=0.40, (basic)), and 3:2 VOF3:EMIC (NF=0.60, (acidic)).  The reagents were purposely not mixed to homogeneity so the contrasting colored materials could be observed.  The mixtures all turned to a uniform, dark brown solid when allowed to sit for a month.


After one month, the bottles containing the three mixtures were placed on a hotplate in the glove box and heated slowly.  In each case the solid mixtures turned to a dark red liquid, similar in appearance to the EMIC/VOCl3 ionic liquids.   The mixtures melted between 29 to 32oC.  After the mixtures became liquid they remained liquid, even after cooling to room temperature.  These results suggest the following reaction takes place:





EMIC + VOF3 EMI]+ + [VOF3Cl]-
Thus, VOF3 appears to form a mixed halide ionic liquid with EMIC.


Since the working electrode is passivated in neat EMIC/VOCl3 ionic liquids (Figures 8 and 9), the electrochemistry of the new liquids was also examined in acetonitrile.  Figure 11A shows a voltammogram made with 11mM EMIC/VOCl3 dissolved in a solution of 0.1M tetrabutylammonium perchlorate (TBAP) in dry CH3CN.    The working electrode was a Pt disk and the reference electrode was a silver wire immersed in 0.1M TBAP in CH3CN.  A series of voltammograms made to different anodic and cathodic limits demonstrated that the reduction at –0.5V and the oxidation at –0.2V were related.  Further, the reduction observed at 0.7V appeared to be coupled with the oxidation observed at 0.9V.  It is believed that this couple is the reduction of V(V) to V(IV) and oxidation back to V(V).  Note that this was not observed as a reversible reaction in any of the EMIC/AlCl3 ionic liquids.  

Figure 11B shows the results of a controlled potential coulometry experiment that was performed on this solution at 0.2V for one hour.  The large, well defined reduction peaks at 0.7V and –0.5V observed in Figure 11A are gone.  The oxidation peak at approximately 1V is now larger and there are several additional oxidation peaks more positive than 1V. The original solution was dark red, exhibiting an intense absorbance peak at 480nm (Figure 12A).  After electrolysis the solution was light blue-green and the absorbance at 480nm was replaced by a low absorbance at 720nm (Figure 12B).  Dent and coworkers13 found that [VOCl4]- was easily reduced to [VOCl4]2-.  Also, Zhang and Holm25 reported the spectrum of [VOCl4]2- in acetonitrile, which exhibits an absorbance peak at 734nm.  Hitchcock and coworkers12 reported that the visible spectrum of [EMI]2[VOCl4] in a basic EMIC/AlCl3 ionic liquid showed a major absorbance peak at 739nm.  These data suggest that the peak at 0.7V is the reduction of [VOCl4]- to [VOCl4]2-.


Figure 13 is a cyclic voltammogram of 25mM [EMI]2[VOCl4] dissolved in a solution of 0.1M TBAP in CH3CN.  Note that the voltammogram of this V(IV) compound is very similar to that for the reduction product of the new ionic liquid, EMIC/VOCl3, shown in Figure 11B.  Controlled potential coulometry was performed at 1.0V to oxidize the [EMI]2[VOCl4] solution.  The bright green solution turned to red or orange-red after only about 0.5 equivalents of electrons had passed. This color change was expected for a V(IV) compound oxidized to V(V), but the electrolysis current remained high.  When one equivalent of electrons had passed, the red-orange color began to fade.  After a total of three equivalents of electrons had passed, the solution was a faint green.  After exhaustive oxidation, a dark precipitate was observed in the cell.  The resulting voltammogram showed no distinct peaks.  This result and the observed colored precipitate suggest that much of the vanadium precipitated.  The second and third equivalents of electrons passed are believed to be due to the oxidation of chloride ion to chlorine gas, which was lost from the solution. 

Spectra were recorded for the [EMI]2[VOCl4] solution before and after oxidation.  The spectrum of the solution of the green V(IV) compound before electrolysis (Figure 14A) exhibits an intense absorbance peak at 720nm and is similar to the spectrum resulting from the one electron reduction of the EMIC/VOCl3 ionic liquid (Figure 12B).  Figure 14B is the spectrum of the [EMI]2[VOCl4] solution after oxidation.  The spectrum shows a dominant absorbance at 480nm, and is nearly identical to the spectrum for the initial solution of the new ionic liquid, EMIC/VOCl3 (Figure 12A). 

 The similarity of the spectra shown in Figures 12A and 14B, and those in Figures 14A and 12B clearly indicate that the vanadium(V) species present in the new liquid is related to the previously characterized vanadium(IV) compound, [EMI]2[VOCl4].  The reduction of the V(V) species is a one electron process.  The oxidation of the V(IV) species involves the one electron oxidation of vanadium and the oxidation of chloride.  If the mixture of EMIC and VOCl3 produces [VOCl4]-, as suggested earlier, then the electrochemical and spectroscopic data suggest the following reversible couple:

[VOCl4]-    +    e-    (    [VOCl4]2-.

When [VOCl4]2- was oxidized, the first equivalent of electrons was consumed by the oxidation of V(IV) to V(V) and explains the first color change.  The continuing high oxidation current suggests that a second process occurred.  We believe that the V(V) product, [VOCl4]-, dissociated producing Cl-, which was oxidized to Cl2 gas:

[VOCl4]-    (    VOCl3    +    Cl-
2Cl-    (    Cl2(g)    +    2e- 

VOCl3 may have been further degraded, as the solution ultimately turned nearly colorless, and yielded a precipitate that may have been a vanadium oxide.

Conclusions


Of the seven oxides of vanadium studied only four showed any solubility in EMIC/AlCl3 ionic liquids: V2O5, NaVO3, Na3VO4, and NH4VO3.  The remaining three, V2O4, V2O3, and VOSO4 were insoluble.  Two solubility trends were found.  First, the oxides were more soluble in Lewis acidic liquids than in neutral or basic liquids.  This was particularly evident for the sodium salts examined.  Secondly, it was found that the ionic compounds were more soluble than the covalent compounds.  In neutral and acidic solvents NaVO3, Na3VO4, and NH4VO3 are believed to exist as ion pairs, while in basic solvents NaCl precipitates
:

NaVO3 + Cl- ( NaCl(s) + VO3-.

An irreversible reduction peak was observed for each vanadium(V) oxide in all ionic liquids in the range from 0.9 to 0.2V.  In acidic liquids two additional irreversible reduction peaks were observed, one in the range 1.7V to 1.2V, and a smaller peak in the range 1.4 to 0.8V.  Thus, it appears that three vanadium(V) species are present and each undergoes reduction to vanadium(IV).  In general, this agrees with the work of Bell and coworkers14.  They found that at temperatures greater than 70oC V2O5 exhibited significant solubility, and various vanadium(V) species were formed depending on the Lewis acidity of the liquid. In acidic ionic liquids they reported that V2O5 reacted to form VOCl3.  The voltammograms of V2O5 and the other oxides that we have reported here also suggest that reaction with the solvent leads to various oxychloride species.  

This project was initiated to assess the use of vanadium oxides as cathode materials in room temperature ionic liquid electrolytes.  V2O5 has already been used successfully as a cathode material for high temperature thermal batteries where it is reduced to V2O4 
,
,
,
,
.  Recently, V2O5 has been used as a cathode material in room temperature ionic liquid electrolyte cells 32.  However, with these cells the V2O5 was “lithiated” (LixV2O5) and the cathode functioned as a “rocking chair” electrode, alternately intercalating Li+ ions into and back out of the V2O5 structure.  Our work has demonstrated that V2O5 and the ionic materials NaVO3, Na3VO4, and NH4VO3 are too soluble to be considered as cathode materials for practical batteries without separators.  This is particularly true when acidic liquids are used because solubility and reactivity was found to be highest in these solvents.  The insoluble materials V2O4, V2O3, or VOSO4 could be considered if solubility is the only criterion for selection.  The sodium salts were not very soluble in the NaCl buffered solvents so they may be considered as possible candidates for cathodes in those media.  When voltammetry was performed on the soluble materials it was found that the reductions were irreversible, so these materials would not function well as cathodes for rechargeable batteries even if the solubility problems were overcome.  However, it may be possible to utilize some of these materials if the solubility and migration of these active materials is controlled by inclusion in an insoluble, conductive matrix, such as a sol-gel.


The electrochemistry and visible spectroscopy of VOCl3 and VOF3 in EMIC/AlCl3 ionic liquids have also been investigated as these compounds are very soluble in EMIC/AlCl3 solvents.  Cyclic voltammograms of VOCl3 in acidic media exhibit three irreversible reduction peaks that fall in the same potential range as the reductions observed for the oxides.  The reduction peaks for VOCl3 appear to represent the same vanadium(V) species and the coulometric and spectroscopic data show that a one electron reduction leads to vanadium(IV) products.  Thus, we conclude that the oxides react with the acidic ionic liquid (probably [Al2Cl7]-) to form oxyhalides.  The experiments with VOF3 suggest that mixed halide products are formed in an analogous fashion.    


A new ionic liquid has been prepared by mixing Lewis acidic VOCl3 with Lewis basic EMIC.  The dark red liquid that results is easily reduced and has a conductivity close to that of a neutral EMIC/AlCl3 ionic liquid.  Mixing VOF3 and EMIC resulted in a dark brown solid with a melting point slightly above room temperature.  This suggests the formation of a second new ionic liquid, perhaps containing mixed halides.


Because experiments carried out in the neat EMIC/VOCl3 ionic liquid appeared to passivate the electrodes, this liquid was examined in acetonitrile.  Comparison of the electrochemical and spectroscopic data to that of a vanadium(IV) species, [EMI]2[VOCl4], showed that [VOCl4]- and [VOCl4]2- form a reversible couple.  Although the neat ionic liquid may be of limited use as a battery electrolyte because of its narrow voltage window, this solvent does stabilize some vanadium oxyhalides not easily studied in other media. 
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Table 2.  Reduction peaks for V(V) oxides and oxide salts in acidic EMIC/AlCl3
ionic liquids.

	Compound
	Reduction peaks in acidic EMIC/AlCl3 ionic liquids

	V2O5
	1.7V
	1.4V
	0.5V

	NaVO3
	1.2V
	1.0V
	0.6V

	Na3VO4
	1.2V
	0.8V
	0.6V

	NH4VO3
	1.7V
	1.3V
	0.9V
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Figure 1.  Cyclic voltammograms of V2O5 in (A) basic (N=0.45), (B) neutral (N=0.50) and (C) acidic (N=0.55) EMIC/AlCl3 ionic liquids.
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Figure 2.  Cyclic voltammograms in an acidic (N=0.55) EMIC/AlCl3 ionic liquid of (A) NaVO3  and (B) Na3VO4; and (C) a similar N=0.55 blank ionic liquid. 
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Figure 3.  A cyclic voltammogram of NH4VO3 in acidic (N=0.55) EMIC/AlCl3 ionic liquid.
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Figure 4.  A cyclic voltammogram of VOCl3 in neutral EMIC/AlCl3 ionic liquid.
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Figure 5.  A cyclic voltammogram of 7mM VOCl3 in neutral EMIC/AlCl3 ionic liquid recorded after a 22 hour electrolysis at 0.25V.
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Figure 6.  Visible spectra of VOCl3 in neutral EMIC/AlCl3 ionic liquid; before electrolysis (V(V) spectrum), and after electrolysis (V(IV) spectrum).
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Figure 7.   Cyclic voltammograms of VOCl3 in acidic EMIC/AlCl3 ionic liquid; (A) prior to electrolysis at 1.0V and (B) after electrolysis for 20 hours.
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Figure 8.  A cyclic voltammogram of a slightly basic EMIC/VOCl3 ionic liquid.
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Figure 9.  A cyclic voltammogram of an acidic EMIC/VOCl3 ionic liquid. 
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Figure 10.  Visible spectrum of 0.4 g of neutral EMIC/VOCl3 ionic liquid in 100 g CH3CN.
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Figure 11.  Cyclic voltammograms of 11mM neutral EMIC/VOCl3 ionic liquid in 0.1M TBAP in CH3CN; (A) before electrolysis, and (B) after electrolysis at 0.2V.
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Figure 12.  Visible spectra of 11mM neutral EMIC/VOCl3 ionic liquid in 0.1M TBAP in CH3CN; (A) before electrolysis, and (B) after electrolysis at 0.2V.
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Figure 13.  A cyclic voltammogram of 25mM [EMI]2[VOCl4] in 0.1M TBAP in CH3CN.  
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Figure 14.  Visible spectra of 25mM [EMI]2[VOCl4] in 0.1M TBAP in CH3CN; (A) before electrolysis and (B) after electrolysis at 1.0V.

Table 1.  Solubilities at room temperature for vanadium oxides and oxide salts in EMIC/AlCl3 ionic liquids.
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		-1.39

		-1.38

		-1.38

		-1.38

		-1.37

		-1.37

		-1.36

		-1.36

		-1.36

		-1.35

		-1.35

		-1.34

		-1.34

		-1.34

		-1.33

		-1.33

		-1.32

		-1.32

		-1.32

		-1.31

		-1.31

		-1.3

		-1.3

		-1.3

		-1.29

		-1.29

		-1.28

		-1.28

		-1.28

		-1.27

		-1.27

		-1.26

		-1.26

		-1.26

		-1.25

		-1.25

		-1.24

		-1.24

		-1.24

		-1.23

		-1.23

		-1.22

		-1.22

		-1.22

		-1.21

		-1.21

		-1.2

		-1.2

		-1.2

		-1.19

		-1.19

		-1.18

		-1.18

		-1.18

		-1.17

		-1.17

		-1.16

		-1.16

		-1.16

		-1.15

		-1.15

		-1.14

		-1.14

		-1.14

		-1.13

		-1.13

		-1.12

		-1.12

		-1.12

		-1.11

		-1.11

		-1.1

		-1.1

		-1.1

		-1.09

		-1.09

		-1.08

		-1.08

		-1.08

		-1.07

		-1.07

		-1.06

		-1.06

		-1.06

		-1.05

		-1.05

		-1.04

		-1.04

		-1.04

		-1.03

		-1.03

		-1.02

		-1.02

		-1.02

		-1.01

		-1.01

		-1

		-0.999

		-0.995

		-0.991

		-0.987

		-0.983

		-0.979

		-0.975

		-0.971

		-0.967

		-0.963

		-0.959

		-0.955

		-0.951

		-0.947

		-0.943

		-0.939

		-0.935

		-0.931

		-0.927

		-0.923

		-0.919

		-0.915

		-0.911

		-0.907

		-0.903

		-0.899

		-0.895

		-0.891

		-0.887

		-0.883

		-0.879

		-0.875

		-0.871

		-0.867

		-0.863

		-0.859

		-0.855

		-0.851

		-0.847

		-0.843

		-0.839

		-0.835

		-0.831

		-0.827

		-0.823

		-0.819

		-0.815

		-0.811

		-0.807

		-0.803

		-0.799

		-0.795

		-0.791

		-0.787

		-0.783

		-0.779

		-0.775

		-0.771

		-0.767

		-0.763

		-0.759

		-0.755

		-0.751

		-0.747

		-0.743

		-0.739

		-0.735

		-0.731

		-0.727

		-0.723

		-0.719

		-0.715

		-0.711

		-0.707

		-0.703

		-0.699

		-0.695

		-0.691

		-0.687

		-0.683

		-0.679

		-0.675

		-0.671

		-0.667

		-0.663

		-0.659

		-0.655

		-0.651

		-0.647

		-0.643

		-0.639

		-0.635

		-0.631

		-0.627

		-0.623

		-0.619

		-0.615

		-0.611

		-0.607

		-0.603

		-0.599

		-0.595

		-0.591

		-0.587

		-0.583

		-0.579

		-0.575

		-0.571

		-0.567

		-0.563

		-0.559

		-0.555

		-0.551

		-0.547

		-0.543

		-0.539

		-0.535

		-0.531

		-0.527

		-0.523

		-0.519

		-0.515

		-0.511

		-0.507

		-0.503

		-0.499

		-0.495

		-0.491

		-0.487

		-0.483

		-0.479

		-0.475

		-0.471

		-0.467

		-0.463

		-0.459

		-0.455

		-0.451

		-0.447

		-0.443

		-0.439

		-0.435

		-0.431

		-0.427

		-0.423

		-0.419

		-0.415

		-0.411

		-0.407

		-0.403

		-0.399

		-0.395

		-0.391

		-0.387

		-0.383

		-0.379

		-0.375

		-0.371

		-0.367

		-0.363

		-0.359

		-0.355

		-0.351

		-0.347

		-0.343

		-0.339

		-0.335

		-0.331

		-0.327

		-0.323

		-0.319

		-0.315

		-0.311

		-0.307

		-0.303

		-0.299

		-0.295

		-0.291

		-0.287

		-0.283

		-0.279

		-0.275

		-0.271

		-0.267

		-0.263

		-0.259

		-0.255

		-0.251

		-0.247

		-0.243

		-0.239

		-0.235

		-0.231

		-0.227

		-0.223

		-0.219

		-0.215

		-0.211

		-0.207

		-0.203

		-0.199

		-0.195

		-0.191

		-0.187

		-0.183

		-0.179

		-0.175

		-0.171

		-0.167

		-0.163

		-0.159

		-0.155

		-0.151

		-0.147

		-0.143

		-0.139

		-0.135

		-0.131

		-0.127

		-0.123

		-0.119

		-0.115

		-0.111

		-0.107

		-0.103

		-0.099

		-0.095

		-0.091

		-0.087

		-0.083

		-0.079

		-0.075

		-0.071

		-0.067

		-0.063

		-0.059

		-0.055

		-0.051

		-0.047

		-0.043

		-0.039

		-0.035

		-0.031

		-0.027

		-0.023

		-0.019

		-0.015

		-0.011

		-0.00701

		-0.00301

		0.000989

		0.00499

		0.00899

		0.013

		0.017

		0.021

		0.025

		0.029

		0.033

		0.037

		0.041

		0.045

		0.049

		0.053

		0.057

		0.061

		0.065

		0.069

		0.073

		0.077

		0.081

		0.085

		0.089

		0.093

		0.097

		0.101

		0.105

		0.109

		0.113

		0.117

		0.121

		0.125

		0.129

		0.133

		0.137

		0.141

		0.145

		0.149

		0.153

		0.157

		0.161

		0.165

		0.169

		0.173

		0.177

		0.181

		0.185

		0.189

		0.193

		0.197

		0.201

		0.205

		0.209

		0.213

		0.217

		0.221

		0.225

		0.229

		0.233

		0.237

		0.241

		0.245

		0.249

		0.253

		0.257

		0.261

		0.265

		0.269

		0.273

		0.277

		0.281

		0.285

		0.289

		0.293

		0.297

		0.301

		0.305

		0.309

		0.313

		0.317

		0.321

		0.325

		0.329

		0.333

		0.337

		0.341

		0.345

		0.349

		0.353

		0.357

		0.361

		0.365

		0.369

		0.373

		0.377

		0.381

		0.385

		0.389

		0.393

		0.397

		0.401

		0.405

		0.409

		0.413

		0.417

		0.421

		0.425

		0.429

		0.433

		0.437

		0.441

		0.445

		0.449

		0.453

		0.457

		0.461

		0.465

		0.469

		0.473

		0.477

		0.481

		0.485

		0.489

		0.493

		0.497

		0.501

		0.505

		0.509

		0.513

		0.517

		0.521

		0.525

		0.529

		0.533

		0.537

		0.541

		0.545

		0.549

		0.553

		0.557

		0.561

		0.565

		0.569

		0.573

		0.577

		0.581

		0.585

		0.589

		0.593

		0.597

		0.601

		0.605

		0.609

		0.613

		0.617

		0.621

		0.625

		0.629

		0.633

		0.637

		0.641

		0.645

		0.649

		0.653

		0.657

		0.661

		0.665

		0.669

		0.673

		0.677

		0.681

		0.685

		0.689

		0.693

		0.697

		0.701

		0.705

		0.709

		0.713

		0.717

		0.721

		0.725

		0.729

		0.733

		0.737

		0.741

		0.745

		0.749

		0.753

		0.757

		0.761

		0.765

		0.769

		0.773

		0.777

		0.781

		0.785

		0.789

		0.793

		0.797

		0.801

		0.805

		0.809

		0.813

		0.817

		0.821

		0.825

		0.829

		0.833

		0.837

		0.841

		0.845

		0.849

		0.853

		0.857

		0.861

		0.865

		0.869

		0.873

		0.877

		0.881

		0.885

		0.889

		0.893

		0.897

		0.901

		0.905

		0.909

		0.913

		0.917

		0.921

		0.925

		0.929

		0.933

		0.937

		0.941

		0.945

		0.949

		0.953

		0.957

		0.961

		0.965

		0.969

		0.973

		0.977

		0.981

		0.985

		0.989

		0.993

		0.997

		1

		1.01

		1.01

		1.01

		1.02

		1.02

		1.03

		1.03

		1.03

		1.04

		1.04

		1.05

		1.05

		1.05

		1.06

		1.06

		1.07

		1.07

		1.07

		1.08

		1.08

		1.09

		1.09

		1.09

		1.1

		1.1

		1.11

		1.11

		1.11

		1.12

		1.12

		1.13

		1.13

		1.13

		1.14

		1.14

		1.15

		1.15

		1.15

		1.16

		1.16

		1.17

		1.17

		1.17

		1.18

		1.18

		1.19

		1.19

		1.19

		1.2

		1.2

		1.21

		1.21

		1.21

		1.22

		1.22

		1.23

		1.23

		1.23

		1.24

		1.24

		1.25

		1.25

		1.25

		1.26

		1.26

		1.27

		1.27

		1.27

		1.28

		1.28

		1.29

		1.29

		1.29

		1.3

		1.3

		1.31

		1.31

		1.31

		1.32

		1.32

		1.33

		1.33

		1.33

		1.34

		1.34

		1.35

		1.35

		1.35

		1.36

		1.36

		1.37

		1.37

		1.37

		1.38

		1.38

		1.39

		1.39

		1.39

		1.4

		1.4

		1.41

		1.41

		1.41

		1.42

		1.42

		1.43

		1.43

		1.43

		1.44

		1.44

		1.45

		1.45

		1.45

		1.46

		1.46

		1.47

		1.47

		1.47

		1.48

		1.48

		1.49

		1.49

		1.49

		1.5

		1.5

		1.51

		1.51

		1.51

		1.52

		1.52

		1.53

		1.53

		1.53

		1.54

		1.54

		1.55

		1.55

		1.55

		1.56

		1.56

		1.57

		1.57

		1.57

		1.58

		1.58

		1.59

		1.59

		1.59

		1.6

		1.6

		1.61

		1.61

		1.61

		1.62

		1.62

		1.63

		1.63

		1.63

		1.64

		1.64

		1.65

		1.65

		1.65

		1.66

		1.66

		1.67

		1.67

		1.67

		1.68

		1.68

		1.69

		1.69

		1.69

		1.7

		1.7

		1.71

		1.71

		1.71

		1.72

		1.72

		1.73

		1.73

		1.73

		1.74

		1.74

		1.75

		1.75

		1.75

		1.76

		1.76

		1.77

		1.77

		1.77

		1.78

		1.78

		1.79

		1.79

		1.79

		1.8

		1.8

		1.81

		1.81

		1.81

		1.82

		1.82

		1.83

		1.83

		1.83

		1.84

		1.84

		1.85

		1.85

		1.85

		1.86

		1.86

		1.87

		1.87

		1.87

		1.88

		1.88

		1.89

		1.89

		1.89

		1.9

		1.9

		1.91

		1.91

		1.91

		1.92

		1.92

		1.93

		1.93

		1.93

		1.94

		1.94

		1.95

		1.95

		1.95

		1.96

		1.96

		1.97

		1.97

		1.97

		1.98

		1.98

		1.99

		1.99

		1.99

		2

		2

		2

		1.99

		1.99

		1.99

		1.98

		1.98

		1.97

		1.97

		1.97

		1.96

		1.96

		1.95

		1.95

		1.95

		1.94

		1.94

		1.93

		1.93

		1.93

		1.92

		1.92

		1.91

		1.91

		1.91

		1.9

		1.9

		1.89

		1.89

		1.89

		1.88

		1.88

		1.87

		1.87

		1.87

		1.86

		1.86

		1.85

		1.85

		1.85

		1.84

		1.84

		1.83

		1.83

		1.83

		1.82

		1.82

		1.81

		1.81

		1.81

		1.8

		1.8

		1.79

		1.79

		1.79

		1.78

		1.78

		1.77

		1.77

		1.77

		1.76

		1.76

		1.75

		1.75

		1.75

		1.74

		1.74

		1.73

		1.73

		1.73

		1.72

		1.72

		1.71

		1.71

		1.71

		1.7

		1.7

		1.69

		1.69

		1.69

		1.68

		1.68

		1.67

		1.67

		1.67

		1.66

		1.66

		1.65

		1.65

		1.65

		1.64

		1.64

		1.63

		1.63

		1.63

		1.62

		1.62

		1.61

		1.61

		1.61

		1.6

		1.6

		1.59

		1.59

		1.59

		1.58

		1.58

		1.57

		1.57

		1.57

		1.56

		1.56

		1.55

		1.55

		1.55

		1.54

		1.54

		1.53

		1.53

		1.53

		1.52

		1.52

		1.51

		1.51

		1.51

		1.5

		1.5

		1.49

		1.49

		1.49

		1.48

		1.48

		1.47

		1.47

		1.47

		1.46

		1.46

		1.45

		1.45

		1.45

		1.44

		1.44

		1.43

		1.43

		1.43

		1.42

		1.42

		1.41

		1.41

		1.41

		1.4

		1.4

		1.39

		1.39

		1.39

		1.38

		1.38

		1.37

		1.37

		1.37

		1.36

		1.36

		1.35

		1.35

		1.35

		1.34

		1.34

		1.33

		1.33

		1.33

		1.32

		1.32

		1.31

		1.31

		1.31

		1.3

		1.3

		1.29

		1.29

		1.29

		1.28

		1.28

		1.27

		1.27

		1.27

		1.26

		1.26

		1.25

		1.25

		1.25

		1.24

		1.24

		1.23

		1.23

		1.23

		1.22

		1.22

		1.21

		1.21

		1.21

		1.2

		1.2

		1.19

		1.19

		1.19

		1.18

		1.18

		1.17

		1.17

		1.17

		1.16

		1.16

		1.15

		1.15

		1.15

		1.14

		1.14

		1.13

		1.13

		1.13

		1.12

		1.12

		1.11

		1.11

		1.11

		1.1

		1.1

		1.09

		1.09

		1.09

		1.08

		1.08

		1.07

		1.07

		1.07

		1.06

		1.06

		1.05

		1.05

		1.05

		1.04

		1.04

		1.03

		1.03

		1.03

		1.02

		1.02

		1.01

		1.01

		1.01

		1

		0.997

		0.993

		0.989

		0.985

		0.981

		0.977

		0.973

		0.969

		0.965

		0.961

		0.957

		0.953

		0.949

		0.945

		0.941

		0.937

		0.933

		0.929

		0.925

		0.921

		0.917

		0.913

		0.909

		0.905

		0.901

		0.897

		0.893

		0.889

		0.885

		0.881

		0.877

		0.873

		0.869

		0.865

		0.861

		0.857

		0.853

		0.849

		0.845

		0.841

		0.837

		0.833

		0.829

		0.825

		0.821

		0.817

		0.813

		0.809

		0.805

		0.801

		0.797

		0.793

		0.789

		0.785

		0.781

		0.777

		0.773

		0.769

		0.765

		0.761

		0.757

		0.753



Potential (V)

Current (uA)

-0.009

0.0151

-0.0062

0.0135

0.0087

0.0017

0.0225

-0.0032

0.0216

0.015

0.0045

0.0279

0.0041

0.0232

0.0196

0.0095

0.033

0.0077

0.029

0.0254

0.0158

0.0364

0.0158

0.0359

0.0291

0.0223

0.0454

0.0192

0.042

0.0375

0.029

0.0502

0.0275

0.0497

0.024

0.0354

0.0596

0.032

0.0565

0.022

0.0472

0.056

0.0448

0.0687

0.036

0.0538

0.069

0.0544

0.09

0.0717

0.078

0.0874

0.064

0.0876

0.063

0.0753

0.09

0.0783

0.116

0.0932

0.103

0.11

0.088

0.113

0.084

0.102

0.114

0.102

0.144

0.121

0.129

0.139

0.115

0.14

0.112

0.132

0.143

0.135

0.168

0.13

0.155

0.165

0.15

0.193

0.146

0.183

0.181

0.178

0.21

0.173

0.199

0.212

0.198

0.243

0.192

0.238

0.231

0.233

0.267

0.237

0.263

0.27

0.26

0.311

0.26

0.305

0.304

0.302

0.332

0.309

0.334

0.349

0.335

0.384

0.338

0.383

0.379

0.381

0.415

0.38

0.412

0.423

0.41

0.465

0.411

0.458

0.454

0.454

0.488

0.454

0.488

0.502

0.484

0.537

0.492

0.533

0.535

0.539

0.576

0.542

0.579

0.592

0.575

0.642

0.594

0.643

0.648

0.648

0.696

0.656

0.71

0.717

0.714

0.77

0.736

0.786

0.797

0.797

0.856

0.822

0.876

0.888

0.888

0.949

0.93

0.974

0.996

0.994

1.06

1.03

1.09

1.1

1.12

1.17

1.16

1.22

1.23

1.24

1.32

1.29

1.36

1.38

1.4

1.46

1.45

1.51

1.51

1.54

1.61

1.57

1.64

1.67

1.67

1.73

1.74

1.82

1.8

1.84

1.9

1.88

1.96

1.97

2

2.06

2.05

2.1

2.13

2.15

2.19

2.18

2.25

2.26

2.25

2.33

2.28

2.36

2.36

2.37

2.46

2.42

2.46

2.46

2.47

2.54

2.53

2.53

2.58

2.59

2.63

2.56

2.66

2.64

2.69

2.68

2.68

2.7

2.75

2.7

2.82

2.75

2.81

2.83

2.84

2.86

2.87

2.94

2.96

2.98

3.02

3.02

3.08

3.1

3.1

3.14

3.13

3.18

3.23

3.26

3.29

3.28

3.37

3.39

3.45

3.48

3.51

3.6

3.66

3.7

3.75

3.76

3.88

3.9

3.97

4.04

4.09

4.19

4.28

4.32

4.39

4.45

4.55

4.65

4.7

4.79

4.85

4.97

5.06

5.12

5.22

5.27

5.42

5.47

5.53

5.65

5.72

5.84

5.94

6

6.1

6.17

6.32

6.42

6.48

6.58

6.65

6.78

6.87

6.98

7.06

7.15

7.28

7.38

7.46

7.54

7.62

7.78

7.82

7.92

7.96

8.08

8.16

8.24

8.32

8.4

8.45

8.58

8.58

8.68
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-5.25

-5.18

-5.14

-5.18

-5.12

-5.11

-5.09

-5.07

-5.07

-5.09

-5.02

-5.02

-4.96

-5.01

-4.93

-4.94

-4.93

-4.9

-4.91

-4.87

-4.85

-4.85

-4.82

-4.82

-4.85

-4.76

-4.8

-4.73

-4.76

-4.73

-4.71

-4.71

-4.63

-4.65

-4.6

-4.56

-4.59

-4.5

-4.58

-4.46

-4.48

-4.46

-4.39

-4.37

-4.34

-4.24

-4.3

-4.13

-4.16

-4.02

-4

-3.93

-3.86

-3.78

-3.71

-3.59

-3.57

-3.37

-3.38

-3.15

-3.09

-2.97

-2.81

-2.68

-2.54

-2.35

-2.28

-1.97

-1.9

-1.71

-1.46

-1.26

-1.1

-0.898

-0.72

-0.577

-0.335

-0.181

-0.031

0.127

0.28

0.465

0.56

0.69

0.83

0.92

1.04

1.23

1.29

1.43

1.51

1.65

1.69

1.78

1.93

1.97

2.06

2.17

2.23

2.31

2.37

2.5

2.58

2.61

2.73

2.84

2.9

2.98

3.09

3.16

3.26

3.37

3.46

3.53

3.64

3.73

3.87

3.86

4.02

4.06

4.18

4.26

4.3

4.38

4.43

4.52

4.65

4.58

4.72

4.72

4.75

4.81

4.81

4.82

4.83

4.78

4.84

4.64

4.69

4.59

4.61

4.44

4.36

4.27

4.17

4.09

4.01

3.82

3.74

3.66

3.61

3.5

3.32

3.26

3.15

3.11

2.96

2.86

2.81

2.71

2.71

2.58

2.5

2.43

2.43

2.37

2.28

2.18

2.2

2.13

2.12

2.05

1.94

1.92

1.95

1.95

1.87

1.81

1.78

1.75

1.78

1.7

1.66

1.67

1.66

1.67

1.61

1.52

1.52

1.6

1.55

1.52

1.46

1.44

1.47

1.49

1.39

1.36

1.38

1.44

1.36

1.4

1.28

1.35

1.32

1.37

1.26

1.31

1.19

1.31

1.22

1.28
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		1.13E+00		1.94E-02		1.94E-08		7.53E-01		-9.00E-03		-9.00E-09

		1.13E+00		1.13E-01		1.13E-07		7.49E-01		1.51E-02		1.51E-08

		1.12E+00		1.06E-01		1.06E-07		7.45E-01		-6.20E-03		-6.20E-09

		1.12E+00		1.65E-01		1.65E-07		7.41E-01		1.35E-02		1.35E-08

		1.11E+00		2.10E-01		2.10E-07		7.37E-01		8.70E-03		8.70E-09

		1.11E+00		2.30E-01		2.30E-07		7.33E-01		1.70E-03		1.70E-09

		1.11E+00		2.79E-01		2.79E-07		7.29E-01		2.25E-02		2.25E-08

		1.10E+00		2.48E-01		2.48E-07		7.25E-01		-3.20E-03		-3.20E-09

		1.10E+00		2.90E-01		2.90E-07		7.21E-01		2.16E-02		2.16E-08

		1.09E+00		3.24E-01		3.24E-07		7.17E-01		1.50E-02		1.50E-08

		1.09E+00		3.23E-01		3.23E-07		7.13E-01		4.50E-03		4.50E-09

		1.09E+00		3.81E-01		3.81E-07		7.09E-01		2.79E-02		2.79E-08

		1.08E+00		3.15E-01		3.15E-07		7.05E-01		4.10E-03		4.10E-09

		1.08E+00		3.57E-01		3.57E-07		7.01E-01		2.32E-02		2.32E-08

		1.07E+00		3.82E-01		3.82E-07		6.97E-01		1.96E-02		1.96E-08

		1.07E+00		3.68E-01		3.68E-07		6.93E-01		9.50E-03		9.50E-09

		1.07E+00		4.29E-01		4.29E-07		6.89E-01		3.30E-02		3.30E-08

		1.06E+00		3.51E-01		3.51E-07		6.85E-01		7.70E-03		7.70E-09

		1.06E+00		4.01E-01		4.01E-07		6.81E-01		2.90E-02		2.90E-08

		1.05E+00		4.08E-01		4.08E-07		6.77E-01		2.54E-02		2.54E-08

		1.05E+00		3.94E-01		3.94E-07		6.73E-01		1.58E-02		1.58E-08

		1.05E+00		4.51E-01		4.51E-07		6.69E-01		3.64E-02		3.64E-08

		1.04E+00		3.72E-01		3.72E-07		6.65E-01		1.58E-02		1.58E-08

		1.04E+00		4.19E-01		4.19E-07		6.61E-01		3.59E-02		3.59E-08

		1.03E+00		4.20E-01		4.20E-07		6.57E-01		2.91E-02		2.91E-08

		1.03E+00		4.10E-01		4.10E-07		6.53E-01		2.23E-02		2.23E-08

		1.03E+00		4.48E-01		4.48E-07		6.49E-01		4.54E-02		4.54E-08

		1.02E+00		3.85E-01		3.85E-07		6.45E-01		1.92E-02		1.92E-08

		1.02E+00		4.35E-01		4.35E-07		6.41E-01		4.20E-02		4.20E-08

		1.01E+00		4.21E-01		4.21E-07		6.37E-01		3.75E-02		3.75E-08

		1.01E+00		4.18E-01		4.18E-07		6.33E-01		2.90E-02		2.90E-08

		1.01E+00		4.55E-01		4.55E-07		6.29E-01		5.02E-02		5.02E-08

		1.00E+00		3.98E-01		3.98E-07		6.25E-01		2.75E-02		2.75E-08

		9.98E-01		4.23E-01		4.23E-07		6.21E-01		4.97E-02		4.97E-08

		9.94E-01		4.39E-01		4.39E-07		6.17E-01		2.40E-02		2.40E-08

		9.90E-01		4.26E-01		4.26E-07		6.13E-01		3.54E-02		3.54E-08

		9.86E-01		4.59E-01		4.59E-07		6.09E-01		5.96E-02		5.96E-08

		9.82E-01		4.02E-01		4.02E-07		6.05E-01		3.20E-02		3.20E-08

		9.78E-01		4.40E-01		4.40E-07		6.01E-01		5.65E-02		5.65E-08

		9.74E-01		4.50E-01		4.50E-07		5.97E-01		2.20E-02		2.20E-08

		9.70E-01		4.23E-01		4.23E-07		5.93E-01		4.72E-02		4.72E-08

		9.66E-01		4.76E-01		4.76E-07		5.89E-01		5.60E-02		5.60E-08

		9.62E-01		4.20E-01		4.20E-07		5.85E-01		4.48E-02		4.48E-08

		9.58E-01		4.50E-01		4.50E-07		5.81E-01		6.87E-02		6.87E-08

		9.54E-01		4.65E-01		4.65E-07		5.77E-01		3.60E-02		3.60E-08

		9.50E-01		4.36E-01		4.36E-07		5.73E-01		5.38E-02		5.38E-08

		9.46E-01		4.90E-01		4.90E-07		5.69E-01		6.90E-02		6.90E-08

		9.42E-01		4.08E-01		4.08E-07		5.65E-01		5.44E-02		5.44E-08

		9.38E-01		4.68E-01		4.68E-07		5.61E-01		9.00E-02		9.00E-08

		9.34E-01		4.95E-01		4.95E-07		5.57E-01		7.17E-02		7.17E-08

		9.30E-01		4.55E-01		4.55E-07		5.53E-01		7.80E-02		7.80E-08

		9.26E-01		5.15E-01		5.15E-07		5.49E-01		8.74E-02		8.74E-08

		9.22E-01		4.38E-01		4.38E-07		5.45E-01		6.40E-02		6.40E-08

		9.18E-01		4.92E-01		4.92E-07		5.41E-01		8.76E-02		8.76E-08

		9.14E-01		4.92E-01		4.92E-07		5.37E-01		6.30E-02		6.30E-08

		9.10E-01		4.82E-01		4.82E-07		5.33E-01		7.53E-02		7.53E-08

		9.06E-01		5.43E-01		5.43E-07		5.29E-01		9.00E-02		9.00E-08

		9.02E-01		4.57E-01		4.57E-07		5.25E-01		7.83E-02		7.83E-08

		8.98E-01		5.19E-01		5.19E-07		5.21E-01		1.16E-01		1.16E-07

		8.94E-01		5.31E-01		5.31E-07		5.17E-01		9.32E-02		9.32E-08

		8.90E-01		5.15E-01		5.15E-07		5.13E-01		1.03E-01		1.03E-07

		8.86E-01		5.55E-01		5.55E-07		5.09E-01		1.10E-01		1.10E-07

		8.82E-01		5.02E-01		5.02E-07		5.05E-01		8.80E-02		8.80E-08

		8.78E-01		5.58E-01		5.58E-07		5.01E-01		1.13E-01		1.13E-07

		8.74E-01		5.67E-01		5.67E-07		4.97E-01		8.40E-02		8.40E-08

		8.70E-01		5.54E-01		5.54E-07		4.93E-01		1.02E-01		1.02E-07

		8.66E-01		5.95E-01		5.95E-07		4.89E-01		1.14E-01		1.14E-07

		8.62E-01		5.45E-01		5.45E-07		4.85E-01		1.02E-01		1.02E-07

		8.58E-01		5.87E-01		5.87E-07		4.81E-01		1.44E-01		1.44E-07

		8.54E-01		6.18E-01		6.18E-07		4.77E-01		1.21E-01		1.21E-07

		8.50E-01		6.00E-01		6.00E-07		4.73E-01		1.29E-01		1.29E-07

		8.46E-01		6.36E-01		6.36E-07		4.69E-01		1.39E-01		1.39E-07

		8.42E-01		5.95E-01		5.95E-07		4.65E-01		1.15E-01		1.15E-07

		8.38E-01		6.40E-01		6.40E-07		4.61E-01		1.40E-01		1.40E-07

		8.34E-01		6.66E-01		6.66E-07		4.57E-01		1.12E-01		1.12E-07

		8.30E-01		6.41E-01		6.41E-07		4.53E-01		1.32E-01		1.32E-07

		8.26E-01		6.89E-01		6.89E-07		4.49E-01		1.43E-01		1.43E-07

		8.22E-01		6.46E-01		6.46E-07		4.45E-01		1.35E-01		1.35E-07

		8.18E-01		6.96E-01		6.96E-07		4.41E-01		1.68E-01		1.68E-07

		8.14E-01		7.23E-01		7.23E-07		4.37E-01		1.30E-01		1.30E-07

		8.10E-01		7.04E-01		7.04E-07		4.33E-01		1.55E-01		1.55E-07

		8.06E-01		7.55E-01		7.55E-07		4.29E-01		1.65E-01		1.65E-07

		8.02E-01		6.88E-01		6.88E-07		4.25E-01		1.50E-01		1.50E-07

		7.98E-01		7.66E-01		7.66E-07		4.21E-01		1.93E-01		1.93E-07

		7.94E-01		7.81E-01		7.81E-07		4.17E-01		1.46E-01		1.46E-07

		7.90E-01		7.65E-01		7.65E-07		4.13E-01		1.83E-01		1.83E-07

		7.86E-01		8.20E-01		8.20E-07		4.09E-01		1.81E-01		1.81E-07

		7.82E-01		7.56E-01		7.56E-07		4.05E-01		1.78E-01		1.78E-07

		7.78E-01		8.29E-01		8.29E-07		4.01E-01		2.10E-01		2.10E-07

		7.74E-01		8.39E-01		8.39E-07		3.97E-01		1.73E-01		1.73E-07

		7.70E-01		8.38E-01		8.38E-07		3.93E-01		1.99E-01		1.99E-07

		7.66E-01		8.74E-01		8.74E-07		3.89E-01		2.12E-01		2.12E-07

		7.62E-01		8.22E-01		8.22E-07		3.85E-01		1.98E-01		1.98E-07

		7.58E-01		9.08E-01		9.08E-07		3.81E-01		2.43E-01		2.43E-07

		7.54E-01		9.18E-01		9.18E-07		3.77E-01		1.92E-01		1.92E-07

		7.50E-01		9.14E-01		9.14E-07		3.73E-01		2.38E-01		2.38E-07

		7.46E-01		9.38E-01		9.38E-07		3.69E-01		2.31E-01		2.31E-07

		7.42E-01		9.12E-01		9.12E-07		3.65E-01		2.33E-01		2.33E-07

		7.38E-01		9.71E-01		9.71E-07		3.61E-01		2.67E-01		2.67E-07

		7.34E-01		9.99E-01		9.99E-07		3.57E-01		2.37E-01		2.37E-07

		7.30E-01		1.00E+00		1.00E-06		3.53E-01		2.63E-01		2.63E-07

		7.26E-01		1.03E+00		1.03E-06		3.49E-01		2.70E-01		2.70E-07

		7.22E-01		9.94E-01		9.94E-07		3.45E-01		2.60E-01		2.60E-07

		7.18E-01		1.06E+00		1.06E-06		3.41E-01		3.11E-01		3.11E-07

		7.14E-01		1.10E+00		1.10E-06		3.37E-01		2.60E-01		2.60E-07

		7.10E-01		1.08E+00		1.08E-06		3.33E-01		3.05E-01		3.05E-07

		7.06E-01		1.11E+00		1.11E-06		3.29E-01		3.04E-01		3.04E-07

		7.02E-01		1.10E+00		1.10E-06		3.25E-01		3.02E-01		3.02E-07

		6.98E-01		1.17E+00		1.17E-06		3.21E-01		3.32E-01		3.32E-07

		6.94E-01		1.21E+00		1.21E-06		3.17E-01		3.09E-01		3.09E-07

		6.90E-01		1.20E+00		1.20E-06		3.13E-01		3.34E-01		3.34E-07

		6.86E-01		1.25E+00		1.25E-06		3.09E-01		3.49E-01		3.49E-07

		6.82E-01		1.23E+00		1.23E-06		3.05E-01		3.35E-01		3.35E-07

		6.78E-01		1.31E+00		1.31E-06		3.01E-01		3.84E-01		3.84E-07

		6.74E-01		1.36E+00		1.36E-06		2.97E-01		3.38E-01		3.38E-07

		6.70E-01		1.37E+00		1.37E-06		2.93E-01		3.83E-01		3.83E-07

		6.66E-01		1.41E+00		1.41E-06		2.89E-01		3.79E-01		3.79E-07

		6.62E-01		1.41E+00		1.41E-06		2.85E-01		3.81E-01		3.81E-07

		6.58E-01		1.51E+00		1.51E-06		2.81E-01		4.15E-01		4.15E-07

		6.54E-01		1.46E+00		1.46E-06		2.77E-01		3.80E-01		3.80E-07

		6.50E-01		1.53E+00		1.53E-06		2.73E-01		4.12E-01		4.12E-07

		6.46E-01		1.51E+00		1.51E-06		2.69E-01		4.23E-01		4.23E-07

		6.42E-01		1.64E+00		1.64E-06		2.65E-01		4.10E-01		4.10E-07

		6.38E-01		1.68E+00		1.68E-06		2.61E-01		4.65E-01		4.65E-07

		6.34E-01		1.77E+00		1.77E-06		2.57E-01		4.11E-01		4.11E-07

		6.30E-01		1.81E+00		1.81E-06		2.53E-01		4.58E-01		4.58E-07

		6.26E-01		1.86E+00		1.86E-06		2.49E-01		4.54E-01		4.54E-07

		6.22E-01		1.94E+00		1.94E-06		2.45E-01		4.54E-01		4.54E-07

		6.18E-01		2.01E+00		2.01E-06		2.41E-01		4.88E-01		4.88E-07

		6.14E-01		2.12E+00		2.12E-06		2.37E-01		4.54E-01		4.54E-07

		6.10E-01		2.17E+00		2.17E-06		2.33E-01		4.88E-01		4.88E-07

		6.06E-01		2.30E+00		2.30E-06		2.29E-01		5.02E-01		5.02E-07

		6.02E-01		2.39E+00		2.39E-06		2.25E-01		4.84E-01		4.84E-07

		5.98E-01		2.50E+00		2.50E-06		2.21E-01		5.37E-01		5.37E-07

		5.94E-01		2.62E+00		2.62E-06		2.17E-01		4.92E-01		4.92E-07

		5.90E-01		2.75E+00		2.75E-06		2.13E-01		5.33E-01		5.33E-07

		5.86E-01		2.89E+00		2.89E-06		2.09E-01		5.35E-01		5.35E-07

		5.82E-01		3.03E+00		3.03E-06		2.05E-01		5.39E-01		5.39E-07

		5.78E-01		3.23E+00		3.23E-06		2.01E-01		5.76E-01		5.76E-07

		5.74E-01		3.37E+00		3.37E-06		1.97E-01		5.42E-01		5.42E-07

		5.70E-01		3.54E+00		3.54E-06		1.93E-01		5.79E-01		5.79E-07

		5.66E-01		3.71E+00		3.71E-06		1.89E-01		5.92E-01		5.92E-07

		5.62E-01		3.97E+00		3.97E-06		1.85E-01		5.75E-01		5.75E-07

		5.58E-01		4.20E+00		4.20E-06		1.81E-01		6.42E-01		6.42E-07

		5.54E-01		4.45E+00		4.45E-06		1.77E-01		5.94E-01		5.94E-07

		5.50E-01		4.72E+00		4.72E-06		1.73E-01		6.43E-01		6.43E-07

		5.46E-01		4.99E+00		4.99E-06		1.69E-01		6.48E-01		6.48E-07

		5.42E-01		5.30E+00		5.30E-06		1.65E-01		6.48E-01		6.48E-07

		5.38E-01		5.57E+00		5.57E-06		1.61E-01		6.96E-01		6.96E-07

		5.34E-01		5.89E+00		5.89E-06		1.57E-01		6.56E-01		6.56E-07

		5.30E-01		6.24E+00		6.24E-06		1.53E-01		7.10E-01		7.10E-07

		5.26E-01		6.60E+00		6.60E-06		1.49E-01		7.17E-01		7.17E-07

		5.22E-01		6.98E+00		6.98E-06		1.45E-01		7.14E-01		7.14E-07

		5.18E-01		7.31E+00		7.31E-06		1.41E-01		7.70E-01		7.70E-07

		5.14E-01		7.72E+00		7.72E-06		1.37E-01		7.36E-01		7.36E-07

		5.10E-01		8.11E+00		8.11E-06		1.33E-01		7.86E-01		7.86E-07

		5.06E-01		8.42E+00		8.42E-06		1.29E-01		7.97E-01		7.97E-07

		5.02E-01		8.82E+00		8.82E-06		1.25E-01		7.97E-01		7.97E-07

		4.98E-01		9.11E+00		9.11E-06		1.21E-01		8.56E-01		8.56E-07

		4.94E-01		9.56E+00		9.56E-06		1.17E-01		8.22E-01		8.22E-07

		4.90E-01		9.86E+00		9.86E-06		1.13E-01		8.76E-01		8.76E-07

		4.86E-01		1.02E+01		1.02E-05		1.09E-01		8.88E-01		8.88E-07

		4.82E-01		1.05E+01		1.05E-05		1.05E-01		8.88E-01		8.88E-07

		4.78E-01		1.08E+01		1.08E-05		1.01E-01		9.49E-01		9.49E-07

		4.74E-01		1.10E+01		1.10E-05		9.70E-02		9.30E-01		9.30E-07

		4.70E-01		1.13E+01		1.13E-05		9.30E-02		9.74E-01		9.74E-07

		4.66E-01		1.16E+01		1.16E-05		8.90E-02		9.96E-01		9.96E-07

		4.62E-01		1.17E+01		1.17E-05		8.50E-02		9.94E-01		9.94E-07

		4.58E-01		1.19E+01		1.19E-05		8.10E-02		1.06E+00		1.06E-06

		4.54E-01		1.21E+01		1.21E-05		7.70E-02		1.03E+00		1.03E-06

		4.50E-01		1.22E+01		1.22E-05		7.30E-02		1.09E+00		1.09E-06

		4.46E-01		1.23E+01		1.23E-05		6.90E-02		1.10E+00		1.10E-06

		4.42E-01		1.22E+01		1.22E-05		6.50E-02		1.12E+00		1.12E-06

		4.38E-01		1.24E+01		1.24E-05		6.10E-02		1.17E+00		1.17E-06

		4.34E-01		1.24E+01		1.24E-05		5.70E-02		1.16E+00		1.16E-06

		4.30E-01		1.24E+01		1.24E-05		5.30E-02		1.22E+00		1.22E-06

		4.26E-01		1.25E+01		1.25E-05		4.90E-02		1.23E+00		1.23E-06

		4.22E-01		1.23E+01		1.23E-05		4.50E-02		1.24E+00		1.24E-06

		4.18E-01		1.23E+01		1.23E-05		4.10E-02		1.32E+00		1.32E-06

		4.14E-01		1.22E+01		1.22E-05		3.70E-02		1.29E+00		1.29E-06

		4.10E-01		1.22E+01		1.22E-05		3.30E-02		1.36E+00		1.36E-06

		4.06E-01		1.22E+01		1.22E-05		2.90E-02		1.38E+00		1.38E-06

		4.02E-01		1.20E+01		1.20E-05		2.50E-02		1.40E+00		1.40E-06

		3.98E-01		1.20E+01		1.20E-05		2.10E-02		1.46E+00		1.46E-06

		3.94E-01		1.19E+01		1.19E-05		1.70E-02		1.45E+00		1.45E-06

		3.90E-01		1.17E+01		1.17E-05		1.30E-02		1.51E+00		1.51E-06

		3.86E-01		1.16E+01		1.16E-05		9.00E-03		1.51E+00		1.51E-06

		3.82E-01		1.15E+01		1.15E-05		5.00E-03		1.54E+00		1.54E-06

		3.78E-01		1.14E+01		1.14E-05		9.99E-04		1.61E+00		1.61E-06

		3.74E-01		1.13E+01		1.13E-05		-3.00E-03		1.57E+00		1.57E-06

		3.70E-01		1.12E+01		1.12E-05		-7.00E-03		1.64E+00		1.64E-06

		3.66E-01		1.12E+01		1.12E-05		-1.10E-02		1.67E+00		1.67E-06

		3.62E-01		1.09E+01		1.09E-05		-1.50E-02		1.67E+00		1.67E-06

		3.58E-01		1.09E+01		1.09E-05		-1.90E-02		1.73E+00		1.73E-06

		3.54E-01		1.08E+01		1.08E-05		-2.30E-02		1.74E+00		1.74E-06

		3.50E-01		1.07E+01		1.07E-05		-2.70E-02		1.82E+00		1.82E-06

		3.46E-01		1.06E+01		1.06E-05		-3.10E-02		1.80E+00		1.80E-06

		3.42E-01		1.05E+01		1.05E-05		-3.50E-02		1.84E+00		1.84E-06

		3.38E-01		1.04E+01		1.04E-05		-3.90E-02		1.90E+00		1.90E-06

		3.34E-01		1.03E+01		1.03E-05		-4.30E-02		1.88E+00		1.88E-06

		3.30E-01		1.03E+01		1.03E-05		-4.70E-02		1.96E+00		1.96E-06

		3.26E-01		1.02E+01		1.02E-05		-5.10E-02		1.97E+00		1.97E-06

		3.22E-01		1.00E+01		1.00E-05		-5.50E-02		2.00E+00		2.00E-06

		3.18E-01		1.01E+01		1.01E-05		-5.90E-02		2.06E+00		2.06E-06

		3.14E-01		1.00E+01		1.00E-05		-6.30E-02		2.05E+00		2.05E-06

		3.10E-01		9.94E+00		9.94E-06		-6.70E-02		2.10E+00		2.10E-06

		3.06E-01		9.91E+00		9.91E-06		-7.10E-02		2.13E+00		2.13E-06

		3.02E-01		9.72E+00		9.72E-06		-7.50E-02		2.15E+00		2.15E-06

		2.98E-01		9.79E+00		9.79E-06		-7.90E-02		2.19E+00		2.19E-06

		2.94E-01		9.67E+00		9.67E-06		-8.30E-02		2.18E+00		2.18E-06

		2.90E-01		9.68E+00		9.68E-06		-8.70E-02		2.25E+00		2.25E-06

		2.86E-01		9.68E+00		9.68E-06		-9.10E-02		2.26E+00		2.26E-06

		2.82E-01		9.59E+00		9.59E-06		-9.50E-02		2.25E+00		2.25E-06

		2.78E-01		9.64E+00		9.64E-06		-9.90E-02		2.33E+00		2.33E-06

		2.74E-01		9.61E+00		9.61E-06		-1.03E-01		2.28E+00		2.28E-06

		2.70E-01		9.58E+00		9.58E-06		-1.07E-01		2.36E+00		2.36E-06

		2.66E-01		9.50E+00		9.50E-06		-1.11E-01		2.36E+00		2.36E-06

		2.62E-01		9.51E+00		9.51E-06		-1.15E-01		2.37E+00		2.37E-06

		2.58E-01		9.55E+00		9.55E-06		-1.19E-01		2.46E+00		2.46E-06

		2.54E-01		9.58E+00		9.58E-06		-1.23E-01		2.42E+00		2.42E-06

		2.50E-01		9.56E+00		9.56E-06		-1.27E-01		2.46E+00		2.46E-06

		2.46E-01		9.56E+00		9.56E-06		-1.31E-01		2.46E+00		2.46E-06

		2.42E-01		9.59E+00		9.59E-06		-1.35E-01		2.47E+00		2.47E-06

		2.38E-01		9.59E+00		9.59E-06		-1.39E-01		2.54E+00		2.54E-06

		2.34E-01		9.67E+00		9.67E-06		-1.43E-01		2.53E+00		2.53E-06

		2.30E-01		9.65E+00		9.65E-06		-1.47E-01		2.53E+00		2.53E-06

		2.26E-01		9.71E+00		9.71E-06		-1.51E-01		2.58E+00		2.58E-06

		2.22E-01		9.76E+00		9.76E-06		-1.55E-01		2.59E+00		2.59E-06

		2.18E-01		9.84E+00		9.84E-06		-1.59E-01		2.63E+00		2.63E-06

		2.14E-01		9.88E+00		9.88E-06		-1.63E-01		2.56E+00		2.56E-06

		2.10E-01		9.92E+00		9.92E-06		-1.67E-01		2.66E+00		2.66E-06

		2.06E-01		1.00E+01		1.00E-05		-1.71E-01		2.64E+00		2.64E-06

		2.02E-01		1.01E+01		1.01E-05		-1.75E-01		2.69E+00		2.69E-06

		1.98E-01		1.03E+01		1.03E-05		-1.79E-01		2.68E+00		2.68E-06

		1.94E-01		1.04E+01		1.04E-05		-1.83E-01		2.68E+00		2.68E-06

		1.90E-01		1.05E+01		1.05E-05		-1.87E-01		2.70E+00		2.70E-06

		1.86E-01		1.06E+01		1.06E-05		-1.91E-01		2.75E+00		2.75E-06

		1.82E-01		1.07E+01		1.07E-05		-1.95E-01		2.70E+00		2.70E-06

		1.78E-01		1.09E+01		1.09E-05		-1.99E-01		2.82E+00		2.82E-06

		1.74E-01		1.11E+01		1.11E-05		-2.03E-01		2.75E+00		2.75E-06

		1.70E-01		1.12E+01		1.12E-05		-2.07E-01		2.81E+00		2.81E-06

		1.66E-01		1.13E+01		1.13E-05		-2.11E-01		2.83E+00		2.83E-06

		1.62E-01		1.16E+01		1.16E-05		-2.15E-01		2.84E+00		2.84E-06

		1.58E-01		1.18E+01		1.18E-05		-2.19E-01		2.86E+00		2.86E-06

		1.54E-01		1.19E+01		1.19E-05		-2.23E-01		2.87E+00		2.87E-06

		1.50E-01		1.22E+01		1.22E-05		-2.27E-01		2.94E+00		2.94E-06

		1.46E-01		1.24E+01		1.24E-05		-2.31E-01		2.96E+00		2.96E-06

		1.42E-01		1.27E+01		1.27E-05		-2.35E-01		2.98E+00		2.98E-06

		1.38E-01		1.29E+01		1.29E-05		-2.39E-01		3.02E+00		3.02E-06

		1.34E-01		1.32E+01		1.32E-05		-2.43E-01		3.02E+00		3.02E-06

		1.30E-01		1.34E+01		1.34E-05		-2.47E-01		3.08E+00		3.08E-06

		1.26E-01		1.35E+01		1.35E-05		-2.51E-01		3.10E+00		3.10E-06

		1.22E-01		1.39E+01		1.39E-05		-2.55E-01		3.10E+00		3.10E-06

		1.18E-01		1.42E+01		1.42E-05		-2.59E-01		3.14E+00		3.14E-06

		1.14E-01		1.44E+01		1.44E-05		-2.63E-01		3.13E+00		3.13E-06

		1.10E-01		1.46E+01		1.46E-05		-2.67E-01		3.18E+00		3.18E-06

		1.06E-01		1.49E+01		1.49E-05		-2.71E-01		3.23E+00		3.23E-06

		1.02E-01		1.52E+01		1.52E-05		-2.75E-01		3.26E+00		3.26E-06

		9.80E-02		1.53E+01		1.53E-05		-2.79E-01		3.29E+00		3.29E-06

		9.40E-02		1.57E+01		1.57E-05		-2.83E-01		3.28E+00		3.28E-06

		9.00E-02		1.58E+01		1.58E-05		-2.87E-01		3.37E+00		3.37E-06

		8.60E-02		1.60E+01		1.60E-05		-2.91E-01		3.39E+00		3.39E-06

		8.20E-02		1.63E+01		1.63E-05		-2.95E-01		3.45E+00		3.45E-06

		7.80E-02		1.65E+01		1.65E-05		-2.99E-01		3.48E+00		3.48E-06

		7.40E-02		1.67E+01		1.67E-05		-3.03E-01		3.51E+00		3.51E-06

		7.00E-02		1.68E+01		1.68E-05		-3.07E-01		3.60E+00		3.60E-06

		6.60E-02		1.70E+01		1.70E-05		-3.11E-01		3.66E+00		3.66E-06

		6.20E-02		1.72E+01		1.72E-05		-3.15E-01		3.70E+00		3.70E-06

		5.80E-02		1.74E+01		1.74E-05		-3.19E-01		3.75E+00		3.75E-06

		5.40E-02		1.76E+01		1.76E-05		-3.23E-01		3.76E+00		3.76E-06

		5.00E-02		1.77E+01		1.77E-05		-3.27E-01		3.88E+00		3.88E-06

		4.60E-02		1.78E+01		1.78E-05		-3.31E-01		3.90E+00		3.90E-06

		4.20E-02		1.80E+01		1.80E-05		-3.35E-01		3.97E+00		3.97E-06

		3.80E-02		1.82E+01		1.82E-05		-3.39E-01		4.04E+00		4.04E-06

		3.40E-02		1.82E+01		1.82E-05		-3.43E-01		4.09E+00		4.09E-06

		3.00E-02		1.84E+01		1.84E-05		-3.47E-01		4.19E+00		4.19E-06

		2.60E-02		1.83E+01		1.83E-05		-3.51E-01		4.28E+00		4.28E-06

		2.20E-02		1.85E+01		1.85E-05		-3.55E-01		4.32E+00		4.32E-06

		1.80E-02		1.82E+01		1.82E-05		-3.59E-01		4.39E+00		4.39E-06

		1.40E-02		1.84E+01		1.84E-05		-3.63E-01		4.45E+00		4.45E-06

		1.00E-02		1.86E+01		1.86E-05		-3.67E-01		4.55E+00		4.55E-06

		6.00E-03		1.84E+01		1.84E-05		-3.71E-01		4.65E+00		4.65E-06

		2.00E-03		1.87E+01		1.87E-05		-3.75E-01		4.70E+00		4.70E-06

		-2.00E-03		1.90E+01		1.90E-05		-3.79E-01		4.79E+00		4.79E-06

		-6.00E-03		1.87E+01		1.87E-05		-3.83E-01		4.85E+00		4.85E-06

		-1.00E-02		1.87E+01		1.87E-05		-3.87E-01		4.97E+00		4.97E-06

		-1.40E-02		1.87E+01		1.87E-05		-3.91E-01		5.06E+00		5.06E-06

		-1.80E-02		1.85E+01		1.85E-05		-3.95E-01		5.12E+00		5.12E-06

		-2.20E-02		1.86E+01		1.86E-05		-3.99E-01		5.22E+00		5.22E-06

		-2.60E-02		1.84E+01		1.84E-05		-4.03E-01		5.27E+00		5.27E-06

		-3.00E-02		1.85E+01		1.85E-05		-4.07E-01		5.42E+00		5.42E-06

		-3.40E-02		1.83E+01		1.83E-05		-4.11E-01		5.47E+00		5.47E-06

		-3.80E-02		1.84E+01		1.84E-05		-4.15E-01		5.53E+00		5.53E-06

		-4.20E-02		1.83E+01		1.83E-05		-4.19E-01		5.65E+00		5.65E-06

		-4.60E-02		1.83E+01		1.83E-05		-4.23E-01		5.72E+00		5.72E-06

		-5.00E-02		1.81E+01		1.81E-05		-4.27E-01		5.84E+00		5.84E-06

		-5.40E-02		1.80E+01		1.80E-05		-4.31E-01		5.94E+00		5.94E-06

		-5.80E-02		1.81E+01		1.81E-05		-4.35E-01		6.00E+00		6.00E-06

		-6.20E-02		1.80E+01		1.80E-05		-4.39E-01		6.10E+00		6.10E-06

		-6.60E-02		1.78E+01		1.78E-05		-4.43E-01		6.17E+00		6.17E-06

		-7.00E-02		1.77E+01		1.77E-05		-4.47E-01		6.32E+00		6.32E-06

		-7.40E-02		1.77E+01		1.77E-05		-4.51E-01		6.42E+00		6.42E-06

		-7.80E-02		1.78E+01		1.78E-05		-4.55E-01		6.48E+00		6.48E-06

		-8.20E-02		1.74E+01		1.74E-05		-4.59E-01		6.58E+00		6.58E-06

		-8.60E-02		1.73E+01		1.73E-05		-4.63E-01		6.65E+00		6.65E-06

		-9.00E-02		1.75E+01		1.75E-05		-4.67E-01		6.78E+00		6.78E-06

		-9.40E-02		1.74E+01		1.74E-05		-4.71E-01		6.87E+00		6.87E-06

		-9.80E-02		1.75E+01		1.75E-05		-4.75E-01		6.98E+00		6.98E-06

		-1.02E-01		1.73E+01		1.73E-05		-4.79E-01		7.06E+00		7.06E-06

		-1.06E-01		1.70E+01		1.70E-05		-4.83E-01		7.15E+00		7.15E-06

		-1.10E-01		1.71E+01		1.71E-05		-4.87E-01		7.28E+00		7.28E-06

		-1.14E-01		1.70E+01		1.70E-05		-4.91E-01		7.38E+00		7.38E-06

		-1.18E-01		1.68E+01		1.68E-05		-4.95E-01		7.46E+00		7.46E-06

		-1.22E-01		1.70E+01		1.70E-05		-4.99E-01		7.54E+00		7.54E-06

		-1.26E-01		1.68E+01		1.68E-05		-5.03E-01		7.62E+00		7.62E-06

		-1.30E-01		1.70E+01		1.70E-05		-5.07E-01		7.78E+00		7.78E-06

		-1.34E-01		1.67E+01		1.67E-05		-5.11E-01		7.82E+00		7.82E-06

		-1.38E-01		1.66E+01		1.66E-05		-5.15E-01		7.92E+00		7.92E-06

		-1.42E-01		1.64E+01		1.64E-05		-5.19E-01		7.96E+00		7.96E-06

		-1.46E-01		1.65E+01		1.65E-05		-5.23E-01		8.08E+00		8.08E-06

		-1.50E-01		1.65E+01		1.65E-05		-5.27E-01		8.16E+00		8.16E-06

		-1.54E-01		1.65E+01		1.65E-05		-5.31E-01		8.24E+00		8.24E-06

		-1.58E-01		1.66E+01		1.66E-05		-5.35E-01		8.32E+00		8.32E-06

		-1.62E-01		1.63E+01		1.63E-05		-5.39E-01		8.40E+00		8.40E-06

		-1.66E-01		1.65E+01		1.65E-05		-5.43E-01		8.45E+00		8.45E-06

		-1.70E-01		1.63E+01		1.63E-05		-5.47E-01		8.58E+00		8.58E-06

		-1.74E-01		1.62E+01		1.62E-05		-5.51E-01		8.58E+00		8.58E-06

		-1.78E-01		1.61E+01		1.61E-05		-5.55E-01		8.68E+00		8.68E-06

		-1.82E-01		1.60E+01		1.60E-05		-5.59E-01		8.70E+00		8.70E-06

		-1.86E-01		1.57E+01		1.57E-05		-5.63E-01		8.78E+00		8.78E-06

		-1.90E-01		1.60E+01		1.60E-05		-5.67E-01		8.89E+00		8.89E-06

		-1.94E-01		1.60E+01		1.60E-05		-5.71E-01		8.93E+00		8.93E-06

		-1.98E-01		1.60E+01		1.60E-05		-5.75E-01		8.99E+00		8.99E-06

		-2.02E-01		1.60E+01		1.60E-05		-5.79E-01		9.02E+00		9.02E-06

		-2.06E-01		1.58E+01		1.58E-05		-5.83E-01		9.07E+00		9.07E-06

		-2.10E-01		1.56E+01		1.56E-05		-5.87E-01		9.14E+00		9.14E-06

		-2.14E-01		1.58E+01		1.58E-05		-5.91E-01		9.19E+00		9.19E-06

		-2.18E-01		1.58E+01		1.58E-05		-5.95E-01		9.22E+00		9.22E-06

		-2.22E-01		1.55E+01		1.55E-05		-5.99E-01		9.29E+00		9.29E-06

		-2.26E-01		1.57E+01		1.57E-05		-6.03E-01		9.30E+00		9.30E-06

		-2.30E-01		1.57E+01		1.57E-05		-6.07E-01		9.37E+00		9.37E-06

		-2.34E-01		1.57E+01		1.57E-05		-6.11E-01		9.37E+00		9.37E-06

		-2.38E-01		1.55E+01		1.55E-05		-6.15E-01		9.40E+00		9.40E-06

		-2.42E-01		1.53E+01		1.53E-05		-6.19E-01		9.43E+00		9.43E-06

		-2.46E-01		1.54E+01		1.54E-05		-6.23E-01		9.45E+00		9.45E-06

		-2.50E-01		1.56E+01		1.56E-05		-6.27E-01		9.53E+00		9.53E-06

		-2.54E-01		1.54E+01		1.54E-05		-6.31E-01		9.51E+00		9.51E-06

		-2.58E-01		1.52E+01		1.52E-05		-6.35E-01		9.56E+00		9.56E-06

		-2.62E-01		1.56E+01		1.56E-05		-6.39E-01		9.56E+00		9.56E-06

		-2.66E-01		1.54E+01		1.54E-05		-6.43E-01		9.56E+00		9.56E-06

		-2.70E-01		1.55E+01		1.55E-05		-6.47E-01		9.63E+00		9.63E-06

		-2.74E-01		1.55E+01		1.55E-05		-6.51E-01		9.63E+00		9.63E-06

		-2.78E-01		1.55E+01		1.55E-05		-6.55E-01		9.62E+00		9.62E-06

		-2.82E-01		1.57E+01		1.57E-05		-6.59E-01		9.62E+00		9.62E-06

		-2.86E-01		1.55E+01		1.55E-05		-6.63E-01		9.60E+00		9.60E-06

		-2.90E-01		1.54E+01		1.54E-05		-6.67E-01		9.66E+00		9.66E-06

		-2.94E-01		1.56E+01		1.56E-05		-6.71E-01		9.62E+00		9.62E-06

		-2.98E-01		1.60E+01		1.60E-05		-6.75E-01		9.66E+00		9.66E-06

		-3.02E-01		1.59E+01		1.59E-05		-6.79E-01		9.64E+00		9.64E-06

		-3.06E-01		1.61E+01		1.61E-05		-6.83E-01		9.64E+00		9.64E-06

		-3.10E-01		1.60E+01		1.60E-05		-6.87E-01		9.66E+00		9.66E-06

		-3.14E-01		1.60E+01		1.60E-05		-6.91E-01		9.64E+00		9.64E-06

		-3.18E-01		1.62E+01		1.62E-05		-6.95E-01		9.65E+00		9.65E-06

		-3.22E-01		1.64E+01		1.64E-05		-6.99E-01		9.64E+00		9.64E-06

		-3.26E-01		1.67E+01		1.67E-05		-7.03E-01		9.61E+00		9.61E-06

		-3.30E-01		1.68E+01		1.68E-05		-7.07E-01		9.65E+00		9.65E-06

		-3.34E-01		1.69E+01		1.69E-05		-7.11E-01		9.61E+00		9.61E-06

		-3.38E-01		1.70E+01		1.70E-05		-7.15E-01		9.60E+00		9.60E-06

		-3.42E-01		1.73E+01		1.73E-05		-7.19E-01		9.63E+00		9.63E-06

		-3.46E-01		1.73E+01		1.73E-05		-7.23E-01		9.58E+00		9.58E-06

		-3.50E-01		1.78E+01		1.78E-05		-7.27E-01		9.61E+00		9.61E-06

		-3.54E-01		1.80E+01		1.80E-05		-7.31E-01		9.58E+00		9.58E-06

		-3.58E-01		1.82E+01		1.82E-05		-7.35E-01		9.57E+00		9.57E-06

		-3.62E-01		1.85E+01		1.85E-05		-7.39E-01		9.55E+00		9.55E-06

		-3.66E-01		1.85E+01		1.85E-05		-7.43E-01		9.51E+00		9.51E-06

		-3.70E-01		1.90E+01		1.90E-05		-7.47E-01		9.54E+00		9.54E-06

		-3.74E-01		1.91E+01		1.91E-05		-7.51E-01		9.49E+00		9.49E-06

		-3.78E-01		1.97E+01		1.97E-05		-7.55E-01		9.48E+00		9.48E-06

		-3.82E-01		1.99E+01		1.99E-05		-7.59E-01		9.50E+00		9.50E-06

		-3.86E-01		2.03E+01		2.03E-05		-7.63E-01		9.46E+00		9.46E-06

		-3.90E-01		2.08E+01		2.08E-05		-7.67E-01		9.45E+00		9.45E-06

		-3.94E-01		2.10E+01		2.10E-05		-7.71E-01		9.42E+00		9.42E-06

		-3.98E-01		2.11E+01		2.11E-05		-7.75E-01		9.43E+00		9.43E-06

		-4.02E-01		2.18E+01		2.18E-05		-7.79E-01		9.45E+00		9.45E-06

		-4.06E-01		2.22E+01		2.22E-05		-7.83E-01		9.37E+00		9.37E-06

		-4.10E-01		2.23E+01		2.23E-05		-7.87E-01		9.38E+00		9.38E-06

		-4.14E-01		2.27E+01		2.27E-05		-7.91E-01		9.34E+00		9.34E-06

		-4.18E-01		2.29E+01		2.29E-05		-7.95E-01		9.29E+00		9.29E-06

		-4.22E-01		2.33E+01		2.33E-05		-7.99E-01		9.36E+00		9.36E-06

		-4.26E-01		2.36E+01		2.36E-05		-8.03E-01		9.26E+00		9.26E-06

		-4.30E-01		2.40E+01		2.40E-05		-8.07E-01		9.33E+00		9.33E-06

		-4.34E-01		2.44E+01		2.44E-05		-8.11E-01		9.25E+00		9.25E-06

		-4.38E-01		2.50E+01		2.50E-05		-8.15E-01		9.27E+00		9.27E-06

		-4.42E-01		2.50E+01		2.50E-05		-8.19E-01		9.26E+00		9.26E-06

		-4.46E-01		2.52E+01		2.52E-05		-8.23E-01		9.19E+00		9.19E-06

		-4.50E-01		2.54E+01		2.54E-05		-8.27E-01		9.20E+00		9.20E-06

		-4.54E-01		2.56E+01		2.56E-05		-8.31E-01		9.16E+00		9.16E-06

		-4.58E-01		2.61E+01		2.61E-05		-8.35E-01		9.14E+00		9.14E-06

		-4.62E-01		2.60E+01		2.60E-05		-8.39E-01		9.19E+00		9.19E-06

		-4.66E-01		2.64E+01		2.64E-05		-8.43E-01		9.08E+00		9.08E-06

		-4.70E-01		2.65E+01		2.65E-05		-8.47E-01		9.14E+00		9.14E-06

		-4.74E-01		2.68E+01		2.68E-05		-8.51E-01		9.08E+00		9.08E-06

		-4.78E-01		2.68E+01		2.68E-05		-8.55E-01		9.11E+00		9.11E-06

		-4.82E-01		2.69E+01		2.69E-05		-8.59E-01		9.10E+00		9.10E-06

		-4.86E-01		2.72E+01		2.72E-05		-8.63E-01		9.04E+00		9.04E-06

		-4.90E-01		2.73E+01		2.73E-05		-8.67E-01		9.05E+00		9.05E-06

		-4.94E-01		2.72E+01		2.72E-05		-8.71E-01		9.07E+00		9.07E-06

		-4.98E-01		2.72E+01		2.72E-05		-8.75E-01		9.03E+00		9.03E-06

		-5.02E-01		2.74E+01		2.74E-05		-8.79E-01		9.07E+00		9.07E-06

		-5.06E-01		2.74E+01		2.74E-05		-8.83E-01		9.00E+00		9.00E-06

		-5.10E-01		2.76E+01		2.76E-05		-8.87E-01		9.07E+00		9.07E-06

		-5.14E-01		2.75E+01		2.75E-05		-8.91E-01		9.00E+00		9.00E-06

		-5.18E-01		2.75E+01		2.75E-05		-8.95E-01		9.04E+00		9.04E-06

		-5.22E-01		2.72E+01		2.72E-05		-8.99E-01		9.07E+00		9.07E-06

		-5.26E-01		2.74E+01		2.74E-05		-9.03E-01		8.99E+00		8.99E-06

		-5.30E-01		2.75E+01		2.75E-05		-9.07E-01		9.08E+00		9.08E-06

		-5.34E-01		2.75E+01		2.75E-05		-9.11E-01		9.01E+00		9.01E-06

		-5.38E-01		2.77E+01		2.77E-05		-9.15E-01		9.03E+00		9.03E-06

		-5.42E-01		2.75E+01		2.75E-05		-9.19E-01		9.02E+00		9.02E-06

		-5.46E-01		2.75E+01		2.75E-05		-9.23E-01		8.98E+00		8.98E-06

		-5.50E-01		2.70E+01		2.70E-05		-9.27E-01		9.04E+00		9.04E-06

		-5.54E-01		2.74E+01		2.74E-05		-9.31E-01		8.98E+00		8.98E-06

		-5.58E-01		2.71E+01		2.71E-05		-9.35E-01		9.02E+00		9.02E-06

		-5.62E-01		2.71E+01		2.71E-05		-9.39E-01		9.02E+00		9.02E-06

		-5.66E-01		2.72E+01		2.72E-05		-9.43E-01		8.98E+00		8.98E-06

		-5.70E-01		2.67E+01		2.67E-05		-9.47E-01		9.01E+00		9.01E-06

		-5.74E-01		2.70E+01		2.70E-05		-9.51E-01		9.00E+00		9.00E-06

		-5.78E-01		2.68E+01		2.68E-05		-9.55E-01		9.03E+00		9.03E-06

		-5.82E-01		2.69E+01		2.69E-05		-9.59E-01		9.04E+00		9.04E-06

		-5.86E-01		2.66E+01		2.66E-05		-9.63E-01		9.00E+00		9.00E-06

		-5.90E-01		2.65E+01		2.65E-05		-9.67E-01		9.06E+00		9.06E-06

		-5.94E-01		2.65E+01		2.65E-05		-9.71E-01		9.06E+00		9.06E-06

		-5.98E-01		2.63E+01		2.63E-05		-9.75E-01		9.10E+00		9.10E-06

		-6.02E-01		2.62E+01		2.62E-05		-9.79E-01		9.10E+00		9.10E-06

		-6.06E-01		2.62E+01		2.62E-05		-9.83E-01		9.10E+00		9.10E-06

		-6.10E-01		2.63E+01		2.63E-05		-9.87E-01		9.16E+00		9.16E-06

		-6.14E-01		2.59E+01		2.59E-05		-9.91E-01		9.15E+00		9.15E-06

		-6.18E-01		2.60E+01		2.60E-05		-9.95E-01		9.17E+00		9.17E-06

		-6.22E-01		2.56E+01		2.56E-05		-9.99E-01		9.22E+00		9.22E-06

		-6.26E-01		2.58E+01		2.58E-05		-1.00E+00		9.22E+00		9.22E-06

		-6.30E-01		2.56E+01		2.56E-05		-1.01E+00		9.27E+00		9.27E-06

		-6.34E-01		2.57E+01		2.57E-05		-1.01E+00		9.30E+00		9.30E-06

		-6.38E-01		2.54E+01		2.54E-05		-1.02E+00		9.33E+00		9.33E-06

		-6.42E-01		2.53E+01		2.53E-05		-1.02E+00		9.37E+00		9.37E-06

		-6.46E-01		2.52E+01		2.52E-05		-1.02E+00		9.38E+00		9.38E-06

		-6.50E-01		2.48E+01		2.48E-05		-1.03E+00		9.49E+00		9.49E-06

		-6.54E-01		2.50E+01		2.50E-05		-1.03E+00		9.45E+00		9.45E-06

		-6.58E-01		2.48E+01		2.48E-05		-1.04E+00		9.51E+00		9.51E-06

		-6.62E-01		2.50E+01		2.50E-05		-1.04E+00		9.57E+00		9.57E-06

		-6.66E-01		2.46E+01		2.46E-05		-1.04E+00		9.58E+00		9.58E-06

		-6.70E-01		2.48E+01		2.48E-05		-1.05E+00		9.66E+00		9.66E-06

		-6.74E-01		2.42E+01		2.42E-05		-1.05E+00		9.68E+00		9.68E-06

		-6.78E-01		2.43E+01		2.43E-05		-1.06E+00		9.77E+00		9.77E-06

		-6.82E-01		2.43E+01		2.43E-05		-1.06E+00		9.77E+00		9.77E-06

		-6.86E-01		2.40E+01		2.40E-05		-1.06E+00		9.85E+00		9.85E-06

		-6.90E-01		2.42E+01		2.42E-05		-1.07E+00		9.94E+00		9.94E-06

		-6.94E-01		2.40E+01		2.40E-05		-1.07E+00		9.95E+00		9.95E-06

		-6.98E-01		2.39E+01		2.39E-05		-1.08E+00		1.00E+01		1.00E-05

		-7.02E-01		2.37E+01		2.37E-05		-1.08E+00		1.01E+01		1.01E-05

		-7.06E-01		2.39E+01		2.39E-05		-1.08E+00		1.02E+01		1.02E-05

		-7.10E-01		2.36E+01		2.36E-05		-1.09E+00		1.02E+01		1.02E-05

		-7.14E-01		2.37E+01		2.37E-05		-1.09E+00		1.03E+01		1.03E-05

		-7.18E-01		2.36E+01		2.36E-05		-1.10E+00		1.04E+01		1.04E-05

		-7.22E-01		2.34E+01		2.34E-05		-1.10E+00		1.04E+01		1.04E-05

		-7.26E-01		2.31E+01		2.31E-05		-1.10E+00		1.05E+01		1.05E-05

		-7.30E-01		2.32E+01		2.32E-05		-1.11E+00		1.06E+01		1.06E-05

		-7.34E-01		2.33E+01		2.33E-05		-1.11E+00		1.06E+01		1.06E-05

		-7.38E-01		2.31E+01		2.31E-05		-1.12E+00		1.07E+01		1.07E-05

		-7.42E-01		2.32E+01		2.32E-05		-1.12E+00		1.08E+01		1.08E-05

		-7.46E-01		2.31E+01		2.31E-05		-1.12E+00		1.09E+01		1.09E-05

		-7.50E-01		2.32E+01		2.32E-05		-1.13E+00		1.10E+01		1.10E-05

		-7.54E-01		2.26E+01		2.26E-05		-1.13E+00		1.10E+01		1.10E-05

		-7.58E-01		2.30E+01		2.30E-05		-1.14E+00		1.11E+01		1.11E-05

		-7.62E-01		2.29E+01		2.29E-05		-1.14E+00		1.12E+01		1.12E-05

		-7.66E-01		2.26E+01		2.26E-05		-1.14E+00		1.12E+01		1.12E-05

		-7.70E-01		2.27E+01		2.27E-05		-1.15E+00		1.14E+01		1.14E-05

		-7.74E-01		2.27E+01		2.27E-05		-1.15E+00		1.14E+01		1.14E-05

		-7.78E-01		2.26E+01		2.26E-05		-1.16E+00		1.16E+01		1.16E-05

		-7.82E-01		2.24E+01		2.24E-05		-1.16E+00		1.16E+01		1.16E-05

		-7.86E-01		2.24E+01		2.24E-05		-1.16E+00		1.17E+01		1.17E-05

		-7.90E-01		2.25E+01		2.25E-05		-1.17E+00		1.18E+01		1.18E-05

		-7.94E-01		2.24E+01		2.24E-05		-1.17E+00		1.19E+01		1.19E-05

		-7.98E-01		2.24E+01		2.24E-05		-1.18E+00		1.20E+01		1.20E-05

		-8.02E-01		2.23E+01		2.23E-05		-1.18E+00		1.21E+01		1.21E-05

		-8.06E-01		2.23E+01		2.23E-05		-1.18E+00		1.21E+01		1.21E-05

		-8.10E-01		2.22E+01		2.22E-05		-1.19E+00		1.22E+01		1.22E-05

		-8.14E-01		2.22E+01		2.22E-05		-1.19E+00		1.23E+01		1.23E-05

		-8.18E-01		2.21E+01		2.21E-05		-1.20E+00		1.24E+01		1.24E-05

		-8.22E-01		2.21E+01		2.21E-05		-1.20E+00		1.25E+01		1.25E-05

		-8.26E-01		2.21E+01		2.21E-05		-1.20E+00		1.26E+01		1.26E-05

		-8.30E-01		2.20E+01		2.20E-05		-1.21E+00		1.27E+01		1.27E-05

		-8.34E-01		2.18E+01		2.18E-05		-1.21E+00		1.27E+01		1.27E-05

		-8.38E-01		2.20E+01		2.20E-05		-1.22E+00		1.28E+01		1.28E-05

		-8.42E-01		2.17E+01		2.17E-05		-1.22E+00		1.29E+01		1.29E-05

		-8.46E-01		2.18E+01		2.18E-05		-1.22E+00		1.30E+01		1.30E-05

		-8.50E-01		2.18E+01		2.18E-05		-1.23E+00		1.31E+01		1.31E-05

		-8.54E-01		2.18E+01		2.18E-05		-1.23E+00		1.31E+01		1.31E-05

		-8.58E-01		2.17E+01		2.17E-05		-1.24E+00		1.32E+01		1.32E-05

		-8.62E-01		2.16E+01		2.16E-05		-1.24E+00		1.33E+01		1.33E-05

		-8.66E-01		2.18E+01		2.18E-05		-1.24E+00		1.34E+01		1.34E-05

		-8.70E-01		2.15E+01		2.15E-05		-1.25E+00		1.35E+01		1.35E-05

		-8.74E-01		2.17E+01		2.17E-05		-1.25E+00		1.35E+01		1.35E-05

		-8.78E-01		2.14E+01		2.14E-05		-1.26E+00		1.36E+01		1.36E-05

		-8.82E-01		2.15E+01		2.15E-05		-1.26E+00		1.37E+01		1.37E-05

		-8.86E-01		2.13E+01		2.13E-05		-1.26E+00		1.37E+01		1.37E-05

		-8.90E-01		2.14E+01		2.14E-05		-1.27E+00		1.38E+01		1.38E-05

		-8.94E-01		2.15E+01		2.15E-05		-1.27E+00		1.38E+01		1.38E-05

		-8.98E-01		2.14E+01		2.14E-05		-1.28E+00		1.39E+01		1.39E-05

		-9.02E-01		2.16E+01		2.16E-05		-1.28E+00		1.40E+01		1.40E-05

		-9.06E-01		2.11E+01		2.11E-05		-1.28E+00		1.40E+01		1.40E-05

		-9.10E-01		2.14E+01		2.14E-05		-1.29E+00		1.41E+01		1.41E-05

		-9.14E-01		2.14E+01		2.14E-05		-1.29E+00		1.41E+01		1.41E-05

		-9.18E-01		2.12E+01		2.12E-05		-1.30E+00		1.42E+01		1.42E-05

		-9.22E-01		2.12E+01		2.12E-05		-1.30E+00		1.43E+01		1.43E-05

		-9.26E-01		2.13E+01		2.13E-05		-1.30E+00		1.43E+01		1.43E-05

		-9.30E-01		2.10E+01		2.10E-05		-1.31E+00		1.44E+01		1.44E-05

		-9.34E-01		2.10E+01		2.10E-05		-1.31E+00		1.44E+01		1.44E-05

		-9.38E-01		2.11E+01		2.11E-05		-1.32E+00		1.45E+01		1.45E-05

		-9.42E-01		2.11E+01		2.11E-05		-1.32E+00		1.45E+01		1.45E-05

		-9.46E-01		2.13E+01		2.13E-05		-1.32E+00		1.45E+01		1.45E-05

		-9.50E-01		2.11E+01		2.11E-05		-1.33E+00		1.46E+01		1.46E-05

		-9.54E-01		2.11E+01		2.11E-05		-1.33E+00		1.46E+01		1.46E-05

		-9.58E-01		2.06E+01		2.06E-05		-1.34E+00		1.47E+01		1.47E-05

		-9.62E-01		2.08E+01		2.08E-05		-1.34E+00		1.47E+01		1.47E-05

		-9.66E-01		2.07E+01		2.07E-05		-1.34E+00		1.48E+01		1.48E-05

		-9.70E-01		2.08E+01		2.08E-05		-1.35E+00		1.48E+01		1.48E-05

		-9.74E-01		2.07E+01		2.07E-05		-1.35E+00		1.48E+01		1.48E-05

		-9.78E-01		2.08E+01		2.08E-05		-1.36E+00		1.49E+01		1.49E-05

		-9.82E-01		2.07E+01		2.07E-05		-1.36E+00		1.49E+01		1.49E-05

		-9.86E-01		2.05E+01		2.05E-05		-1.36E+00		1.49E+01		1.49E-05

		-9.90E-01		2.10E+01		2.10E-05		-1.37E+00		1.50E+01		1.50E-05

		-9.94E-01		2.08E+01		2.08E-05		-1.37E+00		1.50E+01		1.50E-05

		-9.98E-01		2.08E+01		2.08E-05		-1.38E+00		1.51E+01		1.51E-05

		-1.00E+00		2.08E+01		2.08E-05		-1.38E+00		1.51E+01		1.51E-05

		-1.01E+00		2.07E+01		2.07E-05		-1.38E+00		1.51E+01		1.51E-05

		-1.01E+00		2.07E+01		2.07E-05		-1.39E+00		1.52E+01		1.52E-05

		-1.01E+00		2.04E+01		2.04E-05		-1.39E+00		1.51E+01		1.51E-05

		-1.02E+00		2.08E+01		2.08E-05		-1.40E+00		1.52E+01		1.52E-05

		-1.02E+00		2.07E+01		2.07E-05		-1.40E+00		1.52E+01		1.52E-05

		-1.03E+00		2.06E+01		2.06E-05		-1.40E+00		1.52E+01		1.52E-05

		-1.03E+00		2.03E+01		2.03E-05		-1.41E+00		1.53E+01		1.53E-05

		-1.03E+00		2.06E+01		2.06E-05		-1.41E+00		1.53E+01		1.53E-05

		-1.04E+00		2.04E+01		2.04E-05		-1.42E+00		1.53E+01		1.53E-05

		-1.04E+00		2.04E+01		2.04E-05		-1.42E+00		1.53E+01		1.53E-05

		-1.05E+00		2.05E+01		2.05E-05		-1.42E+00		1.53E+01		1.53E-05

		-1.05E+00		2.03E+01		2.03E-05		-1.43E+00		1.54E+01		1.54E-05

		-1.05E+00		2.03E+01		2.03E-05		-1.43E+00		1.54E+01		1.54E-05

		-1.06E+00		2.03E+01		2.03E-05		-1.44E+00		1.54E+01		1.54E-05

		-1.06E+00		2.04E+01		2.04E-05		-1.44E+00		1.54E+01		1.54E-05

		-1.07E+00		2.03E+01		2.03E-05		-1.44E+00		1.54E+01		1.54E-05

		-1.07E+00		2.04E+01		2.04E-05		-1.45E+00		1.55E+01		1.55E-05

		-1.07E+00		2.02E+01		2.02E-05		-1.45E+00		1.54E+01		1.54E-05

		-1.08E+00		2.03E+01		2.03E-05		-1.46E+00		1.55E+01		1.55E-05

		-1.08E+00		2.02E+01		2.02E-05		-1.46E+00		1.55E+01		1.55E-05

		-1.09E+00		2.02E+01		2.02E-05		-1.46E+00		1.55E+01		1.55E-05

		-1.09E+00		2.02E+01		2.02E-05		-1.47E+00		1.56E+01		1.56E-05

		-1.09E+00		2.02E+01		2.02E-05		-1.47E+00		1.56E+01		1.56E-05

		-1.10E+00		2.05E+01		2.05E-05		-1.48E+00		1.56E+01		1.56E-05

		-1.10E+00		2.02E+01		2.02E-05		-1.48E+00		1.56E+01		1.56E-05

		-1.11E+00		2.05E+01		2.05E-05		-1.48E+00		1.56E+01		1.56E-05

		-1.11E+00		2.03E+01		2.03E-05		-1.49E+00		1.57E+01		1.57E-05

		-1.11E+00		2.03E+01		2.03E-05		-1.49E+00		1.57E+01		1.57E-05

		-1.12E+00		2.02E+01		2.02E-05		-1.50E+00		1.58E+01		1.58E-05

		-1.12E+00		2.02E+01		2.02E-05		-1.50E+00		1.58E+01		1.58E-05

		-1.13E+00		2.04E+01		2.04E-05		-1.50E+00		1.58E+01		1.58E-05

		-1.13E+00		2.01E+01		2.01E-05		-1.51E+00		1.58E+01		1.58E-05

		-1.13E+00		2.04E+01		2.04E-05		-1.51E+00		1.59E+01		1.59E-05

		-1.14E+00		2.02E+01		2.02E-05		-1.52E+00		1.59E+01		1.59E-05

		-1.14E+00		2.02E+01		2.02E-05		-1.52E+00		1.60E+01		1.60E-05

		-1.15E+00		2.01E+01		2.01E-05		-1.52E+00		1.60E+01		1.60E-05

		-1.15E+00		2.01E+01		2.01E-05		-1.53E+00		1.61E+01		1.61E-05

		-1.15E+00		2.02E+01		2.02E-05		-1.53E+00		1.60E+01		1.60E-05

		-1.16E+00		2.02E+01		2.02E-05		-1.54E+00		1.62E+01		1.62E-05

		-1.16E+00		1.99E+01		1.99E-05		-1.54E+00		1.62E+01		1.62E-05

		-1.17E+00		2.03E+01		2.03E-05		-1.54E+00		1.62E+01		1.62E-05

		-1.17E+00		2.01E+01		2.01E-05		-1.55E+00		1.63E+01		1.63E-05

		-1.17E+00		2.00E+01		2.00E-05		-1.55E+00		1.63E+01		1.63E-05

		-1.18E+00		2.03E+01		2.03E-05		-1.56E+00		1.65E+01		1.65E-05

		-1.18E+00		2.02E+01		2.02E-05		-1.56E+00		1.65E+01		1.65E-05

		-1.19E+00		2.03E+01		2.03E-05		-1.56E+00		1.66E+01		1.66E-05

		-1.19E+00		1.98E+01		1.98E-05		-1.57E+00		1.67E+01		1.67E-05

		-1.19E+00		2.02E+01		2.02E-05		-1.57E+00		1.67E+01		1.67E-05

		-1.20E+00		2.01E+01		2.01E-05		-1.58E+00		1.68E+01		1.68E-05

		-1.20E+00		2.02E+01		2.02E-05		-1.58E+00		1.69E+01		1.69E-05

		-1.21E+00		2.02E+01		2.02E-05		-1.58E+00		1.69E+01		1.69E-05

		-1.21E+00		2.03E+01		2.03E-05		-1.59E+00		1.71E+01		1.71E-05

		-1.21E+00		2.04E+01		2.04E-05		-1.59E+00		1.71E+01		1.71E-05

		-1.22E+00		2.02E+01		2.02E-05		-1.60E+00		1.72E+01		1.72E-05

		-1.22E+00		2.06E+01		2.06E-05		-1.60E+00		1.74E+01		1.74E-05

		-1.23E+00		2.03E+01		2.03E-05		-1.60E+00		1.74E+01		1.74E-05

		-1.23E+00		2.06E+01		2.06E-05		-1.61E+00		1.76E+01		1.76E-05

		-1.23E+00		2.04E+01		2.04E-05		-1.61E+00		1.77E+01		1.77E-05

		-1.24E+00		2.06E+01		2.06E-05		-1.62E+00		1.78E+01		1.78E-05

		-1.24E+00		2.07E+01		2.07E-05		-1.62E+00		1.79E+01		1.79E-05

		-1.25E+00		2.05E+01		2.05E-05		-1.62E+00		1.81E+01		1.81E-05

		-1.25E+00		2.08E+01		2.08E-05		-1.63E+00		1.82E+01		1.82E-05

		-1.25E+00		2.07E+01		2.07E-05		-1.63E+00		1.83E+01		1.83E-05

		-1.26E+00		2.09E+01		2.09E-05		-1.64E+00		1.85E+01		1.85E-05

		-1.26E+00		2.07E+01		2.07E-05		-1.64E+00		1.87E+01		1.87E-05

		-1.27E+00		2.11E+01		2.11E-05		-1.64E+00		1.87E+01		1.87E-05

		-1.27E+00		2.09E+01		2.09E-05		-1.65E+00		1.91E+01		1.91E-05

		-1.27E+00		2.10E+01		2.10E-05		-1.65E+00		1.92E+01		1.92E-05

		-1.28E+00		2.11E+01		2.11E-05		-1.66E+00		1.94E+01		1.94E-05

		-1.28E+00		2.11E+01		2.11E-05		-1.66E+00		1.95E+01		1.95E-05

		-1.29E+00		2.14E+01		2.14E-05		-1.66E+00		1.98E+01		1.98E-05

		-1.29E+00		2.13E+01		2.13E-05		-1.67E+00		1.99E+01		1.99E-05

		-1.29E+00		2.14E+01		2.14E-05		-1.67E+00		2.01E+01		2.01E-05

		-1.30E+00		2.15E+01		2.15E-05		-1.68E+00		2.04E+01		2.04E-05

		-1.30E+00		2.17E+01		2.17E-05		-1.68E+00		2.06E+01		2.06E-05

		-1.31E+00		2.15E+01		2.15E-05		-1.68E+00		2.09E+01		2.09E-05

		-1.31E+00		2.20E+01		2.20E-05		-1.69E+00		2.12E+01		2.12E-05

		-1.31E+00		2.17E+01		2.17E-05		-1.69E+00		2.13E+01		2.13E-05

		-1.32E+00		2.18E+01		2.18E-05		-1.70E+00		2.17E+01		2.17E-05

		-1.32E+00		2.20E+01		2.20E-05		-1.70E+00		2.19E+01		2.19E-05

		-1.33E+00		2.18E+01		2.18E-05		-1.70E+00		2.24E+01		2.24E-05

		-1.33E+00		2.22E+01		2.22E-05		-1.71E+00		2.26E+01		2.26E-05

		-1.33E+00		2.22E+01		2.22E-05		-1.71E+00		2.29E+01		2.29E-05

		-1.34E+00		2.25E+01		2.25E-05		-1.72E+00		2.32E+01		2.32E-05

		-1.34E+00		2.24E+01		2.24E-05		-1.72E+00		2.35E+01		2.35E-05

		-1.35E+00		2.26E+01		2.26E-05		-1.72E+00		2.38E+01		2.38E-05

		-1.35E+00		2.23E+01		2.23E-05		-1.73E+00		2.43E+01		2.43E-05

		-1.35E+00		2.28E+01		2.28E-05		-1.73E+00		2.46E+01		2.46E-05

		-1.36E+00		2.25E+01		2.25E-05		-1.74E+00		2.48E+01		2.48E-05

		-1.36E+00		2.29E+01		2.29E-05		-1.74E+00		2.53E+01		2.53E-05

		-1.37E+00		2.32E+01		2.32E-05		-1.74E+00		2.56E+01		2.56E-05

		-1.37E+00		2.30E+01		2.30E-05		-1.75E+00		2.60E+01		2.60E-05

		-1.37E+00		2.31E+01		2.31E-05		-1.75E+00		2.64E+01		2.64E-05

		-1.38E+00		2.33E+01		2.33E-05		-1.76E+00		2.70E+01		2.70E-05

		-1.38E+00		2.34E+01		2.34E-05		-1.76E+00		2.73E+01		2.73E-05

		-1.39E+00		2.35E+01		2.35E-05		-1.76E+00		2.77E+01		2.77E-05

		-1.39E+00		2.37E+01		2.37E-05		-1.77E+00		2.84E+01		2.84E-05

		-1.39E+00		2.33E+01		2.33E-05		-1.77E+00		2.86E+01		2.86E-05

		-1.40E+00		2.38E+01		2.38E-05		-1.78E+00		2.93E+01		2.93E-05

		-1.40E+00		2.39E+01		2.39E-05		-1.78E+00		2.95E+01		2.95E-05

		-1.41E+00		2.40E+01		2.40E-05		-1.78E+00		3.02E+01		3.02E-05

		-1.41E+00		2.43E+01		2.43E-05		-1.79E+00		3.06E+01		3.06E-05

		-1.41E+00		2.43E+01		2.43E-05		-1.79E+00		3.11E+01		3.11E-05

		-1.42E+00		2.46E+01		2.46E-05		-1.80E+00		3.17E+01		3.17E-05

		-1.42E+00		2.44E+01		2.44E-05		-1.80E+00		3.23E+01		3.23E-05

		-1.43E+00		2.49E+01		2.49E-05		-1.80E+00		3.28E+01		3.28E-05

		-1.43E+00		2.50E+01		2.50E-05		-1.81E+00		3.34E+01		3.34E-05

		-1.43E+00		2.51E+01		2.51E-05		-1.81E+00		3.39E+01		3.39E-05

		-1.44E+00		2.52E+01		2.52E-05		-1.82E+00		3.45E+01		3.45E-05

		-1.44E+00		2.54E+01		2.54E-05		-1.82E+00		3.51E+01		3.51E-05

		-1.45E+00		2.58E+01		2.58E-05		-1.82E+00		3.58E+01		3.58E-05

		-1.45E+00		2.57E+01		2.57E-05		-1.83E+00		3.62E+01		3.62E-05

		-1.45E+00		2.60E+01		2.60E-05		-1.83E+00		3.68E+01		3.68E-05

		-1.46E+00		2.61E+01		2.61E-05		-1.84E+00		3.75E+01		3.75E-05

		-1.46E+00		2.65E+01		2.65E-05		-1.84E+00		3.82E+01		3.82E-05

		-1.47E+00		2.66E+01		2.66E-05		-1.84E+00		3.90E+01		3.90E-05

		-1.47E+00		2.68E+01		2.68E-05		-1.85E+00		3.95E+01		3.95E-05

		-1.47E+00		2.69E+01		2.69E-05		-1.85E+00		4.01E+01		4.01E-05

		-1.48E+00		2.73E+01		2.73E-05		-1.86E+00		4.10E+01		4.10E-05

		-1.48E+00		2.74E+01		2.74E-05		-1.86E+00		4.16E+01		4.16E-05

		-1.49E+00		2.74E+01		2.74E-05		-1.86E+00		4.24E+01		4.24E-05

		-1.49E+00		2.78E+01		2.78E-05		-1.87E+00		4.30E+01		4.30E-05

		-1.49E+00		2.75E+01		2.75E-05		-1.87E+00		4.39E+01		4.39E-05

		-1.50E+00		2.82E+01		2.82E-05		-1.88E+00		4.47E+01		4.47E-05

		-1.50E+00		2.82E+01		2.82E-05		-1.88E+00		4.55E+01		4.55E-05

		-1.51E+00		2.88E+01		2.88E-05		-1.88E+00		4.64E+01		4.64E-05

		-1.51E+00		2.88E+01		2.88E-05		-1.89E+00		4.71E+01		4.71E-05

		-1.51E+00		2.91E+01		2.91E-05		-1.89E+00		4.82E+01		4.82E-05

		-1.52E+00		2.93E+01		2.93E-05		-1.90E+00		4.88E+01		4.88E-05

		-1.52E+00		2.95E+01		2.95E-05		-1.90E+00		4.98E+01		4.98E-05

		-1.53E+00		2.99E+01		2.99E-05		-1.90E+00		5.06E+01		5.06E-05

		-1.53E+00		3.02E+01		3.02E-05		-1.91E+00		5.16E+01		5.16E-05

		-1.53E+00		3.03E+01		3.03E-05		-1.91E+00		5.25E+01		5.25E-05

		-1.54E+00		3.06E+01		3.06E-05		-1.92E+00		5.35E+01		5.35E-05

		-1.54E+00		3.12E+01		3.12E-05		-1.92E+00		5.44E+01		5.44E-05

		-1.55E+00		3.11E+01		3.11E-05		-1.92E+00		5.56E+01		5.56E-05

		-1.55E+00		3.17E+01		3.17E-05		-1.93E+00		5.64E+01		5.64E-05

		-1.55E+00		3.18E+01		3.18E-05		-1.93E+00		5.75E+01		5.75E-05

		-1.56E+00		3.23E+01		3.23E-05		-1.94E+00		5.89E+01		5.89E-05

		-1.56E+00		3.25E+01		3.25E-05		-1.94E+00		5.95E+01		5.95E-05

		-1.57E+00		3.29E+01		3.29E-05		-1.94E+00		6.09E+01		6.09E-05

		-1.57E+00		3.35E+01		3.35E-05		-1.95E+00		6.21E+01		6.21E-05

		-1.57E+00		3.35E+01		3.35E-05		-1.95E+00		6.31E+01		6.31E-05

		-1.58E+00		3.39E+01		3.39E-05		-1.96E+00		6.42E+01		6.42E-05

		-1.58E+00		3.43E+01		3.43E-05		-1.96E+00		6.53E+01		6.53E-05

		-1.59E+00		3.49E+01		3.49E-05		-1.96E+00		6.66E+01		6.66E-05

		-1.59E+00		3.51E+01		3.51E-05		-1.97E+00		6.79E+01		6.79E-05

		-1.59E+00		3.57E+01		3.57E-05		-1.97E+00		6.92E+01		6.92E-05

		-1.60E+00		3.59E+01		3.59E-05		-1.98E+00		7.03E+01		7.03E-05

		-1.60E+00		3.65E+01		3.65E-05		-1.98E+00		7.19E+01		7.19E-05

		-1.61E+00		3.70E+01		3.70E-05		-1.98E+00		7.32E+01		7.32E-05

		-1.61E+00		3.73E+01		3.73E-05		-1.99E+00		7.44E+01		7.44E-05

		-1.61E+00		3.78E+01		3.78E-05		-1.99E+00		7.59E+01		7.59E-05

		-1.62E+00		3.82E+01		3.82E-05		-2.00E+00		7.74E+01		7.74E-05

		-1.62E+00		3.88E+01		3.88E-05		-2.00E+00		7.90E+01		7.90E-05

		-1.63E+00		3.90E+01		3.90E-05		-2.00E+00		7.68E+01		7.68E-05

		-1.63E+00		3.97E+01		3.97E-05		-1.99E+00		7.49E+01		7.49E-05

		-1.63E+00		4.03E+01		4.03E-05		-1.99E+00		7.29E+01		7.29E-05

		-1.64E+00		4.08E+01		4.08E-05		-1.98E+00		7.10E+01		7.10E-05

		-1.64E+00		4.14E+01		4.14E-05		-1.98E+00		6.93E+01		6.93E-05

		-1.65E+00		4.19E+01		4.19E-05		-1.98E+00		6.78E+01		6.78E-05

		-1.65E+00		4.26E+01		4.26E-05		-1.97E+00		6.58E+01		6.58E-05

		-1.65E+00		4.30E+01		4.30E-05		-1.97E+00		6.43E+01		6.43E-05

		-1.66E+00		4.36E+01		4.36E-05		-1.96E+00		6.28E+01		6.28E-05

		-1.66E+00		4.44E+01		4.44E-05		-1.96E+00		6.12E+01		6.12E-05

		-1.67E+00		4.49E+01		4.49E-05		-1.96E+00		5.99E+01		5.99E-05

		-1.67E+00		4.55E+01		4.55E-05		-1.95E+00		5.84E+01		5.84E-05

		-1.67E+00		4.64E+01		4.64E-05		-1.95E+00		5.71E+01		5.71E-05

		-1.68E+00		4.68E+01		4.68E-05		-1.94E+00		5.57E+01		5.57E-05

		-1.68E+00		4.77E+01		4.77E-05		-1.94E+00		5.44E+01		5.44E-05

		-1.69E+00		4.84E+01		4.84E-05		-1.94E+00		5.32E+01		5.32E-05

		-1.69E+00		4.92E+01		4.92E-05		-1.93E+00		5.20E+01		5.20E-05

		-1.69E+00		4.98E+01		4.98E-05		-1.93E+00		5.07E+01		5.07E-05

		-1.70E+00		5.04E+01		5.04E-05		-1.92E+00		4.95E+01		4.95E-05

		-1.70E+00		5.14E+01		5.14E-05		-1.92E+00		4.83E+01		4.83E-05

		-1.71E+00		5.21E+01		5.21E-05		-1.92E+00		4.74E+01		4.74E-05

		-1.71E+00		5.29E+01		5.29E-05		-1.91E+00		4.63E+01		4.63E-05

		-1.71E+00		5.34E+01		5.34E-05		-1.91E+00		4.51E+01		4.51E-05

		-1.72E+00		5.46E+01		5.46E-05		-1.90E+00		4.43E+01		4.43E-05

		-1.72E+00		5.52E+01		5.52E-05		-1.90E+00		4.31E+01		4.31E-05

		-1.73E+00		5.58E+01		5.58E-05		-1.90E+00		4.23E+01		4.23E-05

		-1.73E+00		5.71E+01		5.71E-05		-1.89E+00		4.12E+01		4.12E-05

		-1.73E+00		5.77E+01		5.77E-05		-1.89E+00		4.04E+01		4.04E-05

		-1.74E+00		5.87E+01		5.87E-05		-1.88E+00		3.94E+01		3.94E-05

		-1.74E+00		5.94E+01		5.94E-05		-1.88E+00		3.84E+01		3.84E-05

		-1.75E+00		6.08E+01		6.08E-05		-1.88E+00		3.75E+01		3.75E-05

		-1.75E+00		6.15E+01		6.15E-05		-1.87E+00		3.66E+01		3.66E-05

		-1.75E+00		6.26E+01		6.26E-05		-1.87E+00		3.59E+01		3.59E-05

		-1.76E+00		6.37E+01		6.37E-05		-1.86E+00		3.52E+01		3.52E-05

		-1.76E+00		6.48E+01		6.48E-05		-1.86E+00		3.43E+01		3.43E-05

		-1.77E+00		6.58E+01		6.58E-05		-1.86E+00		3.36E+01		3.36E-05

		-1.77E+00		6.67E+01		6.67E-05		-1.85E+00		3.29E+01		3.29E-05

		-1.77E+00		6.80E+01		6.80E-05		-1.85E+00		3.21E+01		3.21E-05

		-1.78E+00		6.90E+01		6.90E-05		-1.84E+00		3.15E+01		3.15E-05

		-1.78E+00		7.03E+01		7.03E-05		-1.84E+00		3.08E+01		3.08E-05

		-1.79E+00		7.15E+01		7.15E-05		-1.84E+00		3.01E+01		3.01E-05

		-1.79E+00		7.28E+01		7.28E-05		-1.83E+00		2.95E+01		2.95E-05

		-1.79E+00		7.38E+01		7.38E-05		-1.83E+00		2.88E+01		2.88E-05

		-1.80E+00		7.53E+01		7.53E-05		-1.82E+00		2.82E+01		2.82E-05

		-1.80E+00		7.63E+01		7.63E-05		-1.82E+00		2.76E+01		2.76E-05

		-1.81E+00		7.81E+01		7.81E-05		-1.82E+00		2.70E+01		2.70E-05

		-1.81E+00		7.94E+01		7.94E-05		-1.81E+00		2.64E+01		2.64E-05

		-1.81E+00		8.08E+01		8.08E-05		-1.81E+00		2.58E+01		2.58E-05

		-1.82E+00		8.21E+01		8.21E-05		-1.80E+00		2.53E+01		2.53E-05

		-1.82E+00		8.31E+01		8.31E-05		-1.80E+00		2.46E+01		2.46E-05

		-1.83E+00		8.50E+01		8.50E-05		-1.80E+00		2.42E+01		2.42E-05

		-1.83E+00		8.62E+01		8.62E-05		-1.79E+00		2.37E+01		2.37E-05

		-1.83E+00		8.78E+01		8.78E-05		-1.79E+00		2.32E+01		2.32E-05

		-1.84E+00		8.91E+01		8.91E-05		-1.78E+00		2.26E+01		2.26E-05

		-1.84E+00		9.09E+01		9.09E-05		-1.78E+00		2.22E+01		2.22E-05

		-1.85E+00		9.23E+01		9.23E-05		-1.78E+00		2.16E+01		2.16E-05

		-1.85E+00		9.40E+01		9.40E-05		-1.77E+00		2.12E+01		2.12E-05

		-1.85E+00		9.57E+01		9.57E-05		-1.77E+00		2.07E+01		2.07E-05

		-1.86E+00		9.72E+01		9.72E-05		-1.76E+00		2.02E+01		2.02E-05

		-1.86E+00		9.91E+01		9.91E-05		-1.76E+00		1.99E+01		1.99E-05

		-1.87E+00		1.01E+02		1.01E-04		-1.76E+00		1.94E+01		1.94E-05

		-1.87E+00		1.03E+02		1.03E-04		-1.75E+00		1.90E+01		1.90E-05

		-1.87E+00		1.05E+02		1.05E-04		-1.75E+00		1.86E+01		1.86E-05

		-1.88E+00		1.07E+02		1.07E-04		-1.74E+00		1.83E+01		1.83E-05

		-1.88E+00		1.08E+02		1.08E-04		-1.74E+00		1.79E+01		1.79E-05

		-1.89E+00		1.10E+02		1.10E-04		-1.74E+00		1.74E+01		1.74E-05

		-1.89E+00		1.12E+02		1.12E-04		-1.73E+00		1.71E+01		1.71E-05

		-1.89E+00		1.15E+02		1.15E-04		-1.73E+00		1.67E+01		1.67E-05

		-1.90E+00		1.17E+02		1.17E-04		-1.72E+00		1.66E+01		1.66E-05

		-1.90E+00		1.18E+02		1.18E-04		-1.72E+00		1.60E+01		1.60E-05

		-1.91E+00		1.21E+02		1.21E-04		-1.72E+00		1.59E+01		1.59E-05

		-1.91E+00		1.23E+02		1.23E-04		-1.71E+00		1.54E+01		1.54E-05

		-1.91E+00		1.25E+02		1.25E-04		-1.71E+00		1.51E+01		1.51E-05

		-1.92E+00		1.28E+02		1.28E-04		-1.70E+00		1.49E+01		1.49E-05

		-1.92E+00		1.30E+02		1.30E-04		-1.70E+00		1.46E+01		1.46E-05

		-1.93E+00		1.32E+02		1.32E-04		-1.70E+00		1.43E+01		1.43E-05

		-1.93E+00		1.35E+02		1.35E-04		-1.69E+00		1.40E+01		1.40E-05

		-1.93E+00		1.37E+02		1.37E-04		-1.69E+00		1.37E+01		1.37E-05

		-1.94E+00		1.40E+02		1.40E-04		-1.68E+00		1.35E+01		1.35E-05

		-1.94E+00		1.42E+02		1.42E-04		-1.68E+00		1.32E+01		1.32E-05

		-1.95E+00		1.45E+02		1.45E-04		-1.68E+00		1.29E+01		1.29E-05

		-1.95E+00		1.47E+02		1.47E-04		-1.67E+00		1.27E+01		1.27E-05

		-1.95E+00		1.50E+02		1.50E-04		-1.67E+00		1.25E+01		1.25E-05

		-1.96E+00		1.53E+02		1.53E-04		-1.66E+00		1.23E+01		1.23E-05

		-1.96E+00		1.56E+02		1.56E-04		-1.66E+00		1.20E+01		1.20E-05

		-1.97E+00		1.59E+02		1.59E-04		-1.66E+00		1.18E+01		1.18E-05

		-1.97E+00		1.61E+02		1.61E-04		-1.65E+00		1.15E+01		1.15E-05

		-1.97E+00		1.65E+02		1.65E-04		-1.65E+00		1.13E+01		1.13E-05

		-1.98E+00		1.68E+02		1.68E-04		-1.64E+00		1.12E+01		1.12E-05

		-1.98E+00		1.71E+02		1.71E-04		-1.64E+00		1.09E+01		1.09E-05

		-1.99E+00		1.74E+02		1.74E-04		-1.64E+00		1.07E+01		1.07E-05

		-1.99E+00		1.77E+02		1.77E-04		-1.63E+00		1.05E+01		1.05E-05

		-1.99E+00		1.81E+02		1.81E-04		-1.63E+00		1.04E+01		1.04E-05

		-2.00E+00		1.84E+02		1.84E-04		-1.62E+00		1.02E+01		1.02E-05

		-1.99E+00		1.80E+02		1.80E-04		-1.62E+00		1.00E+01		1.00E-05

		-1.99E+00		1.76E+02		1.76E-04		-1.62E+00		9.83E+00		9.83E-06

		-1.99E+00		1.72E+02		1.72E-04		-1.61E+00		9.72E+00		9.72E-06

		-1.98E+00		1.68E+02		1.68E-04		-1.61E+00		9.53E+00		9.53E-06

		-1.98E+00		1.64E+02		1.64E-04		-1.60E+00		9.43E+00		9.43E-06

		-1.97E+00		1.61E+02		1.61E-04		-1.60E+00		9.25E+00		9.25E-06

		-1.97E+00		1.57E+02		1.57E-04		-1.60E+00		9.11E+00		9.11E-06

		-1.97E+00		1.54E+02		1.54E-04		-1.59E+00		8.96E+00		8.96E-06

		-1.96E+00		1.51E+02		1.51E-04		-1.59E+00		8.82E+00		8.82E-06

		-1.96E+00		1.48E+02		1.48E-04		-1.58E+00		8.72E+00		8.72E-06

		-1.95E+00		1.44E+02		1.44E-04		-1.58E+00		8.58E+00		8.58E-06

		-1.95E+00		1.41E+02		1.41E-04		-1.58E+00		8.45E+00		8.45E-06

		-1.95E+00		1.38E+02		1.38E-04		-1.57E+00		8.34E+00		8.34E-06

		-1.94E+00		1.35E+02		1.35E-04		-1.57E+00		8.22E+00		8.22E-06

		-1.94E+00		1.32E+02		1.32E-04		-1.56E+00		8.15E+00		8.15E-06

		-1.93E+00		1.29E+02		1.29E-04		-1.56E+00		7.98E+00		7.98E-06

		-1.93E+00		1.26E+02		1.26E-04		-1.56E+00		7.89E+00		7.89E-06

		-1.93E+00		1.23E+02		1.23E-04		-1.55E+00		7.79E+00		7.79E-06

		-1.92E+00		1.20E+02		1.20E-04		-1.55E+00		7.70E+00		7.70E-06

		-1.92E+00		1.18E+02		1.18E-04		-1.54E+00		7.63E+00		7.63E-06

		-1.91E+00		1.15E+02		1.15E-04		-1.54E+00		7.51E+00		7.51E-06

		-1.91E+00		1.12E+02		1.12E-04		-1.54E+00		7.42E+00		7.42E-06

		-1.91E+00		1.10E+02		1.10E-04		-1.53E+00		7.35E+00		7.35E-06

		-1.90E+00		1.07E+02		1.07E-04		-1.53E+00		7.25E+00		7.25E-06

		-1.90E+00		1.05E+02		1.05E-04		-1.52E+00		7.18E+00		7.18E-06

		-1.89E+00		1.02E+02		1.02E-04		-1.52E+00		7.06E+00		7.06E-06

		-1.89E+00		1.00E+02		1.00E-04		-1.52E+00		7.02E+00		7.02E-06

		-1.89E+00		9.76E+01		9.76E-05		-1.51E+00		6.91E+00		6.91E-06

		-1.88E+00		9.54E+01		9.54E-05		-1.51E+00		6.86E+00		6.86E-06

		-1.88E+00		9.31E+01		9.31E-05		-1.50E+00		6.83E+00		6.83E-06

		-1.87E+00		9.13E+01		9.13E-05		-1.50E+00		6.74E+00		6.74E-06

		-1.87E+00		8.88E+01		8.88E-05		-1.50E+00		6.66E+00		6.66E-06

		-1.87E+00		8.73E+01		8.73E-05		-1.49E+00		6.61E+00		6.61E-06

		-1.86E+00		8.51E+01		8.51E-05		-1.49E+00		6.51E+00		6.51E-06

		-1.86E+00		8.33E+01		8.33E-05		-1.48E+00		6.51E+00		6.51E-06

		-1.85E+00		8.13E+01		8.13E-05		-1.48E+00		6.38E+00		6.38E-06

		-1.85E+00		7.95E+01		7.95E-05		-1.48E+00		6.38E+00		6.38E-06

		-1.85E+00		7.76E+01		7.76E-05		-1.47E+00		6.30E+00		6.30E-06

		-1.84E+00		7.59E+01		7.59E-05		-1.47E+00		6.26E+00		6.26E-06

		-1.84E+00		7.39E+01		7.39E-05		-1.46E+00		6.23E+00		6.23E-06

		-1.83E+00		7.24E+01		7.24E-05		-1.46E+00		6.18E+00		6.18E-06

		-1.83E+00		7.06E+01		7.06E-05		-1.46E+00		6.11E+00		6.11E-06

		-1.83E+00		6.91E+01		6.91E-05		-1.45E+00		6.08E+00		6.08E-06

		-1.82E+00		6.76E+01		6.76E-05		-1.45E+00		6.01E+00		6.01E-06

		-1.82E+00		6.56E+01		6.56E-05		-1.44E+00		6.04E+00		6.04E-06

		-1.81E+00		6.44E+01		6.44E-05		-1.44E+00		5.92E+00		5.92E-06

		-1.81E+00		6.28E+01		6.28E-05		-1.44E+00		5.88E+00		5.88E-06

		-1.81E+00		6.12E+01		6.12E-05		-1.43E+00		5.86E+00		5.86E-06

		-1.80E+00		5.98E+01		5.98E-05		-1.43E+00		5.82E+00		5.82E-06

		-1.80E+00		5.83E+01		5.83E-05		-1.42E+00		5.83E+00		5.83E-06

		-1.79E+00		5.69E+01		5.69E-05		-1.42E+00		5.76E+00		5.76E-06

		-1.79E+00		5.57E+01		5.57E-05		-1.42E+00		5.73E+00		5.73E-06

		-1.79E+00		5.42E+01		5.42E-05		-1.41E+00		5.66E+00		5.66E-06

		-1.78E+00		5.29E+01		5.29E-05		-1.41E+00		5.66E+00		5.66E-06

		-1.78E+00		5.19E+01		5.19E-05		-1.40E+00		5.65E+00		5.65E-06

		-1.77E+00		5.05E+01		5.05E-05		-1.40E+00		5.52E+00		5.52E-06

		-1.77E+00		4.94E+01		4.94E-05		-1.40E+00		5.55E+00		5.55E-06

		-1.77E+00		4.80E+01		4.80E-05		-1.39E+00		5.48E+00		5.48E-06

		-1.76E+00		4.68E+01		4.68E-05		-1.39E+00		5.48E+00		5.48E-06

		-1.76E+00		4.59E+01		4.59E-05		-1.38E+00		5.46E+00		5.46E-06

		-1.75E+00		4.49E+01		4.49E-05		-1.38E+00		5.40E+00		5.40E-06

		-1.75E+00		4.39E+01		4.39E-05		-1.38E+00		5.38E+00		5.38E-06

		-1.75E+00		4.26E+01		4.26E-05		-1.37E+00		5.35E+00		5.35E-06

		-1.74E+00		4.17E+01		4.17E-05		-1.37E+00		5.31E+00		5.31E-06

		-1.74E+00		4.08E+01		4.08E-05		-1.36E+00		5.31E+00		5.31E-06

		-1.73E+00		3.98E+01		3.98E-05		-1.36E+00		5.26E+00		5.26E-06

		-1.73E+00		3.87E+01		3.87E-05		-1.36E+00		5.26E+00		5.26E-06

		-1.73E+00		3.82E+01		3.82E-05		-1.35E+00		5.20E+00		5.20E-06

		-1.72E+00		3.71E+01		3.71E-05		-1.35E+00		5.19E+00		5.19E-06

		-1.72E+00		3.62E+01		3.62E-05		-1.34E+00		5.18E+00		5.18E-06

		-1.71E+00		3.52E+01		3.52E-05		-1.34E+00		5.11E+00		5.11E-06

		-1.71E+00		3.45E+01		3.45E-05		-1.34E+00		5.13E+00		5.13E-06

		-1.71E+00		3.36E+01		3.36E-05		-1.33E+00		5.07E+00		5.07E-06

		-1.70E+00		3.27E+01		3.27E-05		-1.33E+00		5.07E+00		5.07E-06

		-1.70E+00		3.23E+01		3.23E-05		-1.32E+00		5.07E+00		5.07E-06

		-1.69E+00		3.15E+01		3.15E-05		-1.32E+00		4.98E+00		4.98E-06

		-1.69E+00		3.08E+01		3.08E-05		-1.32E+00		4.99E+00		4.99E-06

		-1.69E+00		3.00E+01		3.00E-05		-1.31E+00		4.94E+00		4.94E-06

		-1.68E+00		2.94E+01		2.94E-05		-1.31E+00		4.93E+00		4.93E-06

		-1.68E+00		2.87E+01		2.87E-05		-1.30E+00		4.94E+00		4.94E-06

		-1.67E+00		2.78E+01		2.78E-05		-1.30E+00		4.86E+00		4.86E-06

		-1.67E+00		2.72E+01		2.72E-05		-1.30E+00		4.91E+00		4.91E-06

		-1.67E+00		2.66E+01		2.66E-05		-1.29E+00		4.86E+00		4.86E-06

		-1.66E+00		2.61E+01		2.61E-05		-1.29E+00		4.86E+00		4.86E-06

		-1.66E+00		2.56E+01		2.56E-05		-1.28E+00		4.82E+00		4.82E-06

		-1.65E+00		2.48E+01		2.48E-05		-1.28E+00		4.81E+00		4.81E-06

		-1.65E+00		2.45E+01		2.45E-05		-1.28E+00		4.79E+00		4.79E-06

		-1.65E+00		2.41E+01		2.41E-05		-1.27E+00		4.76E+00		4.76E-06

		-1.64E+00		2.34E+01		2.34E-05		-1.27E+00		4.71E+00		4.71E-06

		-1.64E+00		2.26E+01		2.26E-05		-1.26E+00		4.74E+00		4.74E-06

		-1.63E+00		2.23E+01		2.23E-05		-1.26E+00		4.66E+00		4.66E-06

		-1.63E+00		2.19E+01		2.19E-05		-1.26E+00		4.67E+00		4.67E-06

		-1.63E+00		2.17E+01		2.17E-05		-1.25E+00		4.66E+00		4.66E-06

		-1.62E+00		2.10E+01		2.10E-05		-1.25E+00		4.61E+00		4.61E-06

		-1.62E+00		2.08E+01		2.08E-05		-1.24E+00		4.63E+00		4.63E-06

		-1.61E+00		2.01E+01		2.01E-05		-1.24E+00		4.59E+00		4.59E-06

		-1.61E+00		1.96E+01		1.96E-05		-1.24E+00		4.58E+00		4.58E-06

		-1.61E+00		1.94E+01		1.94E-05		-1.23E+00		4.56E+00		4.56E-06

		-1.60E+00		1.92E+01		1.92E-05		-1.23E+00		4.54E+00		4.54E-06

		-1.60E+00		1.87E+01		1.87E-05		-1.22E+00		4.51E+00		4.51E-06

		-1.59E+00		1.83E+01		1.83E-05		-1.22E+00		4.46E+00		4.46E-06

		-1.59E+00		1.79E+01		1.79E-05		-1.22E+00		4.46E+00		4.46E-06

		-1.59E+00		1.75E+01		1.75E-05		-1.21E+00		4.45E+00		4.45E-06

		-1.58E+00		1.74E+01		1.74E-05		-1.21E+00		4.43E+00		4.43E-06

		-1.58E+00		1.70E+01		1.70E-05		-1.20E+00		4.43E+00		4.43E-06

		-1.57E+00		1.67E+01		1.67E-05		-1.20E+00		4.38E+00		4.38E-06

		-1.57E+00		1.64E+01		1.64E-05		-1.20E+00		4.35E+00		4.35E-06

		-1.57E+00		1.62E+01		1.62E-05		-1.19E+00		4.38E+00		4.38E-06

		-1.56E+00		1.59E+01		1.59E-05		-1.19E+00		4.30E+00		4.30E-06

		-1.56E+00		1.58E+01		1.58E-05		-1.18E+00		4.37E+00		4.37E-06

		-1.55E+00		1.54E+01		1.54E-05		-1.18E+00		4.24E+00		4.24E-06

		-1.55E+00		1.50E+01		1.50E-05		-1.18E+00		4.30E+00		4.30E-06

		-1.55E+00		1.49E+01		1.49E-05		-1.17E+00		4.23E+00		4.23E-06

		-1.54E+00		1.47E+01		1.47E-05		-1.17E+00		4.25E+00		4.25E-06

		-1.54E+00		1.45E+01		1.45E-05		-1.16E+00		4.20E+00		4.20E-06

		-1.53E+00		1.43E+01		1.43E-05		-1.16E+00		4.18E+00		4.18E-06

		-1.53E+00		1.40E+01		1.40E-05		-1.16E+00		4.18E+00		4.18E-06

		-1.53E+00		1.38E+01		1.38E-05		-1.15E+00		4.18E+00		4.18E-06

		-1.52E+00		1.36E+01		1.36E-05		-1.15E+00		4.13E+00		4.13E-06

		-1.52E+00		1.34E+01		1.34E-05		-1.14E+00		4.16E+00		4.16E-06

		-1.51E+00		1.33E+01		1.33E-05		-1.14E+00		4.06E+00		4.06E-06

		-1.51E+00		1.31E+01		1.31E-05		-1.14E+00		4.11E+00		4.11E-06

		-1.51E+00		1.29E+01		1.29E-05		-1.13E+00		4.06E+00		4.06E-06

		-1.50E+00		1.28E+01		1.28E-05		-1.13E+00		4.04E+00		4.04E-06

		-1.50E+00		1.26E+01		1.26E-05		-1.12E+00		4.07E+00		4.07E-06

		-1.49E+00		1.25E+01		1.25E-05		-1.12E+00		3.97E+00		3.97E-06

		-1.49E+00		1.23E+01		1.23E-05		-1.12E+00		4.01E+00		4.01E-06

		-1.49E+00		1.21E+01		1.21E-05		-1.11E+00		3.96E+00		3.96E-06

		-1.48E+00		1.20E+01		1.20E-05		-1.11E+00		3.94E+00		3.94E-06

		-1.48E+00		1.19E+01		1.19E-05		-1.10E+00		3.96E+00		3.96E-06

		-1.47E+00		1.17E+01		1.17E-05		-1.10E+00		3.86E+00		3.86E-06

		-1.47E+00		1.16E+01		1.16E-05		-1.10E+00		3.89E+00		3.89E-06

		-1.47E+00		1.16E+01		1.16E-05		-1.09E+00		3.88E+00		3.88E-06

		-1.46E+00		1.15E+01		1.15E-05		-1.09E+00		3.83E+00		3.83E-06

		-1.46E+00		1.14E+01		1.14E-05		-1.08E+00		3.86E+00		3.86E-06

		-1.45E+00		1.12E+01		1.12E-05		-1.08E+00		3.75E+00		3.75E-06

		-1.45E+00		1.11E+01		1.11E-05		-1.08E+00		3.81E+00		3.81E-06

		-1.45E+00		1.10E+01		1.10E-05		-1.07E+00		3.75E+00		3.75E-06

		-1.44E+00		1.09E+01		1.09E-05		-1.07E+00		3.72E+00		3.72E-06

		-1.44E+00		1.08E+01		1.08E-05		-1.06E+00		3.73E+00		3.73E-06

		-1.43E+00		1.07E+01		1.07E-05		-1.06E+00		3.65E+00		3.65E-06

		-1.43E+00		1.07E+01		1.07E-05		-1.06E+00		3.68E+00		3.68E-06

		-1.43E+00		1.06E+01		1.06E-05		-1.05E+00		3.62E+00		3.62E-06

		-1.42E+00		1.05E+01		1.05E-05		-1.05E+00		3.60E+00		3.60E-06

		-1.42E+00		1.04E+01		1.04E-05		-1.04E+00		3.62E+00		3.62E-06

		-1.41E+00		1.03E+01		1.03E-05		-1.04E+00		3.55E+00		3.55E-06

		-1.41E+00		1.02E+01		1.02E-05		-1.04E+00		3.55E+00		3.55E-06

		-1.41E+00		1.02E+01		1.02E-05		-1.03E+00		3.54E+00		3.54E-06

		-1.40E+00		1.01E+01		1.01E-05		-1.03E+00		3.47E+00		3.47E-06

		-1.40E+00		1.01E+01		1.01E-05		-1.02E+00		3.52E+00		3.52E-06

		-1.39E+00		9.98E+00		9.98E-06		-1.02E+00		3.43E+00		3.43E-06

		-1.39E+00		9.93E+00		9.93E-06		-1.02E+00		3.44E+00		3.44E-06

		-1.39E+00		9.90E+00		9.90E-06		-1.01E+00		3.40E+00		3.40E-06

		-1.38E+00		9.80E+00		9.80E-06		-1.01E+00		3.38E+00		3.38E-06

		-1.38E+00		9.76E+00		9.76E-06		-1.00E+00		3.39E+00		3.39E-06

		-1.37E+00		9.71E+00		9.71E-06		-9.99E-01		3.34E+00		3.34E-06

		-1.37E+00		9.61E+00		9.61E-06		-9.95E-01		3.34E+00		3.34E-06

		-1.37E+00		9.60E+00		9.60E-06		-9.91E-01		3.31E+00		3.31E-06

		-1.36E+00		9.55E+00		9.55E-06		-9.87E-01		3.28E+00		3.28E-06

		-1.36E+00		9.55E+00		9.55E-06		-9.83E-01		3.26E+00		3.26E-06

		-1.35E+00		9.44E+00		9.44E-06		-9.79E-01		3.20E+00		3.20E-06

		-1.35E+00		9.37E+00		9.37E-06		-9.75E-01		3.24E+00		3.24E-06

		-1.35E+00		9.35E+00		9.35E-06		-9.71E-01		3.20E+00		3.20E-06

		-1.34E+00		9.31E+00		9.31E-06		-9.67E-01		3.15E+00		3.15E-06

		-1.34E+00		9.34E+00		9.34E-06		-9.63E-01		3.17E+00		3.17E-06

		-1.33E+00		9.29E+00		9.29E-06		-9.59E-01		3.10E+00		3.10E-06

		-1.33E+00		9.21E+00		9.21E-06		-9.55E-01		3.09E+00		3.09E-06

		-1.33E+00		9.19E+00		9.19E-06		-9.51E-01		3.09E+00		3.09E-06

		-1.32E+00		9.12E+00		9.12E-06		-9.47E-01		3.04E+00		3.04E-06

		-1.32E+00		9.16E+00		9.16E-06		-9.43E-01		3.07E+00		3.07E-06

		-1.31E+00		9.06E+00		9.06E-06		-9.39E-01		2.94E+00		2.94E-06

		-1.31E+00		9.07E+00		9.07E-06		-9.35E-01		3.00E+00		3.00E-06

		-1.31E+00		9.03E+00		9.03E-06		-9.31E-01		2.94E+00		2.94E-06

		-1.30E+00		9.01E+00		9.01E-06		-9.27E-01		2.90E+00		2.90E-06

		-1.30E+00		9.00E+00		9.00E-06		-9.23E-01		2.91E+00		2.91E-06

		-1.29E+00		8.87E+00		8.87E-06		-9.19E-01		2.84E+00		2.84E-06

		-1.29E+00		8.92E+00		8.92E-06		-9.15E-01		2.83E+00		2.83E-06

		-1.29E+00		8.88E+00		8.88E-06		-9.11E-01		2.80E+00		2.80E-06

		-1.28E+00		8.85E+00		8.85E-06		-9.07E-01		2.77E+00		2.77E-06

		-1.28E+00		8.87E+00		8.87E-06		-9.03E-01		2.74E+00		2.74E-06

		-1.27E+00		8.78E+00		8.78E-06		-8.99E-01		2.68E+00		2.68E-06

		-1.27E+00		8.75E+00		8.75E-06		-8.95E-01		2.66E+00		2.66E-06

		-1.27E+00		8.75E+00		8.75E-06		-8.91E-01		2.66E+00		2.66E-06

		-1.26E+00		8.71E+00		8.71E-06		-8.87E-01		2.58E+00		2.58E-06

		-1.26E+00		8.73E+00		8.73E-06		-8.83E-01		2.56E+00		2.56E-06

		-1.25E+00		8.63E+00		8.63E-06		-8.79E-01		2.45E+00		2.45E-06

		-1.25E+00		8.68E+00		8.68E-06		-8.75E-01		2.49E+00		2.49E-06

		-1.25E+00		8.64E+00		8.64E-06		-8.71E-01		2.39E+00		2.39E-06

		-1.24E+00		8.58E+00		8.58E-06		-8.67E-01		2.38E+00		2.38E-06

		-1.24E+00		8.59E+00		8.59E-06		-8.63E-01		2.33E+00		2.33E-06

		-1.23E+00		8.50E+00		8.50E-06		-8.59E-01		2.30E+00		2.30E-06

		-1.23E+00		8.54E+00		8.54E-06		-8.55E-01		2.25E+00		2.25E-06

		-1.23E+00		8.54E+00		8.54E-06		-8.51E-01		2.24E+00		2.24E-06

		-1.22E+00		8.48E+00		8.48E-06		-8.47E-01		2.15E+00		2.15E-06

		-1.22E+00		8.52E+00		8.52E-06		-8.43E-01		2.14E+00		2.14E-06

		-1.21E+00		8.44E+00		8.44E-06		-8.39E-01		2.03E+00		2.03E-06

		-1.21E+00		8.43E+00		8.43E-06		-8.35E-01		2.05E+00		2.05E-06

		-1.21E+00		8.42E+00		8.42E-06		-8.31E-01		1.98E+00		1.98E-06

		-1.20E+00		8.40E+00		8.40E-06		-8.27E-01		1.98E+00		1.98E-06

		-1.20E+00		8.41E+00		8.41E-06		-8.23E-01		1.89E+00		1.89E-06

		-1.19E+00		8.32E+00		8.32E-06		-8.19E-01		1.84E+00		1.84E-06

		-1.19E+00		8.36E+00		8.36E-06		-8.15E-01		1.82E+00		1.82E-06

		-1.19E+00		8.32E+00		8.32E-06		-8.11E-01		1.78E+00		1.78E-06

		-1.18E+00		8.29E+00		8.29E-06		-8.07E-01		1.78E+00		1.78E-06

		-1.18E+00		8.35E+00		8.35E-06		-8.03E-01		1.71E+00		1.71E-06

		-1.17E+00		8.20E+00		8.20E-06		-7.99E-01		1.67E+00		1.67E-06

		-1.17E+00		8.21E+00		8.21E-06		-7.95E-01		1.62E+00		1.62E-06

		-1.17E+00		8.17E+00		8.17E-06		-7.91E-01		1.60E+00		1.60E-06

		-1.16E+00		8.18E+00		8.18E-06		-7.87E-01		1.54E+00		1.54E-06

		-1.16E+00		8.18E+00		8.18E-06		-7.83E-01		1.56E+00		1.56E-06

		-1.15E+00		8.12E+00		8.12E-06		-7.79E-01		1.47E+00		1.47E-06

		-1.15E+00		8.16E+00		8.16E-06		-7.75E-01		1.48E+00		1.48E-06

		-1.15E+00		8.07E+00		8.07E-06		-7.71E-01		1.43E+00		1.43E-06

		-1.14E+00		8.07E+00		8.07E-06		-7.67E-01		1.40E+00		1.40E-06

		-1.14E+00		8.07E+00		8.07E-06		-7.63E-01		1.39E+00		1.39E-06

		-1.13E+00		8.03E+00		8.03E-06		-7.59E-01		1.32E+00		1.32E-06

		-1.13E+00		8.04E+00		8.04E-06		-7.55E-01		1.32E+00		1.32E-06

		-1.13E+00		7.99E+00		7.99E-06		-7.51E-01		1.29E+00		1.29E-06

		-1.12E+00		7.97E+00		7.97E-06		-7.47E-01		1.25E+00		1.25E-06

		-1.12E+00		7.90E+00		7.90E-06		-7.43E-01		1.26E+00		1.26E-06

		-1.11E+00		7.92E+00		7.92E-06		-7.39E-01		1.19E+00		1.19E-06

		-1.11E+00		7.90E+00		7.90E-06		-7.35E-01		1.20E+00		1.20E-06

		-1.11E+00		7.89E+00		7.89E-06		-7.31E-01		1.17E+00		1.17E-06

		-1.10E+00		7.86E+00		7.86E-06		-7.27E-01		1.14E+00		1.14E-06

		-1.10E+00		7.85E+00		7.85E-06		-7.23E-01		1.14E+00		1.14E-06

		-1.09E+00		7.78E+00		7.78E-06		-7.19E-01		1.08E+00		1.08E-06

		-1.09E+00		7.71E+00		7.71E-06		-7.15E-01		1.09E+00		1.09E-06

		-1.09E+00		7.76E+00		7.76E-06		-7.11E-01		1.07E+00		1.07E-06

		-1.08E+00		7.70E+00		7.70E-06		-7.07E-01		1.03E+00		1.03E-06

		-1.08E+00		7.72E+00		7.72E-06		-7.03E-01		1.04E+00		1.04E-06

		-1.07E+00		7.67E+00		7.67E-06		-6.99E-01		9.68E-01		9.68E-07

		-1.07E+00		7.66E+00		7.66E-06		-6.95E-01		9.98E-01		9.98E-07

		-1.07E+00		7.63E+00		7.63E-06		-6.91E-01		9.58E-01		9.58E-07

		-1.06E+00		7.50E+00		7.50E-06		-6.87E-01		9.37E-01		9.37E-07

		-1.06E+00		7.62E+00		7.62E-06		-6.83E-01		9.34E-01		9.34E-07

		-1.05E+00		7.50E+00		7.50E-06		-6.79E-01		8.76E-01		8.76E-07

		-1.05E+00		7.51E+00		7.51E-06		-6.75E-01		8.93E-01		8.93E-07

		-1.05E+00		7.45E+00		7.45E-06		-6.71E-01		8.72E-01		8.72E-07

		-1.04E+00		7.46E+00		7.46E-06		-6.67E-01		8.39E-01		8.39E-07

		-1.04E+00		7.43E+00		7.43E-06		-6.63E-01		8.41E-01		8.41E-07

		-1.03E+00		7.34E+00		7.34E-06		-6.59E-01		7.77E-01		7.77E-07

		-1.03E+00		7.39E+00		7.39E-06		-6.55E-01		8.06E-01		8.06E-07

		-1.03E+00		7.37E+00		7.37E-06		-6.51E-01		7.63E-01		7.63E-07

		-1.02E+00		7.35E+00		7.35E-06		-6.47E-01		7.40E-01		7.40E-07

		-1.02E+00		7.33E+00		7.33E-06		-6.43E-01		7.32E-01		7.32E-07

		-1.01E+00		7.25E+00		7.25E-06		-6.39E-01		6.76E-01		6.76E-07

		-1.01E+00		7.23E+00		7.23E-06		-6.35E-01		6.90E-01		6.90E-07

		-1.01E+00		7.16E+00		7.16E-06		-6.31E-01		6.66E-01		6.66E-07

		-1.00E+00		7.16E+00		7.16E-06		-6.27E-01		6.29E-01		6.29E-07

		-9.98E-01		7.20E+00		7.20E-06		-6.23E-01		6.26E-01		6.26E-07

		-9.94E-01		7.06E+00		7.06E-06		-6.19E-01		5.60E-01		5.60E-07

		-9.90E-01		7.07E+00		7.07E-06		-6.15E-01		5.94E-01		5.94E-07

		-9.86E-01		7.05E+00		7.05E-06		-6.11E-01		5.46E-01		5.46E-07

		-9.82E-01		6.98E+00		6.98E-06		-6.07E-01		5.22E-01		5.22E-07

		-9.78E-01		6.98E+00		6.98E-06		-6.03E-01		5.13E-01		5.13E-07

		-9.74E-01		6.92E+00		6.92E-06		-5.99E-01		4.65E-01		4.65E-07

		-9.70E-01		6.95E+00		6.95E-06		-5.95E-01		4.71E-01		4.71E-07

		-9.66E-01		6.85E+00		6.85E-06		-5.91E-01		4.44E-01		4.44E-07

		-9.62E-01		6.83E+00		6.83E-06		-5.87E-01		4.11E-01		4.11E-07

		-9.58E-01		6.85E+00		6.85E-06		-5.83E-01		4.07E-01		4.07E-07

		-9.54E-01		6.75E+00		6.75E-06		-5.79E-01		3.40E-01		3.40E-07

		-9.50E-01		6.75E+00		6.75E-06		-5.75E-01		3.71E-01		3.71E-07

		-9.46E-01		6.69E+00		6.69E-06		-5.71E-01		3.29E-01		3.29E-07

		-9.42E-01		6.66E+00		6.66E-06		-5.67E-01		3.01E-01		3.01E-07

		-9.38E-01		6.67E+00		6.67E-06		-5.63E-01		2.87E-01		2.87E-07

		-9.34E-01		6.59E+00		6.59E-06		-5.59E-01		2.38E-01		2.38E-07

		-9.30E-01		6.56E+00		6.56E-06		-5.55E-01		2.53E-01		2.53E-07

		-9.26E-01		6.51E+00		6.51E-06		-5.51E-01		2.15E-01		2.15E-07

		-9.22E-01		6.47E+00		6.47E-06		-5.47E-01		1.84E-01		1.84E-07

		-9.18E-01		6.50E+00		6.50E-06		-5.43E-01		1.79E-01		1.79E-07

		-9.14E-01		6.35E+00		6.35E-06		-5.39E-01		1.36E-01		1.36E-07

		-9.10E-01		6.38E+00		6.38E-06		-5.35E-01		1.20E-01		1.20E-07

		-9.06E-01		6.32E+00		6.32E-06		-5.31E-01		1.08E-01		1.08E-07

		-9.02E-01		6.26E+00		6.26E-06		-5.27E-01		5.97E-02		5.97E-08

		-8.98E-01		6.25E+00		6.25E-06		-5.23E-01		5.62E-02		5.62E-08

		-8.94E-01		6.15E+00		6.15E-06		-5.19E-01		1.73E-02		1.73E-08

		-8.90E-01		6.17E+00		6.17E-06		-5.15E-01		-6.30E-03		-6.30E-09

		-8.86E-01		6.08E+00		6.08E-06		-5.11E-01		-3.30E-02		-3.30E-08

		-8.82E-01		6.02E+00		6.02E-06		-5.07E-01		-6.68E-02		-6.68E-08

		-8.78E-01		6.03E+00		6.03E-06		-5.03E-01		-8.20E-02		-8.20E-08

		-8.74E-01		5.91E+00		5.91E-06		-4.99E-01		-1.33E-01		-1.33E-07

		-8.70E-01		5.92E+00		5.92E-06		-4.95E-01		-1.21E-01		-1.21E-07

		-8.66E-01		5.86E+00		5.86E-06		-4.91E-01		-1.56E-01		-1.56E-07

		-8.62E-01		5.76E+00		5.76E-06		-4.87E-01		-1.92E-01		-1.92E-07

		-8.58E-01		5.72E+00		5.72E-06		-4.83E-01		-2.07E-01		-2.07E-07

		-8.54E-01		5.69E+00		5.69E-06		-4.79E-01		-2.77E-01		-2.77E-07

		-8.50E-01		5.61E+00		5.61E-06		-4.75E-01		-2.47E-01		-2.47E-07

		-8.46E-01		5.58E+00		5.58E-06		-4.71E-01		-2.95E-01		-2.95E-07

		-8.42E-01		5.50E+00		5.50E-06		-4.67E-01		-3.31E-01		-3.31E-07

		-8.38E-01		5.49E+00		5.49E-06		-4.63E-01		-3.51E-01		-3.51E-07

		-8.34E-01		5.34E+00		5.34E-06		-4.59E-01		-4.11E-01		-4.11E-07

		-8.30E-01		5.33E+00		5.33E-06		-4.55E-01		-4.01E-01		-4.01E-07

		-8.26E-01		5.26E+00		5.26E-06		-4.51E-01		-4.38E-01		-4.38E-07

		-8.22E-01		5.17E+00		5.17E-06		-4.47E-01		-4.77E-01		-4.77E-07

		-8.18E-01		5.18E+00		5.18E-06		-4.43E-01		-4.94E-01		-4.94E-07

		-8.14E-01		5.06E+00		5.06E-06		-4.39E-01		-5.57E-01		-5.57E-07

		-8.10E-01		5.09E+00		5.09E-06		-4.35E-01		-5.39E-01		-5.39E-07

		-8.06E-01		5.01E+00		5.01E-06		-4.31E-01		-5.94E-01		-5.94E-07

		-8.02E-01		4.86E+00		4.86E-06		-4.27E-01		-6.24E-01		-6.24E-07

		-7.98E-01		4.91E+00		4.91E-06		-4.23E-01		-6.61E-01		-6.61E-07

		-7.94E-01		4.80E+00		4.80E-06		-4.19E-01		-7.08E-01		-7.08E-07

		-7.90E-01		4.76E+00		4.76E-06		-4.15E-01		-7.06E-01		-7.06E-07

		-7.86E-01		4.72E+00		4.72E-06		-4.11E-01		-7.53E-01		-7.53E-07

		-7.82E-01		4.66E+00		4.66E-06		-4.07E-01		-7.89E-01		-7.89E-07

		-7.78E-01		4.67E+00		4.67E-06		-4.03E-01		-8.17E-01		-8.17E-07

		-7.74E-01		4.47E+00		4.47E-06		-3.99E-01		-8.85E-01		-8.85E-07

		-7.70E-01		4.50E+00		4.50E-06		-3.95E-01		-8.65E-01		-8.65E-07

		-7.66E-01		4.47E+00		4.47E-06		-3.91E-01		-9.26E-01		-9.26E-07

		-7.62E-01		4.34E+00		4.34E-06		-3.87E-01		-9.55E-01		-9.55E-07

		-7.58E-01		4.34E+00		4.34E-06		-3.83E-01		-9.99E-01		-9.99E-07

		-7.54E-01		4.23E+00		4.23E-06		-3.79E-01		-1.05E+00		-1.05E-06

		-7.50E-01		4.23E+00		4.23E-06		-3.75E-01		-1.06E+00		-1.06E-06

		-7.46E-01		4.12E+00		4.12E-06		-3.71E-01		-1.10E+00		-1.10E-06

		-7.42E-01		4.10E+00		4.10E-06		-3.67E-01		-1.15E+00		-1.15E-06

		-7.38E-01		4.12E+00		4.12E-06		-3.63E-01		-1.18E+00		-1.18E-06

		-7.34E-01		4.00E+00		4.00E-06		-3.59E-01		-1.25E+00		-1.25E-06

		-7.30E-01		4.00E+00		4.00E-06		-3.55E-01		-1.24E+00		-1.24E-06

		-7.26E-01		3.91E+00		3.91E-06		-3.51E-01		-1.30E+00		-1.30E-06

		-7.22E-01		3.84E+00		3.84E-06		-3.47E-01		-1.34E+00		-1.34E-06

		-7.18E-01		3.82E+00		3.82E-06		-3.43E-01		-1.39E+00		-1.39E-06

		-7.14E-01		3.75E+00		3.75E-06		-3.39E-01		-1.44E+00		-1.44E-06

		-7.10E-01		3.76E+00		3.76E-06		-3.35E-01		-1.45E+00		-1.45E-06

		-7.06E-01		3.66E+00		3.66E-06		-3.31E-01		-1.50E+00		-1.50E-06

		-7.02E-01		3.63E+00		3.63E-06		-3.27E-01		-1.57E+00		-1.57E-06

		-6.98E-01		3.62E+00		3.62E-06		-3.23E-01		-1.55E+00		-1.55E-06

		-6.94E-01		3.57E+00		3.57E-06		-3.19E-01		-1.69E+00		-1.69E-06

		-6.90E-01		3.53E+00		3.53E-06		-3.15E-01		-1.68E+00		-1.68E-06

		-6.86E-01		3.53E+00		3.53E-06		-3.11E-01		-1.69E+00		-1.69E-06

		-6.82E-01		3.42E+00		3.42E-06		-3.07E-01		-1.76E+00		-1.76E-06

		-6.78E-01		3.42E+00		3.42E-06		-3.03E-01		-1.75E+00		-1.75E-06

		-6.74E-01		3.34E+00		3.34E-06		-2.99E-01		-1.84E+00		-1.84E-06

		-6.70E-01		3.36E+00		3.36E-06		-2.95E-01		-1.83E+00		-1.83E-06

		-6.66E-01		3.29E+00		3.29E-06		-2.91E-01		-1.91E+00		-1.91E-06

		-6.62E-01		3.20E+00		3.20E-06		-2.87E-01		-1.94E+00		-1.94E-06

		-6.58E-01		3.22E+00		3.22E-06		-2.83E-01		-1.88E+00		-1.88E-06

		-6.54E-01		3.09E+00		3.09E-06		-2.79E-01		-1.99E+00		-1.99E-06

		-6.50E-01		3.12E+00		3.12E-06		-2.75E-01		-1.94E+00		-1.94E-06

		-6.46E-01		3.08E+00		3.08E-06		-2.71E-01		-1.99E+00		-1.99E-06

		-6.42E-01		3.05E+00		3.05E-06		-2.67E-01		-1.98E+00		-1.98E-06

		-6.38E-01		2.98E+00		2.98E-06		-2.63E-01		-1.97E+00		-1.97E-06

		-6.34E-01		2.88E+00		2.88E-06		-2.59E-01		-2.03E+00		-2.03E-06

		-6.30E-01		2.93E+00		2.93E-06		-2.55E-01		-2.02E+00		-2.02E-06

		-6.26E-01		2.82E+00		2.82E-06		-2.51E-01		-2.03E+00		-2.03E-06

		-6.22E-01		2.84E+00		2.84E-06		-2.47E-01		-2.05E+00		-2.05E-06

		-6.18E-01		2.78E+00		2.78E-06		-2.43E-01		-1.96E+00		-1.96E-06

		-6.14E-01		2.73E+00		2.73E-06		-2.39E-01		-2.06E+00		-2.06E-06

		-6.10E-01		2.66E+00		2.66E-06		-2.35E-01		-2.01E+00		-2.01E-06

		-6.06E-01		2.67E+00		2.67E-06		-2.31E-01		-2.06E+00		-2.06E-06

		-6.02E-01		2.66E+00		2.66E-06		-2.27E-01		-2.05E+00		-2.05E-06

		-5.98E-01		2.54E+00		2.54E-06		-2.23E-01		-2.02E+00		-2.02E-06

		-5.94E-01		2.47E+00		2.47E-06		-2.19E-01		-2.08E+00		-2.08E-06

		-5.90E-01		2.48E+00		2.48E-06		-2.15E-01		-2.09E+00		-2.09E-06

		-5.86E-01		2.50E+00		2.50E-06		-2.11E-01		-2.11E+00		-2.11E-06

		-5.82E-01		2.42E+00		2.42E-06		-2.07E-01		-2.14E+00		-2.14E-06

		-5.78E-01		2.38E+00		2.38E-06		-2.03E-01		-2.10E+00		-2.10E-06

		-5.74E-01		2.30E+00		2.30E-06		-1.99E-01		-2.22E+00		-2.22E-06

		-5.70E-01		2.27E+00		2.27E-06		-1.95E-01		-2.19E+00		-2.19E-06

		-5.66E-01		2.25E+00		2.25E-06		-1.91E-01		-2.25E+00		-2.25E-06

		-5.62E-01		2.24E+00		2.24E-06		-1.87E-01		-2.29E+00		-2.29E-06

		-5.58E-01		2.16E+00		2.16E-06		-1.83E-01		-2.31E+00		-2.31E-06

		-5.54E-01		2.12E+00		2.12E-06		-1.79E-01		-2.41E+00		-2.41E-06

		-5.50E-01		2.14E+00		2.14E-06		-1.75E-01		-2.41E+00		-2.41E-06

		-5.46E-01		2.06E+00		2.06E-06		-1.71E-01		-2.52E+00		-2.52E-06

		-5.42E-01		1.97E+00		1.97E-06		-1.67E-01		-2.53E+00		-2.53E-06

		-5.38E-01		2.03E+00		2.03E-06		-1.63E-01		-2.61E+00		-2.61E-06

		-5.34E-01		1.88E+00		1.88E-06		-1.59E-01		-2.69E+00		-2.69E-06

		-5.30E-01		1.92E+00		1.92E-06		-1.55E-01		-2.74E+00		-2.74E-06

		-5.26E-01		1.86E+00		1.86E-06		-1.51E-01		-2.82E+00		-2.82E-06

		-5.22E-01		1.80E+00		1.80E-06		-1.47E-01		-2.90E+00		-2.90E-06

		-5.18E-01		1.75E+00		1.75E-06		-1.43E-01		-2.97E+00		-2.97E-06

		-5.14E-01		1.62E+00		1.62E-06		-1.39E-01		-3.09E+00		-3.09E-06

		-5.10E-01		1.68E+00		1.68E-06		-1.35E-01		-3.13E+00		-3.13E-06

		-5.06E-01		1.66E+00		1.66E-06		-1.31E-01		-3.26E+00		-3.26E-06

		-5.02E-01		1.58E+00		1.58E-06		-1.27E-01		-3.32E+00		-3.32E-06

		-4.98E-01		1.51E+00		1.51E-06		-1.23E-01		-3.41E+00		-3.41E-06

		-4.94E-01		1.46E+00		1.46E-06		-1.19E-01		-3.54E+00		-3.54E-06

		-4.90E-01		1.47E+00		1.47E-06		-1.15E-01		-3.61E+00		-3.61E-06

		-4.86E-01		1.41E+00		1.41E-06		-1.11E-01		-3.78E+00		-3.78E-06

		-4.82E-01		1.35E+00		1.35E-06		-1.07E-01		-3.88E+00		-3.88E-06

		-4.78E-01		1.34E+00		1.34E-06		-1.03E-01		-4.01E+00		-4.01E-06

		-4.74E-01		1.21E+00		1.21E-06		-9.90E-02		-4.16E+00		-4.16E-06

		-4.70E-01		1.22E+00		1.22E-06		-9.50E-02		-4.31E+00		-4.31E-06

		-4.66E-01		1.17E+00		1.17E-06		-9.10E-02		-4.43E+00		-4.43E-06

		-4.62E-01		1.10E+00		1.10E-06		-8.70E-02		-4.58E+00		-4.58E-06

		-4.58E-01		1.07E+00		1.07E-06		-8.30E-02		-4.74E+00		-4.74E-06

		-4.54E-01		9.73E-01		9.73E-07		-7.90E-02		-4.93E+00		-4.93E-06

		-4.50E-01		9.74E-01		9.74E-07		-7.50E-02		-5.06E+00		-5.06E-06

		-4.46E-01		9.10E-01		9.10E-07		-7.10E-02		-5.25E+00		-5.25E-06

		-4.42E-01		8.47E-01		8.47E-07		-6.70E-02		-5.42E+00		-5.42E-06

		-4.38E-01		8.21E-01		8.21E-07		-6.30E-02		-5.59E+00		-5.59E-06

		-4.34E-01		7.22E-01		7.22E-07		-5.90E-02		-5.81E+00		-5.81E-06

		-4.30E-01		7.02E-01		7.02E-07		-5.50E-02		-5.98E+00		-5.98E-06

		-4.26E-01		6.64E-01		6.64E-07		-5.10E-02		-6.20E+00		-6.20E-06

		-4.22E-01		6.02E-01		6.02E-07		-4.70E-02		-6.35E+00		-6.35E-06

		-4.18E-01		5.61E-01		5.61E-07		-4.30E-02		-6.60E+00		-6.60E-06

		-4.14E-01		4.64E-01		4.64E-07		-3.90E-02		-6.84E+00		-6.84E-06

		-4.10E-01		4.54E-01		4.54E-07		-3.50E-02		-7.00E+00		-7.00E-06

		-4.06E-01		4.07E-01		4.07E-07		-3.10E-02		-7.24E+00		-7.24E-06

		-4.02E-01		3.33E-01		3.33E-07		-2.70E-02		-7.46E+00		-7.46E-06

		-3.98E-01		3.02E-01		3.02E-07		-2.30E-02		-7.70E+00		-7.70E-06

		-3.94E-01		2.06E-01		2.06E-07		-1.90E-02		-7.91E+00		-7.91E-06

		-3.90E-01		2.00E-01		2.00E-07		-1.50E-02		-8.11E+00		-8.11E-06

		-3.86E-01		1.45E-01		1.45E-07		-1.10E-02		-8.36E+00		-8.36E-06

		-3.82E-01		7.86E-02		7.86E-08		-7.01E-03		-8.56E+00		-8.56E-06

		-3.78E-01		5.70E-02		5.70E-08		-3.01E-03		-8.83E+00		-8.83E-06

		-3.74E-01		-5.50E-02		-5.50E-08		9.89E-04		-9.07E+00		-9.07E-06

		-3.70E-01		-4.50E-02		-4.50E-08		4.99E-03		-9.25E+00		-9.25E-06

		-3.66E-01		-9.60E-02		-9.60E-08		8.99E-03		-9.48E+00		-9.48E-06

		-3.62E-01		-1.65E-01		-1.65E-07		1.30E-02		-9.71E+00		-9.71E-06

		-3.58E-01		-1.89E-01		-1.89E-07		1.70E-02		-9.90E+00		-9.90E-06

		-3.54E-01		-2.99E-01		-2.99E-07		2.10E-02		-1.01E+01		-1.01E-05

		-3.50E-01		-2.73E-01		-2.73E-07		2.50E-02		-1.03E+01		-1.03E-05

		-3.46E-01		-3.46E-01		-3.46E-07		2.90E-02		-1.05E+01		-1.05E-05

		-3.42E-01		-3.94E-01		-3.94E-07		3.30E-02		-1.06E+01		-1.06E-05

		-3.38E-01		-4.22E-01		-4.22E-07		3.70E-02		-1.08E+01		-1.08E-05

		-3.34E-01		-5.16E-01		-5.16E-07		4.10E-02		-1.09E+01		-1.09E-05

		-3.30E-01		-4.95E-01		-4.95E-07		4.50E-02		-1.11E+01		-1.11E-05

		-3.26E-01		-5.41E-01		-5.41E-07		4.90E-02		-1.12E+01		-1.12E-05

		-3.22E-01		-5.93E-01		-5.93E-07		5.30E-02		-1.13E+01		-1.13E-05

		-3.18E-01		-6.33E-01		-6.33E-07		5.70E-02		-1.14E+01		-1.14E-05

		-3.14E-01		-7.07E-01		-7.07E-07		6.10E-02		-1.15E+01		-1.15E-05

		-3.10E-01		-6.98E-01		-6.98E-07		6.50E-02		-1.15E+01		-1.15E-05

		-3.06E-01		-7.38E-01		-7.38E-07		6.90E-02		-1.16E+01		-1.16E-05

		-3.02E-01		-7.85E-01		-7.85E-07		7.30E-02		-1.16E+01		-1.16E-05

		-2.98E-01		-8.19E-01		-8.19E-07		7.70E-02		-1.17E+01		-1.17E-05

		-2.94E-01		-8.86E-01		-8.86E-07		8.10E-02		-1.16E+01		-1.16E-05

		-2.90E-01		-8.90E-01		-8.90E-07		8.50E-02		-1.17E+01		-1.17E-05

		-2.86E-01		-9.07E-01		-9.07E-07		8.90E-02		-1.16E+01		-1.16E-05

		-2.82E-01		-9.71E-01		-9.71E-07		9.30E-02		-1.16E+01		-1.16E-05

		-2.78E-01		-9.99E-01		-9.99E-07		9.70E-02		-1.16E+01		-1.16E-05

		-2.74E-01		-1.06E+00		-1.06E-06		1.01E-01		-1.15E+01		-1.15E-05

		-2.70E-01		-1.06E+00		-1.06E-06		1.05E-01		-1.15E+01		-1.15E-05

		-2.66E-01		-1.09E+00		-1.09E-06		1.09E-01		-1.15E+01		-1.15E-05

		-2.62E-01		-1.16E+00		-1.16E-06		1.13E-01		-1.14E+01		-1.14E-05

		-2.58E-01		-1.19E+00		-1.19E-06		1.17E-01		-1.13E+01		-1.13E-05

		-2.54E-01		-1.26E+00		-1.26E-06		1.21E-01		-1.12E+01		-1.12E-05

		-2.50E-01		-1.26E+00		-1.26E-06		1.25E-01		-1.12E+01		-1.12E-05

		-2.46E-01		-1.30E+00		-1.30E-06		1.29E-01		-1.11E+01		-1.11E-05

		-2.42E-01		-1.35E+00		-1.35E-06		1.33E-01		-1.10E+01		-1.10E-05

		-2.38E-01		-1.41E+00		-1.41E-06		1.37E-01		-1.09E+01		-1.09E-05

		-2.34E-01		-1.50E+00		-1.50E-06		1.41E-01		-1.08E+01		-1.08E-05

		-2.30E-01		-1.49E+00		-1.49E-06		1.45E-01		-1.07E+01		-1.07E-05

		-2.26E-01		-1.60E+00		-1.60E-06		1.49E-01		-1.07E+01		-1.07E-05

		-2.22E-01		-1.63E+00		-1.63E-06		1.53E-01		-1.06E+01		-1.06E-05

		-2.18E-01		-1.72E+00		-1.72E-06		1.57E-01		-1.05E+01		-1.05E-05

		-2.14E-01		-1.76E+00		-1.76E-06		1.61E-01		-1.04E+01		-1.04E-05

		-2.10E-01		-1.79E+00		-1.79E-06		1.65E-01		-1.03E+01		-1.03E-05

		-2.06E-01		-1.83E+00		-1.83E-06		1.69E-01		-1.02E+01		-1.02E-05

		-2.02E-01		-1.88E+00		-1.88E-06		1.73E-01		-1.02E+01		-1.02E-05

		-1.98E-01		-1.98E+00		-1.98E-06		1.77E-01		-1.01E+01		-1.01E-05

		-1.94E-01		-2.08E+00		-2.08E-06		1.81E-01		-1.00E+01		-1.00E-05

		-1.90E-01		-2.12E+00		-2.12E-06		1.85E-01		-9.90E+00		-9.90E-06

		-1.86E-01		-2.17E+00		-2.17E-06		1.89E-01		-9.82E+00		-9.82E-06

		-1.82E-01		-2.26E+00		-2.26E-06		1.93E-01		-9.77E+00		-9.77E-06

		-1.78E-01		-2.29E+00		-2.29E-06		1.97E-01		-9.69E+00		-9.69E-06

		-1.74E-01		-2.39E+00		-2.39E-06		2.01E-01		-9.59E+00		-9.59E-06

		-1.70E-01		-2.40E+00		-2.40E-06		2.05E-01		-9.51E+00		-9.51E-06

		-1.66E-01		-2.53E+00		-2.53E-06		2.09E-01		-9.46E+00		-9.46E-06

		-1.62E-01		-2.62E+00		-2.62E-06		2.13E-01		-9.38E+00		-9.38E-06

		-1.58E-01		-2.68E+00		-2.68E-06		2.17E-01		-9.33E+00		-9.33E-06

		-1.54E-01		-2.79E+00		-2.79E-06		2.21E-01		-9.26E+00		-9.26E-06

		-1.50E-01		-2.84E+00		-2.84E-06		2.25E-01		-9.21E+00		-9.21E-06

		-1.46E-01		-2.88E+00		-2.88E-06		2.29E-01		-9.15E+00		-9.15E-06

		-1.42E-01		-3.03E+00		-3.03E-06		2.33E-01		-9.06E+00		-9.06E-06

		-1.38E-01		-3.12E+00		-3.12E-06		2.37E-01		-9.05E+00		-9.05E-06

		-1.34E-01		-3.25E+00		-3.25E-06		2.41E-01		-8.96E+00		-8.96E-06

		-1.30E-01		-3.30E+00		-3.30E-06		2.45E-01		-8.93E+00		-8.93E-06

		-1.26E-01		-3.41E+00		-3.41E-06		2.49E-01		-8.87E+00		-8.87E-06

		-1.22E-01		-3.52E+00		-3.52E-06		2.53E-01		-8.81E+00		-8.81E-06

		-1.18E-01		-3.66E+00		-3.66E-06		2.57E-01		-8.75E+00		-8.75E-06

		-1.14E-01		-3.81E+00		-3.81E-06		2.61E-01		-8.69E+00		-8.69E-06

		-1.10E-01		-3.90E+00		-3.90E-06		2.65E-01		-8.64E+00		-8.64E-06

		-1.06E-01		-4.12E+00		-4.12E-06		2.69E-01		-8.63E+00		-8.63E-06

		-1.02E-01		-4.25E+00		-4.25E-06		2.73E-01		-8.52E+00		-8.52E-06

		-9.80E-02		-4.44E+00		-4.44E-06		2.77E-01		-8.52E+00		-8.52E-06

		-9.40E-02		-4.64E+00		-4.64E-06		2.81E-01		-8.43E+00		-8.43E-06

		-9.00E-02		-4.83E+00		-4.83E-06		2.85E-01		-8.39E+00		-8.39E-06

		-8.60E-02		-5.02E+00		-5.02E-06		2.89E-01		-8.38E+00		-8.38E-06

		-8.20E-02		-5.29E+00		-5.29E-06		2.93E-01		-8.32E+00		-8.32E-06

		-7.80E-02		-5.54E+00		-5.54E-06		2.97E-01		-8.29E+00		-8.29E-06

		-7.40E-02		-5.78E+00		-5.78E-06		3.01E-01		-8.21E+00		-8.21E-06

		-7.00E-02		-6.00E+00		-6.00E-06		3.05E-01		-8.21E+00		-8.21E-06

		-6.60E-02		-6.30E+00		-6.30E-06		3.09E-01		-8.16E+00		-8.16E-06

		-6.20E-02		-6.55E+00		-6.55E-06		3.13E-01		-8.12E+00		-8.12E-06

		-5.80E-02		-6.83E+00		-6.83E-06		3.17E-01		-8.07E+00		-8.07E-06

		-5.40E-02		-7.18E+00		-7.18E-06		3.21E-01		-8.02E+00		-8.02E-06

		-5.00E-02		-7.49E+00		-7.49E-06		3.25E-01		-7.98E+00		-7.98E-06

		-4.60E-02		-7.81E+00		-7.81E-06		3.29E-01		-7.95E+00		-7.95E-06

		-4.20E-02		-8.07E+00		-8.07E-06		3.33E-01		-7.88E+00		-7.88E-06

		-3.80E-02		-8.40E+00		-8.40E-06		3.37E-01		-7.88E+00		-7.88E-06

		-3.40E-02		-8.79E+00		-8.79E-06		3.41E-01		-7.82E+00		-7.82E-06

		-3.00E-02		-9.09E+00		-9.09E-06		3.45E-01		-7.78E+00		-7.78E-06

		-2.60E-02		-9.42E+00		-9.42E-06		3.49E-01		-7.75E+00		-7.75E-06

		-2.20E-02		-9.78E+00		-9.78E-06		3.53E-01		-7.67E+00		-7.67E-06

		-1.80E-02		-1.01E+01		-1.01E-05		3.57E-01		-7.63E+00		-7.63E-06

		-1.40E-02		-1.05E+01		-1.05E-05		3.61E-01		-7.62E+00		-7.62E-06

		-1.00E-02		-1.08E+01		-1.08E-05		3.65E-01		-7.55E+00		-7.55E-06

		-6.01E-03		-1.11E+01		-1.11E-05		3.69E-01		-7.55E+00		-7.55E-06

		-2.01E-03		-1.15E+01		-1.15E-05		3.73E-01		-7.46E+00		-7.46E-06

		1.99E-03		-1.17E+01		-1.17E-05		3.77E-01		-7.47E+00		-7.47E-06

		5.99E-03		-1.21E+01		-1.21E-05		3.81E-01		-7.38E+00		-7.38E-06

		9.99E-03		-1.24E+01		-1.24E-05		3.85E-01		-7.37E+00		-7.37E-06

		1.40E-02		-1.27E+01		-1.27E-05		3.89E-01		-7.33E+00		-7.33E-06

		1.80E-02		-1.30E+01		-1.30E-05		3.93E-01		-7.30E+00		-7.30E-06

		2.20E-02		-1.32E+01		-1.32E-05		3.97E-01		-7.23E+00		-7.23E-06

		2.60E-02		-1.35E+01		-1.35E-05		4.01E-01		-7.22E+00		-7.22E-06

		3.00E-02		-1.37E+01		-1.37E-05		4.05E-01		-7.14E+00		-7.14E-06

		3.40E-02		-1.39E+01		-1.39E-05		4.09E-01		-7.16E+00		-7.16E-06

		3.80E-02		-1.42E+01		-1.42E-05		4.13E-01		-7.07E+00		-7.07E-06

		4.20E-02		-1.43E+01		-1.43E-05		4.17E-01		-7.08E+00		-7.08E-06

		4.60E-02		-1.46E+01		-1.46E-05		4.21E-01		-7.03E+00		-7.03E-06

		5.00E-02		-1.47E+01		-1.47E-05		4.25E-01		-6.98E+00		-6.98E-06

		5.40E-02		-1.48E+01		-1.48E-05		4.29E-01		-6.94E+00		-6.94E-06

		5.80E-02		-1.49E+01		-1.49E-05		4.33E-01		-6.93E+00		-6.93E-06

		6.20E-02		-1.50E+01		-1.50E-05		4.37E-01		-6.87E+00		-6.87E-06

		6.60E-02		-1.52E+01		-1.52E-05		4.41E-01		-6.86E+00		-6.86E-06

		7.00E-02		-1.53E+01		-1.53E-05		4.45E-01		-6.80E+00		-6.80E-06

		7.40E-02		-1.53E+01		-1.53E-05		4.49E-01		-6.79E+00		-6.79E-06

		7.80E-02		-1.53E+01		-1.53E-05		4.53E-01		-6.72E+00		-6.72E-06

		8.20E-02		-1.53E+01		-1.53E-05		4.57E-01		-6.68E+00		-6.68E-06

		8.60E-02		-1.54E+01		-1.54E-05		4.61E-01		-6.69E+00		-6.69E-06

		9.00E-02		-1.54E+01		-1.54E-05		4.65E-01		-6.58E+00		-6.58E-06

		9.40E-02		-1.54E+01		-1.54E-05		4.69E-01		-6.63E+00		-6.63E-06

		9.80E-02		-1.54E+01		-1.54E-05		4.73E-01		-6.56E+00		-6.56E-06

		1.02E-01		-1.54E+01		-1.54E-05		4.77E-01		-6.54E+00		-6.54E-06

		1.06E-01		-1.54E+01		-1.54E-05		4.81E-01		-6.47E+00		-6.47E-06

		1.10E-01		-1.54E+01		-1.54E-05		4.85E-01		-6.45E+00		-6.45E-06

		1.14E-01		-1.53E+01		-1.53E-05		4.89E-01		-6.46E+00		-6.46E-06

		1.18E-01		-1.52E+01		-1.52E-05		4.93E-01		-6.42E+00		-6.42E-06

		1.22E-01		-1.52E+01		-1.52E-05		4.97E-01		-6.41E+00		-6.41E-06

		1.26E-01		-1.53E+01		-1.53E-05		5.01E-01		-6.40E+00		-6.40E-06

		1.30E-01		-1.51E+01		-1.51E-05		5.05E-01		-6.33E+00		-6.33E-06

		1.34E-01		-1.51E+01		-1.51E-05		5.09E-01		-6.35E+00		-6.35E-06

		1.38E-01		-1.50E+01		-1.50E-05		5.13E-01		-6.31E+00		-6.31E-06

		1.42E-01		-1.49E+01		-1.49E-05		5.17E-01		-6.31E+00		-6.31E-06

		1.46E-01		-1.49E+01		-1.49E-05		5.21E-01		-6.29E+00		-6.29E-06

		1.50E-01		-1.48E+01		-1.48E-05		5.25E-01		-6.20E+00		-6.20E-06

		1.54E-01		-1.48E+01		-1.48E-05		5.29E-01		-6.24E+00		-6.24E-06

		1.58E-01		-1.47E+01		-1.47E-05		5.33E-01		-6.18E+00		-6.18E-06

		1.62E-01		-1.46E+01		-1.46E-05		5.37E-01		-6.17E+00		-6.17E-06

		1.66E-01		-1.46E+01		-1.46E-05		5.41E-01		-6.15E+00		-6.15E-06

		1.70E-01		-1.45E+01		-1.45E-05		5.45E-01		-6.13E+00		-6.13E-06

		1.74E-01		-1.45E+01		-1.45E-05		5.49E-01		-6.11E+00		-6.11E-06

		1.78E-01		-1.44E+01		-1.44E-05		5.53E-01		-6.08E+00		-6.08E-06

		1.82E-01		-1.43E+01		-1.43E-05		5.57E-01		-6.07E+00		-6.07E-06

		1.86E-01		-1.42E+01		-1.42E-05		5.61E-01		-6.06E+00		-6.06E-06

		1.90E-01		-1.41E+01		-1.41E-05		5.65E-01		-5.98E+00		-5.98E-06

		1.94E-01		-1.41E+01		-1.41E-05		5.69E-01		-6.04E+00		-6.04E-06

		1.98E-01		-1.41E+01		-1.41E-05		5.73E-01		-6.00E+00		-6.00E-06

		2.02E-01		-1.40E+01		-1.40E-05		5.77E-01		-5.97E+00		-5.97E-06

		2.06E-01		-1.39E+01		-1.39E-05		5.81E-01		-5.98E+00		-5.98E-06

		2.10E-01		-1.39E+01		-1.39E-05		5.85E-01		-5.94E+00		-5.94E-06

		2.14E-01		-1.37E+01		-1.37E-05		5.89E-01		-5.96E+00		-5.96E-06

		2.18E-01		-1.37E+01		-1.37E-05		5.93E-01		-5.93E+00		-5.93E-06

		2.22E-01		-1.37E+01		-1.37E-05		5.97E-01		-5.89E+00		-5.89E-06

		2.26E-01		-1.36E+01		-1.36E-05		6.01E-01		-5.94E+00		-5.94E-06

		2.30E-01		-1.35E+01		-1.35E-05		6.05E-01		-5.89E+00		-5.89E-06

		2.34E-01		-1.35E+01		-1.35E-05		6.09E-01		-5.93E+00		-5.93E-06

		2.38E-01		-1.35E+01		-1.35E-05		6.13E-01		-5.88E+00		-5.88E-06

		2.42E-01		-1.34E+01		-1.34E-05		6.17E-01		-5.89E+00		-5.89E-06

		2.46E-01		-1.33E+01		-1.33E-05		6.21E-01		-5.89E+00		-5.89E-06

		2.50E-01		-1.33E+01		-1.33E-05		6.25E-01		-5.84E+00		-5.84E-06

		2.54E-01		-1.32E+01		-1.32E-05		6.29E-01		-5.85E+00		-5.85E-06

		2.58E-01		-1.32E+01		-1.32E-05		6.33E-01		-5.86E+00		-5.86E-06

		2.62E-01		-1.32E+01		-1.32E-05		6.37E-01		-5.86E+00		-5.86E-06

		2.66E-01		-1.31E+01		-1.31E-05		6.41E-01		-5.87E+00		-5.87E-06

		2.70E-01		-1.30E+01		-1.30E-05		6.45E-01		-5.84E+00		-5.84E-06

		2.74E-01		-1.30E+01		-1.30E-05		6.49E-01		-5.87E+00		-5.87E-06

		2.78E-01		-1.30E+01		-1.30E-05		6.53E-01		-5.84E+00		-5.84E-06

		2.82E-01		-1.29E+01		-1.29E-05		6.57E-01		-5.82E+00		-5.82E-06

		2.86E-01		-1.29E+01		-1.29E-05		6.61E-01		-5.88E+00		-5.88E-06

		2.90E-01		-1.28E+01		-1.28E-05		6.65E-01		-5.84E+00		-5.84E-06

		2.94E-01		-1.28E+01		-1.28E-05		6.69E-01		-5.91E+00		-5.91E-06

		2.98E-01		-1.28E+01		-1.28E-05		6.73E-01		-5.88E+00		-5.88E-06

		3.02E-01		-1.28E+01		-1.28E-05		6.77E-01		-5.90E+00		-5.90E-06

		3.06E-01		-1.27E+01		-1.27E-05		6.81E-01		-5.88E+00		-5.88E-06

		3.10E-01		-1.26E+01		-1.26E-05		6.85E-01		-5.88E+00		-5.88E-06

		3.14E-01		-1.26E+01		-1.26E-05		6.89E-01		-5.91E+00		-5.91E-06

		3.18E-01		-1.25E+01		-1.25E-05		6.93E-01		-5.95E+00		-5.95E-06

		3.22E-01		-1.25E+01		-1.25E-05		6.97E-01		-5.89E+00		-5.89E-06

		3.26E-01		-1.24E+01		-1.24E-05		7.01E-01		-5.94E+00		-5.94E-06

		3.30E-01		-1.24E+01		-1.24E-05		7.05E-01		-5.93E+00		-5.93E-06

		3.34E-01		-1.24E+01		-1.24E-05		7.09E-01		-5.99E+00		-5.99E-06

		3.38E-01		-1.23E+01		-1.23E-05		7.13E-01		-5.96E+00		-5.96E-06

		3.42E-01		-1.23E+01		-1.23E-05		7.17E-01		-5.98E+00		-5.98E-06

		3.46E-01		-1.22E+01		-1.22E-05		7.21E-01		-5.94E+00		-5.94E-06

		3.50E-01		-1.22E+01		-1.22E-05		7.25E-01		-6.02E+00		-6.02E-06

		3.54E-01		-1.22E+01		-1.22E-05		7.29E-01		-6.01E+00		-6.01E-06

		3.58E-01		-1.22E+01		-1.22E-05		7.33E-01		-6.05E+00		-6.05E-06

		3.62E-01		-1.21E+01		-1.21E-05		7.37E-01		-6.01E+00		-6.01E-06

		3.66E-01		-1.20E+01		-1.20E-05		7.41E-01		-6.09E+00		-6.09E-06

		3.70E-01		-1.20E+01		-1.20E-05		7.45E-01		-6.04E+00		-6.04E-06

		3.74E-01		-1.20E+01		-1.20E-05		7.49E-01		-6.12E+00		-6.12E-06

		3.78E-01		-1.19E+01		-1.19E-05		7.53E-01		-6.07E+00		-6.07E-06

		3.82E-01		-1.19E+01		-1.19E-05		7.57E-01		-6.10E+00		-6.10E-06

		3.86E-01		-1.19E+01		-1.19E-05		7.61E-01		-6.10E+00		-6.10E-06

		3.90E-01		-1.18E+01		-1.18E-05		7.65E-01		-6.13E+00		-6.13E-06

		3.94E-01		-1.17E+01		-1.17E-05		7.69E-01		-6.17E+00		-6.17E-06

		3.98E-01		-1.17E+01		-1.17E-05		7.73E-01		-6.12E+00		-6.12E-06

		4.02E-01		-1.17E+01		-1.17E-05		7.77E-01		-6.16E+00		-6.16E-06

		4.06E-01		-1.16E+01		-1.16E-05		7.81E-01		-6.17E+00		-6.17E-06

		4.10E-01		-1.16E+01		-1.16E-05		7.85E-01		-6.21E+00		-6.21E-06

		4.14E-01		-1.16E+01		-1.16E-05		7.89E-01		-6.21E+00		-6.21E-06

		4.18E-01		-1.16E+01		-1.16E-05		7.93E-01		-6.22E+00		-6.22E-06

		4.22E-01		-1.15E+01		-1.15E-05		7.97E-01		-6.19E+00		-6.19E-06

		4.26E-01		-1.14E+01		-1.14E-05		8.01E-01		-6.22E+00		-6.22E-06

		4.30E-01		-1.14E+01		-1.14E-05		8.05E-01		-6.26E+00		-6.26E-06

		4.34E-01		-1.14E+01		-1.14E-05		8.09E-01		-6.29E+00		-6.29E-06

		4.38E-01		-1.14E+01		-1.14E-05		8.13E-01		-6.30E+00		-6.30E-06

		4.42E-01		-1.14E+01		-1.14E-05		8.17E-01		-6.30E+00		-6.30E-06

		4.46E-01		-1.13E+01		-1.13E-05		8.21E-01		-6.36E+00		-6.36E-06

		4.50E-01		-1.13E+01		-1.13E-05		8.25E-01		-6.35E+00		-6.35E-06

		4.54E-01		-1.13E+01		-1.13E-05		8.29E-01		-6.41E+00		-6.41E-06

		4.58E-01		-1.12E+01		-1.12E-05		8.33E-01		-6.38E+00		-6.38E-06

		4.62E-01		-1.12E+01		-1.12E-05		8.37E-01		-6.45E+00		-6.45E-06

		4.66E-01		-1.11E+01		-1.11E-05		8.41E-01		-6.42E+00		-6.42E-06

		4.70E-01		-1.11E+01		-1.11E-05		8.45E-01		-6.51E+00		-6.51E-06

		4.74E-01		-1.11E+01		-1.11E-05		8.49E-01		-6.55E+00		-6.55E-06

		4.78E-01		-1.11E+01		-1.11E-05		8.53E-01		-6.55E+00		-6.55E-06

		4.82E-01		-1.10E+01		-1.10E-05		8.57E-01		-6.58E+00		-6.58E-06

		4.86E-01		-1.10E+01		-1.10E-05		8.61E-01		-6.64E+00		-6.64E-06

		4.90E-01		-1.10E+01		-1.10E-05		8.65E-01		-6.73E+00		-6.73E-06

		4.94E-01		-1.10E+01		-1.10E-05		8.69E-01		-6.76E+00		-6.76E-06

		4.98E-01		-1.10E+01		-1.10E-05		8.73E-01		-6.80E+00		-6.80E-06

		5.02E-01		-1.08E+01		-1.08E-05		8.77E-01		-6.86E+00		-6.86E-06

		5.06E-01		-1.09E+01		-1.09E-05		8.81E-01		-6.94E+00		-6.94E-06

		5.10E-01		-1.08E+01		-1.08E-05		8.85E-01		-7.05E+00		-7.05E-06

		5.14E-01		-1.09E+01		-1.09E-05		8.89E-01		-7.11E+00		-7.11E-06

		5.18E-01		-1.08E+01		-1.08E-05		8.93E-01		-7.19E+00		-7.19E-06

		5.22E-01		-1.08E+01		-1.08E-05		8.97E-01		-7.28E+00		-7.28E-06

		5.26E-01		-1.07E+01		-1.07E-05		9.01E-01		-7.36E+00		-7.36E-06

		5.30E-01		-1.07E+01		-1.07E-05		9.05E-01		-7.51E+00		-7.51E-06

		5.34E-01		-1.08E+01		-1.08E-05		9.09E-01		-7.64E+00		-7.64E-06

		5.38E-01		-1.07E+01		-1.07E-05		9.13E-01		-7.71E+00		-7.71E-06

		5.42E-01		-1.07E+01		-1.07E-05		9.17E-01		-7.85E+00		-7.85E-06

		5.46E-01		-1.06E+01		-1.06E-05		9.21E-01		-7.98E+00		-7.98E-06

		5.50E-01		-1.06E+01		-1.06E-05		9.25E-01		-8.16E+00		-8.16E-06

		5.54E-01		-1.07E+01		-1.07E-05		9.29E-01		-8.34E+00		-8.34E-06

		5.58E-01		-1.06E+01		-1.06E-05		9.33E-01		-8.44E+00		-8.44E-06

		5.62E-01		-1.06E+01		-1.06E-05		9.37E-01		-8.59E+00		-8.59E-06

		5.66E-01		-1.06E+01		-1.06E-05		9.41E-01		-8.77E+00		-8.77E-06

		5.70E-01		-1.06E+01		-1.06E-05		9.45E-01		-9.03E+00		-9.03E-06

		5.74E-01		-1.06E+01		-1.06E-05		9.49E-01		-9.15E+00		-9.15E-06

		5.78E-01		-1.05E+01		-1.05E-05		9.53E-01		-9.34E+00		-9.34E-06

		5.82E-01		-1.05E+01		-1.05E-05		9.57E-01		-9.54E+00		-9.54E-06

		5.86E-01		-1.05E+01		-1.05E-05		9.61E-01		-9.77E+00		-9.77E-06

		5.90E-01		-1.05E+01		-1.05E-05		9.65E-01		-1.01E+01		-1.01E-05

		5.94E-01		-1.05E+01		-1.05E-05		9.69E-01		-1.03E+01		-1.03E-05

		5.98E-01		-1.05E+01		-1.05E-05		9.73E-01		-1.05E+01		-1.05E-05

		6.02E-01		-1.05E+01		-1.05E-05		9.77E-01		-1.09E+01		-1.09E-05

		6.06E-01		-1.05E+01		-1.05E-05		9.81E-01		-1.10E+01		-1.10E-05

		6.10E-01		-1.05E+01		-1.05E-05		9.85E-01		-1.16E+01		-1.16E-05

		6.14E-01		-1.06E+01		-1.06E-05		9.89E-01		-1.18E+01		-1.18E-05

		6.18E-01		-1.06E+01		-1.06E-05		9.93E-01		-1.21E+01		-1.21E-05

		6.22E-01		-1.06E+01		-1.06E-05		9.97E-01		-1.24E+01		-1.24E-05

		6.26E-01		-1.05E+01		-1.05E-05		1.00E+00		-1.29E+01		-1.29E-05

		6.30E-01		-1.05E+01		-1.05E-05		1.01E+00		-1.34E+01		-1.34E-05

		6.34E-01		-1.06E+01		-1.06E-05		1.01E+00		-1.38E+01		-1.38E-05

		6.38E-01		-1.06E+01		-1.06E-05		1.01E+00		-1.42E+01		-1.42E-05

		6.42E-01		-1.06E+01		-1.06E-05		1.02E+00		-1.47E+01		-1.47E-05

		6.46E-01		-1.06E+01		-1.06E-05		1.02E+00		-1.51E+01		-1.51E-05

		6.50E-01		-1.06E+01		-1.06E-05		1.03E+00		-1.59E+01		-1.59E-05

		6.54E-01		-1.07E+01		-1.07E-05		1.03E+00		-1.63E+01		-1.63E-05

		6.58E-01		-1.07E+01		-1.07E-05		1.03E+00		-1.69E+01		-1.69E-05

		6.62E-01		-1.07E+01		-1.07E-05		1.04E+00		-1.73E+01		-1.73E-05

		6.66E-01		-1.07E+01		-1.07E-05		1.04E+00		-1.79E+01		-1.79E-05

		6.70E-01		-1.07E+01		-1.07E-05		1.05E+00		-1.87E+01		-1.87E-05

		6.74E-01		-1.08E+01		-1.08E-05		1.05E+00		-1.91E+01		-1.91E-05

		6.78E-01		-1.08E+01		-1.08E-05		1.05E+00		-1.98E+01		-1.98E-05

		6.82E-01		-1.08E+01		-1.08E-05		1.06E+00		-2.04E+01		-2.04E-05

		6.86E-01		-1.08E+01		-1.08E-05		1.06E+00		-2.08E+01		-2.08E-05

		6.90E-01		-1.09E+01		-1.09E-05		1.07E+00		-2.17E+01		-2.17E-05

		6.94E-01		-1.09E+01		-1.09E-05		1.07E+00		-2.21E+01		-2.21E-05

		6.98E-01		-1.09E+01		-1.09E-05		1.07E+00		-2.27E+01		-2.27E-05

		7.02E-01		-1.10E+01		-1.10E-05		1.08E+00		-2.31E+01		-2.31E-05

		7.06E-01		-1.10E+01		-1.10E-05		1.08E+00		-2.36E+01		-2.36E-05

		7.10E-01		-1.10E+01		-1.10E-05		1.09E+00		-2.41E+01		-2.41E-05

		7.14E-01		-1.10E+01		-1.10E-05		1.09E+00		-2.44E+01		-2.44E-05

		7.18E-01		-1.10E+01		-1.10E-05		1.09E+00		-2.48E+01		-2.48E-05

		7.22E-01		-1.11E+01		-1.11E-05		1.10E+00		-2.54E+01		-2.54E-05

		7.26E-01		-1.11E+01		-1.11E-05		1.10E+00		-2.54E+01		-2.54E-05

		7.30E-01		-1.11E+01		-1.11E-05		1.11E+00		-2.61E+01		-2.61E-05

		7.34E-01		-1.12E+01		-1.12E-05		1.11E+00		-2.58E+01		-2.58E-05

		7.38E-01		-1.12E+01		-1.12E-05		1.11E+00		-2.63E+01		-2.63E-05

		7.42E-01		-1.12E+01		-1.12E-05		1.12E+00		-2.63E+01		-2.63E-05

		7.46E-01		-1.12E+01		-1.12E-05		1.12E+00		-2.65E+01		-2.65E-05

		7.50E-01		-1.12E+01		-1.12E-05		1.13E+00		-2.69E+01		-2.69E-05

		7.54E-01		-1.13E+01		-1.13E-05		1.13E+00		-2.68E+01		-2.68E-05

		7.58E-01		-1.13E+01		-1.13E-05		1.13E+00		-2.70E+01		-2.70E-05

		7.62E-01		-1.13E+01		-1.13E-05		1.14E+00		-2.71E+01		-2.71E-05

		7.66E-01		-1.14E+01		-1.14E-05		1.14E+00		-2.73E+01		-2.73E-05

		7.70E-01		-1.13E+01		-1.13E-05		1.15E+00		-2.73E+01		-2.73E-05

		7.74E-01		-1.15E+01		-1.15E-05		1.15E+00		-2.73E+01		-2.73E-05

		7.78E-01		-1.14E+01		-1.14E-05		1.15E+00		-2.73E+01		-2.73E-05

		7.82E-01		-1.14E+01		-1.14E-05		1.16E+00		-2.74E+01		-2.74E-05

		7.86E-01		-1.14E+01		-1.14E-05		1.16E+00		-2.74E+01		-2.74E-05

		7.90E-01		-1.14E+01		-1.14E-05		1.17E+00		-2.73E+01		-2.73E-05

		7.94E-01		-1.15E+01		-1.15E-05		1.17E+00		-2.73E+01		-2.73E-05

		7.98E-01		-1.15E+01		-1.15E-05		1.17E+00		-2.71E+01		-2.71E-05

		8.02E-01		-1.15E+01		-1.15E-05		1.18E+00		-2.73E+01		-2.73E-05

		8.06E-01		-1.16E+01		-1.16E-05		1.18E+00		-2.70E+01		-2.70E-05

		8.10E-01		-1.15E+01		-1.15E-05		1.19E+00		-2.72E+01		-2.72E-05

		8.14E-01		-1.16E+01		-1.16E-05		1.19E+00		-2.69E+01		-2.69E-05

		8.18E-01		-1.16E+01		-1.16E-05		1.19E+00		-2.69E+01		-2.69E-05

		8.22E-01		-1.17E+01		-1.17E-05		1.20E+00		-2.66E+01		-2.66E-05

		8.26E-01		-1.17E+01		-1.17E-05		1.20E+00		-2.66E+01		-2.66E-05

		8.30E-01		-1.17E+01		-1.17E-05		1.21E+00		-2.64E+01		-2.64E-05

		8.34E-01		-1.17E+01		-1.17E-05		1.21E+00		-2.62E+01		-2.62E-05

		8.38E-01		-1.18E+01		-1.18E-05		1.21E+00		-2.60E+01		-2.60E-05

		8.42E-01		-1.18E+01		-1.18E-05		1.22E+00		-2.58E+01		-2.58E-05

		8.46E-01		-1.18E+01		-1.18E-05		1.22E+00		-2.57E+01		-2.57E-05

		8.50E-01		-1.19E+01		-1.19E-05		1.23E+00		-2.54E+01		-2.54E-05

		8.54E-01		-1.19E+01		-1.19E-05		1.23E+00		-2.54E+01		-2.54E-05

		8.58E-01		-1.19E+01		-1.19E-05		1.23E+00		-2.51E+01		-2.51E-05

		8.62E-01		-1.20E+01		-1.20E-05		1.24E+00		-2.50E+01		-2.50E-05

		8.66E-01		-1.21E+01		-1.21E-05		1.24E+00		-2.47E+01		-2.47E-05

		8.70E-01		-1.21E+01		-1.21E-05		1.25E+00		-2.46E+01		-2.46E-05

		8.74E-01		-1.22E+01		-1.22E-05		1.25E+00		-2.45E+01		-2.45E-05

		8.78E-01		-1.23E+01		-1.23E-05		1.25E+00		-2.42E+01		-2.42E-05

		8.82E-01		-1.23E+01		-1.23E-05		1.26E+00		-2.40E+01		-2.40E-05

		8.86E-01		-1.24E+01		-1.24E-05		1.26E+00		-2.39E+01		-2.39E-05

		8.90E-01		-1.24E+01		-1.24E-05		1.27E+00		-2.37E+01		-2.37E-05

		8.94E-01		-1.26E+01		-1.26E-05		1.27E+00		-2.34E+01		-2.34E-05

		8.98E-01		-1.27E+01		-1.27E-05		1.27E+00		-2.32E+01		-2.32E-05

		9.02E-01		-1.28E+01		-1.28E-05		1.28E+00		-2.30E+01		-2.30E-05

		9.06E-01		-1.28E+01		-1.28E-05		1.28E+00		-2.30E+01		-2.30E-05

		9.10E-01		-1.29E+01		-1.29E-05		1.29E+00		-2.26E+01		-2.26E-05

		9.14E-01		-1.31E+01		-1.31E-05		1.29E+00		-2.25E+01		-2.25E-05

		9.18E-01		-1.32E+01		-1.32E-05		1.29E+00		-2.22E+01		-2.22E-05

		9.22E-01		-1.33E+01		-1.33E-05		1.30E+00		-2.19E+01		-2.19E-05

		9.26E-01		-1.35E+01		-1.35E-05		1.30E+00		-2.18E+01		-2.18E-05

		9.30E-01		-1.36E+01		-1.36E-05		1.31E+00		-2.16E+01		-2.16E-05

		9.34E-01		-1.38E+01		-1.38E-05		1.31E+00		-2.14E+01		-2.14E-05

		9.38E-01		-1.39E+01		-1.39E-05		1.31E+00		-2.12E+01		-2.12E-05

		9.42E-01		-1.41E+01		-1.41E-05		1.32E+00		-2.11E+01		-2.11E-05

		9.46E-01		-1.42E+01		-1.42E-05		1.32E+00		-2.08E+01		-2.08E-05

		9.50E-01		-1.44E+01		-1.44E-05		1.33E+00		-2.06E+01		-2.06E-05

		9.54E-01		-1.46E+01		-1.46E-05		1.33E+00		-2.05E+01		-2.05E-05

		9.58E-01		-1.48E+01		-1.48E-05		1.33E+00		-2.03E+01		-2.03E-05

		9.62E-01		-1.50E+01		-1.50E-05		1.34E+00		-2.01E+01		-2.01E-05

		9.66E-01		-1.52E+01		-1.52E-05		1.34E+00		-1.99E+01		-1.99E-05

		9.70E-01		-1.55E+01		-1.55E-05		1.35E+00		-1.96E+01		-1.96E-05

		9.74E-01		-1.57E+01		-1.57E-05		1.35E+00		-1.96E+01		-1.96E-05

		9.78E-01		-1.60E+01		-1.60E-05		1.35E+00		-1.95E+01		-1.95E-05

		9.82E-01		-1.63E+01		-1.63E-05		1.36E+00		-1.92E+01		-1.92E-05

		9.86E-01		-1.65E+01		-1.65E-05		1.36E+00		-1.91E+01		-1.91E-05

		9.90E-01		-1.68E+01		-1.68E-05		1.37E+00		-1.88E+01		-1.88E-05

		9.94E-01		-1.73E+01		-1.73E-05		1.37E+00		-1.88E+01		-1.88E-05

		9.98E-01		-1.75E+01		-1.75E-05		1.37E+00		-1.87E+01		-1.87E-05

		1.00E+00		-1.78E+01		-1.78E-05		1.38E+00		-1.85E+01		-1.85E-05

		1.01E+00		-1.83E+01		-1.83E-05		1.38E+00		-1.85E+01		-1.85E-05

		1.01E+00		-1.89E+01		-1.89E-05		1.39E+00		-1.82E+01		-1.82E-05

		1.01E+00		-1.95E+01		-1.95E-05		1.39E+00		-1.83E+01		-1.83E-05

		1.02E+00		-2.00E+01		-2.00E-05		1.39E+00		-1.79E+01		-1.79E-05

		1.02E+00		-2.04E+01		-2.04E-05		1.40E+00		-1.81E+01		-1.81E-05

		1.03E+00		-2.10E+01		-2.10E-05		1.40E+00		-1.78E+01		-1.78E-05

		1.03E+00		-2.14E+01		-2.14E-05		1.41E+00		-1.76E+01		-1.76E-05

		1.03E+00		-2.20E+01		-2.20E-05		1.41E+00		-1.76E+01		-1.76E-05

		1.04E+00		-2.29E+01		-2.29E-05		1.41E+00		-1.76E+01		-1.76E-05

		1.04E+00		-2.38E+01		-2.38E-05		1.42E+00		-1.74E+01		-1.74E-05

		1.05E+00		-2.41E+01		-2.41E-05		1.42E+00		-1.72E+01		-1.72E-05

		1.05E+00		-2.52E+01		-2.52E-05		1.43E+00		-1.72E+01		-1.72E-05

		1.05E+00		-2.55E+01		-2.55E-05		1.43E+00		-1.70E+01		-1.70E-05

		1.06E+00		-2.60E+01		-2.60E-05		1.43E+00		-1.69E+01		-1.69E-05

		1.06E+00		-2.68E+01		-2.68E-05		1.44E+00		-1.66E+01		-1.66E-05

		1.07E+00		-2.74E+01		-2.74E-05		1.44E+00		-1.66E+01		-1.66E-05

		1.07E+00		-2.80E+01		-2.80E-05		1.45E+00		-1.62E+01		-1.62E-05

		1.07E+00		-2.84E+01		-2.84E-05		1.45E+00		-1.65E+01		-1.65E-05

		1.08E+00		-2.92E+01		-2.92E-05		1.45E+00		-1.62E+01		-1.62E-05

		1.08E+00		-2.95E+01		-2.95E-05		1.46E+00		-1.62E+01		-1.62E-05

		1.09E+00		-2.97E+01		-2.97E-05		1.46E+00		-1.62E+01		-1.62E-05

		1.09E+00		-3.04E+01		-3.04E-05		1.47E+00		-1.60E+01		-1.60E-05

		1.09E+00		-3.05E+01		-3.05E-05		1.47E+00		-1.59E+01		-1.59E-05

		1.10E+00		-3.08E+01		-3.08E-05		1.47E+00		-1.58E+01		-1.58E-05

		1.10E+00		-3.11E+01		-3.11E-05		1.48E+00		-1.59E+01		-1.59E-05

		1.11E+00		-3.12E+01		-3.12E-05		1.48E+00		-1.57E+01		-1.57E-05

		1.11E+00		-3.15E+01		-3.15E-05		1.49E+00		-1.56E+01		-1.56E-05

		1.11E+00		-3.15E+01		-3.15E-05		1.49E+00		-1.55E+01		-1.55E-05

		1.12E+00		-3.22E+01		-3.22E-05		1.49E+00		-1.54E+01		-1.54E-05

		1.12E+00		-3.19E+01		-3.19E-05		1.50E+00		-1.54E+01		-1.54E-05

		1.13E+00		-3.19E+01		-3.19E-05		1.50E+00		-1.53E+01		-1.53E-05

		1.13E+00		-3.22E+01		-3.22E-05		1.51E+00		-1.54E+01		-1.54E-05

		1.13E+00		-3.23E+01		-3.23E-05		1.51E+00		-1.53E+01		-1.53E-05

		1.14E+00		-3.23E+01		-3.23E-05		1.51E+00		-1.51E+01		-1.51E-05

		1.14E+00		-3.24E+01		-3.24E-05		1.52E+00		-1.50E+01		-1.50E-05

		1.15E+00		-3.25E+01		-3.25E-05		1.52E+00		-1.51E+01		-1.51E-05

		1.15E+00		-3.27E+01		-3.27E-05		1.53E+00		-1.50E+01		-1.50E-05

		1.15E+00		-3.26E+01		-3.26E-05		1.53E+00		-1.50E+01		-1.50E-05

		1.16E+00		-3.26E+01		-3.26E-05		1.53E+00		-1.49E+01		-1.49E-05

		1.16E+00		-3.27E+01		-3.27E-05		1.54E+00		-1.49E+01		-1.49E-05

		1.17E+00		-3.28E+01		-3.28E-05		1.54E+00		-1.48E+01		-1.48E-05

		1.17E+00		-3.27E+01		-3.27E-05		1.55E+00		-1.47E+01		-1.47E-05

		1.17E+00		-3.28E+01		-3.28E-05		1.55E+00		-1.48E+01		-1.48E-05

		1.18E+00		-3.28E+01		-3.28E-05		1.55E+00		-1.47E+01		-1.47E-05

		1.18E+00		-3.28E+01		-3.28E-05		1.56E+00		-1.47E+01		-1.47E-05

		1.19E+00		-3.29E+01		-3.29E-05		1.56E+00		-1.46E+01		-1.46E-05

		1.19E+00		-3.27E+01		-3.27E-05		1.57E+00		-1.46E+01		-1.46E-05

		1.19E+00		-3.29E+01		-3.29E-05		1.57E+00		-1.46E+01		-1.46E-05

		1.20E+00		-3.27E+01		-3.27E-05		1.57E+00		-1.45E+01		-1.45E-05

		1.20E+00		-3.26E+01		-3.26E-05		1.58E+00		-1.45E+01		-1.45E-05

		1.21E+00		-3.25E+01		-3.25E-05		1.58E+00		-1.45E+01		-1.45E-05

		1.21E+00		-3.25E+01		-3.25E-05		1.59E+00		-1.44E+01		-1.44E-05

		1.21E+00		-3.25E+01		-3.25E-05		1.59E+00		-1.45E+01		-1.45E-05

		1.22E+00		-3.24E+01		-3.24E-05		1.59E+00		-1.44E+01		-1.44E-05

		1.22E+00		-3.20E+01		-3.20E-05		1.60E+00		-1.44E+01		-1.44E-05

		1.23E+00		-3.22E+01		-3.22E-05		1.60E+00		-1.44E+01		-1.44E-05

		1.23E+00		-3.20E+01		-3.20E-05		1.61E+00		-1.43E+01		-1.43E-05

		1.23E+00		-3.18E+01		-3.18E-05		1.61E+00		-1.44E+01		-1.44E-05

		1.24E+00		-3.18E+01		-3.18E-05		1.61E+00		-1.43E+01		-1.43E-05

		1.24E+00		-3.14E+01		-3.14E-05		1.62E+00		-1.44E+01		-1.44E-05

		1.25E+00		-3.15E+01		-3.15E-05		1.62E+00		-1.43E+01		-1.43E-05

		1.25E+00		-3.13E+01		-3.13E-05		1.63E+00		-1.43E+01		-1.43E-05

		1.25E+00		-3.11E+01		-3.11E-05		1.63E+00		-1.44E+01		-1.44E-05

		1.26E+00		-3.09E+01		-3.09E-05		1.63E+00		-1.43E+01		-1.43E-05

		1.26E+00		-3.10E+01		-3.10E-05		1.64E+00		-1.43E+01		-1.43E-05

		1.27E+00		-3.04E+01		-3.04E-05		1.64E+00		-1.44E+01		-1.44E-05

		1.27E+00		-3.04E+01		-3.04E-05		1.65E+00		-1.43E+01		-1.43E-05

		1.27E+00		-3.05E+01		-3.05E-05		1.65E+00		-1.45E+01		-1.45E-05

		1.28E+00		-3.00E+01		-3.00E-05		1.65E+00		-1.44E+01		-1.44E-05

		1.28E+00		-2.99E+01		-2.99E-05		1.66E+00		-1.45E+01		-1.45E-05

		1.29E+00		-2.97E+01		-2.97E-05		1.66E+00		-1.44E+01		-1.44E-05

		1.29E+00		-2.96E+01		-2.96E-05		1.67E+00		-1.45E+01		-1.45E-05

		1.29E+00		-2.91E+01		-2.91E-05		1.67E+00		-1.45E+01		-1.45E-05

		1.30E+00		-2.90E+01		-2.90E-05		1.67E+00		-1.46E+01		-1.46E-05

		1.30E+00		-2.87E+01		-2.87E-05		1.68E+00		-1.46E+01		-1.46E-05

		1.31E+00		-2.86E+01		-2.86E-05		1.68E+00		-1.47E+01		-1.47E-05

		1.31E+00		-2.84E+01		-2.84E-05		1.69E+00		-1.47E+01		-1.47E-05

		1.31E+00		-2.80E+01		-2.80E-05		1.69E+00		-1.48E+01		-1.48E-05

		1.32E+00		-2.78E+01		-2.78E-05		1.69E+00		-1.48E+01		-1.48E-05

		1.32E+00		-2.78E+01		-2.78E-05		1.70E+00		-1.49E+01		-1.49E-05

		1.33E+00		-2.75E+01		-2.75E-05		1.70E+00		-1.49E+01		-1.49E-05

		1.33E+00		-2.71E+01		-2.71E-05		1.71E+00		-1.51E+01		-1.51E-05

		1.33E+00		-2.70E+01		-2.70E-05		1.71E+00		-1.51E+01		-1.51E-05

		1.34E+00		-2.66E+01		-2.66E-05		1.71E+00		-1.53E+01		-1.53E-05

		1.34E+00		-2.65E+01		-2.65E-05		1.72E+00		-1.53E+01		-1.53E-05

		1.35E+00		-2.63E+01		-2.63E-05		1.72E+00		-1.55E+01		-1.55E-05

		1.35E+00		-2.63E+01		-2.63E-05		1.73E+00		-1.55E+01		-1.55E-05

		1.35E+00		-2.60E+01		-2.60E-05		1.73E+00		-1.57E+01		-1.57E-05

		1.36E+00		-2.55E+01		-2.55E-05		1.73E+00		-1.58E+01		-1.58E-05

		1.36E+00		-2.57E+01		-2.57E-05		1.74E+00		-1.59E+01		-1.59E-05

		1.37E+00		-2.51E+01		-2.51E-05		1.74E+00		-1.61E+01		-1.61E-05

		1.37E+00		-2.51E+01		-2.51E-05		1.75E+00		-1.63E+01		-1.63E-05

		1.37E+00		-2.47E+01		-2.47E-05		1.75E+00		-1.64E+01		-1.64E-05

		1.38E+00		-2.50E+01		-2.50E-05		1.75E+00		-1.65E+01		-1.65E-05

		1.38E+00		-2.44E+01		-2.44E-05		1.76E+00		-1.68E+01		-1.68E-05

		1.39E+00		-2.42E+01		-2.42E-05		1.76E+00		-1.70E+01		-1.70E-05

		1.39E+00		-2.42E+01		-2.42E-05		1.77E+00		-1.72E+01		-1.72E-05

		1.39E+00		-2.38E+01		-2.38E-05		1.77E+00		-1.74E+01		-1.74E-05

		1.40E+00		-2.38E+01		-2.38E-05		1.77E+00		-1.77E+01		-1.77E-05

		1.40E+00		-2.36E+01		-2.36E-05		1.78E+00		-1.79E+01		-1.79E-05

		1.41E+00		-2.37E+01		-2.37E-05		1.78E+00		-1.82E+01		-1.82E-05

		1.41E+00		-2.33E+01		-2.33E-05		1.79E+00		-1.86E+01		-1.86E-05

		1.41E+00		-2.32E+01		-2.32E-05		1.79E+00		-1.89E+01		-1.89E-05

		1.42E+00		-2.31E+01		-2.31E-05		1.79E+00		-1.90E+01		-1.90E-05

		1.42E+00		-2.29E+01		-2.29E-05		1.80E+00		-1.97E+01		-1.97E-05

		1.43E+00		-2.26E+01		-2.26E-05		1.80E+00		-1.98E+01		-1.98E-05

		1.43E+00		-2.25E+01		-2.25E-05		1.81E+00		-2.02E+01		-2.02E-05

		1.43E+00		-2.25E+01		-2.25E-05		1.81E+00		-2.04E+01		-2.04E-05

		1.44E+00		-2.24E+01		-2.24E-05		1.81E+00		-2.09E+01		-2.09E-05

		1.44E+00		-2.20E+01		-2.20E-05		1.82E+00		-2.14E+01		-2.14E-05

		1.45E+00		-2.19E+01		-2.19E-05		1.82E+00		-2.18E+01		-2.18E-05

		1.45E+00		-2.21E+01		-2.21E-05		1.83E+00		-2.23E+01		-2.23E-05

		1.45E+00		-2.17E+01		-2.17E-05		1.83E+00		-2.27E+01		-2.27E-05

		1.46E+00		-2.17E+01		-2.17E-05		1.83E+00		-2.33E+01		-2.33E-05

		1.46E+00		-2.14E+01		-2.14E-05		1.84E+00		-2.37E+01		-2.37E-05

		1.47E+00		-2.13E+01		-2.13E-05		1.84E+00		-2.42E+01		-2.42E-05

		1.47E+00		-2.12E+01		-2.12E-05		1.85E+00		-2.47E+01		-2.47E-05

		1.47E+00		-2.09E+01		-2.09E-05		1.85E+00		-2.51E+01		-2.51E-05

		1.48E+00		-2.09E+01		-2.09E-05		1.85E+00		-2.58E+01		-2.58E-05

		1.48E+00		-2.07E+01		-2.07E-05		1.86E+00		-2.61E+01		-2.61E-05

		1.49E+00		-2.08E+01		-2.08E-05		1.86E+00		-2.68E+01		-2.68E-05

		1.49E+00		-2.04E+01		-2.04E-05		1.87E+00		-2.71E+01		-2.71E-05

		1.49E+00		-2.06E+01		-2.06E-05		1.87E+00		-2.78E+01		-2.78E-05

		1.50E+00		-2.02E+01		-2.02E-05		1.87E+00		-2.83E+01		-2.83E-05

		1.50E+00		-2.01E+01		-2.01E-05		1.88E+00		-2.88E+01		-2.88E-05

		1.51E+00		-2.01E+01		-2.01E-05		1.88E+00		-2.93E+01		-2.93E-05

		1.51E+00		-1.99E+01		-1.99E-05		1.89E+00		-3.00E+01		-3.00E-05

		1.51E+00		-2.01E+01		-2.01E-05		1.89E+00		-3.03E+01		-3.03E-05

		1.52E+00		-1.98E+01		-1.98E-05		1.89E+00		-3.07E+01		-3.07E-05

		1.52E+00		-1.96E+01		-1.96E-05		1.90E+00		-3.13E+01		-3.13E-05

		1.53E+00		-1.96E+01		-1.96E-05		1.90E+00		-3.18E+01		-3.18E-05

		1.53E+00		-1.95E+01		-1.95E-05		1.91E+00		-3.24E+01		-3.24E-05

		1.53E+00		-1.95E+01		-1.95E-05		1.91E+00		-3.28E+01		-3.28E-05

		1.54E+00		-1.91E+01		-1.91E-05		1.91E+00		-3.33E+01		-3.33E-05

		1.54E+00		-1.93E+01		-1.93E-05		1.92E+00		-3.38E+01		-3.38E-05

		1.55E+00		-1.90E+01		-1.90E-05		1.92E+00		-3.42E+01		-3.42E-05

		1.55E+00		-1.90E+01		-1.90E-05		1.93E+00		-3.47E+01		-3.47E-05

		1.55E+00		-1.93E+01		-1.93E-05		1.93E+00		-3.52E+01		-3.52E-05

		1.56E+00		-1.88E+01		-1.88E-05		1.93E+00		-3.57E+01		-3.57E-05

		1.56E+00		-1.88E+01		-1.88E-05		1.94E+00		-3.61E+01		-3.61E-05

		1.57E+00		-1.88E+01		-1.88E-05		1.94E+00		-3.66E+01		-3.66E-05

		1.57E+00		-1.86E+01		-1.86E-05		1.95E+00		-3.71E+01		-3.71E-05

		1.57E+00		-1.88E+01		-1.88E-05		1.95E+00		-3.75E+01		-3.75E-05

		1.58E+00		-1.86E+01		-1.86E-05		1.95E+00		-3.79E+01		-3.79E-05

		1.58E+00		-1.88E+01		-1.88E-05		1.96E+00		-3.84E+01		-3.84E-05

		1.59E+00		-1.84E+01		-1.84E-05		1.96E+00		-3.89E+01		-3.89E-05

		1.59E+00		-1.85E+01		-1.85E-05		1.97E+00		-3.94E+01		-3.94E-05

		1.59E+00		-1.83E+01		-1.83E-05		1.97E+00		-3.97E+01		-3.97E-05

		1.60E+00		-1.82E+01		-1.82E-05		1.97E+00		-4.01E+01		-4.01E-05

		1.60E+00		-1.83E+01		-1.83E-05		1.98E+00		-4.05E+01		-4.05E-05

		1.61E+00		-1.82E+01		-1.82E-05		1.98E+00		-4.11E+01		-4.11E-05

		1.61E+00		-1.84E+01		-1.84E-05		1.99E+00		-4.14E+01		-4.14E-05

		1.61E+00		-1.81E+01		-1.81E-05		1.99E+00		-4.18E+01		-4.18E-05

		1.62E+00		-1.79E+01		-1.79E-05		1.99E+00		-4.23E+01		-4.23E-05

		1.62E+00		-1.81E+01		-1.81E-05		2.00E+00		-4.28E+01		-4.28E-05

		1.63E+00		-1.78E+01		-1.78E-05		2.00E+00		-4.32E+01		-4.32E-05

		1.63E+00		-1.81E+01		-1.81E-05		2.00E+00		-4.12E+01		-4.12E-05

		1.63E+00		-1.79E+01		-1.79E-05		1.99E+00		-3.95E+01		-3.95E-05

		1.64E+00		-1.80E+01		-1.80E-05		1.99E+00		-3.79E+01		-3.79E-05

		1.64E+00		-1.77E+01		-1.77E-05		1.99E+00		-3.66E+01		-3.66E-05

		1.65E+00		-1.80E+01		-1.80E-05		1.98E+00		-3.54E+01		-3.54E-05

		1.65E+00		-1.78E+01		-1.78E-05		1.98E+00		-3.42E+01		-3.42E-05

		1.65E+00		-1.79E+01		-1.79E-05		1.97E+00		-3.31E+01		-3.31E-05

		1.66E+00		-1.78E+01		-1.78E-05		1.97E+00		-3.20E+01		-3.20E-05

		1.66E+00		-1.78E+01		-1.78E-05		1.97E+00		-3.13E+01		-3.13E-05

		1.67E+00		-1.79E+01		-1.79E-05		1.96E+00		-3.01E+01		-3.01E-05

		1.67E+00		-1.75E+01		-1.75E-05		1.96E+00		-2.94E+01		-2.94E-05

		1.67E+00		-1.78E+01		-1.78E-05		1.95E+00		-2.83E+01		-2.83E-05

		1.68E+00		-1.78E+01		-1.78E-05		1.95E+00		-2.78E+01		-2.78E-05

		1.68E+00		-1.78E+01		-1.78E-05		1.95E+00		-2.68E+01		-2.68E-05

		1.69E+00		-1.76E+01		-1.76E-05		1.94E+00		-2.62E+01		-2.62E-05

		1.69E+00		-1.79E+01		-1.79E-05		1.94E+00		-2.54E+01		-2.54E-05

		1.69E+00		-1.76E+01		-1.76E-05		1.93E+00		-2.47E+01		-2.47E-05

		1.70E+00		-1.77E+01		-1.77E-05		1.93E+00		-2.40E+01		-2.40E-05

		1.70E+00		-1.76E+01		-1.76E-05		1.93E+00		-2.34E+01		-2.34E-05

		1.71E+00		-1.78E+01		-1.78E-05		1.92E+00		-2.29E+01		-2.29E-05

		1.71E+00		-1.77E+01		-1.77E-05		1.92E+00		-2.21E+01		-2.21E-05

		1.71E+00		-1.76E+01		-1.76E-05		1.91E+00		-2.15E+01		-2.15E-05

		1.72E+00		-1.79E+01		-1.79E-05		1.91E+00		-2.09E+01		-2.09E-05

		1.72E+00		-1.76E+01		-1.76E-05		1.91E+00		-2.05E+01		-2.05E-05

		1.73E+00		-1.79E+01		-1.79E-05		1.90E+00		-1.99E+01		-1.99E-05

		1.73E+00		-1.74E+01		-1.74E-05		1.90E+00		-1.96E+01		-1.96E-05

		1.73E+00		-1.79E+01		-1.79E-05		1.89E+00		-1.90E+01		-1.90E-05

		1.74E+00		-1.80E+01		-1.80E-05		1.89E+00		-1.84E+01		-1.84E-05

		1.74E+00		-1.79E+01		-1.79E-05		1.89E+00		-1.80E+01		-1.80E-05

		1.75E+00		-1.81E+01		-1.81E-05		1.88E+00		-1.76E+01		-1.76E-05

		1.75E+00		-1.80E+01		-1.80E-05		1.88E+00		-1.72E+01		-1.72E-05

		1.75E+00		-1.82E+01		-1.82E-05		1.87E+00		-1.66E+01		-1.66E-05

		1.76E+00		-1.81E+01		-1.81E-05		1.87E+00		-1.63E+01		-1.63E-05

		1.76E+00		-1.83E+01		-1.83E-05		1.87E+00		-1.60E+01		-1.60E-05

		1.77E+00		-1.82E+01		-1.82E-05		1.86E+00		-1.55E+01		-1.55E-05

		1.77E+00		-1.85E+01		-1.85E-05		1.86E+00		-1.51E+01		-1.51E-05

		1.77E+00		-1.85E+01		-1.85E-05		1.85E+00		-1.48E+01		-1.48E-05

		1.78E+00		-1.86E+01		-1.86E-05		1.85E+00		-1.44E+01		-1.44E-05

		1.78E+00		-1.86E+01		-1.86E-05		1.85E+00		-1.41E+01		-1.41E-05

		1.79E+00		-1.89E+01		-1.89E-05		1.84E+00		-1.38E+01		-1.38E-05

		1.79E+00		-1.89E+01		-1.89E-05		1.84E+00		-1.34E+01		-1.34E-05

		1.79E+00		-1.89E+01		-1.89E-05		1.83E+00		-1.29E+01		-1.29E-05

		1.80E+00		-1.92E+01		-1.92E-05		1.83E+00		-1.27E+01		-1.27E-05

		1.80E+00		-1.91E+01		-1.91E-05		1.83E+00		-1.24E+01		-1.24E-05

		1.81E+00		-1.95E+01		-1.95E-05		1.82E+00		-1.21E+01		-1.21E-05

		1.81E+00		-1.93E+01		-1.93E-05		1.82E+00		-1.17E+01		-1.17E-05

		1.81E+00		-2.00E+01		-2.00E-05		1.81E+00		-1.14E+01		-1.14E-05

		1.82E+00		-1.97E+01		-1.97E-05		1.81E+00		-1.11E+01		-1.11E-05

		1.82E+00		-2.00E+01		-2.00E-05		1.81E+00		-1.09E+01		-1.09E-05

		1.83E+00		-2.01E+01		-2.01E-05		1.80E+00		-1.06E+01		-1.06E-05

		1.83E+00		-2.01E+01		-2.01E-05		1.80E+00		-1.03E+01		-1.03E-05

		1.83E+00		-2.06E+01		-2.06E-05		1.79E+00		-1.00E+01		-1.00E-05

		1.84E+00		-2.06E+01		-2.06E-05		1.79E+00		-9.79E+00		-9.79E-06

		1.84E+00		-2.11E+01		-2.11E-05		1.79E+00		-9.62E+00		-9.62E-06

		1.85E+00		-2.10E+01		-2.10E-05		1.78E+00		-9.38E+00		-9.38E-06

		1.85E+00		-2.12E+01		-2.12E-05		1.78E+00		-9.16E+00		-9.16E-06

		1.85E+00		-2.15E+01		-2.15E-05		1.77E+00		-8.92E+00		-8.92E-06

		1.86E+00		-2.16E+01		-2.16E-05		1.77E+00		-8.77E+00		-8.77E-06

		1.86E+00		-2.21E+01		-2.21E-05		1.77E+00		-8.60E+00		-8.60E-06

		1.87E+00		-2.23E+01		-2.23E-05		1.76E+00		-8.40E+00		-8.40E-06

		1.87E+00		-2.26E+01		-2.26E-05		1.76E+00		-8.26E+00		-8.26E-06

		1.87E+00		-2.27E+01		-2.27E-05		1.75E+00		-8.07E+00		-8.07E-06

		1.88E+00		-2.30E+01		-2.30E-05		1.75E+00		-7.93E+00		-7.93E-06

		1.88E+00		-2.33E+01		-2.33E-05		1.75E+00		-7.83E+00		-7.83E-06

		1.89E+00		-2.38E+01		-2.38E-05		1.74E+00		-7.70E+00		-7.70E-06

		1.89E+00		-2.38E+01		-2.38E-05		1.74E+00		-7.54E+00		-7.54E-06

		1.89E+00		-2.44E+01		-2.44E-05		1.73E+00		-7.42E+00		-7.42E-06

		1.90E+00		-2.47E+01		-2.47E-05		1.73E+00		-7.31E+00		-7.31E-06

		1.90E+00		-2.50E+01		-2.50E-05		1.73E+00		-7.23E+00		-7.23E-06

		1.91E+00		-2.53E+01		-2.53E-05		1.72E+00		-7.15E+00		-7.15E-06

		1.91E+00		-2.58E+01		-2.58E-05		1.72E+00		-7.01E+00		-7.01E-06

		1.91E+00		-2.63E+01		-2.63E-05		1.71E+00		-6.94E+00		-6.94E-06

		1.92E+00		-2.65E+01		-2.65E-05		1.71E+00		-6.81E+00		-6.81E-06

		1.92E+00		-2.72E+01		-2.72E-05		1.71E+00		-6.79E+00		-6.79E-06

		1.93E+00		-2.75E+01		-2.75E-05		1.70E+00		-6.66E+00		-6.66E-06

		1.93E+00		-2.82E+01		-2.82E-05		1.70E+00		-6.59E+00		-6.59E-06

		1.93E+00		-2.83E+01		-2.83E-05		1.69E+00		-6.49E+00		-6.49E-06

		1.94E+00		-2.90E+01		-2.90E-05		1.69E+00		-6.44E+00		-6.44E-06

		1.94E+00		-2.95E+01		-2.95E-05		1.69E+00		-6.34E+00		-6.34E-06

		1.95E+00		-3.02E+01		-3.02E-05		1.68E+00		-6.32E+00		-6.32E-06

		1.95E+00		-3.08E+01		-3.08E-05		1.68E+00		-6.19E+00		-6.19E-06

		1.95E+00		-3.12E+01		-3.12E-05		1.67E+00		-6.19E+00		-6.19E-06

		1.96E+00		-3.18E+01		-3.18E-05		1.67E+00		-6.04E+00		-6.04E-06

		1.96E+00		-3.21E+01		-3.21E-05		1.67E+00		-6.03E+00		-6.03E-06

		1.97E+00		-3.32E+01		-3.32E-05		1.66E+00		-5.96E+00		-5.96E-06

		1.97E+00		-3.35E+01		-3.35E-05		1.66E+00		-5.92E+00		-5.92E-06

		1.97E+00		-3.43E+01		-3.43E-05		1.65E+00		-5.85E+00		-5.85E-06

		1.98E+00		-3.49E+01		-3.49E-05		1.65E+00		-5.78E+00		-5.78E-06

		1.98E+00		-3.53E+01		-3.53E-05		1.65E+00		-5.75E+00		-5.75E-06

		1.99E+00		-3.61E+01		-3.61E-05		1.64E+00		-5.71E+00		-5.71E-06

		1.99E+00		-3.67E+01		-3.67E-05		1.64E+00		-5.60E+00		-5.60E-06

		1.99E+00		-3.73E+01		-3.73E-05		1.63E+00		-5.58E+00		-5.58E-06

		2.00E+00		-3.81E+01		-3.81E-05		1.63E+00		-5.53E+00		-5.53E-06

		2.00E+00		-3.89E+01		-3.89E-05		1.63E+00		-5.52E+00		-5.52E-06

		2.00E+00		-3.70E+01		-3.70E-05		1.62E+00		-5.43E+00		-5.43E-06

		1.99E+00		-3.55E+01		-3.55E-05		1.62E+00		-5.42E+00		-5.42E-06

		1.99E+00		-3.41E+01		-3.41E-05		1.61E+00		-5.37E+00		-5.37E-06

		1.99E+00		-3.29E+01		-3.29E-05		1.61E+00		-5.30E+00		-5.30E-06

		1.98E+00		-3.15E+01		-3.15E-05		1.61E+00		-5.31E+00		-5.31E-06

		1.98E+00		-3.04E+01		-3.04E-05		1.60E+00		-5.25E+00		-5.25E-06

		1.97E+00		-2.94E+01		-2.94E-05		1.60E+00		-5.25E+00		-5.25E-06

		1.97E+00		-2.83E+01		-2.83E-05		1.59E+00		-5.18E+00		-5.18E-06

		1.97E+00		-2.73E+01		-2.73E-05		1.59E+00		-5.14E+00		-5.14E-06

		1.96E+00		-2.65E+01		-2.65E-05		1.59E+00		-5.18E+00		-5.18E-06

		1.96E+00		-2.62E+01		-2.62E-05		1.58E+00		-5.12E+00		-5.12E-06

		1.95E+00		-2.46E+01		-2.46E-05		1.58E+00		-5.11E+00		-5.11E-06

		1.95E+00		-2.41E+01		-2.41E-05		1.57E+00		-5.09E+00		-5.09E-06

		1.95E+00		-2.32E+01		-2.32E-05		1.57E+00		-5.07E+00		-5.07E-06

		1.94E+00		-2.26E+01		-2.26E-05		1.57E+00		-5.07E+00		-5.07E-06

		1.94E+00		-2.20E+01		-2.20E-05		1.56E+00		-5.09E+00		-5.09E-06

		1.93E+00		-2.11E+01		-2.11E-05		1.56E+00		-5.02E+00		-5.02E-06

		1.93E+00		-2.10E+01		-2.10E-05		1.55E+00		-5.02E+00		-5.02E-06

		1.93E+00		-2.00E+01		-2.00E-05		1.55E+00		-4.96E+00		-4.96E-06

		1.92E+00		-1.96E+01		-1.96E-05		1.55E+00		-5.01E+00		-5.01E-06

		1.92E+00		-1.88E+01		-1.88E-05		1.54E+00		-4.93E+00		-4.93E-06

		1.91E+00		-1.84E+01		-1.84E-05		1.54E+00		-4.94E+00		-4.94E-06

		1.91E+00		-1.77E+01		-1.77E-05		1.53E+00		-4.93E+00		-4.93E-06

		1.91E+00		-1.73E+01		-1.73E-05		1.53E+00		-4.90E+00		-4.90E-06

		1.90E+00		-1.70E+01		-1.70E-05		1.53E+00		-4.91E+00		-4.91E-06

		1.90E+00		-1.63E+01		-1.63E-05		1.52E+00		-4.87E+00		-4.87E-06

		1.89E+00		-1.60E+01		-1.60E-05		1.52E+00		-4.85E+00		-4.85E-06

		1.89E+00		-1.56E+01		-1.56E-05		1.51E+00		-4.85E+00		-4.85E-06

		1.89E+00		-1.53E+01		-1.53E-05		1.51E+00		-4.82E+00		-4.82E-06

		1.88E+00		-1.48E+01		-1.48E-05		1.51E+00		-4.82E+00		-4.82E-06

		1.88E+00		-1.44E+01		-1.44E-05		1.50E+00		-4.85E+00		-4.85E-06

		1.87E+00		-1.41E+01		-1.41E-05		1.50E+00		-4.76E+00		-4.76E-06

		1.87E+00		-1.37E+01		-1.37E-05		1.49E+00		-4.80E+00		-4.80E-06

		1.87E+00		-1.34E+01		-1.34E-05		1.49E+00		-4.73E+00		-4.73E-06

		1.86E+00		-1.30E+01		-1.30E-05		1.49E+00		-4.76E+00		-4.76E-06

		1.86E+00		-1.27E+01		-1.27E-05		1.48E+00		-4.73E+00		-4.73E-06

		1.85E+00		-1.24E+01		-1.24E-05		1.48E+00		-4.71E+00		-4.71E-06

		1.85E+00		-1.20E+01		-1.20E-05		1.47E+00		-4.71E+00		-4.71E-06

		1.85E+00		-1.19E+01		-1.19E-05		1.47E+00		-4.63E+00		-4.63E-06

		1.84E+00		-1.15E+01		-1.15E-05		1.47E+00		-4.65E+00		-4.65E-06

		1.84E+00		-1.13E+01		-1.13E-05		1.46E+00		-4.60E+00		-4.60E-06

		1.83E+00		-1.10E+01		-1.10E-05		1.46E+00		-4.56E+00		-4.56E-06

		1.83E+00		-1.07E+01		-1.07E-05		1.45E+00		-4.59E+00		-4.59E-06

		1.83E+00		-1.05E+01		-1.05E-05		1.45E+00		-4.50E+00		-4.50E-06

		1.82E+00		-1.03E+01		-1.03E-05		1.45E+00		-4.58E+00		-4.58E-06

		1.82E+00		-1.01E+01		-1.01E-05		1.44E+00		-4.46E+00		-4.46E-06

		1.81E+00		-9.82E+00		-9.82E-06		1.44E+00		-4.48E+00		-4.48E-06

		1.81E+00		-9.54E+00		-9.54E-06		1.43E+00		-4.46E+00		-4.46E-06

		1.81E+00		-9.36E+00		-9.36E-06		1.43E+00		-4.39E+00		-4.39E-06

		1.80E+00		-9.23E+00		-9.23E-06		1.43E+00		-4.37E+00		-4.37E-06

		1.80E+00		-9.02E+00		-9.02E-06		1.42E+00		-4.34E+00		-4.34E-06

		1.79E+00		-8.83E+00		-8.83E-06		1.42E+00		-4.24E+00		-4.24E-06

		1.79E+00		-8.68E+00		-8.68E-06		1.41E+00		-4.30E+00		-4.30E-06

		1.79E+00		-8.45E+00		-8.45E-06		1.41E+00		-4.13E+00		-4.13E-06

		1.78E+00		-8.29E+00		-8.29E-06		1.41E+00		-4.16E+00		-4.16E-06

		1.78E+00		-8.19E+00		-8.19E-06		1.40E+00		-4.02E+00		-4.02E-06

		1.77E+00		-8.05E+00		-8.05E-06		1.40E+00		-4.00E+00		-4.00E-06

		1.77E+00		-7.84E+00		-7.84E-06		1.39E+00		-3.93E+00		-3.93E-06

		1.77E+00		-7.74E+00		-7.74E-06		1.39E+00		-3.86E+00		-3.86E-06

		1.76E+00		-7.74E+00		-7.74E-06		1.39E+00		-3.78E+00		-3.78E-06

		1.76E+00		-7.55E+00		-7.55E-06		1.38E+00		-3.71E+00		-3.71E-06

		1.75E+00		-7.38E+00		-7.38E-06		1.38E+00		-3.59E+00		-3.59E-06

		1.75E+00		-7.26E+00		-7.26E-06		1.37E+00		-3.57E+00		-3.57E-06

		1.75E+00		-7.12E+00		-7.12E-06		1.37E+00		-3.37E+00		-3.37E-06

		1.74E+00		-7.09E+00		-7.09E-06		1.37E+00		-3.38E+00		-3.38E-06

		1.74E+00		-6.98E+00		-6.98E-06		1.36E+00		-3.15E+00		-3.15E-06

		1.73E+00		-6.95E+00		-6.95E-06		1.36E+00		-3.09E+00		-3.09E-06

		1.73E+00		-6.78E+00		-6.78E-06		1.35E+00		-2.97E+00		-2.97E-06

		1.73E+00		-6.71E+00		-6.71E-06		1.35E+00		-2.81E+00		-2.81E-06

		1.72E+00		-6.63E+00		-6.63E-06		1.35E+00		-2.68E+00		-2.68E-06

		1.72E+00		-6.58E+00		-6.58E-06		1.34E+00		-2.54E+00		-2.54E-06

		1.71E+00		-6.44E+00		-6.44E-06		1.34E+00		-2.35E+00		-2.35E-06

		1.71E+00		-6.38E+00		-6.38E-06		1.33E+00		-2.28E+00		-2.28E-06

		1.71E+00		-6.35E+00		-6.35E-06		1.33E+00		-1.97E+00		-1.97E-06

		1.70E+00		-6.31E+00		-6.31E-06		1.33E+00		-1.90E+00		-1.90E-06

		1.70E+00		-6.24E+00		-6.24E-06		1.32E+00		-1.71E+00		-1.71E-06

		1.69E+00		-6.13E+00		-6.13E-06		1.32E+00		-1.46E+00		-1.46E-06

		1.69E+00		-6.09E+00		-6.09E-06		1.31E+00		-1.26E+00		-1.26E-06

		1.69E+00		-5.97E+00		-5.97E-06		1.31E+00		-1.10E+00		-1.10E-06

		1.68E+00		-6.00E+00		-6.00E-06		1.31E+00		-8.98E-01		-8.98E-07

		1.68E+00		-5.93E+00		-5.93E-06		1.30E+00		-7.20E-01		-7.20E-07

		1.67E+00		-5.81E+00		-5.81E-06		1.30E+00		-5.77E-01		-5.77E-07

		1.67E+00		-5.85E+00		-5.85E-06		1.29E+00		-3.35E-01		-3.35E-07

		1.67E+00		-5.69E+00		-5.69E-06		1.29E+00		-1.81E-01		-1.81E-07

		1.66E+00		-5.72E+00		-5.72E-06		1.29E+00		-3.10E-02		-3.10E-08

		1.66E+00		-5.61E+00		-5.61E-06		1.28E+00		1.27E-01		1.27E-07

		1.65E+00		-5.53E+00		-5.53E-06		1.28E+00		2.80E-01		2.80E-07

		1.65E+00		-5.56E+00		-5.56E-06		1.27E+00		4.65E-01		4.65E-07

		1.65E+00		-5.46E+00		-5.46E-06		1.27E+00		5.60E-01		5.60E-07

		1.64E+00		-5.50E+00		-5.50E-06		1.27E+00		6.90E-01		6.90E-07

		1.64E+00		-5.37E+00		-5.37E-06		1.26E+00		8.30E-01		8.30E-07

		1.63E+00		-5.37E+00		-5.37E-06		1.26E+00		9.20E-01		9.20E-07

		1.63E+00		-5.28E+00		-5.28E-06		1.25E+00		1.04E+00		1.04E-06

		1.63E+00		-5.22E+00		-5.22E-06		1.25E+00		1.23E+00		1.23E-06

		1.62E+00		-5.28E+00		-5.28E-06		1.25E+00		1.29E+00		1.29E-06

		1.62E+00		-5.18E+00		-5.18E-06		1.24E+00		1.43E+00		1.43E-06

		1.61E+00		-5.17E+00		-5.17E-06		1.24E+00		1.51E+00		1.51E-06

		1.61E+00		-5.12E+00		-5.12E-06		1.23E+00		1.65E+00		1.65E-06

		1.61E+00		-5.05E+00		-5.05E-06		1.23E+00		1.69E+00		1.69E-06

		1.60E+00		-5.04E+00		-5.04E-06		1.23E+00		1.78E+00		1.78E-06

		1.60E+00		-4.94E+00		-4.94E-06		1.22E+00		1.93E+00		1.93E-06

		1.59E+00		-4.95E+00		-4.95E-06		1.22E+00		1.97E+00		1.97E-06

		1.59E+00		-4.96E+00		-4.96E-06		1.21E+00		2.06E+00		2.06E-06

		1.59E+00		-4.93E+00		-4.93E-06		1.21E+00		2.17E+00		2.17E-06

		1.58E+00		-4.90E+00		-4.90E-06		1.21E+00		2.23E+00		2.23E-06

		1.58E+00		-4.86E+00		-4.86E-06		1.20E+00		2.31E+00		2.31E-06

		1.57E+00		-4.76E+00		-4.76E-06		1.20E+00		2.37E+00		2.37E-06

		1.57E+00		-4.77E+00		-4.77E-06		1.19E+00		2.50E+00		2.50E-06

		1.57E+00		-4.72E+00		-4.72E-06		1.19E+00		2.58E+00		2.58E-06

		1.56E+00		-4.70E+00		-4.70E-06		1.19E+00		2.61E+00		2.61E-06

		1.56E+00		-4.72E+00		-4.72E-06		1.18E+00		2.73E+00		2.73E-06

		1.55E+00		-4.60E+00		-4.60E-06		1.18E+00		2.84E+00		2.84E-06

		1.55E+00		-4.58E+00		-4.58E-06		1.17E+00		2.90E+00		2.90E-06

		1.55E+00		-4.53E+00		-4.53E-06		1.17E+00		2.98E+00		2.98E-06

		1.54E+00		-4.54E+00		-4.54E-06		1.17E+00		3.09E+00		3.09E-06

		1.54E+00		-4.50E+00		-4.50E-06		1.16E+00		3.16E+00		3.16E-06

		1.53E+00		-4.44E+00		-4.44E-06		1.16E+00		3.26E+00		3.26E-06

		1.53E+00		-4.53E+00		-4.53E-06		1.15E+00		3.37E+00		3.37E-06

		1.53E+00		-4.38E+00		-4.38E-06		1.15E+00		3.46E+00		3.46E-06

		1.52E+00		-4.39E+00		-4.39E-06		1.15E+00		3.53E+00		3.53E-06

		1.52E+00		-4.35E+00		-4.35E-06		1.14E+00		3.64E+00		3.64E-06

		1.51E+00		-4.33E+00		-4.33E-06		1.14E+00		3.73E+00		3.73E-06

		1.51E+00		-4.33E+00		-4.33E-06		1.13E+00		3.87E+00		3.87E-06

		1.51E+00		-4.27E+00		-4.27E-06		1.13E+00		3.86E+00		3.86E-06

		1.50E+00		-4.36E+00		-4.36E-06		1.13E+00		4.02E+00		4.02E-06

		1.50E+00		-4.23E+00		-4.23E-06		1.12E+00		4.06E+00		4.06E-06

		1.49E+00		-4.22E+00		-4.22E-06		1.12E+00		4.18E+00		4.18E-06

		1.49E+00		-4.18E+00		-4.18E-06		1.11E+00		4.26E+00		4.26E-06

		1.49E+00		-4.13E+00		-4.13E-06		1.11E+00		4.30E+00		4.30E-06

		1.48E+00		-4.17E+00		-4.17E-06		1.11E+00		4.38E+00		4.38E-06

		1.48E+00		-4.12E+00		-4.12E-06		1.10E+00		4.43E+00		4.43E-06

		1.47E+00		-4.09E+00		-4.09E-06		1.10E+00		4.52E+00		4.52E-06

		1.47E+00		-4.10E+00		-4.10E-06		1.09E+00		4.65E+00		4.65E-06

		1.47E+00		-3.97E+00		-3.97E-06		1.09E+00		4.58E+00		4.58E-06

		1.46E+00		-4.01E+00		-4.01E-06		1.09E+00		4.72E+00		4.72E-06

		1.46E+00		-3.97E+00		-3.97E-06		1.08E+00		4.72E+00		4.72E-06

		1.45E+00		-3.91E+00		-3.91E-06		1.08E+00		4.75E+00		4.75E-06

		1.45E+00		-3.93E+00		-3.93E-06		1.07E+00		4.81E+00		4.81E-06

		1.45E+00		-3.86E+00		-3.86E-06		1.07E+00		4.81E+00		4.81E-06

		1.44E+00		-3.87E+00		-3.87E-06		1.07E+00		4.82E+00		4.82E-06

		1.44E+00		-3.83E+00		-3.83E-06		1.06E+00		4.83E+00		4.83E-06

		1.43E+00		-3.74E+00		-3.74E-06		1.06E+00		4.78E+00		4.78E-06

		1.43E+00		-3.78E+00		-3.78E-06		1.05E+00		4.84E+00		4.84E-06

		1.43E+00		-3.60E+00		-3.60E-06		1.05E+00		4.64E+00		4.64E-06

		1.42E+00		-3.71E+00		-3.71E-06		1.05E+00		4.69E+00		4.69E-06

		1.42E+00		-3.65E+00		-3.65E-06		1.04E+00		4.59E+00		4.59E-06

		1.41E+00		-3.58E+00		-3.58E-06		1.04E+00		4.61E+00		4.61E-06

		1.41E+00		-3.64E+00		-3.64E-06		1.03E+00		4.44E+00		4.44E-06

		1.41E+00		-3.47E+00		-3.47E-06		1.03E+00		4.36E+00		4.36E-06

		1.40E+00		-3.50E+00		-3.50E-06		1.03E+00		4.27E+00		4.27E-06

		1.40E+00		-3.43E+00		-3.43E-06		1.02E+00		4.17E+00		4.17E-06

		1.39E+00		-3.38E+00		-3.38E-06		1.02E+00		4.09E+00		4.09E-06

		1.39E+00		-3.43E+00		-3.43E-06		1.01E+00		4.01E+00		4.01E-06

		1.39E+00		-3.26E+00		-3.26E-06		1.01E+00		3.82E+00		3.82E-06

		1.38E+00		-3.38E+00		-3.38E-06		1.01E+00		3.74E+00		3.74E-06

		1.38E+00		-3.24E+00		-3.24E-06		1.00E+00		3.66E+00		3.66E-06

		1.37E+00		-3.17E+00		-3.17E-06		9.97E-01		3.61E+00		3.61E-06

		1.37E+00		-3.17E+00		-3.17E-06		9.93E-01		3.50E+00		3.50E-06

		1.37E+00		-3.03E+00		-3.03E-06		9.89E-01		3.32E+00		3.32E-06

		1.36E+00		-3.10E+00		-3.10E-06		9.85E-01		3.26E+00		3.26E-06

		1.36E+00		-3.00E+00		-3.00E-06		9.81E-01		3.15E+00		3.15E-06

		1.35E+00		-2.98E+00		-2.98E-06		9.77E-01		3.11E+00		3.11E-06

		1.35E+00		-2.93E+00		-2.93E-06		9.73E-01		2.96E+00		2.96E-06

		1.35E+00		-2.82E+00		-2.82E-06		9.69E-01		2.86E+00		2.86E-06

		1.34E+00		-2.83E+00		-2.83E-06		9.65E-01		2.81E+00		2.81E-06

		1.34E+00		-2.71E+00		-2.71E-06		9.61E-01		2.71E+00		2.71E-06

		1.33E+00		-2.67E+00		-2.67E-06		9.57E-01		2.71E+00		2.71E-06

		1.33E+00		-2.62E+00		-2.62E-06		9.53E-01		2.58E+00		2.58E-06

		1.33E+00		-2.54E+00		-2.54E-06		9.49E-01		2.50E+00		2.50E-06

		1.32E+00		-2.50E+00		-2.50E-06		9.45E-01		2.43E+00		2.43E-06

		1.32E+00		-2.43E+00		-2.43E-06		9.41E-01		2.43E+00		2.43E-06

		1.31E+00		-2.32E+00		-2.32E-06		9.37E-01		2.37E+00		2.37E-06

		1.31E+00		-2.28E+00		-2.28E-06		9.33E-01		2.28E+00		2.28E-06

		1.31E+00		-2.21E+00		-2.21E-06		9.29E-01		2.18E+00		2.18E-06

		1.30E+00		-2.17E+00		-2.17E-06		9.25E-01		2.20E+00		2.20E-06

		1.30E+00		-2.06E+00		-2.06E-06		9.21E-01		2.13E+00		2.13E-06

		1.29E+00		-2.01E+00		-2.01E-06		9.17E-01		2.12E+00		2.12E-06

		1.29E+00		-1.90E+00		-1.90E-06		9.13E-01		2.05E+00		2.05E-06

		1.29E+00		-1.78E+00		-1.78E-06		9.09E-01		1.94E+00		1.94E-06

		1.28E+00		-1.78E+00		-1.78E-06		9.05E-01		1.92E+00		1.92E-06

		1.28E+00		-1.69E+00		-1.69E-06		9.01E-01		1.95E+00		1.95E-06

		1.27E+00		-1.60E+00		-1.60E-06		8.97E-01		1.95E+00		1.95E-06

		1.27E+00		-1.49E+00		-1.49E-06		8.93E-01		1.87E+00		1.87E-06

		1.27E+00		-1.38E+00		-1.38E-06		8.89E-01		1.81E+00		1.81E-06

		1.26E+00		-1.37E+00		-1.37E-06		8.85E-01		1.78E+00		1.78E-06

		1.26E+00		-1.28E+00		-1.28E-06		8.81E-01		1.75E+00		1.75E-06

		1.25E+00		-1.18E+00		-1.18E-06		8.77E-01		1.78E+00		1.78E-06

		1.25E+00		-1.16E+00		-1.16E-06		8.73E-01		1.70E+00		1.70E-06

		1.25E+00		-1.05E+00		-1.05E-06		8.69E-01		1.66E+00		1.66E-06

		1.24E+00		-1.04E+00		-1.04E-06		8.65E-01		1.67E+00		1.67E-06

		1.24E+00		-9.74E-01		-9.74E-07		8.61E-01		1.66E+00		1.66E-06

		1.23E+00		-9.05E-01		-9.05E-07		8.57E-01		1.67E+00		1.67E-06

		1.23E+00		-8.73E-01		-8.73E-07		8.53E-01		1.61E+00		1.61E-06

		1.23E+00		-7.89E-01		-7.89E-07		8.49E-01		1.52E+00		1.52E-06

		1.22E+00		-8.19E-01		-8.19E-07		8.45E-01		1.52E+00		1.52E-06

		1.22E+00		-7.34E-01		-7.34E-07		8.41E-01		1.60E+00		1.60E-06

		1.21E+00		-6.91E-01		-6.91E-07		8.37E-01		1.55E+00		1.55E-06

		1.21E+00		-6.69E-01		-6.69E-07		8.33E-01		1.52E+00		1.52E-06

		1.21E+00		-6.02E-01		-6.02E-07		8.29E-01		1.46E+00		1.46E-06

		1.20E+00		-6.35E-01		-6.35E-07		8.25E-01		1.44E+00		1.44E-06

		1.20E+00		-5.61E-01		-5.61E-07		8.21E-01		1.47E+00		1.47E-06

		1.19E+00		-5.49E-01		-5.49E-07		8.17E-01		1.49E+00		1.49E-06

		1.19E+00		-5.19E-01		-5.19E-07		8.13E-01		1.39E+00		1.39E-06

		1.19E+00		-4.77E-01		-4.77E-07		8.09E-01		1.36E+00		1.36E-06

		1.18E+00		-5.25E-01		-5.25E-07		8.05E-01		1.38E+00		1.38E-06

		1.18E+00		-4.62E-01		-4.62E-07		8.01E-01		1.44E+00		1.44E-06

		1.17E+00		-4.43E-01		-4.43E-07		7.97E-01		1.36E+00		1.36E-06

		1.17E+00		-4.38E-01		-4.38E-07		7.93E-01		1.40E+00		1.40E-06

		1.17E+00		-4.23E-01		-4.23E-07		7.89E-01		1.28E+00		1.28E-06

		1.16E+00		-4.61E-01		-4.61E-07		7.85E-01		1.35E+00		1.35E-06

		1.16E+00		-4.13E-01		-4.13E-07		7.81E-01		1.32E+00		1.32E-06

		1.15E+00		-4.05E-01		-4.05E-07		7.77E-01		1.37E+00		1.37E-06

		1.15E+00		-4.18E-01		-4.18E-07		7.73E-01		1.26E+00		1.26E-06

		1.15E+00		-3.79E-01		-3.79E-07		7.69E-01		1.31E+00		1.31E-06

		1.14E+00		-4.37E-01		-4.37E-07		7.65E-01		1.19E+00		1.19E-06

		1.14E+00		-4.24E-01		-4.24E-07		7.61E-01		1.31E+00		1.31E-06

		1.13E+00		-3.72E-01		-3.72E-07		7.57E-01		1.22E+00		1.22E-06

		1.13E+00		-3.90E-01		-3.90E-07		7.53E-01		1.28E+00		1.28E-06
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		624

		626

		628

		630

		632

		634

		636

		638

		640

		642

		644

		646

		648

		650

		652

		654

		656

		658

		660

		662

		664

		666

		668

		670

		672

		674

		676

		678

		680

		682

		684

		686

		688

		690

		692

		694

		696

		698

		700

		702

		704

		706

		708

		710

		712

		714

		716

		718

		720

		722

		724

		726

		728

		730

		732

		734

		736

		738

		740

		742

		744

		746

		748

		750

		752

		754

		756

		758

		760

		762

		764

		766

		768

		770

		772

		774

		776

		778

		780

		782

		784

		786

		788

		790

		792

		794

		796

		798

		800

		802

		804

		806

		808

		810

		812

		814

		816

		818

		820



Wavelength (nm)

Absorbance

1.77449

2.004028

2.175568

2.262924

2.271271

2.317276

2.307861

2.430862

2.561905

2.740372

2.89035

3.019348

3.095169

3.086761

3.131119

3.092743

3.07785

3.207367

3.161087

3.286118

3.422409

3.44545

3.709229

3.593674

3.788284

3.468369

3.452866

3.337921

3.323715

3.337524

3.347733

3.671173

3.740387

3.47583

3.677429

3.543167

3.746216

3.729782

3.901321

3.862167

3.682404

3.991974

3.775162

3.79364

3.781357

3.556351

3.522308

3.531555

3.469284

3.213028

3.229279

3.083817

2.967438

2.820587

2.682159

2.535751

2.376068

2.210602

2.047775

1.887802

1.730927

1.578629

1.434814

1.298233

1.170242

1.051102

0.9423065

0.84198

0.7518768

0.6711426

0.5994415

0.5357819

0.4803162

0.431427

0.3887634

0.3515778

0.319458

0.2911835

0.2664795

0.2452393

0.2262878

0.2099304

0.1961823

0.1848602

0.1752167

0.1674347

0.1610107

0.1564941

0.1539612

0.1499023

0.1486053

0.1481171

0.148407

0.1490784

0.1509552

0.1522675

0.1558533

0.1585846

0.1630096

0.167572

0.1733093

0.181778

0.1893616

0.1996155

0.2137299

0.2272949

0.2475891

0.270462

0.2955933

0.3284454

0.3664398

0.4125214

0.4597015

0.5199432

0.5852814

0.6625671

0.743576

0.8274536

0.9285278

1.028198

1.141708

1.246933

1.367401

1.488266

1.604797

1.727783

1.848099

1.960617

2.06781

2.166916

2.264816

2.352325

2.426666

2.507233

2.584457

2.630478

2.685028

2.747086

2.772766

2.777466

2.739563

2.771469

2.804382

2.800278

2.798782

2.791138

2.761566

2.781281

2.881683

2.714188

2.673645

2.623093

2.572311

2.499954

2.466354

2.394547

2.343201

2.260574

2.185425

2.100266

2.021576

1.937347

1.843781

1.754974

1.668961

1.584717

1.49588

1.410477

1.333786

1.249741

1.170822

1.093933

1.022934

0.9487

0.8805542

0.8123474

0.7489929

0.6878662

0.6283264

0.5745544

0.5198669

0.4705811

0.424408

0.3848572

0.3455353

0.3094482

0.2767029

0.2473297

0.2180481

0.1953278

0.1726532

0.154129

0.1355896

0.1197815

0.1044006

0.09587097

0.07792664

0.07836914

0.06951904

0.06680298

0.06274414

0.06518555

0.05749512

0.05290222

0.05412292

0.05584717

0.05766296

0.05386353

0.05499268

0.0559082

0.06321716

0.0602417

0.06285095

0.06428528

0.06604004

0.067276

0.07499695

0.0721283

0.07868958

0.0818634

0.08334351

0.08453369

0.08901978

0.09037781

0.09126282

0.09362793

0.0945282

0.09492493

0.09786987

0.1029358

0.09707642

0.09791565

0.09104919

0.06364441

0.1037903

0.0871582

0.097229

0.1009827

0.09129333

0.09906006

0.09188843

0.09461975

0.08718872

0.09089661

0.08387756

0.08750916

0.07907104

0.08563232

0.08052063

0.06910706

0.07754517

0.0662384

0.06503296

0.0728302

0.06544495

0.06159973

0.05511475

0.0471344

0.05252075

0.04670715

0.04776001

0.04884338

0.04412842

0.03535461

0.0435791

0.03700256

0.03581238

0.03617859

0.029953

0.03034973

0.0304718

0.01852417

0.02728271

0.0213623

0.01338196

0.02172852

0.01202393

0.01745605

0.01615906

0.01480103

0.01170349

0.008056641

0.004379272

0.01229858

0.0007171631

0.01124573

-0.003677368

0.01013184

-0.0105896

0.01023865

0.0005950928

-0.008544922

-0.004821777

-0.001663208

0.001251221

-0.003646851

-0.007843018

-0.007751465

-0.007446289

-0.004928589

-0.009552002

-0.01243591

-0.00843811

-0.01797485

-0.01441956

-0.01426697

-0.0133667

-0.01281738

-0.009338379

-0.010849

-0.01490784

-0.01197815

-0.01423645

-0.01419067

-0.01843262

-0.01287842
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		190		1.77449

		192		2.004028

		194		2.175568

		196		2.262924

		198		2.271271

		200		2.317276

		202		2.307861

		204		2.430862

		206		2.561905

		208		2.740372

		210		2.89035

		212		3.019348

		214		3.095169

		216		3.086761

		218		3.131119

		220		3.092743

		222		3.07785

		224		3.207367

		226		3.161087

		228		3.286118

		230		3.422409

		232		3.44545

		234		3.709229

		236		3.593674

		238		3.788284

		240		3.468369

		242		3.452866

		244		3.337921

		246		3.323715

		248		3.337524

		250		3.347733

		252		3.671173

		254		3.740387

		256		3.47583

		258		3.677429

		260		3.543167

		262		3.746216

		264		3.729782

		266		3.901321

		268		3.862167

		270		3.682404

		272		3.991974

		274		3.775162

		276		3.79364

		278		3.781357

		280		3.556351

		282		3.522308

		284		3.531555

		286		3.469284

		288		3.213028

		290		3.229279

		292		3.083817

		294		2.967438

		296		2.820587

		298		2.682159

		300		2.535751

		302		2.376068

		304		2.210602

		306		2.047775

		308		1.887802

		310		1.730927

		312		1.578629

		314		1.434814

		316		1.298233

		318		1.170242

		320		1.051102

		322		0.9423065

		324		0.84198

		326		0.7518768

		328		0.6711426

		330		0.5994415

		332		0.5357819

		334		0.4803162

		336		0.431427

		338		0.3887634

		340		0.3515778

		342		0.319458

		344		0.2911835

		346		0.2664795

		348		0.2452393

		350		0.2262878

		352		0.2099304

		354		0.1961823

		356		0.1848602

		358		0.1752167

		360		0.1674347

		362		0.1610107

		364		0.1564941

		366		0.1539612

		368		0.1499023

		370		0.1486053

		372		0.1481171

		374		0.148407

		376		0.1490784

		378		0.1509552

		380		0.1522675

		382		0.1558533

		384		0.1585846

		386		0.1630096

		388		0.167572

		390		0.1733093

		392		0.181778

		394		0.1893616

		396		0.1996155

		398		0.2137299

		400		0.2272949

		402		0.2475891

		404		0.270462

		406		0.2955933

		408		0.3284454

		410		0.3664398

		412		0.4125214

		414		0.4597015

		416		0.5199432

		418		0.5852814

		420		0.6625671

		422		0.743576

		424		0.8274536

		426		0.9285278

		428		1.028198

		430		1.141708

		432		1.246933

		434		1.367401

		436		1.488266

		438		1.604797

		440		1.727783

		442		1.848099

		444		1.960617

		446		2.06781

		448		2.166916

		450		2.264816

		452		2.352325

		454		2.426666

		456		2.507233

		458		2.584457

		460		2.630478

		462		2.685028

		464		2.747086

		466		2.772766

		468		2.777466

		470		2.739563

		472		2.771469

		474		2.804382

		476		2.800278

		478		2.798782

		480		2.791138

		482		2.761566

		484		2.781281

		486		2.881683

		488		2.714188

		490		2.673645

		492		2.623093

		494		2.572311

		496		2.499954

		498		2.466354

		500		2.394547

		502		2.343201

		504		2.260574

		506		2.185425

		508		2.100266

		510		2.021576

		512		1.937347

		514		1.843781

		516		1.754974

		518		1.668961

		520		1.584717

		522		1.49588

		524		1.410477

		526		1.333786

		528		1.249741

		530		1.170822

		532		1.093933

		534		1.022934

		536		0.9487

		538		0.8805542

		540		0.8123474

		542		0.7489929

		544		0.6878662

		546		0.6283264

		548		0.5745544

		550		0.5198669

		552		0.4705811

		554		0.424408

		556		0.3848572

		558		0.3455353

		560		0.3094482

		562		0.2767029

		564		0.2473297

		566		0.2180481

		568		0.1953278

		570		0.1726532

		572		0.154129

		574		0.1355896

		576		0.1197815

		578		0.1044006

		580		9.59E-02

		582		7.79E-02

		584		7.84E-02

		586		6.95E-02

		588		6.68E-02

		590		6.27E-02

		592		6.52E-02

		594		5.75E-02

		596		5.29E-02

		598		5.41E-02

		600		5.58E-02

		602		5.77E-02

		604		5.39E-02

		606		5.50E-02

		608		0.0559082

		610		6.32E-02

		612		0.0602417

		614		6.29E-02

		616		6.43E-02

		618		6.60E-02

		620		0.067276

		622		7.50E-02

		624		0.0721283

		626		7.87E-02

		628		0.0818634

		630		8.33E-02

		632		8.45E-02

		634		8.90E-02

		636		9.04E-02

		638		9.13E-02

		640		9.36E-02

		642		0.0945282

		644		9.49E-02

		646		9.79E-02

		648		0.1029358

		650		9.71E-02

		652		9.79E-02

		654		9.10E-02

		656		6.36E-02

		658		0.1037903

		660		0.0871582

		662		0.097229

		664		0.1009827

		666		9.13E-02

		668		9.91E-02

		670		9.19E-02

		672		9.46E-02

		674		8.72E-02

		676		9.09E-02

		678		8.39E-02

		680		8.75E-02

		682		7.91E-02

		684		8.56E-02

		686		8.05E-02

		688		6.91E-02

		690		7.75E-02

		692		0.0662384

		694		6.50E-02

		696		0.0728302

		698		6.54E-02

		700		6.16E-02

		702		5.51E-02

		704		0.0471344

		706		5.25E-02

		708		4.67E-02

		710		4.78E-02

		712		4.88E-02

		714		4.41E-02

		716		3.54E-02

		718		0.0435791

		720		3.70E-02

		722		3.58E-02

		724		3.62E-02

		726		0.029953

		728		3.03E-02

		730		0.0304718

		732		1.85E-02

		734		2.73E-02

		736		0.0213623

		738		1.34E-02

		740		2.17E-02

		742		1.20E-02

		744		1.75E-02

		746		1.62E-02

		748		1.48E-02

		750		1.17E-02

		752		8.06E-03

		754		4.38E-03

		756		1.23E-02

		758		7.17E-04

		760		1.12E-02

		762		-3.68E-03

		764		1.01E-02

		766		-0.0105896

		768		1.02E-02

		770		5.95E-04

		772		-8.54E-03

		774		-4.82E-03

		776		-1.66E-03

		778		1.25E-03

		780		-3.65E-03

		782		-7.84E-03

		784		-7.75E-03

		786		-7.45E-03

		788		-4.93E-03

		790		-9.55E-03

		792		-1.24E-02

		794		-8.44E-03

		796		-1.80E-02

		798		-1.44E-02

		800		-1.43E-02

		802		-0.0133667

		804		-1.28E-02

		806		-9.34E-03

		808		-0.010849

		810		-1.49E-02

		812		-1.20E-02

		814		-1.42E-02

		816		-1.42E-02

		818		-1.84E-02

		820		-1.29E-02
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		0.019
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		-0.037
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		-0.073

		-0.077

		-0.081

		-0.085

		-0.089

		-0.093

		-0.097

		-0.101
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		-0.109

		-0.113

		-0.117

		-0.121
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		-0.133

		-0.137
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		-0.145
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		-0.153
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		1.399

		1.395

		1.391

		1.387

		1.383

		1.379

		1.375

		1.371

		1.367

		1.363

		1.359

		1.355

		1.351

		1.347

		1.343

		1.339

		1.335

		1.331

		1.327

		1.323

		1.319

		1.315

		1.311

		1.307

		1.303

		1.299

		1.295

		1.291

		1.287

		1.283

		1.279

		1.275

		1.271

		1.267

		1.263

		1.259

		1.255

		1.251

		1.247

		1.243

		1.239

		1.235

		1.231

		1.227

		1.223

		1.219

		1.215

		1.211

		1.207

		1.203

		1.199

		1.195

		1.191

		1.187

		1.183

		1.179

		1.175

		1.171

		1.167

		1.163

		1.159

		1.155

		1.151

		1.147

		1.143

		1.139

		1.135

		1.131

		1.127

		1.123

		1.119

		1.115

		1.111

		1.107

		1.103

		1.099

		1.095

		1.091

		1.087

		1.083

		1.079

		1.075

		1.071

		1.067

		1.063

		1.059

		1.055

		1.051

		1.047

		1.043

		1.039

		1.035

		1.031

		1.027

		1.023

		1.019

		1.015

		1.011

		1.007

		1.003

		0.99901

		0.99501

		0.99101

		0.98701

		0.98301

		0.97901

		0.97501

		0.97101

		0.96701

		0.96301

		0.95901

		0.95501

		0.95101

		0.94701

		0.94301

		0.93901

		0.93501

		0.93101

		0.92701

		0.92301

		0.91901

		0.91501

		0.91101

		0.90701

		0.90301

		0.89901

		0.89501

		0.89101

		0.88701

		0.88301

		0.87901

		0.87501

		0.87101

		0.86701

		0.86301

		0.85901

		0.85501

		0.85101

		0.84701

		0.84301

		0.83901

		0.83501

		0.83101

		0.82701

		0.82301

		0.81901

		0.81501

		0.81101

		0.80701

		0.80301

		0.79901

		0.79501

		0.79101

		0.78701

		0.78301

		0.77901

		0.77501

		0.77101

		0.76701

		0.76301

		0.75901

		0.75501

		0.75101

		0.74701

		0.74301

		0.73901

		0.73501

		0.73101

		0.72701

		0.72301

		0.71901

		0.71501

		0.71101

		0.70701

		0.70301

		0.69901

		0.69501

		0.69101

		0.68701

		0.68301

		0.67901

		0.67501

		0.67101

		0.66701

		0.66301

		0.65901

		0.65501

		0.65101

		0.64701

		0.64301

		0.63901

		0.63501

		0.63101

		0.62701

		0.62301

		0.61901

		0.61501

		0.61101

		0.60701

		0.60301

		0.59901

		0.59501

		0.59101

		0.58701

		0.58301

		0.57901

		0.57501

		0.57101

		0.56701

		0.56301

		0.55901

		0.55501

		0.55101

		0.54701

		0.54301

		0.53901

		0.53501

		0.53101

		0.52701

		0.52301

		0.51901

		0.51501

		0.51101

		0.50701

		0.50301

		0.49901

		0.49501

		0.49101

		0.48701

		0.48301

		0.47901

		0.47501

		0.47101

		0.46701

		0.46301

		0.45901

		0.45501

		0.45101

		0.44701

		0.44301

		0.43901

		0.43501

		0.43101

		0.42701

		0.42301

		0.41901

		0.41501

		0.41101

		0.40701

		0.40301

		0.39901

		0.39501

		0.39101

		0.38701

		0.38301

		0.37901

		0.37501

		0.37101

		0.36701

		0.36301

		0.35901

		0.35501

		0.35101

		0.34701

		0.34301

		0.33901

		0.33501

		0.33101

		0.32701

		0.32301

		0.31901

		0.31501

		0.31101

		0.30701

		0.30301

		0.29901

		0.29501

		0.29101

		0.28701

		0.28301

		0.27901

		0.27501

		0.27101

		0.26701

		0.26301

		0.25901

		0.25501

		0.25101

		0.24701

		0.24301

		0.23901

		0.23501

		0.23101

		0.22701

		0.22301

		0.21901

		0.21501

		0.21101

		0.20701

		0.20301

		0.19901

		0.19501

		0.19101

		0.18701

		0.18301

		0.17901

		0.17501

		0.17101

		0.16701

		0.16301

		0.15901

		0.15501

		0.15101

		0.14701

		0.14301

		0.13901

		0.13501

		0.13101

		0.12701

		0.12301

		0.11901

		0.11501

		0.11101

		0.10701

		0.10301

		0.099011

		0.095011

		0.091011

		0.087011

		0.083011

		0.079011

		0.075011

		0.071011

		0.067011

		0.063011

		0.059011

		0.055011

		0.051011

		0.047011

		0.043011

		0.039011

		0.035011

		0.031011

		0.027011

		0.023011



Potential (V)

Current (mA)

0.00284

0.00796

0.01279

0.01754

0.0221

0.0268

0.0315

0.0361

0.0408

0.0454

0.0502

0.0549

0.0598

0.0646

0.0694

0.0744

0.0794

0.0843

0.0894

0.0944

0.0996

0.1047

0.11

0.115

0.1202

0.1256

0.1306

0.136

0.1412

0.1465

0.1519

0.1571

0.1626

0.1676

0.1728

0.1781

0.1834

0.1887

0.194

0.199

0.204

0.209

0.215

0.22

0.225

0.23

0.236

0.241

0.246

0.251

0.256

0.262

0.267

0.272

0.277

0.282

0.288

0.293

0.298

0.303

0.308

0.313

0.318

0.323

0.328

0.333

0.338

0.342

0.347

0.352

0.357

0.362

0.367

0.371

0.376

0.38

0.385

0.389

0.394

0.398

0.403

0.407

0.411

0.416

0.42

0.425

0.429

0.433

0.437

0.441

0.445

0.449

0.453

0.457

0.461

0.465

0.468

0.472

0.475

0.478

0.482

0.485

0.488

0.491

0.494

0.497

0.5

0.503

0.505

0.508

0.51

0.513

0.515

0.517

0.519

0.521

0.523

0.525

0.526

0.528

0.529

0.53

0.531

0.532

0.533

0.533

0.534

0.533

0.533

0.533

0.533

0.532

0.532

0.53

0.529

0.528

0.526

0.524

0.522

0.519

0.517

0.514

0.511

0.509

0.505

0.503

0.5

0.497

0.494

0.492

0.49

0.488

0.486

0.484

0.483

0.483

0.482

0.482

0.482

0.482

0.482

0.482

0.483

0.484

0.485

0.486

0.487

0.488

0.489

0.49

0.491

0.492

0.494

0.494

0.496

0.497

0.498

0.499

0.499

0.501

0.502

0.503

0.504

0.504

0.505

0.505

0.506

0.506

0.506

0.506

0.506

0.506

0.505

0.504

0.504

0.502

0.501

0.5

0.498

0.496

0.493

0.491

0.488

0.484

0.48

0.476

0.472

0.466

0.461

0.454

0.447

0.44

0.433

0.426

0.419

0.413

0.407

0.402

0.398

0.394

0.39

0.386

0.384

0.38

0.377

0.375

0.372

0.369

0.367

0.364

0.362

0.359

0.357

0.355

0.353

0.351

0.349

0.347

0.345

0.344

0.342

0.34

0.339

0.337

0.335

0.334

0.332

0.331

0.329

0.328

0.326

0.325

0.324

0.322

0.321

0.319

0.318

0.317

0.316

0.314

0.313

0.312

0.311

0.31

0.308

0.307

0.306

0.305

0.304

0.303

0.302

0.301

0.299

0.299

0.298

0.297

0.296

0.295

0.294

0.292

0.292

0.291

0.29

0.289

0.288

0.288

0.286

0.286

0.285

0.283

0.283

0.282

0.281

0.281

0.279

0.279

0.278

0.277

0.276

0.275

0.275

0.274

0.274

0.273

0.272

0.272

0.27

0.27

0.269

0.268

0.267

0.267

0.266

0.266

0.265

0.264

0.264

0.263

0.262

0.262

0.261

0.261

0.26

0.259

0.259

0.258

0.257

0.257

0.256

0.256

0.255

0.255

0.254

0.254

0.253

0.252

0.252

0.251

0.251

0.25

0.25

0.25

0.249

0.249

0.248

0.248

0.247

0.246

0.247

0.246

0.246

0.246

0.245

0.245

0.245

0.245

0.245

0.245

0.245

0.245

0.246

0.246

0.247

0.247

0.248

0.249

0.25

0.251

0.252

0.254

0.256

0.257

0.259

0.26

0.262

0.264

0.266

0.268

0.27

0.272

0.275

0.277

0.279

0.281

0.283

0.286

0.288

0.29

0.293

0.295

0.297

0.3

0.302

0.304

0.307

0.309

0.311

0.314

0.316

0.318

0.32

0.323

0.325

0.327

0.329

0.331

0.334

0.336

0.338

0.34

0.342

0.344

0.346

0.347

0.349

0.35

0.353

0.354

0.355

0.357

0.358

0.359

0.36

0.361

0.362

0.363

0.364

0.364

0.365

0.365

0.365

0.365

0.365

0.365

0.364

0.364

0.363

0.362

0.361

0.359

0.358

0.355

0.353

0.35

0.347

0.343

0.339

0.335

0.331

0.325

0.321

0.315

0.309

0.302

0.297

0.29

0.283

0.277

0.27

0.263

0.256

0.249

0.243

0.235

0.229

0.222

0.216

0.21

0.203

0.198

0.191

0.186

0.18

0.174

0.169

0.163

0.159

0.154

0.149

0.145

0.1399

0.1355

0.1312

0.127

0.1229

0.1189

0.1148

0.1109

0.1071

0.1033

0.0996

0.0961

0.0929

0.09

0.087

0.0841

0.0815

0.0789

0.0764

0.0739

0.0717

0.0694

0.0672

0.0653

0.063

0.0611

0.0592

0.0572

0.0557

0.0538

0.0523

0.0507

0.0492

0.048

0.0466

0.0457

0.0445

0.0435

0.0427

0.0418

0.0412

0.0403

0.0399

0.0395

0.0392

0.0393

0.039

0.0394

0.0397

0.04

0.0407

0.041

0.0415

0.0418

0.0423

0.0426

0.0428

0.0433

0.0438

0.044

0.0445

0.0446

0.0454

0.0457

0.046

0.0464

0.0466

0.0473

0.0475

0.0478

0.0481

0.0483

0.0487

0.0491

0.0495

0.0498

0.0501

0.0504

0.0508

0.0511

0.0513

0.0516

0.0521

0.0524

0.0527

0.053

0.0534

0.0536

0.0541

0.0542

0.0546

0.0551

0.0554

0.0558

0.0562

0.0566

0.0573

0.0577

0.0583

0.0586

0.0592

0.0598

0.0602

0.061

0.0614

0.0621

0.0625

0.0631

0.0636

0.0641

0.0648

0.0651

0.0657

0.0662

0.0666

0.0671

0.0675

0.068

0.0683

0.0685

0.069

0.0692

0.0697

0.0699

0.0702

0.0706

0.0706

0.071

0.0713

0.0716

0.072

0.0724

0.073

0.0733

0.0739

0.0746

0.0753

0.0762

0.077

0.0778

0.0788

0.0798

0.0809

0.082

0.0833

0.0845

0.086

0.0874

0.0889

0.0904

0.0918

0.0934

0.095

0.0966

0.0982

0.1

0.1017

0.1033

0.1052

0.1069

0.1087

0.1105

0.1122

0.1141

0.1158

0.1176

0.1192

0.1209

0.1226

0.124

0.1256

0.127

0.1284

0.1299

0.131

0.1324

0.1335

0.1347

0.1359

0.1367

0.138

0.1387

0.1398

0.1407

0.1413

0.1423

0.1427

0.1435

0.1441

0.1445

0.1452

0.1454

0.1459

0.1462

0.1465

0.147

0.147

0.1474

0.1475

0.1476

0.1478

0.1478

0.148

0.1479

0.148

0.148

0.1479

0.1481

0.148

0.148

0.148

0.1479

0.1479

0.1477

0.1477

0.1476

0.1475

0.1475

0.1473

0.1472

0.1472

0.147

0.147

0.1469

0.1468

0.1467

0.1466

0.1465

0.1464

0.1463

0.1462

0.146

0.1459

0.1459

0.1458

0.1458

0.1456

0.1454

0.1455

0.1453

0.1453

0.1451

0.145

0.145

0.1448

0.1448

0.1446

0.1445

0.1446

0.1443

0.1443

0.1441

0.1441

0.144

0.1438

0.1438

0.1435

0.1435

0.1434

0.1431

0.1432

0.1428

0.1428

0.1426

0.1424

0.1424

0.1419

0.142

0.1417

0.1415

0.1414

0.141

0.141

0.1407

0.1405

0.1404

0.1401

0.14

0.1397

0.1395

0.1394

0.1391

0.139

0.1388

0.1387

0.1386

0.1385

0.1384

0.1383

0.1383

0.1383

0.1383

0.1383

0.1383

0.1384

0.1384

0.1385

0.1386

0.1387

0.1389

0.139

0.1392

0.1393

0.1396

0.1397

0.1399

0.1401

0.1403

0.1406

0.1407

0.141

0.1411

0.1413

0.1416

0.1418

0.1421

0.1422

0.1424

0.1427

0.1428

0.1432

0.1434

0.1436

0.144

0.144

0.1444

0.1445

0.1446

0.1449

0.1449

0.1452

0.1451

0.1454

0.1454

0.1453

0.1455

0.1453

0.1453

0.1451

0.1448

0.1447

0.1442

0.1439

0.1434

0.1427

0.1421

0.141

0.1402

0.1391

0.138

0.137

0.1357

0.1348

0.1336

0.1326

0.1318

0.1307

0.13

0.1291

0.1284

0.1278

0.1271

0.1267

0.1262

0.1257

0.1253

0.125

0.1246

0.1244

0.1242

0.1239

0.1238

0.1235

0.1235

0.1233

0.1232

0.1231

0.123

0.123

0.1229

0.1229

0.1229

0.1227

0.1229

0.1228

0.1228

0.1228

0.1228

0.123

0.123

0.1231

0.1232

0.1232

0.1234

0.1234

0.1237

0.1239

0.1242

0.1246

0.1248

0.1254

0.1258

0.1263

0.127

0.1279

0.129

0.1302

0.1319

0.1337

0.1355

0.1367

0.1367

0.1357

0.1336

0.1307

0.1274

0.1236

0.1197

0.1156

0.1117

0.1076

0.1033

0.0991

0.0947

0.0904

0.0859

0.0813

0.0769

0.0722

0.0679

0.0634

0.0592

0.0552

0.051

0.0475

0.0437

0.0403

0.0367

0.033

0.0294

0.0256

0.0219

0.0181

0.0144

0.01081

0.0071

0.0035

-0.00018

-0.00385

-0.00736

-0.0109

-0.01439

-0.0179

-0.0213

-0.0245

-0.0279

-0.0311

-0.0343

-0.0372

-0.0402

-0.0432

-0.046

-0.0488

-0.0514

-0.054

-0.0565

-0.0588

-0.0611

-0.063

-0.065

-0.0668

-0.0684

-0.0699

-0.0711

-0.0721

-0.0728

-0.0734

-0.0738

-0.0738

-0.0737

-0.0734

-0.0732

-0.0729

-0.0726

-0.0722

-0.0719

-0.0719

-0.0719

-0.0722

-0.0724

-0.0729

-0.0737

-0.0744

-0.0755

-0.0764

-0.0776

-0.079

-0.0803

-0.0818

-0.0831

-0.0849

-0.0867

-0.0884

-0.0903

-0.092

-0.0941

-0.096

-0.0982

-0.1003

-0.1022

-0.1046

-0.1067

-0.109

-0.1114

-0.1134

-0.116

-0.1184

-0.1208

-0.1232

-0.1256

-0.1283

-0.1307

-0.1334

-0.136

-0.1385

-0.1414

-0.144

-0.147

-0.1497

-0.1525

-0.1555

-0.1584

-0.1616

-0.1645

-0.1677

-0.1709

-0.1741

-0.1775

-0.1807

-0.184

-0.1874

-0.191

-0.194

-0.198

-0.201

-0.205

-0.209

-0.212

-0.216

-0.219

-0.223

-0.227

-0.231

-0.235

-0.238

-0.242

-0.246

-0.25

-0.255

-0.258

-0.263

-0.267

-0.271

-0.275

-0.279

-0.283

-0.288

-0.292

-0.297

-0.3

-0.305

-0.31

-0.314

-0.319

-0.323

-0.328

-0.332

-0.337

-0.341

-0.345

-0.351

-0.355

-0.36

-0.364

-0.369

-0.374

-0.378

-0.383

-0.388

-0.392

-0.397

-0.401

-0.406

-0.411

-0.415

-0.42

-0.424

-0.429

-0.434

-0.438

-0.443

-0.447

-0.452

-0.456

-0.46

-0.465

-0.469

-0.473

-0.477

-0.481

-0.484

-0.488

-0.492

-0.495

-0.498

-0.5

-0.503

-0.505

-0.508

-0.509

-0.511

-0.513

-0.514

-0.515

-0.515

-0.516

-0.516

-0.516

-0.515

-0.513

-0.512

-0.51

-0.507

-0.503

-0.498

-0.492

-0.485

-0.477

-0.468

-0.458

-0.451

-0.444

-0.438

-0.433

-0.429

-0.425

-0.422

-0.42

-0.419

-0.417

-0.416

-0.415

-0.415

-0.416

-0.416

-0.417

-0.418

-0.419

-0.421

-0.422

-0.424

-0.426

-0.428

-0.431

-0.433

-0.436

-0.438

-0.441

-0.444

-0.447

-0.45

-0.454

-0.457

-0.46

-0.463

-0.467

-0.471

-0.475

-0.478

-0.482

-0.486

-0.489

-0.493

-0.497

-0.501

-0.505

-0.51

-0.514

-0.518

-0.522

-0.526

-0.531

-0.535

-0.539

-0.544

-0.548

-0.553

-0.557

-0.562

-0.566

-0.571

-0.576

-0.581

-0.586

-0.59

-0.595

-0.6

-0.604

-0.609

-0.613

-0.619

-0.624

-0.629

-0.634

-0.638

-0.643

-0.648

-0.653

-0.658

-0.663

-0.668

-0.673

-0.678

-0.683

-0.688

-0.693

-0.698

-0.703

-0.709

-0.713

-0.719

-0.724

-0.73

-0.734
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-0.745

-0.75

-0.756

-0.76
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-1.79
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-1.76
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-1.75
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-1.74
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-1.61
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-1.59
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-1.55
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-1.53
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-1.51
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-1.497

-1.492
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-1.475

-1.469

-1.463

-1.458

-1.452

-1.446

-1.44

-1.434

-1.429

-1.423

-1.417

-1.411

-1.405

-1.4

-1.394

-1.388

-1.382

-1.377

-1.371

-1.365

-1.359

-1.353

-1.347

-1.341

-1.336

-1.329

-1.324

-1.319

-1.313

-1.307

-1.301

-1.296

-1.29

-1.284

-1.279

-1.272

-1.267

-1.261

-1.255

-1.25

-1.244

-1.239

-1.232

-1.227

-1.221

-1.215

-1.21

-1.204

-1.198

-1.192

-1.186

-1.181

-1.175

-1.17

-1.164

-1.158

-1.152

-1.147

-1.141

-1.135

-1.129

-1.124

-1.118

-1.113

-1.107

-1.101

-1.096

-1.09

-1.085

-1.079

-1.073
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-1.056

-1.05

-1.045

-1.039

-1.034

-1.028

-1.022

-1.017

-1.011

-1.005

-1

-0.994

-0.988

-0.983

-0.978

-0.972

-0.966

-0.96

-0.955

-0.949

-0.944

-0.939

-0.932

-0.927

-0.922

-0.916
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-0.904
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-0.894

-0.888

-0.883

-0.876

-0.872

-0.867

-0.861

-0.856

-0.849

-0.844

-0.838

-0.833

-0.827

-0.821

-0.816

-0.811

-0.806

-0.8

-0.794

-0.789

-0.783

-0.778

-0.773

-0.767

-0.762

-0.756

-0.751

-0.746

-0.74

-0.735

-0.729

-0.724

-0.718

-0.712
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-0.696
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-0.674
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		2.30E-02		2.84E-03		2.84E-06

		1.90E-02		7.96E-03		7.96E-06

		1.50E-02		1.28E-02		1.28E-05

		1.10E-02		1.75E-02		1.75E-05

		7.00E-03		2.21E-02		2.21E-05

		3.00E-03		2.68E-02		2.68E-05

		-1.00E-03		3.15E-02		3.15E-05

		-5.00E-03		3.61E-02		3.61E-05

		-9.00E-03		4.08E-02		4.08E-05

		-1.30E-02		4.54E-02		4.54E-05

		-1.70E-02		5.02E-02		5.02E-05

		-2.10E-02		5.49E-02		5.49E-05

		-2.50E-02		5.98E-02		5.98E-05

		-2.90E-02		6.46E-02		6.46E-05

		-3.30E-02		6.94E-02		6.94E-05

		-3.70E-02		7.44E-02		7.44E-05

		-4.10E-02		7.94E-02		7.94E-05

		-4.50E-02		8.43E-02		8.43E-05

		-4.90E-02		8.94E-02		8.94E-05

		-5.30E-02		9.44E-02		9.44E-05

		-5.70E-02		9.96E-02		9.96E-05

		-6.10E-02		1.05E-01		1.05E-04

		-6.50E-02		1.10E-01		1.10E-04

		-6.90E-02		1.15E-01		1.15E-04

		-7.30E-02		1.20E-01		1.20E-04

		-7.70E-02		1.26E-01		1.26E-04

		-8.10E-02		1.31E-01		1.31E-04

		-8.50E-02		1.36E-01		1.36E-04

		-8.90E-02		1.41E-01		1.41E-04

		-9.30E-02		1.47E-01		1.47E-04

		-9.70E-02		1.52E-01		1.52E-04

		-1.01E-01		1.57E-01		1.57E-04

		-1.05E-01		1.63E-01		1.63E-04

		-1.09E-01		1.68E-01		1.68E-04

		-1.13E-01		1.73E-01		1.73E-04

		-1.17E-01		1.78E-01		1.78E-04

		-1.21E-01		1.83E-01		1.83E-04

		-1.25E-01		1.89E-01		1.89E-04

		-1.29E-01		1.94E-01		1.94E-04

		-1.33E-01		1.99E-01		1.99E-04

		-1.37E-01		2.04E-01		2.04E-04

		-1.41E-01		2.09E-01		2.09E-04

		-1.45E-01		2.15E-01		2.15E-04

		-1.49E-01		2.20E-01		2.20E-04

		-1.53E-01		2.25E-01		2.25E-04

		-1.57E-01		2.30E-01		2.30E-04

		-1.61E-01		2.36E-01		2.36E-04

		-1.65E-01		2.41E-01		2.41E-04

		-1.69E-01		2.46E-01		2.46E-04

		-1.73E-01		2.51E-01		2.51E-04

		-1.77E-01		2.56E-01		2.56E-04

		-1.81E-01		2.62E-01		2.62E-04

		-1.85E-01		2.67E-01		2.67E-04

		-1.89E-01		2.72E-01		2.72E-04

		-1.93E-01		2.77E-01		2.77E-04

		-1.97E-01		2.82E-01		2.82E-04

		-2.01E-01		2.88E-01		2.88E-04

		-2.05E-01		2.93E-01		2.93E-04

		-2.09E-01		2.98E-01		2.98E-04

		-2.13E-01		3.03E-01		3.03E-04

		-2.17E-01		3.08E-01		3.08E-04

		-2.21E-01		3.13E-01		3.13E-04

		-2.25E-01		3.18E-01		3.18E-04

		-2.29E-01		3.23E-01		3.23E-04

		-2.33E-01		3.28E-01		3.28E-04

		-2.37E-01		3.33E-01		3.33E-04

		-2.41E-01		3.38E-01		3.38E-04

		-2.45E-01		3.42E-01		3.42E-04

		-2.49E-01		3.47E-01		3.47E-04

		-2.53E-01		3.52E-01		3.52E-04

		-2.57E-01		3.57E-01		3.57E-04

		-2.61E-01		3.62E-01		3.62E-04

		-2.65E-01		3.67E-01		3.67E-04

		-2.69E-01		3.71E-01		3.71E-04

		-2.73E-01		3.76E-01		3.76E-04

		-2.77E-01		3.80E-01		3.80E-04

		-2.81E-01		3.85E-01		3.85E-04

		-2.85E-01		3.89E-01		3.89E-04

		-2.89E-01		3.94E-01		3.94E-04

		-2.93E-01		3.98E-01		3.98E-04

		-2.97E-01		4.03E-01		4.03E-04

		-3.01E-01		4.07E-01		4.07E-04

		-3.05E-01		4.11E-01		4.11E-04

		-3.09E-01		4.16E-01		4.16E-04

		-3.13E-01		4.20E-01		4.20E-04

		-3.17E-01		4.25E-01		4.25E-04

		-3.21E-01		4.29E-01		4.29E-04

		-3.25E-01		4.33E-01		4.33E-04

		-3.29E-01		4.37E-01		4.37E-04

		-3.33E-01		4.41E-01		4.41E-04

		-3.37E-01		4.45E-01		4.45E-04

		-3.41E-01		4.49E-01		4.49E-04

		-3.45E-01		4.53E-01		4.53E-04

		-3.49E-01		4.57E-01		4.57E-04

		-3.53E-01		4.61E-01		4.61E-04

		-3.57E-01		4.65E-01		4.65E-04

		-3.61E-01		4.68E-01		4.68E-04

		-3.65E-01		4.72E-01		4.72E-04

		-3.69E-01		4.75E-01		4.75E-04

		-3.73E-01		4.78E-01		4.78E-04

		-3.77E-01		4.82E-01		4.82E-04

		-3.81E-01		4.85E-01		4.85E-04

		-3.85E-01		4.88E-01		4.88E-04

		-3.89E-01		4.91E-01		4.91E-04

		-3.93E-01		4.94E-01		4.94E-04

		-3.97E-01		4.97E-01		4.97E-04

		-4.01E-01		5.00E-01		5.00E-04

		-4.05E-01		5.03E-01		5.03E-04

		-4.09E-01		5.05E-01		5.05E-04

		-4.13E-01		5.08E-01		5.08E-04

		-4.17E-01		5.10E-01		5.10E-04

		-4.21E-01		5.13E-01		5.13E-04

		-4.25E-01		5.15E-01		5.15E-04

		-4.29E-01		5.17E-01		5.17E-04

		-4.33E-01		5.19E-01		5.19E-04

		-4.37E-01		5.21E-01		5.21E-04

		-4.41E-01		5.23E-01		5.23E-04

		-4.45E-01		5.25E-01		5.25E-04

		-4.49E-01		5.26E-01		5.26E-04

		-4.53E-01		5.28E-01		5.28E-04

		-4.57E-01		5.29E-01		5.29E-04

		-4.61E-01		5.30E-01		5.30E-04

		-4.65E-01		5.31E-01		5.31E-04

		-4.69E-01		5.32E-01		5.32E-04

		-4.73E-01		5.33E-01		5.33E-04

		-4.77E-01		5.33E-01		5.33E-04

		-4.81E-01		5.34E-01		5.34E-04

		-4.85E-01		5.33E-01		5.33E-04

		-4.89E-01		5.33E-01		5.33E-04

		-4.93E-01		5.33E-01		5.33E-04

		-4.97E-01		5.33E-01		5.33E-04

		-5.01E-01		5.32E-01		5.32E-04

		-5.05E-01		5.32E-01		5.32E-04

		-5.09E-01		5.30E-01		5.30E-04

		-5.13E-01		5.29E-01		5.29E-04

		-5.17E-01		5.28E-01		5.28E-04

		-5.21E-01		5.26E-01		5.26E-04

		-5.25E-01		5.24E-01		5.24E-04

		-5.29E-01		5.22E-01		5.22E-04

		-5.33E-01		5.19E-01		5.19E-04

		-5.37E-01		5.17E-01		5.17E-04

		-5.41E-01		5.14E-01		5.14E-04

		-5.45E-01		5.11E-01		5.11E-04

		-5.49E-01		5.09E-01		5.09E-04

		-5.53E-01		5.05E-01		5.05E-04

		-5.57E-01		5.03E-01		5.03E-04

		-5.61E-01		5.00E-01		5.00E-04

		-5.65E-01		4.97E-01		4.97E-04

		-5.69E-01		4.94E-01		4.94E-04

		-5.73E-01		4.92E-01		4.92E-04

		-5.77E-01		4.90E-01		4.90E-04

		-5.81E-01		4.88E-01		4.88E-04

		-5.85E-01		4.86E-01		4.86E-04

		-5.89E-01		4.84E-01		4.84E-04

		-5.93E-01		4.83E-01		4.83E-04

		-5.97E-01		4.83E-01		4.83E-04

		-6.01E-01		4.82E-01		4.82E-04

		-6.05E-01		4.82E-01		4.82E-04

		-6.09E-01		4.82E-01		4.82E-04

		-6.13E-01		4.82E-01		4.82E-04

		-6.17E-01		4.82E-01		4.82E-04

		-6.21E-01		4.82E-01		4.82E-04

		-6.25E-01		4.83E-01		4.83E-04

		-6.29E-01		4.84E-01		4.84E-04

		-6.33E-01		4.85E-01		4.85E-04

		-6.37E-01		4.86E-01		4.86E-04

		-6.41E-01		4.87E-01		4.87E-04

		-6.45E-01		4.88E-01		4.88E-04

		-6.49E-01		4.89E-01		4.89E-04

		-6.53E-01		4.90E-01		4.90E-04

		-6.57E-01		4.91E-01		4.91E-04

		-6.61E-01		4.92E-01		4.92E-04

		-6.65E-01		4.94E-01		4.94E-04

		-6.69E-01		4.94E-01		4.94E-04

		-6.73E-01		4.96E-01		4.96E-04

		-6.77E-01		4.97E-01		4.97E-04

		-6.81E-01		4.98E-01		4.98E-04

		-6.85E-01		4.99E-01		4.99E-04

		-6.89E-01		4.99E-01		4.99E-04

		-6.93E-01		5.01E-01		5.01E-04

		-6.97E-01		5.02E-01		5.02E-04

		-7.01E-01		5.03E-01		5.03E-04

		-7.05E-01		5.04E-01		5.04E-04

		-7.09E-01		5.04E-01		5.04E-04

		-7.13E-01		5.05E-01		5.05E-04

		-7.17E-01		5.05E-01		5.05E-04

		-7.21E-01		5.06E-01		5.06E-04

		-7.25E-01		5.06E-01		5.06E-04

		-7.29E-01		5.06E-01		5.06E-04

		-7.33E-01		5.06E-01		5.06E-04

		-7.37E-01		5.06E-01		5.06E-04

		-7.41E-01		5.06E-01		5.06E-04

		-7.45E-01		5.05E-01		5.05E-04

		-7.49E-01		5.04E-01		5.04E-04

		-7.53E-01		5.04E-01		5.04E-04

		-7.57E-01		5.02E-01		5.02E-04

		-7.61E-01		5.01E-01		5.01E-04

		-7.65E-01		5.00E-01		5.00E-04

		-7.69E-01		4.98E-01		4.98E-04

		-7.73E-01		4.96E-01		4.96E-04

		-7.77E-01		4.93E-01		4.93E-04

		-7.81E-01		4.91E-01		4.91E-04

		-7.85E-01		4.88E-01		4.88E-04

		-7.89E-01		4.84E-01		4.84E-04

		-7.93E-01		4.80E-01		4.80E-04

		-7.97E-01		4.76E-01		4.76E-04

		-8.01E-01		4.72E-01		4.72E-04

		-8.05E-01		4.66E-01		4.66E-04

		-8.09E-01		4.61E-01		4.61E-04

		-8.13E-01		4.54E-01		4.54E-04

		-8.17E-01		4.47E-01		4.47E-04

		-8.21E-01		4.40E-01		4.40E-04

		-8.25E-01		4.33E-01		4.33E-04

		-8.29E-01		4.26E-01		4.26E-04

		-8.33E-01		4.19E-01		4.19E-04

		-8.37E-01		4.13E-01		4.13E-04

		-8.41E-01		4.07E-01		4.07E-04

		-8.45E-01		4.02E-01		4.02E-04

		-8.49E-01		3.98E-01		3.98E-04

		-8.53E-01		3.94E-01		3.94E-04

		-8.57E-01		3.90E-01		3.90E-04

		-8.61E-01		3.86E-01		3.86E-04

		-8.65E-01		3.84E-01		3.84E-04

		-8.69E-01		3.80E-01		3.80E-04

		-8.73E-01		3.77E-01		3.77E-04

		-8.77E-01		3.75E-01		3.75E-04

		-8.81E-01		3.72E-01		3.72E-04

		-8.85E-01		3.69E-01		3.69E-04

		-8.89E-01		3.67E-01		3.67E-04

		-8.93E-01		3.64E-01		3.64E-04

		-8.97E-01		3.62E-01		3.62E-04

		-9.01E-01		3.59E-01		3.59E-04

		-9.05E-01		3.57E-01		3.57E-04

		-9.09E-01		3.55E-01		3.55E-04

		-9.13E-01		3.53E-01		3.53E-04

		-9.17E-01		3.51E-01		3.51E-04

		-9.21E-01		3.49E-01		3.49E-04

		-9.25E-01		3.47E-01		3.47E-04

		-9.29E-01		3.45E-01		3.45E-04

		-9.33E-01		3.44E-01		3.44E-04

		-9.37E-01		3.42E-01		3.42E-04

		-9.41E-01		3.40E-01		3.40E-04

		-9.45E-01		3.39E-01		3.39E-04

		-9.49E-01		3.37E-01		3.37E-04

		-9.53E-01		3.35E-01		3.35E-04

		-9.57E-01		3.34E-01		3.34E-04

		-9.61E-01		3.32E-01		3.32E-04

		-9.65E-01		3.31E-01		3.31E-04

		-9.69E-01		3.29E-01		3.29E-04

		-9.73E-01		3.28E-01		3.28E-04

		-9.77E-01		3.26E-01		3.26E-04

		-9.81E-01		3.25E-01		3.25E-04

		-9.85E-01		3.24E-01		3.24E-04

		-9.89E-01		3.22E-01		3.22E-04

		-9.93E-01		3.21E-01		3.21E-04

		-9.97E-01		3.19E-01		3.19E-04

		-1.00E+00		3.18E-01		3.18E-04

		-1.01E+00		3.17E-01		3.17E-04

		-1.01E+00		3.16E-01		3.16E-04

		-1.01E+00		3.14E-01		3.14E-04

		-1.02E+00		3.13E-01		3.13E-04

		-1.02E+00		3.12E-01		3.12E-04

		-1.03E+00		3.11E-01		3.11E-04

		-1.03E+00		3.10E-01		3.10E-04

		-1.03E+00		3.08E-01		3.08E-04

		-1.04E+00		3.07E-01		3.07E-04

		-1.04E+00		3.06E-01		3.06E-04

		-1.05E+00		3.05E-01		3.05E-04

		-1.05E+00		3.04E-01		3.04E-04

		-1.05E+00		3.03E-01		3.03E-04

		-1.06E+00		3.02E-01		3.02E-04

		-1.06E+00		3.01E-01		3.01E-04

		-1.07E+00		2.99E-01		2.99E-04

		-1.07E+00		2.99E-01		2.99E-04

		-1.07E+00		2.98E-01		2.98E-04

		-1.08E+00		2.97E-01		2.97E-04

		-1.08E+00		2.96E-01		2.96E-04

		-1.09E+00		2.95E-01		2.95E-04

		-1.09E+00		2.94E-01		2.94E-04

		-1.09E+00		2.92E-01		2.92E-04

		-1.10E+00		2.92E-01		2.92E-04

		-1.10E+00		2.91E-01		2.91E-04

		-1.11E+00		2.90E-01		2.90E-04

		-1.11E+00		2.89E-01		2.89E-04

		-1.11E+00		2.88E-01		2.88E-04

		-1.12E+00		2.88E-01		2.88E-04

		-1.12E+00		2.86E-01		2.86E-04

		-1.13E+00		2.86E-01		2.86E-04

		-1.13E+00		2.85E-01		2.85E-04

		-1.13E+00		2.83E-01		2.83E-04

		-1.14E+00		2.83E-01		2.83E-04

		-1.14E+00		2.82E-01		2.82E-04

		-1.15E+00		2.81E-01		2.81E-04

		-1.15E+00		2.81E-01		2.81E-04

		-1.15E+00		2.79E-01		2.79E-04

		-1.16E+00		2.79E-01		2.79E-04

		-1.16E+00		2.78E-01		2.78E-04

		-1.17E+00		2.77E-01		2.77E-04

		-1.17E+00		2.76E-01		2.76E-04

		-1.17E+00		2.75E-01		2.75E-04

		-1.18E+00		2.75E-01		2.75E-04

		-1.18E+00		2.74E-01		2.74E-04

		-1.19E+00		2.74E-01		2.74E-04

		-1.19E+00		2.73E-01		2.73E-04

		-1.19E+00		2.72E-01		2.72E-04

		-1.20E+00		2.72E-01		2.72E-04

		-1.20E+00		2.70E-01		2.70E-04

		-1.21E+00		2.70E-01		2.70E-04

		-1.21E+00		2.69E-01		2.69E-04

		-1.21E+00		2.68E-01		2.68E-04

		-1.22E+00		2.67E-01		2.67E-04

		-1.22E+00		2.67E-01		2.67E-04

		-1.23E+00		2.66E-01		2.66E-04

		-1.23E+00		2.66E-01		2.66E-04

		-1.23E+00		2.65E-01		2.65E-04

		-1.24E+00		2.64E-01		2.64E-04

		-1.24E+00		2.64E-01		2.64E-04

		-1.25E+00		2.63E-01		2.63E-04

		-1.25E+00		2.62E-01		2.62E-04

		-1.25E+00		2.62E-01		2.62E-04

		-1.26E+00		2.61E-01		2.61E-04

		-1.26E+00		2.61E-01		2.61E-04

		-1.27E+00		2.60E-01		2.60E-04

		-1.27E+00		2.59E-01		2.59E-04

		-1.27E+00		2.59E-01		2.59E-04

		-1.28E+00		2.58E-01		2.58E-04

		-1.28E+00		2.57E-01		2.57E-04

		-1.29E+00		2.57E-01		2.57E-04

		-1.29E+00		2.56E-01		2.56E-04

		-1.29E+00		2.56E-01		2.56E-04

		-1.30E+00		2.55E-01		2.55E-04

		-1.30E+00		2.55E-01		2.55E-04

		-1.31E+00		2.54E-01		2.54E-04

		-1.31E+00		2.54E-01		2.54E-04

		-1.31E+00		2.53E-01		2.53E-04

		-1.32E+00		2.52E-01		2.52E-04

		-1.32E+00		2.52E-01		2.52E-04

		-1.33E+00		2.51E-01		2.51E-04

		-1.33E+00		2.51E-01		2.51E-04

		-1.33E+00		2.50E-01		2.50E-04

		-1.34E+00		2.50E-01		2.50E-04

		-1.34E+00		2.50E-01		2.50E-04

		-1.35E+00		2.49E-01		2.49E-04

		-1.35E+00		2.49E-01		2.49E-04

		-1.35E+00		2.48E-01		2.48E-04

		-1.36E+00		2.48E-01		2.48E-04

		-1.36E+00		2.47E-01		2.47E-04

		-1.37E+00		2.46E-01		2.46E-04

		-1.37E+00		2.47E-01		2.47E-04

		-1.37E+00		2.46E-01		2.46E-04

		-1.38E+00		2.46E-01		2.46E-04

		-1.38E+00		2.46E-01		2.46E-04

		-1.39E+00		2.45E-01		2.45E-04

		-1.39E+00		2.45E-01		2.45E-04

		-1.39E+00		2.45E-01		2.45E-04

		-1.40E+00		2.45E-01		2.45E-04

		-1.40E+00		2.45E-01		2.45E-04

		-1.41E+00		2.45E-01		2.45E-04

		-1.41E+00		2.45E-01		2.45E-04

		-1.41E+00		2.45E-01		2.45E-04

		-1.42E+00		2.46E-01		2.46E-04

		-1.42E+00		2.46E-01		2.46E-04

		-1.43E+00		2.47E-01		2.47E-04

		-1.43E+00		2.47E-01		2.47E-04

		-1.43E+00		2.48E-01		2.48E-04

		-1.44E+00		2.49E-01		2.49E-04

		-1.44E+00		2.50E-01		2.50E-04

		-1.45E+00		2.51E-01		2.51E-04

		-1.45E+00		2.52E-01		2.52E-04

		-1.45E+00		2.54E-01		2.54E-04

		-1.46E+00		2.56E-01		2.56E-04

		-1.46E+00		2.57E-01		2.57E-04

		-1.47E+00		2.59E-01		2.59E-04

		-1.47E+00		2.60E-01		2.60E-04

		-1.47E+00		2.62E-01		2.62E-04

		-1.48E+00		2.64E-01		2.64E-04

		-1.48E+00		2.66E-01		2.66E-04

		-1.49E+00		2.68E-01		2.68E-04

		-1.49E+00		2.70E-01		2.70E-04

		-1.49E+00		2.72E-01		2.72E-04

		-1.50E+00		2.75E-01		2.75E-04

		-1.50E+00		2.77E-01		2.77E-04

		-1.51E+00		2.79E-01		2.79E-04

		-1.51E+00		2.81E-01		2.81E-04

		-1.51E+00		2.83E-01		2.83E-04

		-1.52E+00		2.86E-01		2.86E-04

		-1.52E+00		2.88E-01		2.88E-04

		-1.53E+00		2.90E-01		2.90E-04

		-1.53E+00		2.93E-01		2.93E-04

		-1.53E+00		2.95E-01		2.95E-04

		-1.54E+00		2.97E-01		2.97E-04

		-1.54E+00		3.00E-01		3.00E-04

		-1.55E+00		3.02E-01		3.02E-04

		-1.55E+00		3.04E-01		3.04E-04

		-1.55E+00		3.07E-01		3.07E-04

		-1.56E+00		3.09E-01		3.09E-04

		-1.56E+00		3.11E-01		3.11E-04

		-1.57E+00		3.14E-01		3.14E-04

		-1.57E+00		3.16E-01		3.16E-04

		-1.57E+00		3.18E-01		3.18E-04

		-1.58E+00		3.20E-01		3.20E-04

		-1.58E+00		3.23E-01		3.23E-04

		-1.59E+00		3.25E-01		3.25E-04

		-1.59E+00		3.27E-01		3.27E-04

		-1.59E+00		3.29E-01		3.29E-04

		-1.60E+00		3.31E-01		3.31E-04

		-1.60E+00		3.34E-01		3.34E-04

		-1.61E+00		3.36E-01		3.36E-04

		-1.61E+00		3.38E-01		3.38E-04

		-1.61E+00		3.40E-01		3.40E-04

		-1.62E+00		3.42E-01		3.42E-04

		-1.62E+00		3.44E-01		3.44E-04

		-1.63E+00		3.46E-01		3.46E-04

		-1.63E+00		3.47E-01		3.47E-04

		-1.63E+00		3.49E-01		3.49E-04

		-1.64E+00		3.50E-01		3.50E-04

		-1.64E+00		3.53E-01		3.53E-04

		-1.65E+00		3.54E-01		3.54E-04

		-1.65E+00		3.55E-01		3.55E-04

		-1.65E+00		3.57E-01		3.57E-04

		-1.66E+00		3.58E-01		3.58E-04

		-1.66E+00		3.59E-01		3.59E-04

		-1.67E+00		3.60E-01		3.60E-04

		-1.67E+00		3.61E-01		3.61E-04

		-1.67E+00		3.62E-01		3.62E-04

		-1.68E+00		3.63E-01		3.63E-04

		-1.68E+00		3.64E-01		3.64E-04

		-1.69E+00		3.64E-01		3.64E-04

		-1.69E+00		3.65E-01		3.65E-04

		-1.69E+00		3.65E-01		3.65E-04

		-1.70E+00		3.65E-01		3.65E-04

		-1.70E+00		3.65E-01		3.65E-04

		-1.71E+00		3.65E-01		3.65E-04

		-1.71E+00		3.65E-01		3.65E-04

		-1.71E+00		3.64E-01		3.64E-04

		-1.72E+00		3.64E-01		3.64E-04

		-1.72E+00		3.63E-01		3.63E-04

		-1.73E+00		3.62E-01		3.62E-04

		-1.73E+00		3.61E-01		3.61E-04

		-1.73E+00		3.59E-01		3.59E-04

		-1.74E+00		3.58E-01		3.58E-04

		-1.74E+00		3.55E-01		3.55E-04

		-1.75E+00		3.53E-01		3.53E-04

		-1.75E+00		3.50E-01		3.50E-04

		-1.75E+00		3.47E-01		3.47E-04

		-1.76E+00		3.43E-01		3.43E-04

		-1.76E+00		3.39E-01		3.39E-04

		-1.77E+00		3.35E-01		3.35E-04

		-1.77E+00		3.31E-01		3.31E-04

		-1.77E+00		3.25E-01		3.25E-04

		-1.78E+00		3.21E-01		3.21E-04

		-1.78E+00		3.15E-01		3.15E-04

		-1.79E+00		3.09E-01		3.09E-04

		-1.79E+00		3.02E-01		3.02E-04

		-1.79E+00		2.97E-01		2.97E-04

		-1.80E+00		2.90E-01		2.90E-04

		-1.80E+00		2.83E-01		2.83E-04

		-1.81E+00		2.77E-01		2.77E-04

		-1.81E+00		2.70E-01		2.70E-04

		-1.81E+00		2.63E-01		2.63E-04

		-1.82E+00		2.56E-01		2.56E-04

		-1.82E+00		2.49E-01		2.49E-04

		-1.83E+00		2.43E-01		2.43E-04

		-1.83E+00		2.35E-01		2.35E-04

		-1.83E+00		2.29E-01		2.29E-04

		-1.84E+00		2.22E-01		2.22E-04

		-1.84E+00		2.16E-01		2.16E-04

		-1.85E+00		2.10E-01		2.10E-04

		-1.85E+00		2.03E-01		2.03E-04

		-1.85E+00		1.98E-01		1.98E-04

		-1.86E+00		1.91E-01		1.91E-04

		-1.86E+00		1.86E-01		1.86E-04

		-1.87E+00		1.80E-01		1.80E-04

		-1.87E+00		1.74E-01		1.74E-04

		-1.87E+00		1.69E-01		1.69E-04

		-1.88E+00		1.63E-01		1.63E-04

		-1.88E+00		1.59E-01		1.59E-04

		-1.89E+00		1.54E-01		1.54E-04

		-1.89E+00		1.49E-01		1.49E-04

		-1.89E+00		1.45E-01		1.45E-04

		-1.90E+00		1.40E-01		1.40E-04

		-1.90E+00		1.36E-01		1.36E-04

		-1.91E+00		1.31E-01		1.31E-04

		-1.91E+00		1.27E-01		1.27E-04

		-1.91E+00		1.23E-01		1.23E-04

		-1.92E+00		1.19E-01		1.19E-04

		-1.92E+00		1.15E-01		1.15E-04

		-1.93E+00		1.11E-01		1.11E-04

		-1.93E+00		1.07E-01		1.07E-04

		-1.93E+00		1.03E-01		1.03E-04

		-1.94E+00		9.96E-02		9.96E-05

		-1.94E+00		9.61E-02		9.61E-05

		-1.95E+00		9.29E-02		9.29E-05

		-1.95E+00		9.00E-02		9.00E-05

		-1.95E+00		8.70E-02		8.70E-05

		-1.96E+00		8.41E-02		8.41E-05

		-1.96E+00		8.15E-02		8.15E-05

		-1.97E+00		7.89E-02		7.89E-05

		-1.97E+00		7.64E-02		7.64E-05

		-1.97E+00		7.39E-02		7.39E-05

		-1.98E+00		7.17E-02		7.17E-05

		-1.98E+00		6.94E-02		6.94E-05

		-1.99E+00		6.72E-02		6.72E-05

		-1.99E+00		6.53E-02		6.53E-05

		-1.99E+00		6.30E-02		6.30E-05

		-2.00E+00		6.11E-02		6.11E-05

		-2.00E+00		5.92E-02		5.92E-05

		-2.00E+00		5.72E-02		5.72E-05

		-1.99E+00		5.57E-02		5.57E-05

		-1.99E+00		5.38E-02		5.38E-05

		-1.99E+00		5.23E-02		5.23E-05

		-1.98E+00		5.07E-02		5.07E-05

		-1.98E+00		4.92E-02		4.92E-05

		-1.97E+00		4.80E-02		4.80E-05

		-1.97E+00		4.66E-02		4.66E-05

		-1.97E+00		4.57E-02		4.57E-05

		-1.96E+00		4.45E-02		4.45E-05

		-1.96E+00		4.35E-02		4.35E-05

		-1.95E+00		4.27E-02		4.27E-05

		-1.95E+00		4.18E-02		4.18E-05

		-1.95E+00		4.12E-02		4.12E-05

		-1.94E+00		4.03E-02		4.03E-05

		-1.94E+00		3.99E-02		3.99E-05

		-1.93E+00		3.95E-02		3.95E-05

		-1.93E+00		3.92E-02		3.92E-05

		-1.93E+00		3.93E-02		3.93E-05

		-1.92E+00		3.90E-02		3.90E-05

		-1.92E+00		3.94E-02		3.94E-05

		-1.91E+00		3.97E-02		3.97E-05

		-1.91E+00		4.00E-02		4.00E-05

		-1.91E+00		4.07E-02		4.07E-05

		-1.90E+00		4.10E-02		4.10E-05

		-1.90E+00		4.15E-02		4.15E-05

		-1.89E+00		4.18E-02		4.18E-05

		-1.89E+00		4.23E-02		4.23E-05

		-1.89E+00		4.26E-02		4.26E-05

		-1.88E+00		4.28E-02		4.28E-05

		-1.88E+00		4.33E-02		4.33E-05

		-1.87E+00		4.38E-02		4.38E-05

		-1.87E+00		4.40E-02		4.40E-05

		-1.87E+00		4.45E-02		4.45E-05

		-1.86E+00		4.46E-02		4.46E-05

		-1.86E+00		4.54E-02		4.54E-05

		-1.85E+00		4.57E-02		4.57E-05

		-1.85E+00		4.60E-02		4.60E-05

		-1.85E+00		4.64E-02		4.64E-05

		-1.84E+00		4.66E-02		4.66E-05

		-1.84E+00		4.73E-02		4.73E-05

		-1.83E+00		4.75E-02		4.75E-05

		-1.83E+00		4.78E-02		4.78E-05

		-1.83E+00		4.81E-02		4.81E-05

		-1.82E+00		4.83E-02		4.83E-05

		-1.82E+00		4.87E-02		4.87E-05

		-1.81E+00		4.91E-02		4.91E-05

		-1.81E+00		4.95E-02		4.95E-05

		-1.81E+00		4.98E-02		4.98E-05

		-1.80E+00		5.01E-02		5.01E-05

		-1.80E+00		5.04E-02		5.04E-05

		-1.79E+00		5.08E-02		5.08E-05

		-1.79E+00		5.11E-02		5.11E-05

		-1.79E+00		5.13E-02		5.13E-05

		-1.78E+00		5.16E-02		5.16E-05

		-1.78E+00		5.21E-02		5.21E-05

		-1.77E+00		5.24E-02		5.24E-05

		-1.77E+00		5.27E-02		5.27E-05

		-1.77E+00		5.30E-02		5.30E-05

		-1.76E+00		5.34E-02		5.34E-05

		-1.76E+00		5.36E-02		5.36E-05

		-1.75E+00		5.41E-02		5.41E-05

		-1.75E+00		5.42E-02		5.42E-05

		-1.75E+00		5.46E-02		5.46E-05

		-1.74E+00		5.51E-02		5.51E-05

		-1.74E+00		5.54E-02		5.54E-05

		-1.73E+00		5.58E-02		5.58E-05

		-1.73E+00		5.62E-02		5.62E-05

		-1.73E+00		5.66E-02		5.66E-05

		-1.72E+00		5.73E-02		5.73E-05

		-1.72E+00		5.77E-02		5.77E-05

		-1.71E+00		5.83E-02		5.83E-05

		-1.71E+00		5.86E-02		5.86E-05

		-1.71E+00		5.92E-02		5.92E-05

		-1.70E+00		5.98E-02		5.98E-05

		-1.70E+00		6.02E-02		6.02E-05

		-1.69E+00		6.10E-02		6.10E-05

		-1.69E+00		6.14E-02		6.14E-05

		-1.69E+00		6.21E-02		6.21E-05

		-1.68E+00		6.25E-02		6.25E-05

		-1.68E+00		6.31E-02		6.31E-05

		-1.67E+00		6.36E-02		6.36E-05

		-1.67E+00		6.41E-02		6.41E-05

		-1.67E+00		6.48E-02		6.48E-05

		-1.66E+00		6.51E-02		6.51E-05

		-1.66E+00		6.57E-02		6.57E-05

		-1.65E+00		6.62E-02		6.62E-05

		-1.65E+00		6.66E-02		6.66E-05

		-1.65E+00		6.71E-02		6.71E-05

		-1.64E+00		6.75E-02		6.75E-05

		-1.64E+00		6.80E-02		6.80E-05

		-1.63E+00		6.83E-02		6.83E-05

		-1.63E+00		6.85E-02		6.85E-05

		-1.63E+00		6.90E-02		6.90E-05

		-1.62E+00		6.92E-02		6.92E-05

		-1.62E+00		6.97E-02		6.97E-05

		-1.61E+00		6.99E-02		6.99E-05

		-1.61E+00		7.02E-02		7.02E-05

		-1.61E+00		7.06E-02		7.06E-05

		-1.60E+00		7.06E-02		7.06E-05

		-1.60E+00		7.10E-02		7.10E-05

		-1.59E+00		7.13E-02		7.13E-05

		-1.59E+00		7.16E-02		7.16E-05

		-1.59E+00		7.20E-02		7.20E-05

		-1.58E+00		7.24E-02		7.24E-05

		-1.58E+00		7.30E-02		7.30E-05

		-1.57E+00		7.33E-02		7.33E-05

		-1.57E+00		7.39E-02		7.39E-05

		-1.57E+00		7.46E-02		7.46E-05

		-1.56E+00		7.53E-02		7.53E-05

		-1.56E+00		7.62E-02		7.62E-05

		-1.55E+00		7.70E-02		7.70E-05

		-1.55E+00		7.78E-02		7.78E-05

		-1.55E+00		7.88E-02		7.88E-05

		-1.54E+00		7.98E-02		7.98E-05

		-1.54E+00		8.09E-02		8.09E-05

		-1.53E+00		8.20E-02		8.20E-05

		-1.53E+00		8.33E-02		8.33E-05

		-1.53E+00		8.45E-02		8.45E-05

		-1.52E+00		8.60E-02		8.60E-05

		-1.52E+00		8.74E-02		8.74E-05

		-1.51E+00		8.89E-02		8.89E-05

		-1.51E+00		9.04E-02		9.04E-05

		-1.51E+00		9.18E-02		9.18E-05

		-1.50E+00		9.34E-02		9.34E-05

		-1.50E+00		9.50E-02		9.50E-05

		-1.49E+00		9.66E-02		9.66E-05

		-1.49E+00		9.82E-02		9.82E-05

		-1.49E+00		1.00E-01		1.00E-04

		-1.48E+00		1.02E-01		1.02E-04

		-1.48E+00		1.03E-01		1.03E-04

		-1.47E+00		1.05E-01		1.05E-04

		-1.47E+00		1.07E-01		1.07E-04

		-1.47E+00		1.09E-01		1.09E-04

		-1.46E+00		1.11E-01		1.11E-04

		-1.46E+00		1.12E-01		1.12E-04

		-1.45E+00		1.14E-01		1.14E-04

		-1.45E+00		1.16E-01		1.16E-04

		-1.45E+00		1.18E-01		1.18E-04

		-1.44E+00		1.19E-01		1.19E-04

		-1.44E+00		1.21E-01		1.21E-04

		-1.43E+00		1.23E-01		1.23E-04

		-1.43E+00		1.24E-01		1.24E-04

		-1.43E+00		1.26E-01		1.26E-04

		-1.42E+00		1.27E-01		1.27E-04

		-1.42E+00		1.28E-01		1.28E-04

		-1.41E+00		1.30E-01		1.30E-04

		-1.41E+00		1.31E-01		1.31E-04

		-1.41E+00		1.32E-01		1.32E-04

		-1.40E+00		1.34E-01		1.34E-04

		-1.40E+00		1.35E-01		1.35E-04

		-1.39E+00		1.36E-01		1.36E-04

		-1.39E+00		1.37E-01		1.37E-04

		-1.39E+00		1.38E-01		1.38E-04

		-1.38E+00		1.39E-01		1.39E-04

		-1.38E+00		1.40E-01		1.40E-04

		-1.37E+00		1.41E-01		1.41E-04

		-1.37E+00		1.41E-01		1.41E-04

		-1.37E+00		1.42E-01		1.42E-04

		-1.36E+00		1.43E-01		1.43E-04

		-1.36E+00		1.44E-01		1.44E-04

		-1.35E+00		1.44E-01		1.44E-04

		-1.35E+00		1.45E-01		1.45E-04

		-1.35E+00		1.45E-01		1.45E-04

		-1.34E+00		1.45E-01		1.45E-04

		-1.34E+00		1.46E-01		1.46E-04

		-1.33E+00		1.46E-01		1.46E-04

		-1.33E+00		1.47E-01		1.47E-04

		-1.33E+00		1.47E-01		1.47E-04

		-1.32E+00		1.47E-01		1.47E-04

		-1.32E+00		1.47E-01		1.47E-04

		-1.31E+00		1.48E-01		1.48E-04

		-1.31E+00		1.48E-01		1.48E-04

		-1.31E+00		1.48E-01		1.48E-04

		-1.30E+00		1.48E-01		1.48E-04

		-1.30E+00		1.48E-01		1.48E-04

		-1.29E+00		1.48E-01		1.48E-04

		-1.29E+00		1.48E-01		1.48E-04

		-1.29E+00		1.48E-01		1.48E-04

		-1.28E+00		1.48E-01		1.48E-04

		-1.28E+00		1.48E-01		1.48E-04

		-1.27E+00		1.48E-01		1.48E-04

		-1.27E+00		1.48E-01		1.48E-04

		-1.27E+00		1.48E-01		1.48E-04

		-1.26E+00		1.48E-01		1.48E-04

		-1.26E+00		1.48E-01		1.48E-04

		-1.25E+00		1.48E-01		1.48E-04

		-1.25E+00		1.48E-01		1.48E-04

		-1.25E+00		1.48E-01		1.48E-04

		-1.24E+00		1.48E-01		1.48E-04

		-1.24E+00		1.48E-01		1.48E-04

		-1.23E+00		1.47E-01		1.47E-04

		-1.23E+00		1.47E-01		1.47E-04

		-1.23E+00		1.47E-01		1.47E-04

		-1.22E+00		1.47E-01		1.47E-04

		-1.22E+00		1.47E-01		1.47E-04

		-1.21E+00		1.47E-01		1.47E-04

		-1.21E+00		1.47E-01		1.47E-04

		-1.21E+00		1.47E-01		1.47E-04

		-1.20E+00		1.47E-01		1.47E-04

		-1.20E+00		1.47E-01		1.47E-04

		-1.19E+00		1.46E-01		1.46E-04

		-1.19E+00		1.46E-01		1.46E-04

		-1.19E+00		1.46E-01		1.46E-04

		-1.18E+00		1.46E-01		1.46E-04

		-1.18E+00		1.46E-01		1.46E-04

		-1.17E+00		1.46E-01		1.46E-04

		-1.17E+00		1.46E-01		1.46E-04

		-1.17E+00		1.46E-01		1.46E-04

		-1.16E+00		1.46E-01		1.46E-04

		-1.16E+00		1.45E-01		1.45E-04

		-1.15E+00		1.46E-01		1.46E-04

		-1.15E+00		1.45E-01		1.45E-04

		-1.15E+00		1.45E-01		1.45E-04

		-1.14E+00		1.45E-01		1.45E-04

		-1.14E+00		1.45E-01		1.45E-04

		-1.13E+00		1.45E-01		1.45E-04

		-1.13E+00		1.45E-01		1.45E-04

		-1.13E+00		1.45E-01		1.45E-04

		-1.12E+00		1.45E-01		1.45E-04

		-1.12E+00		1.45E-01		1.45E-04

		-1.11E+00		1.45E-01		1.45E-04

		-1.11E+00		1.44E-01		1.44E-04

		-1.11E+00		1.44E-01		1.44E-04

		-1.10E+00		1.44E-01		1.44E-04

		-1.10E+00		1.44E-01		1.44E-04

		-1.09E+00		1.44E-01		1.44E-04

		-1.09E+00		1.44E-01		1.44E-04

		-1.09E+00		1.44E-01		1.44E-04

		-1.08E+00		1.44E-01		1.44E-04

		-1.08E+00		1.44E-01		1.44E-04

		-1.07E+00		1.43E-01		1.43E-04

		-1.07E+00		1.43E-01		1.43E-04

		-1.07E+00		1.43E-01		1.43E-04

		-1.06E+00		1.43E-01		1.43E-04

		-1.06E+00		1.43E-01		1.43E-04

		-1.05E+00		1.43E-01		1.43E-04

		-1.05E+00		1.42E-01		1.42E-04

		-1.05E+00		1.42E-01		1.42E-04

		-1.04E+00		1.42E-01		1.42E-04

		-1.04E+00		1.42E-01		1.42E-04

		-1.03E+00		1.42E-01		1.42E-04

		-1.03E+00		1.42E-01		1.42E-04

		-1.03E+00		1.41E-01		1.41E-04

		-1.02E+00		1.41E-01		1.41E-04

		-1.02E+00		1.41E-01		1.41E-04

		-1.01E+00		1.41E-01		1.41E-04

		-1.01E+00		1.41E-01		1.41E-04

		-1.01E+00		1.40E-01		1.40E-04

		-1.00E+00		1.40E-01		1.40E-04

		-9.97E-01		1.40E-01		1.40E-04

		-9.93E-01		1.40E-01		1.40E-04

		-9.89E-01		1.40E-01		1.40E-04

		-9.85E-01		1.39E-01		1.39E-04

		-9.81E-01		1.39E-01		1.39E-04

		-9.77E-01		1.39E-01		1.39E-04

		-9.73E-01		1.39E-01		1.39E-04

		-9.69E-01		1.39E-01		1.39E-04

		-9.65E-01		1.39E-01		1.39E-04

		-9.61E-01		1.39E-01		1.39E-04

		-9.57E-01		1.38E-01		1.38E-04

		-9.53E-01		1.38E-01		1.38E-04

		-9.49E-01		1.38E-01		1.38E-04

		-9.45E-01		1.38E-01		1.38E-04

		-9.41E-01		1.38E-01		1.38E-04

		-9.37E-01		1.38E-01		1.38E-04

		-9.33E-01		1.38E-01		1.38E-04

		-9.29E-01		1.38E-01		1.38E-04

		-9.25E-01		1.38E-01		1.38E-04

		-9.21E-01		1.39E-01		1.39E-04

		-9.17E-01		1.39E-01		1.39E-04

		-9.13E-01		1.39E-01		1.39E-04

		-9.09E-01		1.39E-01		1.39E-04

		-9.05E-01		1.39E-01		1.39E-04

		-9.01E-01		1.39E-01		1.39E-04

		-8.97E-01		1.39E-01		1.39E-04

		-8.93E-01		1.40E-01		1.40E-04

		-8.89E-01		1.40E-01		1.40E-04

		-8.85E-01		1.40E-01		1.40E-04

		-8.81E-01		1.40E-01		1.40E-04

		-8.77E-01		1.40E-01		1.40E-04

		-8.73E-01		1.41E-01		1.41E-04

		-8.69E-01		1.41E-01		1.41E-04

		-8.65E-01		1.41E-01		1.41E-04

		-8.61E-01		1.41E-01		1.41E-04

		-8.57E-01		1.41E-01		1.41E-04

		-8.53E-01		1.42E-01		1.42E-04

		-8.49E-01		1.42E-01		1.42E-04

		-8.45E-01		1.42E-01		1.42E-04

		-8.41E-01		1.42E-01		1.42E-04

		-8.37E-01		1.42E-01		1.42E-04

		-8.33E-01		1.43E-01		1.43E-04

		-8.29E-01		1.43E-01		1.43E-04

		-8.25E-01		1.43E-01		1.43E-04

		-8.21E-01		1.43E-01		1.43E-04

		-8.17E-01		1.44E-01		1.44E-04

		-8.13E-01		1.44E-01		1.44E-04

		-8.09E-01		1.44E-01		1.44E-04

		-8.05E-01		1.44E-01		1.44E-04

		-8.01E-01		1.45E-01		1.45E-04

		-7.97E-01		1.45E-01		1.45E-04

		-7.93E-01		1.45E-01		1.45E-04

		-7.89E-01		1.45E-01		1.45E-04

		-7.85E-01		1.45E-01		1.45E-04

		-7.81E-01		1.45E-01		1.45E-04

		-7.77E-01		1.45E-01		1.45E-04

		-7.73E-01		1.45E-01		1.45E-04

		-7.69E-01		1.45E-01		1.45E-04

		-7.65E-01		1.46E-01		1.46E-04

		-7.61E-01		1.45E-01		1.45E-04

		-7.57E-01		1.45E-01		1.45E-04

		-7.53E-01		1.45E-01		1.45E-04

		-7.49E-01		1.45E-01		1.45E-04

		-7.45E-01		1.45E-01		1.45E-04

		-7.41E-01		1.44E-01		1.44E-04

		-7.37E-01		1.44E-01		1.44E-04

		-7.33E-01		1.43E-01		1.43E-04

		-7.29E-01		1.43E-01		1.43E-04

		-7.25E-01		1.42E-01		1.42E-04

		-7.21E-01		1.41E-01		1.41E-04

		-7.17E-01		1.40E-01		1.40E-04

		-7.13E-01		1.39E-01		1.39E-04

		-7.09E-01		1.38E-01		1.38E-04

		-7.05E-01		1.37E-01		1.37E-04

		-7.01E-01		1.36E-01		1.36E-04

		-6.97E-01		1.35E-01		1.35E-04

		-6.93E-01		1.34E-01		1.34E-04

		-6.89E-01		1.33E-01		1.33E-04

		-6.85E-01		1.32E-01		1.32E-04

		-6.81E-01		1.31E-01		1.31E-04

		-6.77E-01		1.30E-01		1.30E-04

		-6.73E-01		1.29E-01		1.29E-04

		-6.69E-01		1.28E-01		1.28E-04

		-6.65E-01		1.28E-01		1.28E-04

		-6.61E-01		1.27E-01		1.27E-04

		-6.57E-01		1.27E-01		1.27E-04

		-6.53E-01		1.26E-01		1.26E-04

		-6.49E-01		1.26E-01		1.26E-04

		-6.45E-01		1.25E-01		1.25E-04

		-6.41E-01		1.25E-01		1.25E-04

		-6.37E-01		1.25E-01		1.25E-04

		-6.33E-01		1.24E-01		1.24E-04

		-6.29E-01		1.24E-01		1.24E-04

		-6.25E-01		1.24E-01		1.24E-04

		-6.21E-01		1.24E-01		1.24E-04

		-6.17E-01		1.24E-01		1.24E-04

		-6.13E-01		1.24E-01		1.24E-04

		-6.09E-01		1.23E-01		1.23E-04

		-6.05E-01		1.23E-01		1.23E-04

		-6.01E-01		1.23E-01		1.23E-04

		-5.97E-01		1.23E-01		1.23E-04

		-5.93E-01		1.23E-01		1.23E-04

		-5.89E-01		1.23E-01		1.23E-04

		-5.85E-01		1.23E-01		1.23E-04

		-5.81E-01		1.23E-01		1.23E-04

		-5.77E-01		1.23E-01		1.23E-04

		-5.73E-01		1.23E-01		1.23E-04

		-5.69E-01		1.23E-01		1.23E-04

		-5.65E-01		1.23E-01		1.23E-04

		-5.61E-01		1.23E-01		1.23E-04

		-5.57E-01		1.23E-01		1.23E-04

		-5.53E-01		1.23E-01		1.23E-04

		-5.49E-01		1.23E-01		1.23E-04

		-5.45E-01		1.23E-01		1.23E-04

		-5.41E-01		1.23E-01		1.23E-04

		-5.37E-01		1.23E-01		1.23E-04

		-5.33E-01		1.23E-01		1.23E-04

		-5.29E-01		1.23E-01		1.23E-04

		-5.25E-01		1.24E-01		1.24E-04

		-5.21E-01		1.24E-01		1.24E-04

		-5.17E-01		1.24E-01		1.24E-04

		-5.13E-01		1.25E-01		1.25E-04

		-5.09E-01		1.25E-01		1.25E-04

		-5.05E-01		1.25E-01		1.25E-04

		-5.01E-01		1.26E-01		1.26E-04

		-4.97E-01		1.26E-01		1.26E-04

		-4.93E-01		1.27E-01		1.27E-04

		-4.89E-01		1.28E-01		1.28E-04

		-4.85E-01		1.29E-01		1.29E-04

		-4.81E-01		1.30E-01		1.30E-04

		-4.77E-01		1.32E-01		1.32E-04

		-4.73E-01		1.34E-01		1.34E-04

		-4.69E-01		1.36E-01		1.36E-04

		-4.65E-01		1.37E-01		1.37E-04

		-4.61E-01		1.37E-01		1.37E-04

		-4.57E-01		1.36E-01		1.36E-04

		-4.53E-01		1.34E-01		1.34E-04

		-4.49E-01		1.31E-01		1.31E-04

		-4.45E-01		1.27E-01		1.27E-04

		-4.41E-01		1.24E-01		1.24E-04

		-4.37E-01		1.20E-01		1.20E-04

		-4.33E-01		1.16E-01		1.16E-04

		-4.29E-01		1.12E-01		1.12E-04

		-4.25E-01		1.08E-01		1.08E-04

		-4.21E-01		1.03E-01		1.03E-04

		-4.17E-01		9.91E-02		9.91E-05

		-4.13E-01		9.47E-02		9.47E-05

		-4.09E-01		9.04E-02		9.04E-05

		-4.05E-01		8.59E-02		8.59E-05

		-4.01E-01		8.13E-02		8.13E-05

		-3.97E-01		7.69E-02		7.69E-05

		-3.93E-01		7.22E-02		7.22E-05

		-3.89E-01		6.79E-02		6.79E-05

		-3.85E-01		6.34E-02		6.34E-05

		-3.81E-01		5.92E-02		5.92E-05

		-3.77E-01		5.52E-02		5.52E-05

		-3.73E-01		5.10E-02		5.10E-05

		-3.69E-01		4.75E-02		4.75E-05

		-3.65E-01		4.37E-02		4.37E-05

		-3.61E-01		4.03E-02		4.03E-05

		-3.57E-01		3.67E-02		3.67E-05

		-3.53E-01		3.30E-02		3.30E-05

		-3.49E-01		2.94E-02		2.94E-05

		-3.45E-01		2.56E-02		2.56E-05

		-3.41E-01		2.19E-02		2.19E-05

		-3.37E-01		1.81E-02		1.81E-05

		-3.33E-01		1.44E-02		1.44E-05

		-3.29E-01		1.08E-02		1.08E-05

		-3.25E-01		7.10E-03		7.10E-06

		-3.21E-01		3.50E-03		3.50E-06

		-3.17E-01		-1.80E-04		-1.80E-07

		-3.13E-01		-3.85E-03		-3.85E-06

		-3.09E-01		-7.36E-03		-7.36E-06

		-3.05E-01		-1.09E-02		-1.09E-05

		-3.01E-01		-1.44E-02		-1.44E-05

		-2.97E-01		-1.79E-02		-1.79E-05

		-2.93E-01		-2.13E-02		-2.13E-05

		-2.89E-01		-2.45E-02		-2.45E-05

		-2.85E-01		-2.79E-02		-2.79E-05

		-2.81E-01		-3.11E-02		-3.11E-05

		-2.77E-01		-3.43E-02		-3.43E-05

		-2.73E-01		-3.72E-02		-3.72E-05

		-2.69E-01		-4.02E-02		-4.02E-05

		-2.65E-01		-4.32E-02		-4.32E-05

		-2.61E-01		-4.60E-02		-4.60E-05

		-2.57E-01		-4.88E-02		-4.88E-05

		-2.53E-01		-5.14E-02		-5.14E-05

		-2.49E-01		-5.40E-02		-5.40E-05

		-2.45E-01		-5.65E-02		-5.65E-05

		-2.41E-01		-5.88E-02		-5.88E-05

		-2.37E-01		-6.11E-02		-6.11E-05

		-2.33E-01		-6.30E-02		-6.30E-05

		-2.29E-01		-6.50E-02		-6.50E-05

		-2.25E-01		-6.68E-02		-6.68E-05

		-2.21E-01		-6.84E-02		-6.84E-05

		-2.17E-01		-6.99E-02		-6.99E-05

		-2.13E-01		-7.11E-02		-7.11E-05

		-2.09E-01		-7.21E-02		-7.21E-05

		-2.05E-01		-7.28E-02		-7.28E-05

		-2.01E-01		-7.34E-02		-7.34E-05

		-1.97E-01		-7.38E-02		-7.38E-05

		-1.93E-01		-7.38E-02		-7.38E-05

		-1.89E-01		-7.37E-02		-7.37E-05

		-1.85E-01		-7.34E-02		-7.34E-05

		-1.81E-01		-7.32E-02		-7.32E-05

		-1.77E-01		-7.29E-02		-7.29E-05

		-1.73E-01		-7.26E-02		-7.26E-05

		-1.69E-01		-7.22E-02		-7.22E-05

		-1.65E-01		-7.19E-02		-7.19E-05

		-1.61E-01		-7.19E-02		-7.19E-05

		-1.57E-01		-7.19E-02		-7.19E-05

		-1.53E-01		-7.22E-02		-7.22E-05

		-1.49E-01		-7.24E-02		-7.24E-05

		-1.45E-01		-7.29E-02		-7.29E-05

		-1.41E-01		-7.37E-02		-7.37E-05

		-1.37E-01		-7.44E-02		-7.44E-05

		-1.33E-01		-7.55E-02		-7.55E-05

		-1.29E-01		-7.64E-02		-7.64E-05

		-1.25E-01		-7.76E-02		-7.76E-05

		-1.21E-01		-7.90E-02		-7.90E-05

		-1.17E-01		-8.03E-02		-8.03E-05

		-1.13E-01		-8.18E-02		-8.18E-05

		-1.09E-01		-8.31E-02		-8.31E-05

		-1.05E-01		-8.49E-02		-8.49E-05

		-1.01E-01		-8.67E-02		-8.67E-05

		-9.70E-02		-8.84E-02		-8.84E-05

		-9.30E-02		-9.03E-02		-9.03E-05

		-8.90E-02		-9.20E-02		-9.20E-05

		-8.50E-02		-9.41E-02		-9.41E-05

		-8.10E-02		-9.60E-02		-9.60E-05

		-7.70E-02		-9.82E-02		-9.82E-05

		-7.30E-02		-1.00E-01		-1.00E-04

		-6.90E-02		-1.02E-01		-1.02E-04

		-6.50E-02		-1.05E-01		-1.05E-04

		-6.10E-02		-1.07E-01		-1.07E-04

		-5.70E-02		-1.09E-01		-1.09E-04

		-5.30E-02		-1.11E-01		-1.11E-04

		-4.90E-02		-1.13E-01		-1.13E-04

		-4.50E-02		-1.16E-01		-1.16E-04

		-4.10E-02		-1.18E-01		-1.18E-04

		-3.70E-02		-1.21E-01		-1.21E-04

		-3.30E-02		-1.23E-01		-1.23E-04

		-2.90E-02		-1.26E-01		-1.26E-04

		-2.50E-02		-1.28E-01		-1.28E-04

		-2.10E-02		-1.31E-01		-1.31E-04

		-1.70E-02		-1.33E-01		-1.33E-04

		-1.30E-02		-1.36E-01		-1.36E-04

		-9.01E-03		-1.39E-01		-1.39E-04

		-5.01E-03		-1.41E-01		-1.41E-04

		-1.01E-03		-1.44E-01		-1.44E-04

		2.99E-03		-1.47E-01		-1.47E-04

		6.99E-03		-1.50E-01		-1.50E-04

		1.10E-02		-1.53E-01		-1.53E-04

		1.50E-02		-1.56E-01		-1.56E-04

		1.90E-02		-1.58E-01		-1.58E-04

		2.30E-02		-1.62E-01		-1.62E-04

		2.70E-02		-1.65E-01		-1.65E-04

		3.10E-02		-1.68E-01		-1.68E-04

		3.50E-02		-1.71E-01		-1.71E-04

		3.90E-02		-1.74E-01		-1.74E-04

		4.30E-02		-1.78E-01		-1.78E-04

		4.70E-02		-1.81E-01		-1.81E-04

		5.10E-02		-1.84E-01		-1.84E-04

		5.50E-02		-1.87E-01		-1.87E-04

		5.90E-02		-1.91E-01		-1.91E-04

		6.30E-02		-1.94E-01		-1.94E-04

		6.70E-02		-1.98E-01		-1.98E-04

		7.10E-02		-2.01E-01		-2.01E-04

		7.50E-02		-2.05E-01		-2.05E-04

		7.90E-02		-2.09E-01		-2.09E-04

		8.30E-02		-2.12E-01		-2.12E-04

		8.70E-02		-2.16E-01		-2.16E-04

		9.10E-02		-2.19E-01		-2.19E-04

		9.50E-02		-2.23E-01		-2.23E-04

		9.90E-02		-2.27E-01		-2.27E-04

		1.03E-01		-2.31E-01		-2.31E-04

		1.07E-01		-2.35E-01		-2.35E-04

		1.11E-01		-2.38E-01		-2.38E-04

		1.15E-01		-2.42E-01		-2.42E-04

		1.19E-01		-2.46E-01		-2.46E-04

		1.23E-01		-2.50E-01		-2.50E-04

		1.27E-01		-2.55E-01		-2.55E-04

		1.31E-01		-2.58E-01		-2.58E-04

		1.35E-01		-2.63E-01		-2.63E-04

		1.39E-01		-2.67E-01		-2.67E-04

		1.43E-01		-2.71E-01		-2.71E-04

		1.47E-01		-2.75E-01		-2.75E-04

		1.51E-01		-2.79E-01		-2.79E-04

		1.55E-01		-2.83E-01		-2.83E-04

		1.59E-01		-2.88E-01		-2.88E-04

		1.63E-01		-2.92E-01		-2.92E-04

		1.67E-01		-2.97E-01		-2.97E-04

		1.71E-01		-3.00E-01		-3.00E-04

		1.75E-01		-3.05E-01		-3.05E-04

		1.79E-01		-3.10E-01		-3.10E-04

		1.83E-01		-3.14E-01		-3.14E-04

		1.87E-01		-3.19E-01		-3.19E-04

		1.91E-01		-3.23E-01		-3.23E-04

		1.95E-01		-3.28E-01		-3.28E-04

		1.99E-01		-3.32E-01		-3.32E-04

		2.03E-01		-3.37E-01		-3.37E-04

		2.07E-01		-3.41E-01		-3.41E-04

		2.11E-01		-3.45E-01		-3.45E-04

		2.15E-01		-3.51E-01		-3.51E-04

		2.19E-01		-3.55E-01		-3.55E-04

		2.23E-01		-3.60E-01		-3.60E-04

		2.27E-01		-3.64E-01		-3.64E-04

		2.31E-01		-3.69E-01		-3.69E-04

		2.35E-01		-3.74E-01		-3.74E-04

		2.39E-01		-3.78E-01		-3.78E-04

		2.43E-01		-3.83E-01		-3.83E-04

		2.47E-01		-3.88E-01		-3.88E-04

		2.51E-01		-3.92E-01		-3.92E-04

		2.55E-01		-3.97E-01		-3.97E-04

		2.59E-01		-4.01E-01		-4.01E-04

		2.63E-01		-4.06E-01		-4.06E-04

		2.67E-01		-4.11E-01		-4.11E-04

		2.71E-01		-4.15E-01		-4.15E-04

		2.75E-01		-4.20E-01		-4.20E-04

		2.79E-01		-4.24E-01		-4.24E-04

		2.83E-01		-4.29E-01		-4.29E-04

		2.87E-01		-4.34E-01		-4.34E-04

		2.91E-01		-4.38E-01		-4.38E-04

		2.95E-01		-4.43E-01		-4.43E-04

		2.99E-01		-4.47E-01		-4.47E-04

		3.03E-01		-4.52E-01		-4.52E-04

		3.07E-01		-4.56E-01		-4.56E-04

		3.11E-01		-4.60E-01		-4.60E-04

		3.15E-01		-4.65E-01		-4.65E-04

		3.19E-01		-4.69E-01		-4.69E-04

		3.23E-01		-4.73E-01		-4.73E-04

		3.27E-01		-4.77E-01		-4.77E-04

		3.31E-01		-4.81E-01		-4.81E-04

		3.35E-01		-4.84E-01		-4.84E-04

		3.39E-01		-4.88E-01		-4.88E-04

		3.43E-01		-4.92E-01		-4.92E-04

		3.47E-01		-4.95E-01		-4.95E-04

		3.51E-01		-4.98E-01		-4.98E-04

		3.55E-01		-5.00E-01		-5.00E-04

		3.59E-01		-5.03E-01		-5.03E-04

		3.63E-01		-5.05E-01		-5.05E-04

		3.67E-01		-5.08E-01		-5.08E-04

		3.71E-01		-5.09E-01		-5.09E-04

		3.75E-01		-5.11E-01		-5.11E-04

		3.79E-01		-5.13E-01		-5.13E-04

		3.83E-01		-5.14E-01		-5.14E-04

		3.87E-01		-5.15E-01		-5.15E-04

		3.91E-01		-5.15E-01		-5.15E-04

		3.95E-01		-5.16E-01		-5.16E-04

		3.99E-01		-5.16E-01		-5.16E-04

		4.03E-01		-5.16E-01		-5.16E-04

		4.07E-01		-5.15E-01		-5.15E-04

		4.11E-01		-5.13E-01		-5.13E-04

		4.15E-01		-5.12E-01		-5.12E-04

		4.19E-01		-5.10E-01		-5.10E-04

		4.23E-01		-5.07E-01		-5.07E-04

		4.27E-01		-5.03E-01		-5.03E-04

		4.31E-01		-4.98E-01		-4.98E-04

		4.35E-01		-4.92E-01		-4.92E-04

		4.39E-01		-4.85E-01		-4.85E-04

		4.43E-01		-4.77E-01		-4.77E-04

		4.47E-01		-4.68E-01		-4.68E-04

		4.51E-01		-4.58E-01		-4.58E-04

		4.55E-01		-4.51E-01		-4.51E-04

		4.59E-01		-4.44E-01		-4.44E-04

		4.63E-01		-4.38E-01		-4.38E-04

		4.67E-01		-4.33E-01		-4.33E-04

		4.71E-01		-4.29E-01		-4.29E-04

		4.75E-01		-4.25E-01		-4.25E-04

		4.79E-01		-4.22E-01		-4.22E-04

		4.83E-01		-4.20E-01		-4.20E-04

		4.87E-01		-4.19E-01		-4.19E-04

		4.91E-01		-4.17E-01		-4.17E-04

		4.95E-01		-4.16E-01		-4.16E-04

		4.99E-01		-4.15E-01		-4.15E-04

		5.03E-01		-4.15E-01		-4.15E-04

		5.07E-01		-4.16E-01		-4.16E-04

		5.11E-01		-4.16E-01		-4.16E-04

		5.15E-01		-4.17E-01		-4.17E-04

		5.19E-01		-4.18E-01		-4.18E-04

		5.23E-01		-4.19E-01		-4.19E-04

		5.27E-01		-4.21E-01		-4.21E-04

		5.31E-01		-4.22E-01		-4.22E-04

		5.35E-01		-4.24E-01		-4.24E-04

		5.39E-01		-4.26E-01		-4.26E-04

		5.43E-01		-4.28E-01		-4.28E-04

		5.47E-01		-4.31E-01		-4.31E-04

		5.51E-01		-4.33E-01		-4.33E-04

		5.55E-01		-4.36E-01		-4.36E-04

		5.59E-01		-4.38E-01		-4.38E-04

		5.63E-01		-4.41E-01		-4.41E-04

		5.67E-01		-4.44E-01		-4.44E-04

		5.71E-01		-4.47E-01		-4.47E-04

		5.75E-01		-4.50E-01		-4.50E-04

		5.79E-01		-4.54E-01		-4.54E-04

		5.83E-01		-4.57E-01		-4.57E-04

		5.87E-01		-4.60E-01		-4.60E-04

		5.91E-01		-4.63E-01		-4.63E-04

		5.95E-01		-4.67E-01		-4.67E-04

		5.99E-01		-4.71E-01		-4.71E-04

		6.03E-01		-4.75E-01		-4.75E-04

		6.07E-01		-4.78E-01		-4.78E-04

		6.11E-01		-4.82E-01		-4.82E-04

		6.15E-01		-4.86E-01		-4.86E-04

		6.19E-01		-4.89E-01		-4.89E-04

		6.23E-01		-4.93E-01		-4.93E-04

		6.27E-01		-4.97E-01		-4.97E-04

		6.31E-01		-5.01E-01		-5.01E-04

		6.35E-01		-5.05E-01		-5.05E-04

		6.39E-01		-5.10E-01		-5.10E-04

		6.43E-01		-5.14E-01		-5.14E-04

		6.47E-01		-5.18E-01		-5.18E-04

		6.51E-01		-5.22E-01		-5.22E-04

		6.55E-01		-5.26E-01		-5.26E-04

		6.59E-01		-5.31E-01		-5.31E-04

		6.63E-01		-5.35E-01		-5.35E-04

		6.67E-01		-5.39E-01		-5.39E-04

		6.71E-01		-5.44E-01		-5.44E-04

		6.75E-01		-5.48E-01		-5.48E-04

		6.79E-01		-5.53E-01		-5.53E-04

		6.83E-01		-5.57E-01		-5.57E-04

		6.87E-01		-5.62E-01		-5.62E-04

		6.91E-01		-5.66E-01		-5.66E-04

		6.95E-01		-5.71E-01		-5.71E-04

		6.99E-01		-5.76E-01		-5.76E-04

		7.03E-01		-5.81E-01		-5.81E-04

		7.07E-01		-5.86E-01		-5.86E-04

		7.11E-01		-5.90E-01		-5.90E-04

		7.15E-01		-5.95E-01		-5.95E-04

		7.19E-01		-6.00E-01		-6.00E-04

		7.23E-01		-6.04E-01		-6.04E-04

		7.27E-01		-6.09E-01		-6.09E-04

		7.31E-01		-6.13E-01		-6.13E-04

		7.35E-01		-6.19E-01		-6.19E-04

		7.39E-01		-6.24E-01		-6.24E-04

		7.43E-01		-6.29E-01		-6.29E-04

		7.47E-01		-6.34E-01		-6.34E-04

		7.51E-01		-6.38E-01		-6.38E-04

		7.55E-01		-6.43E-01		-6.43E-04

		7.59E-01		-6.48E-01		-6.48E-04

		7.63E-01		-6.53E-01		-6.53E-04

		7.67E-01		-6.58E-01		-6.58E-04

		7.71E-01		-6.63E-01		-6.63E-04

		7.75E-01		-6.68E-01		-6.68E-04

		7.79E-01		-6.73E-01		-6.73E-04

		7.83E-01		-6.78E-01		-6.78E-04

		7.87E-01		-6.83E-01		-6.83E-04

		7.91E-01		-6.88E-01		-6.88E-04

		7.95E-01		-6.93E-01		-6.93E-04

		7.99E-01		-6.98E-01		-6.98E-04

		8.03E-01		-7.03E-01		-7.03E-04

		8.07E-01		-7.09E-01		-7.09E-04

		8.11E-01		-7.13E-01		-7.13E-04

		8.15E-01		-7.19E-01		-7.19E-04

		8.19E-01		-7.24E-01		-7.24E-04

		8.23E-01		-7.30E-01		-7.30E-04

		8.27E-01		-7.34E-01		-7.34E-04

		8.31E-01		-7.39E-01		-7.39E-04

		8.35E-01		-7.45E-01		-7.45E-04

		8.39E-01		-7.50E-01		-7.50E-04

		8.43E-01		-7.56E-01		-7.56E-04

		8.47E-01		-7.60E-01		-7.60E-04

		8.51E-01		-7.66E-01		-7.66E-04

		8.55E-01		-7.71E-01		-7.71E-04

		8.59E-01		-7.76E-01		-7.76E-04

		8.63E-01		-7.82E-01		-7.82E-04

		8.67E-01		-7.87E-01		-7.87E-04

		8.71E-01		-7.92E-01		-7.92E-04

		8.75E-01		-7.97E-01		-7.97E-04

		8.79E-01		-8.02E-01		-8.02E-04

		8.83E-01		-8.08E-01		-8.08E-04

		8.87E-01		-8.13E-01		-8.13E-04

		8.91E-01		-8.18E-01		-8.18E-04

		8.95E-01		-8.23E-01		-8.23E-04

		8.99E-01		-8.29E-01		-8.29E-04

		9.03E-01		-8.34E-01		-8.34E-04

		9.07E-01		-8.39E-01		-8.39E-04

		9.11E-01		-8.45E-01		-8.45E-04

		9.15E-01		-8.50E-01		-8.50E-04

		9.19E-01		-8.55E-01		-8.55E-04

		9.23E-01		-8.61E-01		-8.61E-04

		9.27E-01		-8.66E-01		-8.66E-04

		9.31E-01		-8.71E-01		-8.71E-04

		9.35E-01		-8.77E-01		-8.77E-04

		9.39E-01		-8.82E-01		-8.82E-04

		9.43E-01		-8.87E-01		-8.87E-04

		9.47E-01		-8.93E-01		-8.93E-04

		9.51E-01		-8.98E-01		-8.98E-04

		9.55E-01		-9.03E-01		-9.03E-04

		9.59E-01		-9.09E-01		-9.09E-04

		9.63E-01		-9.14E-01		-9.14E-04

		9.67E-01		-9.20E-01		-9.20E-04

		9.71E-01		-9.25E-01		-9.25E-04

		9.75E-01		-9.30E-01		-9.30E-04

		9.79E-01		-9.36E-01		-9.36E-04

		9.83E-01		-9.41E-01		-9.41E-04

		9.87E-01		-9.47E-01		-9.47E-04

		9.91E-01		-9.51E-01		-9.51E-04

		9.95E-01		-9.57E-01		-9.57E-04

		9.99E-01		-9.63E-01		-9.63E-04

		1.00E+00		-9.68E-01		-9.68E-04

		1.01E+00		-9.74E-01		-9.74E-04

		1.01E+00		-9.78E-01		-9.78E-04

		1.02E+00		-9.84E-01		-9.84E-04

		1.02E+00		-9.89E-01		-9.89E-04

		1.02E+00		-9.95E-01		-9.95E-04

		1.03E+00		-1.00E+00		-1.00E-03

		1.03E+00		-1.01E+00		-1.01E-03

		1.04E+00		-1.01E+00		-1.01E-03

		1.04E+00		-1.02E+00		-1.02E-03

		1.04E+00		-1.02E+00		-1.02E-03

		1.05E+00		-1.03E+00		-1.03E-03

		1.05E+00		-1.03E+00		-1.03E-03

		1.06E+00		-1.04E+00		-1.04E-03

		1.06E+00		-1.04E+00		-1.04E-03

		1.06E+00		-1.05E+00		-1.05E-03

		1.07E+00		-1.06E+00		-1.06E-03

		1.07E+00		-1.06E+00		-1.06E-03

		1.08E+00		-1.07E+00		-1.07E-03

		1.08E+00		-1.07E+00		-1.07E-03

		1.08E+00		-1.08E+00		-1.08E-03

		1.09E+00		-1.08E+00		-1.08E-03

		1.09E+00		-1.09E+00		-1.09E-03

		1.10E+00		-1.09E+00		-1.09E-03

		1.10E+00		-1.10E+00		-1.10E-03

		1.10E+00		-1.10E+00		-1.10E-03

		1.11E+00		-1.11E+00		-1.11E-03

		1.11E+00		-1.12E+00		-1.12E-03

		1.12E+00		-1.12E+00		-1.12E-03

		1.12E+00		-1.13E+00		-1.13E-03

		1.12E+00		-1.13E+00		-1.13E-03

		1.13E+00		-1.14E+00		-1.14E-03

		1.13E+00		-1.14E+00		-1.14E-03

		1.14E+00		-1.15E+00		-1.15E-03

		1.14E+00		-1.15E+00		-1.15E-03

		1.14E+00		-1.16E+00		-1.16E-03

		1.15E+00		-1.16E+00		-1.16E-03

		1.15E+00		-1.17E+00		-1.17E-03

		1.16E+00		-1.18E+00		-1.18E-03

		1.16E+00		-1.18E+00		-1.18E-03

		1.16E+00		-1.19E+00		-1.19E-03

		1.17E+00		-1.19E+00		-1.19E-03

		1.17E+00		-1.20E+00		-1.20E-03

		1.18E+00		-1.20E+00		-1.20E-03

		1.18E+00		-1.21E+00		-1.21E-03

		1.18E+00		-1.21E+00		-1.21E-03

		1.19E+00		-1.22E+00		-1.22E-03

		1.19E+00		-1.23E+00		-1.23E-03

		1.20E+00		-1.23E+00		-1.23E-03

		1.20E+00		-1.24E+00		-1.24E-03

		1.20E+00		-1.24E+00		-1.24E-03

		1.21E+00		-1.25E+00		-1.25E-03

		1.21E+00		-1.25E+00		-1.25E-03

		1.22E+00		-1.26E+00		-1.26E-03

		1.22E+00		-1.26E+00		-1.26E-03

		1.22E+00		-1.27E+00		-1.27E-03

		1.23E+00		-1.28E+00		-1.28E-03

		1.23E+00		-1.28E+00		-1.28E-03

		1.24E+00		-1.29E+00		-1.29E-03

		1.24E+00		-1.29E+00		-1.29E-03

		1.24E+00		-1.30E+00		-1.30E-03

		1.25E+00		-1.30E+00		-1.30E-03

		1.25E+00		-1.31E+00		-1.31E-03

		1.26E+00		-1.32E+00		-1.32E-03

		1.26E+00		-1.32E+00		-1.32E-03

		1.26E+00		-1.33E+00		-1.33E-03

		1.27E+00		-1.33E+00		-1.33E-03

		1.27E+00		-1.34E+00		-1.34E-03

		1.28E+00		-1.34E+00		-1.34E-03

		1.28E+00		-1.35E+00		-1.35E-03

		1.28E+00		-1.35E+00		-1.35E-03

		1.29E+00		-1.36E+00		-1.36E-03

		1.29E+00		-1.37E+00		-1.37E-03

		1.30E+00		-1.37E+00		-1.37E-03

		1.30E+00		-1.38E+00		-1.38E-03

		1.30E+00		-1.38E+00		-1.38E-03

		1.31E+00		-1.39E+00		-1.39E-03

		1.31E+00		-1.39E+00		-1.39E-03

		1.32E+00		-1.40E+00		-1.40E-03

		1.32E+00		-1.40E+00		-1.40E-03

		1.32E+00		-1.41E+00		-1.41E-03

		1.33E+00		-1.42E+00		-1.42E-03

		1.33E+00		-1.42E+00		-1.42E-03

		1.34E+00		-1.43E+00		-1.43E-03

		1.34E+00		-1.43E+00		-1.43E-03

		1.34E+00		-1.44E+00		-1.44E-03

		1.35E+00		-1.44E+00		-1.44E-03

		1.35E+00		-1.45E+00		-1.45E-03

		1.36E+00		-1.46E+00		-1.46E-03

		1.36E+00		-1.46E+00		-1.46E-03

		1.36E+00		-1.47E+00		-1.47E-03

		1.37E+00		-1.47E+00		-1.47E-03

		1.37E+00		-1.48E+00		-1.48E-03

		1.38E+00		-1.48E+00		-1.48E-03

		1.38E+00		-1.49E+00		-1.49E-03

		1.38E+00		-1.50E+00		-1.50E-03

		1.39E+00		-1.50E+00		-1.50E-03

		1.39E+00		-1.51E+00		-1.51E-03

		1.40E+00		-1.51E+00		-1.51E-03

		1.40E+00		-1.52E+00		-1.52E-03

		1.40E+00		-1.52E+00		-1.52E-03

		1.41E+00		-1.53E+00		-1.53E-03

		1.41E+00		-1.53E+00		-1.53E-03

		1.42E+00		-1.54E+00		-1.54E-03

		1.42E+00		-1.55E+00		-1.55E-03

		1.42E+00		-1.55E+00		-1.55E-03

		1.43E+00		-1.56E+00		-1.56E-03

		1.43E+00		-1.56E+00		-1.56E-03

		1.44E+00		-1.57E+00		-1.57E-03

		1.44E+00		-1.57E+00		-1.57E-03

		1.44E+00		-1.58E+00		-1.58E-03

		1.45E+00		-1.59E+00		-1.59E-03

		1.45E+00		-1.59E+00		-1.59E-03

		1.46E+00		-1.60E+00		-1.60E-03

		1.46E+00		-1.60E+00		-1.60E-03

		1.46E+00		-1.61E+00		-1.61E-03

		1.47E+00		-1.61E+00		-1.61E-03

		1.47E+00		-1.62E+00		-1.62E-03

		1.48E+00		-1.63E+00		-1.63E-03

		1.48E+00		-1.63E+00		-1.63E-03

		1.48E+00		-1.64E+00		-1.64E-03

		1.49E+00		-1.64E+00		-1.64E-03

		1.49E+00		-1.65E+00		-1.65E-03

		1.50E+00		-1.65E+00		-1.65E-03

		1.50E+00		-1.66E+00		-1.66E-03

		1.50E+00		-1.67E+00		-1.67E-03

		1.51E+00		-1.67E+00		-1.67E-03

		1.51E+00		-1.68E+00		-1.68E-03

		1.52E+00		-1.68E+00		-1.68E-03

		1.52E+00		-1.69E+00		-1.69E-03

		1.52E+00		-1.69E+00		-1.69E-03

		1.53E+00		-1.70E+00		-1.70E-03

		1.53E+00		-1.71E+00		-1.71E-03

		1.54E+00		-1.71E+00		-1.71E-03

		1.54E+00		-1.72E+00		-1.72E-03

		1.54E+00		-1.72E+00		-1.72E-03

		1.55E+00		-1.73E+00		-1.73E-03

		1.55E+00		-1.73E+00		-1.73E-03

		1.56E+00		-1.74E+00		-1.74E-03

		1.56E+00		-1.75E+00		-1.75E-03

		1.56E+00		-1.75E+00		-1.75E-03

		1.57E+00		-1.76E+00		-1.76E-03

		1.57E+00		-1.76E+00		-1.76E-03

		1.58E+00		-1.77E+00		-1.77E-03

		1.58E+00		-1.77E+00		-1.77E-03

		1.58E+00		-1.78E+00		-1.78E-03

		1.59E+00		-1.79E+00		-1.79E-03

		1.59E+00		-1.79E+00		-1.79E-03

		1.60E+00		-1.80E+00		-1.80E-03

		1.60E+00		-1.80E+00		-1.80E-03

		1.60E+00		-1.81E+00		-1.81E-03

		1.61E+00		-1.81E+00		-1.81E-03

		1.61E+00		-1.82E+00		-1.82E-03

		1.62E+00		-1.83E+00		-1.83E-03

		1.62E+00		-1.83E+00		-1.83E-03

		1.62E+00		-1.84E+00		-1.84E-03

		1.63E+00		-1.84E+00		-1.84E-03

		1.63E+00		-1.85E+00		-1.85E-03

		1.64E+00		-1.85E+00		-1.85E-03

		1.64E+00		-1.86E+00		-1.86E-03

		1.64E+00		-1.87E+00		-1.87E-03

		1.65E+00		-1.87E+00		-1.87E-03

		1.65E+00		-1.88E+00		-1.88E-03

		1.66E+00		-1.88E+00		-1.88E-03

		1.66E+00		-1.89E+00		-1.89E-03

		1.66E+00		-1.89E+00		-1.89E-03

		1.67E+00		-1.90E+00		-1.90E-03

		1.67E+00		-1.90E+00		-1.90E-03

		1.68E+00		-1.91E+00		-1.91E-03

		1.68E+00		-1.92E+00		-1.92E-03

		1.68E+00		-1.92E+00		-1.92E-03

		1.69E+00		-1.93E+00		-1.93E-03

		1.69E+00		-1.93E+00		-1.93E-03

		1.70E+00		-1.94E+00		-1.94E-03

		1.70E+00		-1.95E+00		-1.95E-03

		1.70E+00		-1.95E+00		-1.95E-03

		1.71E+00		-1.96E+00		-1.96E-03

		1.71E+00		-1.96E+00		-1.96E-03

		1.72E+00		-1.97E+00		-1.97E-03

		1.72E+00		-1.98E+00		-1.98E-03

		1.72E+00		-1.98E+00		-1.98E-03

		1.73E+00		-1.99E+00		-1.99E-03

		1.73E+00		-1.99E+00		-1.99E-03

		1.74E+00		-2.00E+00		-2.00E-03

		1.74E+00		-2.01E+00		-2.01E-03

		1.74E+00		-2.01E+00		-2.01E-03

		1.75E+00		-2.02E+00		-2.02E-03

		1.75E+00		-2.02E+00		-2.02E-03

		1.76E+00		-2.03E+00		-2.03E-03

		1.76E+00		-2.03E+00		-2.03E-03

		1.76E+00		-2.04E+00		-2.04E-03

		1.77E+00		-2.05E+00		-2.05E-03

		1.77E+00		-2.05E+00		-2.05E-03

		1.78E+00		-2.06E+00		-2.06E-03

		1.78E+00		-2.06E+00		-2.06E-03

		1.78E+00		-2.07E+00		-2.07E-03

		1.79E+00		-2.07E+00		-2.07E-03

		1.79E+00		-2.08E+00		-2.08E-03

		1.80E+00		-2.09E+00		-2.09E-03

		1.80E+00		-2.09E+00		-2.09E-03

		1.80E+00		-2.10E+00		-2.10E-03

		1.81E+00		-2.10E+00		-2.10E-03

		1.81E+00		-2.11E+00		-2.11E-03

		1.82E+00		-2.11E+00		-2.11E-03

		1.82E+00		-2.12E+00		-2.12E-03

		1.82E+00		-2.13E+00		-2.13E-03

		1.83E+00		-2.13E+00		-2.13E-03

		1.83E+00		-2.14E+00		-2.14E-03

		1.84E+00		-2.14E+00		-2.14E-03

		1.84E+00		-2.15E+00		-2.15E-03

		1.84E+00		-2.16E+00		-2.16E-03

		1.85E+00		-2.16E+00		-2.16E-03

		1.85E+00		-2.16E+00		-2.16E-03

		1.86E+00		-2.17E+00		-2.17E-03

		1.86E+00		-2.18E+00		-2.18E-03

		1.86E+00		-2.18E+00		-2.18E-03

		1.87E+00		-2.19E+00		-2.19E-03

		1.87E+00		-2.19E+00		-2.19E-03

		1.88E+00		-2.20E+00		-2.20E-03

		1.88E+00		-2.21E+00		-2.21E-03

		1.88E+00		-2.21E+00		-2.21E-03

		1.89E+00		-2.22E+00		-2.22E-03

		1.89E+00		-2.22E+00		-2.22E-03

		1.90E+00		-2.23E+00		-2.23E-03

		1.90E+00		-2.24E+00		-2.24E-03

		1.90E+00		-2.24E+00		-2.24E-03

		1.91E+00		-2.25E+00		-2.25E-03

		1.91E+00		-2.25E+00		-2.25E-03

		1.92E+00		-2.26E+00		-2.26E-03

		1.92E+00		-2.26E+00		-2.26E-03

		1.92E+00		-2.27E+00		-2.27E-03

		1.93E+00		-2.28E+00		-2.28E-03

		1.93E+00		-2.28E+00		-2.28E-03

		1.94E+00		-2.29E+00		-2.29E-03

		1.94E+00		-2.29E+00		-2.29E-03

		1.94E+00		-2.30E+00		-2.30E-03

		1.95E+00		-2.30E+00		-2.30E-03

		1.95E+00		-2.31E+00		-2.31E-03

		1.96E+00		-2.32E+00		-2.32E-03

		1.96E+00		-2.32E+00		-2.32E-03

		1.96E+00		-2.33E+00		-2.33E-03

		1.97E+00		-2.33E+00		-2.33E-03

		1.97E+00		-2.34E+00		-2.34E-03

		1.98E+00		-2.35E+00		-2.35E-03

		1.98E+00		-2.35E+00		-2.35E-03

		1.98E+00		-2.36E+00		-2.36E-03

		1.99E+00		-2.36E+00		-2.36E-03

		1.99E+00		-2.37E+00		-2.37E-03

		2.00E+00		-2.37E+00		-2.37E-03

		2.00E+00		-2.38E+00		-2.38E-03

		2.00E+00		-2.37E+00		-2.37E-03

		1.99E+00		-2.37E+00		-2.37E-03

		1.99E+00		-2.36E+00		-2.36E-03

		1.98E+00		-2.35E+00		-2.35E-03

		1.98E+00		-2.35E+00		-2.35E-03

		1.98E+00		-2.34E+00		-2.34E-03

		1.97E+00		-2.34E+00		-2.34E-03

		1.97E+00		-2.33E+00		-2.33E-03

		1.96E+00		-2.33E+00		-2.33E-03

		1.96E+00		-2.32E+00		-2.32E-03

		1.96E+00		-2.31E+00		-2.31E-03

		1.95E+00		-2.31E+00		-2.31E-03

		1.95E+00		-2.30E+00		-2.30E-03

		1.94E+00		-2.30E+00		-2.30E-03

		1.94E+00		-2.29E+00		-2.29E-03

		1.94E+00		-2.28E+00		-2.28E-03

		1.93E+00		-2.28E+00		-2.28E-03

		1.93E+00		-2.27E+00		-2.27E-03

		1.92E+00		-2.27E+00		-2.27E-03

		1.92E+00		-2.26E+00		-2.26E-03

		1.92E+00		-2.25E+00		-2.25E-03

		1.91E+00		-2.25E+00		-2.25E-03

		1.91E+00		-2.24E+00		-2.24E-03

		1.90E+00		-2.23E+00		-2.23E-03

		1.90E+00		-2.23E+00		-2.23E-03

		1.90E+00		-2.22E+00		-2.22E-03

		1.89E+00		-2.22E+00		-2.22E-03

		1.89E+00		-2.21E+00		-2.21E-03

		1.88E+00		-2.20E+00		-2.20E-03

		1.88E+00		-2.20E+00		-2.20E-03

		1.88E+00		-2.19E+00		-2.19E-03

		1.87E+00		-2.19E+00		-2.19E-03

		1.87E+00		-2.18E+00		-2.18E-03

		1.86E+00		-2.18E+00		-2.18E-03

		1.86E+00		-2.17E+00		-2.17E-03

		1.86E+00		-2.16E+00		-2.16E-03

		1.85E+00		-2.16E+00		-2.16E-03

		1.85E+00		-2.15E+00		-2.15E-03

		1.84E+00		-2.15E+00		-2.15E-03

		1.84E+00		-2.14E+00		-2.14E-03

		1.84E+00		-2.13E+00		-2.13E-03

		1.83E+00		-2.13E+00		-2.13E-03

		1.83E+00		-2.12E+00		-2.12E-03

		1.82E+00		-2.12E+00		-2.12E-03

		1.82E+00		-2.11E+00		-2.11E-03

		1.82E+00		-2.10E+00		-2.10E-03

		1.81E+00		-2.10E+00		-2.10E-03

		1.81E+00		-2.09E+00		-2.09E-03

		1.80E+00		-2.09E+00		-2.09E-03

		1.80E+00		-2.08E+00		-2.08E-03

		1.80E+00		-2.07E+00		-2.07E-03

		1.79E+00		-2.07E+00		-2.07E-03

		1.79E+00		-2.06E+00		-2.06E-03

		1.78E+00		-2.06E+00		-2.06E-03

		1.78E+00		-2.05E+00		-2.05E-03

		1.78E+00		-2.04E+00		-2.04E-03

		1.77E+00		-2.04E+00		-2.04E-03

		1.77E+00		-2.03E+00		-2.03E-03

		1.76E+00		-2.03E+00		-2.03E-03

		1.76E+00		-2.02E+00		-2.02E-03

		1.76E+00		-2.02E+00		-2.02E-03

		1.75E+00		-2.01E+00		-2.01E-03

		1.75E+00		-2.00E+00		-2.00E-03

		1.74E+00		-2.00E+00		-2.00E-03

		1.74E+00		-1.99E+00		-1.99E-03

		1.74E+00		-1.98E+00		-1.98E-03

		1.73E+00		-1.98E+00		-1.98E-03

		1.73E+00		-1.97E+00		-1.97E-03

		1.72E+00		-1.97E+00		-1.97E-03

		1.72E+00		-1.96E+00		-1.96E-03

		1.72E+00		-1.95E+00		-1.95E-03

		1.71E+00		-1.95E+00		-1.95E-03

		1.71E+00		-1.94E+00		-1.94E-03

		1.70E+00		-1.94E+00		-1.94E-03

		1.70E+00		-1.93E+00		-1.93E-03

		1.70E+00		-1.92E+00		-1.92E-03

		1.69E+00		-1.92E+00		-1.92E-03

		1.69E+00		-1.91E+00		-1.91E-03

		1.68E+00		-1.91E+00		-1.91E-03

		1.68E+00		-1.90E+00		-1.90E-03

		1.68E+00		-1.90E+00		-1.90E-03

		1.67E+00		-1.89E+00		-1.89E-03

		1.67E+00		-1.88E+00		-1.88E-03

		1.66E+00		-1.88E+00		-1.88E-03

		1.66E+00		-1.87E+00		-1.87E-03

		1.66E+00		-1.87E+00		-1.87E-03

		1.65E+00		-1.86E+00		-1.86E-03

		1.65E+00		-1.85E+00		-1.85E-03

		1.64E+00		-1.85E+00		-1.85E-03

		1.64E+00		-1.84E+00		-1.84E-03

		1.64E+00		-1.84E+00		-1.84E-03

		1.63E+00		-1.83E+00		-1.83E-03

		1.63E+00		-1.82E+00		-1.82E-03

		1.62E+00		-1.82E+00		-1.82E-03

		1.62E+00		-1.81E+00		-1.81E-03

		1.62E+00		-1.81E+00		-1.81E-03

		1.61E+00		-1.80E+00		-1.80E-03

		1.61E+00		-1.79E+00		-1.79E-03

		1.60E+00		-1.79E+00		-1.79E-03

		1.60E+00		-1.78E+00		-1.78E-03

		1.60E+00		-1.78E+00		-1.78E-03

		1.59E+00		-1.77E+00		-1.77E-03

		1.59E+00		-1.76E+00		-1.76E-03

		1.58E+00		-1.76E+00		-1.76E-03

		1.58E+00		-1.75E+00		-1.75E-03

		1.58E+00		-1.75E+00		-1.75E-03

		1.57E+00		-1.74E+00		-1.74E-03

		1.57E+00		-1.73E+00		-1.73E-03

		1.56E+00		-1.73E+00		-1.73E-03

		1.56E+00		-1.72E+00		-1.72E-03

		1.56E+00		-1.72E+00		-1.72E-03

		1.55E+00		-1.71E+00		-1.71E-03

		1.55E+00		-1.70E+00		-1.70E-03

		1.54E+00		-1.70E+00		-1.70E-03

		1.54E+00		-1.69E+00		-1.69E-03

		1.54E+00		-1.69E+00		-1.69E-03

		1.53E+00		-1.68E+00		-1.68E-03

		1.53E+00		-1.67E+00		-1.67E-03

		1.52E+00		-1.67E+00		-1.67E-03

		1.52E+00		-1.66E+00		-1.66E-03

		1.52E+00		-1.66E+00		-1.66E-03

		1.51E+00		-1.65E+00		-1.65E-03

		1.51E+00		-1.65E+00		-1.65E-03

		1.50E+00		-1.64E+00		-1.64E-03

		1.50E+00		-1.64E+00		-1.64E-03

		1.50E+00		-1.63E+00		-1.63E-03

		1.49E+00		-1.63E+00		-1.63E-03

		1.49E+00		-1.62E+00		-1.62E-03

		1.48E+00		-1.61E+00		-1.61E-03

		1.48E+00		-1.61E+00		-1.61E-03

		1.48E+00		-1.60E+00		-1.60E-03

		1.47E+00		-1.60E+00		-1.60E-03

		1.47E+00		-1.59E+00		-1.59E-03

		1.46E+00		-1.58E+00		-1.58E-03

		1.46E+00		-1.58E+00		-1.58E-03

		1.46E+00		-1.57E+00		-1.57E-03

		1.45E+00		-1.57E+00		-1.57E-03

		1.45E+00		-1.56E+00		-1.56E-03

		1.44E+00		-1.56E+00		-1.56E-03

		1.44E+00		-1.55E+00		-1.55E-03

		1.44E+00		-1.55E+00		-1.55E-03

		1.43E+00		-1.54E+00		-1.54E-03

		1.43E+00		-1.53E+00		-1.53E-03

		1.42E+00		-1.53E+00		-1.53E-03

		1.42E+00		-1.52E+00		-1.52E-03

		1.42E+00		-1.51E+00		-1.51E-03

		1.41E+00		-1.51E+00		-1.51E-03

		1.41E+00		-1.50E+00		-1.50E-03

		1.40E+00		-1.50E+00		-1.50E-03

		1.40E+00		-1.49E+00		-1.49E-03

		1.40E+00		-1.49E+00		-1.49E-03

		1.39E+00		-1.48E+00		-1.48E-03

		1.39E+00		-1.48E+00		-1.48E-03

		1.38E+00		-1.47E+00		-1.47E-03

		1.38E+00		-1.46E+00		-1.46E-03

		1.38E+00		-1.46E+00		-1.46E-03

		1.37E+00		-1.45E+00		-1.45E-03

		1.37E+00		-1.45E+00		-1.45E-03

		1.36E+00		-1.44E+00		-1.44E-03

		1.36E+00		-1.43E+00		-1.43E-03

		1.36E+00		-1.43E+00		-1.43E-03

		1.35E+00		-1.42E+00		-1.42E-03

		1.35E+00		-1.42E+00		-1.42E-03

		1.34E+00		-1.41E+00		-1.41E-03

		1.34E+00		-1.41E+00		-1.41E-03

		1.34E+00		-1.40E+00		-1.40E-03

		1.33E+00		-1.39E+00		-1.39E-03

		1.33E+00		-1.39E+00		-1.39E-03

		1.32E+00		-1.38E+00		-1.38E-03

		1.32E+00		-1.38E+00		-1.38E-03

		1.32E+00		-1.37E+00		-1.37E-03

		1.31E+00		-1.37E+00		-1.37E-03

		1.31E+00		-1.36E+00		-1.36E-03

		1.30E+00		-1.35E+00		-1.35E-03

		1.30E+00		-1.35E+00		-1.35E-03

		1.30E+00		-1.34E+00		-1.34E-03

		1.29E+00		-1.34E+00		-1.34E-03

		1.29E+00		-1.33E+00		-1.33E-03

		1.28E+00		-1.32E+00		-1.32E-03

		1.28E+00		-1.32E+00		-1.32E-03

		1.28E+00		-1.31E+00		-1.31E-03

		1.27E+00		-1.31E+00		-1.31E-03

		1.27E+00		-1.30E+00		-1.30E-03

		1.26E+00		-1.30E+00		-1.30E-03

		1.26E+00		-1.29E+00		-1.29E-03

		1.26E+00		-1.28E+00		-1.28E-03

		1.25E+00		-1.28E+00		-1.28E-03

		1.25E+00		-1.27E+00		-1.27E-03

		1.24E+00		-1.27E+00		-1.27E-03

		1.24E+00		-1.26E+00		-1.26E-03

		1.24E+00		-1.26E+00		-1.26E-03

		1.23E+00		-1.25E+00		-1.25E-03

		1.23E+00		-1.24E+00		-1.24E-03

		1.22E+00		-1.24E+00		-1.24E-03

		1.22E+00		-1.23E+00		-1.23E-03

		1.22E+00		-1.23E+00		-1.23E-03

		1.21E+00		-1.22E+00		-1.22E-03

		1.21E+00		-1.22E+00		-1.22E-03

		1.20E+00		-1.21E+00		-1.21E-03

		1.20E+00		-1.20E+00		-1.20E-03

		1.20E+00		-1.20E+00		-1.20E-03

		1.19E+00		-1.19E+00		-1.19E-03

		1.19E+00		-1.19E+00		-1.19E-03

		1.18E+00		-1.18E+00		-1.18E-03

		1.18E+00		-1.18E+00		-1.18E-03

		1.18E+00		-1.17E+00		-1.17E-03

		1.17E+00		-1.16E+00		-1.16E-03

		1.17E+00		-1.16E+00		-1.16E-03

		1.16E+00		-1.15E+00		-1.15E-03

		1.16E+00		-1.15E+00		-1.15E-03

		1.16E+00		-1.14E+00		-1.14E-03

		1.15E+00		-1.14E+00		-1.14E-03

		1.15E+00		-1.13E+00		-1.13E-03

		1.14E+00		-1.12E+00		-1.12E-03

		1.14E+00		-1.12E+00		-1.12E-03

		1.14E+00		-1.11E+00		-1.11E-03

		1.13E+00		-1.11E+00		-1.11E-03

		1.13E+00		-1.10E+00		-1.10E-03

		1.12E+00		-1.10E+00		-1.10E-03

		1.12E+00		-1.09E+00		-1.09E-03

		1.12E+00		-1.09E+00		-1.09E-03

		1.11E+00		-1.08E+00		-1.08E-03

		1.11E+00		-1.07E+00		-1.07E-03

		1.10E+00		-1.07E+00		-1.07E-03

		1.10E+00		-1.06E+00		-1.06E-03

		1.10E+00		-1.06E+00		-1.06E-03

		1.09E+00		-1.05E+00		-1.05E-03

		1.09E+00		-1.05E+00		-1.05E-03

		1.08E+00		-1.04E+00		-1.04E-03

		1.08E+00		-1.03E+00		-1.03E-03

		1.08E+00		-1.03E+00		-1.03E-03

		1.07E+00		-1.02E+00		-1.02E-03

		1.07E+00		-1.02E+00		-1.02E-03

		1.06E+00		-1.01E+00		-1.01E-03

		1.06E+00		-1.01E+00		-1.01E-03

		1.06E+00		-1.00E+00		-1.00E-03

		1.05E+00		-9.94E-01		-9.94E-04

		1.05E+00		-9.88E-01		-9.88E-04

		1.04E+00		-9.83E-01		-9.83E-04

		1.04E+00		-9.78E-01		-9.78E-04

		1.04E+00		-9.72E-01		-9.72E-04

		1.03E+00		-9.66E-01		-9.66E-04

		1.03E+00		-9.60E-01		-9.60E-04

		1.02E+00		-9.55E-01		-9.55E-04

		1.02E+00		-9.49E-01		-9.49E-04

		1.02E+00		-9.44E-01		-9.44E-04

		1.01E+00		-9.39E-01		-9.39E-04

		1.01E+00		-9.32E-01		-9.32E-04

		1.00E+00		-9.27E-01		-9.27E-04

		9.99E-01		-9.22E-01		-9.22E-04

		9.95E-01		-9.16E-01		-9.16E-04

		9.91E-01		-9.11E-01		-9.11E-04

		9.87E-01		-9.04E-01		-9.04E-04

		9.83E-01		-8.99E-01		-8.99E-04

		9.79E-01		-8.94E-01		-8.94E-04

		9.75E-01		-8.88E-01		-8.88E-04

		9.71E-01		-8.83E-01		-8.83E-04

		9.67E-01		-8.76E-01		-8.76E-04

		9.63E-01		-8.72E-01		-8.72E-04

		9.59E-01		-8.67E-01		-8.67E-04

		9.55E-01		-8.61E-01		-8.61E-04

		9.51E-01		-8.56E-01		-8.56E-04

		9.47E-01		-8.49E-01		-8.49E-04

		9.43E-01		-8.44E-01		-8.44E-04

		9.39E-01		-8.38E-01		-8.38E-04

		9.35E-01		-8.33E-01		-8.33E-04

		9.31E-01		-8.27E-01		-8.27E-04

		9.27E-01		-8.21E-01		-8.21E-04

		9.23E-01		-8.16E-01		-8.16E-04

		9.19E-01		-8.11E-01		-8.11E-04

		9.15E-01		-8.06E-01		-8.06E-04

		9.11E-01		-8.00E-01		-8.00E-04

		9.07E-01		-7.94E-01		-7.94E-04

		9.03E-01		-7.89E-01		-7.89E-04

		8.99E-01		-7.83E-01		-7.83E-04

		8.95E-01		-7.78E-01		-7.78E-04

		8.91E-01		-7.73E-01		-7.73E-04

		8.87E-01		-7.67E-01		-7.67E-04

		8.83E-01		-7.62E-01		-7.62E-04

		8.79E-01		-7.56E-01		-7.56E-04

		8.75E-01		-7.51E-01		-7.51E-04

		8.71E-01		-7.46E-01		-7.46E-04

		8.67E-01		-7.40E-01		-7.40E-04

		8.63E-01		-7.35E-01		-7.35E-04

		8.59E-01		-7.29E-01		-7.29E-04

		8.55E-01		-7.24E-01		-7.24E-04

		8.51E-01		-7.18E-01		-7.18E-04

		8.47E-01		-7.12E-01		-7.12E-04

		8.43E-01		-7.07E-01		-7.07E-04

		8.39E-01		-7.02E-01		-7.02E-04

		8.35E-01		-6.96E-01		-6.96E-04

		8.31E-01		-6.91E-01		-6.91E-04

		8.27E-01		-6.85E-01		-6.85E-04

		8.23E-01		-6.80E-01		-6.80E-04

		8.19E-01		-6.74E-01		-6.74E-04

		8.15E-01		-6.69E-01		-6.69E-04

		8.11E-01		-6.63E-01		-6.63E-04

		8.07E-01		-6.58E-01		-6.58E-04

		8.03E-01		-6.52E-01		-6.52E-04

		7.99E-01		-6.47E-01		-6.47E-04

		7.95E-01		-6.42E-01		-6.42E-04

		7.91E-01		-6.36E-01		-6.36E-04

		7.87E-01		-6.31E-01		-6.31E-04

		7.83E-01		-6.25E-01		-6.25E-04

		7.79E-01		-6.20E-01		-6.20E-04

		7.75E-01		-6.15E-01		-6.15E-04

		7.71E-01		-6.09E-01		-6.09E-04

		7.67E-01		-6.04E-01		-6.04E-04

		7.63E-01		-5.99E-01		-5.99E-04

		7.59E-01		-5.94E-01		-5.94E-04

		7.55E-01		-5.88E-01		-5.88E-04

		7.51E-01		-5.83E-01		-5.83E-04

		7.47E-01		-5.77E-01		-5.77E-04

		7.43E-01		-5.72E-01		-5.72E-04

		7.39E-01		-5.67E-01		-5.67E-04

		7.35E-01		-5.62E-01		-5.62E-04

		7.31E-01		-5.56E-01		-5.56E-04

		7.27E-01		-5.51E-01		-5.51E-04

		7.23E-01		-5.46E-01		-5.46E-04

		7.19E-01		-5.40E-01		-5.40E-04

		7.15E-01		-5.35E-01		-5.35E-04

		7.11E-01		-5.30E-01		-5.30E-04

		7.07E-01		-5.24E-01		-5.24E-04

		7.03E-01		-5.19E-01		-5.19E-04

		6.99E-01		-5.14E-01		-5.14E-04

		6.95E-01		-5.08E-01		-5.08E-04

		6.91E-01		-5.03E-01		-5.03E-04

		6.87E-01		-4.97E-01		-4.97E-04

		6.83E-01		-4.92E-01		-4.92E-04

		6.79E-01		-4.87E-01		-4.87E-04

		6.75E-01		-4.82E-01		-4.82E-04

		6.71E-01		-4.77E-01		-4.77E-04

		6.67E-01		-4.71E-01		-4.71E-04

		6.63E-01		-4.66E-01		-4.66E-04

		6.59E-01		-4.60E-01		-4.60E-04

		6.55E-01		-4.55E-01		-4.55E-04

		6.51E-01		-4.51E-01		-4.51E-04

		6.47E-01		-4.45E-01		-4.45E-04

		6.43E-01		-4.40E-01		-4.40E-04

		6.39E-01		-4.35E-01		-4.35E-04

		6.35E-01		-4.30E-01		-4.30E-04

		6.31E-01		-4.24E-01		-4.24E-04

		6.27E-01		-4.19E-01		-4.19E-04

		6.23E-01		-4.14E-01		-4.14E-04

		6.19E-01		-4.09E-01		-4.09E-04

		6.15E-01		-4.04E-01		-4.04E-04

		6.11E-01		-3.99E-01		-3.99E-04

		6.07E-01		-3.93E-01		-3.93E-04

		6.03E-01		-3.89E-01		-3.89E-04

		5.99E-01		-3.83E-01		-3.83E-04

		5.95E-01		-3.78E-01		-3.78E-04

		5.91E-01		-3.73E-01		-3.73E-04

		5.87E-01		-3.68E-01		-3.68E-04

		5.83E-01		-3.63E-01		-3.63E-04

		5.79E-01		-3.58E-01		-3.58E-04

		5.75E-01		-3.53E-01		-3.53E-04

		5.71E-01		-3.48E-01		-3.48E-04

		5.67E-01		-3.43E-01		-3.43E-04

		5.63E-01		-3.38E-01		-3.38E-04

		5.59E-01		-3.33E-01		-3.33E-04

		5.55E-01		-3.28E-01		-3.28E-04

		5.51E-01		-3.23E-01		-3.23E-04

		5.47E-01		-3.17E-01		-3.17E-04

		5.43E-01		-3.13E-01		-3.13E-04

		5.39E-01		-3.08E-01		-3.08E-04

		5.35E-01		-3.03E-01		-3.03E-04

		5.31E-01		-2.98E-01		-2.98E-04

		5.27E-01		-2.93E-01		-2.93E-04

		5.23E-01		-2.88E-01		-2.88E-04

		5.19E-01		-2.83E-01		-2.83E-04

		5.15E-01		-2.79E-01		-2.79E-04

		5.11E-01		-2.74E-01		-2.74E-04

		5.07E-01		-2.69E-01		-2.69E-04

		5.03E-01		-2.64E-01		-2.64E-04

		4.99E-01		-2.59E-01		-2.59E-04

		4.95E-01		-2.54E-01		-2.54E-04

		4.91E-01		-2.49E-01		-2.49E-04

		4.87E-01		-2.45E-01		-2.45E-04

		4.83E-01		-2.40E-01		-2.40E-04

		4.79E-01		-2.35E-01		-2.35E-04

		4.75E-01		-2.31E-01		-2.31E-04

		4.71E-01		-2.26E-01		-2.26E-04

		4.67E-01		-2.21E-01		-2.21E-04

		4.63E-01		-2.16E-01		-2.16E-04

		4.59E-01		-2.12E-01		-2.12E-04

		4.55E-01		-2.07E-01		-2.07E-04

		4.51E-01		-2.03E-01		-2.03E-04

		4.47E-01		-1.98E-01		-1.98E-04

		4.43E-01		-1.93E-01		-1.93E-04

		4.39E-01		-1.89E-01		-1.89E-04

		4.35E-01		-1.84E-01		-1.84E-04

		4.31E-01		-1.80E-01		-1.80E-04

		4.27E-01		-1.75E-01		-1.75E-04

		4.23E-01		-1.71E-01		-1.71E-04

		4.19E-01		-1.67E-01		-1.67E-04

		4.15E-01		-1.62E-01		-1.62E-04

		4.11E-01		-1.58E-01		-1.58E-04

		4.07E-01		-1.53E-01		-1.53E-04

		4.03E-01		-1.50E-01		-1.50E-04

		3.99E-01		-1.45E-01		-1.45E-04

		3.95E-01		-1.41E-01		-1.41E-04

		3.91E-01		-1.37E-01		-1.37E-04

		3.87E-01		-1.33E-01		-1.33E-04

		3.83E-01		-1.29E-01		-1.29E-04

		3.79E-01		-1.25E-01		-1.25E-04

		3.75E-01		-1.21E-01		-1.21E-04

		3.71E-01		-1.17E-01		-1.17E-04

		3.67E-01		-1.13E-01		-1.13E-04

		3.63E-01		-1.09E-01		-1.09E-04

		3.59E-01		-1.05E-01		-1.05E-04

		3.55E-01		-1.02E-01		-1.02E-04

		3.51E-01		-9.80E-02		-9.80E-05

		3.47E-01		-9.42E-02		-9.42E-05

		3.43E-01		-9.08E-02		-9.08E-05

		3.39E-01		-8.73E-02		-8.73E-05

		3.35E-01		-8.36E-02		-8.36E-05

		3.31E-01		-8.03E-02		-8.03E-05

		3.27E-01		-7.67E-02		-7.67E-05

		3.23E-01		-7.36E-02		-7.36E-05

		3.19E-01		-7.03E-02		-7.03E-05

		3.15E-01		-6.71E-02		-6.71E-05

		3.11E-01		-6.42E-02		-6.42E-05

		3.07E-01		-6.09E-02		-6.09E-05

		3.03E-01		-5.81E-02		-5.81E-05

		2.99E-01		-5.52E-02		-5.52E-05

		2.95E-01		-5.25E-02		-5.25E-05

		2.91E-01		-4.98E-02		-4.98E-05

		2.87E-01		-4.71E-02		-4.71E-05

		2.83E-01		-4.48E-02		-4.48E-05

		2.79E-01		-4.23E-02		-4.23E-05

		2.75E-01		-4.02E-02		-4.02E-05

		2.71E-01		-3.80E-02		-3.80E-05

		2.67E-01		-3.59E-02		-3.59E-05

		2.63E-01		-3.40E-02		-3.40E-05

		2.59E-01		-3.22E-02		-3.22E-05

		2.55E-01		-3.05E-02		-3.05E-05

		2.51E-01		-2.88E-02		-2.88E-05

		2.47E-01		-2.72E-02		-2.72E-05

		2.43E-01		-2.57E-02		-2.57E-05

		2.39E-01		-2.44E-02		-2.44E-05

		2.35E-01		-2.32E-02		-2.32E-05

		2.31E-01		-2.19E-02		-2.19E-05

		2.27E-01		-2.09E-02		-2.09E-05

		2.23E-01		-1.98E-02		-1.98E-05

		2.19E-01		-1.90E-02		-1.90E-05

		2.15E-01		-1.82E-02		-1.82E-05

		2.11E-01		-1.72E-02		-1.72E-05

		2.07E-01		-1.66E-02		-1.66E-05

		2.03E-01		-1.58E-02		-1.58E-05

		1.99E-01		-1.53E-02		-1.53E-05

		1.95E-01		-1.47E-02		-1.47E-05

		1.91E-01		-1.41E-02		-1.41E-05

		1.87E-01		-1.36E-02		-1.36E-05

		1.83E-01		-1.30E-02		-1.30E-05

		1.79E-01		-1.27E-02		-1.27E-05

		1.75E-01		-1.21E-02		-1.21E-05

		1.71E-01		-1.17E-02		-1.17E-05

		1.67E-01		-1.13E-02		-1.13E-05

		1.63E-01		-1.08E-02		-1.08E-05

		1.59E-01		-1.04E-02		-1.04E-05

		1.55E-01		-9.90E-03		-9.90E-06

		1.51E-01		-9.38E-03		-9.38E-06

		1.47E-01		-8.86E-03		-8.86E-06

		1.43E-01		-8.26E-03		-8.26E-06

		1.39E-01		-7.79E-03		-7.79E-06

		1.35E-01		-7.11E-03		-7.11E-06

		1.31E-01		-6.43E-03		-6.43E-06

		1.27E-01		-5.67E-03		-5.67E-06

		1.23E-01		-4.81E-03		-4.81E-06

		1.19E-01		-4.06E-03		-4.06E-06

		1.15E-01		-3.07E-03		-3.07E-06

		1.11E-01		-2.05E-03		-2.05E-06

		1.07E-01		-9.00E-04		-9.00E-07

		1.03E-01		2.94E-04		2.94E-07

		9.90E-02		1.46E-03		1.46E-06

		9.50E-02		2.81E-03		2.81E-06

		9.10E-02		4.31E-03		4.31E-06

		8.70E-02		5.98E-03		5.98E-06

		8.30E-02		7.65E-03		7.65E-06

		7.90E-02		9.38E-03		9.38E-06

		7.50E-02		1.13E-02		1.13E-05

		7.10E-02		1.33E-02		1.33E-05

		6.70E-02		1.55E-02		1.55E-05

		6.30E-02		1.76E-02		1.76E-05

		5.90E-02		1.99E-02		1.99E-05

		5.50E-02		2.24E-02		2.24E-05

		5.10E-02		2.49E-02		2.49E-05

		4.70E-02		2.78E-02		2.78E-05

		4.30E-02		3.05E-02		3.05E-05

		3.90E-02		3.33E-02		3.33E-05

		3.50E-02		3.63E-02		3.63E-05

		3.10E-02		3.93E-02		3.93E-05

		2.70E-02		4.26E-02		4.26E-05

		2.30E-02		4.58E-02		4.58E-05
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		-0.783

		-0.787

		-0.791

		-0.795

		-0.799

		-0.803

		-0.807

		-0.811

		-0.815

		-0.819

		-0.823

		-0.827

		-0.831

		-0.835

		-0.839

		-0.843

		-0.847

		-0.851

		-0.855

		-0.859

		-0.863

		-0.867

		-0.871

		-0.875

		-0.879

		-0.883

		-0.887

		-0.891

		-0.895

		-0.899

		-0.903

		-0.907

		-0.911

		-0.915

		-0.919

		-0.923

		-0.927

		-0.931

		-0.935

		-0.939

		-0.943

		-0.947

		-0.951

		-0.955

		-0.959

		-0.963

		-0.967

		-0.971

		-0.975

		-0.979

		-0.983

		-0.987

		-0.991

		-0.995

		-0.999

		-0.995

		-0.991

		-0.987

		-0.983

		-0.979

		-0.975

		-0.971

		-0.967

		-0.963

		-0.959

		-0.955

		-0.951

		-0.947

		-0.943

		-0.939

		-0.935

		-0.931

		-0.927

		-0.923

		-0.919

		-0.915

		-0.911

		-0.907

		-0.903

		-0.899

		-0.895

		-0.891

		-0.887

		-0.883

		-0.879

		-0.875

		-0.871

		-0.867

		-0.863

		-0.859

		-0.855

		-0.851

		-0.847

		-0.843

		-0.839

		-0.835

		-0.831

		-0.827

		-0.823

		-0.819

		-0.815

		-0.811

		-0.807

		-0.803

		-0.799

		-0.795

		-0.791

		-0.787

		-0.783

		-0.779

		-0.775

		-0.771

		-0.767

		-0.763

		-0.759

		-0.755

		-0.751

		-0.747

		-0.743

		-0.739

		-0.735

		-0.731

		-0.727

		-0.723

		-0.719

		-0.715

		-0.711

		-0.707

		-0.703

		-0.699

		-0.695

		-0.691

		-0.687

		-0.683

		-0.679

		-0.675

		-0.671

		-0.667

		-0.663

		-0.659

		-0.655

		-0.651

		-0.647

		-0.643

		-0.639

		-0.635

		-0.631

		-0.627

		-0.623

		-0.619

		-0.615

		-0.611

		-0.607

		-0.603

		-0.599

		-0.595

		-0.591

		-0.587

		-0.583

		-0.579

		-0.575

		-0.571

		-0.567

		-0.563

		-0.559

		-0.555

		-0.551

		-0.547

		-0.543

		-0.539

		-0.535

		-0.531

		-0.527

		-0.523

		-0.519

		-0.515

		-0.511

		-0.507

		-0.503

		-0.499

		-0.495

		-0.491

		-0.487

		-0.483

		-0.479

		-0.475

		-0.471

		-0.467

		-0.463

		-0.459

		-0.455

		-0.451

		-0.447

		-0.443

		-0.439

		-0.435

		-0.431

		-0.427

		-0.423

		-0.419

		-0.415

		-0.411

		-0.407

		-0.403

		-0.399

		-0.395

		-0.391

		-0.387

		-0.383

		-0.379

		-0.375

		-0.371

		-0.367

		-0.363

		-0.359

		-0.355

		-0.351

		-0.347

		-0.343

		-0.339

		-0.335

		-0.331

		-0.327

		-0.323

		-0.319

		-0.315

		-0.311

		-0.307

		-0.303

		-0.299

		-0.295

		-0.291

		-0.287

		-0.283

		-0.279

		-0.275

		-0.271

		-0.267

		-0.263

		-0.259

		-0.255

		-0.251

		-0.247

		-0.243

		-0.239

		-0.235

		-0.231

		-0.227

		-0.223

		-0.219

		-0.215

		-0.211

		-0.207

		-0.203

		-0.199

		-0.195

		-0.191

		-0.187

		-0.183

		-0.179

		-0.175

		-0.171

		-0.167

		-0.163

		-0.159

		-0.155

		-0.151

		-0.147

		-0.143

		-0.139

		-0.135

		-0.131

		-0.127

		-0.123

		-0.119

		-0.115

		-0.111

		-0.107

		-0.103

		-0.098999

		-0.094999

		-0.090999

		-0.086999

		-0.082999

		-0.078999

		-0.074999

		-0.070999

		-0.066999

		-0.062999

		-0.058999

		-0.054999

		-0.050999

		-0.046999

		-0.042999

		-0.038999

		-0.034999

		-0.030999

		-0.026999

		-0.022999

		-0.018999

		-0.014999

		-0.010999

		-0.0069987

		-0.0029987

		0.0010013

		0.0050013

		0.0090013

		0.013001

		0.017001

		0.021001

		0.025001

		0.029001

		0.033001

		0.037001

		0.041001

		0.045001

		0.049001

		0.053001

		0.057001

		0.061001

		0.065001

		0.069001

		0.073001

		0.077001

		0.081001

		0.085001

		0.089001

		0.093001

		0.097001

		0.101

		0.105

		0.109

		0.113

		0.117

		0.121

		0.125

		0.129

		0.133

		0.137

		0.141

		0.145

		0.149

		0.153

		0.157

		0.161

		0.165

		0.169

		0.173

		0.177

		0.181

		0.185

		0.189

		0.193

		0.197

		0.201

		0.205

		0.209

		0.213

		0.217

		0.221

		0.225

		0.229

		0.233

		0.237

		0.241

		0.245

		0.249

		0.253

		0.257

		0.261

		0.265

		0.269

		0.273

		0.277

		0.281

		0.285

		0.289

		0.293

		0.297

		0.301

		0.305

		0.309

		0.313

		0.317

		0.321

		0.325

		0.329

		0.333

		0.337

		0.341

		0.345

		0.349

		0.353

		0.357

		0.361

		0.365

		0.369

		0.373

		0.377

		0.381

		0.385

		0.389

		0.393

		0.397

		0.401

		0.405

		0.409

		0.413

		0.417

		0.421

		0.425

		0.429

		0.433

		0.437

		0.441

		0.445

		0.449

		0.453

		0.457

		0.461

		0.465

		0.469

		0.473

		0.477

		0.481

		0.485

		0.489

		0.493

		0.497

		0.501

		0.505

		0.509

		0.513

		0.517

		0.521

		0.525

		0.529

		0.533

		0.537

		0.541

		0.545

		0.549

		0.553

		0.557

		0.561

		0.565

		0.569

		0.573

		0.577

		0.581

		0.585

		0.589

		0.593

		0.597

		0.601

		0.605

		0.609

		0.613

		0.617

		0.621

		0.625

		0.629

		0.633

		0.637

		0.641

		0.645

		0.649

		0.653

		0.657

		0.661

		0.665

		0.669

		0.673

		0.677

		0.681

		0.685

		0.689

		0.693

		0.697

		0.701

		0.705

		0.709

		0.713

		0.717

		0.721

		0.725

		0.729

		0.733

		0.737

		0.741

		0.745

		0.749

		0.753

		0.757

		0.761

		0.765

		0.769

		0.773

		0.777

		0.781

		0.785

		0.789

		0.793

		0.797

		0.801

		0.805

		0.809

		0.813

		0.817

		0.821

		0.825

		0.829

		0.833

		0.837

		0.841

		0.845

		0.849

		0.853

		0.857

		0.861

		0.865

		0.869

		0.873

		0.877

		0.881

		0.885

		0.889

		0.893

		0.897

		0.901

		0.905

		0.909

		0.913

		0.917

		0.921

		0.925

		0.929

		0.933

		0.937

		0.941

		0.945

		0.949

		0.953

		0.957

		0.961

		0.965

		0.969

		0.973

		0.977

		0.981

		0.985

		0.989

		0.993

		0.997

		1.001

		1.005

		1.009

		1.013

		1.017

		1.021

		1.025

		1.029

		1.033

		1.037

		1.041

		1.045

		1.049

		1.053

		1.057

		1.061

		1.065

		1.069

		1.073

		1.077

		1.081

		1.085

		1.089

		1.093

		1.097

		1.101

		1.105

		1.109

		1.113

		1.117

		1.121

		1.125

		1.129

		1.133

		1.137

		1.141

		1.145

		1.149

		1.153

		1.157

		1.161

		1.165

		1.169

		1.173

		1.177

		1.181

		1.185

		1.189

		1.193

		1.197

		1.201

		1.205

		1.209

		1.213

		1.217

		1.221

		1.225

		1.229

		1.233

		1.237

		1.241

		1.245

		1.249

		1.253

		1.257

		1.261

		1.265

		1.269

		1.273

		1.277

		1.281

		1.285

		1.289

		1.293

		1.297

		1.301

		1.305

		1.309

		1.313

		1.317

		1.321

		1.325

		1.329

		1.333

		1.337

		1.341

		1.345

		1.349

		1.353

		1.357

		1.361

		1.365

		1.369

		1.373

		1.377

		1.381

		1.385

		1.389

		1.393

		1.397

		1.401

		1.405

		1.409

		1.413

		1.417

		1.421

		1.425

		1.429

		1.433

		1.437

		1.441

		1.445

		1.449

		1.453

		1.457

		1.461

		1.465

		1.469

		1.473

		1.477

		1.481

		1.485

		1.489

		1.493

		1.497

		1.501

		1.505

		1.509

		1.513

		1.517

		1.521

		1.525

		1.529

		1.533

		1.537

		1.541

		1.545

		1.549

		1.553

		1.557

		1.561

		1.565

		1.569

		1.573

		1.577

		1.581

		1.585

		1.589

		1.593

		1.597

		1.601

		1.605

		1.609

		1.613

		1.617

		1.621

		1.625

		1.629

		1.633

		1.637

		1.641

		1.645

		1.649

		1.653

		1.657

		1.661

		1.665

		1.669

		1.673

		1.677

		1.681

		1.685

		1.689

		1.693

		1.697

		1.701

		1.705

		1.709

		1.713

		1.717

		1.721

		1.725

		1.729

		1.733

		1.737

		1.741

		1.745

		1.749

		1.753

		1.757

		1.761

		1.765

		1.769

		1.773

		1.777

		1.781

		1.785

		1.789

		1.793

		1.797

		1.801

		1.805

		1.809

		1.813

		1.817

		1.821

		1.825

		1.829

		1.833

		1.837

		1.841

		1.845

		1.849

		1.853

		1.857

		1.861

		1.865

		1.869

		1.873

		1.877

		1.881

		1.885

		1.889

		1.893

		1.897

		1.901

		1.905

		1.909

		1.913

		1.917

		1.921

		1.925

		1.929

		1.933

		1.937

		1.941

		1.945

		1.949

		1.953

		1.957

		1.961

		1.965

		1.969

		1.973

		1.977

		1.981

		1.985

		1.989

		1.993

		1.997

		2.001

		2.005

		2.009

		2.013

		2.017

		2.021

		2.025

		2.029

		2.033

		2.037

		2.041

		2.045

		2.049

		2.053

		2.057

		2.061

		2.065

		2.069

		2.073

		2.077

		2.081

		2.085

		2.089

		2.093

		2.097

		2.101

		2.105

		2.109

		2.113

		2.117

		2.121

		2.125

		2.129

		2.133

		2.137

		2.141

		2.145

		2.149

		2.153

		2.157

		2.161

		2.165

		2.169

		2.173

		2.177

		2.181

		2.185

		2.189

		2.193

		2.197

		2.201

		2.205

		2.209

		2.213

		2.217

		2.221

		2.225

		2.229

		2.233

		2.237

		2.241

		2.245

		2.249

		2.253

		2.257

		2.261

		2.265

		2.269

		2.273

		2.277

		2.281

		2.285

		2.289

		2.293

		2.297

		2.301

		2.305

		2.309

		2.313

		2.317

		2.321

		2.325

		2.329

		2.333

		2.337

		2.341

		2.345

		2.349

		2.353

		2.357

		2.361

		2.365

		2.369

		2.373

		2.377

		2.381

		2.385

		2.389

		2.393

		2.397

		2.401

		2.405

		2.409

		2.413

		2.417

		2.421

		2.425

		2.429

		2.433

		2.437

		2.441

		2.445

		2.449

		2.453

		2.457

		2.461

		2.465

		2.469

		2.473

		2.477

		2.481

		2.485

		2.489

		2.493

		2.497

		2.501

		2.497

		2.493

		2.489

		2.485

		2.481

		2.477

		2.473

		2.469

		2.465

		2.461

		2.457

		2.453

		2.449

		2.445

		2.441

		2.437

		2.433

		2.429

		2.425

		2.421

		2.417

		2.413

		2.409

		2.405

		2.401

		2.397

		2.393

		2.389

		2.385

		2.381

		2.377

		2.373

		2.369

		2.365

		2.361

		2.357

		2.353

		2.349

		2.345

		2.341

		2.337

		2.333

		2.329

		2.325

		2.321

		2.317

		2.313

		2.309

		2.305

		2.301

		2.297

		2.293

		2.289

		2.285

		2.281

		2.277

		2.273

		2.269

		2.265

		2.261

		2.257

		2.253

		2.249

		2.245

		2.241

		2.237

		2.233

		2.229

		2.225

		2.221

		2.217

		2.213

		2.209

		2.205

		2.201

		2.197

		2.193

		2.189

		2.185

		2.181

		2.177

		2.173

		2.169

		2.165

		2.161

		2.157

		2.153

		2.149

		2.145

		2.141

		2.137

		2.133

		2.129

		2.125

		2.121

		2.117

		2.113

		2.109

		2.105

		2.101

		2.097

		2.093

		2.089

		2.085

		2.081

		2.077

		2.073

		2.069

		2.065

		2.061

		2.057

		2.053

		2.049

		2.045

		2.041

		2.037

		2.033

		2.029

		2.025

		2.021

		2.017

		2.013

		2.009

		2.005

		2.001

		1.997

		1.993

		1.989

		1.985

		1.981

		1.977

		1.973

		1.969

		1.965

		1.961

		1.957

		1.953

		1.949

		1.945

		1.941

		1.937

		1.933

		1.929

		1.925

		1.921

		1.917

		1.913

		1.909

		1.905

		1.901

		1.897

		1.893

		1.889

		1.885

		1.881

		1.877

		1.873

		1.869

		1.865

		1.861

		1.857

		1.853

		1.849

		1.845

		1.841

		1.837

		1.833

		1.829

		1.825

		1.821

		1.817

		1.813

		1.809

		1.805

		1.801

		1.797

		1.793

		1.789

		1.785

		1.781

		1.777

		1.773

		1.769

		1.765

		1.761

		1.757

		1.753

		1.749

		1.745

		1.741

		1.737

		1.733

		1.729

		1.725

		1.721

		1.717

		1.713

		1.709

		1.705

		1.701

		1.697

		1.693

		1.689

		1.685

		1.681

		1.677

		1.673

		1.669

		1.665

		1.661

		1.657

		1.653

		1.649

		1.645

		1.641

		1.637

		1.633

		1.629

		1.625

		1.621

		1.617

		1.613

		1.609

		1.605

		1.601

		1.597

		1.593

		1.589

		1.585

		1.581

		1.577

		1.573

		1.569

		1.565

		1.561

		1.557

		1.553

		1.549

		1.545

		1.541

		1.537

		1.533

		1.529

		1.525

		1.521

		1.517

		1.513

		1.509

		1.505

		1.501

		1.497

		1.493

		1.489

		1.485

		1.481

		1.477

		1.473

		1.469

		1.465

		1.461

		1.457

		1.453

		1.449

		1.445

		1.441

		1.437

		1.433

		1.429

		1.425

		1.421

		1.417

		1.413

		1.409

		1.405

		1.401

		1.397

		1.393

		1.389

		1.385

		1.381

		1.377

		1.373

		1.369

		1.365

		1.361

		1.357

		1.353

		1.349

		1.345

		1.341

		1.337

		1.333

		1.329

		1.325

		1.321

		1.317

		1.313

		1.309

		1.305

		1.301

		1.297

		1.293

		1.289

		1.285

		1.281

		1.277

		1.273

		1.269

		1.265

		1.261

		1.257

		1.253

		1.249

		1.245

		1.241

		1.237

		1.233

		1.229

		1.225

		1.221

		1.217

		1.213

		1.209

		1.205

		1.201

		1.197

		1.193

		1.189

		1.185

		1.181

		1.177

		1.173

		1.169

		1.165

		1.161

		1.157

		1.153

		1.149

		1.145

		1.141

		1.137

		1.133

		1.129

		1.125

		1.121

		1.117

		1.113

		1.109

		1.105

		1.101

		1.097

		1.093

		1.089

		1.085

		1.081

		1.077

		1.073

		1.069

		1.065

		1.061

		1.057

		1.053

		1.049

		1.045

		1.041

		1.037

		1.033

		1.029

		1.025

		1.021

		1.017

		1.013

		1.009

		1.005

		1.001

		0.99702

		0.99302

		0.98902

		0.98502

		0.98102

		0.97702

		0.97302

		0.96902

		0.96502

		0.96102

		0.95702

		0.95302

		0.94902

		0.94502



Potential (V)

Current (mA)

0.00301

0.00792

0.01256

0.01734

0.0219

0.0263

0.0307

0.035

0.0394

0.0437

0.048

0.0521

0.0562

0.0606

0.0648

0.069

0.073

0.0774

0.0816

0.0859

0.0901

0.0942

0.0985

0.1028

0.1072

0.1113

0.1156

0.1198

0.124

0.1286

0.1327

0.1369

0.1411

0.1453

0.1497

0.1538

0.1581

0.1623

0.1664

0.1709

0.1749

0.1793

0.1835

0.1876

0.192

0.196

0.2

0.205

0.209

0.214

0.218

0.222

0.226

0.23

0.235

0.239

0.244

0.248

0.252

0.256

0.261

0.265

0.269

0.274

0.278

0.282

0.286

0.29

0.294

0.298

0.302

0.307

0.311

0.315

0.319

0.323

0.327

0.332

0.336

0.339

0.343

0.347

0.352

0.356

0.36

0.364

0.367

0.372

0.375

0.379

0.383

0.387

0.391

0.395

0.399

0.402

0.406

0.41

0.414

0.418

0.421

0.424

0.428

0.432

0.436

0.438

0.442

0.446

0.449

0.453

0.456

0.459

0.462

0.466

0.469

0.471

0.475

0.478

0.481

0.484

0.486

0.489

0.492

0.494

0.497

0.499

0.502

0.504

0.506

0.508

0.51

0.512

0.514

0.515

0.516

0.518

0.518

0.519

0.52

0.52

0.52

0.52

0.52

0.519

0.518

0.516

0.514

0.512

0.51

0.506

0.502
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-0.38

-0.376

-0.372

-0.368

-0.364

-0.36

-0.356

-0.352

-0.348

-0.344

-0.34

-0.336

-0.332

-0.329

-0.325

-0.321

-0.317

-0.314

-0.31

-0.306

-0.303

-0.299

-0.297

-0.293

-0.289

-0.287

-0.284

-0.281

-0.278

-0.274

-0.272

-0.269

-0.266

-0.263

-0.26

-0.258

-0.254

-0.252

-0.25

-0.247

-0.245

-0.242

-0.24

-0.238

-0.236

-0.234

-0.233

-0.231

-0.229

-0.227

-0.225

-0.224

-0.222

-0.221

-0.22

-0.218

-0.217

-0.216

-0.215

-0.214

-0.212

-0.211

-0.21

-0.209

-0.208

-0.207

-0.206

-0.205

-0.204

-0.203

-0.202

-0.201

-0.2

-0.199

-0.198

-0.196

-0.196

-0.194

-0.193

-0.191

-0.19

-0.189

-0.187

-0.186

-0.184

-0.182

-0.18

-0.178

-0.176

-0.175

-0.172

-0.17

-0.168

-0.166

-0.163

-0.161

-0.158

-0.156

-0.153

-0.15

-0.1468

-0.1438

-0.1408

-0.1376

-0.1343

-0.1311

-0.1277

-0.1245

-0.1209

-0.1173

-0.1136

-0.1101

-0.1066

-0.1028

-0.0991

-0.0952

-0.0914

-0.0877

-0.0837

-0.0798

-0.0757

-0.0718

-0.0679

-0.0636

-0.0596

-0.0552

-0.0512

-0.047

-0.0426

-0.0384

-0.0338

-0.0296

-0.0252

-0.0207

-0.0165

-0.0118

-0.00744

-0.00298

0.00158

0.00607

0.01064

0.01505

0.0196

0.0241

0.0284

0.033

0.0373

0.042

0.0464

0.0509

0.0555

0.0598

0.0644

0.0689

0.0734

0.078

0.0823

0.087

0.0914

0.0961

0.1007

0.1052

0.1098

0.1143

0.119

0.1235

0.1281

0.1328

0.1372

0.1418

0.1463

0.1508

0.1552

0.1598

0.1643

0.1686

0.173

0.1774

0.1818

0.1863

0.19

0.195

0.199

0.204

0.208

0.212

0.216

0.22

0.225

0.228

0.233

0.237

0.241

0.246

0.249

0.254

0.258

0.262

0.266

0.27

0.274

0.278

0.282

0.286

0.29

0.294

0.297
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		9.45E-01		3.01E-03		3.01E-06

		9.41E-01		7.92E-03		7.92E-06

		9.37E-01		1.26E-02		1.26E-05

		9.33E-01		1.73E-02		1.73E-05

		9.29E-01		2.19E-02		2.19E-05

		9.25E-01		2.63E-02		2.63E-05

		9.21E-01		3.07E-02		3.07E-05

		9.17E-01		3.50E-02		3.50E-05

		9.13E-01		3.94E-02		3.94E-05

		9.09E-01		4.37E-02		4.37E-05

		9.05E-01		4.80E-02		4.80E-05

		9.01E-01		5.21E-02		5.21E-05

		8.97E-01		5.62E-02		5.62E-05

		8.93E-01		6.06E-02		6.06E-05

		8.89E-01		6.48E-02		6.48E-05

		8.85E-01		6.90E-02		6.90E-05

		8.81E-01		7.30E-02		7.30E-05

		8.77E-01		7.74E-02		7.74E-05

		8.73E-01		8.16E-02		8.16E-05

		8.69E-01		8.59E-02		8.59E-05

		8.65E-01		9.01E-02		9.01E-05

		8.61E-01		9.42E-02		9.42E-05

		8.57E-01		9.85E-02		9.85E-05

		8.53E-01		1.03E-01		1.03E-04

		8.49E-01		1.07E-01		1.07E-04

		8.45E-01		1.11E-01		1.11E-04

		8.41E-01		1.16E-01		1.16E-04

		8.37E-01		1.20E-01		1.20E-04

		8.33E-01		1.24E-01		1.24E-04

		8.29E-01		1.29E-01		1.29E-04

		8.25E-01		1.33E-01		1.33E-04

		8.21E-01		1.37E-01		1.37E-04

		8.17E-01		1.41E-01		1.41E-04

		8.13E-01		1.45E-01		1.45E-04

		8.09E-01		1.50E-01		1.50E-04

		8.05E-01		1.54E-01		1.54E-04

		8.01E-01		1.58E-01		1.58E-04

		7.97E-01		1.62E-01		1.62E-04

		7.93E-01		1.66E-01		1.66E-04

		7.89E-01		1.71E-01		1.71E-04

		7.85E-01		1.75E-01		1.75E-04

		7.81E-01		1.79E-01		1.79E-04

		7.77E-01		1.84E-01		1.84E-04

		7.73E-01		1.88E-01		1.88E-04

		7.69E-01		1.92E-01		1.92E-04

		7.65E-01		1.96E-01		1.96E-04

		7.61E-01		2.00E-01		2.00E-04

		7.57E-01		2.05E-01		2.05E-04

		7.53E-01		2.09E-01		2.09E-04

		7.49E-01		2.14E-01		2.14E-04

		7.45E-01		2.18E-01		2.18E-04

		7.41E-01		2.22E-01		2.22E-04

		7.37E-01		2.26E-01		2.26E-04

		7.33E-01		2.30E-01		2.30E-04

		7.29E-01		2.35E-01		2.35E-04

		7.25E-01		2.39E-01		2.39E-04

		7.21E-01		2.44E-01		2.44E-04

		7.17E-01		2.48E-01		2.48E-04

		7.13E-01		2.52E-01		2.52E-04

		7.09E-01		2.56E-01		2.56E-04

		7.05E-01		2.61E-01		2.61E-04

		7.01E-01		2.65E-01		2.65E-04

		6.97E-01		2.69E-01		2.69E-04

		6.93E-01		2.74E-01		2.74E-04

		6.89E-01		2.78E-01		2.78E-04

		6.85E-01		2.82E-01		2.82E-04

		6.81E-01		2.86E-01		2.86E-04

		6.77E-01		2.90E-01		2.90E-04

		6.73E-01		2.94E-01		2.94E-04

		6.69E-01		2.98E-01		2.98E-04

		6.65E-01		3.02E-01		3.02E-04

		6.61E-01		3.07E-01		3.07E-04

		6.57E-01		3.11E-01		3.11E-04

		6.53E-01		3.15E-01		3.15E-04

		6.49E-01		3.19E-01		3.19E-04

		6.45E-01		3.23E-01		3.23E-04

		6.41E-01		3.27E-01		3.27E-04

		6.37E-01		3.32E-01		3.32E-04

		6.33E-01		3.36E-01		3.36E-04

		6.29E-01		3.39E-01		3.39E-04

		6.25E-01		3.43E-01		3.43E-04

		6.21E-01		3.47E-01		3.47E-04

		6.17E-01		3.52E-01		3.52E-04

		6.13E-01		3.56E-01		3.56E-04

		6.09E-01		3.60E-01		3.60E-04

		6.05E-01		3.64E-01		3.64E-04

		6.01E-01		3.67E-01		3.67E-04

		5.97E-01		3.72E-01		3.72E-04

		5.93E-01		3.75E-01		3.75E-04

		5.89E-01		3.79E-01		3.79E-04

		5.85E-01		3.83E-01		3.83E-04

		5.81E-01		3.87E-01		3.87E-04

		5.77E-01		3.91E-01		3.91E-04

		5.73E-01		3.95E-01		3.95E-04

		5.69E-01		3.99E-01		3.99E-04

		5.65E-01		4.02E-01		4.02E-04

		5.61E-01		4.06E-01		4.06E-04

		5.57E-01		4.10E-01		4.10E-04

		5.53E-01		4.14E-01		4.14E-04

		5.49E-01		4.18E-01		4.18E-04

		5.45E-01		4.21E-01		4.21E-04

		5.41E-01		4.24E-01		4.24E-04

		5.37E-01		4.28E-01		4.28E-04

		5.33E-01		4.32E-01		4.32E-04

		5.29E-01		4.36E-01		4.36E-04

		5.25E-01		4.38E-01		4.38E-04

		5.21E-01		4.42E-01		4.42E-04

		5.17E-01		4.46E-01		4.46E-04

		5.13E-01		4.49E-01		4.49E-04

		5.09E-01		4.53E-01		4.53E-04

		5.05E-01		4.56E-01		4.56E-04

		5.01E-01		4.59E-01		4.59E-04

		4.97E-01		4.62E-01		4.62E-04

		4.93E-01		4.66E-01		4.66E-04

		4.89E-01		4.69E-01		4.69E-04

		4.85E-01		4.71E-01		4.71E-04

		4.81E-01		4.75E-01		4.75E-04

		4.77E-01		4.78E-01		4.78E-04

		4.73E-01		4.81E-01		4.81E-04

		4.69E-01		4.84E-01		4.84E-04

		4.65E-01		4.86E-01		4.86E-04

		4.61E-01		4.89E-01		4.89E-04

		4.57E-01		4.92E-01		4.92E-04

		4.53E-01		4.94E-01		4.94E-04

		4.49E-01		4.97E-01		4.97E-04

		4.45E-01		4.99E-01		4.99E-04

		4.41E-01		5.02E-01		5.02E-04

		4.37E-01		5.04E-01		5.04E-04

		4.33E-01		5.06E-01		5.06E-04

		4.29E-01		5.08E-01		5.08E-04

		4.25E-01		5.10E-01		5.10E-04

		4.21E-01		5.12E-01		5.12E-04

		4.17E-01		5.14E-01		5.14E-04

		4.13E-01		5.15E-01		5.15E-04

		4.09E-01		5.16E-01		5.16E-04

		4.05E-01		5.18E-01		5.18E-04

		4.01E-01		5.18E-01		5.18E-04

		3.97E-01		5.19E-01		5.19E-04

		3.93E-01		5.20E-01		5.20E-04

		3.89E-01		5.20E-01		5.20E-04

		3.85E-01		5.20E-01		5.20E-04

		3.81E-01		5.20E-01		5.20E-04

		3.77E-01		5.20E-01		5.20E-04

		3.73E-01		5.19E-01		5.19E-04

		3.69E-01		5.18E-01		5.18E-04

		3.65E-01		5.16E-01		5.16E-04

		3.61E-01		5.14E-01		5.14E-04

		3.57E-01		5.12E-01		5.12E-04

		3.53E-01		5.10E-01		5.10E-04

		3.49E-01		5.06E-01		5.06E-04

		3.45E-01		5.02E-01		5.02E-04

		3.41E-01		4.97E-01		4.97E-04

		3.37E-01		4.91E-01		4.91E-04

		3.33E-01		4.85E-01		4.85E-04

		3.29E-01		4.78E-01		4.78E-04

		3.25E-01		4.70E-01		4.70E-04

		3.21E-01		4.62E-01		4.62E-04

		3.17E-01		4.54E-01		4.54E-04

		3.13E-01		4.46E-01		4.46E-04

		3.09E-01		4.39E-01		4.39E-04

		3.05E-01		4.33E-01		4.33E-04

		3.01E-01		4.26E-01		4.26E-04

		2.97E-01		4.21E-01		4.21E-04

		2.93E-01		4.16E-01		4.16E-04

		2.89E-01		4.11E-01		4.11E-04

		2.85E-01		4.06E-01		4.06E-04

		2.81E-01		4.02E-01		4.02E-04

		2.77E-01		3.98E-01		3.98E-04

		2.73E-01		3.94E-01		3.94E-04

		2.69E-01		3.90E-01		3.90E-04

		2.65E-01		3.86E-01		3.86E-04

		2.61E-01		3.83E-01		3.83E-04

		2.57E-01		3.80E-01		3.80E-04

		2.53E-01		3.76E-01		3.76E-04

		2.49E-01		3.73E-01		3.73E-04

		2.45E-01		3.70E-01		3.70E-04

		2.41E-01		3.68E-01		3.68E-04

		2.37E-01		3.65E-01		3.65E-04

		2.33E-01		3.62E-01		3.62E-04

		2.29E-01		3.59E-01		3.59E-04

		2.25E-01		3.57E-01		3.57E-04

		2.21E-01		3.54E-01		3.54E-04

		2.17E-01		3.52E-01		3.52E-04

		2.13E-01		3.50E-01		3.50E-04

		2.09E-01		3.47E-01		3.47E-04

		2.05E-01		3.45E-01		3.45E-04

		2.01E-01		3.43E-01		3.43E-04

		1.97E-01		3.41E-01		3.41E-04

		1.93E-01		3.39E-01		3.39E-04

		1.89E-01		3.37E-01		3.37E-04

		1.85E-01		3.34E-01		3.34E-04

		1.81E-01		3.33E-01		3.33E-04

		1.77E-01		3.30E-01		3.30E-04

		1.73E-01		3.29E-01		3.29E-04

		1.69E-01		3.27E-01		3.27E-04

		1.65E-01		3.25E-01		3.25E-04

		1.61E-01		3.24E-01		3.24E-04

		1.57E-01		3.22E-01		3.22E-04

		1.53E-01		3.20E-01		3.20E-04

		1.49E-01		3.18E-01		3.18E-04

		1.45E-01		3.16E-01		3.16E-04

		1.41E-01		3.15E-01		3.15E-04

		1.37E-01		3.13E-01		3.13E-04

		1.33E-01		3.12E-01		3.12E-04

		1.29E-01		3.10E-01		3.10E-04

		1.25E-01		3.08E-01		3.08E-04

		1.21E-01		3.07E-01		3.07E-04

		1.17E-01		3.05E-01		3.05E-04

		1.13E-01		3.04E-01		3.04E-04

		1.09E-01		3.02E-01		3.02E-04

		1.05E-01		3.01E-01		3.01E-04

		1.01E-01		3.00E-01		3.00E-04

		9.70E-02		2.98E-01		2.98E-04

		9.30E-02		2.97E-01		2.97E-04

		8.90E-02		2.95E-01		2.95E-04

		8.50E-02		2.94E-01		2.94E-04

		8.10E-02		2.93E-01		2.93E-04

		7.70E-02		2.92E-01		2.92E-04

		7.30E-02		2.91E-01		2.91E-04

		6.90E-02		2.89E-01		2.89E-04

		6.50E-02		2.88E-01		2.88E-04

		6.10E-02		2.86E-01		2.86E-04

		5.70E-02		2.85E-01		2.85E-04

		5.30E-02		2.84E-01		2.84E-04

		4.90E-02		2.83E-01		2.83E-04

		4.50E-02		2.82E-01		2.82E-04

		4.10E-02		2.80E-01		2.80E-04

		3.70E-02		2.79E-01		2.79E-04

		3.30E-02		2.79E-01		2.79E-04

		2.90E-02		2.77E-01		2.77E-04

		2.50E-02		2.76E-01		2.76E-04

		2.10E-02		2.75E-01		2.75E-04

		1.70E-02		2.74E-01		2.74E-04

		1.30E-02		2.73E-01		2.73E-04

		9.00E-03		2.72E-01		2.72E-04

		5.00E-03		2.71E-01		2.71E-04

		9.99E-04		2.70E-01		2.70E-04

		-3.00E-03		2.69E-01		2.69E-04

		-7.00E-03		2.68E-01		2.68E-04

		-1.10E-02		2.67E-01		2.67E-04

		-1.50E-02		2.66E-01		2.66E-04

		-1.90E-02		2.65E-01		2.65E-04

		-2.30E-02		2.64E-01		2.64E-04

		-2.70E-02		2.63E-01		2.63E-04

		-3.10E-02		2.62E-01		2.62E-04

		-3.50E-02		2.61E-01		2.61E-04

		-3.90E-02		2.60E-01		2.60E-04

		-4.30E-02		2.60E-01		2.60E-04

		-4.70E-02		2.59E-01		2.59E-04

		-5.10E-02		2.58E-01		2.58E-04

		-5.50E-02		2.57E-01		2.57E-04

		-5.90E-02		2.56E-01		2.56E-04

		-6.30E-02		2.55E-01		2.55E-04

		-6.70E-02		2.54E-01		2.54E-04

		-7.10E-02		2.54E-01		2.54E-04

		-7.50E-02		2.53E-01		2.53E-04

		-7.90E-02		2.52E-01		2.52E-04

		-8.30E-02		2.51E-01		2.51E-04

		-8.70E-02		2.51E-01		2.51E-04

		-9.10E-02		2.50E-01		2.50E-04

		-9.50E-02		2.49E-01		2.49E-04

		-9.90E-02		2.48E-01		2.48E-04

		-1.03E-01		2.47E-01		2.47E-04

		-1.07E-01		2.47E-01		2.47E-04

		-1.11E-01		2.46E-01		2.46E-04

		-1.15E-01		2.46E-01		2.46E-04

		-1.19E-01		2.45E-01		2.45E-04

		-1.23E-01		2.44E-01		2.44E-04

		-1.27E-01		2.44E-01		2.44E-04

		-1.31E-01		2.43E-01		2.43E-04

		-1.35E-01		2.42E-01		2.42E-04

		-1.39E-01		2.42E-01		2.42E-04

		-1.43E-01		2.42E-01		2.42E-04

		-1.47E-01		2.42E-01		2.42E-04

		-1.51E-01		2.40E-01		2.40E-04

		-1.55E-01		2.40E-01		2.40E-04

		-1.59E-01		2.40E-01		2.40E-04

		-1.63E-01		2.39E-01		2.39E-04

		-1.67E-01		2.40E-01		2.40E-04

		-1.71E-01		2.38E-01		2.38E-04

		-1.75E-01		2.38E-01		2.38E-04

		-1.79E-01		2.38E-01		2.38E-04

		-1.83E-01		2.38E-01		2.38E-04

		-1.87E-01		2.39E-01		2.39E-04

		-1.91E-01		2.38E-01		2.38E-04

		-1.95E-01		2.38E-01		2.38E-04

		-1.99E-01		2.39E-01		2.39E-04

		-2.03E-01		2.40E-01		2.40E-04

		-2.07E-01		2.40E-01		2.40E-04

		-2.11E-01		2.40E-01		2.40E-04

		-2.15E-01		2.42E-01		2.42E-04

		-2.19E-01		2.42E-01		2.42E-04

		-2.23E-01		2.43E-01		2.43E-04

		-2.27E-01		2.45E-01		2.45E-04

		-2.31E-01		2.46E-01		2.46E-04

		-2.35E-01		2.48E-01		2.48E-04

		-2.39E-01		2.50E-01		2.50E-04

		-2.43E-01		2.51E-01		2.51E-04

		-2.47E-01		2.54E-01		2.54E-04

		-2.51E-01		2.55E-01		2.55E-04

		-2.55E-01		2.57E-01		2.57E-04

		-2.59E-01		2.59E-01		2.59E-04

		-2.63E-01		2.62E-01		2.62E-04

		-2.67E-01		2.64E-01		2.64E-04

		-2.71E-01		2.66E-01		2.66E-04

		-2.75E-01		2.69E-01		2.69E-04

		-2.79E-01		2.71E-01		2.71E-04

		-2.83E-01		2.74E-01		2.74E-04

		-2.87E-01		2.77E-01		2.77E-04

		-2.91E-01		2.80E-01		2.80E-04

		-2.95E-01		2.83E-01		2.83E-04

		-2.99E-01		2.86E-01		2.86E-04

		-3.03E-01		2.88E-01		2.88E-04

		-3.07E-01		2.91E-01		2.91E-04

		-3.11E-01		2.94E-01		2.94E-04

		-3.15E-01		2.97E-01		2.97E-04

		-3.19E-01		3.00E-01		3.00E-04

		-3.23E-01		3.03E-01		3.03E-04

		-3.27E-01		3.06E-01		3.06E-04

		-3.31E-01		3.09E-01		3.09E-04

		-3.35E-01		3.12E-01		3.12E-04

		-3.39E-01		3.15E-01		3.15E-04

		-3.43E-01		3.18E-01		3.18E-04

		-3.47E-01		3.22E-01		3.22E-04

		-3.51E-01		3.25E-01		3.25E-04

		-3.55E-01		3.28E-01		3.28E-04

		-3.59E-01		3.31E-01		3.31E-04

		-3.63E-01		3.34E-01		3.34E-04

		-3.67E-01		3.37E-01		3.37E-04

		-3.71E-01		3.40E-01		3.40E-04

		-3.75E-01		3.43E-01		3.43E-04

		-3.79E-01		3.46E-01		3.46E-04

		-3.83E-01		3.49E-01		3.49E-04

		-3.87E-01		3.52E-01		3.52E-04

		-3.91E-01		3.56E-01		3.56E-04

		-3.95E-01		3.58E-01		3.58E-04

		-3.99E-01		3.62E-01		3.62E-04

		-4.03E-01		3.65E-01		3.65E-04

		-4.07E-01		3.68E-01		3.68E-04

		-4.11E-01		3.71E-01		3.71E-04

		-4.15E-01		3.74E-01		3.74E-04

		-4.19E-01		3.78E-01		3.78E-04

		-4.23E-01		3.81E-01		3.81E-04

		-4.27E-01		3.84E-01		3.84E-04

		-4.31E-01		3.87E-01		3.87E-04

		-4.35E-01		3.90E-01		3.90E-04

		-4.39E-01		3.93E-01		3.93E-04

		-4.43E-01		3.96E-01		3.96E-04

		-4.47E-01		4.00E-01		4.00E-04

		-4.51E-01		4.02E-01		4.02E-04

		-4.55E-01		4.06E-01		4.06E-04

		-4.59E-01		4.09E-01		4.09E-04

		-4.63E-01		4.11E-01		4.11E-04

		-4.67E-01		4.15E-01		4.15E-04

		-4.71E-01		4.17E-01		4.17E-04

		-4.75E-01		4.20E-01		4.20E-04

		-4.79E-01		4.23E-01		4.23E-04

		-4.83E-01		4.26E-01		4.26E-04

		-4.87E-01		4.29E-01		4.29E-04

		-4.91E-01		4.31E-01		4.31E-04

		-4.95E-01		4.34E-01		4.34E-04

		-4.99E-01		4.36E-01		4.36E-04

		-5.03E-01		4.39E-01		4.39E-04

		-5.07E-01		4.42E-01		4.42E-04

		-5.11E-01		4.44E-01		4.44E-04

		-5.15E-01		4.47E-01		4.47E-04

		-5.19E-01		4.50E-01		4.50E-04

		-5.23E-01		4.52E-01		4.52E-04

		-5.27E-01		4.54E-01		4.54E-04

		-5.31E-01		4.56E-01		4.56E-04

		-5.35E-01		4.59E-01		4.59E-04

		-5.39E-01		4.61E-01		4.61E-04

		-5.43E-01		4.64E-01		4.64E-04

		-5.47E-01		4.66E-01		4.66E-04

		-5.51E-01		4.68E-01		4.68E-04

		-5.55E-01		4.70E-01		4.70E-04

		-5.59E-01		4.73E-01		4.73E-04

		-5.63E-01		4.75E-01		4.75E-04

		-5.67E-01		4.77E-01		4.77E-04

		-5.71E-01		4.79E-01		4.79E-04

		-5.75E-01		4.81E-01		4.81E-04

		-5.79E-01		4.82E-01		4.82E-04

		-5.83E-01		4.84E-01		4.84E-04

		-5.87E-01		4.86E-01		4.86E-04

		-5.91E-01		4.88E-01		4.88E-04

		-5.95E-01		4.90E-01		4.90E-04

		-5.99E-01		4.91E-01		4.91E-04

		-6.03E-01		4.92E-01		4.92E-04

		-6.07E-01		4.94E-01		4.94E-04

		-6.11E-01		4.95E-01		4.95E-04

		-6.15E-01		4.96E-01		4.96E-04

		-6.19E-01		4.97E-01		4.97E-04

		-6.23E-01		4.98E-01		4.98E-04

		-6.27E-01		4.99E-01		4.99E-04

		-6.31E-01		5.00E-01		5.00E-04

		-6.35E-01		5.01E-01		5.01E-04

		-6.39E-01		5.02E-01		5.02E-04

		-6.43E-01		5.02E-01		5.02E-04

		-6.47E-01		5.02E-01		5.02E-04

		-6.51E-01		5.03E-01		5.03E-04

		-6.55E-01		5.03E-01		5.03E-04

		-6.59E-01		5.03E-01		5.03E-04

		-6.63E-01		5.04E-01		5.04E-04

		-6.67E-01		5.03E-01		5.03E-04

		-6.71E-01		5.03E-01		5.03E-04

		-6.75E-01		5.03E-01		5.03E-04

		-6.79E-01		5.03E-01		5.03E-04

		-6.83E-01		5.03E-01		5.03E-04

		-6.87E-01		5.02E-01		5.02E-04

		-6.91E-01		5.02E-01		5.02E-04

		-6.95E-01		5.01E-01		5.01E-04

		-6.99E-01		5.01E-01		5.01E-04

		-7.03E-01		5.00E-01		5.00E-04

		-7.07E-01		5.00E-01		5.00E-04

		-7.11E-01		4.99E-01		4.99E-04

		-7.15E-01		4.98E-01		4.98E-04

		-7.19E-01		4.98E-01		4.98E-04

		-7.23E-01		4.96E-01		4.96E-04

		-7.27E-01		4.95E-01		4.95E-04

		-7.31E-01		4.94E-01		4.94E-04

		-7.35E-01		4.93E-01		4.93E-04

		-7.39E-01		4.92E-01		4.92E-04

		-7.43E-01		4.90E-01		4.90E-04

		-7.47E-01		4.89E-01		4.89E-04

		-7.51E-01		4.88E-01		4.88E-04

		-7.55E-01		4.88E-01		4.88E-04

		-7.59E-01		4.87E-01		4.87E-04

		-7.63E-01		4.86E-01		4.86E-04

		-7.67E-01		4.86E-01		4.86E-04

		-7.71E-01		4.84E-01		4.84E-04

		-7.75E-01		4.84E-01		4.84E-04

		-7.79E-01		4.83E-01		4.83E-04

		-7.83E-01		4.82E-01		4.82E-04

		-7.87E-01		4.82E-01		4.82E-04

		-7.91E-01		4.82E-01		4.82E-04

		-7.95E-01		4.82E-01		4.82E-04

		-7.99E-01		4.81E-01		4.81E-04

		-8.03E-01		4.81E-01		4.81E-04

		-8.07E-01		4.80E-01		4.80E-04

		-8.11E-01		4.79E-01		4.79E-04

		-8.15E-01		4.78E-01		4.78E-04

		-8.19E-01		4.77E-01		4.77E-04

		-8.23E-01		4.78E-01		4.78E-04

		-8.27E-01		4.78E-01		4.78E-04

		-8.31E-01		4.78E-01		4.78E-04

		-8.35E-01		4.78E-01		4.78E-04

		-8.39E-01		4.78E-01		4.78E-04

		-8.43E-01		4.79E-01		4.79E-04

		-8.47E-01		4.78E-01		4.78E-04

		-8.51E-01		4.76E-01		4.76E-04

		-8.55E-01		4.75E-01		4.75E-04

		-8.59E-01		4.74E-01		4.74E-04

		-8.63E-01		4.73E-01		4.73E-04

		-8.67E-01		4.72E-01		4.72E-04

		-8.71E-01		4.71E-01		4.71E-04

		-8.75E-01		4.74E-01		4.74E-04

		-8.79E-01		4.71E-01		4.71E-04

		-8.83E-01		4.70E-01		4.70E-04

		-8.87E-01		4.68E-01		4.68E-04

		-8.91E-01		4.68E-01		4.68E-04

		-8.95E-01		4.67E-01		4.67E-04

		-8.99E-01		4.66E-01		4.66E-04

		-9.03E-01		4.66E-01		4.66E-04

		-9.07E-01		4.64E-01		4.64E-04

		-9.11E-01		4.64E-01		4.64E-04

		-9.15E-01		4.64E-01		4.64E-04

		-9.19E-01		4.62E-01		4.62E-04

		-9.23E-01		4.60E-01		4.60E-04

		-9.27E-01		4.58E-01		4.58E-04

		-9.31E-01		4.56E-01		4.56E-04

		-9.35E-01		4.56E-01		4.56E-04

		-9.39E-01		4.60E-01		4.60E-04

		-9.43E-01		4.57E-01		4.57E-04

		-9.47E-01		4.56E-01		4.56E-04

		-9.51E-01		4.54E-01		4.54E-04

		-9.55E-01		4.56E-01		4.56E-04

		-9.59E-01		4.54E-01		4.54E-04

		-9.63E-01		4.58E-01		4.58E-04

		-9.67E-01		4.56E-01		4.56E-04

		-9.71E-01		4.54E-01		4.54E-04

		-9.75E-01		4.53E-01		4.53E-04

		-9.79E-01		4.51E-01		4.51E-04

		-9.83E-01		4.50E-01		4.50E-04

		-9.87E-01		4.48E-01		4.48E-04

		-9.91E-01		4.47E-01		4.47E-04

		-9.95E-01		4.46E-01		4.46E-04

		-9.99E-01		4.45E-01		4.45E-04

		-9.95E-01		4.44E-01		4.44E-04

		-9.91E-01		4.38E-01		4.38E-04

		-9.87E-01		4.35E-01		4.35E-04

		-9.83E-01		4.32E-01		4.32E-04

		-9.79E-01		4.33E-01		4.33E-04

		-9.75E-01		4.28E-01		4.28E-04

		-9.71E-01		4.25E-01		4.25E-04

		-9.67E-01		4.22E-01		4.22E-04

		-9.63E-01		4.20E-01		4.20E-04

		-9.59E-01		4.18E-01		4.18E-04

		-9.55E-01		4.18E-01		4.18E-04

		-9.51E-01		4.18E-01		4.18E-04

		-9.47E-01		4.15E-01		4.15E-04

		-9.43E-01		4.14E-01		4.14E-04

		-9.39E-01		4.12E-01		4.12E-04

		-9.35E-01		4.17E-01		4.17E-04

		-9.31E-01		4.11E-01		4.11E-04

		-9.27E-01		4.10E-01		4.10E-04

		-9.23E-01		4.07E-01		4.07E-04

		-9.19E-01		4.05E-01		4.05E-04

		-9.15E-01		4.02E-01		4.02E-04

		-9.11E-01		3.99E-01		3.99E-04

		-9.07E-01		3.98E-01		3.98E-04

		-9.03E-01		3.98E-01		3.98E-04

		-8.99E-01		3.97E-01		3.97E-04

		-8.95E-01		3.95E-01		3.95E-04

		-8.91E-01		3.93E-01		3.93E-04

		-8.87E-01		3.90E-01		3.90E-04

		-8.83E-01		3.89E-01		3.89E-04

		-8.79E-01		3.87E-01		3.87E-04

		-8.75E-01		3.85E-01		3.85E-04

		-8.71E-01		3.84E-01		3.84E-04

		-8.67E-01		3.81E-01		3.81E-04

		-8.63E-01		3.80E-01		3.80E-04

		-8.59E-01		3.83E-01		3.83E-04

		-8.55E-01		3.81E-01		3.81E-04

		-8.51E-01		3.78E-01		3.78E-04

		-8.47E-01		3.79E-01		3.79E-04

		-8.43E-01		3.75E-01		3.75E-04

		-8.39E-01		3.72E-01		3.72E-04

		-8.35E-01		3.71E-01		3.71E-04

		-8.31E-01		3.68E-01		3.68E-04

		-8.27E-01		3.65E-01		3.65E-04

		-8.23E-01		3.62E-01		3.62E-04

		-8.19E-01		3.60E-01		3.60E-04

		-8.15E-01		3.59E-01		3.59E-04

		-8.11E-01		3.56E-01		3.56E-04

		-8.07E-01		3.54E-01		3.54E-04

		-8.03E-01		3.52E-01		3.52E-04

		-7.99E-01		3.50E-01		3.50E-04

		-7.95E-01		3.51E-01		3.51E-04

		-7.91E-01		3.49E-01		3.49E-04

		-7.87E-01		3.48E-01		3.48E-04

		-7.83E-01		3.47E-01		3.47E-04

		-7.79E-01		3.46E-01		3.46E-04

		-7.75E-01		3.44E-01		3.44E-04

		-7.71E-01		3.41E-01		3.41E-04

		-7.67E-01		3.40E-01		3.40E-04

		-7.63E-01		3.38E-01		3.38E-04

		-7.59E-01		3.36E-01		3.36E-04

		-7.55E-01		3.34E-01		3.34E-04

		-7.51E-01		3.32E-01		3.32E-04

		-7.47E-01		3.34E-01		3.34E-04

		-7.43E-01		3.32E-01		3.32E-04

		-7.39E-01		3.30E-01		3.30E-04

		-7.35E-01		3.28E-01		3.28E-04

		-7.31E-01		3.26E-01		3.26E-04

		-7.27E-01		3.24E-01		3.24E-04

		-7.23E-01		3.23E-01		3.23E-04

		-7.19E-01		3.22E-01		3.22E-04

		-7.15E-01		3.20E-01		3.20E-04

		-7.11E-01		3.18E-01		3.18E-04

		-7.07E-01		3.16E-01		3.16E-04

		-7.03E-01		3.14E-01		3.14E-04

		-6.99E-01		3.14E-01		3.14E-04

		-6.95E-01		3.11E-01		3.11E-04

		-6.91E-01		3.10E-01		3.10E-04

		-6.87E-01		3.08E-01		3.08E-04

		-6.83E-01		3.06E-01		3.06E-04

		-6.79E-01		3.05E-01		3.05E-04

		-6.75E-01		3.03E-01		3.03E-04

		-6.71E-01		3.04E-01		3.04E-04

		-6.67E-01		3.03E-01		3.03E-04

		-6.63E-01		3.00E-01		3.00E-04

		-6.59E-01		2.98E-01		2.98E-04

		-6.55E-01		2.96E-01		2.96E-04

		-6.51E-01		2.96E-01		2.96E-04

		-6.47E-01		2.94E-01		2.94E-04

		-6.43E-01		2.92E-01		2.92E-04

		-6.39E-01		2.90E-01		2.90E-04

		-6.35E-01		2.89E-01		2.89E-04

		-6.31E-01		2.88E-01		2.88E-04

		-6.27E-01		2.85E-01		2.85E-04

		-6.23E-01		2.84E-01		2.84E-04

		-6.19E-01		2.82E-01		2.82E-04

		-6.15E-01		2.80E-01		2.80E-04

		-6.11E-01		2.78E-01		2.78E-04

		-6.07E-01		2.77E-01		2.77E-04

		-6.03E-01		2.75E-01		2.75E-04

		-5.99E-01		2.74E-01		2.74E-04

		-5.95E-01		2.72E-01		2.72E-04

		-5.91E-01		2.71E-01		2.71E-04

		-5.87E-01		2.69E-01		2.69E-04

		-5.83E-01		2.68E-01		2.68E-04

		-5.79E-01		2.66E-01		2.66E-04

		-5.75E-01		2.65E-01		2.65E-04

		-5.71E-01		2.64E-01		2.64E-04

		-5.67E-01		2.62E-01		2.62E-04

		-5.63E-01		2.61E-01		2.61E-04

		-5.59E-01		2.59E-01		2.59E-04

		-5.55E-01		2.58E-01		2.58E-04

		-5.51E-01		2.57E-01		2.57E-04

		-5.47E-01		2.55E-01		2.55E-04

		-5.43E-01		2.55E-01		2.55E-04

		-5.39E-01		2.54E-01		2.54E-04

		-5.35E-01		2.53E-01		2.53E-04

		-5.31E-01		2.54E-01		2.54E-04

		-5.27E-01		2.52E-01		2.52E-04

		-5.23E-01		2.50E-01		2.50E-04

		-5.19E-01		2.48E-01		2.48E-04

		-5.15E-01		2.47E-01		2.47E-04

		-5.11E-01		2.45E-01		2.45E-04

		-5.07E-01		2.44E-01		2.44E-04

		-5.03E-01		2.43E-01		2.43E-04

		-4.99E-01		2.42E-01		2.42E-04

		-4.95E-01		2.40E-01		2.40E-04

		-4.91E-01		2.38E-01		2.38E-04

		-4.87E-01		2.37E-01		2.37E-04

		-4.83E-01		2.35E-01		2.35E-04

		-4.79E-01		2.33E-01		2.33E-04

		-4.75E-01		2.31E-01		2.31E-04

		-4.71E-01		2.30E-01		2.30E-04

		-4.67E-01		2.28E-01		2.28E-04

		-4.63E-01		2.26E-01		2.26E-04

		-4.59E-01		2.24E-01		2.24E-04

		-4.55E-01		2.22E-01		2.22E-04

		-4.51E-01		2.20E-01		2.20E-04

		-4.47E-01		2.18E-01		2.18E-04

		-4.43E-01		2.16E-01		2.16E-04

		-4.39E-01		2.14E-01		2.14E-04

		-4.35E-01		2.12E-01		2.12E-04

		-4.31E-01		2.10E-01		2.10E-04

		-4.27E-01		2.08E-01		2.08E-04

		-4.23E-01		2.06E-01		2.06E-04

		-4.19E-01		2.05E-01		2.05E-04

		-4.15E-01		2.04E-01		2.04E-04

		-4.11E-01		2.02E-01		2.02E-04

		-4.07E-01		1.99E-01		1.99E-04

		-4.03E-01		1.97E-01		1.97E-04

		-3.99E-01		1.97E-01		1.97E-04

		-3.95E-01		1.94E-01		1.94E-04

		-3.91E-01		1.92E-01		1.92E-04

		-3.87E-01		1.90E-01		1.90E-04

		-3.83E-01		1.88E-01		1.88E-04

		-3.79E-01		1.86E-01		1.86E-04

		-3.75E-01		1.83E-01		1.83E-04

		-3.71E-01		1.82E-01		1.82E-04

		-3.67E-01		1.79E-01		1.79E-04

		-3.63E-01		1.77E-01		1.77E-04

		-3.59E-01		1.74E-01		1.74E-04

		-3.55E-01		1.72E-01		1.72E-04

		-3.51E-01		1.70E-01		1.70E-04

		-3.47E-01		1.68E-01		1.68E-04

		-3.43E-01		1.66E-01		1.66E-04

		-3.39E-01		1.64E-01		1.64E-04

		-3.35E-01		1.61E-01		1.61E-04

		-3.31E-01		1.59E-01		1.59E-04

		-3.27E-01		1.56E-01		1.56E-04

		-3.23E-01		1.54E-01		1.54E-04

		-3.19E-01		1.52E-01		1.52E-04

		-3.15E-01		1.49E-01		1.49E-04

		-3.11E-01		1.47E-01		1.47E-04

		-3.07E-01		1.44E-01		1.44E-04

		-3.03E-01		1.42E-01		1.42E-04

		-2.99E-01		1.40E-01		1.40E-04

		-2.95E-01		1.38E-01		1.38E-04

		-2.91E-01		1.35E-01		1.35E-04

		-2.87E-01		1.33E-01		1.33E-04

		-2.83E-01		1.31E-01		1.31E-04

		-2.79E-01		1.29E-01		1.29E-04

		-2.75E-01		1.27E-01		1.27E-04

		-2.71E-01		1.25E-01		1.25E-04

		-2.67E-01		1.23E-01		1.23E-04

		-2.63E-01		1.21E-01		1.21E-04

		-2.59E-01		1.19E-01		1.19E-04

		-2.55E-01		1.17E-01		1.17E-04

		-2.51E-01		1.15E-01		1.15E-04

		-2.47E-01		1.13E-01		1.13E-04

		-2.43E-01		1.11E-01		1.11E-04

		-2.39E-01		1.09E-01		1.09E-04

		-2.35E-01		1.08E-01		1.08E-04

		-2.31E-01		1.06E-01		1.06E-04

		-2.27E-01		1.04E-01		1.04E-04

		-2.23E-01		1.03E-01		1.03E-04

		-2.19E-01		1.01E-01		1.01E-04

		-2.15E-01		9.93E-02		9.93E-05

		-2.11E-01		9.78E-02		9.78E-05

		-2.07E-01		9.63E-02		9.63E-05

		-2.03E-01		9.50E-02		9.50E-05

		-1.99E-01		9.35E-02		9.35E-05

		-1.95E-01		9.25E-02		9.25E-05

		-1.91E-01		9.12E-02		9.12E-05

		-1.87E-01		8.98E-02		8.98E-05

		-1.83E-01		8.88E-02		8.88E-05

		-1.79E-01		8.76E-02		8.76E-05

		-1.75E-01		8.66E-02		8.66E-05

		-1.71E-01		8.55E-02		8.55E-05

		-1.67E-01		8.46E-02		8.46E-05

		-1.63E-01		8.38E-02		8.38E-05

		-1.59E-01		8.28E-02		8.28E-05

		-1.55E-01		8.22E-02		8.22E-05

		-1.51E-01		8.14E-02		8.14E-05

		-1.47E-01		8.07E-02		8.07E-05

		-1.43E-01		8.02E-02		8.02E-05

		-1.39E-01		7.96E-02		7.96E-05

		-1.35E-01		7.91E-02		7.91E-05

		-1.31E-01		7.86E-02		7.86E-05

		-1.27E-01		7.83E-02		7.83E-05

		-1.23E-01		7.80E-02		7.80E-05

		-1.19E-01		7.76E-02		7.76E-05

		-1.15E-01		7.74E-02		7.74E-05

		-1.11E-01		7.70E-02		7.70E-05

		-1.07E-01		7.69E-02		7.69E-05

		-1.03E-01		7.66E-02		7.66E-05

		-9.90E-02		7.65E-02		7.65E-05

		-9.50E-02		7.63E-02		7.63E-05

		-9.10E-02		7.62E-02		7.62E-05

		-8.70E-02		7.61E-02		7.61E-05

		-8.30E-02		7.60E-02		7.60E-05

		-7.90E-02		7.62E-02		7.62E-05

		-7.50E-02		7.59E-02		7.59E-05

		-7.10E-02		7.58E-02		7.58E-05

		-6.70E-02		7.57E-02		7.57E-05

		-6.30E-02		7.59E-02		7.59E-05

		-5.90E-02		7.57E-02		7.57E-05

		-5.50E-02		7.56E-02		7.56E-05

		-5.10E-02		7.56E-02		7.56E-05

		-4.70E-02		7.56E-02		7.56E-05

		-4.30E-02		7.55E-02		7.55E-05

		-3.90E-02		7.55E-02		7.55E-05

		-3.50E-02		7.55E-02		7.55E-05

		-3.10E-02		7.55E-02		7.55E-05

		-2.70E-02		7.55E-02		7.55E-05

		-2.30E-02		7.56E-02		7.56E-05

		-1.90E-02		7.55E-02		7.55E-05

		-1.50E-02		7.55E-02		7.55E-05

		-1.10E-02		7.56E-02		7.56E-05

		-7.00E-03		7.56E-02		7.56E-05

		-3.00E-03		7.57E-02		7.57E-05

		1.00E-03		7.57E-02		7.57E-05

		5.00E-03		7.56E-02		7.56E-05

		9.00E-03		7.57E-02		7.57E-05

		1.30E-02		7.56E-02		7.56E-05

		1.70E-02		7.58E-02		7.58E-05

		2.10E-02		7.57E-02		7.57E-05

		2.50E-02		7.57E-02		7.57E-05

		2.90E-02		7.58E-02		7.58E-05

		3.30E-02		7.58E-02		7.58E-05

		3.70E-02		7.60E-02		7.60E-05

		4.10E-02		7.58E-02		7.58E-05

		4.50E-02		7.59E-02		7.59E-05

		4.90E-02		7.61E-02		7.61E-05

		5.30E-02		7.59E-02		7.59E-05

		5.70E-02		7.62E-02		7.62E-05

		6.10E-02		7.61E-02		7.61E-05

		6.50E-02		7.62E-02		7.62E-05

		6.90E-02		7.63E-02		7.63E-05

		7.30E-02		7.62E-02		7.62E-05

		7.70E-02		7.66E-02		7.66E-05

		8.10E-02		7.64E-02		7.64E-05

		8.50E-02		7.66E-02		7.66E-05

		8.90E-02		7.66E-02		7.66E-05

		9.30E-02		7.66E-02		7.66E-05

		9.70E-02		7.70E-02		7.70E-05

		1.01E-01		7.68E-02		7.68E-05

		1.05E-01		7.71E-02		7.71E-05

		1.09E-01		7.71E-02		7.71E-05

		1.13E-01		7.72E-02		7.72E-05

		1.17E-01		7.74E-02		7.74E-05

		1.21E-01		7.72E-02		7.72E-05

		1.25E-01		7.75E-02		7.75E-05

		1.29E-01		7.75E-02		7.75E-05

		1.33E-01		7.76E-02		7.76E-05

		1.37E-01		7.79E-02		7.79E-05

		1.41E-01		7.77E-02		7.77E-05

		1.45E-01		7.79E-02		7.79E-05

		1.49E-01		7.79E-02		7.79E-05

		1.53E-01		7.81E-02		7.81E-05

		1.57E-01		7.83E-02		7.83E-05

		1.61E-01		7.81E-02		7.81E-05

		1.65E-01		7.84E-02		7.84E-05

		1.69E-01		7.84E-02		7.84E-05

		1.73E-01		7.86E-02		7.86E-05

		1.77E-01		7.87E-02		7.87E-05

		1.81E-01		7.86E-02		7.86E-05

		1.85E-01		7.88E-02		7.88E-05

		1.89E-01		7.88E-02		7.88E-05

		1.93E-01		7.90E-02		7.90E-05

		1.97E-01		7.90E-02		7.90E-05

		2.01E-01		7.90E-02		7.90E-05

		2.05E-01		7.92E-02		7.92E-05

		2.09E-01		7.92E-02		7.92E-05

		2.13E-01		7.93E-02		7.93E-05

		2.17E-01		7.95E-02		7.95E-05

		2.21E-01		7.94E-02		7.94E-05

		2.25E-01		7.96E-02		7.96E-05

		2.29E-01		7.96E-02		7.96E-05

		2.33E-01		7.97E-02		7.97E-05

		2.37E-01		8.00E-02		8.00E-05

		2.41E-01		7.99E-02		7.99E-05

		2.45E-01		8.00E-02		8.00E-05

		2.49E-01		8.01E-02		8.01E-05

		2.53E-01		8.02E-02		8.02E-05

		2.57E-01		8.02E-02		8.02E-05

		2.61E-01		8.03E-02		8.03E-05

		2.65E-01		8.04E-02		8.04E-05

		2.69E-01		8.05E-02		8.05E-05

		2.73E-01		8.05E-02		8.05E-05

		2.77E-01		8.06E-02		8.06E-05

		2.81E-01		8.06E-02		8.06E-05

		2.85E-01		8.07E-02		8.07E-05

		2.89E-01		8.07E-02		8.07E-05

		2.93E-01		8.07E-02		8.07E-05

		2.97E-01		8.10E-02		8.10E-05

		3.01E-01		8.10E-02		8.10E-05

		3.05E-01		8.10E-02		8.10E-05

		3.09E-01		8.11E-02		8.11E-05

		3.13E-01		8.11E-02		8.11E-05

		3.17E-01		8.13E-02		8.13E-05

		3.21E-01		8.12E-02		8.12E-05

		3.25E-01		8.14E-02		8.14E-05

		3.29E-01		8.14E-02		8.14E-05

		3.33E-01		8.13E-02		8.13E-05

		3.37E-01		8.16E-02		8.16E-05

		3.41E-01		8.14E-02		8.14E-05

		3.45E-01		8.16E-02		8.16E-05

		3.49E-01		8.16E-02		8.16E-05

		3.53E-01		8.16E-02		8.16E-05

		3.57E-01		8.18E-02		8.18E-05

		3.61E-01		8.16E-02		8.16E-05

		3.65E-01		8.18E-02		8.18E-05

		3.69E-01		8.18E-02		8.18E-05

		3.73E-01		8.18E-02		8.18E-05

		3.77E-01		8.20E-02		8.20E-05

		3.81E-01		8.17E-02		8.17E-05

		3.85E-01		8.20E-02		8.20E-05

		3.89E-01		8.20E-02		8.20E-05

		3.93E-01		8.19E-02		8.19E-05

		3.97E-01		8.22E-02		8.22E-05

		4.01E-01		8.19E-02		8.19E-05

		4.05E-01		8.21E-02		8.21E-05

		4.09E-01		8.21E-02		8.21E-05

		4.13E-01		8.20E-02		8.20E-05

		4.17E-01		8.22E-02		8.22E-05

		4.21E-01		8.19E-02		8.19E-05

		4.25E-01		8.22E-02		8.22E-05

		4.29E-01		8.20E-02		8.20E-05

		4.33E-01		8.20E-02		8.20E-05

		4.37E-01		8.22E-02		8.22E-05

		4.41E-01		8.20E-02		8.20E-05

		4.45E-01		8.21E-02		8.21E-05

		4.49E-01		8.20E-02		8.20E-05

		4.53E-01		8.20E-02		8.20E-05

		4.57E-01		8.22E-02		8.22E-05

		4.61E-01		8.20E-02		8.20E-05

		4.65E-01		8.22E-02		8.22E-05

		4.69E-01		8.19E-02		8.19E-05

		4.73E-01		8.21E-02		8.21E-05

		4.77E-01		8.20E-02		8.20E-05

		4.81E-01		8.18E-02		8.18E-05

		4.85E-01		8.20E-02		8.20E-05

		4.89E-01		8.18E-02		8.18E-05

		4.93E-01		8.18E-02		8.18E-05

		4.97E-01		8.18E-02		8.18E-05

		5.01E-01		8.16E-02		8.16E-05

		5.05E-01		8.17E-02		8.17E-05

		5.09E-01		8.16E-02		8.16E-05

		5.13E-01		8.14E-02		8.14E-05

		5.17E-01		8.14E-02		8.14E-05

		5.21E-01		8.13E-02		8.13E-05

		5.25E-01		8.13E-02		8.13E-05

		5.29E-01		8.11E-02		8.11E-05

		5.33E-01		8.11E-02		8.11E-05

		5.37E-01		8.09E-02		8.09E-05

		5.41E-01		8.07E-02		8.07E-05

		5.45E-01		8.06E-02		8.06E-05

		5.49E-01		8.06E-02		8.06E-05

		5.53E-01		8.03E-02		8.03E-05

		5.57E-01		8.01E-02		8.01E-05

		5.61E-01		7.98E-02		7.98E-05

		5.65E-01		7.96E-02		7.96E-05

		5.69E-01		7.94E-02		7.94E-05

		5.73E-01		7.91E-02		7.91E-05

		5.77E-01		7.88E-02		7.88E-05

		5.81E-01		7.83E-02		7.83E-05

		5.85E-01		7.79E-02		7.79E-05

		5.89E-01		7.76E-02		7.76E-05

		5.93E-01		7.70E-02		7.70E-05

		5.97E-01		7.66E-02		7.66E-05

		6.01E-01		7.59E-02		7.59E-05

		6.05E-01		7.52E-02		7.52E-05

		6.09E-01		7.47E-02		7.47E-05

		6.13E-01		7.38E-02		7.38E-05

		6.17E-01		7.31E-02		7.31E-05

		6.21E-01		7.20E-02		7.20E-05

		6.25E-01		7.11E-02		7.11E-05

		6.29E-01		7.04E-02		7.04E-05

		6.33E-01		6.90E-02		6.90E-05

		6.37E-01		6.79E-02		6.79E-05

		6.41E-01		6.66E-02		6.66E-05

		6.45E-01		6.54E-02		6.54E-05

		6.49E-01		6.41E-02		6.41E-05

		6.53E-01		6.25E-02		6.25E-05

		6.57E-01		6.11E-02		6.11E-05

		6.61E-01		5.94E-02		5.94E-05

		6.65E-01		5.78E-02		5.78E-05

		6.69E-01		5.62E-02		5.62E-05

		6.73E-01		5.42E-02		5.42E-05

		6.77E-01		5.25E-02		5.25E-05

		6.81E-01		5.04E-02		5.04E-05

		6.85E-01		4.87E-02		4.87E-05

		6.89E-01		4.67E-02		4.67E-05

		6.93E-01		4.44E-02		4.44E-05

		6.97E-01		4.24E-02		4.24E-05

		7.01E-01		4.00E-02		4.00E-05

		7.05E-01		3.79E-02		3.79E-05

		7.09E-01		3.56E-02		3.56E-05

		7.13E-01		3.32E-02		3.32E-05

		7.17E-01		3.09E-02		3.09E-05

		7.21E-01		2.82E-02		2.82E-05

		7.25E-01		2.58E-02		2.58E-05

		7.29E-01		2.34E-02		2.34E-05

		7.33E-01		2.08E-02		2.08E-05

		7.37E-01		1.81E-02		1.81E-05

		7.41E-01		1.53E-02		1.53E-05

		7.45E-01		1.29E-02		1.29E-05

		7.49E-01		1.03E-02		1.03E-05

		7.53E-01		7.44E-03		7.44E-06

		7.57E-01		4.68E-03		4.68E-06

		7.61E-01		1.87E-03		1.87E-06

		7.65E-01		-8.40E-04		-8.40E-07

		7.69E-01		-3.60E-03		-3.60E-06

		7.73E-01		-6.47E-03		-6.47E-06

		7.77E-01		-9.36E-03		-9.36E-06

		7.81E-01		-1.23E-02		-1.23E-05

		7.85E-01		-1.52E-02		-1.52E-05

		7.89E-01		-1.81E-02		-1.81E-05

		7.93E-01		-2.10E-02		-2.10E-05

		7.97E-01		-2.42E-02		-2.42E-05

		8.01E-01		-2.72E-02		-2.72E-05

		8.05E-01		-3.02E-02		-3.02E-05

		8.09E-01		-3.32E-02		-3.32E-05

		8.13E-01		-3.62E-02		-3.62E-05

		8.17E-01		-3.96E-02		-3.96E-05

		8.21E-01		-4.27E-02		-4.27E-05

		8.25E-01		-4.58E-02		-4.58E-05

		8.29E-01		-4.90E-02		-4.90E-05

		8.33E-01		-5.23E-02		-5.23E-05

		8.37E-01		-5.57E-02		-5.57E-05

		8.41E-01		-5.89E-02		-5.89E-05

		8.45E-01		-6.21E-02		-6.21E-05

		8.49E-01		-6.54E-02		-6.54E-05

		8.53E-01		-6.88E-02		-6.88E-05

		8.57E-01		-7.22E-02		-7.22E-05

		8.61E-01		-7.55E-02		-7.55E-05

		8.65E-01		-7.89E-02		-7.89E-05

		8.69E-01		-8.21E-02		-8.21E-05

		8.73E-01		-8.56E-02		-8.56E-05

		8.77E-01		-8.92E-02		-8.92E-05

		8.81E-01		-9.26E-02		-9.26E-05

		8.85E-01		-9.61E-02		-9.61E-05

		8.89E-01		-9.94E-02		-9.94E-05

		8.93E-01		-1.03E-01		-1.03E-04

		8.97E-01		-1.07E-01		-1.07E-04

		9.01E-01		-1.10E-01		-1.10E-04

		9.05E-01		-1.14E-01		-1.14E-04

		9.09E-01		-1.17E-01		-1.17E-04

		9.13E-01		-1.21E-01		-1.21E-04

		9.17E-01		-1.24E-01		-1.24E-04

		9.21E-01		-1.28E-01		-1.28E-04

		9.25E-01		-1.32E-01		-1.32E-04

		9.29E-01		-1.35E-01		-1.35E-04

		9.33E-01		-1.39E-01		-1.39E-04

		9.37E-01		-1.43E-01		-1.43E-04

		9.41E-01		-1.46E-01		-1.46E-04

		9.45E-01		-1.50E-01		-1.50E-04

		9.49E-01		-1.54E-01		-1.54E-04

		9.53E-01		-1.58E-01		-1.58E-04

		9.57E-01		-1.61E-01		-1.61E-04

		9.61E-01		-1.65E-01		-1.65E-04

		9.65E-01		-1.69E-01		-1.69E-04

		9.69E-01		-1.73E-01		-1.73E-04

		9.73E-01		-1.77E-01		-1.77E-04

		9.77E-01		-1.81E-01		-1.81E-04

		9.81E-01		-1.85E-01		-1.85E-04

		9.85E-01		-1.89E-01		-1.89E-04

		9.89E-01		-1.93E-01		-1.93E-04

		9.93E-01		-1.97E-01		-1.97E-04

		9.97E-01		-2.01E-01		-2.01E-04

		1.00E+00		-2.05E-01		-2.05E-04

		1.01E+00		-2.09E-01		-2.09E-04

		1.01E+00		-2.13E-01		-2.13E-04

		1.01E+00		-2.17E-01		-2.17E-04

		1.02E+00		-2.21E-01		-2.21E-04

		1.02E+00		-2.25E-01		-2.25E-04

		1.03E+00		-2.29E-01		-2.29E-04

		1.03E+00		-2.33E-01		-2.33E-04

		1.03E+00		-2.37E-01		-2.37E-04

		1.04E+00		-2.41E-01		-2.41E-04

		1.04E+00		-2.45E-01		-2.45E-04

		1.05E+00		-2.49E-01		-2.49E-04

		1.05E+00		-2.53E-01		-2.53E-04

		1.05E+00		-2.57E-01		-2.57E-04

		1.06E+00		-2.61E-01		-2.61E-04

		1.06E+00		-2.66E-01		-2.66E-04

		1.07E+00		-2.70E-01		-2.70E-04

		1.07E+00		-2.74E-01		-2.74E-04

		1.07E+00		-2.78E-01		-2.78E-04

		1.08E+00		-2.82E-01		-2.82E-04

		1.08E+00		-2.86E-01		-2.86E-04

		1.09E+00		-2.90E-01		-2.90E-04

		1.09E+00		-2.94E-01		-2.94E-04

		1.09E+00		-2.99E-01		-2.99E-04

		1.10E+00		-3.03E-01		-3.03E-04

		1.10E+00		-3.07E-01		-3.07E-04

		1.11E+00		-3.11E-01		-3.11E-04

		1.11E+00		-3.16E-01		-3.16E-04

		1.11E+00		-3.20E-01		-3.20E-04

		1.12E+00		-3.24E-01		-3.24E-04

		1.12E+00		-3.28E-01		-3.28E-04

		1.13E+00		-3.33E-01		-3.33E-04

		1.13E+00		-3.37E-01		-3.37E-04

		1.13E+00		-3.41E-01		-3.41E-04

		1.14E+00		-3.46E-01		-3.46E-04

		1.14E+00		-3.50E-01		-3.50E-04

		1.15E+00		-3.54E-01		-3.54E-04

		1.15E+00		-3.58E-01		-3.58E-04

		1.15E+00		-3.63E-01		-3.63E-04

		1.16E+00		-3.68E-01		-3.68E-04

		1.16E+00		-3.72E-01		-3.72E-04

		1.17E+00		-3.76E-01		-3.76E-04

		1.17E+00		-3.80E-01		-3.80E-04

		1.17E+00		-3.84E-01		-3.84E-04

		1.18E+00		-3.88E-01		-3.88E-04

		1.18E+00		-3.93E-01		-3.93E-04

		1.19E+00		-3.97E-01		-3.97E-04

		1.19E+00		-4.01E-01		-4.01E-04

		1.19E+00		-4.05E-01		-4.05E-04

		1.20E+00		-4.09E-01		-4.09E-04

		1.20E+00		-4.14E-01		-4.14E-04

		1.21E+00		-4.18E-01		-4.18E-04

		1.21E+00		-4.22E-01		-4.22E-04

		1.21E+00		-4.26E-01		-4.26E-04

		1.22E+00		-4.30E-01		-4.30E-04

		1.22E+00		-4.34E-01		-4.34E-04

		1.23E+00		-4.38E-01		-4.38E-04

		1.23E+00		-4.42E-01		-4.42E-04

		1.23E+00		-4.47E-01		-4.47E-04

		1.24E+00		-4.51E-01		-4.51E-04

		1.24E+00		-4.55E-01		-4.55E-04

		1.25E+00		-4.59E-01		-4.59E-04

		1.25E+00		-4.63E-01		-4.63E-04

		1.25E+00		-4.68E-01		-4.68E-04

		1.26E+00		-4.72E-01		-4.72E-04

		1.26E+00		-4.76E-01		-4.76E-04

		1.27E+00		-4.80E-01		-4.80E-04

		1.27E+00		-4.84E-01		-4.84E-04

		1.27E+00		-4.89E-01		-4.89E-04

		1.28E+00		-4.92E-01		-4.92E-04

		1.28E+00		-4.96E-01		-4.96E-04

		1.29E+00		-5.00E-01		-5.00E-04

		1.29E+00		-5.04E-01		-5.04E-04

		1.29E+00		-5.08E-01		-5.08E-04

		1.30E+00		-5.12E-01		-5.12E-04

		1.30E+00		-5.16E-01		-5.16E-04

		1.31E+00		-5.20E-01		-5.20E-04

		1.31E+00		-5.24E-01		-5.24E-04

		1.31E+00		-5.28E-01		-5.28E-04

		1.32E+00		-5.32E-01		-5.32E-04

		1.32E+00		-5.36E-01		-5.36E-04

		1.33E+00		-5.39E-01		-5.39E-04

		1.33E+00		-5.43E-01		-5.43E-04

		1.33E+00		-5.47E-01		-5.47E-04

		1.34E+00		-5.51E-01		-5.51E-04

		1.34E+00		-5.55E-01		-5.55E-04

		1.35E+00		-5.58E-01		-5.58E-04

		1.35E+00		-5.62E-01		-5.62E-04

		1.35E+00		-5.66E-01		-5.66E-04

		1.36E+00		-5.70E-01		-5.70E-04

		1.36E+00		-5.73E-01		-5.73E-04

		1.37E+00		-5.77E-01		-5.77E-04

		1.37E+00		-5.81E-01		-5.81E-04

		1.37E+00		-5.84E-01		-5.84E-04

		1.38E+00		-5.88E-01		-5.88E-04

		1.38E+00		-5.91E-01		-5.91E-04

		1.39E+00		-5.94E-01		-5.94E-04

		1.39E+00		-5.98E-01		-5.98E-04

		1.39E+00		-6.01E-01		-6.01E-04

		1.40E+00		-6.05E-01		-6.05E-04

		1.40E+00		-6.08E-01		-6.08E-04

		1.41E+00		-6.11E-01		-6.11E-04

		1.41E+00		-6.14E-01		-6.14E-04

		1.41E+00		-6.17E-01		-6.17E-04

		1.42E+00		-6.20E-01		-6.20E-04

		1.42E+00		-6.23E-01		-6.23E-04

		1.43E+00		-6.26E-01		-6.26E-04

		1.43E+00		-6.29E-01		-6.29E-04

		1.43E+00		-6.31E-01		-6.31E-04

		1.44E+00		-6.34E-01		-6.34E-04

		1.44E+00		-6.36E-01		-6.36E-04

		1.45E+00		-6.39E-01		-6.39E-04

		1.45E+00		-6.41E-01		-6.41E-04

		1.45E+00		-6.44E-01		-6.44E-04

		1.46E+00		-6.46E-01		-6.46E-04

		1.46E+00		-6.48E-01		-6.48E-04

		1.47E+00		-6.50E-01		-6.50E-04

		1.47E+00		-6.52E-01		-6.52E-04

		1.47E+00		-6.54E-01		-6.54E-04

		1.48E+00		-6.55E-01		-6.55E-04

		1.48E+00		-6.57E-01		-6.57E-04

		1.49E+00		-6.58E-01		-6.58E-04

		1.49E+00		-6.60E-01		-6.60E-04

		1.49E+00		-6.61E-01		-6.61E-04

		1.50E+00		-6.61E-01		-6.61E-04

		1.50E+00		-6.62E-01		-6.62E-04

		1.51E+00		-6.63E-01		-6.63E-04

		1.51E+00		-6.63E-01		-6.63E-04

		1.51E+00		-6.64E-01		-6.64E-04

		1.52E+00		-6.64E-01		-6.64E-04

		1.52E+00		-6.64E-01		-6.64E-04

		1.53E+00		-6.65E-01		-6.65E-04

		1.53E+00		-6.65E-01		-6.65E-04

		1.53E+00		-6.65E-01		-6.65E-04

		1.54E+00		-6.64E-01		-6.64E-04

		1.54E+00		-6.64E-01		-6.64E-04

		1.55E+00		-6.64E-01		-6.64E-04

		1.55E+00		-6.64E-01		-6.64E-04

		1.55E+00		-6.64E-01		-6.64E-04

		1.56E+00		-6.64E-01		-6.64E-04

		1.56E+00		-6.63E-01		-6.63E-04

		1.57E+00		-6.63E-01		-6.63E-04

		1.57E+00		-6.70E-01		-6.70E-04

		1.57E+00		-6.70E-01		-6.70E-04

		1.58E+00		-6.69E-01		-6.69E-04

		1.58E+00		-6.69E-01		-6.69E-04

		1.59E+00		-6.68E-01		-6.68E-04

		1.59E+00		-6.68E-01		-6.68E-04

		1.59E+00		-6.68E-01		-6.68E-04

		1.60E+00		-6.68E-01		-6.68E-04

		1.60E+00		-6.68E-01		-6.68E-04

		1.61E+00		-6.69E-01		-6.69E-04

		1.61E+00		-6.70E-01		-6.70E-04

		1.61E+00		-6.70E-01		-6.70E-04

		1.62E+00		-6.70E-01		-6.70E-04

		1.62E+00		-6.71E-01		-6.71E-04

		1.63E+00		-6.72E-01		-6.72E-04

		1.63E+00		-6.73E-01		-6.73E-04

		1.63E+00		-6.74E-01		-6.74E-04

		1.64E+00		-6.75E-01		-6.75E-04

		1.64E+00		-6.76E-01		-6.76E-04

		1.65E+00		-6.77E-01		-6.77E-04

		1.65E+00		-6.78E-01		-6.78E-04

		1.65E+00		-6.78E-01		-6.78E-04

		1.66E+00		-6.79E-01		-6.79E-04

		1.66E+00		-6.80E-01		-6.80E-04

		1.67E+00		-6.80E-01		-6.80E-04

		1.67E+00		-6.81E-01		-6.81E-04

		1.67E+00		-6.82E-01		-6.82E-04

		1.68E+00		-6.82E-01		-6.82E-04

		1.68E+00		-6.83E-01		-6.83E-04

		1.69E+00		-6.83E-01		-6.83E-04

		1.69E+00		-6.84E-01		-6.84E-04

		1.69E+00		-6.84E-01		-6.84E-04

		1.70E+00		-6.85E-01		-6.85E-04

		1.70E+00		-6.84E-01		-6.84E-04

		1.71E+00		-6.85E-01		-6.85E-04

		1.71E+00		-6.85E-01		-6.85E-04

		1.71E+00		-6.85E-01		-6.85E-04

		1.72E+00		-6.85E-01		-6.85E-04

		1.72E+00		-6.84E-01		-6.84E-04

		1.73E+00		-6.84E-01		-6.84E-04

		1.73E+00		-6.84E-01		-6.84E-04

		1.73E+00		-6.83E-01		-6.83E-04

		1.74E+00		-6.82E-01		-6.82E-04

		1.74E+00		-6.81E-01		-6.81E-04

		1.75E+00		-6.80E-01		-6.80E-04

		1.75E+00		-6.78E-01		-6.78E-04

		1.75E+00		-6.77E-01		-6.77E-04

		1.76E+00		-6.75E-01		-6.75E-04

		1.76E+00		-6.72E-01		-6.72E-04

		1.77E+00		-6.70E-01		-6.70E-04

		1.77E+00		-6.66E-01		-6.66E-04

		1.77E+00		-6.63E-01		-6.63E-04

		1.78E+00		-6.59E-01		-6.59E-04

		1.78E+00		-6.55E-01		-6.55E-04

		1.79E+00		-6.51E-01		-6.51E-04

		1.79E+00		-6.47E-01		-6.47E-04

		1.79E+00		-6.44E-01		-6.44E-04

		1.80E+00		-6.40E-01		-6.40E-04

		1.80E+00		-6.36E-01		-6.36E-04

		1.81E+00		-6.32E-01		-6.32E-04

		1.81E+00		-6.29E-01		-6.29E-04

		1.81E+00		-6.26E-01		-6.26E-04

		1.82E+00		-6.22E-01		-6.22E-04

		1.82E+00		-6.19E-01		-6.19E-04

		1.83E+00		-6.17E-01		-6.17E-04

		1.83E+00		-6.15E-01		-6.15E-04

		1.83E+00		-6.13E-01		-6.13E-04

		1.84E+00		-6.11E-01		-6.11E-04

		1.84E+00		-6.10E-01		-6.10E-04

		1.85E+00		-6.08E-01		-6.08E-04

		1.85E+00		-6.07E-01		-6.07E-04

		1.85E+00		-6.06E-01		-6.06E-04

		1.86E+00		-6.06E-01		-6.06E-04

		1.86E+00		-6.05E-01		-6.05E-04

		1.87E+00		-6.05E-01		-6.05E-04

		1.87E+00		-6.05E-01		-6.05E-04

		1.87E+00		-6.05E-01		-6.05E-04

		1.88E+00		-6.06E-01		-6.06E-04

		1.88E+00		-6.06E-01		-6.06E-04

		1.89E+00		-6.07E-01		-6.07E-04

		1.89E+00		-6.09E-01		-6.09E-04

		1.89E+00		-6.10E-01		-6.10E-04

		1.90E+00		-6.11E-01		-6.11E-04

		1.90E+00		-6.13E-01		-6.13E-04

		1.91E+00		-6.14E-01		-6.14E-04

		1.91E+00		-6.16E-01		-6.16E-04

		1.91E+00		-6.18E-01		-6.18E-04

		1.92E+00		-6.20E-01		-6.20E-04

		1.92E+00		-6.22E-01		-6.22E-04

		1.93E+00		-6.24E-01		-6.24E-04

		1.93E+00		-6.26E-01		-6.26E-04

		1.93E+00		-6.29E-01		-6.29E-04

		1.94E+00		-6.31E-01		-6.31E-04

		1.94E+00		-6.34E-01		-6.34E-04

		1.95E+00		-6.36E-01		-6.36E-04

		1.95E+00		-6.39E-01		-6.39E-04

		1.95E+00		-6.42E-01		-6.42E-04

		1.96E+00		-6.45E-01		-6.45E-04

		1.96E+00		-6.48E-01		-6.48E-04

		1.97E+00		-6.50E-01		-6.50E-04

		1.97E+00		-6.54E-01		-6.54E-04

		1.97E+00		-6.56E-01		-6.56E-04

		1.98E+00		-6.60E-01		-6.60E-04

		1.98E+00		-6.63E-01		-6.63E-04

		1.99E+00		-6.66E-01		-6.66E-04

		1.99E+00		-6.70E-01		-6.70E-04

		1.99E+00		-6.73E-01		-6.73E-04

		2.00E+00		-6.77E-01		-6.77E-04

		2.00E+00		-6.81E-01		-6.81E-04

		2.01E+00		-6.84E-01		-6.84E-04

		2.01E+00		-6.88E-01		-6.88E-04

		2.01E+00		-6.91E-01		-6.91E-04

		2.02E+00		-6.95E-01		-6.95E-04

		2.02E+00		-6.98E-01		-6.98E-04

		2.03E+00		-7.02E-01		-7.02E-04

		2.03E+00		-7.06E-01		-7.06E-04

		2.03E+00		-7.10E-01		-7.10E-04

		2.04E+00		-7.14E-01		-7.14E-04

		2.04E+00		-7.18E-01		-7.18E-04

		2.05E+00		-7.21E-01		-7.21E-04

		2.05E+00		-7.25E-01		-7.25E-04

		2.05E+00		-7.30E-01		-7.30E-04

		2.06E+00		-7.33E-01		-7.33E-04

		2.06E+00		-7.37E-01		-7.37E-04

		2.07E+00		-7.41E-01		-7.41E-04

		2.07E+00		-7.45E-01		-7.45E-04

		2.07E+00		-7.49E-01		-7.49E-04

		2.08E+00		-7.53E-01		-7.53E-04

		2.08E+00		-7.57E-01		-7.57E-04

		2.09E+00		-7.61E-01		-7.61E-04

		2.09E+00		-7.65E-01		-7.65E-04

		2.09E+00		-7.70E-01		-7.70E-04

		2.10E+00		-7.74E-01		-7.74E-04

		2.10E+00		-7.78E-01		-7.78E-04

		2.11E+00		-7.82E-01		-7.82E-04

		2.11E+00		-7.86E-01		-7.86E-04

		2.11E+00		-7.91E-01		-7.91E-04

		2.12E+00		-7.95E-01		-7.95E-04

		2.12E+00		-7.99E-01		-7.99E-04

		2.13E+00		-8.03E-01		-8.03E-04

		2.13E+00		-8.08E-01		-8.08E-04

		2.13E+00		-8.13E-01		-8.13E-04

		2.14E+00		-8.17E-01		-8.17E-04

		2.14E+00		-8.22E-01		-8.22E-04

		2.15E+00		-8.26E-01		-8.26E-04

		2.15E+00		-8.30E-01		-8.30E-04

		2.15E+00		-8.35E-01		-8.35E-04

		2.16E+00		-8.39E-01		-8.39E-04

		2.16E+00		-8.44E-01		-8.44E-04

		2.17E+00		-8.48E-01		-8.48E-04

		2.17E+00		-8.53E-01		-8.53E-04

		2.17E+00		-8.58E-01		-8.58E-04

		2.18E+00		-8.62E-01		-8.62E-04

		2.18E+00		-8.66E-01		-8.66E-04

		2.19E+00		-8.71E-01		-8.71E-04

		2.19E+00		-8.76E-01		-8.76E-04

		2.19E+00		-8.80E-01		-8.80E-04

		2.20E+00		-8.85E-01		-8.85E-04

		2.20E+00		-8.90E-01		-8.90E-04

		2.21E+00		-8.94E-01		-8.94E-04

		2.21E+00		-8.99E-01		-8.99E-04

		2.21E+00		-9.03E-01		-9.03E-04

		2.22E+00		-9.08E-01		-9.08E-04

		2.22E+00		-9.12E-01		-9.12E-04

		2.23E+00		-9.17E-01		-9.17E-04

		2.23E+00		-9.22E-01		-9.22E-04

		2.23E+00		-9.26E-01		-9.26E-04

		2.24E+00		-9.31E-01		-9.31E-04

		2.24E+00		-9.36E-01		-9.36E-04

		2.25E+00		-9.40E-01		-9.40E-04

		2.25E+00		-9.45E-01		-9.45E-04

		2.25E+00		-9.50E-01		-9.50E-04

		2.26E+00		-9.54E-01		-9.54E-04

		2.26E+00		-9.59E-01		-9.59E-04

		2.27E+00		-9.64E-01		-9.64E-04

		2.27E+00		-9.69E-01		-9.69E-04

		2.27E+00		-9.73E-01		-9.73E-04

		2.28E+00		-9.78E-01		-9.78E-04

		2.28E+00		-9.83E-01		-9.83E-04

		2.29E+00		-9.87E-01		-9.87E-04

		2.29E+00		-9.92E-01		-9.92E-04

		2.29E+00		-9.96E-01		-9.96E-04

		2.30E+00		-1.01E+00		-1.01E-03

		2.30E+00		-1.01E+00		-1.01E-03

		2.31E+00		-1.02E+00		-1.02E-03

		2.31E+00		-1.02E+00		-1.02E-03

		2.31E+00		-1.03E+00		-1.03E-03

		2.32E+00		-1.03E+00		-1.03E-03

		2.32E+00		-1.04E+00		-1.04E-03

		2.33E+00		-1.04E+00		-1.04E-03

		2.33E+00		-1.05E+00		-1.05E-03

		2.33E+00		-1.05E+00		-1.05E-03

		2.34E+00		-1.06E+00		-1.06E-03

		2.34E+00		-1.06E+00		-1.06E-03

		2.35E+00		-1.07E+00		-1.07E-03

		2.35E+00		-1.07E+00		-1.07E-03

		2.35E+00		-1.08E+00		-1.08E-03

		2.36E+00		-1.08E+00		-1.08E-03

		2.36E+00		-1.09E+00		-1.09E-03

		2.37E+00		-1.09E+00		-1.09E-03

		2.37E+00		-1.10E+00		-1.10E-03

		2.37E+00		-1.10E+00		-1.10E-03

		2.38E+00		-1.11E+00		-1.11E-03

		2.38E+00		-1.11E+00		-1.11E-03

		2.39E+00		-1.12E+00		-1.12E-03

		2.39E+00		-1.12E+00		-1.12E-03

		2.39E+00		-1.13E+00		-1.13E-03

		2.40E+00		-1.13E+00		-1.13E-03

		2.40E+00		-1.14E+00		-1.14E-03

		2.41E+00		-1.14E+00		-1.14E-03

		2.41E+00		-1.15E+00		-1.15E-03

		2.41E+00		-1.15E+00		-1.15E-03

		2.42E+00		-1.16E+00		-1.16E-03

		2.42E+00		-1.16E+00		-1.16E-03

		2.43E+00		-1.17E+00		-1.17E-03

		2.43E+00		-1.17E+00		-1.17E-03

		2.43E+00		-1.18E+00		-1.18E-03

		2.44E+00		-1.18E+00		-1.18E-03

		2.44E+00		-1.19E+00		-1.19E-03

		2.45E+00		-1.19E+00		-1.19E-03

		2.45E+00		-1.20E+00		-1.20E-03

		2.45E+00		-1.20E+00		-1.20E-03

		2.46E+00		-1.21E+00		-1.21E-03

		2.46E+00		-1.21E+00		-1.21E-03

		2.47E+00		-1.22E+00		-1.22E-03

		2.47E+00		-1.22E+00		-1.22E-03

		2.47E+00		-1.23E+00		-1.23E-03

		2.48E+00		-1.23E+00		-1.23E-03

		2.48E+00		-1.24E+00		-1.24E-03

		2.49E+00		-1.24E+00		-1.24E-03

		2.49E+00		-1.25E+00		-1.25E-03

		2.49E+00		-1.25E+00		-1.25E-03

		2.50E+00		-1.26E+00		-1.26E-03

		2.50E+00		-1.26E+00		-1.26E-03

		2.50E+00		-1.26E+00		-1.26E-03

		2.49E+00		-1.26E+00		-1.26E-03

		2.49E+00		-1.25E+00		-1.25E-03

		2.49E+00		-1.24E+00		-1.24E-03

		2.48E+00		-1.24E+00		-1.24E-03

		2.48E+00		-1.23E+00		-1.23E-03

		2.47E+00		-1.23E+00		-1.23E-03

		2.47E+00		-1.22E+00		-1.22E-03

		2.47E+00		-1.22E+00		-1.22E-03

		2.46E+00		-1.21E+00		-1.21E-03

		2.46E+00		-1.21E+00		-1.21E-03

		2.45E+00		-1.20E+00		-1.20E-03

		2.45E+00		-1.20E+00		-1.20E-03

		2.45E+00		-1.19E+00		-1.19E-03

		2.44E+00		-1.19E+00		-1.19E-03

		2.44E+00		-1.18E+00		-1.18E-03

		2.43E+00		-1.18E+00		-1.18E-03

		2.43E+00		-1.17E+00		-1.17E-03

		2.43E+00		-1.17E+00		-1.17E-03

		2.42E+00		-1.16E+00		-1.16E-03

		2.42E+00		-1.16E+00		-1.16E-03

		2.41E+00		-1.15E+00		-1.15E-03

		2.41E+00		-1.15E+00		-1.15E-03

		2.41E+00		-1.14E+00		-1.14E-03

		2.40E+00		-1.14E+00		-1.14E-03

		2.40E+00		-1.13E+00		-1.13E-03

		2.39E+00		-1.13E+00		-1.13E-03

		2.39E+00		-1.12E+00		-1.12E-03

		2.39E+00		-1.12E+00		-1.12E-03

		2.38E+00		-1.11E+00		-1.11E-03

		2.38E+00		-1.11E+00		-1.11E-03

		2.37E+00		-1.10E+00		-1.10E-03

		2.37E+00		-1.10E+00		-1.10E-03

		2.37E+00		-1.09E+00		-1.09E-03

		2.36E+00		-1.09E+00		-1.09E-03

		2.36E+00		-1.08E+00		-1.08E-03

		2.35E+00		-1.08E+00		-1.08E-03

		2.35E+00		-1.07E+00		-1.07E-03

		2.35E+00		-1.07E+00		-1.07E-03

		2.34E+00		-1.06E+00		-1.06E-03

		2.34E+00		-1.06E+00		-1.06E-03

		2.33E+00		-1.05E+00		-1.05E-03

		2.33E+00		-1.05E+00		-1.05E-03

		2.33E+00		-1.04E+00		-1.04E-03

		2.32E+00		-1.04E+00		-1.04E-03

		2.32E+00		-1.03E+00		-1.03E-03

		2.31E+00		-1.03E+00		-1.03E-03

		2.31E+00		-1.02E+00		-1.02E-03

		2.31E+00		-1.02E+00		-1.02E-03

		2.30E+00		-1.01E+00		-1.01E-03

		2.30E+00		-1.01E+00		-1.01E-03

		2.29E+00		-1.00E+00		-1.00E-03

		2.29E+00		-9.98E-01		-9.98E-04

		2.29E+00		-9.93E-01		-9.93E-04

		2.28E+00		-9.88E-01		-9.88E-04

		2.28E+00		-9.83E-01		-9.83E-04

		2.27E+00		-9.78E-01		-9.78E-04

		2.27E+00		-9.73E-01		-9.73E-04

		2.27E+00		-9.68E-01		-9.68E-04

		2.26E+00		-9.63E-01		-9.63E-04

		2.26E+00		-9.58E-01		-9.58E-04

		2.25E+00		-9.53E-01		-9.53E-04

		2.25E+00		-9.47E-01		-9.47E-04

		2.25E+00		-9.42E-01		-9.42E-04

		2.24E+00		-9.37E-01		-9.37E-04

		2.24E+00		-9.32E-01		-9.32E-04

		2.23E+00		-9.27E-01		-9.27E-04

		2.23E+00		-9.22E-01		-9.22E-04

		2.23E+00		-9.17E-01		-9.17E-04

		2.22E+00		-9.12E-01		-9.12E-04

		2.22E+00		-9.07E-01		-9.07E-04

		2.21E+00		-9.02E-01		-9.02E-04

		2.21E+00		-8.98E-01		-8.98E-04

		2.21E+00		-8.92E-01		-8.92E-04

		2.20E+00		-8.87E-01		-8.87E-04

		2.20E+00		-8.82E-01		-8.82E-04

		2.19E+00		-8.78E-01		-8.78E-04

		2.19E+00		-8.72E-01		-8.72E-04

		2.19E+00		-8.67E-01		-8.67E-04

		2.18E+00		-8.62E-01		-8.62E-04

		2.18E+00		-8.57E-01		-8.57E-04

		2.17E+00		-8.53E-01		-8.53E-04

		2.17E+00		-8.47E-01		-8.47E-04

		2.17E+00		-8.42E-01		-8.42E-04

		2.16E+00		-8.38E-01		-8.38E-04

		2.16E+00		-8.32E-01		-8.32E-04

		2.15E+00		-8.28E-01		-8.28E-04

		2.15E+00		-8.22E-01		-8.22E-04

		2.15E+00		-8.18E-01		-8.18E-04

		2.14E+00		-8.13E-01		-8.13E-04

		2.14E+00		-8.08E-01		-8.08E-04

		2.13E+00		-8.03E-01		-8.03E-04

		2.13E+00		-7.98E-01		-7.98E-04

		2.13E+00		-7.93E-01		-7.93E-04

		2.12E+00		-7.88E-01		-7.88E-04

		2.12E+00		-7.83E-01		-7.83E-04

		2.11E+00		-7.78E-01		-7.78E-04

		2.11E+00		-7.73E-01		-7.73E-04

		2.11E+00		-7.68E-01		-7.68E-04

		2.10E+00		-7.63E-01		-7.63E-04

		2.10E+00		-7.58E-01		-7.58E-04

		2.09E+00		-7.54E-01		-7.54E-04

		2.09E+00		-7.49E-01		-7.49E-04

		2.09E+00		-7.44E-01		-7.44E-04

		2.08E+00		-7.39E-01		-7.39E-04

		2.08E+00		-7.34E-01		-7.34E-04

		2.07E+00		-7.29E-01		-7.29E-04

		2.07E+00		-7.24E-01		-7.24E-04

		2.07E+00		-7.20E-01		-7.20E-04

		2.06E+00		-7.15E-01		-7.15E-04

		2.06E+00		-7.10E-01		-7.10E-04

		2.05E+00		-7.05E-01		-7.05E-04

		2.05E+00		-7.01E-01		-7.01E-04

		2.05E+00		-6.96E-01		-6.96E-04

		2.04E+00		-6.91E-01		-6.91E-04

		2.04E+00		-6.86E-01		-6.86E-04

		2.03E+00		-6.81E-01		-6.81E-04

		2.03E+00		-6.77E-01		-6.77E-04

		2.03E+00		-6.72E-01		-6.72E-04

		2.02E+00		-6.67E-01		-6.67E-04

		2.02E+00		-6.62E-01		-6.62E-04

		2.01E+00		-6.57E-01		-6.57E-04

		2.01E+00		-6.52E-01		-6.52E-04

		2.01E+00		-6.47E-01		-6.47E-04

		2.00E+00		-6.42E-01		-6.42E-04

		2.00E+00		-6.38E-01		-6.38E-04

		1.99E+00		-6.33E-01		-6.33E-04

		1.99E+00		-6.28E-01		-6.28E-04

		1.99E+00		-6.23E-01		-6.23E-04

		1.98E+00		-6.18E-01		-6.18E-04

		1.98E+00		-6.14E-01		-6.14E-04

		1.97E+00		-6.08E-01		-6.08E-04

		1.97E+00		-6.04E-01		-6.04E-04

		1.97E+00		-5.99E-01		-5.99E-04

		1.96E+00		-5.94E-01		-5.94E-04

		1.96E+00		-5.90E-01		-5.90E-04

		1.95E+00		-5.85E-01		-5.85E-04

		1.95E+00		-5.80E-01		-5.80E-04

		1.95E+00		-5.75E-01		-5.75E-04

		1.94E+00		-5.70E-01		-5.70E-04

		1.94E+00		-5.66E-01		-5.66E-04

		1.93E+00		-5.61E-01		-5.61E-04

		1.93E+00		-5.56E-01		-5.56E-04

		1.93E+00		-5.52E-01		-5.52E-04

		1.92E+00		-5.47E-01		-5.47E-04

		1.92E+00		-5.42E-01		-5.42E-04

		1.91E+00		-5.38E-01		-5.38E-04

		1.91E+00		-5.33E-01		-5.33E-04

		1.91E+00		-5.28E-01		-5.28E-04

		1.90E+00		-5.24E-01		-5.24E-04

		1.90E+00		-5.19E-01		-5.19E-04

		1.89E+00		-5.14E-01		-5.14E-04

		1.89E+00		-5.10E-01		-5.10E-04

		1.89E+00		-5.05E-01		-5.05E-04

		1.88E+00		-5.00E-01		-5.00E-04

		1.88E+00		-4.96E-01		-4.96E-04

		1.87E+00		-4.92E-01		-4.92E-04

		1.87E+00		-4.89E-01		-4.89E-04

		1.87E+00		-4.85E-01		-4.85E-04

		1.86E+00		-4.81E-01		-4.81E-04

		1.86E+00		-4.77E-01		-4.77E-04

		1.85E+00		-4.72E-01		-4.72E-04

		1.85E+00		-4.67E-01		-4.67E-04

		1.85E+00		-4.62E-01		-4.62E-04

		1.84E+00		-4.58E-01		-4.58E-04

		1.84E+00		-4.54E-01		-4.54E-04

		1.83E+00		-4.49E-01		-4.49E-04

		1.83E+00		-4.44E-01		-4.44E-04

		1.83E+00		-4.41E-01		-4.41E-04

		1.82E+00		-4.36E-01		-4.36E-04

		1.82E+00		-4.31E-01		-4.31E-04

		1.81E+00		-4.27E-01		-4.27E-04

		1.81E+00		-4.23E-01		-4.23E-04

		1.81E+00		-4.18E-01		-4.18E-04

		1.80E+00		-4.14E-01		-4.14E-04

		1.80E+00		-4.10E-01		-4.10E-04

		1.79E+00		-4.06E-01		-4.06E-04

		1.79E+00		-4.01E-01		-4.01E-04

		1.79E+00		-3.97E-01		-3.97E-04

		1.78E+00		-3.93E-01		-3.93E-04

		1.78E+00		-3.89E-01		-3.89E-04

		1.77E+00		-3.84E-01		-3.84E-04

		1.77E+00		-3.80E-01		-3.80E-04

		1.77E+00		-3.76E-01		-3.76E-04

		1.76E+00		-3.72E-01		-3.72E-04

		1.76E+00		-3.68E-01		-3.68E-04

		1.75E+00		-3.64E-01		-3.64E-04

		1.75E+00		-3.60E-01		-3.60E-04

		1.75E+00		-3.56E-01		-3.56E-04

		1.74E+00		-3.52E-01		-3.52E-04

		1.74E+00		-3.48E-01		-3.48E-04

		1.73E+00		-3.44E-01		-3.44E-04

		1.73E+00		-3.40E-01		-3.40E-04

		1.73E+00		-3.36E-01		-3.36E-04

		1.72E+00		-3.32E-01		-3.32E-04

		1.72E+00		-3.29E-01		-3.29E-04

		1.71E+00		-3.25E-01		-3.25E-04

		1.71E+00		-3.21E-01		-3.21E-04

		1.71E+00		-3.17E-01		-3.17E-04

		1.70E+00		-3.14E-01		-3.14E-04

		1.70E+00		-3.10E-01		-3.10E-04

		1.69E+00		-3.06E-01		-3.06E-04

		1.69E+00		-3.03E-01		-3.03E-04

		1.69E+00		-2.99E-01		-2.99E-04

		1.68E+00		-2.97E-01		-2.97E-04

		1.68E+00		-2.93E-01		-2.93E-04

		1.67E+00		-2.89E-01		-2.89E-04

		1.67E+00		-2.87E-01		-2.87E-04

		1.67E+00		-2.84E-01		-2.84E-04

		1.66E+00		-2.81E-01		-2.81E-04

		1.66E+00		-2.78E-01		-2.78E-04

		1.65E+00		-2.74E-01		-2.74E-04

		1.65E+00		-2.72E-01		-2.72E-04

		1.65E+00		-2.69E-01		-2.69E-04

		1.64E+00		-2.66E-01		-2.66E-04

		1.64E+00		-2.63E-01		-2.63E-04

		1.63E+00		-2.60E-01		-2.60E-04

		1.63E+00		-2.58E-01		-2.58E-04

		1.63E+00		-2.54E-01		-2.54E-04

		1.62E+00		-2.52E-01		-2.52E-04

		1.62E+00		-2.50E-01		-2.50E-04

		1.61E+00		-2.47E-01		-2.47E-04

		1.61E+00		-2.45E-01		-2.45E-04

		1.61E+00		-2.42E-01		-2.42E-04

		1.60E+00		-2.40E-01		-2.40E-04

		1.60E+00		-2.38E-01		-2.38E-04

		1.59E+00		-2.36E-01		-2.36E-04

		1.59E+00		-2.34E-01		-2.34E-04

		1.59E+00		-2.33E-01		-2.33E-04

		1.58E+00		-2.31E-01		-2.31E-04

		1.58E+00		-2.29E-01		-2.29E-04

		1.57E+00		-2.27E-01		-2.27E-04

		1.57E+00		-2.25E-01		-2.25E-04

		1.57E+00		-2.24E-01		-2.24E-04

		1.56E+00		-2.22E-01		-2.22E-04

		1.56E+00		-2.21E-01		-2.21E-04

		1.55E+00		-2.20E-01		-2.20E-04

		1.55E+00		-2.18E-01		-2.18E-04

		1.55E+00		-2.17E-01		-2.17E-04

		1.54E+00		-2.16E-01		-2.16E-04

		1.54E+00		-2.15E-01		-2.15E-04

		1.53E+00		-2.14E-01		-2.14E-04

		1.53E+00		-2.12E-01		-2.12E-04

		1.53E+00		-2.11E-01		-2.11E-04

		1.52E+00		-2.10E-01		-2.10E-04

		1.52E+00		-2.09E-01		-2.09E-04

		1.51E+00		-2.08E-01		-2.08E-04

		1.51E+00		-2.07E-01		-2.07E-04

		1.51E+00		-2.06E-01		-2.06E-04

		1.50E+00		-2.05E-01		-2.05E-04

		1.50E+00		-2.04E-01		-2.04E-04

		1.49E+00		-2.03E-01		-2.03E-04

		1.49E+00		-2.02E-01		-2.02E-04

		1.49E+00		-2.01E-01		-2.01E-04

		1.48E+00		-2.00E-01		-2.00E-04

		1.48E+00		-1.99E-01		-1.99E-04

		1.47E+00		-1.98E-01		-1.98E-04

		1.47E+00		-1.96E-01		-1.96E-04

		1.47E+00		-1.96E-01		-1.96E-04

		1.46E+00		-1.94E-01		-1.94E-04

		1.46E+00		-1.93E-01		-1.93E-04

		1.45E+00		-1.91E-01		-1.91E-04

		1.45E+00		-1.90E-01		-1.90E-04

		1.45E+00		-1.89E-01		-1.89E-04

		1.44E+00		-1.87E-01		-1.87E-04

		1.44E+00		-1.86E-01		-1.86E-04

		1.43E+00		-1.84E-01		-1.84E-04

		1.43E+00		-1.82E-01		-1.82E-04

		1.43E+00		-1.80E-01		-1.80E-04

		1.42E+00		-1.78E-01		-1.78E-04

		1.42E+00		-1.76E-01		-1.76E-04

		1.41E+00		-1.75E-01		-1.75E-04

		1.41E+00		-1.72E-01		-1.72E-04

		1.41E+00		-1.70E-01		-1.70E-04

		1.40E+00		-1.68E-01		-1.68E-04

		1.40E+00		-1.66E-01		-1.66E-04

		1.39E+00		-1.63E-01		-1.63E-04

		1.39E+00		-1.61E-01		-1.61E-04

		1.39E+00		-1.58E-01		-1.58E-04

		1.38E+00		-1.56E-01		-1.56E-04

		1.38E+00		-1.53E-01		-1.53E-04

		1.37E+00		-1.50E-01		-1.50E-04

		1.37E+00		-1.47E-01		-1.47E-04

		1.37E+00		-1.44E-01		-1.44E-04

		1.36E+00		-1.41E-01		-1.41E-04

		1.36E+00		-1.38E-01		-1.38E-04

		1.35E+00		-1.34E-01		-1.34E-04

		1.35E+00		-1.31E-01		-1.31E-04

		1.35E+00		-1.28E-01		-1.28E-04

		1.34E+00		-1.25E-01		-1.25E-04

		1.34E+00		-1.21E-01		-1.21E-04

		1.33E+00		-1.17E-01		-1.17E-04

		1.33E+00		-1.14E-01		-1.14E-04

		1.33E+00		-1.10E-01		-1.10E-04

		1.32E+00		-1.07E-01		-1.07E-04

		1.32E+00		-1.03E-01		-1.03E-04

		1.31E+00		-9.91E-02		-9.91E-05

		1.31E+00		-9.52E-02		-9.52E-05

		1.31E+00		-9.14E-02		-9.14E-05

		1.30E+00		-8.77E-02		-8.77E-05

		1.30E+00		-8.37E-02		-8.37E-05

		1.29E+00		-7.98E-02		-7.98E-05

		1.29E+00		-7.57E-02		-7.57E-05

		1.29E+00		-7.18E-02		-7.18E-05

		1.28E+00		-6.79E-02		-6.79E-05

		1.28E+00		-6.36E-02		-6.36E-05

		1.27E+00		-5.96E-02		-5.96E-05

		1.27E+00		-5.52E-02		-5.52E-05

		1.27E+00		-5.12E-02		-5.12E-05

		1.26E+00		-4.70E-02		-4.70E-05

		1.26E+00		-4.26E-02		-4.26E-05

		1.25E+00		-3.84E-02		-3.84E-05

		1.25E+00		-3.38E-02		-3.38E-05

		1.25E+00		-2.96E-02		-2.96E-05

		1.24E+00		-2.52E-02		-2.52E-05

		1.24E+00		-2.07E-02		-2.07E-05

		1.23E+00		-1.65E-02		-1.65E-05

		1.23E+00		-1.18E-02		-1.18E-05

		1.23E+00		-7.44E-03		-7.44E-06

		1.22E+00		-2.98E-03		-2.98E-06

		1.22E+00		1.58E-03		1.58E-06

		1.21E+00		6.07E-03		6.07E-06

		1.21E+00		1.06E-02		1.06E-05

		1.21E+00		1.51E-02		1.51E-05

		1.20E+00		1.96E-02		1.96E-05

		1.20E+00		2.41E-02		2.41E-05

		1.19E+00		2.84E-02		2.84E-05

		1.19E+00		3.30E-02		3.30E-05

		1.19E+00		3.73E-02		3.73E-05

		1.18E+00		4.20E-02		4.20E-05

		1.18E+00		4.64E-02		4.64E-05

		1.17E+00		5.09E-02		5.09E-05

		1.17E+00		5.55E-02		5.55E-05

		1.17E+00		5.98E-02		5.98E-05

		1.16E+00		6.44E-02		6.44E-05

		1.16E+00		6.89E-02		6.89E-05

		1.15E+00		7.34E-02		7.34E-05

		1.15E+00		7.80E-02		7.80E-05

		1.15E+00		8.23E-02		8.23E-05

		1.14E+00		8.70E-02		8.70E-05

		1.14E+00		9.14E-02		9.14E-05

		1.13E+00		9.61E-02		9.61E-05

		1.13E+00		1.01E-01		1.01E-04

		1.13E+00		1.05E-01		1.05E-04

		1.12E+00		1.10E-01		1.10E-04

		1.12E+00		1.14E-01		1.14E-04

		1.11E+00		1.19E-01		1.19E-04

		1.11E+00		1.24E-01		1.24E-04

		1.11E+00		1.28E-01		1.28E-04

		1.10E+00		1.33E-01		1.33E-04

		1.10E+00		1.37E-01		1.37E-04

		1.09E+00		1.42E-01		1.42E-04

		1.09E+00		1.46E-01		1.46E-04

		1.09E+00		1.51E-01		1.51E-04

		1.08E+00		1.55E-01		1.55E-04

		1.08E+00		1.60E-01		1.60E-04

		1.07E+00		1.64E-01		1.64E-04

		1.07E+00		1.69E-01		1.69E-04

		1.07E+00		1.73E-01		1.73E-04

		1.06E+00		1.77E-01		1.77E-04

		1.06E+00		1.82E-01		1.82E-04

		1.05E+00		1.86E-01		1.86E-04

		1.05E+00		1.90E-01		1.90E-04

		1.05E+00		1.95E-01		1.95E-04

		1.04E+00		1.99E-01		1.99E-04

		1.04E+00		2.04E-01		2.04E-04

		1.03E+00		2.08E-01		2.08E-04

		1.03E+00		2.12E-01		2.12E-04

		1.03E+00		2.16E-01		2.16E-04

		1.02E+00		2.20E-01		2.20E-04

		1.02E+00		2.25E-01		2.25E-04

		1.01E+00		2.28E-01		2.28E-04

		1.01E+00		2.33E-01		2.33E-04

		1.01E+00		2.37E-01		2.37E-04

		1.00E+00		2.41E-01		2.41E-04

		9.97E-01		2.46E-01		2.46E-04

		9.93E-01		2.49E-01		2.49E-04

		9.89E-01		2.54E-01		2.54E-04

		9.85E-01		2.58E-01		2.58E-04

		9.81E-01		2.62E-01		2.62E-04

		9.77E-01		2.66E-01		2.66E-04

		9.73E-01		2.70E-01		2.70E-04

		9.69E-01		2.74E-01		2.74E-04

		9.65E-01		2.78E-01		2.78E-04

		9.61E-01		2.82E-01		2.82E-04

		9.57E-01		2.86E-01		2.86E-04

		9.53E-01		2.90E-01		2.90E-04

		9.49E-01		2.94E-01		2.94E-04

		9.45E-01		2.97E-01		2.97E-04
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		-0.070012

		-0.066012

		-0.062012

		-0.058012

		-0.054012

		-0.050012

		-0.046012

		-0.042012

		-0.038012

		-0.034012

		-0.030012

		-0.026012

		-0.022012

		-0.018012

		-0.014012

		-0.010012

		-0.0060115

		-0.0020115

		0.0019885

		0.0059885

		0.0099885

		0.013988

		0.017988

		0.021988

		0.025988

		0.029988

		0.033988

		0.037988

		0.041988

		0.045988

		0.049988

		0.053988

		0.057988

		0.061988

		0.065988

		0.069988

		0.073988

		0.077988

		0.081988

		0.085988

		0.089988

		0.093988

		0.097988

		0.10199

		0.10599

		0.10999

		0.11399

		0.11799

		0.12199

		0.12599

		0.12999

		0.13399

		0.13799

		0.14199

		0.14599

		0.14999

		0.15399

		0.15799

		0.16199

		0.16599

		0.16999

		0.17399

		0.17799

		0.18199

		0.18599

		0.18999

		0.19399

		0.19799

		0.20199

		0.20599

		0.20999

		0.21399

		0.21799

		0.22199

		0.22599

		0.22999

		0.23399

		0.23799

		0.24199

		0.24599

		0.24999

		0.25399

		0.25799

		0.26199

		0.26599

		0.26999

		0.27399

		0.27799

		0.28199

		0.28599

		0.28999

		0.29399

		0.29799

		0.30199

		0.30599

		0.30999

		0.31399

		0.31799

		0.32199

		0.32599

		0.32999

		0.33399

		0.33799

		0.34199

		0.34599

		0.34999

		0.35399

		0.35799

		0.36199

		0.36599

		0.36999

		0.37399

		0.37799

		0.38199

		0.38599

		0.38999

		0.39399

		0.39799

		0.40199

		0.40599

		0.40999

		0.41399

		0.41799

		0.42199

		0.42599

		0.42999

		0.43399

		0.43799

		0.44199

		0.44599

		0.44999

		0.45399

		0.45799

		0.46199

		0.46599

		0.46999

		0.47399

		0.47799

		0.48199

		0.48599

		0.48999

		0.49399

		0.49799

		0.50199

		0.50599

		0.50999

		0.51399

		0.51799

		0.52199

		0.52599

		0.52999

		0.53399

		0.53799

		0.54199

		0.54599

		0.54999

		0.55399

		0.55799

		0.56199

		0.56599

		0.56999

		0.57399

		0.57799

		0.58199

		0.58599

		0.58999

		0.59399

		0.59799

		0.60199

		0.60599

		0.60999

		0.61399

		0.61799

		0.62199

		0.62599

		0.62999

		0.63399

		0.63799

		0.64199

		0.64599

		0.64999

		0.65399

		0.65799

		0.66199

		0.66599

		0.66999

		0.67399

		0.67799

		0.68199

		0.68599

		0.68999

		0.69399

		0.69799

		0.70199

		0.70599

		0.70999

		0.71399

		0.71799

		0.72199

		0.72599

		0.72999

		0.73399

		0.73799

		0.74199

		0.74599

		0.74999

		0.75399

		0.75799

		0.76199

		0.76599

		0.76999

		0.77399

		0.77799

		0.78199

		0.78599

		0.78999

		0.79399

		0.79799

		0.80199

		0.80599

		0.80999

		0.81399

		0.81799

		0.82199

		0.82599

		0.82999

		0.83399

		0.83799

		0.84199

		0.84599

		0.84999

		0.85399

		0.85799

		0.86199

		0.86599

		0.86999

		0.87399

		0.87799

		0.88199

		0.88599

		0.88999

		0.89399

		0.89799

		0.90199

		0.90599

		0.90999

		0.91399

		0.91799

		0.92199

		0.92599

		0.92999

		0.93399

		0.93799

		0.94199

		0.94599

		0.94999

		0.95399

		0.95799

		0.96199

		0.96599

		0.96999

		0.97399

		0.97799

		0.98199

		0.98599

		0.98999

		0.99399

		0.99799

		1.002

		1.006

		1.01

		1.014

		1.018

		1.022

		1.026

		1.03

		1.034

		1.038

		1.042

		1.046

		1.05

		1.054

		1.058

		1.062

		1.066

		1.07

		1.074

		1.078

		1.082

		1.086

		1.09

		1.094

		1.098

		1.102

		1.106

		1.11

		1.114

		1.118

		1.122

		1.126

		1.13

		1.134

		1.138

		1.142

		1.146

		1.15

		1.154

		1.158

		1.162

		1.166

		1.17

		1.174

		1.178

		1.182

		1.186

		1.19

		1.194

		1.198

		1.202

		1.206

		1.21

		1.214

		1.218

		1.222

		1.226

		1.23

		1.234

		1.238

		1.242

		1.246

		1.25

		1.254

		1.258

		1.262

		1.266

		1.27

		1.274

		1.278

		1.282

		1.286

		1.29

		1.294

		1.298

		1.302

		1.306

		1.31

		1.314

		1.318

		1.322

		1.326

		1.33

		1.334

		1.338

		1.342

		1.346

		1.35

		1.354

		1.358

		1.362

		1.366

		1.37

		1.374

		1.378

		1.382

		1.386

		1.39

		1.394

		1.398

		1.402

		1.406

		1.41

		1.414

		1.418

		1.422

		1.426

		1.43

		1.434

		1.438

		1.442

		1.446

		1.45

		1.454

		1.458

		1.462

		1.466

		1.47

		1.474

		1.478

		1.482

		1.486

		1.49

		1.494

		1.498

		1.502

		1.506

		1.51

		1.514

		1.518

		1.522

		1.526

		1.53

		1.534

		1.538

		1.542

		1.546

		1.55

		1.554

		1.558

		1.562

		1.566

		1.57

		1.574

		1.578

		1.582

		1.586

		1.59

		1.594

		1.598

		1.602

		1.606

		1.61

		1.614

		1.618

		1.622

		1.626

		1.63

		1.634

		1.638

		1.642

		1.646

		1.65

		1.654

		1.658

		1.662

		1.666

		1.67

		1.674

		1.678

		1.682

		1.686

		1.69

		1.694

		1.698

		1.702

		1.706

		1.71

		1.714

		1.718

		1.722

		1.726

		1.73

		1.734

		1.738

		1.742

		1.746

		1.75

		1.754

		1.758

		1.762

		1.766

		1.77

		1.774

		1.778

		1.782

		1.786

		1.79

		1.794

		1.798

		1.802

		1.806

		1.81

		1.814

		1.818

		1.822

		1.826

		1.83

		1.834

		1.838

		1.842

		1.846

		1.85

		1.854

		1.858

		1.862

		1.866

		1.87

		1.874

		1.878

		1.882

		1.886

		1.89

		1.894

		1.898

		1.902

		1.906

		1.91

		1.914

		1.918

		1.922

		1.926

		1.93

		1.934

		1.938

		1.942

		1.946

		1.95

		1.954

		1.958

		1.962

		1.966

		1.97

		1.974

		1.978

		1.982

		1.986

		1.99

		1.994

		1.998

		2.002

		1.998

		1.994

		1.99

		1.986

		1.982

		1.978

		1.974

		1.97

		1.966

		1.962

		1.958

		1.954

		1.95

		1.946

		1.942

		1.938

		1.934

		1.93

		1.926

		1.922

		1.918

		1.914

		1.91

		1.906

		1.902

		1.898

		1.894

		1.89

		1.886

		1.882

		1.878

		1.874

		1.87

		1.866

		1.862

		1.858

		1.854

		1.85

		1.846

		1.842

		1.838

		1.834

		1.83

		1.826

		1.822

		1.818

		1.814

		1.81

		1.806

		1.802

		1.798

		1.794

		1.79

		1.786

		1.782

		1.778

		1.774

		1.77

		1.766

		1.762

		1.758

		1.754

		1.75

		1.746

		1.742

		1.738

		1.734

		1.73

		1.726

		1.722

		1.718

		1.714

		1.71

		1.706

		1.702

		1.698

		1.694

		1.69

		1.686

		1.682

		1.678

		1.674

		1.67

		1.666

		1.662

		1.658

		1.654

		1.65

		1.646

		1.642

		1.638

		1.634

		1.63

		1.626

		1.622

		1.618

		1.614

		1.61

		1.606

		1.602

		1.598

		1.594

		1.59

		1.586

		1.582

		1.578

		1.574

		1.57

		1.566

		1.562

		1.558

		1.554

		1.55

		1.546

		1.542

		1.538

		1.534

		1.53

		1.526

		1.522

		1.518

		1.514

		1.51

		1.506

		1.502

		1.498

		1.494

		1.49

		1.486

		1.482

		1.478

		1.474

		1.47

		1.466

		1.462

		1.458

		1.454

		1.45

		1.446

		1.442

		1.438

		1.434

		1.43

		1.426

		1.422

		1.418

		1.414

		1.41

		1.406

		1.402

		1.398

		1.394

		1.39

		1.386

		1.382

		1.378

		1.374

		1.37

		1.366

		1.362

		1.358

		1.354

		1.35

		1.346

		1.342

		1.338

		1.334

		1.33

		1.326

		1.322

		1.318

		1.314

		1.31

		1.306

		1.302

		1.298

		1.294

		1.29

		1.286

		1.282

		1.278

		1.274

		1.27

		1.266

		1.262

		1.258

		1.254

		1.25

		1.246

		1.242

		1.238

		1.234

		1.23

		1.226

		1.222

		1.218

		1.214

		1.21

		1.206

		1.202

		1.198

		1.194

		1.19

		1.186

		1.182

		1.178

		1.174

		1.17

		1.166

		1.162

		1.158

		1.154

		1.15

		1.146

		1.142

		1.138

		1.134

		1.13



Potential (V)

Current (uA)

0.0194

0.113

0.106

0.165

0.21

0.23

0.279

0.248

0.29

0.324

0.323

0.381

0.315

0.357

0.382

0.368

0.429

0.351

0.401

0.408

0.394

0.451

0.372

0.419

0.42

0.41

0.448

0.385

0.435

0.421

0.418

0.455

0.398

0.423

0.439

0.426

0.459

0.402

0.44

0.45

0.423

0.476

0.42

0.45

0.465

0.436

0.49

0.408

0.468

0.495

0.455

0.515

0.438

0.492

0.492

0.482

0.543

0.457

0.519

0.531

0.515

0.555

0.502

0.558

0.567

0.554

0.595

0.545

0.587

0.618

0.6

0.636

0.595

0.64

0.666

0.641

0.689

0.646

0.696

0.723

0.704

0.755

0.688

0.766

0.781

0.765

0.82

0.756

0.829

0.839

0.838

0.874

0.822

0.908

0.918

0.914

0.938

0.912

0.971

0.999

1.003

1.031

0.994

1.055

1.104

1.078

1.112

1.104

1.166

1.21

1.201

1.25

1.227

1.305

1.361

1.366

1.406

1.41

1.507

1.46

1.53

1.51

1.64

1.68

1.77

1.81

1.86

1.94

2.01

2.12

2.17

2.3

2.39

2.5

2.62

2.75

2.89

3.03

3.23

3.37

3.54

3.71

3.97

4.2

4.45

4.72

4.99

5.3

5.57

5.89

6.24

6.6

6.98

7.31

7.72

8.11

8.42

8.82

9.11

9.56

9.86

10.19

10.53

10.78

11.04

11.28

11.58

11.68

11.88

12.07

12.19

12.26

12.23

12.4

12.41

12.38

12.45

12.32

12.27

12.22

12.19

12.19

12.04

11.95

11.86

11.69

11.62

11.5

11.38

11.27

11.22

11.15

10.94

10.9

10.78

10.66

10.63

10.49

10.44

10.33

10.25

10.21

10.01

10.06

10.01

9.94

9.91

9.72

9.79

9.67

9.68

9.68

9.59

9.64

9.61

9.58

9.5

9.51

9.55

9.58

9.56

9.56

9.59

9.59

9.67

9.65

9.71

9.76

9.84

9.88

9.92

10

10.14

10.28

10.39

10.49

10.56

10.7

10.93

11.08

11.15

11.34

11.59

11.75

11.9

12.2

12.41

12.66

12.9

13.16

13.35

13.53

13.92

14.15

14.44

14.62

14.87

15.2

15.33

15.67

15.78

16.01

16.33

16.5

16.7

16.77

17.03

17.21

17.38

17.57

17.67

17.75

18

18.2

18.2

18.4

18.3

18.5

18.2

18.4

18.6

18.4

18.7

19

18.7

18.7

18.7

18.5

18.6

18.4

18.5

18.3

18.4

18.3

18.3

18.1

18

18.1

18

17.8

17.7

17.7

17.8

17.4

17.3

17.5

17.4

17.5

17.3

17

17.1

17

16.8

17

16.8

17

16.7

16.6

16.4

16.5

16.5

16.5

16.6

16.3

16.5

16.3

16.2

16.1

16

15.7

16

16

16

16

15.8

15.6

15.8

15.8

15.5

15.7

15.7

15.7

15.5

15.3

15.4

15.6

15.4

15.2

15.6

15.4

15.5

15.5

15.5

15.7

15.5

15.4

15.6

16

15.9

16.1

16

16

16.2

16.4

16.7

16.8

16.9

17

17.3

17.3

17.8

18

18.2

18.5

18.5

19

19.1

19.7

19.9

20.3

20.8

21

21.1

21.8

22.2

22.3

22.7

22.9

23.3

23.6

24

24.4

25

25

25.2

25.4

25.6

26.1

26

26.4

26.5

26.8

26.8

26.9

27.2

27.3

27.2

27.2

27.4

27.4

27.6

27.5

27.5

27.2

27.4

27.5

27.5

27.7

27.5

27.5

27

27.4

27.1

27.1

27.2

26.7

27

26.8

26.9

26.6

26.5

26.5

26.3

26.2

26.2

26.3

25.9

26

25.6

25.8

25.6

25.7

25.4

25.3

25.2

24.8

25

24.8

25

24.6

24.8

24.2

24.3

24.3

24

24.2

24

23.9

23.7

23.9

23.6

23.7

23.6

23.4

23.1

23.2

23.3

23.1

23.2

23.1

23.2

22.6

23

22.9

22.6

22.7

22.7

22.6

22.4

22.4

22.5

22.4

22.4

22.3

22.3

22.2

22.2

22.1

22.1

22.1

22

21.8

22

21.7

21.8

21.8

21.8

21.7

21.6

21.8

21.5

21.7

21.4

21.5

21.3

21.4

21.5

21.4

21.6

21.1

21.4

21.4

21.2

21.2

21.3

21

21

21.1

21.1

21.3

21.1

21.1

20.6

20.8

20.7

20.8

20.7

20.8

20.7

20.5

21

20.8

20.8

20.8

20.7

20.7

20.4

20.8

20.7

20.6

20.3

20.6

20.4

20.4

20.5

20.3

20.3

20.3

20.4

20.3

20.4

20.2

20.3

20.2

20.2

20.2

20.2

20.5

20.2

20.5

20.3

20.3

20.2

20.2

20.4

20.1

20.4

20.2

20.2

20.1

20.1

20.2

20.2

19.9

20.3

20.1

20

20.3

20.2

20.3

19.8

20.2

20.1

20.2

20.2

20.3

20.4

20.2

20.6

20.3

20.6

20.4

20.6

20.7

20.5

20.8

20.7

20.9

20.7

21.1

20.9

21

21.1

21.1

21.4

21.3

21.4

21.5

21.7

21.5

22

21.7

21.8

22

21.8

22.2

22.2

22.5

22.4

22.6

22.3

22.8

22.5

22.9

23.2

23

23.1

23.3

23.4

23.5

23.7

23.3

23.8

23.9

24

24.3

24.3

24.6

24.4

24.9

25

25.1

25.2

25.4

25.8

25.7

26

26.1

26.5

26.6

26.8

26.9

27.3

27.4

27.4

27.8

27.5

28.2

28.2

28.8

28.8

29.1

29.3

29.5

29.9

30.2

30.3

30.6

31.2

31.1

31.7

31.8

32.3

32.5

32.9

33.5

33.5

33.9

34.3

34.9

35.1

35.7

35.9

36.5

37

37.3

37.8

38.2

38.8

39

39.7

40.3

40.8

41.4

41.9

42.6

43

43.6

44.4

44.9

45.5

46.4

46.8

47.7

48.4

49.2

49.8

50.4

51.4

52.1

52.9

53.4

54.6

55.2

55.8

57.1

57.7

58.7

59.4

60.8

61.5

62.6

63.7

64.8

65.8

66.7

68

69

70.3

71.5

72.8

73.8

75.3

76.3

78.1

79.4

80.8

82.1

83.1

85

86.2

87.8

89.1

90.9

92.3

94

95.7

97.2

99.1

101.1

102.9

104.6

106.5

108.3

110.3

112.2

114.5

116.6

118.2

120.7

122.8

125.3

127.5

130.2

132.2

134.5

137.2

139.5

142.3

145

147.2

150.1

152.7

155.6

158.7

161.3

164.8

167.8

171

174.4

177.2

180.9

184.2

179.8

175.8

171.7

168.1

164

160.9

157.3

153.6

150.7

147.6
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		1.13E+00		1.94E-02		1.94E-08		7.53E-01		-9.00E-03		-9.00E-09

		1.13E+00		1.13E-01		1.13E-07		7.49E-01		1.51E-02		1.51E-08

		1.12E+00		1.06E-01		1.06E-07		7.45E-01		-6.20E-03		-6.20E-09

		1.12E+00		1.65E-01		1.65E-07		7.41E-01		1.35E-02		1.35E-08

		1.11E+00		2.10E-01		2.10E-07		7.37E-01		8.70E-03		8.70E-09

		1.11E+00		2.30E-01		2.30E-07		7.33E-01		1.70E-03		1.70E-09

		1.11E+00		2.79E-01		2.79E-07		7.29E-01		2.25E-02		2.25E-08

		1.10E+00		2.48E-01		2.48E-07		7.25E-01		-3.20E-03		-3.20E-09

		1.10E+00		2.90E-01		2.90E-07		7.21E-01		2.16E-02		2.16E-08

		1.09E+00		3.24E-01		3.24E-07		7.17E-01		1.50E-02		1.50E-08

		1.09E+00		3.23E-01		3.23E-07		7.13E-01		4.50E-03		4.50E-09

		1.09E+00		3.81E-01		3.81E-07		7.09E-01		2.79E-02		2.79E-08

		1.08E+00		3.15E-01		3.15E-07		7.05E-01		4.10E-03		4.10E-09

		1.08E+00		3.57E-01		3.57E-07		7.01E-01		2.32E-02		2.32E-08

		1.07E+00		3.82E-01		3.82E-07		6.97E-01		1.96E-02		1.96E-08

		1.07E+00		3.68E-01		3.68E-07		6.93E-01		9.50E-03		9.50E-09

		1.07E+00		4.29E-01		4.29E-07		6.89E-01		3.30E-02		3.30E-08

		1.06E+00		3.51E-01		3.51E-07		6.85E-01		7.70E-03		7.70E-09

		1.06E+00		4.01E-01		4.01E-07		6.81E-01		2.90E-02		2.90E-08

		1.05E+00		4.08E-01		4.08E-07		6.77E-01		2.54E-02		2.54E-08

		1.05E+00		3.94E-01		3.94E-07		6.73E-01		1.58E-02		1.58E-08

		1.05E+00		4.51E-01		4.51E-07		6.69E-01		3.64E-02		3.64E-08

		1.04E+00		3.72E-01		3.72E-07		6.65E-01		1.58E-02		1.58E-08

		1.04E+00		4.19E-01		4.19E-07		6.61E-01		3.59E-02		3.59E-08

		1.03E+00		4.20E-01		4.20E-07		6.57E-01		2.91E-02		2.91E-08

		1.03E+00		4.10E-01		4.10E-07		6.53E-01		2.23E-02		2.23E-08

		1.03E+00		4.48E-01		4.48E-07		6.49E-01		4.54E-02		4.54E-08

		1.02E+00		3.85E-01		3.85E-07		6.45E-01		1.92E-02		1.92E-08

		1.02E+00		4.35E-01		4.35E-07		6.41E-01		4.20E-02		4.20E-08

		1.01E+00		4.21E-01		4.21E-07		6.37E-01		3.75E-02		3.75E-08

		1.01E+00		4.18E-01		4.18E-07		6.33E-01		2.90E-02		2.90E-08

		1.01E+00		4.55E-01		4.55E-07		6.29E-01		5.02E-02		5.02E-08

		1.00E+00		3.98E-01		3.98E-07		6.25E-01		2.75E-02		2.75E-08

		9.98E-01		4.23E-01		4.23E-07		6.21E-01		4.97E-02		4.97E-08

		9.94E-01		4.39E-01		4.39E-07		6.17E-01		2.40E-02		2.40E-08

		9.90E-01		4.26E-01		4.26E-07		6.13E-01		3.54E-02		3.54E-08

		9.86E-01		4.59E-01		4.59E-07		6.09E-01		5.96E-02		5.96E-08

		9.82E-01		4.02E-01		4.02E-07		6.05E-01		3.20E-02		3.20E-08

		9.78E-01		4.40E-01		4.40E-07		6.01E-01		5.65E-02		5.65E-08

		9.74E-01		4.50E-01		4.50E-07		5.97E-01		2.20E-02		2.20E-08

		9.70E-01		4.23E-01		4.23E-07		5.93E-01		4.72E-02		4.72E-08

		9.66E-01		4.76E-01		4.76E-07		5.89E-01		5.60E-02		5.60E-08

		9.62E-01		4.20E-01		4.20E-07		5.85E-01		4.48E-02		4.48E-08

		9.58E-01		4.50E-01		4.50E-07		5.81E-01		6.87E-02		6.87E-08

		9.54E-01		4.65E-01		4.65E-07		5.77E-01		3.60E-02		3.60E-08

		9.50E-01		4.36E-01		4.36E-07		5.73E-01		5.38E-02		5.38E-08

		9.46E-01		4.90E-01		4.90E-07		5.69E-01		6.90E-02		6.90E-08

		9.42E-01		4.08E-01		4.08E-07		5.65E-01		5.44E-02		5.44E-08

		9.38E-01		4.68E-01		4.68E-07		5.61E-01		9.00E-02		9.00E-08

		9.34E-01		4.95E-01		4.95E-07		5.57E-01		7.17E-02		7.17E-08

		9.30E-01		4.55E-01		4.55E-07		5.53E-01		7.80E-02		7.80E-08

		9.26E-01		5.15E-01		5.15E-07		5.49E-01		8.74E-02		8.74E-08

		9.22E-01		4.38E-01		4.38E-07		5.45E-01		6.40E-02		6.40E-08

		9.18E-01		4.92E-01		4.92E-07		5.41E-01		8.76E-02		8.76E-08

		9.14E-01		4.92E-01		4.92E-07		5.37E-01		6.30E-02		6.30E-08

		9.10E-01		4.82E-01		4.82E-07		5.33E-01		7.53E-02		7.53E-08

		9.06E-01		5.43E-01		5.43E-07		5.29E-01		9.00E-02		9.00E-08

		9.02E-01		4.57E-01		4.57E-07		5.25E-01		7.83E-02		7.83E-08

		8.98E-01		5.19E-01		5.19E-07		5.21E-01		1.16E-01		1.16E-07

		8.94E-01		5.31E-01		5.31E-07		5.17E-01		9.32E-02		9.32E-08

		8.90E-01		5.15E-01		5.15E-07		5.13E-01		1.03E-01		1.03E-07

		8.86E-01		5.55E-01		5.55E-07		5.09E-01		1.10E-01		1.10E-07

		8.82E-01		5.02E-01		5.02E-07		5.05E-01		8.80E-02		8.80E-08

		8.78E-01		5.58E-01		5.58E-07		5.01E-01		1.13E-01		1.13E-07

		8.74E-01		5.67E-01		5.67E-07		4.97E-01		8.40E-02		8.40E-08

		8.70E-01		5.54E-01		5.54E-07		4.93E-01		1.02E-01		1.02E-07

		8.66E-01		5.95E-01		5.95E-07		4.89E-01		1.14E-01		1.14E-07

		8.62E-01		5.45E-01		5.45E-07		4.85E-01		1.02E-01		1.02E-07

		8.58E-01		5.87E-01		5.87E-07		4.81E-01		1.44E-01		1.44E-07

		8.54E-01		6.18E-01		6.18E-07		4.77E-01		1.21E-01		1.21E-07

		8.50E-01		6.00E-01		6.00E-07		4.73E-01		1.29E-01		1.29E-07

		8.46E-01		6.36E-01		6.36E-07		4.69E-01		1.39E-01		1.39E-07

		8.42E-01		5.95E-01		5.95E-07		4.65E-01		1.15E-01		1.15E-07

		8.38E-01		6.40E-01		6.40E-07		4.61E-01		1.40E-01		1.40E-07

		8.34E-01		6.66E-01		6.66E-07		4.57E-01		1.12E-01		1.12E-07

		8.30E-01		6.41E-01		6.41E-07		4.53E-01		1.32E-01		1.32E-07

		8.26E-01		6.89E-01		6.89E-07		4.49E-01		1.43E-01		1.43E-07

		8.22E-01		6.46E-01		6.46E-07		4.45E-01		1.35E-01		1.35E-07

		8.18E-01		6.96E-01		6.96E-07		4.41E-01		1.68E-01		1.68E-07

		8.14E-01		7.23E-01		7.23E-07		4.37E-01		1.30E-01		1.30E-07

		8.10E-01		7.04E-01		7.04E-07		4.33E-01		1.55E-01		1.55E-07

		8.06E-01		7.55E-01		7.55E-07		4.29E-01		1.65E-01		1.65E-07

		8.02E-01		6.88E-01		6.88E-07		4.25E-01		1.50E-01		1.50E-07

		7.98E-01		7.66E-01		7.66E-07		4.21E-01		1.93E-01		1.93E-07

		7.94E-01		7.81E-01		7.81E-07		4.17E-01		1.46E-01		1.46E-07

		7.90E-01		7.65E-01		7.65E-07		4.13E-01		1.83E-01		1.83E-07

		7.86E-01		8.20E-01		8.20E-07		4.09E-01		1.81E-01		1.81E-07

		7.82E-01		7.56E-01		7.56E-07		4.05E-01		1.78E-01		1.78E-07

		7.78E-01		8.29E-01		8.29E-07		4.01E-01		2.10E-01		2.10E-07

		7.74E-01		8.39E-01		8.39E-07		3.97E-01		1.73E-01		1.73E-07

		7.70E-01		8.38E-01		8.38E-07		3.93E-01		1.99E-01		1.99E-07

		7.66E-01		8.74E-01		8.74E-07		3.89E-01		2.12E-01		2.12E-07

		7.62E-01		8.22E-01		8.22E-07		3.85E-01		1.98E-01		1.98E-07

		7.58E-01		9.08E-01		9.08E-07		3.81E-01		2.43E-01		2.43E-07

		7.54E-01		9.18E-01		9.18E-07		3.77E-01		1.92E-01		1.92E-07

		7.50E-01		9.14E-01		9.14E-07		3.73E-01		2.38E-01		2.38E-07

		7.46E-01		9.38E-01		9.38E-07		3.69E-01		2.31E-01		2.31E-07

		7.42E-01		9.12E-01		9.12E-07		3.65E-01		2.33E-01		2.33E-07

		7.38E-01		9.71E-01		9.71E-07		3.61E-01		2.67E-01		2.67E-07

		7.34E-01		9.99E-01		9.99E-07		3.57E-01		2.37E-01		2.37E-07

		7.30E-01		1.00E+00		1.00E-06		3.53E-01		2.63E-01		2.63E-07

		7.26E-01		1.03E+00		1.03E-06		3.49E-01		2.70E-01		2.70E-07

		7.22E-01		9.94E-01		9.94E-07		3.45E-01		2.60E-01		2.60E-07

		7.18E-01		1.06E+00		1.06E-06		3.41E-01		3.11E-01		3.11E-07

		7.14E-01		1.10E+00		1.10E-06		3.37E-01		2.60E-01		2.60E-07

		7.10E-01		1.08E+00		1.08E-06		3.33E-01		3.05E-01		3.05E-07

		7.06E-01		1.11E+00		1.11E-06		3.29E-01		3.04E-01		3.04E-07

		7.02E-01		1.10E+00		1.10E-06		3.25E-01		3.02E-01		3.02E-07

		6.98E-01		1.17E+00		1.17E-06		3.21E-01		3.32E-01		3.32E-07

		6.94E-01		1.21E+00		1.21E-06		3.17E-01		3.09E-01		3.09E-07

		6.90E-01		1.20E+00		1.20E-06		3.13E-01		3.34E-01		3.34E-07

		6.86E-01		1.25E+00		1.25E-06		3.09E-01		3.49E-01		3.49E-07

		6.82E-01		1.23E+00		1.23E-06		3.05E-01		3.35E-01		3.35E-07

		6.78E-01		1.31E+00		1.31E-06		3.01E-01		3.84E-01		3.84E-07

		6.74E-01		1.36E+00		1.36E-06		2.97E-01		3.38E-01		3.38E-07

		6.70E-01		1.37E+00		1.37E-06		2.93E-01		3.83E-01		3.83E-07

		6.66E-01		1.41E+00		1.41E-06		2.89E-01		3.79E-01		3.79E-07

		6.62E-01		1.41E+00		1.41E-06		2.85E-01		3.81E-01		3.81E-07

		6.58E-01		1.51E+00		1.51E-06		2.81E-01		4.15E-01		4.15E-07

		6.54E-01		1.46E+00		1.46E-06		2.77E-01		3.80E-01		3.80E-07

		6.50E-01		1.53E+00		1.53E-06		2.73E-01		4.12E-01		4.12E-07

		6.46E-01		1.51E+00		1.51E-06		2.69E-01		4.23E-01		4.23E-07

		6.42E-01		1.64E+00		1.64E-06		2.65E-01		4.10E-01		4.10E-07

		6.38E-01		1.68E+00		1.68E-06		2.61E-01		4.65E-01		4.65E-07

		6.34E-01		1.77E+00		1.77E-06		2.57E-01		4.11E-01		4.11E-07

		6.30E-01		1.81E+00		1.81E-06		2.53E-01		4.58E-01		4.58E-07

		6.26E-01		1.86E+00		1.86E-06		2.49E-01		4.54E-01		4.54E-07

		6.22E-01		1.94E+00		1.94E-06		2.45E-01		4.54E-01		4.54E-07

		6.18E-01		2.01E+00		2.01E-06		2.41E-01		4.88E-01		4.88E-07

		6.14E-01		2.12E+00		2.12E-06		2.37E-01		4.54E-01		4.54E-07

		6.10E-01		2.17E+00		2.17E-06		2.33E-01		4.88E-01		4.88E-07

		6.06E-01		2.30E+00		2.30E-06		2.29E-01		5.02E-01		5.02E-07

		6.02E-01		2.39E+00		2.39E-06		2.25E-01		4.84E-01		4.84E-07

		5.98E-01		2.50E+00		2.50E-06		2.21E-01		5.37E-01		5.37E-07

		5.94E-01		2.62E+00		2.62E-06		2.17E-01		4.92E-01		4.92E-07

		5.90E-01		2.75E+00		2.75E-06		2.13E-01		5.33E-01		5.33E-07

		5.86E-01		2.89E+00		2.89E-06		2.09E-01		5.35E-01		5.35E-07

		5.82E-01		3.03E+00		3.03E-06		2.05E-01		5.39E-01		5.39E-07

		5.78E-01		3.23E+00		3.23E-06		2.01E-01		5.76E-01		5.76E-07

		5.74E-01		3.37E+00		3.37E-06		1.97E-01		5.42E-01		5.42E-07

		5.70E-01		3.54E+00		3.54E-06		1.93E-01		5.79E-01		5.79E-07

		5.66E-01		3.71E+00		3.71E-06		1.89E-01		5.92E-01		5.92E-07

		5.62E-01		3.97E+00		3.97E-06		1.85E-01		5.75E-01		5.75E-07

		5.58E-01		4.20E+00		4.20E-06		1.81E-01		6.42E-01		6.42E-07

		5.54E-01		4.45E+00		4.45E-06		1.77E-01		5.94E-01		5.94E-07

		5.50E-01		4.72E+00		4.72E-06		1.73E-01		6.43E-01		6.43E-07

		5.46E-01		4.99E+00		4.99E-06		1.69E-01		6.48E-01		6.48E-07

		5.42E-01		5.30E+00		5.30E-06		1.65E-01		6.48E-01		6.48E-07

		5.38E-01		5.57E+00		5.57E-06		1.61E-01		6.96E-01		6.96E-07

		5.34E-01		5.89E+00		5.89E-06		1.57E-01		6.56E-01		6.56E-07

		5.30E-01		6.24E+00		6.24E-06		1.53E-01		7.10E-01		7.10E-07

		5.26E-01		6.60E+00		6.60E-06		1.49E-01		7.17E-01		7.17E-07

		5.22E-01		6.98E+00		6.98E-06		1.45E-01		7.14E-01		7.14E-07

		5.18E-01		7.31E+00		7.31E-06		1.41E-01		7.70E-01		7.70E-07

		5.14E-01		7.72E+00		7.72E-06		1.37E-01		7.36E-01		7.36E-07

		5.10E-01		8.11E+00		8.11E-06		1.33E-01		7.86E-01		7.86E-07

		5.06E-01		8.42E+00		8.42E-06		1.29E-01		7.97E-01		7.97E-07

		5.02E-01		8.82E+00		8.82E-06		1.25E-01		7.97E-01		7.97E-07

		4.98E-01		9.11E+00		9.11E-06		1.21E-01		8.56E-01		8.56E-07

		4.94E-01		9.56E+00		9.56E-06		1.17E-01		8.22E-01		8.22E-07

		4.90E-01		9.86E+00		9.86E-06		1.13E-01		8.76E-01		8.76E-07

		4.86E-01		1.02E+01		1.02E-05		1.09E-01		8.88E-01		8.88E-07

		4.82E-01		1.05E+01		1.05E-05		1.05E-01		8.88E-01		8.88E-07

		4.78E-01		1.08E+01		1.08E-05		1.01E-01		9.49E-01		9.49E-07

		4.74E-01		1.10E+01		1.10E-05		9.70E-02		9.30E-01		9.30E-07

		4.70E-01		1.13E+01		1.13E-05		9.30E-02		9.74E-01		9.74E-07

		4.66E-01		1.16E+01		1.16E-05		8.90E-02		9.96E-01		9.96E-07

		4.62E-01		1.17E+01		1.17E-05		8.50E-02		9.94E-01		9.94E-07

		4.58E-01		1.19E+01		1.19E-05		8.10E-02		1.06E+00		1.06E-06

		4.54E-01		1.21E+01		1.21E-05		7.70E-02		1.03E+00		1.03E-06

		4.50E-01		1.22E+01		1.22E-05		7.30E-02		1.09E+00		1.09E-06

		4.46E-01		1.23E+01		1.23E-05		6.90E-02		1.10E+00		1.10E-06

		4.42E-01		1.22E+01		1.22E-05		6.50E-02		1.12E+00		1.12E-06

		4.38E-01		1.24E+01		1.24E-05		6.10E-02		1.17E+00		1.17E-06

		4.34E-01		1.24E+01		1.24E-05		5.70E-02		1.16E+00		1.16E-06

		4.30E-01		1.24E+01		1.24E-05		5.30E-02		1.22E+00		1.22E-06

		4.26E-01		1.25E+01		1.25E-05		4.90E-02		1.23E+00		1.23E-06

		4.22E-01		1.23E+01		1.23E-05		4.50E-02		1.24E+00		1.24E-06

		4.18E-01		1.23E+01		1.23E-05		4.10E-02		1.32E+00		1.32E-06

		4.14E-01		1.22E+01		1.22E-05		3.70E-02		1.29E+00		1.29E-06

		4.10E-01		1.22E+01		1.22E-05		3.30E-02		1.36E+00		1.36E-06

		4.06E-01		1.22E+01		1.22E-05		2.90E-02		1.38E+00		1.38E-06

		4.02E-01		1.20E+01		1.20E-05		2.50E-02		1.40E+00		1.40E-06

		3.98E-01		1.20E+01		1.20E-05		2.10E-02		1.46E+00		1.46E-06

		3.94E-01		1.19E+01		1.19E-05		1.70E-02		1.45E+00		1.45E-06

		3.90E-01		1.17E+01		1.17E-05		1.30E-02		1.51E+00		1.51E-06

		3.86E-01		1.16E+01		1.16E-05		9.00E-03		1.51E+00		1.51E-06

		3.82E-01		1.15E+01		1.15E-05		5.00E-03		1.54E+00		1.54E-06

		3.78E-01		1.14E+01		1.14E-05		9.99E-04		1.61E+00		1.61E-06

		3.74E-01		1.13E+01		1.13E-05		-3.00E-03		1.57E+00		1.57E-06

		3.70E-01		1.12E+01		1.12E-05		-7.00E-03		1.64E+00		1.64E-06

		3.66E-01		1.12E+01		1.12E-05		-1.10E-02		1.67E+00		1.67E-06

		3.62E-01		1.09E+01		1.09E-05		-1.50E-02		1.67E+00		1.67E-06

		3.58E-01		1.09E+01		1.09E-05		-1.90E-02		1.73E+00		1.73E-06

		3.54E-01		1.08E+01		1.08E-05		-2.30E-02		1.74E+00		1.74E-06

		3.50E-01		1.07E+01		1.07E-05		-2.70E-02		1.82E+00		1.82E-06

		3.46E-01		1.06E+01		1.06E-05		-3.10E-02		1.80E+00		1.80E-06

		3.42E-01		1.05E+01		1.05E-05		-3.50E-02		1.84E+00		1.84E-06

		3.38E-01		1.04E+01		1.04E-05		-3.90E-02		1.90E+00		1.90E-06

		3.34E-01		1.03E+01		1.03E-05		-4.30E-02		1.88E+00		1.88E-06

		3.30E-01		1.03E+01		1.03E-05		-4.70E-02		1.96E+00		1.96E-06

		3.26E-01		1.02E+01		1.02E-05		-5.10E-02		1.97E+00		1.97E-06

		3.22E-01		1.00E+01		1.00E-05		-5.50E-02		2.00E+00		2.00E-06

		3.18E-01		1.01E+01		1.01E-05		-5.90E-02		2.06E+00		2.06E-06

		3.14E-01		1.00E+01		1.00E-05		-6.30E-02		2.05E+00		2.05E-06

		3.10E-01		9.94E+00		9.94E-06		-6.70E-02		2.10E+00		2.10E-06

		3.06E-01		9.91E+00		9.91E-06		-7.10E-02		2.13E+00		2.13E-06

		3.02E-01		9.72E+00		9.72E-06		-7.50E-02		2.15E+00		2.15E-06

		2.98E-01		9.79E+00		9.79E-06		-7.90E-02		2.19E+00		2.19E-06

		2.94E-01		9.67E+00		9.67E-06		-8.30E-02		2.18E+00		2.18E-06

		2.90E-01		9.68E+00		9.68E-06		-8.70E-02		2.25E+00		2.25E-06

		2.86E-01		9.68E+00		9.68E-06		-9.10E-02		2.26E+00		2.26E-06

		2.82E-01		9.59E+00		9.59E-06		-9.50E-02		2.25E+00		2.25E-06

		2.78E-01		9.64E+00		9.64E-06		-9.90E-02		2.33E+00		2.33E-06

		2.74E-01		9.61E+00		9.61E-06		-1.03E-01		2.28E+00		2.28E-06

		2.70E-01		9.58E+00		9.58E-06		-1.07E-01		2.36E+00		2.36E-06

		2.66E-01		9.50E+00		9.50E-06		-1.11E-01		2.36E+00		2.36E-06

		2.62E-01		9.51E+00		9.51E-06		-1.15E-01		2.37E+00		2.37E-06

		2.58E-01		9.55E+00		9.55E-06		-1.19E-01		2.46E+00		2.46E-06

		2.54E-01		9.58E+00		9.58E-06		-1.23E-01		2.42E+00		2.42E-06

		2.50E-01		9.56E+00		9.56E-06		-1.27E-01		2.46E+00		2.46E-06

		2.46E-01		9.56E+00		9.56E-06		-1.31E-01		2.46E+00		2.46E-06

		2.42E-01		9.59E+00		9.59E-06		-1.35E-01		2.47E+00		2.47E-06

		2.38E-01		9.59E+00		9.59E-06		-1.39E-01		2.54E+00		2.54E-06

		2.34E-01		9.67E+00		9.67E-06		-1.43E-01		2.53E+00		2.53E-06

		2.30E-01		9.65E+00		9.65E-06		-1.47E-01		2.53E+00		2.53E-06

		2.26E-01		9.71E+00		9.71E-06		-1.51E-01		2.58E+00		2.58E-06

		2.22E-01		9.76E+00		9.76E-06		-1.55E-01		2.59E+00		2.59E-06

		2.18E-01		9.84E+00		9.84E-06		-1.59E-01		2.63E+00		2.63E-06

		2.14E-01		9.88E+00		9.88E-06		-1.63E-01		2.56E+00		2.56E-06

		2.10E-01		9.92E+00		9.92E-06		-1.67E-01		2.66E+00		2.66E-06

		2.06E-01		1.00E+01		1.00E-05		-1.71E-01		2.64E+00		2.64E-06

		2.02E-01		1.01E+01		1.01E-05		-1.75E-01		2.69E+00		2.69E-06

		1.98E-01		1.03E+01		1.03E-05		-1.79E-01		2.68E+00		2.68E-06

		1.94E-01		1.04E+01		1.04E-05		-1.83E-01		2.68E+00		2.68E-06

		1.90E-01		1.05E+01		1.05E-05		-1.87E-01		2.70E+00		2.70E-06

		1.86E-01		1.06E+01		1.06E-05		-1.91E-01		2.75E+00		2.75E-06

		1.82E-01		1.07E+01		1.07E-05		-1.95E-01		2.70E+00		2.70E-06

		1.78E-01		1.09E+01		1.09E-05		-1.99E-01		2.82E+00		2.82E-06

		1.74E-01		1.11E+01		1.11E-05		-2.03E-01		2.75E+00		2.75E-06

		1.70E-01		1.12E+01		1.12E-05		-2.07E-01		2.81E+00		2.81E-06

		1.66E-01		1.13E+01		1.13E-05		-2.11E-01		2.83E+00		2.83E-06

		1.62E-01		1.16E+01		1.16E-05		-2.15E-01		2.84E+00		2.84E-06

		1.58E-01		1.18E+01		1.18E-05		-2.19E-01		2.86E+00		2.86E-06

		1.54E-01		1.19E+01		1.19E-05		-2.23E-01		2.87E+00		2.87E-06

		1.50E-01		1.22E+01		1.22E-05		-2.27E-01		2.94E+00		2.94E-06

		1.46E-01		1.24E+01		1.24E-05		-2.31E-01		2.96E+00		2.96E-06

		1.42E-01		1.27E+01		1.27E-05		-2.35E-01		2.98E+00		2.98E-06

		1.38E-01		1.29E+01		1.29E-05		-2.39E-01		3.02E+00		3.02E-06

		1.34E-01		1.32E+01		1.32E-05		-2.43E-01		3.02E+00		3.02E-06

		1.30E-01		1.34E+01		1.34E-05		-2.47E-01		3.08E+00		3.08E-06

		1.26E-01		1.35E+01		1.35E-05		-2.51E-01		3.10E+00		3.10E-06

		1.22E-01		1.39E+01		1.39E-05		-2.55E-01		3.10E+00		3.10E-06

		1.18E-01		1.42E+01		1.42E-05		-2.59E-01		3.14E+00		3.14E-06

		1.14E-01		1.44E+01		1.44E-05		-2.63E-01		3.13E+00		3.13E-06

		1.10E-01		1.46E+01		1.46E-05		-2.67E-01		3.18E+00		3.18E-06

		1.06E-01		1.49E+01		1.49E-05		-2.71E-01		3.23E+00		3.23E-06

		1.02E-01		1.52E+01		1.52E-05		-2.75E-01		3.26E+00		3.26E-06

		9.80E-02		1.53E+01		1.53E-05		-2.79E-01		3.29E+00		3.29E-06

		9.40E-02		1.57E+01		1.57E-05		-2.83E-01		3.28E+00		3.28E-06

		9.00E-02		1.58E+01		1.58E-05		-2.87E-01		3.37E+00		3.37E-06

		8.60E-02		1.60E+01		1.60E-05		-2.91E-01		3.39E+00		3.39E-06

		8.20E-02		1.63E+01		1.63E-05		-2.95E-01		3.45E+00		3.45E-06

		7.80E-02		1.65E+01		1.65E-05		-2.99E-01		3.48E+00		3.48E-06

		7.40E-02		1.67E+01		1.67E-05		-3.03E-01		3.51E+00		3.51E-06

		7.00E-02		1.68E+01		1.68E-05		-3.07E-01		3.60E+00		3.60E-06

		6.60E-02		1.70E+01		1.70E-05		-3.11E-01		3.66E+00		3.66E-06

		6.20E-02		1.72E+01		1.72E-05		-3.15E-01		3.70E+00		3.70E-06

		5.80E-02		1.74E+01		1.74E-05		-3.19E-01		3.75E+00		3.75E-06

		5.40E-02		1.76E+01		1.76E-05		-3.23E-01		3.76E+00		3.76E-06

		5.00E-02		1.77E+01		1.77E-05		-3.27E-01		3.88E+00		3.88E-06

		4.60E-02		1.78E+01		1.78E-05		-3.31E-01		3.90E+00		3.90E-06

		4.20E-02		1.80E+01		1.80E-05		-3.35E-01		3.97E+00		3.97E-06

		3.80E-02		1.82E+01		1.82E-05		-3.39E-01		4.04E+00		4.04E-06

		3.40E-02		1.82E+01		1.82E-05		-3.43E-01		4.09E+00		4.09E-06

		3.00E-02		1.84E+01		1.84E-05		-3.47E-01		4.19E+00		4.19E-06

		2.60E-02		1.83E+01		1.83E-05		-3.51E-01		4.28E+00		4.28E-06

		2.20E-02		1.85E+01		1.85E-05		-3.55E-01		4.32E+00		4.32E-06

		1.80E-02		1.82E+01		1.82E-05		-3.59E-01		4.39E+00		4.39E-06

		1.40E-02		1.84E+01		1.84E-05		-3.63E-01		4.45E+00		4.45E-06

		1.00E-02		1.86E+01		1.86E-05		-3.67E-01		4.55E+00		4.55E-06

		6.00E-03		1.84E+01		1.84E-05		-3.71E-01		4.65E+00		4.65E-06

		2.00E-03		1.87E+01		1.87E-05		-3.75E-01		4.70E+00		4.70E-06

		-2.00E-03		1.90E+01		1.90E-05		-3.79E-01		4.79E+00		4.79E-06

		-6.00E-03		1.87E+01		1.87E-05		-3.83E-01		4.85E+00		4.85E-06

		-1.00E-02		1.87E+01		1.87E-05		-3.87E-01		4.97E+00		4.97E-06

		-1.40E-02		1.87E+01		1.87E-05		-3.91E-01		5.06E+00		5.06E-06

		-1.80E-02		1.85E+01		1.85E-05		-3.95E-01		5.12E+00		5.12E-06

		-2.20E-02		1.86E+01		1.86E-05		-3.99E-01		5.22E+00		5.22E-06

		-2.60E-02		1.84E+01		1.84E-05		-4.03E-01		5.27E+00		5.27E-06

		-3.00E-02		1.85E+01		1.85E-05		-4.07E-01		5.42E+00		5.42E-06

		-3.40E-02		1.83E+01		1.83E-05		-4.11E-01		5.47E+00		5.47E-06

		-3.80E-02		1.84E+01		1.84E-05		-4.15E-01		5.53E+00		5.53E-06

		-4.20E-02		1.83E+01		1.83E-05		-4.19E-01		5.65E+00		5.65E-06

		-4.60E-02		1.83E+01		1.83E-05		-4.23E-01		5.72E+00		5.72E-06

		-5.00E-02		1.81E+01		1.81E-05		-4.27E-01		5.84E+00		5.84E-06

		-5.40E-02		1.80E+01		1.80E-05		-4.31E-01		5.94E+00		5.94E-06

		-5.80E-02		1.81E+01		1.81E-05		-4.35E-01		6.00E+00		6.00E-06

		-6.20E-02		1.80E+01		1.80E-05		-4.39E-01		6.10E+00		6.10E-06

		-6.60E-02		1.78E+01		1.78E-05		-4.43E-01		6.17E+00		6.17E-06

		-7.00E-02		1.77E+01		1.77E-05		-4.47E-01		6.32E+00		6.32E-06

		-7.40E-02		1.77E+01		1.77E-05		-4.51E-01		6.42E+00		6.42E-06

		-7.80E-02		1.78E+01		1.78E-05		-4.55E-01		6.48E+00		6.48E-06

		-8.20E-02		1.74E+01		1.74E-05		-4.59E-01		6.58E+00		6.58E-06

		-8.60E-02		1.73E+01		1.73E-05		-4.63E-01		6.65E+00		6.65E-06

		-9.00E-02		1.75E+01		1.75E-05		-4.67E-01		6.78E+00		6.78E-06

		-9.40E-02		1.74E+01		1.74E-05		-4.71E-01		6.87E+00		6.87E-06

		-9.80E-02		1.75E+01		1.75E-05		-4.75E-01		6.98E+00		6.98E-06

		-1.02E-01		1.73E+01		1.73E-05		-4.79E-01		7.06E+00		7.06E-06

		-1.06E-01		1.70E+01		1.70E-05		-4.83E-01		7.15E+00		7.15E-06

		-1.10E-01		1.71E+01		1.71E-05		-4.87E-01		7.28E+00		7.28E-06

		-1.14E-01		1.70E+01		1.70E-05		-4.91E-01		7.38E+00		7.38E-06

		-1.18E-01		1.68E+01		1.68E-05		-4.95E-01		7.46E+00		7.46E-06

		-1.22E-01		1.70E+01		1.70E-05		-4.99E-01		7.54E+00		7.54E-06

		-1.26E-01		1.68E+01		1.68E-05		-5.03E-01		7.62E+00		7.62E-06

		-1.30E-01		1.70E+01		1.70E-05		-5.07E-01		7.78E+00		7.78E-06

		-1.34E-01		1.67E+01		1.67E-05		-5.11E-01		7.82E+00		7.82E-06

		-1.38E-01		1.66E+01		1.66E-05		-5.15E-01		7.92E+00		7.92E-06

		-1.42E-01		1.64E+01		1.64E-05		-5.19E-01		7.96E+00		7.96E-06

		-1.46E-01		1.65E+01		1.65E-05		-5.23E-01		8.08E+00		8.08E-06

		-1.50E-01		1.65E+01		1.65E-05		-5.27E-01		8.16E+00		8.16E-06

		-1.54E-01		1.65E+01		1.65E-05		-5.31E-01		8.24E+00		8.24E-06

		-1.58E-01		1.66E+01		1.66E-05		-5.35E-01		8.32E+00		8.32E-06

		-1.62E-01		1.63E+01		1.63E-05		-5.39E-01		8.40E+00		8.40E-06

		-1.66E-01		1.65E+01		1.65E-05		-5.43E-01		8.45E+00		8.45E-06

		-1.70E-01		1.63E+01		1.63E-05		-5.47E-01		8.58E+00		8.58E-06

		-1.74E-01		1.62E+01		1.62E-05		-5.51E-01		8.58E+00		8.58E-06

		-1.78E-01		1.61E+01		1.61E-05		-5.55E-01		8.68E+00		8.68E-06

		-1.82E-01		1.60E+01		1.60E-05		-5.59E-01		8.70E+00		8.70E-06

		-1.86E-01		1.57E+01		1.57E-05		-5.63E-01		8.78E+00		8.78E-06

		-1.90E-01		1.60E+01		1.60E-05		-5.67E-01		8.89E+00		8.89E-06

		-1.94E-01		1.60E+01		1.60E-05		-5.71E-01		8.93E+00		8.93E-06

		-1.98E-01		1.60E+01		1.60E-05		-5.75E-01		8.99E+00		8.99E-06

		-2.02E-01		1.60E+01		1.60E-05		-5.79E-01		9.02E+00		9.02E-06

		-2.06E-01		1.58E+01		1.58E-05		-5.83E-01		9.07E+00		9.07E-06

		-2.10E-01		1.56E+01		1.56E-05		-5.87E-01		9.14E+00		9.14E-06

		-2.14E-01		1.58E+01		1.58E-05		-5.91E-01		9.19E+00		9.19E-06

		-2.18E-01		1.58E+01		1.58E-05		-5.95E-01		9.22E+00		9.22E-06

		-2.22E-01		1.55E+01		1.55E-05		-5.99E-01		9.29E+00		9.29E-06

		-2.26E-01		1.57E+01		1.57E-05		-6.03E-01		9.30E+00		9.30E-06

		-2.30E-01		1.57E+01		1.57E-05		-6.07E-01		9.37E+00		9.37E-06

		-2.34E-01		1.57E+01		1.57E-05		-6.11E-01		9.37E+00		9.37E-06

		-2.38E-01		1.55E+01		1.55E-05		-6.15E-01		9.40E+00		9.40E-06

		-2.42E-01		1.53E+01		1.53E-05		-6.19E-01		9.43E+00		9.43E-06

		-2.46E-01		1.54E+01		1.54E-05		-6.23E-01		9.45E+00		9.45E-06

		-2.50E-01		1.56E+01		1.56E-05		-6.27E-01		9.53E+00		9.53E-06

		-2.54E-01		1.54E+01		1.54E-05		-6.31E-01		9.51E+00		9.51E-06

		-2.58E-01		1.52E+01		1.52E-05		-6.35E-01		9.56E+00		9.56E-06

		-2.62E-01		1.56E+01		1.56E-05		-6.39E-01		9.56E+00		9.56E-06

		-2.66E-01		1.54E+01		1.54E-05		-6.43E-01		9.56E+00		9.56E-06

		-2.70E-01		1.55E+01		1.55E-05		-6.47E-01		9.63E+00		9.63E-06

		-2.74E-01		1.55E+01		1.55E-05		-6.51E-01		9.63E+00		9.63E-06

		-2.78E-01		1.55E+01		1.55E-05		-6.55E-01		9.62E+00		9.62E-06

		-2.82E-01		1.57E+01		1.57E-05		-6.59E-01		9.62E+00		9.62E-06

		-2.86E-01		1.55E+01		1.55E-05		-6.63E-01		9.60E+00		9.60E-06

		-2.90E-01		1.54E+01		1.54E-05		-6.67E-01		9.66E+00		9.66E-06

		-2.94E-01		1.56E+01		1.56E-05		-6.71E-01		9.62E+00		9.62E-06

		-2.98E-01		1.60E+01		1.60E-05		-6.75E-01		9.66E+00		9.66E-06

		-3.02E-01		1.59E+01		1.59E-05		-6.79E-01		9.64E+00		9.64E-06

		-3.06E-01		1.61E+01		1.61E-05		-6.83E-01		9.64E+00		9.64E-06

		-3.10E-01		1.60E+01		1.60E-05		-6.87E-01		9.66E+00		9.66E-06

		-3.14E-01		1.60E+01		1.60E-05		-6.91E-01		9.64E+00		9.64E-06

		-3.18E-01		1.62E+01		1.62E-05		-6.95E-01		9.65E+00		9.65E-06

		-3.22E-01		1.64E+01		1.64E-05		-6.99E-01		9.64E+00		9.64E-06

		-3.26E-01		1.67E+01		1.67E-05		-7.03E-01		9.61E+00		9.61E-06

		-3.30E-01		1.68E+01		1.68E-05		-7.07E-01		9.65E+00		9.65E-06

		-3.34E-01		1.69E+01		1.69E-05		-7.11E-01		9.61E+00		9.61E-06

		-3.38E-01		1.70E+01		1.70E-05		-7.15E-01		9.60E+00		9.60E-06

		-3.42E-01		1.73E+01		1.73E-05		-7.19E-01		9.63E+00		9.63E-06

		-3.46E-01		1.73E+01		1.73E-05		-7.23E-01		9.58E+00		9.58E-06

		-3.50E-01		1.78E+01		1.78E-05		-7.27E-01		9.61E+00		9.61E-06

		-3.54E-01		1.80E+01		1.80E-05		-7.31E-01		9.58E+00		9.58E-06

		-3.58E-01		1.82E+01		1.82E-05		-7.35E-01		9.57E+00		9.57E-06

		-3.62E-01		1.85E+01		1.85E-05		-7.39E-01		9.55E+00		9.55E-06

		-3.66E-01		1.85E+01		1.85E-05		-7.43E-01		9.51E+00		9.51E-06

		-3.70E-01		1.90E+01		1.90E-05		-7.47E-01		9.54E+00		9.54E-06

		-3.74E-01		1.91E+01		1.91E-05		-7.51E-01		9.49E+00		9.49E-06

		-3.78E-01		1.97E+01		1.97E-05		-7.55E-01		9.48E+00		9.48E-06

		-3.82E-01		1.99E+01		1.99E-05		-7.59E-01		9.50E+00		9.50E-06

		-3.86E-01		2.03E+01		2.03E-05		-7.63E-01		9.46E+00		9.46E-06

		-3.90E-01		2.08E+01		2.08E-05		-7.67E-01		9.45E+00		9.45E-06

		-3.94E-01		2.10E+01		2.10E-05		-7.71E-01		9.42E+00		9.42E-06

		-3.98E-01		2.11E+01		2.11E-05		-7.75E-01		9.43E+00		9.43E-06

		-4.02E-01		2.18E+01		2.18E-05		-7.79E-01		9.45E+00		9.45E-06

		-4.06E-01		2.22E+01		2.22E-05		-7.83E-01		9.37E+00		9.37E-06

		-4.10E-01		2.23E+01		2.23E-05		-7.87E-01		9.38E+00		9.38E-06

		-4.14E-01		2.27E+01		2.27E-05		-7.91E-01		9.34E+00		9.34E-06

		-4.18E-01		2.29E+01		2.29E-05		-7.95E-01		9.29E+00		9.29E-06

		-4.22E-01		2.33E+01		2.33E-05		-7.99E-01		9.36E+00		9.36E-06

		-4.26E-01		2.36E+01		2.36E-05		-8.03E-01		9.26E+00		9.26E-06

		-4.30E-01		2.40E+01		2.40E-05		-8.07E-01		9.33E+00		9.33E-06

		-4.34E-01		2.44E+01		2.44E-05		-8.11E-01		9.25E+00		9.25E-06

		-4.38E-01		2.50E+01		2.50E-05		-8.15E-01		9.27E+00		9.27E-06

		-4.42E-01		2.50E+01		2.50E-05		-8.19E-01		9.26E+00		9.26E-06

		-4.46E-01		2.52E+01		2.52E-05		-8.23E-01		9.19E+00		9.19E-06

		-4.50E-01		2.54E+01		2.54E-05		-8.27E-01		9.20E+00		9.20E-06

		-4.54E-01		2.56E+01		2.56E-05		-8.31E-01		9.16E+00		9.16E-06

		-4.58E-01		2.61E+01		2.61E-05		-8.35E-01		9.14E+00		9.14E-06

		-4.62E-01		2.60E+01		2.60E-05		-8.39E-01		9.19E+00		9.19E-06

		-4.66E-01		2.64E+01		2.64E-05		-8.43E-01		9.08E+00		9.08E-06

		-4.70E-01		2.65E+01		2.65E-05		-8.47E-01		9.14E+00		9.14E-06

		-4.74E-01		2.68E+01		2.68E-05		-8.51E-01		9.08E+00		9.08E-06

		-4.78E-01		2.68E+01		2.68E-05		-8.55E-01		9.11E+00		9.11E-06

		-4.82E-01		2.69E+01		2.69E-05		-8.59E-01		9.10E+00		9.10E-06

		-4.86E-01		2.72E+01		2.72E-05		-8.63E-01		9.04E+00		9.04E-06

		-4.90E-01		2.73E+01		2.73E-05		-8.67E-01		9.05E+00		9.05E-06

		-4.94E-01		2.72E+01		2.72E-05		-8.71E-01		9.07E+00		9.07E-06

		-4.98E-01		2.72E+01		2.72E-05		-8.75E-01		9.03E+00		9.03E-06

		-5.02E-01		2.74E+01		2.74E-05		-8.79E-01		9.07E+00		9.07E-06

		-5.06E-01		2.74E+01		2.74E-05		-8.83E-01		9.00E+00		9.00E-06

		-5.10E-01		2.76E+01		2.76E-05		-8.87E-01		9.07E+00		9.07E-06

		-5.14E-01		2.75E+01		2.75E-05		-8.91E-01		9.00E+00		9.00E-06

		-5.18E-01		2.75E+01		2.75E-05		-8.95E-01		9.04E+00		9.04E-06

		-5.22E-01		2.72E+01		2.72E-05		-8.99E-01		9.07E+00		9.07E-06

		-5.26E-01		2.74E+01		2.74E-05		-9.03E-01		8.99E+00		8.99E-06

		-5.30E-01		2.75E+01		2.75E-05		-9.07E-01		9.08E+00		9.08E-06

		-5.34E-01		2.75E+01		2.75E-05		-9.11E-01		9.01E+00		9.01E-06

		-5.38E-01		2.77E+01		2.77E-05		-9.15E-01		9.03E+00		9.03E-06

		-5.42E-01		2.75E+01		2.75E-05		-9.19E-01		9.02E+00		9.02E-06

		-5.46E-01		2.75E+01		2.75E-05		-9.23E-01		8.98E+00		8.98E-06

		-5.50E-01		2.70E+01		2.70E-05		-9.27E-01		9.04E+00		9.04E-06

		-5.54E-01		2.74E+01		2.74E-05		-9.31E-01		8.98E+00		8.98E-06

		-5.58E-01		2.71E+01		2.71E-05		-9.35E-01		9.02E+00		9.02E-06

		-5.62E-01		2.71E+01		2.71E-05		-9.39E-01		9.02E+00		9.02E-06

		-5.66E-01		2.72E+01		2.72E-05		-9.43E-01		8.98E+00		8.98E-06

		-5.70E-01		2.67E+01		2.67E-05		-9.47E-01		9.01E+00		9.01E-06

		-5.74E-01		2.70E+01		2.70E-05		-9.51E-01		9.00E+00		9.00E-06

		-5.78E-01		2.68E+01		2.68E-05		-9.55E-01		9.03E+00		9.03E-06

		-5.82E-01		2.69E+01		2.69E-05		-9.59E-01		9.04E+00		9.04E-06

		-5.86E-01		2.66E+01		2.66E-05		-9.63E-01		9.00E+00		9.00E-06

		-5.90E-01		2.65E+01		2.65E-05		-9.67E-01		9.06E+00		9.06E-06

		-5.94E-01		2.65E+01		2.65E-05		-9.71E-01		9.06E+00		9.06E-06

		-5.98E-01		2.63E+01		2.63E-05		-9.75E-01		9.10E+00		9.10E-06

		-6.02E-01		2.62E+01		2.62E-05		-9.79E-01		9.10E+00		9.10E-06

		-6.06E-01		2.62E+01		2.62E-05		-9.83E-01		9.10E+00		9.10E-06

		-6.10E-01		2.63E+01		2.63E-05		-9.87E-01		9.16E+00		9.16E-06

		-6.14E-01		2.59E+01		2.59E-05		-9.91E-01		9.15E+00		9.15E-06

		-6.18E-01		2.60E+01		2.60E-05		-9.95E-01		9.17E+00		9.17E-06

		-6.22E-01		2.56E+01		2.56E-05		-9.99E-01		9.22E+00		9.22E-06

		-6.26E-01		2.58E+01		2.58E-05		-1.00E+00		9.22E+00		9.22E-06

		-6.30E-01		2.56E+01		2.56E-05		-1.01E+00		9.27E+00		9.27E-06

		-6.34E-01		2.57E+01		2.57E-05		-1.01E+00		9.30E+00		9.30E-06

		-6.38E-01		2.54E+01		2.54E-05		-1.02E+00		9.33E+00		9.33E-06

		-6.42E-01		2.53E+01		2.53E-05		-1.02E+00		9.37E+00		9.37E-06

		-6.46E-01		2.52E+01		2.52E-05		-1.02E+00		9.38E+00		9.38E-06

		-6.50E-01		2.48E+01		2.48E-05		-1.03E+00		9.49E+00		9.49E-06

		-6.54E-01		2.50E+01		2.50E-05		-1.03E+00		9.45E+00		9.45E-06

		-6.58E-01		2.48E+01		2.48E-05		-1.04E+00		9.51E+00		9.51E-06

		-6.62E-01		2.50E+01		2.50E-05		-1.04E+00		9.57E+00		9.57E-06

		-6.66E-01		2.46E+01		2.46E-05		-1.04E+00		9.58E+00		9.58E-06

		-6.70E-01		2.48E+01		2.48E-05		-1.05E+00		9.66E+00		9.66E-06

		-6.74E-01		2.42E+01		2.42E-05		-1.05E+00		9.68E+00		9.68E-06

		-6.78E-01		2.43E+01		2.43E-05		-1.06E+00		9.77E+00		9.77E-06

		-6.82E-01		2.43E+01		2.43E-05		-1.06E+00		9.77E+00		9.77E-06

		-6.86E-01		2.40E+01		2.40E-05		-1.06E+00		9.85E+00		9.85E-06

		-6.90E-01		2.42E+01		2.42E-05		-1.07E+00		9.94E+00		9.94E-06

		-6.94E-01		2.40E+01		2.40E-05		-1.07E+00		9.95E+00		9.95E-06

		-6.98E-01		2.39E+01		2.39E-05		-1.08E+00		1.00E+01		1.00E-05

		-7.02E-01		2.37E+01		2.37E-05		-1.08E+00		1.01E+01		1.01E-05

		-7.06E-01		2.39E+01		2.39E-05		-1.08E+00		1.02E+01		1.02E-05

		-7.10E-01		2.36E+01		2.36E-05		-1.09E+00		1.02E+01		1.02E-05

		-7.14E-01		2.37E+01		2.37E-05		-1.09E+00		1.03E+01		1.03E-05

		-7.18E-01		2.36E+01		2.36E-05		-1.10E+00		1.04E+01		1.04E-05

		-7.22E-01		2.34E+01		2.34E-05		-1.10E+00		1.04E+01		1.04E-05

		-7.26E-01		2.31E+01		2.31E-05		-1.10E+00		1.05E+01		1.05E-05

		-7.30E-01		2.32E+01		2.32E-05		-1.11E+00		1.06E+01		1.06E-05

		-7.34E-01		2.33E+01		2.33E-05		-1.11E+00		1.06E+01		1.06E-05

		-7.38E-01		2.31E+01		2.31E-05		-1.12E+00		1.07E+01		1.07E-05

		-7.42E-01		2.32E+01		2.32E-05		-1.12E+00		1.08E+01		1.08E-05

		-7.46E-01		2.31E+01		2.31E-05		-1.12E+00		1.09E+01		1.09E-05

		-7.50E-01		2.32E+01		2.32E-05		-1.13E+00		1.10E+01		1.10E-05

		-7.54E-01		2.26E+01		2.26E-05		-1.13E+00		1.10E+01		1.10E-05

		-7.58E-01		2.30E+01		2.30E-05		-1.14E+00		1.11E+01		1.11E-05

		-7.62E-01		2.29E+01		2.29E-05		-1.14E+00		1.12E+01		1.12E-05

		-7.66E-01		2.26E+01		2.26E-05		-1.14E+00		1.12E+01		1.12E-05

		-7.70E-01		2.27E+01		2.27E-05		-1.15E+00		1.14E+01		1.14E-05

		-7.74E-01		2.27E+01		2.27E-05		-1.15E+00		1.14E+01		1.14E-05

		-7.78E-01		2.26E+01		2.26E-05		-1.16E+00		1.16E+01		1.16E-05

		-7.82E-01		2.24E+01		2.24E-05		-1.16E+00		1.16E+01		1.16E-05

		-7.86E-01		2.24E+01		2.24E-05		-1.16E+00		1.17E+01		1.17E-05

		-7.90E-01		2.25E+01		2.25E-05		-1.17E+00		1.18E+01		1.18E-05

		-7.94E-01		2.24E+01		2.24E-05		-1.17E+00		1.19E+01		1.19E-05

		-7.98E-01		2.24E+01		2.24E-05		-1.18E+00		1.20E+01		1.20E-05

		-8.02E-01		2.23E+01		2.23E-05		-1.18E+00		1.21E+01		1.21E-05

		-8.06E-01		2.23E+01		2.23E-05		-1.18E+00		1.21E+01		1.21E-05

		-8.10E-01		2.22E+01		2.22E-05		-1.19E+00		1.22E+01		1.22E-05

		-8.14E-01		2.22E+01		2.22E-05		-1.19E+00		1.23E+01		1.23E-05

		-8.18E-01		2.21E+01		2.21E-05		-1.20E+00		1.24E+01		1.24E-05

		-8.22E-01		2.21E+01		2.21E-05		-1.20E+00		1.25E+01		1.25E-05

		-8.26E-01		2.21E+01		2.21E-05		-1.20E+00		1.26E+01		1.26E-05

		-8.30E-01		2.20E+01		2.20E-05		-1.21E+00		1.27E+01		1.27E-05

		-8.34E-01		2.18E+01		2.18E-05		-1.21E+00		1.27E+01		1.27E-05

		-8.38E-01		2.20E+01		2.20E-05		-1.22E+00		1.28E+01		1.28E-05

		-8.42E-01		2.17E+01		2.17E-05		-1.22E+00		1.29E+01		1.29E-05

		-8.46E-01		2.18E+01		2.18E-05		-1.22E+00		1.30E+01		1.30E-05

		-8.50E-01		2.18E+01		2.18E-05		-1.23E+00		1.31E+01		1.31E-05

		-8.54E-01		2.18E+01		2.18E-05		-1.23E+00		1.31E+01		1.31E-05

		-8.58E-01		2.17E+01		2.17E-05		-1.24E+00		1.32E+01		1.32E-05

		-8.62E-01		2.16E+01		2.16E-05		-1.24E+00		1.33E+01		1.33E-05

		-8.66E-01		2.18E+01		2.18E-05		-1.24E+00		1.34E+01		1.34E-05

		-8.70E-01		2.15E+01		2.15E-05		-1.25E+00		1.35E+01		1.35E-05

		-8.74E-01		2.17E+01		2.17E-05		-1.25E+00		1.35E+01		1.35E-05

		-8.78E-01		2.14E+01		2.14E-05		-1.26E+00		1.36E+01		1.36E-05

		-8.82E-01		2.15E+01		2.15E-05		-1.26E+00		1.37E+01		1.37E-05

		-8.86E-01		2.13E+01		2.13E-05		-1.26E+00		1.37E+01		1.37E-05

		-8.90E-01		2.14E+01		2.14E-05		-1.27E+00		1.38E+01		1.38E-05

		-8.94E-01		2.15E+01		2.15E-05		-1.27E+00		1.38E+01		1.38E-05

		-8.98E-01		2.14E+01		2.14E-05		-1.28E+00		1.39E+01		1.39E-05

		-9.02E-01		2.16E+01		2.16E-05		-1.28E+00		1.40E+01		1.40E-05

		-9.06E-01		2.11E+01		2.11E-05		-1.28E+00		1.40E+01		1.40E-05

		-9.10E-01		2.14E+01		2.14E-05		-1.29E+00		1.41E+01		1.41E-05

		-9.14E-01		2.14E+01		2.14E-05		-1.29E+00		1.41E+01		1.41E-05

		-9.18E-01		2.12E+01		2.12E-05		-1.30E+00		1.42E+01		1.42E-05

		-9.22E-01		2.12E+01		2.12E-05		-1.30E+00		1.43E+01		1.43E-05

		-9.26E-01		2.13E+01		2.13E-05		-1.30E+00		1.43E+01		1.43E-05

		-9.30E-01		2.10E+01		2.10E-05		-1.31E+00		1.44E+01		1.44E-05

		-9.34E-01		2.10E+01		2.10E-05		-1.31E+00		1.44E+01		1.44E-05

		-9.38E-01		2.11E+01		2.11E-05		-1.32E+00		1.45E+01		1.45E-05

		-9.42E-01		2.11E+01		2.11E-05		-1.32E+00		1.45E+01		1.45E-05

		-9.46E-01		2.13E+01		2.13E-05		-1.32E+00		1.45E+01		1.45E-05

		-9.50E-01		2.11E+01		2.11E-05		-1.33E+00		1.46E+01		1.46E-05

		-9.54E-01		2.11E+01		2.11E-05		-1.33E+00		1.46E+01		1.46E-05

		-9.58E-01		2.06E+01		2.06E-05		-1.34E+00		1.47E+01		1.47E-05

		-9.62E-01		2.08E+01		2.08E-05		-1.34E+00		1.47E+01		1.47E-05

		-9.66E-01		2.07E+01		2.07E-05		-1.34E+00		1.48E+01		1.48E-05

		-9.70E-01		2.08E+01		2.08E-05		-1.35E+00		1.48E+01		1.48E-05

		-9.74E-01		2.07E+01		2.07E-05		-1.35E+00		1.48E+01		1.48E-05

		-9.78E-01		2.08E+01		2.08E-05		-1.36E+00		1.49E+01		1.49E-05

		-9.82E-01		2.07E+01		2.07E-05		-1.36E+00		1.49E+01		1.49E-05

		-9.86E-01		2.05E+01		2.05E-05		-1.36E+00		1.49E+01		1.49E-05

		-9.90E-01		2.10E+01		2.10E-05		-1.37E+00		1.50E+01		1.50E-05

		-9.94E-01		2.08E+01		2.08E-05		-1.37E+00		1.50E+01		1.50E-05

		-9.98E-01		2.08E+01		2.08E-05		-1.38E+00		1.51E+01		1.51E-05

		-1.00E+00		2.08E+01		2.08E-05		-1.38E+00		1.51E+01		1.51E-05

		-1.01E+00		2.07E+01		2.07E-05		-1.38E+00		1.51E+01		1.51E-05

		-1.01E+00		2.07E+01		2.07E-05		-1.39E+00		1.52E+01		1.52E-05

		-1.01E+00		2.04E+01		2.04E-05		-1.39E+00		1.51E+01		1.51E-05

		-1.02E+00		2.08E+01		2.08E-05		-1.40E+00		1.52E+01		1.52E-05

		-1.02E+00		2.07E+01		2.07E-05		-1.40E+00		1.52E+01		1.52E-05

		-1.03E+00		2.06E+01		2.06E-05		-1.40E+00		1.52E+01		1.52E-05

		-1.03E+00		2.03E+01		2.03E-05		-1.41E+00		1.53E+01		1.53E-05

		-1.03E+00		2.06E+01		2.06E-05		-1.41E+00		1.53E+01		1.53E-05

		-1.04E+00		2.04E+01		2.04E-05		-1.42E+00		1.53E+01		1.53E-05

		-1.04E+00		2.04E+01		2.04E-05		-1.42E+00		1.53E+01		1.53E-05

		-1.05E+00		2.05E+01		2.05E-05		-1.42E+00		1.53E+01		1.53E-05

		-1.05E+00		2.03E+01		2.03E-05		-1.43E+00		1.54E+01		1.54E-05

		-1.05E+00		2.03E+01		2.03E-05		-1.43E+00		1.54E+01		1.54E-05

		-1.06E+00		2.03E+01		2.03E-05		-1.44E+00		1.54E+01		1.54E-05

		-1.06E+00		2.04E+01		2.04E-05		-1.44E+00		1.54E+01		1.54E-05

		-1.07E+00		2.03E+01		2.03E-05		-1.44E+00		1.54E+01		1.54E-05

		-1.07E+00		2.04E+01		2.04E-05		-1.45E+00		1.55E+01		1.55E-05

		-1.07E+00		2.02E+01		2.02E-05		-1.45E+00		1.54E+01		1.54E-05

		-1.08E+00		2.03E+01		2.03E-05		-1.46E+00		1.55E+01		1.55E-05

		-1.08E+00		2.02E+01		2.02E-05		-1.46E+00		1.55E+01		1.55E-05

		-1.09E+00		2.02E+01		2.02E-05		-1.46E+00		1.55E+01		1.55E-05

		-1.09E+00		2.02E+01		2.02E-05		-1.47E+00		1.56E+01		1.56E-05

		-1.09E+00		2.02E+01		2.02E-05		-1.47E+00		1.56E+01		1.56E-05

		-1.10E+00		2.05E+01		2.05E-05		-1.48E+00		1.56E+01		1.56E-05

		-1.10E+00		2.02E+01		2.02E-05		-1.48E+00		1.56E+01		1.56E-05

		-1.11E+00		2.05E+01		2.05E-05		-1.48E+00		1.56E+01		1.56E-05

		-1.11E+00		2.03E+01		2.03E-05		-1.49E+00		1.57E+01		1.57E-05

		-1.11E+00		2.03E+01		2.03E-05		-1.49E+00		1.57E+01		1.57E-05

		-1.12E+00		2.02E+01		2.02E-05		-1.50E+00		1.58E+01		1.58E-05

		-1.12E+00		2.02E+01		2.02E-05		-1.50E+00		1.58E+01		1.58E-05

		-1.13E+00		2.04E+01		2.04E-05		-1.50E+00		1.58E+01		1.58E-05

		-1.13E+00		2.01E+01		2.01E-05		-1.51E+00		1.58E+01		1.58E-05

		-1.13E+00		2.04E+01		2.04E-05		-1.51E+00		1.59E+01		1.59E-05

		-1.14E+00		2.02E+01		2.02E-05		-1.52E+00		1.59E+01		1.59E-05

		-1.14E+00		2.02E+01		2.02E-05		-1.52E+00		1.60E+01		1.60E-05

		-1.15E+00		2.01E+01		2.01E-05		-1.52E+00		1.60E+01		1.60E-05

		-1.15E+00		2.01E+01		2.01E-05		-1.53E+00		1.61E+01		1.61E-05

		-1.15E+00		2.02E+01		2.02E-05		-1.53E+00		1.60E+01		1.60E-05

		-1.16E+00		2.02E+01		2.02E-05		-1.54E+00		1.62E+01		1.62E-05

		-1.16E+00		1.99E+01		1.99E-05		-1.54E+00		1.62E+01		1.62E-05

		-1.17E+00		2.03E+01		2.03E-05		-1.54E+00		1.62E+01		1.62E-05

		-1.17E+00		2.01E+01		2.01E-05		-1.55E+00		1.63E+01		1.63E-05

		-1.17E+00		2.00E+01		2.00E-05		-1.55E+00		1.63E+01		1.63E-05

		-1.18E+00		2.03E+01		2.03E-05		-1.56E+00		1.65E+01		1.65E-05

		-1.18E+00		2.02E+01		2.02E-05		-1.56E+00		1.65E+01		1.65E-05

		-1.19E+00		2.03E+01		2.03E-05		-1.56E+00		1.66E+01		1.66E-05

		-1.19E+00		1.98E+01		1.98E-05		-1.57E+00		1.67E+01		1.67E-05

		-1.19E+00		2.02E+01		2.02E-05		-1.57E+00		1.67E+01		1.67E-05

		-1.20E+00		2.01E+01		2.01E-05		-1.58E+00		1.68E+01		1.68E-05

		-1.20E+00		2.02E+01		2.02E-05		-1.58E+00		1.69E+01		1.69E-05

		-1.21E+00		2.02E+01		2.02E-05		-1.58E+00		1.69E+01		1.69E-05

		-1.21E+00		2.03E+01		2.03E-05		-1.59E+00		1.71E+01		1.71E-05

		-1.21E+00		2.04E+01		2.04E-05		-1.59E+00		1.71E+01		1.71E-05

		-1.22E+00		2.02E+01		2.02E-05		-1.60E+00		1.72E+01		1.72E-05

		-1.22E+00		2.06E+01		2.06E-05		-1.60E+00		1.74E+01		1.74E-05

		-1.23E+00		2.03E+01		2.03E-05		-1.60E+00		1.74E+01		1.74E-05

		-1.23E+00		2.06E+01		2.06E-05		-1.61E+00		1.76E+01		1.76E-05

		-1.23E+00		2.04E+01		2.04E-05		-1.61E+00		1.77E+01		1.77E-05

		-1.24E+00		2.06E+01		2.06E-05		-1.62E+00		1.78E+01		1.78E-05

		-1.24E+00		2.07E+01		2.07E-05		-1.62E+00		1.79E+01		1.79E-05

		-1.25E+00		2.05E+01		2.05E-05		-1.62E+00		1.81E+01		1.81E-05

		-1.25E+00		2.08E+01		2.08E-05		-1.63E+00		1.82E+01		1.82E-05

		-1.25E+00		2.07E+01		2.07E-05		-1.63E+00		1.83E+01		1.83E-05

		-1.26E+00		2.09E+01		2.09E-05		-1.64E+00		1.85E+01		1.85E-05

		-1.26E+00		2.07E+01		2.07E-05		-1.64E+00		1.87E+01		1.87E-05

		-1.27E+00		2.11E+01		2.11E-05		-1.64E+00		1.87E+01		1.87E-05

		-1.27E+00		2.09E+01		2.09E-05		-1.65E+00		1.91E+01		1.91E-05

		-1.27E+00		2.10E+01		2.10E-05		-1.65E+00		1.92E+01		1.92E-05

		-1.28E+00		2.11E+01		2.11E-05		-1.66E+00		1.94E+01		1.94E-05

		-1.28E+00		2.11E+01		2.11E-05		-1.66E+00		1.95E+01		1.95E-05

		-1.29E+00		2.14E+01		2.14E-05		-1.66E+00		1.98E+01		1.98E-05

		-1.29E+00		2.13E+01		2.13E-05		-1.67E+00		1.99E+01		1.99E-05

		-1.29E+00		2.14E+01		2.14E-05		-1.67E+00		2.01E+01		2.01E-05

		-1.30E+00		2.15E+01		2.15E-05		-1.68E+00		2.04E+01		2.04E-05

		-1.30E+00		2.17E+01		2.17E-05		-1.68E+00		2.06E+01		2.06E-05

		-1.31E+00		2.15E+01		2.15E-05		-1.68E+00		2.09E+01		2.09E-05

		-1.31E+00		2.20E+01		2.20E-05		-1.69E+00		2.12E+01		2.12E-05

		-1.31E+00		2.17E+01		2.17E-05		-1.69E+00		2.13E+01		2.13E-05

		-1.32E+00		2.18E+01		2.18E-05		-1.70E+00		2.17E+01		2.17E-05

		-1.32E+00		2.20E+01		2.20E-05		-1.70E+00		2.19E+01		2.19E-05

		-1.33E+00		2.18E+01		2.18E-05		-1.70E+00		2.24E+01		2.24E-05

		-1.33E+00		2.22E+01		2.22E-05		-1.71E+00		2.26E+01		2.26E-05

		-1.33E+00		2.22E+01		2.22E-05		-1.71E+00		2.29E+01		2.29E-05

		-1.34E+00		2.25E+01		2.25E-05		-1.72E+00		2.32E+01		2.32E-05

		-1.34E+00		2.24E+01		2.24E-05		-1.72E+00		2.35E+01		2.35E-05

		-1.35E+00		2.26E+01		2.26E-05		-1.72E+00		2.38E+01		2.38E-05

		-1.35E+00		2.23E+01		2.23E-05		-1.73E+00		2.43E+01		2.43E-05

		-1.35E+00		2.28E+01		2.28E-05		-1.73E+00		2.46E+01		2.46E-05

		-1.36E+00		2.25E+01		2.25E-05		-1.74E+00		2.48E+01		2.48E-05

		-1.36E+00		2.29E+01		2.29E-05		-1.74E+00		2.53E+01		2.53E-05

		-1.37E+00		2.32E+01		2.32E-05		-1.74E+00		2.56E+01		2.56E-05

		-1.37E+00		2.30E+01		2.30E-05		-1.75E+00		2.60E+01		2.60E-05

		-1.37E+00		2.31E+01		2.31E-05		-1.75E+00		2.64E+01		2.64E-05

		-1.38E+00		2.33E+01		2.33E-05		-1.76E+00		2.70E+01		2.70E-05

		-1.38E+00		2.34E+01		2.34E-05		-1.76E+00		2.73E+01		2.73E-05

		-1.39E+00		2.35E+01		2.35E-05		-1.76E+00		2.77E+01		2.77E-05

		-1.39E+00		2.37E+01		2.37E-05		-1.77E+00		2.84E+01		2.84E-05

		-1.39E+00		2.33E+01		2.33E-05		-1.77E+00		2.86E+01		2.86E-05

		-1.40E+00		2.38E+01		2.38E-05		-1.78E+00		2.93E+01		2.93E-05

		-1.40E+00		2.39E+01		2.39E-05		-1.78E+00		2.95E+01		2.95E-05

		-1.41E+00		2.40E+01		2.40E-05		-1.78E+00		3.02E+01		3.02E-05

		-1.41E+00		2.43E+01		2.43E-05		-1.79E+00		3.06E+01		3.06E-05

		-1.41E+00		2.43E+01		2.43E-05		-1.79E+00		3.11E+01		3.11E-05

		-1.42E+00		2.46E+01		2.46E-05		-1.80E+00		3.17E+01		3.17E-05

		-1.42E+00		2.44E+01		2.44E-05		-1.80E+00		3.23E+01		3.23E-05

		-1.43E+00		2.49E+01		2.49E-05		-1.80E+00		3.28E+01		3.28E-05

		-1.43E+00		2.50E+01		2.50E-05		-1.81E+00		3.34E+01		3.34E-05

		-1.43E+00		2.51E+01		2.51E-05		-1.81E+00		3.39E+01		3.39E-05

		-1.44E+00		2.52E+01		2.52E-05		-1.82E+00		3.45E+01		3.45E-05

		-1.44E+00		2.54E+01		2.54E-05		-1.82E+00		3.51E+01		3.51E-05

		-1.45E+00		2.58E+01		2.58E-05		-1.82E+00		3.58E+01		3.58E-05

		-1.45E+00		2.57E+01		2.57E-05		-1.83E+00		3.62E+01		3.62E-05

		-1.45E+00		2.60E+01		2.60E-05		-1.83E+00		3.68E+01		3.68E-05

		-1.46E+00		2.61E+01		2.61E-05		-1.84E+00		3.75E+01		3.75E-05

		-1.46E+00		2.65E+01		2.65E-05		-1.84E+00		3.82E+01		3.82E-05

		-1.47E+00		2.66E+01		2.66E-05		-1.84E+00		3.90E+01		3.90E-05

		-1.47E+00		2.68E+01		2.68E-05		-1.85E+00		3.95E+01		3.95E-05

		-1.47E+00		2.69E+01		2.69E-05		-1.85E+00		4.01E+01		4.01E-05

		-1.48E+00		2.73E+01		2.73E-05		-1.86E+00		4.10E+01		4.10E-05

		-1.48E+00		2.74E+01		2.74E-05		-1.86E+00		4.16E+01		4.16E-05

		-1.49E+00		2.74E+01		2.74E-05		-1.86E+00		4.24E+01		4.24E-05

		-1.49E+00		2.78E+01		2.78E-05		-1.87E+00		4.30E+01		4.30E-05

		-1.49E+00		2.75E+01		2.75E-05		-1.87E+00		4.39E+01		4.39E-05

		-1.50E+00		2.82E+01		2.82E-05		-1.88E+00		4.47E+01		4.47E-05

		-1.50E+00		2.82E+01		2.82E-05		-1.88E+00		4.55E+01		4.55E-05

		-1.51E+00		2.88E+01		2.88E-05		-1.88E+00		4.64E+01		4.64E-05

		-1.51E+00		2.88E+01		2.88E-05		-1.89E+00		4.71E+01		4.71E-05

		-1.51E+00		2.91E+01		2.91E-05		-1.89E+00		4.82E+01		4.82E-05

		-1.52E+00		2.93E+01		2.93E-05		-1.90E+00		4.88E+01		4.88E-05

		-1.52E+00		2.95E+01		2.95E-05		-1.90E+00		4.98E+01		4.98E-05

		-1.53E+00		2.99E+01		2.99E-05		-1.90E+00		5.06E+01		5.06E-05

		-1.53E+00		3.02E+01		3.02E-05		-1.91E+00		5.16E+01		5.16E-05

		-1.53E+00		3.03E+01		3.03E-05		-1.91E+00		5.25E+01		5.25E-05

		-1.54E+00		3.06E+01		3.06E-05		-1.92E+00		5.35E+01		5.35E-05

		-1.54E+00		3.12E+01		3.12E-05		-1.92E+00		5.44E+01		5.44E-05

		-1.55E+00		3.11E+01		3.11E-05		-1.92E+00		5.56E+01		5.56E-05

		-1.55E+00		3.17E+01		3.17E-05		-1.93E+00		5.64E+01		5.64E-05

		-1.55E+00		3.18E+01		3.18E-05		-1.93E+00		5.75E+01		5.75E-05

		-1.56E+00		3.23E+01		3.23E-05		-1.94E+00		5.89E+01		5.89E-05

		-1.56E+00		3.25E+01		3.25E-05		-1.94E+00		5.95E+01		5.95E-05

		-1.57E+00		3.29E+01		3.29E-05		-1.94E+00		6.09E+01		6.09E-05

		-1.57E+00		3.35E+01		3.35E-05		-1.95E+00		6.21E+01		6.21E-05

		-1.57E+00		3.35E+01		3.35E-05		-1.95E+00		6.31E+01		6.31E-05

		-1.58E+00		3.39E+01		3.39E-05		-1.96E+00		6.42E+01		6.42E-05

		-1.58E+00		3.43E+01		3.43E-05		-1.96E+00		6.53E+01		6.53E-05

		-1.59E+00		3.49E+01		3.49E-05		-1.96E+00		6.66E+01		6.66E-05

		-1.59E+00		3.51E+01		3.51E-05		-1.97E+00		6.79E+01		6.79E-05

		-1.59E+00		3.57E+01		3.57E-05		-1.97E+00		6.92E+01		6.92E-05

		-1.60E+00		3.59E+01		3.59E-05		-1.98E+00		7.03E+01		7.03E-05

		-1.60E+00		3.65E+01		3.65E-05		-1.98E+00		7.19E+01		7.19E-05

		-1.61E+00		3.70E+01		3.70E-05		-1.98E+00		7.32E+01		7.32E-05

		-1.61E+00		3.73E+01		3.73E-05		-1.99E+00		7.44E+01		7.44E-05

		-1.61E+00		3.78E+01		3.78E-05		-1.99E+00		7.59E+01		7.59E-05

		-1.62E+00		3.82E+01		3.82E-05		-2.00E+00		7.74E+01		7.74E-05

		-1.62E+00		3.88E+01		3.88E-05		-2.00E+00		7.90E+01		7.90E-05

		-1.63E+00		3.90E+01		3.90E-05		-2.00E+00		7.68E+01		7.68E-05

		-1.63E+00		3.97E+01		3.97E-05		-1.99E+00		7.49E+01		7.49E-05

		-1.63E+00		4.03E+01		4.03E-05		-1.99E+00		7.29E+01		7.29E-05

		-1.64E+00		4.08E+01		4.08E-05		-1.98E+00		7.10E+01		7.10E-05

		-1.64E+00		4.14E+01		4.14E-05		-1.98E+00		6.93E+01		6.93E-05

		-1.65E+00		4.19E+01		4.19E-05		-1.98E+00		6.78E+01		6.78E-05

		-1.65E+00		4.26E+01		4.26E-05		-1.97E+00		6.58E+01		6.58E-05

		-1.65E+00		4.30E+01		4.30E-05		-1.97E+00		6.43E+01		6.43E-05

		-1.66E+00		4.36E+01		4.36E-05		-1.96E+00		6.28E+01		6.28E-05

		-1.66E+00		4.44E+01		4.44E-05		-1.96E+00		6.12E+01		6.12E-05

		-1.67E+00		4.49E+01		4.49E-05		-1.96E+00		5.99E+01		5.99E-05

		-1.67E+00		4.55E+01		4.55E-05		-1.95E+00		5.84E+01		5.84E-05

		-1.67E+00		4.64E+01		4.64E-05		-1.95E+00		5.71E+01		5.71E-05

		-1.68E+00		4.68E+01		4.68E-05		-1.94E+00		5.57E+01		5.57E-05

		-1.68E+00		4.77E+01		4.77E-05		-1.94E+00		5.44E+01		5.44E-05

		-1.69E+00		4.84E+01		4.84E-05		-1.94E+00		5.32E+01		5.32E-05

		-1.69E+00		4.92E+01		4.92E-05		-1.93E+00		5.20E+01		5.20E-05

		-1.69E+00		4.98E+01		4.98E-05		-1.93E+00		5.07E+01		5.07E-05

		-1.70E+00		5.04E+01		5.04E-05		-1.92E+00		4.95E+01		4.95E-05

		-1.70E+00		5.14E+01		5.14E-05		-1.92E+00		4.83E+01		4.83E-05

		-1.71E+00		5.21E+01		5.21E-05		-1.92E+00		4.74E+01		4.74E-05

		-1.71E+00		5.29E+01		5.29E-05		-1.91E+00		4.63E+01		4.63E-05

		-1.71E+00		5.34E+01		5.34E-05		-1.91E+00		4.51E+01		4.51E-05

		-1.72E+00		5.46E+01		5.46E-05		-1.90E+00		4.43E+01		4.43E-05

		-1.72E+00		5.52E+01		5.52E-05		-1.90E+00		4.31E+01		4.31E-05

		-1.73E+00		5.58E+01		5.58E-05		-1.90E+00		4.23E+01		4.23E-05

		-1.73E+00		5.71E+01		5.71E-05		-1.89E+00		4.12E+01		4.12E-05

		-1.73E+00		5.77E+01		5.77E-05		-1.89E+00		4.04E+01		4.04E-05

		-1.74E+00		5.87E+01		5.87E-05		-1.88E+00		3.94E+01		3.94E-05

		-1.74E+00		5.94E+01		5.94E-05		-1.88E+00		3.84E+01		3.84E-05

		-1.75E+00		6.08E+01		6.08E-05		-1.88E+00		3.75E+01		3.75E-05

		-1.75E+00		6.15E+01		6.15E-05		-1.87E+00		3.66E+01		3.66E-05

		-1.75E+00		6.26E+01		6.26E-05		-1.87E+00		3.59E+01		3.59E-05

		-1.76E+00		6.37E+01		6.37E-05		-1.86E+00		3.52E+01		3.52E-05

		-1.76E+00		6.48E+01		6.48E-05		-1.86E+00		3.43E+01		3.43E-05

		-1.77E+00		6.58E+01		6.58E-05		-1.86E+00		3.36E+01		3.36E-05

		-1.77E+00		6.67E+01		6.67E-05		-1.85E+00		3.29E+01		3.29E-05

		-1.77E+00		6.80E+01		6.80E-05		-1.85E+00		3.21E+01		3.21E-05

		-1.78E+00		6.90E+01		6.90E-05		-1.84E+00		3.15E+01		3.15E-05

		-1.78E+00		7.03E+01		7.03E-05		-1.84E+00		3.08E+01		3.08E-05

		-1.79E+00		7.15E+01		7.15E-05		-1.84E+00		3.01E+01		3.01E-05

		-1.79E+00		7.28E+01		7.28E-05		-1.83E+00		2.95E+01		2.95E-05

		-1.79E+00		7.38E+01		7.38E-05		-1.83E+00		2.88E+01		2.88E-05

		-1.80E+00		7.53E+01		7.53E-05		-1.82E+00		2.82E+01		2.82E-05

		-1.80E+00		7.63E+01		7.63E-05		-1.82E+00		2.76E+01		2.76E-05

		-1.81E+00		7.81E+01		7.81E-05		-1.82E+00		2.70E+01		2.70E-05

		-1.81E+00		7.94E+01		7.94E-05		-1.81E+00		2.64E+01		2.64E-05

		-1.81E+00		8.08E+01		8.08E-05		-1.81E+00		2.58E+01		2.58E-05

		-1.82E+00		8.21E+01		8.21E-05		-1.80E+00		2.53E+01		2.53E-05

		-1.82E+00		8.31E+01		8.31E-05		-1.80E+00		2.46E+01		2.46E-05

		-1.83E+00		8.50E+01		8.50E-05		-1.80E+00		2.42E+01		2.42E-05

		-1.83E+00		8.62E+01		8.62E-05		-1.79E+00		2.37E+01		2.37E-05

		-1.83E+00		8.78E+01		8.78E-05		-1.79E+00		2.32E+01		2.32E-05

		-1.84E+00		8.91E+01		8.91E-05		-1.78E+00		2.26E+01		2.26E-05

		-1.84E+00		9.09E+01		9.09E-05		-1.78E+00		2.22E+01		2.22E-05

		-1.85E+00		9.23E+01		9.23E-05		-1.78E+00		2.16E+01		2.16E-05

		-1.85E+00		9.40E+01		9.40E-05		-1.77E+00		2.12E+01		2.12E-05

		-1.85E+00		9.57E+01		9.57E-05		-1.77E+00		2.07E+01		2.07E-05

		-1.86E+00		9.72E+01		9.72E-05		-1.76E+00		2.02E+01		2.02E-05

		-1.86E+00		9.91E+01		9.91E-05		-1.76E+00		1.99E+01		1.99E-05

		-1.87E+00		1.01E+02		1.01E-04		-1.76E+00		1.94E+01		1.94E-05

		-1.87E+00		1.03E+02		1.03E-04		-1.75E+00		1.90E+01		1.90E-05

		-1.87E+00		1.05E+02		1.05E-04		-1.75E+00		1.86E+01		1.86E-05

		-1.88E+00		1.07E+02		1.07E-04		-1.74E+00		1.83E+01		1.83E-05

		-1.88E+00		1.08E+02		1.08E-04		-1.74E+00		1.79E+01		1.79E-05

		-1.89E+00		1.10E+02		1.10E-04		-1.74E+00		1.74E+01		1.74E-05

		-1.89E+00		1.12E+02		1.12E-04		-1.73E+00		1.71E+01		1.71E-05

		-1.89E+00		1.15E+02		1.15E-04		-1.73E+00		1.67E+01		1.67E-05

		-1.90E+00		1.17E+02		1.17E-04		-1.72E+00		1.66E+01		1.66E-05

		-1.90E+00		1.18E+02		1.18E-04		-1.72E+00		1.60E+01		1.60E-05

		-1.91E+00		1.21E+02		1.21E-04		-1.72E+00		1.59E+01		1.59E-05

		-1.91E+00		1.23E+02		1.23E-04		-1.71E+00		1.54E+01		1.54E-05

		-1.91E+00		1.25E+02		1.25E-04		-1.71E+00		1.51E+01		1.51E-05

		-1.92E+00		1.28E+02		1.28E-04		-1.70E+00		1.49E+01		1.49E-05

		-1.92E+00		1.30E+02		1.30E-04		-1.70E+00		1.46E+01		1.46E-05

		-1.93E+00		1.32E+02		1.32E-04		-1.70E+00		1.43E+01		1.43E-05

		-1.93E+00		1.35E+02		1.35E-04		-1.69E+00		1.40E+01		1.40E-05

		-1.93E+00		1.37E+02		1.37E-04		-1.69E+00		1.37E+01		1.37E-05

		-1.94E+00		1.40E+02		1.40E-04		-1.68E+00		1.35E+01		1.35E-05

		-1.94E+00		1.42E+02		1.42E-04		-1.68E+00		1.32E+01		1.32E-05

		-1.95E+00		1.45E+02		1.45E-04		-1.68E+00		1.29E+01		1.29E-05

		-1.95E+00		1.47E+02		1.47E-04		-1.67E+00		1.27E+01		1.27E-05

		-1.95E+00		1.50E+02		1.50E-04		-1.67E+00		1.25E+01		1.25E-05

		-1.96E+00		1.53E+02		1.53E-04		-1.66E+00		1.23E+01		1.23E-05

		-1.96E+00		1.56E+02		1.56E-04		-1.66E+00		1.20E+01		1.20E-05

		-1.97E+00		1.59E+02		1.59E-04		-1.66E+00		1.18E+01		1.18E-05

		-1.97E+00		1.61E+02		1.61E-04		-1.65E+00		1.15E+01		1.15E-05

		-1.97E+00		1.65E+02		1.65E-04		-1.65E+00		1.13E+01		1.13E-05

		-1.98E+00		1.68E+02		1.68E-04		-1.64E+00		1.12E+01		1.12E-05

		-1.98E+00		1.71E+02		1.71E-04		-1.64E+00		1.09E+01		1.09E-05

		-1.99E+00		1.74E+02		1.74E-04		-1.64E+00		1.07E+01		1.07E-05

		-1.99E+00		1.77E+02		1.77E-04		-1.63E+00		1.05E+01		1.05E-05

		-1.99E+00		1.81E+02		1.81E-04		-1.63E+00		1.04E+01		1.04E-05

		-2.00E+00		1.84E+02		1.84E-04		-1.62E+00		1.02E+01		1.02E-05

		-1.99E+00		1.80E+02		1.80E-04		-1.62E+00		1.00E+01		1.00E-05

		-1.99E+00		1.76E+02		1.76E-04		-1.62E+00		9.83E+00		9.83E-06

		-1.99E+00		1.72E+02		1.72E-04		-1.61E+00		9.72E+00		9.72E-06

		-1.98E+00		1.68E+02		1.68E-04		-1.61E+00		9.53E+00		9.53E-06

		-1.98E+00		1.64E+02		1.64E-04		-1.60E+00		9.43E+00		9.43E-06

		-1.97E+00		1.61E+02		1.61E-04		-1.60E+00		9.25E+00		9.25E-06

		-1.97E+00		1.57E+02		1.57E-04		-1.60E+00		9.11E+00		9.11E-06

		-1.97E+00		1.54E+02		1.54E-04		-1.59E+00		8.96E+00		8.96E-06

		-1.96E+00		1.51E+02		1.51E-04		-1.59E+00		8.82E+00		8.82E-06

		-1.96E+00		1.48E+02		1.48E-04		-1.58E+00		8.72E+00		8.72E-06

		-1.95E+00		1.44E+02		1.44E-04		-1.58E+00		8.58E+00		8.58E-06

		-1.95E+00		1.41E+02		1.41E-04		-1.58E+00		8.45E+00		8.45E-06

		-1.95E+00		1.38E+02		1.38E-04		-1.57E+00		8.34E+00		8.34E-06

		-1.94E+00		1.35E+02		1.35E-04		-1.57E+00		8.22E+00		8.22E-06

		-1.94E+00		1.32E+02		1.32E-04		-1.56E+00		8.15E+00		8.15E-06

		-1.93E+00		1.29E+02		1.29E-04		-1.56E+00		7.98E+00		7.98E-06

		-1.93E+00		1.26E+02		1.26E-04		-1.56E+00		7.89E+00		7.89E-06

		-1.93E+00		1.23E+02		1.23E-04		-1.55E+00		7.79E+00		7.79E-06

		-1.92E+00		1.20E+02		1.20E-04		-1.55E+00		7.70E+00		7.70E-06

		-1.92E+00		1.18E+02		1.18E-04		-1.54E+00		7.63E+00		7.63E-06

		-1.91E+00		1.15E+02		1.15E-04		-1.54E+00		7.51E+00		7.51E-06

		-1.91E+00		1.12E+02		1.12E-04		-1.54E+00		7.42E+00		7.42E-06

		-1.91E+00		1.10E+02		1.10E-04		-1.53E+00		7.35E+00		7.35E-06

		-1.90E+00		1.07E+02		1.07E-04		-1.53E+00		7.25E+00		7.25E-06

		-1.90E+00		1.05E+02		1.05E-04		-1.52E+00		7.18E+00		7.18E-06

		-1.89E+00		1.02E+02		1.02E-04		-1.52E+00		7.06E+00		7.06E-06

		-1.89E+00		1.00E+02		1.00E-04		-1.52E+00		7.02E+00		7.02E-06

		-1.89E+00		9.76E+01		9.76E-05		-1.51E+00		6.91E+00		6.91E-06

		-1.88E+00		9.54E+01		9.54E-05		-1.51E+00		6.86E+00		6.86E-06

		-1.88E+00		9.31E+01		9.31E-05		-1.50E+00		6.83E+00		6.83E-06

		-1.87E+00		9.13E+01		9.13E-05		-1.50E+00		6.74E+00		6.74E-06

		-1.87E+00		8.88E+01		8.88E-05		-1.50E+00		6.66E+00		6.66E-06

		-1.87E+00		8.73E+01		8.73E-05		-1.49E+00		6.61E+00		6.61E-06

		-1.86E+00		8.51E+01		8.51E-05		-1.49E+00		6.51E+00		6.51E-06

		-1.86E+00		8.33E+01		8.33E-05		-1.48E+00		6.51E+00		6.51E-06

		-1.85E+00		8.13E+01		8.13E-05		-1.48E+00		6.38E+00		6.38E-06

		-1.85E+00		7.95E+01		7.95E-05		-1.48E+00		6.38E+00		6.38E-06

		-1.85E+00		7.76E+01		7.76E-05		-1.47E+00		6.30E+00		6.30E-06

		-1.84E+00		7.59E+01		7.59E-05		-1.47E+00		6.26E+00		6.26E-06

		-1.84E+00		7.39E+01		7.39E-05		-1.46E+00		6.23E+00		6.23E-06

		-1.83E+00		7.24E+01		7.24E-05		-1.46E+00		6.18E+00		6.18E-06

		-1.83E+00		7.06E+01		7.06E-05		-1.46E+00		6.11E+00		6.11E-06

		-1.83E+00		6.91E+01		6.91E-05		-1.45E+00		6.08E+00		6.08E-06

		-1.82E+00		6.76E+01		6.76E-05		-1.45E+00		6.01E+00		6.01E-06

		-1.82E+00		6.56E+01		6.56E-05		-1.44E+00		6.04E+00		6.04E-06

		-1.81E+00		6.44E+01		6.44E-05		-1.44E+00		5.92E+00		5.92E-06

		-1.81E+00		6.28E+01		6.28E-05		-1.44E+00		5.88E+00		5.88E-06

		-1.81E+00		6.12E+01		6.12E-05		-1.43E+00		5.86E+00		5.86E-06

		-1.80E+00		5.98E+01		5.98E-05		-1.43E+00		5.82E+00		5.82E-06

		-1.80E+00		5.83E+01		5.83E-05		-1.42E+00		5.83E+00		5.83E-06

		-1.79E+00		5.69E+01		5.69E-05		-1.42E+00		5.76E+00		5.76E-06

		-1.79E+00		5.57E+01		5.57E-05		-1.42E+00		5.73E+00		5.73E-06

		-1.79E+00		5.42E+01		5.42E-05		-1.41E+00		5.66E+00		5.66E-06

		-1.78E+00		5.29E+01		5.29E-05		-1.41E+00		5.66E+00		5.66E-06

		-1.78E+00		5.19E+01		5.19E-05		-1.40E+00		5.65E+00		5.65E-06

		-1.77E+00		5.05E+01		5.05E-05		-1.40E+00		5.52E+00		5.52E-06

		-1.77E+00		4.94E+01		4.94E-05		-1.40E+00		5.55E+00		5.55E-06

		-1.77E+00		4.80E+01		4.80E-05		-1.39E+00		5.48E+00		5.48E-06

		-1.76E+00		4.68E+01		4.68E-05		-1.39E+00		5.48E+00		5.48E-06

		-1.76E+00		4.59E+01		4.59E-05		-1.38E+00		5.46E+00		5.46E-06

		-1.75E+00		4.49E+01		4.49E-05		-1.38E+00		5.40E+00		5.40E-06

		-1.75E+00		4.39E+01		4.39E-05		-1.38E+00		5.38E+00		5.38E-06

		-1.75E+00		4.26E+01		4.26E-05		-1.37E+00		5.35E+00		5.35E-06

		-1.74E+00		4.17E+01		4.17E-05		-1.37E+00		5.31E+00		5.31E-06

		-1.74E+00		4.08E+01		4.08E-05		-1.36E+00		5.31E+00		5.31E-06

		-1.73E+00		3.98E+01		3.98E-05		-1.36E+00		5.26E+00		5.26E-06

		-1.73E+00		3.87E+01		3.87E-05		-1.36E+00		5.26E+00		5.26E-06

		-1.73E+00		3.82E+01		3.82E-05		-1.35E+00		5.20E+00		5.20E-06

		-1.72E+00		3.71E+01		3.71E-05		-1.35E+00		5.19E+00		5.19E-06

		-1.72E+00		3.62E+01		3.62E-05		-1.34E+00		5.18E+00		5.18E-06

		-1.71E+00		3.52E+01		3.52E-05		-1.34E+00		5.11E+00		5.11E-06

		-1.71E+00		3.45E+01		3.45E-05		-1.34E+00		5.13E+00		5.13E-06

		-1.71E+00		3.36E+01		3.36E-05		-1.33E+00		5.07E+00		5.07E-06

		-1.70E+00		3.27E+01		3.27E-05		-1.33E+00		5.07E+00		5.07E-06

		-1.70E+00		3.23E+01		3.23E-05		-1.32E+00		5.07E+00		5.07E-06

		-1.69E+00		3.15E+01		3.15E-05		-1.32E+00		4.98E+00		4.98E-06

		-1.69E+00		3.08E+01		3.08E-05		-1.32E+00		4.99E+00		4.99E-06

		-1.69E+00		3.00E+01		3.00E-05		-1.31E+00		4.94E+00		4.94E-06

		-1.68E+00		2.94E+01		2.94E-05		-1.31E+00		4.93E+00		4.93E-06

		-1.68E+00		2.87E+01		2.87E-05		-1.30E+00		4.94E+00		4.94E-06

		-1.67E+00		2.78E+01		2.78E-05		-1.30E+00		4.86E+00		4.86E-06

		-1.67E+00		2.72E+01		2.72E-05		-1.30E+00		4.91E+00		4.91E-06

		-1.67E+00		2.66E+01		2.66E-05		-1.29E+00		4.86E+00		4.86E-06

		-1.66E+00		2.61E+01		2.61E-05		-1.29E+00		4.86E+00		4.86E-06

		-1.66E+00		2.56E+01		2.56E-05		-1.28E+00		4.82E+00		4.82E-06

		-1.65E+00		2.48E+01		2.48E-05		-1.28E+00		4.81E+00		4.81E-06

		-1.65E+00		2.45E+01		2.45E-05		-1.28E+00		4.79E+00		4.79E-06

		-1.65E+00		2.41E+01		2.41E-05		-1.27E+00		4.76E+00		4.76E-06

		-1.64E+00		2.34E+01		2.34E-05		-1.27E+00		4.71E+00		4.71E-06

		-1.64E+00		2.26E+01		2.26E-05		-1.26E+00		4.74E+00		4.74E-06

		-1.63E+00		2.23E+01		2.23E-05		-1.26E+00		4.66E+00		4.66E-06

		-1.63E+00		2.19E+01		2.19E-05		-1.26E+00		4.67E+00		4.67E-06

		-1.63E+00		2.17E+01		2.17E-05		-1.25E+00		4.66E+00		4.66E-06

		-1.62E+00		2.10E+01		2.10E-05		-1.25E+00		4.61E+00		4.61E-06

		-1.62E+00		2.08E+01		2.08E-05		-1.24E+00		4.63E+00		4.63E-06

		-1.61E+00		2.01E+01		2.01E-05		-1.24E+00		4.59E+00		4.59E-06

		-1.61E+00		1.96E+01		1.96E-05		-1.24E+00		4.58E+00		4.58E-06

		-1.61E+00		1.94E+01		1.94E-05		-1.23E+00		4.56E+00		4.56E-06

		-1.60E+00		1.92E+01		1.92E-05		-1.23E+00		4.54E+00		4.54E-06

		-1.60E+00		1.87E+01		1.87E-05		-1.22E+00		4.51E+00		4.51E-06

		-1.59E+00		1.83E+01		1.83E-05		-1.22E+00		4.46E+00		4.46E-06

		-1.59E+00		1.79E+01		1.79E-05		-1.22E+00		4.46E+00		4.46E-06

		-1.59E+00		1.75E+01		1.75E-05		-1.21E+00		4.45E+00		4.45E-06

		-1.58E+00		1.74E+01		1.74E-05		-1.21E+00		4.43E+00		4.43E-06

		-1.58E+00		1.70E+01		1.70E-05		-1.20E+00		4.43E+00		4.43E-06

		-1.57E+00		1.67E+01		1.67E-05		-1.20E+00		4.38E+00		4.38E-06

		-1.57E+00		1.64E+01		1.64E-05		-1.20E+00		4.35E+00		4.35E-06

		-1.57E+00		1.62E+01		1.62E-05		-1.19E+00		4.38E+00		4.38E-06

		-1.56E+00		1.59E+01		1.59E-05		-1.19E+00		4.30E+00		4.30E-06

		-1.56E+00		1.58E+01		1.58E-05		-1.18E+00		4.37E+00		4.37E-06

		-1.55E+00		1.54E+01		1.54E-05		-1.18E+00		4.24E+00		4.24E-06

		-1.55E+00		1.50E+01		1.50E-05		-1.18E+00		4.30E+00		4.30E-06

		-1.55E+00		1.49E+01		1.49E-05		-1.17E+00		4.23E+00		4.23E-06

		-1.54E+00		1.47E+01		1.47E-05		-1.17E+00		4.25E+00		4.25E-06

		-1.54E+00		1.45E+01		1.45E-05		-1.16E+00		4.20E+00		4.20E-06

		-1.53E+00		1.43E+01		1.43E-05		-1.16E+00		4.18E+00		4.18E-06

		-1.53E+00		1.40E+01		1.40E-05		-1.16E+00		4.18E+00		4.18E-06

		-1.53E+00		1.38E+01		1.38E-05		-1.15E+00		4.18E+00		4.18E-06

		-1.52E+00		1.36E+01		1.36E-05		-1.15E+00		4.13E+00		4.13E-06

		-1.52E+00		1.34E+01		1.34E-05		-1.14E+00		4.16E+00		4.16E-06

		-1.51E+00		1.33E+01		1.33E-05		-1.14E+00		4.06E+00		4.06E-06

		-1.51E+00		1.31E+01		1.31E-05		-1.14E+00		4.11E+00		4.11E-06

		-1.51E+00		1.29E+01		1.29E-05		-1.13E+00		4.06E+00		4.06E-06

		-1.50E+00		1.28E+01		1.28E-05		-1.13E+00		4.04E+00		4.04E-06

		-1.50E+00		1.26E+01		1.26E-05		-1.12E+00		4.07E+00		4.07E-06

		-1.49E+00		1.25E+01		1.25E-05		-1.12E+00		3.97E+00		3.97E-06

		-1.49E+00		1.23E+01		1.23E-05		-1.12E+00		4.01E+00		4.01E-06

		-1.49E+00		1.21E+01		1.21E-05		-1.11E+00		3.96E+00		3.96E-06

		-1.48E+00		1.20E+01		1.20E-05		-1.11E+00		3.94E+00		3.94E-06

		-1.48E+00		1.19E+01		1.19E-05		-1.10E+00		3.96E+00		3.96E-06

		-1.47E+00		1.17E+01		1.17E-05		-1.10E+00		3.86E+00		3.86E-06

		-1.47E+00		1.16E+01		1.16E-05		-1.10E+00		3.89E+00		3.89E-06

		-1.47E+00		1.16E+01		1.16E-05		-1.09E+00		3.88E+00		3.88E-06

		-1.46E+00		1.15E+01		1.15E-05		-1.09E+00		3.83E+00		3.83E-06

		-1.46E+00		1.14E+01		1.14E-05		-1.08E+00		3.86E+00		3.86E-06

		-1.45E+00		1.12E+01		1.12E-05		-1.08E+00		3.75E+00		3.75E-06

		-1.45E+00		1.11E+01		1.11E-05		-1.08E+00		3.81E+00		3.81E-06

		-1.45E+00		1.10E+01		1.10E-05		-1.07E+00		3.75E+00		3.75E-06

		-1.44E+00		1.09E+01		1.09E-05		-1.07E+00		3.72E+00		3.72E-06

		-1.44E+00		1.08E+01		1.08E-05		-1.06E+00		3.73E+00		3.73E-06

		-1.43E+00		1.07E+01		1.07E-05		-1.06E+00		3.65E+00		3.65E-06

		-1.43E+00		1.07E+01		1.07E-05		-1.06E+00		3.68E+00		3.68E-06

		-1.43E+00		1.06E+01		1.06E-05		-1.05E+00		3.62E+00		3.62E-06

		-1.42E+00		1.05E+01		1.05E-05		-1.05E+00		3.60E+00		3.60E-06

		-1.42E+00		1.04E+01		1.04E-05		-1.04E+00		3.62E+00		3.62E-06

		-1.41E+00		1.03E+01		1.03E-05		-1.04E+00		3.55E+00		3.55E-06

		-1.41E+00		1.02E+01		1.02E-05		-1.04E+00		3.55E+00		3.55E-06

		-1.41E+00		1.02E+01		1.02E-05		-1.03E+00		3.54E+00		3.54E-06

		-1.40E+00		1.01E+01		1.01E-05		-1.03E+00		3.47E+00		3.47E-06

		-1.40E+00		1.01E+01		1.01E-05		-1.02E+00		3.52E+00		3.52E-06

		-1.39E+00		9.98E+00		9.98E-06		-1.02E+00		3.43E+00		3.43E-06

		-1.39E+00		9.93E+00		9.93E-06		-1.02E+00		3.44E+00		3.44E-06

		-1.39E+00		9.90E+00		9.90E-06		-1.01E+00		3.40E+00		3.40E-06

		-1.38E+00		9.80E+00		9.80E-06		-1.01E+00		3.38E+00		3.38E-06

		-1.38E+00		9.76E+00		9.76E-06		-1.00E+00		3.39E+00		3.39E-06

		-1.37E+00		9.71E+00		9.71E-06		-9.99E-01		3.34E+00		3.34E-06

		-1.37E+00		9.61E+00		9.61E-06		-9.95E-01		3.34E+00		3.34E-06

		-1.37E+00		9.60E+00		9.60E-06		-9.91E-01		3.31E+00		3.31E-06

		-1.36E+00		9.55E+00		9.55E-06		-9.87E-01		3.28E+00		3.28E-06

		-1.36E+00		9.55E+00		9.55E-06		-9.83E-01		3.26E+00		3.26E-06

		-1.35E+00		9.44E+00		9.44E-06		-9.79E-01		3.20E+00		3.20E-06

		-1.35E+00		9.37E+00		9.37E-06		-9.75E-01		3.24E+00		3.24E-06

		-1.35E+00		9.35E+00		9.35E-06		-9.71E-01		3.20E+00		3.20E-06

		-1.34E+00		9.31E+00		9.31E-06		-9.67E-01		3.15E+00		3.15E-06

		-1.34E+00		9.34E+00		9.34E-06		-9.63E-01		3.17E+00		3.17E-06

		-1.33E+00		9.29E+00		9.29E-06		-9.59E-01		3.10E+00		3.10E-06

		-1.33E+00		9.21E+00		9.21E-06		-9.55E-01		3.09E+00		3.09E-06

		-1.33E+00		9.19E+00		9.19E-06		-9.51E-01		3.09E+00		3.09E-06

		-1.32E+00		9.12E+00		9.12E-06		-9.47E-01		3.04E+00		3.04E-06

		-1.32E+00		9.16E+00		9.16E-06		-9.43E-01		3.07E+00		3.07E-06

		-1.31E+00		9.06E+00		9.06E-06		-9.39E-01		2.94E+00		2.94E-06

		-1.31E+00		9.07E+00		9.07E-06		-9.35E-01		3.00E+00		3.00E-06

		-1.31E+00		9.03E+00		9.03E-06		-9.31E-01		2.94E+00		2.94E-06

		-1.30E+00		9.01E+00		9.01E-06		-9.27E-01		2.90E+00		2.90E-06

		-1.30E+00		9.00E+00		9.00E-06		-9.23E-01		2.91E+00		2.91E-06

		-1.29E+00		8.87E+00		8.87E-06		-9.19E-01		2.84E+00		2.84E-06

		-1.29E+00		8.92E+00		8.92E-06		-9.15E-01		2.83E+00		2.83E-06

		-1.29E+00		8.88E+00		8.88E-06		-9.11E-01		2.80E+00		2.80E-06

		-1.28E+00		8.85E+00		8.85E-06		-9.07E-01		2.77E+00		2.77E-06

		-1.28E+00		8.87E+00		8.87E-06		-9.03E-01		2.74E+00		2.74E-06

		-1.27E+00		8.78E+00		8.78E-06		-8.99E-01		2.68E+00		2.68E-06

		-1.27E+00		8.75E+00		8.75E-06		-8.95E-01		2.66E+00		2.66E-06

		-1.27E+00		8.75E+00		8.75E-06		-8.91E-01		2.66E+00		2.66E-06

		-1.26E+00		8.71E+00		8.71E-06		-8.87E-01		2.58E+00		2.58E-06

		-1.26E+00		8.73E+00		8.73E-06		-8.83E-01		2.56E+00		2.56E-06

		-1.25E+00		8.63E+00		8.63E-06		-8.79E-01		2.45E+00		2.45E-06

		-1.25E+00		8.68E+00		8.68E-06		-8.75E-01		2.49E+00		2.49E-06

		-1.25E+00		8.64E+00		8.64E-06		-8.71E-01		2.39E+00		2.39E-06

		-1.24E+00		8.58E+00		8.58E-06		-8.67E-01		2.38E+00		2.38E-06

		-1.24E+00		8.59E+00		8.59E-06		-8.63E-01		2.33E+00		2.33E-06

		-1.23E+00		8.50E+00		8.50E-06		-8.59E-01		2.30E+00		2.30E-06

		-1.23E+00		8.54E+00		8.54E-06		-8.55E-01		2.25E+00		2.25E-06

		-1.23E+00		8.54E+00		8.54E-06		-8.51E-01		2.24E+00		2.24E-06

		-1.22E+00		8.48E+00		8.48E-06		-8.47E-01		2.15E+00		2.15E-06

		-1.22E+00		8.52E+00		8.52E-06		-8.43E-01		2.14E+00		2.14E-06

		-1.21E+00		8.44E+00		8.44E-06		-8.39E-01		2.03E+00		2.03E-06

		-1.21E+00		8.43E+00		8.43E-06		-8.35E-01		2.05E+00		2.05E-06

		-1.21E+00		8.42E+00		8.42E-06		-8.31E-01		1.98E+00		1.98E-06

		-1.20E+00		8.40E+00		8.40E-06		-8.27E-01		1.98E+00		1.98E-06

		-1.20E+00		8.41E+00		8.41E-06		-8.23E-01		1.89E+00		1.89E-06

		-1.19E+00		8.32E+00		8.32E-06		-8.19E-01		1.84E+00		1.84E-06

		-1.19E+00		8.36E+00		8.36E-06		-8.15E-01		1.82E+00		1.82E-06

		-1.19E+00		8.32E+00		8.32E-06		-8.11E-01		1.78E+00		1.78E-06

		-1.18E+00		8.29E+00		8.29E-06		-8.07E-01		1.78E+00		1.78E-06

		-1.18E+00		8.35E+00		8.35E-06		-8.03E-01		1.71E+00		1.71E-06

		-1.17E+00		8.20E+00		8.20E-06		-7.99E-01		1.67E+00		1.67E-06

		-1.17E+00		8.21E+00		8.21E-06		-7.95E-01		1.62E+00		1.62E-06

		-1.17E+00		8.17E+00		8.17E-06		-7.91E-01		1.60E+00		1.60E-06

		-1.16E+00		8.18E+00		8.18E-06		-7.87E-01		1.54E+00		1.54E-06

		-1.16E+00		8.18E+00		8.18E-06		-7.83E-01		1.56E+00		1.56E-06

		-1.15E+00		8.12E+00		8.12E-06		-7.79E-01		1.47E+00		1.47E-06

		-1.15E+00		8.16E+00		8.16E-06		-7.75E-01		1.48E+00		1.48E-06

		-1.15E+00		8.07E+00		8.07E-06		-7.71E-01		1.43E+00		1.43E-06

		-1.14E+00		8.07E+00		8.07E-06		-7.67E-01		1.40E+00		1.40E-06

		-1.14E+00		8.07E+00		8.07E-06		-7.63E-01		1.39E+00		1.39E-06

		-1.13E+00		8.03E+00		8.03E-06		-7.59E-01		1.32E+00		1.32E-06

		-1.13E+00		8.04E+00		8.04E-06		-7.55E-01		1.32E+00		1.32E-06

		-1.13E+00		7.99E+00		7.99E-06		-7.51E-01		1.29E+00		1.29E-06

		-1.12E+00		7.97E+00		7.97E-06		-7.47E-01		1.25E+00		1.25E-06

		-1.12E+00		7.90E+00		7.90E-06		-7.43E-01		1.26E+00		1.26E-06

		-1.11E+00		7.92E+00		7.92E-06		-7.39E-01		1.19E+00		1.19E-06

		-1.11E+00		7.90E+00		7.90E-06		-7.35E-01		1.20E+00		1.20E-06

		-1.11E+00		7.89E+00		7.89E-06		-7.31E-01		1.17E+00		1.17E-06

		-1.10E+00		7.86E+00		7.86E-06		-7.27E-01		1.14E+00		1.14E-06

		-1.10E+00		7.85E+00		7.85E-06		-7.23E-01		1.14E+00		1.14E-06

		-1.09E+00		7.78E+00		7.78E-06		-7.19E-01		1.08E+00		1.08E-06

		-1.09E+00		7.71E+00		7.71E-06		-7.15E-01		1.09E+00		1.09E-06

		-1.09E+00		7.76E+00		7.76E-06		-7.11E-01		1.07E+00		1.07E-06

		-1.08E+00		7.70E+00		7.70E-06		-7.07E-01		1.03E+00		1.03E-06

		-1.08E+00		7.72E+00		7.72E-06		-7.03E-01		1.04E+00		1.04E-06

		-1.07E+00		7.67E+00		7.67E-06		-6.99E-01		9.68E-01		9.68E-07

		-1.07E+00		7.66E+00		7.66E-06		-6.95E-01		9.98E-01		9.98E-07

		-1.07E+00		7.63E+00		7.63E-06		-6.91E-01		9.58E-01		9.58E-07

		-1.06E+00		7.50E+00		7.50E-06		-6.87E-01		9.37E-01		9.37E-07

		-1.06E+00		7.62E+00		7.62E-06		-6.83E-01		9.34E-01		9.34E-07

		-1.05E+00		7.50E+00		7.50E-06		-6.79E-01		8.76E-01		8.76E-07

		-1.05E+00		7.51E+00		7.51E-06		-6.75E-01		8.93E-01		8.93E-07

		-1.05E+00		7.45E+00		7.45E-06		-6.71E-01		8.72E-01		8.72E-07

		-1.04E+00		7.46E+00		7.46E-06		-6.67E-01		8.39E-01		8.39E-07

		-1.04E+00		7.43E+00		7.43E-06		-6.63E-01		8.41E-01		8.41E-07

		-1.03E+00		7.34E+00		7.34E-06		-6.59E-01		7.77E-01		7.77E-07

		-1.03E+00		7.39E+00		7.39E-06		-6.55E-01		8.06E-01		8.06E-07

		-1.03E+00		7.37E+00		7.37E-06		-6.51E-01		7.63E-01		7.63E-07

		-1.02E+00		7.35E+00		7.35E-06		-6.47E-01		7.40E-01		7.40E-07

		-1.02E+00		7.33E+00		7.33E-06		-6.43E-01		7.32E-01		7.32E-07

		-1.01E+00		7.25E+00		7.25E-06		-6.39E-01		6.76E-01		6.76E-07

		-1.01E+00		7.23E+00		7.23E-06		-6.35E-01		6.90E-01		6.90E-07

		-1.01E+00		7.16E+00		7.16E-06		-6.31E-01		6.66E-01		6.66E-07

		-1.00E+00		7.16E+00		7.16E-06		-6.27E-01		6.29E-01		6.29E-07

		-9.98E-01		7.20E+00		7.20E-06		-6.23E-01		6.26E-01		6.26E-07

		-9.94E-01		7.06E+00		7.06E-06		-6.19E-01		5.60E-01		5.60E-07

		-9.90E-01		7.07E+00		7.07E-06		-6.15E-01		5.94E-01		5.94E-07

		-9.86E-01		7.05E+00		7.05E-06		-6.11E-01		5.46E-01		5.46E-07

		-9.82E-01		6.98E+00		6.98E-06		-6.07E-01		5.22E-01		5.22E-07

		-9.78E-01		6.98E+00		6.98E-06		-6.03E-01		5.13E-01		5.13E-07

		-9.74E-01		6.92E+00		6.92E-06		-5.99E-01		4.65E-01		4.65E-07

		-9.70E-01		6.95E+00		6.95E-06		-5.95E-01		4.71E-01		4.71E-07

		-9.66E-01		6.85E+00		6.85E-06		-5.91E-01		4.44E-01		4.44E-07

		-9.62E-01		6.83E+00		6.83E-06		-5.87E-01		4.11E-01		4.11E-07

		-9.58E-01		6.85E+00		6.85E-06		-5.83E-01		4.07E-01		4.07E-07

		-9.54E-01		6.75E+00		6.75E-06		-5.79E-01		3.40E-01		3.40E-07

		-9.50E-01		6.75E+00		6.75E-06		-5.75E-01		3.71E-01		3.71E-07

		-9.46E-01		6.69E+00		6.69E-06		-5.71E-01		3.29E-01		3.29E-07

		-9.42E-01		6.66E+00		6.66E-06		-5.67E-01		3.01E-01		3.01E-07

		-9.38E-01		6.67E+00		6.67E-06		-5.63E-01		2.87E-01		2.87E-07

		-9.34E-01		6.59E+00		6.59E-06		-5.59E-01		2.38E-01		2.38E-07

		-9.30E-01		6.56E+00		6.56E-06		-5.55E-01		2.53E-01		2.53E-07

		-9.26E-01		6.51E+00		6.51E-06		-5.51E-01		2.15E-01		2.15E-07

		-9.22E-01		6.47E+00		6.47E-06		-5.47E-01		1.84E-01		1.84E-07

		-9.18E-01		6.50E+00		6.50E-06		-5.43E-01		1.79E-01		1.79E-07

		-9.14E-01		6.35E+00		6.35E-06		-5.39E-01		1.36E-01		1.36E-07

		-9.10E-01		6.38E+00		6.38E-06		-5.35E-01		1.20E-01		1.20E-07

		-9.06E-01		6.32E+00		6.32E-06		-5.31E-01		1.08E-01		1.08E-07

		-9.02E-01		6.26E+00		6.26E-06		-5.27E-01		5.97E-02		5.97E-08

		-8.98E-01		6.25E+00		6.25E-06		-5.23E-01		5.62E-02		5.62E-08

		-8.94E-01		6.15E+00		6.15E-06		-5.19E-01		1.73E-02		1.73E-08

		-8.90E-01		6.17E+00		6.17E-06		-5.15E-01		-6.30E-03		-6.30E-09

		-8.86E-01		6.08E+00		6.08E-06		-5.11E-01		-3.30E-02		-3.30E-08

		-8.82E-01		6.02E+00		6.02E-06		-5.07E-01		-6.68E-02		-6.68E-08

		-8.78E-01		6.03E+00		6.03E-06		-5.03E-01		-8.20E-02		-8.20E-08

		-8.74E-01		5.91E+00		5.91E-06		-4.99E-01		-1.33E-01		-1.33E-07

		-8.70E-01		5.92E+00		5.92E-06		-4.95E-01		-1.21E-01		-1.21E-07

		-8.66E-01		5.86E+00		5.86E-06		-4.91E-01		-1.56E-01		-1.56E-07

		-8.62E-01		5.76E+00		5.76E-06		-4.87E-01		-1.92E-01		-1.92E-07

		-8.58E-01		5.72E+00		5.72E-06		-4.83E-01		-2.07E-01		-2.07E-07

		-8.54E-01		5.69E+00		5.69E-06		-4.79E-01		-2.77E-01		-2.77E-07

		-8.50E-01		5.61E+00		5.61E-06		-4.75E-01		-2.47E-01		-2.47E-07

		-8.46E-01		5.58E+00		5.58E-06		-4.71E-01		-2.95E-01		-2.95E-07

		-8.42E-01		5.50E+00		5.50E-06		-4.67E-01		-3.31E-01		-3.31E-07

		-8.38E-01		5.49E+00		5.49E-06		-4.63E-01		-3.51E-01		-3.51E-07

		-8.34E-01		5.34E+00		5.34E-06		-4.59E-01		-4.11E-01		-4.11E-07

		-8.30E-01		5.33E+00		5.33E-06		-4.55E-01		-4.01E-01		-4.01E-07

		-8.26E-01		5.26E+00		5.26E-06		-4.51E-01		-4.38E-01		-4.38E-07

		-8.22E-01		5.17E+00		5.17E-06		-4.47E-01		-4.77E-01		-4.77E-07

		-8.18E-01		5.18E+00		5.18E-06		-4.43E-01		-4.94E-01		-4.94E-07

		-8.14E-01		5.06E+00		5.06E-06		-4.39E-01		-5.57E-01		-5.57E-07

		-8.10E-01		5.09E+00		5.09E-06		-4.35E-01		-5.39E-01		-5.39E-07

		-8.06E-01		5.01E+00		5.01E-06		-4.31E-01		-5.94E-01		-5.94E-07

		-8.02E-01		4.86E+00		4.86E-06		-4.27E-01		-6.24E-01		-6.24E-07

		-7.98E-01		4.91E+00		4.91E-06		-4.23E-01		-6.61E-01		-6.61E-07

		-7.94E-01		4.80E+00		4.80E-06		-4.19E-01		-7.08E-01		-7.08E-07

		-7.90E-01		4.76E+00		4.76E-06		-4.15E-01		-7.06E-01		-7.06E-07

		-7.86E-01		4.72E+00		4.72E-06		-4.11E-01		-7.53E-01		-7.53E-07

		-7.82E-01		4.66E+00		4.66E-06		-4.07E-01		-7.89E-01		-7.89E-07

		-7.78E-01		4.67E+00		4.67E-06		-4.03E-01		-8.17E-01		-8.17E-07

		-7.74E-01		4.47E+00		4.47E-06		-3.99E-01		-8.85E-01		-8.85E-07

		-7.70E-01		4.50E+00		4.50E-06		-3.95E-01		-8.65E-01		-8.65E-07

		-7.66E-01		4.47E+00		4.47E-06		-3.91E-01		-9.26E-01		-9.26E-07

		-7.62E-01		4.34E+00		4.34E-06		-3.87E-01		-9.55E-01		-9.55E-07

		-7.58E-01		4.34E+00		4.34E-06		-3.83E-01		-9.99E-01		-9.99E-07

		-7.54E-01		4.23E+00		4.23E-06		-3.79E-01		-1.05E+00		-1.05E-06

		-7.50E-01		4.23E+00		4.23E-06		-3.75E-01		-1.06E+00		-1.06E-06

		-7.46E-01		4.12E+00		4.12E-06		-3.71E-01		-1.10E+00		-1.10E-06

		-7.42E-01		4.10E+00		4.10E-06		-3.67E-01		-1.15E+00		-1.15E-06

		-7.38E-01		4.12E+00		4.12E-06		-3.63E-01		-1.18E+00		-1.18E-06

		-7.34E-01		4.00E+00		4.00E-06		-3.59E-01		-1.25E+00		-1.25E-06

		-7.30E-01		4.00E+00		4.00E-06		-3.55E-01		-1.24E+00		-1.24E-06

		-7.26E-01		3.91E+00		3.91E-06		-3.51E-01		-1.30E+00		-1.30E-06

		-7.22E-01		3.84E+00		3.84E-06		-3.47E-01		-1.34E+00		-1.34E-06

		-7.18E-01		3.82E+00		3.82E-06		-3.43E-01		-1.39E+00		-1.39E-06

		-7.14E-01		3.75E+00		3.75E-06		-3.39E-01		-1.44E+00		-1.44E-06

		-7.10E-01		3.76E+00		3.76E-06		-3.35E-01		-1.45E+00		-1.45E-06

		-7.06E-01		3.66E+00		3.66E-06		-3.31E-01		-1.50E+00		-1.50E-06

		-7.02E-01		3.63E+00		3.63E-06		-3.27E-01		-1.57E+00		-1.57E-06

		-6.98E-01		3.62E+00		3.62E-06		-3.23E-01		-1.55E+00		-1.55E-06

		-6.94E-01		3.57E+00		3.57E-06		-3.19E-01		-1.69E+00		-1.69E-06

		-6.90E-01		3.53E+00		3.53E-06		-3.15E-01		-1.68E+00		-1.68E-06

		-6.86E-01		3.53E+00		3.53E-06		-3.11E-01		-1.69E+00		-1.69E-06

		-6.82E-01		3.42E+00		3.42E-06		-3.07E-01		-1.76E+00		-1.76E-06

		-6.78E-01		3.42E+00		3.42E-06		-3.03E-01		-1.75E+00		-1.75E-06

		-6.74E-01		3.34E+00		3.34E-06		-2.99E-01		-1.84E+00		-1.84E-06

		-6.70E-01		3.36E+00		3.36E-06		-2.95E-01		-1.83E+00		-1.83E-06

		-6.66E-01		3.29E+00		3.29E-06		-2.91E-01		-1.91E+00		-1.91E-06

		-6.62E-01		3.20E+00		3.20E-06		-2.87E-01		-1.94E+00		-1.94E-06

		-6.58E-01		3.22E+00		3.22E-06		-2.83E-01		-1.88E+00		-1.88E-06

		-6.54E-01		3.09E+00		3.09E-06		-2.79E-01		-1.99E+00		-1.99E-06

		-6.50E-01		3.12E+00		3.12E-06		-2.75E-01		-1.94E+00		-1.94E-06

		-6.46E-01		3.08E+00		3.08E-06		-2.71E-01		-1.99E+00		-1.99E-06

		-6.42E-01		3.05E+00		3.05E-06		-2.67E-01		-1.98E+00		-1.98E-06

		-6.38E-01		2.98E+00		2.98E-06		-2.63E-01		-1.97E+00		-1.97E-06

		-6.34E-01		2.88E+00		2.88E-06		-2.59E-01		-2.03E+00		-2.03E-06

		-6.30E-01		2.93E+00		2.93E-06		-2.55E-01		-2.02E+00		-2.02E-06

		-6.26E-01		2.82E+00		2.82E-06		-2.51E-01		-2.03E+00		-2.03E-06

		-6.22E-01		2.84E+00		2.84E-06		-2.47E-01		-2.05E+00		-2.05E-06

		-6.18E-01		2.78E+00		2.78E-06		-2.43E-01		-1.96E+00		-1.96E-06

		-6.14E-01		2.73E+00		2.73E-06		-2.39E-01		-2.06E+00		-2.06E-06

		-6.10E-01		2.66E+00		2.66E-06		-2.35E-01		-2.01E+00		-2.01E-06

		-6.06E-01		2.67E+00		2.67E-06		-2.31E-01		-2.06E+00		-2.06E-06

		-6.02E-01		2.66E+00		2.66E-06		-2.27E-01		-2.05E+00		-2.05E-06

		-5.98E-01		2.54E+00		2.54E-06		-2.23E-01		-2.02E+00		-2.02E-06

		-5.94E-01		2.47E+00		2.47E-06		-2.19E-01		-2.08E+00		-2.08E-06

		-5.90E-01		2.48E+00		2.48E-06		-2.15E-01		-2.09E+00		-2.09E-06

		-5.86E-01		2.50E+00		2.50E-06		-2.11E-01		-2.11E+00		-2.11E-06

		-5.82E-01		2.42E+00		2.42E-06		-2.07E-01		-2.14E+00		-2.14E-06

		-5.78E-01		2.38E+00		2.38E-06		-2.03E-01		-2.10E+00		-2.10E-06

		-5.74E-01		2.30E+00		2.30E-06		-1.99E-01		-2.22E+00		-2.22E-06

		-5.70E-01		2.27E+00		2.27E-06		-1.95E-01		-2.19E+00		-2.19E-06

		-5.66E-01		2.25E+00		2.25E-06		-1.91E-01		-2.25E+00		-2.25E-06

		-5.62E-01		2.24E+00		2.24E-06		-1.87E-01		-2.29E+00		-2.29E-06

		-5.58E-01		2.16E+00		2.16E-06		-1.83E-01		-2.31E+00		-2.31E-06

		-5.54E-01		2.12E+00		2.12E-06		-1.79E-01		-2.41E+00		-2.41E-06

		-5.50E-01		2.14E+00		2.14E-06		-1.75E-01		-2.41E+00		-2.41E-06

		-5.46E-01		2.06E+00		2.06E-06		-1.71E-01		-2.52E+00		-2.52E-06

		-5.42E-01		1.97E+00		1.97E-06		-1.67E-01		-2.53E+00		-2.53E-06

		-5.38E-01		2.03E+00		2.03E-06		-1.63E-01		-2.61E+00		-2.61E-06

		-5.34E-01		1.88E+00		1.88E-06		-1.59E-01		-2.69E+00		-2.69E-06

		-5.30E-01		1.92E+00		1.92E-06		-1.55E-01		-2.74E+00		-2.74E-06

		-5.26E-01		1.86E+00		1.86E-06		-1.51E-01		-2.82E+00		-2.82E-06

		-5.22E-01		1.80E+00		1.80E-06		-1.47E-01		-2.90E+00		-2.90E-06

		-5.18E-01		1.75E+00		1.75E-06		-1.43E-01		-2.97E+00		-2.97E-06

		-5.14E-01		1.62E+00		1.62E-06		-1.39E-01		-3.09E+00		-3.09E-06

		-5.10E-01		1.68E+00		1.68E-06		-1.35E-01		-3.13E+00		-3.13E-06

		-5.06E-01		1.66E+00		1.66E-06		-1.31E-01		-3.26E+00		-3.26E-06

		-5.02E-01		1.58E+00		1.58E-06		-1.27E-01		-3.32E+00		-3.32E-06

		-4.98E-01		1.51E+00		1.51E-06		-1.23E-01		-3.41E+00		-3.41E-06

		-4.94E-01		1.46E+00		1.46E-06		-1.19E-01		-3.54E+00		-3.54E-06

		-4.90E-01		1.47E+00		1.47E-06		-1.15E-01		-3.61E+00		-3.61E-06

		-4.86E-01		1.41E+00		1.41E-06		-1.11E-01		-3.78E+00		-3.78E-06

		-4.82E-01		1.35E+00		1.35E-06		-1.07E-01		-3.88E+00		-3.88E-06

		-4.78E-01		1.34E+00		1.34E-06		-1.03E-01		-4.01E+00		-4.01E-06

		-4.74E-01		1.21E+00		1.21E-06		-9.90E-02		-4.16E+00		-4.16E-06

		-4.70E-01		1.22E+00		1.22E-06		-9.50E-02		-4.31E+00		-4.31E-06

		-4.66E-01		1.17E+00		1.17E-06		-9.10E-02		-4.43E+00		-4.43E-06

		-4.62E-01		1.10E+00		1.10E-06		-8.70E-02		-4.58E+00		-4.58E-06

		-4.58E-01		1.07E+00		1.07E-06		-8.30E-02		-4.74E+00		-4.74E-06

		-4.54E-01		9.73E-01		9.73E-07		-7.90E-02		-4.93E+00		-4.93E-06

		-4.50E-01		9.74E-01		9.74E-07		-7.50E-02		-5.06E+00		-5.06E-06

		-4.46E-01		9.10E-01		9.10E-07		-7.10E-02		-5.25E+00		-5.25E-06

		-4.42E-01		8.47E-01		8.47E-07		-6.70E-02		-5.42E+00		-5.42E-06

		-4.38E-01		8.21E-01		8.21E-07		-6.30E-02		-5.59E+00		-5.59E-06

		-4.34E-01		7.22E-01		7.22E-07		-5.90E-02		-5.81E+00		-5.81E-06

		-4.30E-01		7.02E-01		7.02E-07		-5.50E-02		-5.98E+00		-5.98E-06

		-4.26E-01		6.64E-01		6.64E-07		-5.10E-02		-6.20E+00		-6.20E-06

		-4.22E-01		6.02E-01		6.02E-07		-4.70E-02		-6.35E+00		-6.35E-06

		-4.18E-01		5.61E-01		5.61E-07		-4.30E-02		-6.60E+00		-6.60E-06

		-4.14E-01		4.64E-01		4.64E-07		-3.90E-02		-6.84E+00		-6.84E-06

		-4.10E-01		4.54E-01		4.54E-07		-3.50E-02		-7.00E+00		-7.00E-06

		-4.06E-01		4.07E-01		4.07E-07		-3.10E-02		-7.24E+00		-7.24E-06

		-4.02E-01		3.33E-01		3.33E-07		-2.70E-02		-7.46E+00		-7.46E-06

		-3.98E-01		3.02E-01		3.02E-07		-2.30E-02		-7.70E+00		-7.70E-06

		-3.94E-01		2.06E-01		2.06E-07		-1.90E-02		-7.91E+00		-7.91E-06

		-3.90E-01		2.00E-01		2.00E-07		-1.50E-02		-8.11E+00		-8.11E-06

		-3.86E-01		1.45E-01		1.45E-07		-1.10E-02		-8.36E+00		-8.36E-06

		-3.82E-01		7.86E-02		7.86E-08		-7.01E-03		-8.56E+00		-8.56E-06

		-3.78E-01		5.70E-02		5.70E-08		-3.01E-03		-8.83E+00		-8.83E-06

		-3.74E-01		-5.50E-02		-5.50E-08		9.89E-04		-9.07E+00		-9.07E-06

		-3.70E-01		-4.50E-02		-4.50E-08		4.99E-03		-9.25E+00		-9.25E-06

		-3.66E-01		-9.60E-02		-9.60E-08		8.99E-03		-9.48E+00		-9.48E-06

		-3.62E-01		-1.65E-01		-1.65E-07		1.30E-02		-9.71E+00		-9.71E-06

		-3.58E-01		-1.89E-01		-1.89E-07		1.70E-02		-9.90E+00		-9.90E-06

		-3.54E-01		-2.99E-01		-2.99E-07		2.10E-02		-1.01E+01		-1.01E-05

		-3.50E-01		-2.73E-01		-2.73E-07		2.50E-02		-1.03E+01		-1.03E-05

		-3.46E-01		-3.46E-01		-3.46E-07		2.90E-02		-1.05E+01		-1.05E-05

		-3.42E-01		-3.94E-01		-3.94E-07		3.30E-02		-1.06E+01		-1.06E-05

		-3.38E-01		-4.22E-01		-4.22E-07		3.70E-02		-1.08E+01		-1.08E-05

		-3.34E-01		-5.16E-01		-5.16E-07		4.10E-02		-1.09E+01		-1.09E-05

		-3.30E-01		-4.95E-01		-4.95E-07		4.50E-02		-1.11E+01		-1.11E-05

		-3.26E-01		-5.41E-01		-5.41E-07		4.90E-02		-1.12E+01		-1.12E-05

		-3.22E-01		-5.93E-01		-5.93E-07		5.30E-02		-1.13E+01		-1.13E-05

		-3.18E-01		-6.33E-01		-6.33E-07		5.70E-02		-1.14E+01		-1.14E-05

		-3.14E-01		-7.07E-01		-7.07E-07		6.10E-02		-1.15E+01		-1.15E-05

		-3.10E-01		-6.98E-01		-6.98E-07		6.50E-02		-1.15E+01		-1.15E-05

		-3.06E-01		-7.38E-01		-7.38E-07		6.90E-02		-1.16E+01		-1.16E-05

		-3.02E-01		-7.85E-01		-7.85E-07		7.30E-02		-1.16E+01		-1.16E-05

		-2.98E-01		-8.19E-01		-8.19E-07		7.70E-02		-1.17E+01		-1.17E-05

		-2.94E-01		-8.86E-01		-8.86E-07		8.10E-02		-1.16E+01		-1.16E-05

		-2.90E-01		-8.90E-01		-8.90E-07		8.50E-02		-1.17E+01		-1.17E-05

		-2.86E-01		-9.07E-01		-9.07E-07		8.90E-02		-1.16E+01		-1.16E-05

		-2.82E-01		-9.71E-01		-9.71E-07		9.30E-02		-1.16E+01		-1.16E-05

		-2.78E-01		-9.99E-01		-9.99E-07		9.70E-02		-1.16E+01		-1.16E-05

		-2.74E-01		-1.06E+00		-1.06E-06		1.01E-01		-1.15E+01		-1.15E-05

		-2.70E-01		-1.06E+00		-1.06E-06		1.05E-01		-1.15E+01		-1.15E-05

		-2.66E-01		-1.09E+00		-1.09E-06		1.09E-01		-1.15E+01		-1.15E-05

		-2.62E-01		-1.16E+00		-1.16E-06		1.13E-01		-1.14E+01		-1.14E-05

		-2.58E-01		-1.19E+00		-1.19E-06		1.17E-01		-1.13E+01		-1.13E-05

		-2.54E-01		-1.26E+00		-1.26E-06		1.21E-01		-1.12E+01		-1.12E-05

		-2.50E-01		-1.26E+00		-1.26E-06		1.25E-01		-1.12E+01		-1.12E-05

		-2.46E-01		-1.30E+00		-1.30E-06		1.29E-01		-1.11E+01		-1.11E-05

		-2.42E-01		-1.35E+00		-1.35E-06		1.33E-01		-1.10E+01		-1.10E-05

		-2.38E-01		-1.41E+00		-1.41E-06		1.37E-01		-1.09E+01		-1.09E-05

		-2.34E-01		-1.50E+00		-1.50E-06		1.41E-01		-1.08E+01		-1.08E-05

		-2.30E-01		-1.49E+00		-1.49E-06		1.45E-01		-1.07E+01		-1.07E-05

		-2.26E-01		-1.60E+00		-1.60E-06		1.49E-01		-1.07E+01		-1.07E-05

		-2.22E-01		-1.63E+00		-1.63E-06		1.53E-01		-1.06E+01		-1.06E-05

		-2.18E-01		-1.72E+00		-1.72E-06		1.57E-01		-1.05E+01		-1.05E-05

		-2.14E-01		-1.76E+00		-1.76E-06		1.61E-01		-1.04E+01		-1.04E-05

		-2.10E-01		-1.79E+00		-1.79E-06		1.65E-01		-1.03E+01		-1.03E-05

		-2.06E-01		-1.83E+00		-1.83E-06		1.69E-01		-1.02E+01		-1.02E-05

		-2.02E-01		-1.88E+00		-1.88E-06		1.73E-01		-1.02E+01		-1.02E-05

		-1.98E-01		-1.98E+00		-1.98E-06		1.77E-01		-1.01E+01		-1.01E-05

		-1.94E-01		-2.08E+00		-2.08E-06		1.81E-01		-1.00E+01		-1.00E-05

		-1.90E-01		-2.12E+00		-2.12E-06		1.85E-01		-9.90E+00		-9.90E-06

		-1.86E-01		-2.17E+00		-2.17E-06		1.89E-01		-9.82E+00		-9.82E-06

		-1.82E-01		-2.26E+00		-2.26E-06		1.93E-01		-9.77E+00		-9.77E-06

		-1.78E-01		-2.29E+00		-2.29E-06		1.97E-01		-9.69E+00		-9.69E-06

		-1.74E-01		-2.39E+00		-2.39E-06		2.01E-01		-9.59E+00		-9.59E-06

		-1.70E-01		-2.40E+00		-2.40E-06		2.05E-01		-9.51E+00		-9.51E-06

		-1.66E-01		-2.53E+00		-2.53E-06		2.09E-01		-9.46E+00		-9.46E-06

		-1.62E-01		-2.62E+00		-2.62E-06		2.13E-01		-9.38E+00		-9.38E-06

		-1.58E-01		-2.68E+00		-2.68E-06		2.17E-01		-9.33E+00		-9.33E-06

		-1.54E-01		-2.79E+00		-2.79E-06		2.21E-01		-9.26E+00		-9.26E-06

		-1.50E-01		-2.84E+00		-2.84E-06		2.25E-01		-9.21E+00		-9.21E-06

		-1.46E-01		-2.88E+00		-2.88E-06		2.29E-01		-9.15E+00		-9.15E-06

		-1.42E-01		-3.03E+00		-3.03E-06		2.33E-01		-9.06E+00		-9.06E-06

		-1.38E-01		-3.12E+00		-3.12E-06		2.37E-01		-9.05E+00		-9.05E-06

		-1.34E-01		-3.25E+00		-3.25E-06		2.41E-01		-8.96E+00		-8.96E-06

		-1.30E-01		-3.30E+00		-3.30E-06		2.45E-01		-8.93E+00		-8.93E-06

		-1.26E-01		-3.41E+00		-3.41E-06		2.49E-01		-8.87E+00		-8.87E-06

		-1.22E-01		-3.52E+00		-3.52E-06		2.53E-01		-8.81E+00		-8.81E-06

		-1.18E-01		-3.66E+00		-3.66E-06		2.57E-01		-8.75E+00		-8.75E-06

		-1.14E-01		-3.81E+00		-3.81E-06		2.61E-01		-8.69E+00		-8.69E-06

		-1.10E-01		-3.90E+00		-3.90E-06		2.65E-01		-8.64E+00		-8.64E-06

		-1.06E-01		-4.12E+00		-4.12E-06		2.69E-01		-8.63E+00		-8.63E-06

		-1.02E-01		-4.25E+00		-4.25E-06		2.73E-01		-8.52E+00		-8.52E-06

		-9.80E-02		-4.44E+00		-4.44E-06		2.77E-01		-8.52E+00		-8.52E-06

		-9.40E-02		-4.64E+00		-4.64E-06		2.81E-01		-8.43E+00		-8.43E-06

		-9.00E-02		-4.83E+00		-4.83E-06		2.85E-01		-8.39E+00		-8.39E-06

		-8.60E-02		-5.02E+00		-5.02E-06		2.89E-01		-8.38E+00		-8.38E-06

		-8.20E-02		-5.29E+00		-5.29E-06		2.93E-01		-8.32E+00		-8.32E-06

		-7.80E-02		-5.54E+00		-5.54E-06		2.97E-01		-8.29E+00		-8.29E-06

		-7.40E-02		-5.78E+00		-5.78E-06		3.01E-01		-8.21E+00		-8.21E-06

		-7.00E-02		-6.00E+00		-6.00E-06		3.05E-01		-8.21E+00		-8.21E-06

		-6.60E-02		-6.30E+00		-6.30E-06		3.09E-01		-8.16E+00		-8.16E-06

		-6.20E-02		-6.55E+00		-6.55E-06		3.13E-01		-8.12E+00		-8.12E-06

		-5.80E-02		-6.83E+00		-6.83E-06		3.17E-01		-8.07E+00		-8.07E-06

		-5.40E-02		-7.18E+00		-7.18E-06		3.21E-01		-8.02E+00		-8.02E-06

		-5.00E-02		-7.49E+00		-7.49E-06		3.25E-01		-7.98E+00		-7.98E-06

		-4.60E-02		-7.81E+00		-7.81E-06		3.29E-01		-7.95E+00		-7.95E-06

		-4.20E-02		-8.07E+00		-8.07E-06		3.33E-01		-7.88E+00		-7.88E-06

		-3.80E-02		-8.40E+00		-8.40E-06		3.37E-01		-7.88E+00		-7.88E-06

		-3.40E-02		-8.79E+00		-8.79E-06		3.41E-01		-7.82E+00		-7.82E-06

		-3.00E-02		-9.09E+00		-9.09E-06		3.45E-01		-7.78E+00		-7.78E-06

		-2.60E-02		-9.42E+00		-9.42E-06		3.49E-01		-7.75E+00		-7.75E-06

		-2.20E-02		-9.78E+00		-9.78E-06		3.53E-01		-7.67E+00		-7.67E-06

		-1.80E-02		-1.01E+01		-1.01E-05		3.57E-01		-7.63E+00		-7.63E-06

		-1.40E-02		-1.05E+01		-1.05E-05		3.61E-01		-7.62E+00		-7.62E-06

		-1.00E-02		-1.08E+01		-1.08E-05		3.65E-01		-7.55E+00		-7.55E-06

		-6.01E-03		-1.11E+01		-1.11E-05		3.69E-01		-7.55E+00		-7.55E-06

		-2.01E-03		-1.15E+01		-1.15E-05		3.73E-01		-7.46E+00		-7.46E-06

		1.99E-03		-1.17E+01		-1.17E-05		3.77E-01		-7.47E+00		-7.47E-06

		5.99E-03		-1.21E+01		-1.21E-05		3.81E-01		-7.38E+00		-7.38E-06

		9.99E-03		-1.24E+01		-1.24E-05		3.85E-01		-7.37E+00		-7.37E-06

		1.40E-02		-1.27E+01		-1.27E-05		3.89E-01		-7.33E+00		-7.33E-06

		1.80E-02		-1.30E+01		-1.30E-05		3.93E-01		-7.30E+00		-7.30E-06

		2.20E-02		-1.32E+01		-1.32E-05		3.97E-01		-7.23E+00		-7.23E-06

		2.60E-02		-1.35E+01		-1.35E-05		4.01E-01		-7.22E+00		-7.22E-06

		3.00E-02		-1.37E+01		-1.37E-05		4.05E-01		-7.14E+00		-7.14E-06

		3.40E-02		-1.39E+01		-1.39E-05		4.09E-01		-7.16E+00		-7.16E-06

		3.80E-02		-1.42E+01		-1.42E-05		4.13E-01		-7.07E+00		-7.07E-06

		4.20E-02		-1.43E+01		-1.43E-05		4.17E-01		-7.08E+00		-7.08E-06

		4.60E-02		-1.46E+01		-1.46E-05		4.21E-01		-7.03E+00		-7.03E-06

		5.00E-02		-1.47E+01		-1.47E-05		4.25E-01		-6.98E+00		-6.98E-06

		5.40E-02		-1.48E+01		-1.48E-05		4.29E-01		-6.94E+00		-6.94E-06

		5.80E-02		-1.49E+01		-1.49E-05		4.33E-01		-6.93E+00		-6.93E-06

		6.20E-02		-1.50E+01		-1.50E-05		4.37E-01		-6.87E+00		-6.87E-06

		6.60E-02		-1.52E+01		-1.52E-05		4.41E-01		-6.86E+00		-6.86E-06

		7.00E-02		-1.53E+01		-1.53E-05		4.45E-01		-6.80E+00		-6.80E-06

		7.40E-02		-1.53E+01		-1.53E-05		4.49E-01		-6.79E+00		-6.79E-06

		7.80E-02		-1.53E+01		-1.53E-05		4.53E-01		-6.72E+00		-6.72E-06

		8.20E-02		-1.53E+01		-1.53E-05		4.57E-01		-6.68E+00		-6.68E-06

		8.60E-02		-1.54E+01		-1.54E-05		4.61E-01		-6.69E+00		-6.69E-06

		9.00E-02		-1.54E+01		-1.54E-05		4.65E-01		-6.58E+00		-6.58E-06

		9.40E-02		-1.54E+01		-1.54E-05		4.69E-01		-6.63E+00		-6.63E-06

		9.80E-02		-1.54E+01		-1.54E-05		4.73E-01		-6.56E+00		-6.56E-06

		1.02E-01		-1.54E+01		-1.54E-05		4.77E-01		-6.54E+00		-6.54E-06

		1.06E-01		-1.54E+01		-1.54E-05		4.81E-01		-6.47E+00		-6.47E-06

		1.10E-01		-1.54E+01		-1.54E-05		4.85E-01		-6.45E+00		-6.45E-06

		1.14E-01		-1.53E+01		-1.53E-05		4.89E-01		-6.46E+00		-6.46E-06

		1.18E-01		-1.52E+01		-1.52E-05		4.93E-01		-6.42E+00		-6.42E-06

		1.22E-01		-1.52E+01		-1.52E-05		4.97E-01		-6.41E+00		-6.41E-06

		1.26E-01		-1.53E+01		-1.53E-05		5.01E-01		-6.40E+00		-6.40E-06

		1.30E-01		-1.51E+01		-1.51E-05		5.05E-01		-6.33E+00		-6.33E-06

		1.34E-01		-1.51E+01		-1.51E-05		5.09E-01		-6.35E+00		-6.35E-06

		1.38E-01		-1.50E+01		-1.50E-05		5.13E-01		-6.31E+00		-6.31E-06

		1.42E-01		-1.49E+01		-1.49E-05		5.17E-01		-6.31E+00		-6.31E-06

		1.46E-01		-1.49E+01		-1.49E-05		5.21E-01		-6.29E+00		-6.29E-06

		1.50E-01		-1.48E+01		-1.48E-05		5.25E-01		-6.20E+00		-6.20E-06

		1.54E-01		-1.48E+01		-1.48E-05		5.29E-01		-6.24E+00		-6.24E-06

		1.58E-01		-1.47E+01		-1.47E-05		5.33E-01		-6.18E+00		-6.18E-06

		1.62E-01		-1.46E+01		-1.46E-05		5.37E-01		-6.17E+00		-6.17E-06

		1.66E-01		-1.46E+01		-1.46E-05		5.41E-01		-6.15E+00		-6.15E-06

		1.70E-01		-1.45E+01		-1.45E-05		5.45E-01		-6.13E+00		-6.13E-06

		1.74E-01		-1.45E+01		-1.45E-05		5.49E-01		-6.11E+00		-6.11E-06

		1.78E-01		-1.44E+01		-1.44E-05		5.53E-01		-6.08E+00		-6.08E-06

		1.82E-01		-1.43E+01		-1.43E-05		5.57E-01		-6.07E+00		-6.07E-06

		1.86E-01		-1.42E+01		-1.42E-05		5.61E-01		-6.06E+00		-6.06E-06

		1.90E-01		-1.41E+01		-1.41E-05		5.65E-01		-5.98E+00		-5.98E-06

		1.94E-01		-1.41E+01		-1.41E-05		5.69E-01		-6.04E+00		-6.04E-06

		1.98E-01		-1.41E+01		-1.41E-05		5.73E-01		-6.00E+00		-6.00E-06

		2.02E-01		-1.40E+01		-1.40E-05		5.77E-01		-5.97E+00		-5.97E-06

		2.06E-01		-1.39E+01		-1.39E-05		5.81E-01		-5.98E+00		-5.98E-06

		2.10E-01		-1.39E+01		-1.39E-05		5.85E-01		-5.94E+00		-5.94E-06

		2.14E-01		-1.37E+01		-1.37E-05		5.89E-01		-5.96E+00		-5.96E-06

		2.18E-01		-1.37E+01		-1.37E-05		5.93E-01		-5.93E+00		-5.93E-06

		2.22E-01		-1.37E+01		-1.37E-05		5.97E-01		-5.89E+00		-5.89E-06

		2.26E-01		-1.36E+01		-1.36E-05		6.01E-01		-5.94E+00		-5.94E-06

		2.30E-01		-1.35E+01		-1.35E-05		6.05E-01		-5.89E+00		-5.89E-06

		2.34E-01		-1.35E+01		-1.35E-05		6.09E-01		-5.93E+00		-5.93E-06

		2.38E-01		-1.35E+01		-1.35E-05		6.13E-01		-5.88E+00		-5.88E-06

		2.42E-01		-1.34E+01		-1.34E-05		6.17E-01		-5.89E+00		-5.89E-06

		2.46E-01		-1.33E+01		-1.33E-05		6.21E-01		-5.89E+00		-5.89E-06

		2.50E-01		-1.33E+01		-1.33E-05		6.25E-01		-5.84E+00		-5.84E-06

		2.54E-01		-1.32E+01		-1.32E-05		6.29E-01		-5.85E+00		-5.85E-06

		2.58E-01		-1.32E+01		-1.32E-05		6.33E-01		-5.86E+00		-5.86E-06

		2.62E-01		-1.32E+01		-1.32E-05		6.37E-01		-5.86E+00		-5.86E-06

		2.66E-01		-1.31E+01		-1.31E-05		6.41E-01		-5.87E+00		-5.87E-06

		2.70E-01		-1.30E+01		-1.30E-05		6.45E-01		-5.84E+00		-5.84E-06

		2.74E-01		-1.30E+01		-1.30E-05		6.49E-01		-5.87E+00		-5.87E-06

		2.78E-01		-1.30E+01		-1.30E-05		6.53E-01		-5.84E+00		-5.84E-06

		2.82E-01		-1.29E+01		-1.29E-05		6.57E-01		-5.82E+00		-5.82E-06

		2.86E-01		-1.29E+01		-1.29E-05		6.61E-01		-5.88E+00		-5.88E-06

		2.90E-01		-1.28E+01		-1.28E-05		6.65E-01		-5.84E+00		-5.84E-06

		2.94E-01		-1.28E+01		-1.28E-05		6.69E-01		-5.91E+00		-5.91E-06

		2.98E-01		-1.28E+01		-1.28E-05		6.73E-01		-5.88E+00		-5.88E-06

		3.02E-01		-1.28E+01		-1.28E-05		6.77E-01		-5.90E+00		-5.90E-06

		3.06E-01		-1.27E+01		-1.27E-05		6.81E-01		-5.88E+00		-5.88E-06

		3.10E-01		-1.26E+01		-1.26E-05		6.85E-01		-5.88E+00		-5.88E-06

		3.14E-01		-1.26E+01		-1.26E-05		6.89E-01		-5.91E+00		-5.91E-06

		3.18E-01		-1.25E+01		-1.25E-05		6.93E-01		-5.95E+00		-5.95E-06

		3.22E-01		-1.25E+01		-1.25E-05		6.97E-01		-5.89E+00		-5.89E-06

		3.26E-01		-1.24E+01		-1.24E-05		7.01E-01		-5.94E+00		-5.94E-06

		3.30E-01		-1.24E+01		-1.24E-05		7.05E-01		-5.93E+00		-5.93E-06

		3.34E-01		-1.24E+01		-1.24E-05		7.09E-01		-5.99E+00		-5.99E-06

		3.38E-01		-1.23E+01		-1.23E-05		7.13E-01		-5.96E+00		-5.96E-06

		3.42E-01		-1.23E+01		-1.23E-05		7.17E-01		-5.98E+00		-5.98E-06

		3.46E-01		-1.22E+01		-1.22E-05		7.21E-01		-5.94E+00		-5.94E-06

		3.50E-01		-1.22E+01		-1.22E-05		7.25E-01		-6.02E+00		-6.02E-06

		3.54E-01		-1.22E+01		-1.22E-05		7.29E-01		-6.01E+00		-6.01E-06

		3.58E-01		-1.22E+01		-1.22E-05		7.33E-01		-6.05E+00		-6.05E-06

		3.62E-01		-1.21E+01		-1.21E-05		7.37E-01		-6.01E+00		-6.01E-06

		3.66E-01		-1.20E+01		-1.20E-05		7.41E-01		-6.09E+00		-6.09E-06

		3.70E-01		-1.20E+01		-1.20E-05		7.45E-01		-6.04E+00		-6.04E-06

		3.74E-01		-1.20E+01		-1.20E-05		7.49E-01		-6.12E+00		-6.12E-06

		3.78E-01		-1.19E+01		-1.19E-05		7.53E-01		-6.07E+00		-6.07E-06

		3.82E-01		-1.19E+01		-1.19E-05		7.57E-01		-6.10E+00		-6.10E-06

		3.86E-01		-1.19E+01		-1.19E-05		7.61E-01		-6.10E+00		-6.10E-06

		3.90E-01		-1.18E+01		-1.18E-05		7.65E-01		-6.13E+00		-6.13E-06

		3.94E-01		-1.17E+01		-1.17E-05		7.69E-01		-6.17E+00		-6.17E-06

		3.98E-01		-1.17E+01		-1.17E-05		7.73E-01		-6.12E+00		-6.12E-06

		4.02E-01		-1.17E+01		-1.17E-05		7.77E-01		-6.16E+00		-6.16E-06

		4.06E-01		-1.16E+01		-1.16E-05		7.81E-01		-6.17E+00		-6.17E-06

		4.10E-01		-1.16E+01		-1.16E-05		7.85E-01		-6.21E+00		-6.21E-06

		4.14E-01		-1.16E+01		-1.16E-05		7.89E-01		-6.21E+00		-6.21E-06

		4.18E-01		-1.16E+01		-1.16E-05		7.93E-01		-6.22E+00		-6.22E-06

		4.22E-01		-1.15E+01		-1.15E-05		7.97E-01		-6.19E+00		-6.19E-06

		4.26E-01		-1.14E+01		-1.14E-05		8.01E-01		-6.22E+00		-6.22E-06

		4.30E-01		-1.14E+01		-1.14E-05		8.05E-01		-6.26E+00		-6.26E-06

		4.34E-01		-1.14E+01		-1.14E-05		8.09E-01		-6.29E+00		-6.29E-06

		4.38E-01		-1.14E+01		-1.14E-05		8.13E-01		-6.30E+00		-6.30E-06

		4.42E-01		-1.14E+01		-1.14E-05		8.17E-01		-6.30E+00		-6.30E-06

		4.46E-01		-1.13E+01		-1.13E-05		8.21E-01		-6.36E+00		-6.36E-06

		4.50E-01		-1.13E+01		-1.13E-05		8.25E-01		-6.35E+00		-6.35E-06

		4.54E-01		-1.13E+01		-1.13E-05		8.29E-01		-6.41E+00		-6.41E-06

		4.58E-01		-1.12E+01		-1.12E-05		8.33E-01		-6.38E+00		-6.38E-06

		4.62E-01		-1.12E+01		-1.12E-05		8.37E-01		-6.45E+00		-6.45E-06

		4.66E-01		-1.11E+01		-1.11E-05		8.41E-01		-6.42E+00		-6.42E-06

		4.70E-01		-1.11E+01		-1.11E-05		8.45E-01		-6.51E+00		-6.51E-06

		4.74E-01		-1.11E+01		-1.11E-05		8.49E-01		-6.55E+00		-6.55E-06

		4.78E-01		-1.11E+01		-1.11E-05		8.53E-01		-6.55E+00		-6.55E-06

		4.82E-01		-1.10E+01		-1.10E-05		8.57E-01		-6.58E+00		-6.58E-06

		4.86E-01		-1.10E+01		-1.10E-05		8.61E-01		-6.64E+00		-6.64E-06

		4.90E-01		-1.10E+01		-1.10E-05		8.65E-01		-6.73E+00		-6.73E-06

		4.94E-01		-1.10E+01		-1.10E-05		8.69E-01		-6.76E+00		-6.76E-06

		4.98E-01		-1.10E+01		-1.10E-05		8.73E-01		-6.80E+00		-6.80E-06

		5.02E-01		-1.08E+01		-1.08E-05		8.77E-01		-6.86E+00		-6.86E-06

		5.06E-01		-1.09E+01		-1.09E-05		8.81E-01		-6.94E+00		-6.94E-06

		5.10E-01		-1.08E+01		-1.08E-05		8.85E-01		-7.05E+00		-7.05E-06

		5.14E-01		-1.09E+01		-1.09E-05		8.89E-01		-7.11E+00		-7.11E-06

		5.18E-01		-1.08E+01		-1.08E-05		8.93E-01		-7.19E+00		-7.19E-06

		5.22E-01		-1.08E+01		-1.08E-05		8.97E-01		-7.28E+00		-7.28E-06

		5.26E-01		-1.07E+01		-1.07E-05		9.01E-01		-7.36E+00		-7.36E-06

		5.30E-01		-1.07E+01		-1.07E-05		9.05E-01		-7.51E+00		-7.51E-06

		5.34E-01		-1.08E+01		-1.08E-05		9.09E-01		-7.64E+00		-7.64E-06

		5.38E-01		-1.07E+01		-1.07E-05		9.13E-01		-7.71E+00		-7.71E-06

		5.42E-01		-1.07E+01		-1.07E-05		9.17E-01		-7.85E+00		-7.85E-06

		5.46E-01		-1.06E+01		-1.06E-05		9.21E-01		-7.98E+00		-7.98E-06

		5.50E-01		-1.06E+01		-1.06E-05		9.25E-01		-8.16E+00		-8.16E-06

		5.54E-01		-1.07E+01		-1.07E-05		9.29E-01		-8.34E+00		-8.34E-06

		5.58E-01		-1.06E+01		-1.06E-05		9.33E-01		-8.44E+00		-8.44E-06

		5.62E-01		-1.06E+01		-1.06E-05		9.37E-01		-8.59E+00		-8.59E-06

		5.66E-01		-1.06E+01		-1.06E-05		9.41E-01		-8.77E+00		-8.77E-06

		5.70E-01		-1.06E+01		-1.06E-05		9.45E-01		-9.03E+00		-9.03E-06

		5.74E-01		-1.06E+01		-1.06E-05		9.49E-01		-9.15E+00		-9.15E-06

		5.78E-01		-1.05E+01		-1.05E-05		9.53E-01		-9.34E+00		-9.34E-06

		5.82E-01		-1.05E+01		-1.05E-05		9.57E-01		-9.54E+00		-9.54E-06

		5.86E-01		-1.05E+01		-1.05E-05		9.61E-01		-9.77E+00		-9.77E-06

		5.90E-01		-1.05E+01		-1.05E-05		9.65E-01		-1.01E+01		-1.01E-05

		5.94E-01		-1.05E+01		-1.05E-05		9.69E-01		-1.03E+01		-1.03E-05

		5.98E-01		-1.05E+01		-1.05E-05		9.73E-01		-1.05E+01		-1.05E-05

		6.02E-01		-1.05E+01		-1.05E-05		9.77E-01		-1.09E+01		-1.09E-05

		6.06E-01		-1.05E+01		-1.05E-05		9.81E-01		-1.10E+01		-1.10E-05

		6.10E-01		-1.05E+01		-1.05E-05		9.85E-01		-1.16E+01		-1.16E-05

		6.14E-01		-1.06E+01		-1.06E-05		9.89E-01		-1.18E+01		-1.18E-05

		6.18E-01		-1.06E+01		-1.06E-05		9.93E-01		-1.21E+01		-1.21E-05

		6.22E-01		-1.06E+01		-1.06E-05		9.97E-01		-1.24E+01		-1.24E-05

		6.26E-01		-1.05E+01		-1.05E-05		1.00E+00		-1.29E+01		-1.29E-05

		6.30E-01		-1.05E+01		-1.05E-05		1.01E+00		-1.34E+01		-1.34E-05

		6.34E-01		-1.06E+01		-1.06E-05		1.01E+00		-1.38E+01		-1.38E-05

		6.38E-01		-1.06E+01		-1.06E-05		1.01E+00		-1.42E+01		-1.42E-05

		6.42E-01		-1.06E+01		-1.06E-05		1.02E+00		-1.47E+01		-1.47E-05

		6.46E-01		-1.06E+01		-1.06E-05		1.02E+00		-1.51E+01		-1.51E-05

		6.50E-01		-1.06E+01		-1.06E-05		1.03E+00		-1.59E+01		-1.59E-05

		6.54E-01		-1.07E+01		-1.07E-05		1.03E+00		-1.63E+01		-1.63E-05

		6.58E-01		-1.07E+01		-1.07E-05		1.03E+00		-1.69E+01		-1.69E-05

		6.62E-01		-1.07E+01		-1.07E-05		1.04E+00		-1.73E+01		-1.73E-05

		6.66E-01		-1.07E+01		-1.07E-05		1.04E+00		-1.79E+01		-1.79E-05

		6.70E-01		-1.07E+01		-1.07E-05		1.05E+00		-1.87E+01		-1.87E-05

		6.74E-01		-1.08E+01		-1.08E-05		1.05E+00		-1.91E+01		-1.91E-05

		6.78E-01		-1.08E+01		-1.08E-05		1.05E+00		-1.98E+01		-1.98E-05

		6.82E-01		-1.08E+01		-1.08E-05		1.06E+00		-2.04E+01		-2.04E-05

		6.86E-01		-1.08E+01		-1.08E-05		1.06E+00		-2.08E+01		-2.08E-05

		6.90E-01		-1.09E+01		-1.09E-05		1.07E+00		-2.17E+01		-2.17E-05

		6.94E-01		-1.09E+01		-1.09E-05		1.07E+00		-2.21E+01		-2.21E-05

		6.98E-01		-1.09E+01		-1.09E-05		1.07E+00		-2.27E+01		-2.27E-05

		7.02E-01		-1.10E+01		-1.10E-05		1.08E+00		-2.31E+01		-2.31E-05

		7.06E-01		-1.10E+01		-1.10E-05		1.08E+00		-2.36E+01		-2.36E-05

		7.10E-01		-1.10E+01		-1.10E-05		1.09E+00		-2.41E+01		-2.41E-05

		7.14E-01		-1.10E+01		-1.10E-05		1.09E+00		-2.44E+01		-2.44E-05

		7.18E-01		-1.10E+01		-1.10E-05		1.09E+00		-2.48E+01		-2.48E-05

		7.22E-01		-1.11E+01		-1.11E-05		1.10E+00		-2.54E+01		-2.54E-05

		7.26E-01		-1.11E+01		-1.11E-05		1.10E+00		-2.54E+01		-2.54E-05

		7.30E-01		-1.11E+01		-1.11E-05		1.11E+00		-2.61E+01		-2.61E-05

		7.34E-01		-1.12E+01		-1.12E-05		1.11E+00		-2.58E+01		-2.58E-05

		7.38E-01		-1.12E+01		-1.12E-05		1.11E+00		-2.63E+01		-2.63E-05

		7.42E-01		-1.12E+01		-1.12E-05		1.12E+00		-2.63E+01		-2.63E-05

		7.46E-01		-1.12E+01		-1.12E-05		1.12E+00		-2.65E+01		-2.65E-05

		7.50E-01		-1.12E+01		-1.12E-05		1.13E+00		-2.69E+01		-2.69E-05

		7.54E-01		-1.13E+01		-1.13E-05		1.13E+00		-2.68E+01		-2.68E-05

		7.58E-01		-1.13E+01		-1.13E-05		1.13E+00		-2.70E+01		-2.70E-05

		7.62E-01		-1.13E+01		-1.13E-05		1.14E+00		-2.71E+01		-2.71E-05

		7.66E-01		-1.14E+01		-1.14E-05		1.14E+00		-2.73E+01		-2.73E-05

		7.70E-01		-1.13E+01		-1.13E-05		1.15E+00		-2.73E+01		-2.73E-05

		7.74E-01		-1.15E+01		-1.15E-05		1.15E+00		-2.73E+01		-2.73E-05

		7.78E-01		-1.14E+01		-1.14E-05		1.15E+00		-2.73E+01		-2.73E-05

		7.82E-01		-1.14E+01		-1.14E-05		1.16E+00		-2.74E+01		-2.74E-05

		7.86E-01		-1.14E+01		-1.14E-05		1.16E+00		-2.74E+01		-2.74E-05

		7.90E-01		-1.14E+01		-1.14E-05		1.17E+00		-2.73E+01		-2.73E-05

		7.94E-01		-1.15E+01		-1.15E-05		1.17E+00		-2.73E+01		-2.73E-05

		7.98E-01		-1.15E+01		-1.15E-05		1.17E+00		-2.71E+01		-2.71E-05

		8.02E-01		-1.15E+01		-1.15E-05		1.18E+00		-2.73E+01		-2.73E-05

		8.06E-01		-1.16E+01		-1.16E-05		1.18E+00		-2.70E+01		-2.70E-05

		8.10E-01		-1.15E+01		-1.15E-05		1.19E+00		-2.72E+01		-2.72E-05

		8.14E-01		-1.16E+01		-1.16E-05		1.19E+00		-2.69E+01		-2.69E-05

		8.18E-01		-1.16E+01		-1.16E-05		1.19E+00		-2.69E+01		-2.69E-05

		8.22E-01		-1.17E+01		-1.17E-05		1.20E+00		-2.66E+01		-2.66E-05

		8.26E-01		-1.17E+01		-1.17E-05		1.20E+00		-2.66E+01		-2.66E-05

		8.30E-01		-1.17E+01		-1.17E-05		1.21E+00		-2.64E+01		-2.64E-05

		8.34E-01		-1.17E+01		-1.17E-05		1.21E+00		-2.62E+01		-2.62E-05

		8.38E-01		-1.18E+01		-1.18E-05		1.21E+00		-2.60E+01		-2.60E-05

		8.42E-01		-1.18E+01		-1.18E-05		1.22E+00		-2.58E+01		-2.58E-05

		8.46E-01		-1.18E+01		-1.18E-05		1.22E+00		-2.57E+01		-2.57E-05

		8.50E-01		-1.19E+01		-1.19E-05		1.23E+00		-2.54E+01		-2.54E-05

		8.54E-01		-1.19E+01		-1.19E-05		1.23E+00		-2.54E+01		-2.54E-05

		8.58E-01		-1.19E+01		-1.19E-05		1.23E+00		-2.51E+01		-2.51E-05

		8.62E-01		-1.20E+01		-1.20E-05		1.24E+00		-2.50E+01		-2.50E-05

		8.66E-01		-1.21E+01		-1.21E-05		1.24E+00		-2.47E+01		-2.47E-05

		8.70E-01		-1.21E+01		-1.21E-05		1.25E+00		-2.46E+01		-2.46E-05

		8.74E-01		-1.22E+01		-1.22E-05		1.25E+00		-2.45E+01		-2.45E-05

		8.78E-01		-1.23E+01		-1.23E-05		1.25E+00		-2.42E+01		-2.42E-05

		8.82E-01		-1.23E+01		-1.23E-05		1.26E+00		-2.40E+01		-2.40E-05

		8.86E-01		-1.24E+01		-1.24E-05		1.26E+00		-2.39E+01		-2.39E-05

		8.90E-01		-1.24E+01		-1.24E-05		1.27E+00		-2.37E+01		-2.37E-05

		8.94E-01		-1.26E+01		-1.26E-05		1.27E+00		-2.34E+01		-2.34E-05

		8.98E-01		-1.27E+01		-1.27E-05		1.27E+00		-2.32E+01		-2.32E-05

		9.02E-01		-1.28E+01		-1.28E-05		1.28E+00		-2.30E+01		-2.30E-05

		9.06E-01		-1.28E+01		-1.28E-05		1.28E+00		-2.30E+01		-2.30E-05

		9.10E-01		-1.29E+01		-1.29E-05		1.29E+00		-2.26E+01		-2.26E-05

		9.14E-01		-1.31E+01		-1.31E-05		1.29E+00		-2.25E+01		-2.25E-05

		9.18E-01		-1.32E+01		-1.32E-05		1.29E+00		-2.22E+01		-2.22E-05

		9.22E-01		-1.33E+01		-1.33E-05		1.30E+00		-2.19E+01		-2.19E-05

		9.26E-01		-1.35E+01		-1.35E-05		1.30E+00		-2.18E+01		-2.18E-05

		9.30E-01		-1.36E+01		-1.36E-05		1.31E+00		-2.16E+01		-2.16E-05

		9.34E-01		-1.38E+01		-1.38E-05		1.31E+00		-2.14E+01		-2.14E-05

		9.38E-01		-1.39E+01		-1.39E-05		1.31E+00		-2.12E+01		-2.12E-05

		9.42E-01		-1.41E+01		-1.41E-05		1.32E+00		-2.11E+01		-2.11E-05

		9.46E-01		-1.42E+01		-1.42E-05		1.32E+00		-2.08E+01		-2.08E-05

		9.50E-01		-1.44E+01		-1.44E-05		1.33E+00		-2.06E+01		-2.06E-05

		9.54E-01		-1.46E+01		-1.46E-05		1.33E+00		-2.05E+01		-2.05E-05

		9.58E-01		-1.48E+01		-1.48E-05		1.33E+00		-2.03E+01		-2.03E-05

		9.62E-01		-1.50E+01		-1.50E-05		1.34E+00		-2.01E+01		-2.01E-05

		9.66E-01		-1.52E+01		-1.52E-05		1.34E+00		-1.99E+01		-1.99E-05

		9.70E-01		-1.55E+01		-1.55E-05		1.35E+00		-1.96E+01		-1.96E-05

		9.74E-01		-1.57E+01		-1.57E-05		1.35E+00		-1.96E+01		-1.96E-05

		9.78E-01		-1.60E+01		-1.60E-05		1.35E+00		-1.95E+01		-1.95E-05

		9.82E-01		-1.63E+01		-1.63E-05		1.36E+00		-1.92E+01		-1.92E-05

		9.86E-01		-1.65E+01		-1.65E-05		1.36E+00		-1.91E+01		-1.91E-05

		9.90E-01		-1.68E+01		-1.68E-05		1.37E+00		-1.88E+01		-1.88E-05

		9.94E-01		-1.73E+01		-1.73E-05		1.37E+00		-1.88E+01		-1.88E-05

		9.98E-01		-1.75E+01		-1.75E-05		1.37E+00		-1.87E+01		-1.87E-05

		1.00E+00		-1.78E+01		-1.78E-05		1.38E+00		-1.85E+01		-1.85E-05

		1.01E+00		-1.83E+01		-1.83E-05		1.38E+00		-1.85E+01		-1.85E-05

		1.01E+00		-1.89E+01		-1.89E-05		1.39E+00		-1.82E+01		-1.82E-05

		1.01E+00		-1.95E+01		-1.95E-05		1.39E+00		-1.83E+01		-1.83E-05

		1.02E+00		-2.00E+01		-2.00E-05		1.39E+00		-1.79E+01		-1.79E-05

		1.02E+00		-2.04E+01		-2.04E-05		1.40E+00		-1.81E+01		-1.81E-05

		1.03E+00		-2.10E+01		-2.10E-05		1.40E+00		-1.78E+01		-1.78E-05

		1.03E+00		-2.14E+01		-2.14E-05		1.41E+00		-1.76E+01		-1.76E-05

		1.03E+00		-2.20E+01		-2.20E-05		1.41E+00		-1.76E+01		-1.76E-05

		1.04E+00		-2.29E+01		-2.29E-05		1.41E+00		-1.76E+01		-1.76E-05

		1.04E+00		-2.38E+01		-2.38E-05		1.42E+00		-1.74E+01		-1.74E-05

		1.05E+00		-2.41E+01		-2.41E-05		1.42E+00		-1.72E+01		-1.72E-05

		1.05E+00		-2.52E+01		-2.52E-05		1.43E+00		-1.72E+01		-1.72E-05

		1.05E+00		-2.55E+01		-2.55E-05		1.43E+00		-1.70E+01		-1.70E-05

		1.06E+00		-2.60E+01		-2.60E-05		1.43E+00		-1.69E+01		-1.69E-05

		1.06E+00		-2.68E+01		-2.68E-05		1.44E+00		-1.66E+01		-1.66E-05

		1.07E+00		-2.74E+01		-2.74E-05		1.44E+00		-1.66E+01		-1.66E-05

		1.07E+00		-2.80E+01		-2.80E-05		1.45E+00		-1.62E+01		-1.62E-05

		1.07E+00		-2.84E+01		-2.84E-05		1.45E+00		-1.65E+01		-1.65E-05

		1.08E+00		-2.92E+01		-2.92E-05		1.45E+00		-1.62E+01		-1.62E-05

		1.08E+00		-2.95E+01		-2.95E-05		1.46E+00		-1.62E+01		-1.62E-05

		1.09E+00		-2.97E+01		-2.97E-05		1.46E+00		-1.62E+01		-1.62E-05

		1.09E+00		-3.04E+01		-3.04E-05		1.47E+00		-1.60E+01		-1.60E-05

		1.09E+00		-3.05E+01		-3.05E-05		1.47E+00		-1.59E+01		-1.59E-05

		1.10E+00		-3.08E+01		-3.08E-05		1.47E+00		-1.58E+01		-1.58E-05

		1.10E+00		-3.11E+01		-3.11E-05		1.48E+00		-1.59E+01		-1.59E-05

		1.11E+00		-3.12E+01		-3.12E-05		1.48E+00		-1.57E+01		-1.57E-05

		1.11E+00		-3.15E+01		-3.15E-05		1.49E+00		-1.56E+01		-1.56E-05

		1.11E+00		-3.15E+01		-3.15E-05		1.49E+00		-1.55E+01		-1.55E-05

		1.12E+00		-3.22E+01		-3.22E-05		1.49E+00		-1.54E+01		-1.54E-05

		1.12E+00		-3.19E+01		-3.19E-05		1.50E+00		-1.54E+01		-1.54E-05

		1.13E+00		-3.19E+01		-3.19E-05		1.50E+00		-1.53E+01		-1.53E-05

		1.13E+00		-3.22E+01		-3.22E-05		1.51E+00		-1.54E+01		-1.54E-05

		1.13E+00		-3.23E+01		-3.23E-05		1.51E+00		-1.53E+01		-1.53E-05

		1.14E+00		-3.23E+01		-3.23E-05		1.51E+00		-1.51E+01		-1.51E-05

		1.14E+00		-3.24E+01		-3.24E-05		1.52E+00		-1.50E+01		-1.50E-05

		1.15E+00		-3.25E+01		-3.25E-05		1.52E+00		-1.51E+01		-1.51E-05

		1.15E+00		-3.27E+01		-3.27E-05		1.53E+00		-1.50E+01		-1.50E-05

		1.15E+00		-3.26E+01		-3.26E-05		1.53E+00		-1.50E+01		-1.50E-05

		1.16E+00		-3.26E+01		-3.26E-05		1.53E+00		-1.49E+01		-1.49E-05

		1.16E+00		-3.27E+01		-3.27E-05		1.54E+00		-1.49E+01		-1.49E-05

		1.17E+00		-3.28E+01		-3.28E-05		1.54E+00		-1.48E+01		-1.48E-05

		1.17E+00		-3.27E+01		-3.27E-05		1.55E+00		-1.47E+01		-1.47E-05

		1.17E+00		-3.28E+01		-3.28E-05		1.55E+00		-1.48E+01		-1.48E-05

		1.18E+00		-3.28E+01		-3.28E-05		1.55E+00		-1.47E+01		-1.47E-05

		1.18E+00		-3.28E+01		-3.28E-05		1.56E+00		-1.47E+01		-1.47E-05

		1.19E+00		-3.29E+01		-3.29E-05		1.56E+00		-1.46E+01		-1.46E-05

		1.19E+00		-3.27E+01		-3.27E-05		1.57E+00		-1.46E+01		-1.46E-05

		1.19E+00		-3.29E+01		-3.29E-05		1.57E+00		-1.46E+01		-1.46E-05

		1.20E+00		-3.27E+01		-3.27E-05		1.57E+00		-1.45E+01		-1.45E-05

		1.20E+00		-3.26E+01		-3.26E-05		1.58E+00		-1.45E+01		-1.45E-05

		1.21E+00		-3.25E+01		-3.25E-05		1.58E+00		-1.45E+01		-1.45E-05

		1.21E+00		-3.25E+01		-3.25E-05		1.59E+00		-1.44E+01		-1.44E-05

		1.21E+00		-3.25E+01		-3.25E-05		1.59E+00		-1.45E+01		-1.45E-05

		1.22E+00		-3.24E+01		-3.24E-05		1.59E+00		-1.44E+01		-1.44E-05

		1.22E+00		-3.20E+01		-3.20E-05		1.60E+00		-1.44E+01		-1.44E-05

		1.23E+00		-3.22E+01		-3.22E-05		1.60E+00		-1.44E+01		-1.44E-05

		1.23E+00		-3.20E+01		-3.20E-05		1.61E+00		-1.43E+01		-1.43E-05

		1.23E+00		-3.18E+01		-3.18E-05		1.61E+00		-1.44E+01		-1.44E-05

		1.24E+00		-3.18E+01		-3.18E-05		1.61E+00		-1.43E+01		-1.43E-05

		1.24E+00		-3.14E+01		-3.14E-05		1.62E+00		-1.44E+01		-1.44E-05

		1.25E+00		-3.15E+01		-3.15E-05		1.62E+00		-1.43E+01		-1.43E-05

		1.25E+00		-3.13E+01		-3.13E-05		1.63E+00		-1.43E+01		-1.43E-05

		1.25E+00		-3.11E+01		-3.11E-05		1.63E+00		-1.44E+01		-1.44E-05

		1.26E+00		-3.09E+01		-3.09E-05		1.63E+00		-1.43E+01		-1.43E-05

		1.26E+00		-3.10E+01		-3.10E-05		1.64E+00		-1.43E+01		-1.43E-05

		1.27E+00		-3.04E+01		-3.04E-05		1.64E+00		-1.44E+01		-1.44E-05

		1.27E+00		-3.04E+01		-3.04E-05		1.65E+00		-1.43E+01		-1.43E-05

		1.27E+00		-3.05E+01		-3.05E-05		1.65E+00		-1.45E+01		-1.45E-05

		1.28E+00		-3.00E+01		-3.00E-05		1.65E+00		-1.44E+01		-1.44E-05

		1.28E+00		-2.99E+01		-2.99E-05		1.66E+00		-1.45E+01		-1.45E-05

		1.29E+00		-2.97E+01		-2.97E-05		1.66E+00		-1.44E+01		-1.44E-05

		1.29E+00		-2.96E+01		-2.96E-05		1.67E+00		-1.45E+01		-1.45E-05

		1.29E+00		-2.91E+01		-2.91E-05		1.67E+00		-1.45E+01		-1.45E-05

		1.30E+00		-2.90E+01		-2.90E-05		1.67E+00		-1.46E+01		-1.46E-05

		1.30E+00		-2.87E+01		-2.87E-05		1.68E+00		-1.46E+01		-1.46E-05

		1.31E+00		-2.86E+01		-2.86E-05		1.68E+00		-1.47E+01		-1.47E-05

		1.31E+00		-2.84E+01		-2.84E-05		1.69E+00		-1.47E+01		-1.47E-05

		1.31E+00		-2.80E+01		-2.80E-05		1.69E+00		-1.48E+01		-1.48E-05

		1.32E+00		-2.78E+01		-2.78E-05		1.69E+00		-1.48E+01		-1.48E-05

		1.32E+00		-2.78E+01		-2.78E-05		1.70E+00		-1.49E+01		-1.49E-05

		1.33E+00		-2.75E+01		-2.75E-05		1.70E+00		-1.49E+01		-1.49E-05

		1.33E+00		-2.71E+01		-2.71E-05		1.71E+00		-1.51E+01		-1.51E-05

		1.33E+00		-2.70E+01		-2.70E-05		1.71E+00		-1.51E+01		-1.51E-05

		1.34E+00		-2.66E+01		-2.66E-05		1.71E+00		-1.53E+01		-1.53E-05

		1.34E+00		-2.65E+01		-2.65E-05		1.72E+00		-1.53E+01		-1.53E-05

		1.35E+00		-2.63E+01		-2.63E-05		1.72E+00		-1.55E+01		-1.55E-05

		1.35E+00		-2.63E+01		-2.63E-05		1.73E+00		-1.55E+01		-1.55E-05

		1.35E+00		-2.60E+01		-2.60E-05		1.73E+00		-1.57E+01		-1.57E-05

		1.36E+00		-2.55E+01		-2.55E-05		1.73E+00		-1.58E+01		-1.58E-05

		1.36E+00		-2.57E+01		-2.57E-05		1.74E+00		-1.59E+01		-1.59E-05

		1.37E+00		-2.51E+01		-2.51E-05		1.74E+00		-1.61E+01		-1.61E-05

		1.37E+00		-2.51E+01		-2.51E-05		1.75E+00		-1.63E+01		-1.63E-05

		1.37E+00		-2.47E+01		-2.47E-05		1.75E+00		-1.64E+01		-1.64E-05

		1.38E+00		-2.50E+01		-2.50E-05		1.75E+00		-1.65E+01		-1.65E-05

		1.38E+00		-2.44E+01		-2.44E-05		1.76E+00		-1.68E+01		-1.68E-05

		1.39E+00		-2.42E+01		-2.42E-05		1.76E+00		-1.70E+01		-1.70E-05

		1.39E+00		-2.42E+01		-2.42E-05		1.77E+00		-1.72E+01		-1.72E-05

		1.39E+00		-2.38E+01		-2.38E-05		1.77E+00		-1.74E+01		-1.74E-05

		1.40E+00		-2.38E+01		-2.38E-05		1.77E+00		-1.77E+01		-1.77E-05

		1.40E+00		-2.36E+01		-2.36E-05		1.78E+00		-1.79E+01		-1.79E-05

		1.41E+00		-2.37E+01		-2.37E-05		1.78E+00		-1.82E+01		-1.82E-05

		1.41E+00		-2.33E+01		-2.33E-05		1.79E+00		-1.86E+01		-1.86E-05

		1.41E+00		-2.32E+01		-2.32E-05		1.79E+00		-1.89E+01		-1.89E-05

		1.42E+00		-2.31E+01		-2.31E-05		1.79E+00		-1.90E+01		-1.90E-05

		1.42E+00		-2.29E+01		-2.29E-05		1.80E+00		-1.97E+01		-1.97E-05

		1.43E+00		-2.26E+01		-2.26E-05		1.80E+00		-1.98E+01		-1.98E-05

		1.43E+00		-2.25E+01		-2.25E-05		1.81E+00		-2.02E+01		-2.02E-05

		1.43E+00		-2.25E+01		-2.25E-05		1.81E+00		-2.04E+01		-2.04E-05

		1.44E+00		-2.24E+01		-2.24E-05		1.81E+00		-2.09E+01		-2.09E-05

		1.44E+00		-2.20E+01		-2.20E-05		1.82E+00		-2.14E+01		-2.14E-05

		1.45E+00		-2.19E+01		-2.19E-05		1.82E+00		-2.18E+01		-2.18E-05

		1.45E+00		-2.21E+01		-2.21E-05		1.83E+00		-2.23E+01		-2.23E-05

		1.45E+00		-2.17E+01		-2.17E-05		1.83E+00		-2.27E+01		-2.27E-05

		1.46E+00		-2.17E+01		-2.17E-05		1.83E+00		-2.33E+01		-2.33E-05

		1.46E+00		-2.14E+01		-2.14E-05		1.84E+00		-2.37E+01		-2.37E-05

		1.47E+00		-2.13E+01		-2.13E-05		1.84E+00		-2.42E+01		-2.42E-05

		1.47E+00		-2.12E+01		-2.12E-05		1.85E+00		-2.47E+01		-2.47E-05

		1.47E+00		-2.09E+01		-2.09E-05		1.85E+00		-2.51E+01		-2.51E-05

		1.48E+00		-2.09E+01		-2.09E-05		1.85E+00		-2.58E+01		-2.58E-05

		1.48E+00		-2.07E+01		-2.07E-05		1.86E+00		-2.61E+01		-2.61E-05

		1.49E+00		-2.08E+01		-2.08E-05		1.86E+00		-2.68E+01		-2.68E-05

		1.49E+00		-2.04E+01		-2.04E-05		1.87E+00		-2.71E+01		-2.71E-05

		1.49E+00		-2.06E+01		-2.06E-05		1.87E+00		-2.78E+01		-2.78E-05

		1.50E+00		-2.02E+01		-2.02E-05		1.87E+00		-2.83E+01		-2.83E-05

		1.50E+00		-2.01E+01		-2.01E-05		1.88E+00		-2.88E+01		-2.88E-05

		1.51E+00		-2.01E+01		-2.01E-05		1.88E+00		-2.93E+01		-2.93E-05

		1.51E+00		-1.99E+01		-1.99E-05		1.89E+00		-3.00E+01		-3.00E-05

		1.51E+00		-2.01E+01		-2.01E-05		1.89E+00		-3.03E+01		-3.03E-05

		1.52E+00		-1.98E+01		-1.98E-05		1.89E+00		-3.07E+01		-3.07E-05

		1.52E+00		-1.96E+01		-1.96E-05		1.90E+00		-3.13E+01		-3.13E-05

		1.53E+00		-1.96E+01		-1.96E-05		1.90E+00		-3.18E+01		-3.18E-05

		1.53E+00		-1.95E+01		-1.95E-05		1.91E+00		-3.24E+01		-3.24E-05

		1.53E+00		-1.95E+01		-1.95E-05		1.91E+00		-3.28E+01		-3.28E-05

		1.54E+00		-1.91E+01		-1.91E-05		1.91E+00		-3.33E+01		-3.33E-05

		1.54E+00		-1.93E+01		-1.93E-05		1.92E+00		-3.38E+01		-3.38E-05

		1.55E+00		-1.90E+01		-1.90E-05		1.92E+00		-3.42E+01		-3.42E-05

		1.55E+00		-1.90E+01		-1.90E-05		1.93E+00		-3.47E+01		-3.47E-05

		1.55E+00		-1.93E+01		-1.93E-05		1.93E+00		-3.52E+01		-3.52E-05

		1.56E+00		-1.88E+01		-1.88E-05		1.93E+00		-3.57E+01		-3.57E-05

		1.56E+00		-1.88E+01		-1.88E-05		1.94E+00		-3.61E+01		-3.61E-05

		1.57E+00		-1.88E+01		-1.88E-05		1.94E+00		-3.66E+01		-3.66E-05

		1.57E+00		-1.86E+01		-1.86E-05		1.95E+00		-3.71E+01		-3.71E-05

		1.57E+00		-1.88E+01		-1.88E-05		1.95E+00		-3.75E+01		-3.75E-05

		1.58E+00		-1.86E+01		-1.86E-05		1.95E+00		-3.79E+01		-3.79E-05

		1.58E+00		-1.88E+01		-1.88E-05		1.96E+00		-3.84E+01		-3.84E-05

		1.59E+00		-1.84E+01		-1.84E-05		1.96E+00		-3.89E+01		-3.89E-05

		1.59E+00		-1.85E+01		-1.85E-05		1.97E+00		-3.94E+01		-3.94E-05

		1.59E+00		-1.83E+01		-1.83E-05		1.97E+00		-3.97E+01		-3.97E-05

		1.60E+00		-1.82E+01		-1.82E-05		1.97E+00		-4.01E+01		-4.01E-05

		1.60E+00		-1.83E+01		-1.83E-05		1.98E+00		-4.05E+01		-4.05E-05

		1.61E+00		-1.82E+01		-1.82E-05		1.98E+00		-4.11E+01		-4.11E-05

		1.61E+00		-1.84E+01		-1.84E-05		1.99E+00		-4.14E+01		-4.14E-05

		1.61E+00		-1.81E+01		-1.81E-05		1.99E+00		-4.18E+01		-4.18E-05

		1.62E+00		-1.79E+01		-1.79E-05		1.99E+00		-4.23E+01		-4.23E-05

		1.62E+00		-1.81E+01		-1.81E-05		2.00E+00		-4.28E+01		-4.28E-05

		1.63E+00		-1.78E+01		-1.78E-05		2.00E+00		-4.32E+01		-4.32E-05

		1.63E+00		-1.81E+01		-1.81E-05		2.00E+00		-4.12E+01		-4.12E-05

		1.63E+00		-1.79E+01		-1.79E-05		1.99E+00		-3.95E+01		-3.95E-05

		1.64E+00		-1.80E+01		-1.80E-05		1.99E+00		-3.79E+01		-3.79E-05

		1.64E+00		-1.77E+01		-1.77E-05		1.99E+00		-3.66E+01		-3.66E-05

		1.65E+00		-1.80E+01		-1.80E-05		1.98E+00		-3.54E+01		-3.54E-05

		1.65E+00		-1.78E+01		-1.78E-05		1.98E+00		-3.42E+01		-3.42E-05

		1.65E+00		-1.79E+01		-1.79E-05		1.97E+00		-3.31E+01		-3.31E-05

		1.66E+00		-1.78E+01		-1.78E-05		1.97E+00		-3.20E+01		-3.20E-05

		1.66E+00		-1.78E+01		-1.78E-05		1.97E+00		-3.13E+01		-3.13E-05

		1.67E+00		-1.79E+01		-1.79E-05		1.96E+00		-3.01E+01		-3.01E-05

		1.67E+00		-1.75E+01		-1.75E-05		1.96E+00		-2.94E+01		-2.94E-05

		1.67E+00		-1.78E+01		-1.78E-05		1.95E+00		-2.83E+01		-2.83E-05

		1.68E+00		-1.78E+01		-1.78E-05		1.95E+00		-2.78E+01		-2.78E-05

		1.68E+00		-1.78E+01		-1.78E-05		1.95E+00		-2.68E+01		-2.68E-05

		1.69E+00		-1.76E+01		-1.76E-05		1.94E+00		-2.62E+01		-2.62E-05

		1.69E+00		-1.79E+01		-1.79E-05		1.94E+00		-2.54E+01		-2.54E-05

		1.69E+00		-1.76E+01		-1.76E-05		1.93E+00		-2.47E+01		-2.47E-05

		1.70E+00		-1.77E+01		-1.77E-05		1.93E+00		-2.40E+01		-2.40E-05

		1.70E+00		-1.76E+01		-1.76E-05		1.93E+00		-2.34E+01		-2.34E-05

		1.71E+00		-1.78E+01		-1.78E-05		1.92E+00		-2.29E+01		-2.29E-05

		1.71E+00		-1.77E+01		-1.77E-05		1.92E+00		-2.21E+01		-2.21E-05

		1.71E+00		-1.76E+01		-1.76E-05		1.91E+00		-2.15E+01		-2.15E-05

		1.72E+00		-1.79E+01		-1.79E-05		1.91E+00		-2.09E+01		-2.09E-05

		1.72E+00		-1.76E+01		-1.76E-05		1.91E+00		-2.05E+01		-2.05E-05

		1.73E+00		-1.79E+01		-1.79E-05		1.90E+00		-1.99E+01		-1.99E-05

		1.73E+00		-1.74E+01		-1.74E-05		1.90E+00		-1.96E+01		-1.96E-05

		1.73E+00		-1.79E+01		-1.79E-05		1.89E+00		-1.90E+01		-1.90E-05

		1.74E+00		-1.80E+01		-1.80E-05		1.89E+00		-1.84E+01		-1.84E-05

		1.74E+00		-1.79E+01		-1.79E-05		1.89E+00		-1.80E+01		-1.80E-05

		1.75E+00		-1.81E+01		-1.81E-05		1.88E+00		-1.76E+01		-1.76E-05

		1.75E+00		-1.80E+01		-1.80E-05		1.88E+00		-1.72E+01		-1.72E-05

		1.75E+00		-1.82E+01		-1.82E-05		1.87E+00		-1.66E+01		-1.66E-05

		1.76E+00		-1.81E+01		-1.81E-05		1.87E+00		-1.63E+01		-1.63E-05

		1.76E+00		-1.83E+01		-1.83E-05		1.87E+00		-1.60E+01		-1.60E-05

		1.77E+00		-1.82E+01		-1.82E-05		1.86E+00		-1.55E+01		-1.55E-05

		1.77E+00		-1.85E+01		-1.85E-05		1.86E+00		-1.51E+01		-1.51E-05

		1.77E+00		-1.85E+01		-1.85E-05		1.85E+00		-1.48E+01		-1.48E-05

		1.78E+00		-1.86E+01		-1.86E-05		1.85E+00		-1.44E+01		-1.44E-05

		1.78E+00		-1.86E+01		-1.86E-05		1.85E+00		-1.41E+01		-1.41E-05

		1.79E+00		-1.89E+01		-1.89E-05		1.84E+00		-1.38E+01		-1.38E-05

		1.79E+00		-1.89E+01		-1.89E-05		1.84E+00		-1.34E+01		-1.34E-05

		1.79E+00		-1.89E+01		-1.89E-05		1.83E+00		-1.29E+01		-1.29E-05

		1.80E+00		-1.92E+01		-1.92E-05		1.83E+00		-1.27E+01		-1.27E-05

		1.80E+00		-1.91E+01		-1.91E-05		1.83E+00		-1.24E+01		-1.24E-05

		1.81E+00		-1.95E+01		-1.95E-05		1.82E+00		-1.21E+01		-1.21E-05

		1.81E+00		-1.93E+01		-1.93E-05		1.82E+00		-1.17E+01		-1.17E-05

		1.81E+00		-2.00E+01		-2.00E-05		1.81E+00		-1.14E+01		-1.14E-05

		1.82E+00		-1.97E+01		-1.97E-05		1.81E+00		-1.11E+01		-1.11E-05

		1.82E+00		-2.00E+01		-2.00E-05		1.81E+00		-1.09E+01		-1.09E-05

		1.83E+00		-2.01E+01		-2.01E-05		1.80E+00		-1.06E+01		-1.06E-05

		1.83E+00		-2.01E+01		-2.01E-05		1.80E+00		-1.03E+01		-1.03E-05

		1.83E+00		-2.06E+01		-2.06E-05		1.79E+00		-1.00E+01		-1.00E-05

		1.84E+00		-2.06E+01		-2.06E-05		1.79E+00		-9.79E+00		-9.79E-06

		1.84E+00		-2.11E+01		-2.11E-05		1.79E+00		-9.62E+00		-9.62E-06

		1.85E+00		-2.10E+01		-2.10E-05		1.78E+00		-9.38E+00		-9.38E-06

		1.85E+00		-2.12E+01		-2.12E-05		1.78E+00		-9.16E+00		-9.16E-06

		1.85E+00		-2.15E+01		-2.15E-05		1.77E+00		-8.92E+00		-8.92E-06

		1.86E+00		-2.16E+01		-2.16E-05		1.77E+00		-8.77E+00		-8.77E-06

		1.86E+00		-2.21E+01		-2.21E-05		1.77E+00		-8.60E+00		-8.60E-06

		1.87E+00		-2.23E+01		-2.23E-05		1.76E+00		-8.40E+00		-8.40E-06

		1.87E+00		-2.26E+01		-2.26E-05		1.76E+00		-8.26E+00		-8.26E-06

		1.87E+00		-2.27E+01		-2.27E-05		1.75E+00		-8.07E+00		-8.07E-06

		1.88E+00		-2.30E+01		-2.30E-05		1.75E+00		-7.93E+00		-7.93E-06

		1.88E+00		-2.33E+01		-2.33E-05		1.75E+00		-7.83E+00		-7.83E-06

		1.89E+00		-2.38E+01		-2.38E-05		1.74E+00		-7.70E+00		-7.70E-06

		1.89E+00		-2.38E+01		-2.38E-05		1.74E+00		-7.54E+00		-7.54E-06

		1.89E+00		-2.44E+01		-2.44E-05		1.73E+00		-7.42E+00		-7.42E-06

		1.90E+00		-2.47E+01		-2.47E-05		1.73E+00		-7.31E+00		-7.31E-06

		1.90E+00		-2.50E+01		-2.50E-05		1.73E+00		-7.23E+00		-7.23E-06

		1.91E+00		-2.53E+01		-2.53E-05		1.72E+00		-7.15E+00		-7.15E-06

		1.91E+00		-2.58E+01		-2.58E-05		1.72E+00		-7.01E+00		-7.01E-06

		1.91E+00		-2.63E+01		-2.63E-05		1.71E+00		-6.94E+00		-6.94E-06

		1.92E+00		-2.65E+01		-2.65E-05		1.71E+00		-6.81E+00		-6.81E-06

		1.92E+00		-2.72E+01		-2.72E-05		1.71E+00		-6.79E+00		-6.79E-06

		1.93E+00		-2.75E+01		-2.75E-05		1.70E+00		-6.66E+00		-6.66E-06

		1.93E+00		-2.82E+01		-2.82E-05		1.70E+00		-6.59E+00		-6.59E-06

		1.93E+00		-2.83E+01		-2.83E-05		1.69E+00		-6.49E+00		-6.49E-06

		1.94E+00		-2.90E+01		-2.90E-05		1.69E+00		-6.44E+00		-6.44E-06

		1.94E+00		-2.95E+01		-2.95E-05		1.69E+00		-6.34E+00		-6.34E-06

		1.95E+00		-3.02E+01		-3.02E-05		1.68E+00		-6.32E+00		-6.32E-06

		1.95E+00		-3.08E+01		-3.08E-05		1.68E+00		-6.19E+00		-6.19E-06

		1.95E+00		-3.12E+01		-3.12E-05		1.67E+00		-6.19E+00		-6.19E-06

		1.96E+00		-3.18E+01		-3.18E-05		1.67E+00		-6.04E+00		-6.04E-06

		1.96E+00		-3.21E+01		-3.21E-05		1.67E+00		-6.03E+00		-6.03E-06

		1.97E+00		-3.32E+01		-3.32E-05		1.66E+00		-5.96E+00		-5.96E-06

		1.97E+00		-3.35E+01		-3.35E-05		1.66E+00		-5.92E+00		-5.92E-06

		1.97E+00		-3.43E+01		-3.43E-05		1.65E+00		-5.85E+00		-5.85E-06

		1.98E+00		-3.49E+01		-3.49E-05		1.65E+00		-5.78E+00		-5.78E-06

		1.98E+00		-3.53E+01		-3.53E-05		1.65E+00		-5.75E+00		-5.75E-06

		1.99E+00		-3.61E+01		-3.61E-05		1.64E+00		-5.71E+00		-5.71E-06

		1.99E+00		-3.67E+01		-3.67E-05		1.64E+00		-5.60E+00		-5.60E-06

		1.99E+00		-3.73E+01		-3.73E-05		1.63E+00		-5.58E+00		-5.58E-06

		2.00E+00		-3.81E+01		-3.81E-05		1.63E+00		-5.53E+00		-5.53E-06

		2.00E+00		-3.89E+01		-3.89E-05		1.63E+00		-5.52E+00		-5.52E-06

		2.00E+00		-3.70E+01		-3.70E-05		1.62E+00		-5.43E+00		-5.43E-06

		1.99E+00		-3.55E+01		-3.55E-05		1.62E+00		-5.42E+00		-5.42E-06

		1.99E+00		-3.41E+01		-3.41E-05		1.61E+00		-5.37E+00		-5.37E-06

		1.99E+00		-3.29E+01		-3.29E-05		1.61E+00		-5.30E+00		-5.30E-06

		1.98E+00		-3.15E+01		-3.15E-05		1.61E+00		-5.31E+00		-5.31E-06

		1.98E+00		-3.04E+01		-3.04E-05		1.60E+00		-5.25E+00		-5.25E-06

		1.97E+00		-2.94E+01		-2.94E-05		1.60E+00		-5.25E+00		-5.25E-06

		1.97E+00		-2.83E+01		-2.83E-05		1.59E+00		-5.18E+00		-5.18E-06

		1.97E+00		-2.73E+01		-2.73E-05		1.59E+00		-5.14E+00		-5.14E-06

		1.96E+00		-2.65E+01		-2.65E-05		1.59E+00		-5.18E+00		-5.18E-06

		1.96E+00		-2.62E+01		-2.62E-05		1.58E+00		-5.12E+00		-5.12E-06

		1.95E+00		-2.46E+01		-2.46E-05		1.58E+00		-5.11E+00		-5.11E-06

		1.95E+00		-2.41E+01		-2.41E-05		1.57E+00		-5.09E+00		-5.09E-06

		1.95E+00		-2.32E+01		-2.32E-05		1.57E+00		-5.07E+00		-5.07E-06

		1.94E+00		-2.26E+01		-2.26E-05		1.57E+00		-5.07E+00		-5.07E-06

		1.94E+00		-2.20E+01		-2.20E-05		1.56E+00		-5.09E+00		-5.09E-06

		1.93E+00		-2.11E+01		-2.11E-05		1.56E+00		-5.02E+00		-5.02E-06

		1.93E+00		-2.10E+01		-2.10E-05		1.55E+00		-5.02E+00		-5.02E-06

		1.93E+00		-2.00E+01		-2.00E-05		1.55E+00		-4.96E+00		-4.96E-06

		1.92E+00		-1.96E+01		-1.96E-05		1.55E+00		-5.01E+00		-5.01E-06

		1.92E+00		-1.88E+01		-1.88E-05		1.54E+00		-4.93E+00		-4.93E-06

		1.91E+00		-1.84E+01		-1.84E-05		1.54E+00		-4.94E+00		-4.94E-06

		1.91E+00		-1.77E+01		-1.77E-05		1.53E+00		-4.93E+00		-4.93E-06

		1.91E+00		-1.73E+01		-1.73E-05		1.53E+00		-4.90E+00		-4.90E-06

		1.90E+00		-1.70E+01		-1.70E-05		1.53E+00		-4.91E+00		-4.91E-06

		1.90E+00		-1.63E+01		-1.63E-05		1.52E+00		-4.87E+00		-4.87E-06

		1.89E+00		-1.60E+01		-1.60E-05		1.52E+00		-4.85E+00		-4.85E-06

		1.89E+00		-1.56E+01		-1.56E-05		1.51E+00		-4.85E+00		-4.85E-06

		1.89E+00		-1.53E+01		-1.53E-05		1.51E+00		-4.82E+00		-4.82E-06

		1.88E+00		-1.48E+01		-1.48E-05		1.51E+00		-4.82E+00		-4.82E-06

		1.88E+00		-1.44E+01		-1.44E-05		1.50E+00		-4.85E+00		-4.85E-06

		1.87E+00		-1.41E+01		-1.41E-05		1.50E+00		-4.76E+00		-4.76E-06

		1.87E+00		-1.37E+01		-1.37E-05		1.49E+00		-4.80E+00		-4.80E-06

		1.87E+00		-1.34E+01		-1.34E-05		1.49E+00		-4.73E+00		-4.73E-06

		1.86E+00		-1.30E+01		-1.30E-05		1.49E+00		-4.76E+00		-4.76E-06

		1.86E+00		-1.27E+01		-1.27E-05		1.48E+00		-4.73E+00		-4.73E-06

		1.85E+00		-1.24E+01		-1.24E-05		1.48E+00		-4.71E+00		-4.71E-06

		1.85E+00		-1.20E+01		-1.20E-05		1.47E+00		-4.71E+00		-4.71E-06

		1.85E+00		-1.19E+01		-1.19E-05		1.47E+00		-4.63E+00		-4.63E-06

		1.84E+00		-1.15E+01		-1.15E-05		1.47E+00		-4.65E+00		-4.65E-06

		1.84E+00		-1.13E+01		-1.13E-05		1.46E+00		-4.60E+00		-4.60E-06

		1.83E+00		-1.10E+01		-1.10E-05		1.46E+00		-4.56E+00		-4.56E-06

		1.83E+00		-1.07E+01		-1.07E-05		1.45E+00		-4.59E+00		-4.59E-06

		1.83E+00		-1.05E+01		-1.05E-05		1.45E+00		-4.50E+00		-4.50E-06

		1.82E+00		-1.03E+01		-1.03E-05		1.45E+00		-4.58E+00		-4.58E-06

		1.82E+00		-1.01E+01		-1.01E-05		1.44E+00		-4.46E+00		-4.46E-06

		1.81E+00		-9.82E+00		-9.82E-06		1.44E+00		-4.48E+00		-4.48E-06

		1.81E+00		-9.54E+00		-9.54E-06		1.43E+00		-4.46E+00		-4.46E-06

		1.81E+00		-9.36E+00		-9.36E-06		1.43E+00		-4.39E+00		-4.39E-06

		1.80E+00		-9.23E+00		-9.23E-06		1.43E+00		-4.37E+00		-4.37E-06

		1.80E+00		-9.02E+00		-9.02E-06		1.42E+00		-4.34E+00		-4.34E-06

		1.79E+00		-8.83E+00		-8.83E-06		1.42E+00		-4.24E+00		-4.24E-06

		1.79E+00		-8.68E+00		-8.68E-06		1.41E+00		-4.30E+00		-4.30E-06

		1.79E+00		-8.45E+00		-8.45E-06		1.41E+00		-4.13E+00		-4.13E-06

		1.78E+00		-8.29E+00		-8.29E-06		1.41E+00		-4.16E+00		-4.16E-06

		1.78E+00		-8.19E+00		-8.19E-06		1.40E+00		-4.02E+00		-4.02E-06

		1.77E+00		-8.05E+00		-8.05E-06		1.40E+00		-4.00E+00		-4.00E-06

		1.77E+00		-7.84E+00		-7.84E-06		1.39E+00		-3.93E+00		-3.93E-06

		1.77E+00		-7.74E+00		-7.74E-06		1.39E+00		-3.86E+00		-3.86E-06

		1.76E+00		-7.74E+00		-7.74E-06		1.39E+00		-3.78E+00		-3.78E-06

		1.76E+00		-7.55E+00		-7.55E-06		1.38E+00		-3.71E+00		-3.71E-06

		1.75E+00		-7.38E+00		-7.38E-06		1.38E+00		-3.59E+00		-3.59E-06

		1.75E+00		-7.26E+00		-7.26E-06		1.37E+00		-3.57E+00		-3.57E-06

		1.75E+00		-7.12E+00		-7.12E-06		1.37E+00		-3.37E+00		-3.37E-06

		1.74E+00		-7.09E+00		-7.09E-06		1.37E+00		-3.38E+00		-3.38E-06

		1.74E+00		-6.98E+00		-6.98E-06		1.36E+00		-3.15E+00		-3.15E-06

		1.73E+00		-6.95E+00		-6.95E-06		1.36E+00		-3.09E+00		-3.09E-06

		1.73E+00		-6.78E+00		-6.78E-06		1.35E+00		-2.97E+00		-2.97E-06

		1.73E+00		-6.71E+00		-6.71E-06		1.35E+00		-2.81E+00		-2.81E-06

		1.72E+00		-6.63E+00		-6.63E-06		1.35E+00		-2.68E+00		-2.68E-06

		1.72E+00		-6.58E+00		-6.58E-06		1.34E+00		-2.54E+00		-2.54E-06

		1.71E+00		-6.44E+00		-6.44E-06		1.34E+00		-2.35E+00		-2.35E-06

		1.71E+00		-6.38E+00		-6.38E-06		1.33E+00		-2.28E+00		-2.28E-06

		1.71E+00		-6.35E+00		-6.35E-06		1.33E+00		-1.97E+00		-1.97E-06

		1.70E+00		-6.31E+00		-6.31E-06		1.33E+00		-1.90E+00		-1.90E-06

		1.70E+00		-6.24E+00		-6.24E-06		1.32E+00		-1.71E+00		-1.71E-06

		1.69E+00		-6.13E+00		-6.13E-06		1.32E+00		-1.46E+00		-1.46E-06

		1.69E+00		-6.09E+00		-6.09E-06		1.31E+00		-1.26E+00		-1.26E-06

		1.69E+00		-5.97E+00		-5.97E-06		1.31E+00		-1.10E+00		-1.10E-06

		1.68E+00		-6.00E+00		-6.00E-06		1.31E+00		-8.98E-01		-8.98E-07

		1.68E+00		-5.93E+00		-5.93E-06		1.30E+00		-7.20E-01		-7.20E-07

		1.67E+00		-5.81E+00		-5.81E-06		1.30E+00		-5.77E-01		-5.77E-07

		1.67E+00		-5.85E+00		-5.85E-06		1.29E+00		-3.35E-01		-3.35E-07

		1.67E+00		-5.69E+00		-5.69E-06		1.29E+00		-1.81E-01		-1.81E-07

		1.66E+00		-5.72E+00		-5.72E-06		1.29E+00		-3.10E-02		-3.10E-08

		1.66E+00		-5.61E+00		-5.61E-06		1.28E+00		1.27E-01		1.27E-07

		1.65E+00		-5.53E+00		-5.53E-06		1.28E+00		2.80E-01		2.80E-07

		1.65E+00		-5.56E+00		-5.56E-06		1.27E+00		4.65E-01		4.65E-07

		1.65E+00		-5.46E+00		-5.46E-06		1.27E+00		5.60E-01		5.60E-07

		1.64E+00		-5.50E+00		-5.50E-06		1.27E+00		6.90E-01		6.90E-07

		1.64E+00		-5.37E+00		-5.37E-06		1.26E+00		8.30E-01		8.30E-07

		1.63E+00		-5.37E+00		-5.37E-06		1.26E+00		9.20E-01		9.20E-07

		1.63E+00		-5.28E+00		-5.28E-06		1.25E+00		1.04E+00		1.04E-06

		1.63E+00		-5.22E+00		-5.22E-06		1.25E+00		1.23E+00		1.23E-06

		1.62E+00		-5.28E+00		-5.28E-06		1.25E+00		1.29E+00		1.29E-06

		1.62E+00		-5.18E+00		-5.18E-06		1.24E+00		1.43E+00		1.43E-06

		1.61E+00		-5.17E+00		-5.17E-06		1.24E+00		1.51E+00		1.51E-06

		1.61E+00		-5.12E+00		-5.12E-06		1.23E+00		1.65E+00		1.65E-06

		1.61E+00		-5.05E+00		-5.05E-06		1.23E+00		1.69E+00		1.69E-06

		1.60E+00		-5.04E+00		-5.04E-06		1.23E+00		1.78E+00		1.78E-06

		1.60E+00		-4.94E+00		-4.94E-06		1.22E+00		1.93E+00		1.93E-06

		1.59E+00		-4.95E+00		-4.95E-06		1.22E+00		1.97E+00		1.97E-06

		1.59E+00		-4.96E+00		-4.96E-06		1.21E+00		2.06E+00		2.06E-06

		1.59E+00		-4.93E+00		-4.93E-06		1.21E+00		2.17E+00		2.17E-06

		1.58E+00		-4.90E+00		-4.90E-06		1.21E+00		2.23E+00		2.23E-06

		1.58E+00		-4.86E+00		-4.86E-06		1.20E+00		2.31E+00		2.31E-06

		1.57E+00		-4.76E+00		-4.76E-06		1.20E+00		2.37E+00		2.37E-06

		1.57E+00		-4.77E+00		-4.77E-06		1.19E+00		2.50E+00		2.50E-06

		1.57E+00		-4.72E+00		-4.72E-06		1.19E+00		2.58E+00		2.58E-06

		1.56E+00		-4.70E+00		-4.70E-06		1.19E+00		2.61E+00		2.61E-06

		1.56E+00		-4.72E+00		-4.72E-06		1.18E+00		2.73E+00		2.73E-06

		1.55E+00		-4.60E+00		-4.60E-06		1.18E+00		2.84E+00		2.84E-06

		1.55E+00		-4.58E+00		-4.58E-06		1.17E+00		2.90E+00		2.90E-06

		1.55E+00		-4.53E+00		-4.53E-06		1.17E+00		2.98E+00		2.98E-06

		1.54E+00		-4.54E+00		-4.54E-06		1.17E+00		3.09E+00		3.09E-06

		1.54E+00		-4.50E+00		-4.50E-06		1.16E+00		3.16E+00		3.16E-06

		1.53E+00		-4.44E+00		-4.44E-06		1.16E+00		3.26E+00		3.26E-06

		1.53E+00		-4.53E+00		-4.53E-06		1.15E+00		3.37E+00		3.37E-06

		1.53E+00		-4.38E+00		-4.38E-06		1.15E+00		3.46E+00		3.46E-06

		1.52E+00		-4.39E+00		-4.39E-06		1.15E+00		3.53E+00		3.53E-06

		1.52E+00		-4.35E+00		-4.35E-06		1.14E+00		3.64E+00		3.64E-06

		1.51E+00		-4.33E+00		-4.33E-06		1.14E+00		3.73E+00		3.73E-06

		1.51E+00		-4.33E+00		-4.33E-06		1.13E+00		3.87E+00		3.87E-06

		1.51E+00		-4.27E+00		-4.27E-06		1.13E+00		3.86E+00		3.86E-06

		1.50E+00		-4.36E+00		-4.36E-06		1.13E+00		4.02E+00		4.02E-06

		1.50E+00		-4.23E+00		-4.23E-06		1.12E+00		4.06E+00		4.06E-06

		1.49E+00		-4.22E+00		-4.22E-06		1.12E+00		4.18E+00		4.18E-06

		1.49E+00		-4.18E+00		-4.18E-06		1.11E+00		4.26E+00		4.26E-06

		1.49E+00		-4.13E+00		-4.13E-06		1.11E+00		4.30E+00		4.30E-06

		1.48E+00		-4.17E+00		-4.17E-06		1.11E+00		4.38E+00		4.38E-06

		1.48E+00		-4.12E+00		-4.12E-06		1.10E+00		4.43E+00		4.43E-06

		1.47E+00		-4.09E+00		-4.09E-06		1.10E+00		4.52E+00		4.52E-06

		1.47E+00		-4.10E+00		-4.10E-06		1.09E+00		4.65E+00		4.65E-06

		1.47E+00		-3.97E+00		-3.97E-06		1.09E+00		4.58E+00		4.58E-06

		1.46E+00		-4.01E+00		-4.01E-06		1.09E+00		4.72E+00		4.72E-06

		1.46E+00		-3.97E+00		-3.97E-06		1.08E+00		4.72E+00		4.72E-06

		1.45E+00		-3.91E+00		-3.91E-06		1.08E+00		4.75E+00		4.75E-06

		1.45E+00		-3.93E+00		-3.93E-06		1.07E+00		4.81E+00		4.81E-06

		1.45E+00		-3.86E+00		-3.86E-06		1.07E+00		4.81E+00		4.81E-06

		1.44E+00		-3.87E+00		-3.87E-06		1.07E+00		4.82E+00		4.82E-06

		1.44E+00		-3.83E+00		-3.83E-06		1.06E+00		4.83E+00		4.83E-06

		1.43E+00		-3.74E+00		-3.74E-06		1.06E+00		4.78E+00		4.78E-06

		1.43E+00		-3.78E+00		-3.78E-06		1.05E+00		4.84E+00		4.84E-06

		1.43E+00		-3.60E+00		-3.60E-06		1.05E+00		4.64E+00		4.64E-06

		1.42E+00		-3.71E+00		-3.71E-06		1.05E+00		4.69E+00		4.69E-06

		1.42E+00		-3.65E+00		-3.65E-06		1.04E+00		4.59E+00		4.59E-06

		1.41E+00		-3.58E+00		-3.58E-06		1.04E+00		4.61E+00		4.61E-06

		1.41E+00		-3.64E+00		-3.64E-06		1.03E+00		4.44E+00		4.44E-06

		1.41E+00		-3.47E+00		-3.47E-06		1.03E+00		4.36E+00		4.36E-06

		1.40E+00		-3.50E+00		-3.50E-06		1.03E+00		4.27E+00		4.27E-06

		1.40E+00		-3.43E+00		-3.43E-06		1.02E+00		4.17E+00		4.17E-06

		1.39E+00		-3.38E+00		-3.38E-06		1.02E+00		4.09E+00		4.09E-06

		1.39E+00		-3.43E+00		-3.43E-06		1.01E+00		4.01E+00		4.01E-06

		1.39E+00		-3.26E+00		-3.26E-06		1.01E+00		3.82E+00		3.82E-06

		1.38E+00		-3.38E+00		-3.38E-06		1.01E+00		3.74E+00		3.74E-06

		1.38E+00		-3.24E+00		-3.24E-06		1.00E+00		3.66E+00		3.66E-06

		1.37E+00		-3.17E+00		-3.17E-06		9.97E-01		3.61E+00		3.61E-06

		1.37E+00		-3.17E+00		-3.17E-06		9.93E-01		3.50E+00		3.50E-06

		1.37E+00		-3.03E+00		-3.03E-06		9.89E-01		3.32E+00		3.32E-06

		1.36E+00		-3.10E+00		-3.10E-06		9.85E-01		3.26E+00		3.26E-06

		1.36E+00		-3.00E+00		-3.00E-06		9.81E-01		3.15E+00		3.15E-06

		1.35E+00		-2.98E+00		-2.98E-06		9.77E-01		3.11E+00		3.11E-06

		1.35E+00		-2.93E+00		-2.93E-06		9.73E-01		2.96E+00		2.96E-06

		1.35E+00		-2.82E+00		-2.82E-06		9.69E-01		2.86E+00		2.86E-06

		1.34E+00		-2.83E+00		-2.83E-06		9.65E-01		2.81E+00		2.81E-06

		1.34E+00		-2.71E+00		-2.71E-06		9.61E-01		2.71E+00		2.71E-06

		1.33E+00		-2.67E+00		-2.67E-06		9.57E-01		2.71E+00		2.71E-06

		1.33E+00		-2.62E+00		-2.62E-06		9.53E-01		2.58E+00		2.58E-06

		1.33E+00		-2.54E+00		-2.54E-06		9.49E-01		2.50E+00		2.50E-06

		1.32E+00		-2.50E+00		-2.50E-06		9.45E-01		2.43E+00		2.43E-06

		1.32E+00		-2.43E+00		-2.43E-06		9.41E-01		2.43E+00		2.43E-06

		1.31E+00		-2.32E+00		-2.32E-06		9.37E-01		2.37E+00		2.37E-06

		1.31E+00		-2.28E+00		-2.28E-06		9.33E-01		2.28E+00		2.28E-06

		1.31E+00		-2.21E+00		-2.21E-06		9.29E-01		2.18E+00		2.18E-06

		1.30E+00		-2.17E+00		-2.17E-06		9.25E-01		2.20E+00		2.20E-06

		1.30E+00		-2.06E+00		-2.06E-06		9.21E-01		2.13E+00		2.13E-06

		1.29E+00		-2.01E+00		-2.01E-06		9.17E-01		2.12E+00		2.12E-06

		1.29E+00		-1.90E+00		-1.90E-06		9.13E-01		2.05E+00		2.05E-06

		1.29E+00		-1.78E+00		-1.78E-06		9.09E-01		1.94E+00		1.94E-06

		1.28E+00		-1.78E+00		-1.78E-06		9.05E-01		1.92E+00		1.92E-06

		1.28E+00		-1.69E+00		-1.69E-06		9.01E-01		1.95E+00		1.95E-06

		1.27E+00		-1.60E+00		-1.60E-06		8.97E-01		1.95E+00		1.95E-06

		1.27E+00		-1.49E+00		-1.49E-06		8.93E-01		1.87E+00		1.87E-06

		1.27E+00		-1.38E+00		-1.38E-06		8.89E-01		1.81E+00		1.81E-06

		1.26E+00		-1.37E+00		-1.37E-06		8.85E-01		1.78E+00		1.78E-06

		1.26E+00		-1.28E+00		-1.28E-06		8.81E-01		1.75E+00		1.75E-06

		1.25E+00		-1.18E+00		-1.18E-06		8.77E-01		1.78E+00		1.78E-06

		1.25E+00		-1.16E+00		-1.16E-06		8.73E-01		1.70E+00		1.70E-06

		1.25E+00		-1.05E+00		-1.05E-06		8.69E-01		1.66E+00		1.66E-06

		1.24E+00		-1.04E+00		-1.04E-06		8.65E-01		1.67E+00		1.67E-06

		1.24E+00		-9.74E-01		-9.74E-07		8.61E-01		1.66E+00		1.66E-06

		1.23E+00		-9.05E-01		-9.05E-07		8.57E-01		1.67E+00		1.67E-06

		1.23E+00		-8.73E-01		-8.73E-07		8.53E-01		1.61E+00		1.61E-06

		1.23E+00		-7.89E-01		-7.89E-07		8.49E-01		1.52E+00		1.52E-06

		1.22E+00		-8.19E-01		-8.19E-07		8.45E-01		1.52E+00		1.52E-06

		1.22E+00		-7.34E-01		-7.34E-07		8.41E-01		1.60E+00		1.60E-06

		1.21E+00		-6.91E-01		-6.91E-07		8.37E-01		1.55E+00		1.55E-06

		1.21E+00		-6.69E-01		-6.69E-07		8.33E-01		1.52E+00		1.52E-06

		1.21E+00		-6.02E-01		-6.02E-07		8.29E-01		1.46E+00		1.46E-06

		1.20E+00		-6.35E-01		-6.35E-07		8.25E-01		1.44E+00		1.44E-06

		1.20E+00		-5.61E-01		-5.61E-07		8.21E-01		1.47E+00		1.47E-06

		1.19E+00		-5.49E-01		-5.49E-07		8.17E-01		1.49E+00		1.49E-06

		1.19E+00		-5.19E-01		-5.19E-07		8.13E-01		1.39E+00		1.39E-06

		1.19E+00		-4.77E-01		-4.77E-07		8.09E-01		1.36E+00		1.36E-06

		1.18E+00		-5.25E-01		-5.25E-07		8.05E-01		1.38E+00		1.38E-06

		1.18E+00		-4.62E-01		-4.62E-07		8.01E-01		1.44E+00		1.44E-06

		1.17E+00		-4.43E-01		-4.43E-07		7.97E-01		1.36E+00		1.36E-06

		1.17E+00		-4.38E-01		-4.38E-07		7.93E-01		1.40E+00		1.40E-06

		1.17E+00		-4.23E-01		-4.23E-07		7.89E-01		1.28E+00		1.28E-06

		1.16E+00		-4.61E-01		-4.61E-07		7.85E-01		1.35E+00		1.35E-06

		1.16E+00		-4.13E-01		-4.13E-07		7.81E-01		1.32E+00		1.32E-06

		1.15E+00		-4.05E-01		-4.05E-07		7.77E-01		1.37E+00		1.37E-06

		1.15E+00		-4.18E-01		-4.18E-07		7.73E-01		1.26E+00		1.26E-06

		1.15E+00		-3.79E-01		-3.79E-07		7.69E-01		1.31E+00		1.31E-06

		1.14E+00		-4.37E-01		-4.37E-07		7.65E-01		1.19E+00		1.19E-06

		1.14E+00		-4.24E-01		-4.24E-07		7.61E-01		1.31E+00		1.31E-06

		1.13E+00		-3.72E-01		-3.72E-07		7.57E-01		1.22E+00		1.22E-06

		1.13E+00		-3.90E-01		-3.90E-07		7.53E-01		1.28E+00		1.28E-06
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