Plasmonic ELISA for the Ultrasensitive Detection of Disease Biomarkers with the Naked Eye

Roberto de la Rica1,* and Molly M. Stevens1,*

1Department of Materials, Department of Bioengineering and Institute for Biomedical Engineering, Imperial College London, Exhibition Road, London, SW7 2AZ (UK)

*Correspondence to: m.stevens@imperial.ac.uk, roberto.delarica@gmail.com

In resource constrained countries, affordable methodologies for the detection of disease biomarkers at ultralow concentrations can potentially improve the standard of living.1,2 However, current strategies for ultrasensitive detection often require sophisticated instruments that may not be available in laboratories with fewer resources.3-11 Here, we circumvent this problem by introducing a signal generation mechanism for biosensing that enables the detection of a few molecules of analyte with the naked eye. The enzyme label of an enzyme-linked immunosorbent assay (ELISA) controls the growth of gold nanoparticles and generates colored solutions with distinct tonality when the analyte is present. Prostate specific antigen (PSA) and HIV-1 capsid antigen p24 were detected in whole serum at the ultralow concentration of 10-18 g·mL-1. p24 was also detected with the naked eye in the sera of HIV-infected patients showing viral loads undetectable by a gold standard nucleic acid-based test.

Figure 1 shows a schematic representation of the ELISA experiments performed here. The target molecule is captured with specific antibodies on a disposable substrate and subsequently labelled with an enzyme, for example via a biotin-streptavidin linkage. In conventional colorimetric ELISA, the signal is generated by the conversion of the enzyme substrate into a coloured molecule (Fig. 1a) and the intensity of the colour of the solution is quantified by measuring the absorbance with a plate reader. Although the distinction between non-coloured and coloured solution may be detected with the naked eye, this can only be achieved with confidence at high concentrations of the target molecule, therefore making a naked-eye inspection unsuitable for ultrasensitive detection. In our approach, hereby referred to as plasmonic ELISA, the generation of coloured solutions of characteristic tonality is utilized to detect a target molecule with the naked eye (Fig. 1b).12-14 In the proposed method, the biocatalytic cycle of the enzyme label is linked to the growth of gold nanoparticles in order to obtain blue- or red-coloured solutions in the presence or in the absence of the analyte, respectively (Fig. 2). In the absence of the analyte, the reduction of gold ions with hydrogen peroxide occurs at a fast rate and quasi-spherical, non-aggregated gold nanoparticles are obtained (Figs. 2a and 2b). Under these conditions, the solution is expected to acquire a red colour. In the presence of the analyte, the enzyme catalase consumes hydrogen peroxide (Figs. 2a and 2c). This slows down the kinetics of crystal growth, which results in the growth of nanocrystals showing an ill-defined morphology comprised of aggregated nanoparticles. As a consequence, the solution turns blue. The blue and red colours are easily distinguishable at a glance, therefore facilitating the detection of the analyte with the naked eye.

To test the impact of the concentration of hydrogen peroxide on the morphology and optical properties of nanoparticles grown according to Fig. 2a, different concentrations of hydrogen peroxide were added to a solution containing gold ions (0.1 mM) in MES buffer (1 mM, pH 6.5).  In Fig. 3a, the tonality of the solution changes from red to blue in the narrow concentration range between 120 and 100 M, and the color intensity decreases as the concentration of hydrogen peroxide decreases in the concentration range between 80 and 20 M. Therefore, it should be possible to control the color of the nanoparticle solution to be blue when the biocatalytic action of the enzyme reduces the concentration of hydrogen peroxide below 120 M.

A deeper insight into the process leading to the color change can be obtained from Fig. 3b. Here, the spectra of the nanoparticle dispersions broaden and red-shift when the concentration of hydrogen peroxide drops below 120 M. This is attributed to the formation of clusters of nanoparticles at low concentrations of hydrogen peroxide, which is confirmed by TEM inspection (Figs. 3c and 3d, and section S1 in the Supplementary Information). Furthermore, it is also possible to monitor the growth of gold nanoparticles by measuring the absorbance at 550 nm with a conventional plate reader, as shown in Fig. 3e (see also Section S2 in the Supplementary Information). All in all, the results shown in Fig. 3 indicate that the final morphology and state of aggregation of gold nanoparticles grown according to the reaction in Fig. 2a is extremely sensitive to the concentration of hydrogen peroxide added to the growth solution, which results in an abrupt change in the color of the solution from red to blue when the concentration of reducing agent decreases below 120 M. This observation is attributed to the reduction of gold ions by hydrogen peroxide in the presence of MES. It has been reported that MES is a mild reducing agent that can generate blue-colored nanoparticle dispersions comprising aggregated nanoparticles, and that red dispersions can be obtained when adding a supplementary reducing agent such as glucose.[15] Similarly, we can tune the tonality of the as-grown nanoparticle solution by adding hydrogen peroxide to a solution containing gold ions in MES buffer. Since the concentration of MES is constant in all experiments, the increasing concentration of hydrogen peroxide is the driving factor to obtain non-aggregated red nanoparticle dispersions.

After demonstrating the growth of nanoparticle solutions of characteristic tonality via reduction of gold ions with hydrogen peroxide, we adapted this process as the signal generation mechanism in plasmonic ELISA. To this end, we designed sandwich ELISA assays for the detection of two model analytes: prostate specific antigen (PSA) and HIV-1 capsid antigen p24. PSA has been recognized as a valuable biomarker for cancer recurrence in patients that have undergone radical prostatectomy.16,5 For these patients, it is vital to detect minute concentrations of PSA at the earliest stage possible to improve their survival rates. The detection of p24 holds great promise for the diagnosis of HIV infection in laboratories with fewer resources where expensive nucleic acid-based tests may not be available.1 For these laboratories, lowering the limit of detection of conventional ELISA assays is crucial to match the outstanding sensitivity of “gold standard” nucleic acid-based tests.2

A schematic representation of the sandwich ELISA format is available in Figure 1. Figure 4 shows the results for the detection of PSA and p24 with plasmonic ELISA when these proteins were spiked into whole serum. In both cases, the limit of detection defined as the lowest concentration of analyte that yields a blue-colored nanoparticle solution was 10-18 g·mL-1. The blue color could be easily differentiated from the red color obtained at lower concentrations of the analyte (see also Section S3 of the Supplementary Information). This observation is attributed to the biocatalytic action of catalase, which decreases the concentration of hydrogen peroxide and favors the generation of blue solutions of nanoparticles. The blue color is only observed in the presence of the analyte because the concentration of catalase is intimately related to the concentration of the analyte via the exquisite specificity of the antibodies.  Control experiments performed by spiking an unrelated globular protein, BSA, in the serum resulted in red-colored dispersions of nanoparticles because the antibodies cannot specifically recognize this protein. Therefore, these experiments unequivocally demonstrate that the blue color observed in the presence of PSA and p24 is not generated by non-specific interactions with the substrate but is in fact related to biospecific recognition by antibodies. Furthermore, in Fig. 4 the ability to detect with the naked eye could be corroborated by measuring the decrease in the absorbance measured at 550 nm with a conventional plate reader (-A550), as previously suggested in Fig. 3e. In these calibration curves, the limit of detection defined as the lowest assayed concentration of analyte that yields a signal higher than three times the standard deviation of the blank is 10-18 g·mL-1 for both target molecules. These results validate the utilization of plasmonic ELISA for the identification of serum proteins at ultralow concentrations with the naked eye. The outstandingly low limit of detection is attributed to the high efficiency of the enzyme to fine-tune the concentration of hydrogen peroxide, 17-19 which is the driving force to yield nanocrystals with different morphology and optical properties as previously demonstrated in Figure 3.

The naked-eye detection of p24 at ultralow concentrations with a conventional ELISA format could be a powerful alternative to costly nucleic acid-based tests for diagnosing HIV infection.1 However, to implement plasmonic ELISA in resource-constrained countries, it is also essential to demonstrate the robustness of the analytical procedure against possible interferences found in real samples. To study the impact of real matrices in the detection of p24, sera from 30 donors were assayed with plasmonic ELISA as shown in Fig. 5. 20 donors were HIV-infected patients whose viral load was determined with the nucleic acid-based test (Figs. 5a and 5b). Among these, 10 donors showed a viral load lower than 50 copies, and therefore could not be diagnosed by the nucleic acid-based test alone (Fig. 5b). 10 HIV-negative donors were also included to exclude the possibility of biased results due to non-specific interactions (Fig. 5c). A negative control consisting of PBS buffer was included in triplicate. With plasmonic ELISA, samples from HIV-negative donors yielded red nanoparticle dispersions, whereas samples from HIV-positive donors were clearly distinguished by their blue color, in accordance with the results shown in Fig. 4b. Remarkably, plasmonic ELISA was able to detect at a glance HIV-positive samples that were undetectable by the “gold standard” nucleic acid-based test (Fig. 5b). Moreover, the naked eye detection could be confirmed with a plate reader, since all the HIV-negative samples yielded a signal within three times the standard deviation of a negative control (± 0.009), while sera from HIV infected patients always generated a higher signal regardless of the viral load.

In conclusion, we have demonstrated the detection of analytes with the naked eye by imparting a new signal generation mechanism to conventional ELISA. The reduced cost and ultrasensitive detection of p24 could be useful for diagnosing HIV-infection in resource-constrained countries. One could envision that in the future the detection in decentralized studies could be even further improved if plasmonic ELISA is integrated with sophisticated microfluidic devices for in-field measurements of complex samples such as blood and plasma.20 Although the detection with the naked eye seems perfectly suited for detecting analytes in laboratories with fewer resources, it is inherently inaccurate for quantifying the concentration of the target molecule, and therefore assessing the exact concentration of the analyte may be difficult with plasmonic ELISA. This potential limitation is well justified by the extremely low limit of detection of plasmonic ELISA, which allows one to determine the presence of analytes that would otherwise be undetectable with classic colorimetric ELISA or with the polymerase chain reaction. The methodology proposed here could potentially be adapted for the detection of any analyte as long as antibodies directed against it were available, therefore making plasmonic ELISA a versatile tool for the detection other clinically relevant molecules at a glance.

Methods

Sandwich assay for PSA: 96-well polystyrene plates (Corning) were modified with mouse monoclonal anti-PSA (100 L, Abcam) diluted 1:300 in PBS at 4oC overnight. After washing the plates three times with wash buffer (R&D systems), the plates were blocked with blocking buffer (1 mg·mL-1 BSA in PBS) for 1h at room temperature. Subsequently, the plates were washed three times with wash buffer and PSA (100 L, Sigma) was added to the desired final concentration by diluting a stock solution with bovine serum (Invitrogen). After 2 hours, the plates were washed three times with wash buffer and rabbit polyclonal anti-PSA (100 L, Sigma) diluted 1:100 in blocking buffer was added for 2 hours at room temperature. Next, the plates were washed three times and biotinylated goat anti-rabbit IgG was added (100 L, Sigma) diluted 1:300 in blocking buffer for 1 h at room temperature. After washing three times, the streptavidin-catalase conjugate was added (100 L, see Fig. S11 in the Supplementary Information for conjugate preparation) diluted 1:300 in blocking buffer for 30 minutes at room temperature.

Sandwich assay for p24: 96-well polystyrene plates (Corning) were modified with goat anti-human IgG-Fc specific (100 L, Sigma) diluted 1:100 in bicarbonate buffer (100 mM, pH 9.6) for 2 h at room temperature. After washing three times with wash buffer, the plates were blocked with blocking buffer for 1h at room temperature. Then, human monoclonal anti-p24 (100 L, produced by Dr. S. Zolla-Pazner and provided by the Centre for AIDS Reagents, NIBSC (a Centre of the Health Protection Agency), UK ) diluted 1:300 in PBS was added at 4oC overnight. After washing the plates three times with wash buffer, p24 (100 L, Thermo Scientific) was added to the desired concentration by diluting a stock solution with undiluted human serum from a healthy donor (Sera Lab). Alternatively, undiluted serum samples from donors (100 L) were added to generate the data set shown in Fig. 5. After 2 hours, the plates were washed three times with wash buffer and rabbit polyclonal anti-p24 (100 L, Thermo Scientific) diluted 1:1000 in blocking buffer was added for 2 hours at room temperature. Next, the plates were washed three times and biotinylated goat anti-rabbit IgG was added (100 L, Sigma) diluted 1:300 in blocking buffer for 1 h at room temperature. After washing three times, the streptavidin-catalase conjugate was added (100 L, Fig. S11 in the Supplementary Information) diluted 1:300 in blocking buffer for 30 minutes at room temperature.

Nanoparticle growth (signal generation): After washing the plates three times with wash buffer, two times with PBS and once with deionized water, hydrogen peroxide (100 L, 240 M) in MES buffer (2-(N-morpholino)ethanesulfonic acid, 1mM pH 6.5) was added to each well of the plate. After 30 minutes, freshly prepared gold (III) chloride trihydrate (100 L, 0.2 mM) in MES buffer was added to each well. The absorbance at 550 nm was recorded after 15 minutes with a SpectraMax M5 plate reader (Molecular Devices). Photographs were taken after 15 (Fig. 3) or 30 minutes (Figs. 4 and 5) after the addition of the gold precursor. Experiments performed with different concentrations of hydrogen peroxide (Fig. 3) were performed in a same fashion but varying the concentration of reducing agent. TEM samples were prepared on copper-supported carbon films by depositing a drop of solution and letting it dry. TEM images were recorded with a JEOL JEM 2010 FEG-TEM microscope operating at an acceleration voltage of 200 kV.

Author contributions

R.R. elaborated the concept, designed and performed experiments and wrote the paper. M.M.S. supervised the project, participated in scientific discussions and revised the paper.

References

1. Patton, J.C., Coovadia, A.H., Meyers, T.M. & Sherman, G.G. Evaluation of the ultrasensitive human immunodeficiency virus type (HIV-1) p24 antigen assay performed on dried blood spots for diagnosis of HIV-1 infection in infants. Clin. Vaccine Immunol. 15, 388-391 (2008).

2. Tang, S. & Hewlett, I. Nanoparticle-based immunoassays for sensitive and early detection of HIV-1 Capsid (p24) antigen. J. Infect. Dis. 201, S59-S64 (2010).

3. Rodriguez-Lorenzo, L., de la Rica, R., Alvarez-Puebla, R., Liz-Marzan, L.M. & Stevens M.M. Plasmonic nanosensors with inverse sensitivity by means of enzyme-guided crystal growth. Nat. Mater. 11, 604-607 (2012).

4. Nam, J.M., Thaxton, C. S. & Mirkin C.A. Nanoparticle-based bio-bar codes for the ultrasensitive detection of proteins. Science 301, 1884-1886 (2003)

5. Rissin, D.M. et al. Single-molecule enzyme-linked immunosorbent assay detects serum proteins at subfemtomolar concentrations. Nat. Biotechnol. 28, 595-599 (2010)

6. Tabakman, M.N. et al. Plasmonic substrates for multiplexed protein microarrays with femtomolar sensitivity and broad dynamic range. Nat. Comm. 2, DOI: 10.1038/ncomms1477 (2011)

7. Laromaine, A., Koh, L.L., Murugesan, M., Ulijn, R.V. & Stevens, M.M. Protease-triggered dispersion of nanoparticle assemblies. J. Am. Chem. Soc. 129, 4156-4157 (2007)

8. de la Rica, R., Baldi, A., Fernandez-Sanchez, C. & Matsui, H. Single-cell pathogen detection with a reverse-phase immunoassay on impedimetric transducers. Anal. Chem. 81, 7732-7736 (2009)

9. de la Rica, R., Fratila, R.M., Szarpak, A., Huskens, J. & Velders, A.H. Multivalent nanoparticle networks as ultrasensitive enzyme sensors. Angew. Chem. Int. Ed. 50, 5703-5706 (2011)

10. Rodriguez-Lorenzo, L. et al. Zeptomol detection through controlled ultrasensitive surface-enhanced raman scattering. J. Am. Chem. Soc. 131, 4616-4618 (2009)

11. Chen, S., Svedendahl, M., Van Duyne, R.P.  & Käll M. Plasmon-Enhanced Colorimetric ELISA with Single Molecule Sensitivity. Nano Lett. 11, 1826-1830 (2011)

12. Kowalczyk, B., Walker, D.A., Soh S. & Grzybowski, B.A. Nanoparticle supracrystals and layered supracrystals as chemical amplifiers. Angew. Chem. Int. Ed. 49, 5737-5741 (2009).

13. Aili, D., Selegard, R., Baltzer, L., Enander, K. & Liedberg, B. Colorimetric Protein Sensing by Controlled Assembly of Gold Nanoparticles Functionalized with Synthetic Receptors. Small 5, 2445-2452 (2009)

14. Qu, W., Liu, Y., Liu, D., Wang, Z. & Jiang, X. Copper-Mediated Amplification Allows Readout of Immunoassays by the Naked Eye. Angew. Chem. Int. Ed. 50, 3442-3445 (2011)

15. Engelbrekt, C., Sørensen, K.H., Zhang, J., Welinder, A.C., Jensen, P.S. & Ulstrup, J. Green synthesis of gold nanoparticles with starch–glucose and application in bioelectrochemistry. J. Mat. Chem. 19, 7839-7847 (2009)

16. Thaxton, C.S. et al. Nanoparticle-based bio-barcode assay redefines ‘‘undetectable’’ PSA and biochemical recurrence after radical prostatectomy. Proc. Natl. Acad. Sci. USA 106, 18437-18442 (2009)

17. de la Rica, R. & Matsui, H. Urease as a nanoreactor for growing crystalline ZnO nanoshells at room temperature. Angew. Chem. Int. Ed. 47, 5415-5417 (2008)

17. Pejoux, C., de la Rica, R. & Matsui, H. Biomimetic Crystallization of Sulfide Semiconductor Nanoparticles in Aqueous Solution. Small 6, 999-1002 (2010)

19. de la Rica, R., Fabijanic, K.I., Baldi, A. & Matsui, H. Biomimetic crystallization nanolithography: simultaneous nanopatterning and crystallization. Angew. Chem. Int. Ed. 49, 1447-1450 (2010).

20. Fan, R. et al, Integrated barcode chips for rapid, multiplexed analysis of proteins in microliter quantities of blood. Nat Biotechnol. 26, 1373-1378 (2008).

Acknowledgements

We are thankful to G. S. Cooke and S. Kaye (Faculty of Medicine, Imperial College London) for the kind gift of human samples containing different viral loads. M.M.S. thanks the engineering and physical sciences research council (EPSRC) and European research council (ERC) starting investigator grant “Naturale” for funding. This research was supported by a Marie Curie Intra European Fellowship within the 7th European Community Framework Programme (R.R.). The monoclonal antibody to HIV-1 p24 from S. Zolla-Pazner was provided by the Centre for AIDS Reagents, National Institute for Biological Standards and Control (NIBSC) (a Centre of the Health Protection Agency), UK.

Additional information:

Supplementary information accompanies this paper at www.nature.com/naturenanotechnology. Reprints and permission information is available online at http://npg.nature.com/reprintsandpermissions/. Correspondence and requests for materials should be addressed to R.R. or M.M.S.

Figure captions

Figure 1. Schematic representation of the sandwich ELISA format used here and two possible signal generation mechanisms. In sandwich ELISA the target molecule is anchored to the substrate by capture antibodies and recognized by primary antibodies. In the present work, the enzyme is linked to the immunocomplex through interactions between enzyme-decorated streptavidin and biotinylated secondary antibodies. a, in conventional colorimetric ELISA enzymatic biocatalysis generates a coloured compound. b, in plasmonic ELISA the biocatalytic cycle of the enzyme generates coloured nanoparticle solutions of characteristic tonality (S: substrate, P: product, NP: nanoparticle).

Figure 2: Generation of coloured solutions for detection with the naked eye. a, In the presence of hydrogen peroxide, gold ions are reduced. b, High concentrations of hydrogen peroxide favour the formation of non-aggregated, spherical nanoparticles that give rise to a red solution. c, When the concentration of hydrogen peroxide decreases, for example due to the biocatalytic action of the enzyme catalase, aggregates of nanoparticles are formed and this turns the solution blue.

Figure 3. Generation of nanoparticle solutions with different colours depends on the concentration of hydrogen peroxide. Different concentrations of hydrogen peroxide were added to a solution containing gold ions (0.1 mM) in MES buffer (1mM, pH 6.5). a, Photograph showing the generation of nanoparticle solutions with different colours and intensities after 15 minutes. The tonality of the solution changes from red to blue between 120 and 100 M. b, UV-Vis spectra for the following hydrogen peroxide concentrations: 200 (●), 180 (●), 160 (●), 140 (●), 120 (●), 100 (●), 80 (●), 60 (●), 40 (●) and 20 (●) M. The LSPR peak red-shifts when the concentration of hydrogen peroxide is 100 M or lower. c,d, Transmission electron microscopy (TEM) images of nanoparticles grown with hydrogen peroxide with the concentration of 100 M (c) and 120 M (d). Scale bar in c is 50nm, and in d is 100nm. e, Graph showing the absorbance of the solutions at 550nm vary with the concentration of hydrogen peroxide.

Figure 4. Naked-eye detection of serum proteins with plasmonic ELISA. a, PSA. b, p24. PSA and p24 can be detected by the generation of blue nanoparticle solutions. The signal (-A550) is expressed as the decrease in absorbance with respect to the blank monitored at 550 nm. Blue curves were obtained by spiking PSA into bovine serum or p24 in female serum. Red curves were obtained by spiking the unrelated protein BSA. Error bars are the standard deviation of three independent measurements.

Figure 5. Detection of p24 in sera from donors with different viral loads. The order in the photograph is directly related to the order in the table. a, HIV-infected samples with a high viral load yield blue-coloured nanoparticle solutions. b, HIV-infected patients with a viral load undetectable with the nucleic acid-based test yield blue-coloured nanoparticle solutions; c) Non-infected HIV-negative (HIV-ve) donors yield red-coloured nanoparticle solutions.