Supporting Information

Double positively charged polyamide nanofiltration membrane with PEI/Zr4+ for Cr3+ and trimethoprim removal

Jinqiang Wang 1,2,4, Zhaoyang Su 1, Nigel J. D. Graham 3, Hongkai Liu 1, Kai Sun 4, Wenzheng Yu 1*

1 Key Laboratory of Drinking Water Science and Technology, Research Centre for Eco-Environmental Sciences, Chinese Academy of Sciences, Beijing, China, 100086

2 Center for Environment and Health in Water Source Area of South-to-North Water Diversion, School of Public Health, Hubei University of Medicine, Shiyan, China, 442000

3 Department of Civil and Environmental Engineering, Imperial College London, South Kensington Campus, London SW7 2AZ, UK

4 State Key Laboratory of Urban Water Resource and Environment, School of Environment, Harbin Institute of Technology, Harbin, China, 150001

wangjinqiangkgs@outlook.com; wangjinqiang@hbmu.edu.cn; zysu@rcees.ac.cn; n.graham@imperial.ac.uk; liuliu9900@163.com; ksun@hit.edu.cn; wzyu@rcees.ac.cn

Figure S1. Molecular structures of (a) polyamide layer, (b) hyperbranced PEI, (c)NHS, (d) EDC and (e) trimethoprim.

Figure S2. The real installation of “dead-end” nanofiltration system: ① nitrogen gas cylinder; ② relief value; ③ ultrafiltration cup; ④ electronic balance; ⑤ computer (recording one data per second).

Figure S3. The solute in the feed solution is divided into three parts during the filtration process: (1) interception in the concentrate solution (Mi, mg); (2) adsorption on the surface of the NF membrane (Ma, mg); (3) permeance in the filtrate solution (Mp, mg). Vf, Vp and Vc are the volume (L) of the feed solution, filtrate solution and concentrate solution, respectively; Cf, Cp and Cc are the concentration (mg/L) of the feed solution, filtrate solution and concentrate solution, respectively.

Table S1 The contents of C, N and O elements and the ratio of elements on the surface of PA, PEI-PA and PEI/Zr4+-PA NF membranes.

|  | Content of Elements (%) |  |  |  | Ratio of Elements |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | C1s | N1s | O1s | Zr3d | O/N | C/O | C/N |
| PA | 69.51 | 9.39 | 20.07 | 0.06 | 2.14 | 3.46 | 7.40 |
| PEI-PA | 70.2 | 15.89 | 13.26 | 0.02 | 0.83 | 5.29 | 4.42 |
| PEI/Zr4+-PA | 69.7 | 16.98 | 13.13 | 0.19 | 0.77 | 5.31 | 4.10 |