Effect of Crystal Habits on the Surface Energy and Cohesion of Crystalline Powders

Umang V. Shaha, Dolapo Olusanmib, Ajit S. Narangb, Munir A. Hussainb, John F. Gamblec, Michael J. Tobync, Jerry Y. Y. Henga,*

a	Surfaces and Particle Engineering Laboratory (SPEL), Department of Chemical Engineering, Imperial College London, South Kensington Campus, London SW7 2AZ, UK

b   Bristol-Myers Squibb Pharmaceuticals, 1 Squibb Drive, New Brunswick, NJ 08903, USA

c   Bristol-Myers Squibb Pharmaceuticals, Reeds Lane, Moreton, Wirral CH46 1QW, UK

*Corresponding Author: jerry.heng@imperial.ac.uk

Phone: +44-(0)207-594-0784. Fax: +44-(0)207-594-5700 Web: www.imperial.ac.uk/spel

Abstract

The role of surface properties, influenced by particle processing, in particle-particle interactions (powder cohesion) is investigated in this study. Wetting behaviour of mefenamic acid was found to be anisotropic by sessile drop contact angle measurements on macroscopic (>1 cm) single crystals, with variations in contact angle of water from 56.3o to 92.0o. This is attributed to variations in surface chemical functionality at specific facets, and confirmed using X-ray Photoelectron Spectroscopy (XPS). Using a Finite Dilution Inverse Gas Chromatography (FD-IGC) approach, the surface energy heterogeneity of powders was determined. The surface energy profile of different mefenamic acid crystal habits was directly related to the relative exposure of different crystal facets. Cohesion, determined by a uniaxial compression test, was also found to relate to surface energy of the powders.  By employing a surface modification (silanisation) approach, the contribution from crystal shape from surface area and surface energy was decoupled.  By “normalising” contribution from surface energy and surface area, needle shaped crystals were found to be ~2.5× more cohesive compared to elongated plates or hexagonal cuboid shapes crystals.

Key Words: Crystal Habit, Surface Energy Heterogeneity, Macroscopic Single Crystal, Solvent Polarity, Crystal Aspect Ratio, Cohesion

- Introduction

The role of the physicochemical properties of particulate pharmaceutical materials on their cohesion and powder flow properties has attracted extensive research interest in the past four decades (Feng et al., 2007; Kaerger et al., 2004; Lam and Nakagawa, 1994; Podczeck and Mia, 1996; Podczeck and Révész, 1993; Ridgway and Morland, 1977).  Understanding the role of physicochemical properties on cohesion and the development of strategies to control cohesion by tailoring the properties of pharmaceutical materials may be critically important for efficient and cost effective processing (Hou and Sun, 2008).  The effect of particle shape and size on powder flow and cohesion is referred extensively in the literature (Jones et al., 2003).  Moreland and Ridgway were the first to report the effect of particle shape on bulk density (Ridgway and Morland, 1977).  Podczeck and Mia reported the effect of particle size and shape on the Hausner ratio and angle of internal friction (Podczeck and Mia, 1996).  They found particles with higher aspect ratio (needle shaped crystal) showed a higher angle of internal friction. Kaerger et al. investigated the effect of particle shape and size on flow and compaction behaviour of blends, reporting that blends containing spherical paracetamol particles (prepared using crystallisation by sonication) with microcrystalline cellulose had improved flow properties compared to micronised particles (Kaerger et al., 2004).  Gamble et al. investigated the effect of different sub-populations e.g. agglomerates and primary particles, highlighting the effect of the presence of agglomerates in enhancing the flow properties of bulk primary particles (Gamble et al., 2011).  Di Martino et al. studied the effect of different crystal shapes of ibuprofen on compression and flow properties, highlighting improved densification of the smooth coin type crystal habit compared to other crystals habits, which were attributed to the increase in powder bed porosity.

Crystals of the same polymorphic form with different crystal shapes (habits) can be obtained by varying the relative growth rates of the different crystals facets.  This in turn, can be dependent on material intrinsic properties or be affected by properties of the crystallisation solvent, crystal growth inhibitors or additives (Berkovitch-Yellin, 1985; Bourne and Davey, 1976; Lovette et al., 2008). Crystal habits not only determine the main bulk properties of the crystalline material (e.g. bulk density, flowability and mechanical strength) but also alter the surface energy (Ho et al., 2012).

Surface energy of crystalline pharmaceutical materials has been shown to be anisotropic (Heng et al., 2006a, 2007; Ho et al., 2008; Ho et al., 2010). Facet specific surface energy of organic crystalline material was directly correlated with the chemical functional groups exposed on the crystal facet surfaces using contact angle and X-ray Photoelectron Spectroscopy (XPS) measurements. Considering the facet specific surface energy of a crystalline material, it is postulated that surface energetics of the crystalline powders depend on the relative surface energy contributions of the different crystal facets. Using D-mannitol as a model system, Ho et al. demonstrated that decreasing the aspect ratio of needle shaped crystals resulted in a decreasing shift in the overall contribution of the dispersive component of the surface energy. This was attributed to the increasing contribution of the facet showing lowest dispersive component of surface energy  (facet (011)) (Ho et al., 2012). The ability to tailor crystal habits will result in the change in the relative contribution of different crystal facets. This change will result in a dissimilar surface energy of the crystalline powders, which may have an impact on powder cohesion.

Although it is well known that particle-particle interactions, e.g. cohesion/ adhesion, are governed by the surface, the effect of crystal shapes on powder flow properties have not considered the impact of the anisotropic surface properties of the crystals. Considering that particle shape, surface energy and surface area can influence flow properties, it is essential to understand the contribution of each of these factors.

This study aims to firstly study the effect of crystal habit on surface energy and cohesion of crystalline pharmaceutical powders. Secondly, an approach to decouple the contributions of surface energy and particle shape is presented. Mefenamic Acid, a non-steroidal, anti-inflammatory drug, is used as a model compound. Macroscopic single crystals of mefenamic acid are grown and used for determining facet specific surface energies. This is then correlated to the surface energy heterogeneity measurements of crystalline powders of mefenamic acid crystallised in different crystal habits. Cohesion values of different shape mefenamic crystal were measured using a uniaxial compression test. Results were correlated with surface energy and crystal shape to elucidate their respective effect on cohesion. Further, the effect of surface energy on cohesion was “normalised” with silanisation of mefenamic acid, allowing de-coupling the contribution of crystal shape on cohesion from that of surface energy and surface area.

- Materials

Mefenamic acid (2-(2, 3-dimethylphenyl) amino benzoic acid) (99.0% Sigma Aldrich, Dorset, UK), acetone (>99.5%) and methanol (>99.5%) were obtained from VWR BDH Prolabo, Lutterworth, UK and used for growth of a macroscopic single crystal of mefenamic acid.  Toluene (>99.5%), diethyl ether (>99.5%), ethyl acetate (>99.5%), dichloromethane (>99.0%), acetone (>99.5%), isopropyl alcohol (>99.5%) and methanol (>99.5%) were all received from VWR BDH Prolabo, Lutterworth, UK and used without further purification for crystallisation of different crystal habits of mefenamic acid.  Deionised water, ethylene glycol (>99.0%, Sigma Aldrich, Dorset, UK), formamide (>99.5%, Acros Organics, Loughborough, UK) and diiodomethane (>99.0%, Acros Organics, Loughborough, UK) were used as probe liquids for contact angle measurements.  n-hexane (>99.0%), ethyl acetate (>99.5%), and dichloromethane (>99.5%) were obtained from VWR BDH Prolabo, Lutterworth, UK ), whereas n-heptane (99.0), n-octane (99.0%), n-nonane (99.0%), and n-decane (99.0%) were obtained from Sigma Aldrich, Dorset, UK and used without further purification as  probe liquids in inverse phase gas chromatography.

3. Methods

3.1 Growth of Mefenamic Acid Macroscopic Single Crystal

Mefenamic acid seed crystals of a few millimetres in size were obtained from slow evaporation of a supersaturated solution of mefenamic acid in acetone or methanol at room temperature. Macroscopic single crystals were obtained by slow solvent evaporation from saturated methanol solution at room temperature.  A saturated solution of mefenamic acid in methanol was prepared under constant stirring.  A single seed of mefenamic acid crystal was tied with an aramid fibre and suspended in the saturated solution, which is kept without stirring. Slow evaporation of the solvent was maintained resulting in the crystal growth. The saturated solution of mefenamic acid in methanol was periodically changed.  Macroscopic single crystals of mefenamic acid obtained were dried under ambient conditions and used for further characterisation and contact angle measurements.

3.2 Crystallisation of Mefenamic Acid from Different Solvent Systems

Saturated solutions of mefenamic acid in seven different organic solvents with varying polarity were prepared at 50 oC. A single step cooling profile was adopted.  Saturated solutions of mefenamic acid at 50 oC were transferred to an incubator (Surface Measurement Systems Ltd., London, UK) maintained at 4 oC. Mefenamic acid crystals obtained after 24 hours were filtered through general-purpose laboratory filter paper (Whatman, UK) and dried under ambient conditions. Dried crystals were stored in the glass container and used for further characterisation.

3.3 Silanisation of Mefenamic Acid Powders

Recrystallised mefenamic acid powders were silanised using a protocol reported in the literature (Al-Chalabi et al., 1990).  In a typical process, 500 mg of mefenamic acid powder was added to a 50 mL 5% (v/v) solution of dichlorodimethylsilane in cyclohexane. The mixture was refluxed at 80 oC for 24 hours. Then, the reaction mixture is allowed to cool down to room temperature and filtered using general-purpose laboratory filter paper (Whatman, UK) followed by drying in a vacuum oven at 80 oC for 4 hours.  Post silanisation, the silanised mefenamic acid powders were stored in a glass vial at ambient conditions.

3.4 Single Crystal X-ray Diffraction for Crystal Facet Indexing

The indexing of the crystal faces was performed using an Oxford Diffraction Xcalibur 3E diffractometer (Agilent Technologies, Oxford, UK) equipped with ceramic XRD C-tech tube and Oxford Diffraction Sapphire detector. Single crystal X-ray diffraction data was obtained at 50 kV and 40 mA.  Based on the single crystal X-ray diffraction data crystal facets were indexed using Agilent CrysAlisPro (Agilent Technologies, Oxford, UK) software system.

3.5 Contact Angle Measurements of a Macroscopic Single Crystal

A Krüss Drop Shape Analyser DSA 10 (Krüss GmbH, Hamburg, Germany) was used for the static sessile drop contact angle measurement. Analytical grade DI water, diiodomethane, ethylene glycol and formamide were used as probe liquids and the measurements were carried out at ambient conditions.  Properties of probe liquids can be found in existing literature (Heng et al., 2006b).  The shape of the droplet was fitted with a tangent method to obtain the contact angle using the Drop Shape Analysis software (DSA version 1.0, Krüss GmbH, Hamburg, Germany). A minimum of 3 droplets on 4 different crystals facets of a macroscopic single crystal was measured. The measurements were repeated for two different single crystals.

3.6 Surface Energy Analysis

Surface Energy Analyser (SEA) (Surface Measurement Systems Ltd., London, UK), equipped with flame ionisation detector, was used to characterise the surface energy heterogeneity for mefenamic acid powders. ~1 g powders of different crystal habits were separately packed into pre-silanised iGC columns and conditioned with helium purge for 2 hours at 30 oC, followed by pulse injection measurements. Methane was used to determine column dead time and helium was used as a carrier gas. A series of dispersive n-alkane probes (hexane, heptane, octane, nonane and decane) at a range of concentrations were injected with an objective of obtaining target surface coverage (n/nm) ranging from 0.7% to 10% to determine adsorption isotherms. The dispersive surface energy is then calculated using the Schultz method (Schultz et al., 1987). Mono-polar probes (dichloromethane and ethyl acetate) were injected at the same series of concentrations to determine non-dispersive interactions. Surface energy due to the non-dispersive interactions was calculated using the vOCG method reported in the literature (Das et al., 2010; Van Oss et al., 1988). Detailed method for determining surface energy heterogeneity can be referred from Ho and Heng (Ho and Heng, 2013).

3.7 Surface Area Analysis

Approximately 1 g of crystalline mefenamic samples was conditioned under helium purge at 40 oC for at least 12 hours, and the mass of samples post-conditioning is measured. A fully automated Micromeritics Tristar 3000 (Micromeritics, Norcross, USA) system was used for the measurement of isotherms at -195.8 oC. The surface area was calculated using the BET model (Brunauer et al., 1938) based on the linear region of the nitrogen adsorption isotherm (from p/po = 0.05 to 0.3) using the Micromeritics Analysis Software (Micromeritics, Norcross, USA).

3.8 Particle Size and Shape Analysis

Morphologi G3S particle characterisation system (Malvern Instruments Ltd., Malvern, UK) equipped with dry powder dispersion unit was used for particle shape and size analysis. Particles were dry dispersed using the dry sample dispersion unit on a sample glass plate mounted on an automatic stage. Particle imaging was conducted using a 20x lens with the vertical z-stacking enabled to obtain information for the three dimensionality of the sample. Raw data were filtered using the analysis software (version 8.0) to remove partially imaged or overlapping particles on a sample by sample basis using a combination of convexity, solidity and particle width filters. Details of the data analysis method can be found elsewhere (Gamble et al., 2011).

3.9 Scanning Electron Microscopy

Mefenamic acid powders were stuck on the stubs using carbon adhesive tape and coated with gold.  SEM images were obtained with table-top scanning electron microscope (Hitachi High-Technologies Europe GmbH, Krefeld, Germany) at an acceleration voltage of 15 kV. The SEM was equipped with a solid-state backscatter detector and operated in a standard imaging mode for obtaining the images.

3.10 Polymorph Identification

Powder X-ray diffraction spectra for the Mefenamic acid powders were measured using a PANalytical X’Pert Pro MPD (PANalytical B.V., Almelo, Netherlands). Measurements were performed at 40 mA and 40 kV. Diffraction data was collected using a CuK X-ray source (1.541 Å) with Nickel filter, a fixed 10 mm mask, a soller slit of 0.04 rad, an antiscatter slit of 1/2o and a divergence slit of 1/4o, over an angular range from 5o–60o 2θ in continuous scan mode using step size of 0.08o 2θ and time per step of 35s.

3.11 Uniaxial Compression Test

Powder cohesion was measured using a simple method adopted from the test originally developed for soil mechanics (ASTM D2166, BS1377: Part 7: 1990:7.2 and BS 1377: Part 2: 1990 7.3) (Head, 1994). Cylindrical compacts were prepared using 5mm evacuable IR die (Specac Ltd., Slough, UK) at a minimum of three different compaction loads using an SMS texture analyser TA.XT2i (Stable Micro Systems Ltd., Godalming, UK). The compacts varied in height depending on the bulk density of the material; however, the L/D ratio of at least 2:1 was maintained for the compacts. Unconfined yield strengths of the compacts were measured using texture analyser. All the measurements were performed with a 36 mm diameter cylindrical aluminium probe and a 5 kg load cell using a displacement compression mode with test speeds of 0.02 mm/s. Yield stress was determined following the above mentioned method for compacts prepared at minimum of three different compaction loads.

- Results

4.1 Anisotropic Wettability of Mefenamic Acid Crystals

Three different polymorphs of mefenamic acid are reported. All three polymorphs are known to be triclinic with space group P1, however with different lattice parameters (SeethaLekshmi and Guru Row, 2012).  Single crystals X-ray diffraction analysis revealed the crystals to be of form-I with crystal lattice parameters a=14.6 Å, b=6.8 Å and c=7.7 Å; α=119.6 o, β=103.9 o, γ=91.3o, which agrees well with the crystal structure for polymorphic form-I reported in the Cambridge crystal Structural Database (CSD) (Ref Code: XYANAC). Single crystal X-ray diffraction was used to index crystals from crystallisation solvent methanol and found to have four major indexed facets (001), (112), (100) and (011).

The contact angles of water, formamide, ethylene glycol and diiodomethane were measured on available facets of the form-I mefenamic acid crystals.  Contact angles determined for a minimum of three droplets on two different crystals are reported in Table 1. Contact angle measurements demonstrated that, particularly for the water probe, sessile drop contact angle varies for crystal facets (001), (011) and (112), (100).  Contact angles for water vary from 56o for (001) to 92o for (112). This confirms anisotropic wettability of the mefenamic acid crystal. The order of hydrophilicity for different facets, considering water contact angle measurements, is as follows: (001) > (100) > (011) > (112).

The differences in the contact angles can be explained by the variations in the local surface chemistry, differences in type and density of functional groups on different crystal facets. Based on crystallographic evaluation of mefenamic acid form-I, the phenyl ring with the carboxylic acid functional group and the imino bridge is found to be coplanar.  The carbonyl functional group accepts a hydrogen bond from the amine and forms the imino bridge. Furthermore, due to the carboxylic acid functional group’s tendency to self-associate, mefenamic acid molecules form symmetric dimers and adjacent dimers are linked through C-H interactions involving aromatic C-H and alkylated phenyl ring (SeethaLekshmi and Guru Row, 2012). Planes form different crystal facets, which slices through the crystal at different angles resulting in different proportions of functional end groups on different crystal facets. Crystallographic structures at the (001) and (112) facets, generated from mefenamic acid polymorphic form-I structure obtained from CSD using Mercury software, shows –OH functional group exposed on the surface with H-bonding potential for facet (001), whereas negligible H-bonding potential was observed for facet (112). The –OH functional groups, which are not involved in any hydrogen bonding in the crystal structure and available to act as electron donor (O) and acceptor (H) are considered to be available to interact with probe liquid for contact angle measurements.

This analysis provides only an estimate of the potential contribution of hydroxyl as well as methyl functional groups on the surface.  Investigating molecular orientation for individual crystal facets using Mercury software, facet (100) was found to have the highest concentration of available hydroxyl functional groups per unit area, whereas facet (112) has no hydroxyl functional group available.  Considering the fact that (112) has no hydroxyl groups and has the presence of methyl groups, it is the most hydrophobic crystal facet. However, though facet (100) has the highest hydroxyl group density, methyl group density is equally high, which limits its hydrophilicity. Facet (001) has moderate density of hydroxyl groups and also contains equal density of carbonyl group (electron donor), both of which can participate in hydrogen bonding. For facet (001), the density of groups that can participate in hydrogen bonding is equal to that of facet (100) and absence of methyl functional group on facet (001) may result in higher hydrophilicity of the facet.

Facet (100) has a higher concentration of hydroxyl groups and an equivalent concentration of methyl groups per unit area compared to (011). The higher hydrophilicity of facet (100) compared to facet (011) can be attributed to the higher concentration of the hydroxyl functional groups per unit cell area. However, analysis here provide first order estimation of contribution from different functional groups, it does have limitations. Surface contributions of phenyl group as well as surface orientation of hydroxyl, carbonyl or methyl functional group is not considered in the analysis.

Facet specific surface chemistry of mefenamic acid single crystals was characterised using X-ray photoelectron spectroscopy. The order of polarity determined by XPS, which is in agreement with the hydrophilicity order as calculated on the basis of sessile drop contact angle for water as a probe liquid ((001) > (100) > (011) > (112)).

4.2 Effect of Crystal Habit on Surface Energy

4.2.1 Preparation of Crystals with Varying Crystal Habits

It is well documented in the literature that crystal-solution interface determines many interfacial physical phenomena. In the current context this relates to crystal growth and wetting (Berkovitch-Yellin, 1985; Bourne and Davey, 1976; Lovette et al., 2008). Crystal surface contribution at the solvent interface may be different from the bulk crystallographic structure, which depends on possible reconstruction and relaxation of surface. For solvents, atomic arrangement at the interface is postulated to be relatively ordered compared to bulk liquid, considering the periodic potential it experiences at the crystal surface (Bourne and Davey, 1976; Davey et al., 1988). Despite of extensive research, a well characterised mechanism by which solution-crystal interface influences crystal growth is elusive (Singh and Banerjee, 2013).

Solvents varying in the polar component of the Hansen solubility parameter, ranging from 1.4 MPa1/2-12.3 MPa1/2 (which represents energy from dipolar intermolecular forces between molecules) (Hansen, 2007), were used for crystallisation of mefenamic acid to investigate effect of crystallisation solvent polarity on crystal habits. Crystals obtained from different solvent systems are shown in Figure 1. It is evident from the scanning electron micrographs that mefenamic acid crystals grown from non-polar solvents such as toluene and diethyl ether result in needle shape crystals (Figure 1(a)), mefenamic acid crystals grown from polar aprotic solvents such as ethyl acetate, dichloromethane and acetone result in elongated plate shape crystals (Figure 1(b), (c) and (d)), whereas mefenamic acid grown from polar protic solvents such as isopropyl alcohol and methanol result in hexagonal cuboid shaped crystals (Figure 1(e), (f)). Quantitative analysis of the crystal elongation was conducted using image analysis of the crystals obtained from all seven different solvent systems using Malvern Morphologi G3S (see section 4.2.2.)

Powder X-ray diffraction spectra were obtained for mefenamic acid crystals obtained from all seven solvent systems. X-ray diffraction patterns obtained were compared with the reference powder spectrum reported in CSD for mefenamic acid form-I (Ref Code: XYANAC) (Figure 2) and powder X-ray diffractograms for mefenamic acid crystal form-II and III by SeethaLekshmi and Guru Row (SeethaLekshmi and Guru Row, 2012). Crystals obtained from all seven solvent systems were identified to be of polymorphic form-I, which is known to be the most stable crystal polymorph. Analysis of the powder diffraction spectra from different crystal habits showed varying peak intensity, which depends on the amount of sample used, particle size, packing and sample thickness (Pecharsky and Zavalij, 2005). In addition to the variations in peak intensity, a peak at ~12.6o 2 was observed for the mefenamic acid crystals obtained from all solvents except toluene, and this peak was more prominent for mefenamic acid crystals obtained from methanol and acetone. Referring to the reference pattern for form-I mefenamic acid, a weak peak at ~12.66o 2 can also be found. This peak is not observed in the powder X-ray diffraction patterns for mefenamic acid form-II or III. Although, no correlation between peak intensity and differences in crystal aspect ratio or relative surface area ratio of crystal facets was observed, it is important to note that all diffractograms matches with that of mefenamic acid form-I.

4.2.2 Effect of Crystal Habit on Surface Energy

The γd distributions of the mefenamic acid crystals with varying crystal habits are summarised in Figure 3. An ascending trend in the γd profiles, whereas descending trend in γAB profiles was observed with descending crystal elongation (Figures 4 and 5), i.e. considering two different extremes, γd for needle shape crystals, which were obtained from toluene, ranges from 42.1 mJ/m2 to 39.9 mJ/m2, whereas for hexagonal cuboids shape crystals, γd ranges from 51.3 mJ/m2 to 46.4 mJ/m2 from the lower to higher fractional surface coverage (0.7%-10%).

Ascending γd profiles with descending crystal elongation can be attributed to increasing/decreasing relative contribution of different crystal facets with changing crystal habits. To investigate the effect of the relative contribution of different facets on γd profile, we consider contribution from two major facets namely (001) and (112) and how it varies with different crystallisation solvents.

Mefenamic acid crystal facet (001) is demonstrated to have –OH, –C=O and –C6H5 functional groups exposed on the surface which can result in strong hydrogen bonding interactions between facet (001) and protic-polar solvents (Davey et al., 1988), whereas the surface of facet (112) has –CH3 and –C6H5 functional end groups resulting in very weak polar interaction, which can result in strong interaction with the non-polar solvents e.g. DEE. With changing solvent polarity from the non-polar to polar-protic and polar-aprotic solvent, solvent interaction with crystal facet (112) will decrease and interaction with crystal facet (001) will increase. Bourne and Davey proposed that favourable interaction between the solvent with a particular crystal facet results in reduction of interfacial tensions, resulting in enhanced growth of the crystal facet.

Bourne and Davey explained the growth of sucrose from aqueous solutions with this mechanism (Bourne and Davey, 1976). Considering the mechanism proposed by Bourne and Davey, with increasing solvent polarity, increase in solvent interaction with mefenamic acid crystal facet (001) can result in increased growth of that facet, resulting in lower morphological importance of facet (001) compared to facet (112). This can result in lowering the relative contribution of facet (001) compared to (112) and leading to a change in crystal habit from elongated needles to hexagonal cuboids. This is consistent with the experimental observations reported in section 4.2.1. As the relative contribution of facet (001) decreases with increasing solvent polarity, crystals obtained with methanol will have a lower relative contribution compared to crystals obtained from toluene and reverse is true for the (112) facet.

The shapes of crystals obtained from ethyl acetate, dichloromethane and isopropyl alcohol are needles, elongated plates and hexagonal cuboids, while surface area of crystals obtained from all three solvents are 0.29 m2/g, 0.24 m2/g, and 0.15 m2/g, respectively.

γd at a fractional coverage (n/nm = 0.04) is shown as a function of solvent polarity in Figure 4, and suggest that γd increases with increasing solvent polarity. Figure 5 shows acid-base component of surface energy as a function of solvent polarity.  Acid-base surface energy at a fractional surface coverage of 0.04 was found to vary with increasing solvent polarity.  Although some scatter in the data can be observed, a weak trend of reducing acid-base surface energy with increasing solvent polarity was observed.  Decrease in acid-base surface energy can be explained by lower relative contribution from facet (001).

In the current analysis, the γd distribution is dependent on elongation rather than particle size or indeed the BET surface area as the data is normalised for surface coverage. This further confirms that the relative exposure of different crystal facets plays a crucial role in overall surface energy of powder samples.

4.3 Effect of Crystal Habits on Cohesion

Unconfined yield stresses were measured using a uniaxial compression test as adapted from the literature (Wang, 2013). Figure 6 shows the unconfined yield stresses for mefenamic acid crystals obtained from seven different crystallisation solvents measured at three different consolidation stresses ranging from 500 - 2500 kPa. Yield stress (Y-axis) was plotted as a function of consolidation stress (X-axis). The cohesion value was determined by linear extrapolation of the yield stress best-fit line at different consolidation stresses and with an angle of friction being a tan-1 function of the gradient of the best-fit line.  Further details of the theory of the uniaxial compression can be found elsewhere (Head, 1994; Wang, 2013). Cohesion as a function of the polar component of the Hansen solubility parameter for the different crystallisation solvents used is shown in Figure 7. The data suggest that the use of crystallisation solvents tend to result in crystals with lower crystal elongation, and thereby decreasing cohesion. Higher cohesion for mefenamic acid crystal obtained from toluene (elongated needle shape) can be attributed to the high surface area of the crystals and high surface exposure of polar functional groups (Waknis et al., 2014). Comparing cohesion for mefenamic acid crystals obtained from ethyl acetate (needle shaped crystals) with isopropyl alcohol and dichloromethane, where surface area is comparable; cohesion is found to decrease from 5.7 kPa for ethyl acetate to 3.5 kPa for isopropyl alcohol and 1.8 kPa for dichloromethane. Higher cohesion of needle shaped crystals can be attributed to the combined effect of crystal shape and surface energy.

4.4 Isolating Contribution of Crystal Habit on Cohesion

This study investigates the effect of crystal shape on cohesion by isolating the effect of surface energy.  The approach adopted here is to modify the surface chemistry of recrystallised mefenamic acid powders by silanisation. The modification is expected to result in the formation of silane layers on the particulate surface with target functional end groups, methyl for this study. Mefenamic acid powders crystallised from three different solvents were functionalised with dichlorodimethylsilane resulting in methyl functional end groups and confirmed using X-ray Photoelectron Spectroscopy.  Powder X-ray diffraction (PXRD) was used for characterisation of crystallinity of mefenamic acid post silanisation. Results of PXRD pre and post silanisation, detected no change in crystallinity as a result of silanisation.

Figure 8 presents the surface energy heterogeneity profiles before and after silanisation of mefenamic acid crystals obtained from ethyl acetate, dichloromethane and isopropyl alcohol. It is evident that post silanisation, mefenamic acid crystals with three different shapes (needles, elongated plates and hexagonal cuboids) show very similar surface energy heterogeneity profile. Further to that, as a result of silanisation, the surface becomes energetically homogeneous resulting in γd changing from ~34.0 mJ/m2 to ~32.0 mJ/m2 with variation in fractional surface coverage from 0.7% to 10%. Silanisation has normalised the effect of surface energy on cohesion. The silanised samples have similar surface area and surface energy but distinct crystal habit, which allows the contribution of crystal habit (quantified by crystal elongation) on cohesion to be determined.

Figure 9 reports, unconfined yield stress measurements for mefenamic crystals before and after silanisation. Post silanisation cohesion value calculated for mefenamic acid crystals obtained from ethyl acetate was 2.3 kPa, compared to 0.93 kPa for mefenamic crystals obtained from dichloromethane and 0.90 kPa for mefenamic acid crystals obtained from isopropyl alcohol.  Cohesion values obtained post silanisation represent cohesion after “normalising” effect of surface energy and surface area, thus revealing that needle shaped crystals show ~2.5× higher cohesion compared to hexagonal cuboids or elongated plate shaped crystals for mefenamic acid.

- Conclusion

Facet specific energetics of a macroscopic single crystal of mefenamic acid can be related to the surface energetic profiles of the corresponding powder samples. Mefenamic acid crystal with different crystal habits ranging from elongated needles to hexagonal cuboids, were obtained by varying the crystallisation solvent polarity. The surface energy profiles of mefenamic acid powders with varying crystal habits were correlated to the relative exposure of different crystal facets. Elongated needle shaped mefenamic acid crystals were found to be about eight times more cohesive compared to hexagonal cube shaped crystals. This was attributed to the combined effect of surface energy and surface area of the mefenamic acid crystals. Contribution from crystal shape on cohesion of mefenamic acid was decoupled from that of surface energy and surface area. By “normalising” contribution from surface area and surface energy on cohesion, hexagonal cuboid or elongated plate shaped crystals was found to be ~2.5× less cohesive compared to the needle shaped crystals. This study has demonstrated potential for tailoring particle surface properties with a specific aim to control cohesion by crystal habit engineering.

Acknowledgement

We thank Dr. Andrew J. White for help with collecting and analysing single crystal X-ray diffraction data and crystal indexing using the CrysAlisPro software package, and Jose V. Parambil for his help with Material Studio software package.

References

Al-Chalabi, S.A.M, Jones, A.R., Luckham, P.F., 1990, A simple method for improving the dispersability of micron-sized solid spheres. J. Aerosol Sci. 21, 821-826.

Berkovitch-Yellin, Z., 1985. Toward an ab initio derivation of crystal morphology. J. Am. Chem. Soc. 107, 8239-8253.

Bourne, J.R., Davey, R.J., 1976. The role of solvent-solute interactions in determining crystal growth mechanisms from solution: I. The surface entropy factor. J. Cryst. Growth 36, 278-286.

Brunauer, S., Emmett, P.H., Teller, E., 1938. Adsorption of gases in multimolecular layers. J. Am. Chem. Soc. 60, 309-319.

Das, S.C., Larson, I., Morton, D.A.V., Stewart, P.J., 2010. Determination of the polar and total surface energy distributions of particulates by inverse gas chromatography. Langmuir 27, 521-523.

Davey, R.J., Milisavljevic, B., Bourne, J.R., 1988. Solvent interactions at crystal surfaces: the kinetic story of .alpha.-resorcinol. J. Phys. Chem. 92, 2032-2036.

Feng, Y., Grant, D.J.W., Sun, C.C., 2007. Influence of crystal structure on the tableting properties of n-alkyl 4-hydroxybenzoate esters (parabens). J. Pharm. Sci. 96, 3324-3333.

Gamble, J.F., Chiu, W.S., Tobyn, M.J., 2011. Investigation into the impact of sub-populations of agglomerates on the particle size distribution and flow properties of conventional microcrystalline cellulose grades. Pharm. Dev. Technol. 16, 542-548.

Hansen, C.M., 2007. Hansen Solubility Parameters: A User's Handbook. 2nd Ed. CRC Press: Boca Raton, FL. p179-182.

Head, K.H., 1994. Manual of soil laboratory testing, 2 ed. Pantech Press, New York.

Heng, J.Y.Y., Bismarck, A., Lee, A.F., Wilson, K., Williams, D.R., 2006a. Anisotropic surface energetics and wettability of macroscopic form I paracetamol crystals. Langmuir 22, 2760-2769.

Heng, J.Y.Y., Bismarck, A., Lee, A.F., Wilson, K., Williams, D.R., 2007. Anisotropic surface chemistry of aspirin crystals. J. Pharm. Sci. 96, 2134-2144.

Heng, J.Y.Y., Thielmann, F., Williams, D.R., 2006b. The effects of milling on the surface properties of form I paracetamol crystals. Pharm. Res. 23, 1918-1927.

Ho, R., Heng, J.Y.Y., 2013. A review of inverse gas chromatography and its development as a tool to characterize anisotropic surface properties of pharmaceutical solids. Kona Powder Part. J.	 30, 164-180.

Ho, R., Heng, J.Y.Y., Dilworth, S.E., Williams, D.R., 2008. Wetting behavior of ibuprofen racemate surfaces. J. Adhes. 84, 483-501.

Ho, R., Hinder, S.J., Watts, J.F., Dilworth, S.E., Williams, D.R., Heng, J.Y.Y., 2010. Determination of surface heterogeneity of d-mannitol by sessile drop contact angle and finite concentration inverse gas chromatography. Int. J. Pharm. 387, 79-86.

Ho, R., Naderi, M., Heng, J.Y.Y., Williams, D.R., Thielmann, F., Bouza, P., Keith, A., Thiele, G., Burnett, D., 2012. Effect of milling on particle shape and surface energy heterogeneity of needle-shaped crystals. Pharm. Res. 29, 2806-2816.

Hou, H., Sun, C.C., 2008. Quantifying effects of particulate properties on powder flow properties using a ring shear tester. J. Pharm. Sci. 97, 4030-4039.

Jones, R., Pollock, H.M., Geldart, D., Verlinden, A., 2003. Inter-particle forces in cohesive powders studied by AFM: effects of relative humidity, particle size and wall adhesion. Powder Technol. 132, 196-210.

Kaerger, J.S., Edge, S., Price, R., 2004. Influence of particle size and shape on flowability and compactibility of binary mixtures of paracetamol and microcrystalline cellulose. Eur. J. Pharm. Sci. 22, 173-179.

Khoo, J.Y., Shah, U.V., Schaepertoens, M., Williams, D.R., Heng, J.Y.Y., 2013. Process-induced phase transformation of carbamazepine dihydrate to its polymorphic anhydrates. Powder Technol. 236, 114-121.

Lam, D.C.C., Nakagawa, M., 1994. Packing of particles (Part 3) Effect of particle size distribution shape on composite packing density of bimodal mixtures. J. Ceram. Soc. Jpn. 102, 133-138.

Lovette, M.A., Browning, A.R., Griffin, D.W., Sizemore, J.P., Snyder, R.C., Doherty, M.F., 2008. Crystal shape engineering. Ind. Eng. Chem. Res. 47, 9812-9833.

Pecharsky, V.K., Zavalij, P.Y., 2005. Fundamentals of powder diffraction and structural characterization of materials, 1 ed. Springer, New York.

Podczeck, F., Mia, Y., 1996. The influence of particle size and shape on the angle of internal friction and the flow factor of unlubricated and lubricated powders. Int. J. Pharm. 144, 187-194.

Podczeck, F., Révész, P., 1993. Evaluation of the properties of microcrystalline and microfine cellulose powders. Int. J. Pharm. 91, 183-193.

Ridgway, K., Morland, I., 1977. The bulk density of mixtures of particles of different shapes. J. Pharm. Pharmacol. 29, 58P-58P.

Schultz, J., Lavielle, L., Martin, C., 1987. The role of the interface in carbon fibre-epoxy composites. J. Adhes. 23, 45-60.

SeethaLekshmi, S., Guru Row, T.N., 2012. Conformational polymorphism in a non-steroidal anti-inflammatory drug, mefenamic acid. Cryst. Growth Des. 12, 4283-4289.

Singh, M.K., Banerjee, A., 2013. Role of solvent and external growth environments to determine growth morphology of molecular crystals. Cryst. Growth Des. 13, 2413-2425.

Van Oss, C.J., Chaudhury, M.K., Good, R.J., 1988. Interfacial Lifshitz-van der Waals and polar interactions in macroscopic systems. Chem. Rev. 88, 927-941.

Waknis, V., Chu, E., Schlam, R., Sidorenko, A., Badawy, S., Yin, S., Narang, A.S., 2014. Molecular basis of crystal mophology-dependent adhesion behaviour of mefenamic acid during tableting. Pharm. Res. 31, 160-172.

Wang, D., 2013. Advanced physical characterisation of milled pharmaceutical solids, PhD Thesis, Imperial College London, London.

Table 1 Contact angle of four different probe liquids measured on four different facets of mefenamic acid single crystal.

| Facet | Probe Liquids |  |  |  |
| --- | --- | --- | --- | --- |
|  | water | diiodomethane | formamide | ethylene glycol |
| (001) | 59.5±1.8 | 27.0±2.1 | 35.4±3.2 | 41.3±2.2 |
| (112) | 92.0±3.0 | 19.3±3.1 | 50.2±4.1 | 36.1±2.4 |
| (100) | 56.3±3.8 | 42.9±2.0 | 38.7±1.6 | 36.0±1.6 |
| (011) | 72.6±2.8 | 11.5±2.6 | 34.9±2.1 | 49.3±4.2 |

List of Figures

Figure 1	Mefenamic acid crystals obtained from (a) toluene, (b) DEE, (c) EA, (d) DCM, (e) acetone, (f) IPA, and (g) methanol.

Figure 2	Powder X-ray diffractograms for mefenamic acid crystals obtained from (a) methanol, (b) IPA, (c) acetone, (d) DCM, (e) EA, (f) DEE, (g) toluene, and (h) mefenamic acid-form-I reference pattern.

Figure 3	Dispersive component of surface energy as a function of fractional surface coverage for mefenamic crystals obtained from seven different solvents (error bars represent standard deviation of three measurements).

Figure 4	Correlation between mefenamic acid elongation data (squares) obtained from solvents with varying polar component of the Hansen Solubility parameter and dispersive component of surface energy (diamonds) (isostere at n/nm=0.04).

Figure 5	Acid-base surface energy as a function of solvent polar component of the Hansen solubility parameter (isostere at n/nm=0.04).

Figure 6	Unconfined yield stress as a function of consolidation stress for mefenamic acid crystals obtained from different solvents.

Figure 7	Cohesion versus polar component of the Hansen solubility parameter of solvent from which mefenamic crystals are obtained.

Figure 8	Surface energy heterogeneity profiles for mefenamic acid crystals before and after silanisation.

Figure 9	Unconfined yield stress for mefenamic acid crystals before and after silanisation (error bars represent standard deviation of three measurements).

100μm

100μm

500μm

500μm

(d)

(c)

(b)

(a)

1000μm

500μm

500μm

(g)

(f)

(e)

Figure 1 Mefenamic acid crystals obtained from (a) toluene, (b) DEE, (c) EA, (d) DCM, (e) acetone, (f) IPA, and (g) methanol.

(a)

(h)

(g)

(f)

(e)

(d)

(c)

(b)

Figure 2 Powder X-ray diffractograms for mefenamic acid crystals obtained from (a) methanol, (b) IPA, (c) acetone, (d) DCM, (e) EA, (f) DEE, (g) toluene, and (h) mefenamic acid-form-I reference pattern.

Figure 3 Dispersive component of surface energy as a function of fractional surface coverage for mefenamic crystals obtained from seven different solvents (error bars represent standard deviation of three measurements).

Figure 4 Correlation between mefenamic acid elongation data (squares) obtained from solvents with varying polar component of the Hansen Solubility parameter and dispersive component of surface energy (diamonds) (isostere at n/nm=0.04).

Figure 5 Acid-base surface energy as a function of solvent polar component of the Hansen solubility parameter (isostere at n/nm=0.04).

Figure 6 Unconfined yield stress as a function of consolidation stress for mefenamic acid crystals obtained from different solvents.

Figure 7 Cohesion versus polar component of the Hansen solubility parameter of solvent from which mefenamic crystals are obtained.

Figure 8 Surface energy heterogeneity profiles for mefenamic acid crystals before and after silanisation.

Figure 9 Unconfined yield stress for mefenamic acid crystals before and after silanisation (error bars represent standard deviation of three measurements).