# Supplementary information:

# Poison Mitigation Strategies for the use of Impure Hydrogen in Electrochemical Hydrogen Pumps and Fuel Cells

C Jacksona, LFJM Raymakersb, MJJ Mulderb, ARJ Kucernaka

aDepartment of Chemistry, Imperial College London, Imperial College Rd, London, UK, SW7 2AZ

bHyET (Hydrogen) BV, Westervoortsedijk 71K, 6827 AV Arnhem, The Netherlands

- Contents

1.	Explosion limits in Hydrogen and air/oxygen systems	1

2.	Ozone generation	1

3.	Tables of Jmin for each impure H2 feed	2

4.	Offline regeneration of EHP cells – H2 + 20 ppm CO	3

5.	Offline regeneration of EHP cells – SMR-WGS H2	4

6.	Offline regeneration of EHP cells – H2 + 5 ppm H2S	5

7.	Offline regeneration of EHP cells – SMR-WGS-H2S H2	6

8.	References	6

# Explosion limits in Hydrogen and air/oxygen systems

In hydrogen-air mixtures, the explosive limits are 3.4 – 4.4% (lower explosive limit) to 73.1 – 77.6% (upper explosive limit) of air in H2 from 20 – 100 °C and 1 – 5 bar[1]. Thus, at concentrations of less than 3.4% air in H2, the mixture is not explosive, or at concentrations of above 77.6% air in H2, the mixture is not explosive. In hydrogen-oxygen mixtures, the explosive limits are 3.8 – 4.6% (lower explosive limit) to 94.6 – 95.4% (upper explosive limit) of O2 in H2 from 20 – 80 °C and 1 – 5 bar[1]. Thus, at concentrations of less than 3.8% O2 in H2, the mixture is not explosive, or at concentrations of above 95.4% O2 in H2, the mixture is not explosive.  The lower explosion limits for hydrogen-air and hydrogen-oxygen mixtures are similar, with hydrogen-oxygen as a slightly higher value, due to the similar mean molar heat capacities of O2 (31.594 kJ.mol-1) and N2 (33.536 kJ.mol-1), as described by Chen[2].

# Ozone generation

Ozone is predominately generated by three techniques, ultraviolet exposure of O2 or air, electrolysis of perchloric acid or electrical discharge applied to O2 or air[3]. When using electrical discharge applied to O2, up to 7% O3 in O2 may be generated using ~ 11 kWh/kg and if the electrical discharge is applied to air, up to 4% O3 in air with ~ 25 kWh/kg energy requirement[4]. However, if air is used as an oxygen source, N2 in air may react to form N2O and N2O5[4].

In this work, an ozone generator (BMT801; BMT Messtechnik GmbH, Germany) powered with a power supply (EA-PS 2032-025, EA Elektro-Automatik GmbH & Co.KG) was used to generate ~4% O3 in O2 using pure O2 as a feed. The ozone composition was confirmed by UV/Vis dual beam spectrometer (UV4-200, ATI-Unicam) at the known ozone UV absorption peak (λmax = 253.7nm, =3000±30 dm3 mol-1 cm-1) [5].

# Tables of Jmin for each impure H2 feed

Table S1: Long term limiting EHP performance as a function of mitigation strategy when operating with different feeds. Long term extrapolated performance jminjmax in %, for the EHP polarised at 100 mV and 200 mV, with and without an O2 or O2/O3 bleed, using Pt/Pt or PtRu/Pt MEAs. See Eq. 17.

|  |  | Extrapolated steady-state performance with mitigation strategy jminjmax/ % |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Anode/Cathode | Feed | Voltage / mV | No mitigation | O2 bleed | O2/O3 bleed |
| Pt/Pt | H2+20 ppm CO | 100 | 0.0 | 29.3 | 41.0 |
| Pt/Pt | H2+20 ppm CO | 200 | 0.0 | 72.7 | 73.6 |
| PtRu/Pt | H2 | 100 | 96.5 | - | - |
| PtRu/Pt | H2 | 200 | 93.9 | - | - |
| PtRu/Pt | H2+20 ppm CO | 100 | 0.0 | 89.3 | 91.2 |
| PtRu/Pt | H2+20 ppm CO | 200 | 0.0 | 88.5 | 88.9 |
| PtRu/Pt | SMR-WGS | 100 | 2.6 | 48.5a | 59.7 |
| PtRu/Pt | SMR-WGS | 200 | 4.6 | 66.2a | 72.6 |
| PtRu/Pt | H2 + 100 ppb H2S | 100 | 85.4a | 98.5 | 98.1 |
| PtRu/Pt | H2 + 100 ppb H2S | 200 | 84.4a | 98.8 | 97.8 |
| PtRu/Pt | H2 + 1 ppm H2S | 100 | 14.5a | 6.3 | 58.6 |
| PtRu/Pt | H2 + 1 ppm H2S | 200 | 2.2a | 0.0 | 15.8 |
| PtRu/Pt | SMR-WGS-H2S | 100 | 1.1 | 33.6 | 66.7 |
| PtRu/Pt | SMR-WGS-H2S | 200 | 0.0 | 61.5 | 73.5 |

a oscillating, unstable current decay

# Offline regeneration of EHP cells – H2 + 20 ppm CO

A

B

C

E

D

Figure S1: Effect of offline N2 and O2 treatment on EHP recovery after operation on H2+20 ppm CO. Chronoamperometry at a cell temperature of 35 °C, feed to the anode at a RH of 75% and flowrate of 200 mL.min-1 of N2, H2, H2+20 ppm CO, or 50 mL.min-1 O2/~4% O3 + O2. Gas composition as indicated on the graph with offline O2 potentiostatic. A) PtRu/Pt MEA at 200 mV with 5 minutes N2, B) Pt/Pt MEA at 100 mV with 1 minute O2, C) Pt/Pt MEA at 200 mV with 1 minute O2, D) PtRu/Pt MEA at 100 mV with 1 minute O2, E) PtRu/Pt MEA at 200 mV with 1 minute O2.

# Offline regeneration of EHP cells – SMR-WGS H2

A

B

E

F

C

D

H

G

Figure S2: Effect of offline O2 treatment on EHP recovery after operation on SMR-WGS H2. Chronoamperometry at a cell temperature of 35 °C, feed to the anode at a RH of 75% and flowrate of 200 mL.min-1 of N2, SMR-WGS H2, or 50 mL.min-1 O2/~4% O3 + O2. Gas composition as indicated on the graph with offline O2 potentiostatic. A) PtRu/Pt MEA at 100 mV with 1 minute O2, B) PtRu/Pt MEA at 100 mV with 5 minutes O2, C) PtRu/Pt MEA at 100 mV with 15 minutes O2, D) PtRu/Pt MEA at 100 mV with 15 minutes ~4% O3 + O2 and E) PtRu/Pt MEA at 200 mV with 1 minute O2, F) PtRu/Pt MEA at 200 mV with 5 minutes O2, G) PtRu/Pt MEA at 200 mV with 5 minutes O2, H) PtRu/Pt MEA at 200 mV with 15 minutes ~4% O3 + O2.

# Offline regeneration of EHP cells – H2 + 5 ppm H2S

A

B

C

D

E

F

G

Figure S3: Effect of offline N2 and O2 treatment on EHP recovery after operation on H2+5 ppm H2S. Chronoamperometry at a cell temperature of 35 °C, feed to the anode at a RH of 75% and flowrate of 200 mL.min-1 of N2, H2, H2+5 ppm H2S or 50 mL.min-1 O2/~4% O3 + O2. Gas composition as indicated on the graph with offline O2 potentiostatic. A) PtRu/Pt MEA at 100 mV with 15 minutes O2, B) PtRu/Pt MEA at 100 mV with 15 minutes ~4% O3 + O2, C) PtRu/Pt MEA at 100 mV with 20 minutes ~4% O3 + O2 D) PtRu/Pt MEA at 200 mV with 15 minutes O2 and E) PtRu/Pt MEA at 200 mV with 15 minutes ~4% O3 + O2 F) PtRu/Pt MEA at 200 mV with 20 minutes ~4% O3 + O2, G) PtRu/Pt MEA at 200 mV with 19 minutes N2.

# Offline regeneration of EHP cells – SMR-WGS-H2S H2

A

B

Figure S4: Effect of offline N2 and O2/O3 treatment on EHP recovery after operation with SMR-WGS-H2S H2. Chronoamperometry at a cell temperature of 35 °C, feed to the anode at a RH of 75% and flowrate of 200 mL.min-1 of N2, H2, SMR-WGS-H2S H2, or 50 mL.min-1 O2/~4% O3 + O2. Gas composition as indicated on the graph with offline O2 potentiostatic. A) PtRu/Pt MEA at 100 mV with 15 minutes ~4% O3 + O2 and B) PtRu/Pt MEA at 200 mV with 15 minutes ~4% O3 + O2.

# References

[1] V. Schroeder, K. Holtappels, in, 2005.

[2] C.-C. Chen, Industrial & Engineering Chemistry Research, 50 (2011) 10283-10291.

[3] P.A. Balakrishnan, A. Arunagiri, P.G. Rao, in, 2002, pp. 77-86.

[4] S. Stucki, Process Technologies for Water Treatment, Springer US, 2013.

[5] K. Rakness, G. Gordon, B. Langlais, W. Masschelein, N. Matsumoto, Y. Richard, C.M. Robson, I. Somiya, Ozone-Science & Engineering, 18 (1996) 209-229.