## Slide 1: Lessons from solar water splitting prototype field tests
Anna Hankin
anna.hankin@imperial.ac.uk

## Slide 2: Materials and reactor development for photoelectrochemical hydrogen production
Aim:
Reactor development for up-scaled photoelectrochemical H2 production
Key objectives:
Synthesis and optimization of photoelectrode materials
Development of optics for reactor irradiation
Operation and characterisation of up-scaled PEC reactor prototypes
~ 30 - 50 cm2 scale
~ 1 cm2 scale
2

## Slide 3
Stellenbosch, South Africa
Reactor + concentrator optics

## Slide 4: Coupling optics and photoelectrochemical reactors
Al-coated mirror
Ag-coated mirror
  Light concentrated by a factor of four ( 4 suns)
  Light reflected by Al and Ag mirrors
4
Cosine receptor
Cosine receptor
  Reactor + optics mounted on a 2-axis tracking platform

## Slide 5: Different irradiance strategies

## Slide 6
PV-biased photoelectrochemical device
Photoelectrochemical device
Device taxonomy: Nielander, Shaner, Lewis et al., Energy Environ. Sci., 8, 16 – 25 (2015)

## Slide 7
Optical concentration & two-sided irradiation
N. Vu and S. Shin, Energies, 2016, 9, 71
J. Karp et al., Opt. Express, 2011, 19, 673

## Slide 8
Linear Fresnel lens #1
Linear Fresnel lens #2
Linear Fresnel lens #3
Stepped waveguide
Waveguide edge
/ light fed into PEC reactor
Light concentration using linear Fresnel lenses and waveguides (COMSOL Multiphysics model)

## Slide 9
9

## Slide 10
10

## Slide 11
Ta foil current collector
RHE reference electrode
Flow inlets
Electrical contacts
11

## Slide 12
FTO / WO3 / BiVO4 / NiOOH photoanode degradation under 4 x sun irradiance
12

## Slide 14
Why double-sided irradiation?

## Slide 15
Photoanode: FTO/WO3/BiVO4/NiOOH
Cathode: Nickel mesh
Photoactive area: 36 cm2
Membrane: Nafion 115
Electrolyte: pH7, 0.1 M KPi (K2HPO4/KH2PO4)
Optical pathway
WO3/ BiVO4
H2O
H2O
Membrane
Quartz
PV
Ni mesh
+
-
Optical pathway
WO3/ BiVO4
H2O
H2O
Membrane
Quartz
PV
Ni mesh
+
-
Other modes of operation?
Optical and electronic pathways:
15

## Slide 16
16

## Slide 17: PV-PEC operation: side-by-side or tandem?
Chart: Time (s)
| 0 | 0.99999999747524271 | 1.9999999949504854 | 2.9999999924257281 | 3.9999999899009708 | 4.9999999873762135 | 5.9999999848514562 | 6.999999982326699 | 7.9999999798019417 | 8.9999999772771844 | 9.9999999747524271 | 10.99999997222767 | 11.999999969702912 | 12.999999967178155 | 13.999999964653398 | 14.999999962128641 | 15.999999959603883 | 16.999999957079126 | 17.999999954554369 | 18.999999952029611 | 19.999999949504854 | 20.999999946980097 | 21.99999994445534 | 22.999999941930582 | 23.999999939405825 | 24.999999936881068 | 25.99999993435631 | 26.999999931831553 | 27.999999929306796 | 28.999999926782039 | 29.999999924257281 | 30.999999921732524 | 31.999999919207767 | 32.999999916683009 | 33.999999914158252 | 34.999999911633495 | 35.999999909108737 | 36.99999990658398 | 37.999999904059223 | 38.999999901534466 | 39.999999899009708 | 40.999999896484951 | 41.999999893960194 | 42.999999891435436 | 43.999999888910679 | 44.999999886385922 | 45.999999883861165 | 46.999999881336407 | 47.99999987881165 | 48.999999876286893 | 49.999999873762135 | 50.999999871237378 | 51.999999868712621 | 52.999999866187864 | 53.999999863663106 | 54.999999861138349 | 55.999999858613592 | 56.999999856088834 | 57.999999853564077 | 58.99999985103932
Side-by-side | 83.8623 | 83.6792 | 83.5266 | 83.4961 | 83.3435 | 83.252 | 83.0383 | 82.9468 | 82.8552 | 82.7332 | 82.6416 | 82.55 | 82.4585 | 82.3364 | 82.2754 | 82.1838 | 82.1228 | 81.9397 | 81.8481 | 81.7566 | 81.6345 | 81.604 | 81.5735 | 81.4819 | 81.3904 | 81.2683 | 81.2073 | 81.1462 | 81.0547 | 80.9631 | 80.8105 | 80.8411 | 80.78 | 80.6274 | 80.6274 | 80.4749 | 80.4443 | 80.4138 | 80.3528 | 80.2917 | 80.1697 | 80.1086 | 80.1392 | 79.9866 | 79.895 | 79.834 | 79.834 | 79.7729 | 79.7119 | 79.6204 | 79.5898 | 79.5288 | 79.4983 | 79.4373 | 79.4067 | 79.3152 | 79.2847 | 79.2542 | 79.1016 | 79.1626
Tandem | 13.9313 | 13.9221 | 13.9221 | 13.913 | 13.9008 | 13.9069 | 13.8916 | 13.8855 | 13.8916 | 13.8947 | 13.8824 | 13.8794 | 13.8794 | 13.8763 | 13.8794 | 13.8611 | 13.8794 | 13.8641 | 13.8641 | 13.8641 | 13.8611 | 13.855 | 13.855 | 13.855 | 13.8611 | 13.8489 | 13.8397 | 13.8458 | 13.8397 | 13.8489 | 13.8336 | 13.8367 | 13.8245 | 13.8336 | 13.8367 | 13.8245 | 13.8123 | 13.8031 | 13.7939 | 13.7909 | 13.7634 | 13.7665 | 13.7665 | 13.739 | 13.7268 | 13.7421 | 13.7177 | 13.7268 | 13.7115 | 13.7146 | 13.7268 | 13.7115 | 13.7054 | 13.7085 | 13.7024 | 13.7146 | 13.7024 | 13.7085 | 13.7054 | 13.7024
PVs in tandem vs side-by-side, with WO3/BiVO4 /NiOOH electrode with 0.5 M Na2SO3
Chart: Cell potential difference / V
WO3/BiVO4/NiOOH electrode with 0.5 M Na2SO3 hole scavenger.
17

## Slide 18
Directly irradiated
With concentrator optics

## Slide 19
Irradiance measurements
A spectrophotometer is needed!
Cosine receptor

## Slide 20
Chart: Spectral irradiance, F / W m-2 nm-1
Our Abet Technologies Solar Simulator output (with AM 1.5 filter)
TiO2
Si
20

## Slide 21
Chart: Wavelength / nm
Low sensitivity!
Spectral response of a Si photodiode
21

## Slide 22
Temporal measurements recorded during experiments at Stellenbosch
Cloudless day
Cloudy day
22

## Slide 23
Photoelectrode materials
& other components

## Slide 24
Materials
  FTO / WO3 / BiVO4 / NiOOH photoanode (15 cm x 2 cm)
    1M pH 9 borate buffer
    Ta foil current collector (insulated from electrolyte)
    Back-side illumination
  Cation permeable membrane (Nafion 115)
  Ni cathode
    1M pH 9 borate buffer
  c-Si PV (Mr Watt, Italy)
    Mounted externally
For non-concentrated & concentrated irradiance tests

## Slide 25
30 cm2 PV cell (Mr Watt, Italy), under continuous illumination by simulated sunlight (AM 1.5 G, 100 mW cm-2). Power output = 621 mW
  c-Si PV (Mr Watt, Italy)

## Slide 26
Materials
  FTO / WO3 / BiVO4 / NiOOH photoanode (15 cm x 2 cm)
    1M pH 9 borate buffer
    Tantalum foil current collector (insulated from electrolyte)
    Back-side illumination
  Cation permeable membrane (Nafion 115)
  FTO / Au / Sb2Se3 / CdS / TiO2 / Pt photocathode (s)
  (4 lots of 3 cm x 2 cm, connected in parallel)
    0.1 M H2SO4
    Tantalum backing foil current collector
    Front-side illumination
For non-concentrated irradiance tests with mirrors:

## Slide 27: Engineering photoanodes for up-scaled solar water splitting
500 nm
500 nm
1 µm
1 µm
FTO | WO3 nanoneedles
FTO | WO3 nanoneedles | BiVO4 | NiFeOOH
200 nm
2.5 cm
4 cm
1.5 cm
17 cm
27

## Slide 28: Engineering photoelectrodes for up-scaled solar water splitting
High-performance and stable photocathodes for solar water splitting
3 electrode arrangement
FTO | Au | Sb2Se3 | CdS | TiO2 | Pt
Pt mesh counter electrode
Ag/AgCl (4 M KCl) reference electrode
0.1 M H2SO4 (pH 1, quiescent)
Scan rate: 5 mV s-1
Chart: Electrode potential, ERHE / V
Yang et al. Nat Commun 2020, 11, 861.

## Slide 29
Electrode Potential (RHE) / V
Current density
0
-0.6
-0.4
-0.2
0
0.2
0.4
0.6
0.8
1.0
1.2
1.4
1.6
1.8
2.0
Photoanode current
Photocathode current
H2O splitting spontaneity under device irradiation
//
//

## Slide 30
Electrode Potential (RHE) / V
Current density
0
-0.6
-0.4
-0.2
0
0.2
0.4
0.6
0.8
1.0
1.2
1.4
1.6
1.8
2.0
Photoanode current
Photocathode current
H2O splitting spontaneity under device irradiation
//
//

## Slide 31
Reactor operation with two waveguides
PV-biased photoelectrochemical device
Device taxonomy: Nielander, Shaner, Lewis et al., Energy Environ. Sci., 8, 16 – 25 (2015)

## Slide 32
Spontaneous operation with WO|BVO|NiOOH photoanode, Ni cathode & Si PV (with lenses & waveguides)
Chart: Experiment duration / min

## Slide 33
FTO / WO3 / BiVO4 / NiOOH photoanode degradation promoted by:
    High current & high temperature (under concentrated light)
    Excessive PV bias at low irradiance (under low, diffuse irradiance)

## Slide 34: Photoanode degradation during PV-PEC operation
Photoanodes are excessively biased by the PV during periods of low irradiance (cloudy conditions)
Temperature effect – particularly with concentrated light
Large-scale AA-CVD method requires more optimisation to improve uniformity
Influence of flow dynamics in the up-scaled system was greater than expected
15 cm
4 cm

## Slide 35
Investigating mechanical and (photo)electrochemical stability of scalable WO3 and BiVO4 based photoanodes (20 °C)
Chart: Electrode potential, E vs RHE / V
Chart: Electrode potential, E vs RHE / V
Chart: Electrode potential, E vs RHE / V
LSV curves in 0.1 M H2SO4 (pH 0.8), with and without 0.5 M Na2SO3 as a hole scavenger. Scan rate: 20 mV s-1.
Creasey et al., J. Mater. Chem. A, 2025.
Planar
Hybrid
Nanoneedle

## Slide 36
Investigating mechanical and (photo)electrochemical stability of scalable WO3 and BiVO4 based photoanodes
Chart: Time / hours
Chart: Time / hours
36

## Slide 37
Reactor operation with two mirrors
Photoelectrochemical device
Device taxonomy: Nielander, Shaner, Lewis et al., Energy Environ. Sci., 8, 16 – 25 (2015)

## Slide 38
Light re-direction using mirrors (non-concentrated light)

## Slide 39
Spontaneous PEC reactor operation with WO3 | BiVO4 | NiOOH photoanode
& Au | Sb2Se3 | CdS | TiO2 | Pt photocathode
with mirrors
Chart: Time / hr : min
Solar elevation at AM 1.5 | 41.8 | 41.8

## Slide 40
Photoanode & photocathode (with mirrors)
Chart: Experiment duration / min

## Slide 41
Chart: Experiment duration / min
Full PEC operation with photoanode & photocathode (with mirrors)
No photoelectrode degradation observed during this experiment

## Slide 42
Bismuth vanadate degradation

## Slide 43
Toma et al., Nat. Commun., 2016, 7, 12012
The Materials Project Pourbaix diagrams
next-gen.materialsproject.org/pourbaix
Pourbaix predictions for BiVO4

## Slide 44
Bismuth Pourbaix diagram
The Materials Project Pourbaix diagrams
next-gen.materialsproject.org/pourbaix

## Slide 45
Zhang et al., J. Phys. Chem. C, 2019, 123, 38.
Zhang et al., ACS Appl. Energy Mater. 2020, 3, 10, 9523

## Slide 46
PEC-MS
WO3 (nanoneedles) | BiVO4
1 M borate (pH 9)
Room temperature

## Slide 47
Influences of different reactor components on overall performance need to be understood, to make sure that while optimising for one thing, other issues are not exacerbated.
More needs to be done to explore thermal effects within integrated systems
Matching between photoelectrode(s) and PV performance needs to be investigated
More needs to be done on the effect of electrolyte on bubble detachment and gas collection efficiency
Multiple methods for guiding light into reactors needs to be explored
Should photoelectrochemical reactors move around to track the sun? On not?
Takeaway points

## Slide 48
Huge thank you to the group, our collaborators and sponsors