Mechanism of Action in NiOH2/NiOOH Photoactuators – Electronic Supplementary Information

Joseph H. L. Hadden*, Marie Bouchet, George Morgan, D. Jason Riley

Department of Materials, Imperial College London, Price Consort Road, London, SW7 2AZ

Appendix 1 – Table of video data

Table S1 Key for Actuator Videos showing active and substrate layer thicknesses and brief description of treatment.

| Video Number | Active layer thickness (ha) / μm | Substrate layer thickness (hs) / μm | Treatment |
| --- | --- | --- | --- |
| S1 | 1 | 2 | Illumination 100 mW cm-2 |
| S2 | 2 | 5 | Illumination 100 mW cm-2 |
| S3 | 5 | 6 | Illumination 100 mW cm-2 |
| S4 | 10 | 9 | Illumination 100 mW cm-2 |
| S5 | 2 | 3 | Humidity decrease according to Figure S1. |

Figure S1 Change in relative humidity inside glovebag with time under N2 atmosphere

Appendix 2

Appendix 3 – Python script for conversion of bending radius to C-parameter change

Plot of (𝒙𝟎−𝒙)=𝒇(𝒙𝟎) for different values of 𝜺𝒂𝒊 as per equation 2:

import matplotlib.pyplot as plt

import numpy as np

def epsi (x,y):

return(((0.8*x+(1-x)*0.4605)/(y*0.8+(1-y)*0.4605))-1)*100;

x=[i for i in range (0,10001)]

y=[i for i in range (0,10001)]

n=len(x)

z=n*[n*[0]]

S1=[]

S2=[]

S3=[]

S4=[]

S5=[]

S6=[]

S7=[]

S8=[]

S9=[]

S10=[]

Ys1=[]

Ys2=[]

Ys3=[]

Ys4=[]

Ys5=[]

Ys6=[]

Ys7=[]

Ys8=[]

Ys9=[]

Ys10=[]

for k in range (0,n):

for l in range(k,n):

z[k][l]=epsi(k/10000,l/10000)

if -0.110 <= z[k][l] and z[k][l]<= -0.09:

Ys1.append(l/100)

S1.append(l/100-k/100)

if -0.210 <= z[k][l] and z[k][l]<= -0.19:

Ys2.append(l/100)

S2.append(l/100-k/100)

if -0.310 <= z[k][l] and z[k][l]<= -0.29:

Ys3.append(l/100)

S3.append(l/100-k/100)

if -0.410 <= z[k][l] and z[k][l]<= -0.39:

Ys4.append(l/100)

S4.append(l/100-k/100)

if -0.510 <= z[k][l] and z[k][l]<= -0.49:

Ys5.append(l/100)

S5.append(l/100-k/100)

if -0.610 <= z[k][l] and z[k][l]<= -0.59:

Ys6.append(l/100)

S6.append(l/100-k/100)

if -0.710 <= z[k][l] and z[k][l]<= -0.69:

Ys7.append(l/100)

S7.append(l/100-k/100)

if -0.810 <= z[k][l] and z[k][l]<= -0.79:

Ys8.append(l/100)

S8.append(l/100-k/100)

if -0.910 <= z[k][l] and z[k][l]<= -0.89:

Ys9.append(l/100)

S9.append(l/100-k/100)

if -1.10 <= z[k][l] and z[k][l]<= -0.99:

Ys10.append(l/100)

S10.append(l/100-k/100)

fig = plt.figure(figsize = (10, 5))

plt.plot(Ys1, S1,c='lightblue',label='epsI=0.1%')

plt.plot(Ys2, S2,c='cyan')

plt.plot(Ys3, S3,c='blue',label='epsI=0.3%')

plt.plot(Ys4, S4,c='green')

plt.plot(Ys5, S5,c='yellow',label='epsI=0.5%')

plt.plot(Ys6, S6,c='coral')

plt.plot(Ys7, S7,c='red', label='epsI=0.7%')

plt.plot(Ys8, S8,c='brown')

plt.plot(Ys9, S9,c='black')

plt.plot(Ys10, S10,c='grey',label='epsI=1%')

plt.xlabel('xo : before actuation (%)')

plt.ylabel('(xo-x) humidity concentration change during actuation(%)')

plt.xlim(40,60)

plt.legend()

plt.show()

if -0.610 <= z[k][l] and z[k][l]<= -0.59:

Ys6.append(l/100)

S6.append(l/100-k/100)

if -0.710 <= z[k][l] and z[k][l]<= -0.69:

Ys7.append(l/100)

S7.append(l/100-k/100)

if -0.810 <= z[k][l] and z[k][l]<= -0.79:

Ys8.append(l/100)

S8.append(l/100-k/100)

if -0.910 <= z[k][l] and z[k][l]<= -0.89:

Ys9.append(l/100)

S9.append(l/100-k/100)

if -1.10 <= z[k][l] and z[k][l]<= -0.99:

Ys10.append(l/100)

S10.append(l/100-k/100)

fig = plt.figure(figsize = (10, 5))

plt.plot(Ys1, S1,c='lightblue',label='epsI=0.1%')

plt.plot(Ys2, S2,c='cyan')

plt.plot(Ys3, S3,c='blue',label='epsI=0.3%')

plt.plot(Ys4, S4,c='green')

plt.plot(Ys5, S5,c='yellow',label='epsI=0.5%')

plt.plot(Ys6, S6,c='coral')

plt.plot(Ys7, S7,c='red', label='epsI=0.7%')

plt.plot(Ys8, S8,c='brown')

plt.plot(Ys9, S9,c='black')

plt.plot(Ys10, S10,c='grey',label='epsI=1%')

plt.xlabel('xo : before actuation (%)')

plt.ylabel('(xo-x) humidity concentration change during actuation(%)')

plt.xlim(40,60)

plt.legend()

plt.show()

Appendix 4 – Supplementary Figures and Tables

Figure S2 Synthetic method for production of tri-layer actuator devices

Figure S3 Video Snapshot showing sputter (green) and analysis (red) areas during a typical ToF-SIMS analysis

(a)

(b)

(c)

Figure S4 Potential traces vs time for galvanostatic electrochemical deposition of actuator layers. (a) Deposition of Ni substrate layer (b) Deposition of Ni(OH)2 active layer onto Ni/Au substrate (Insert is magnification of first 1000 s)(c) Deposition of Ni(OH)2 onto FTO substrate

Figure S5 EDX spectra for electrodeposited layers showing the substrate Ni layer (black) and the Ni/Au/Ni(OH)2 tri-layer device (red) deposited on FTO (a) Whole spectrum taken up to 10 keV (b) Detailed spectrum of low BE region

(a)

(b)

Table S2: EDX atomic percentages in deposited layers on FTO.

| Deposited Layers | Element / atomic % |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | C | O | Na | S | Ni | Au |
| Ni Only | 7 | 8 | 3 | 1 | 81 | 0 |
| Ni/Au/Ni(OH)2 | 6 | 54 | 9 | 11 | 18 | 2 |

Figure S6 XRD diffractogram of the substrate and tri-layer actuator after each synthetic step. * denotes a peak assigned to FTO substrate.

Figure S7 Cyclic Voltammetry of tri-layer Ni/Au/Ni(OH)2 actuator. CV was performed at 50 mV s-1