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ABSTRACT

Transient liquid holdup effects are a crucial aspect of the behaviour of many unsaturated packed beds systems. This study examined both a model system consisting of spherical glass beads and a system containing slightly porous (about 5% water accessible porosity) rock particles. Experiments on different column heights show that the initial wetting front moving through the packed bed takes the form of a soliton or standing wave.
The final drainage of the bed when the liquid addition is turned off shows slightly more complex behaviour than that of the initial wetting of the bed. It was demonstrated that, if the behaviour of the liquid held around the particles is separated from that held within the particles, the same relatively simple model can be used to describe the drainage of both the model glass bead system and the slightly porous ore system despite the apparent differences in their behaviour, such as a much longer time to achieve the steady state, and a markedly different shape to the initial overall saturation versus time curve. 
This simple model assumed that, for the liquid between the particles, gravity was the dominant force and that capillarity could be neglected. Neglecting capillarity probably accounts for the slight discrepancy between the experimental and simulated liquid holdup results in the porous ore system at intermediate drainage times.
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1. Introduction
The behaviour of unsaturated gravity driven flow of liquid through packed beds of particles is important to number of different processes ranging from trickle bed reactors (TBRs) to heap leaching. 
A trickle bed reactor is a two phase system (liquid and gas) in which fluids usually flow co-currently through a fixed bed of typically porous catalysts or reactant solids (Luciani et al., 2002). The unsteady state operation of TBRs by periodically modulating the liquid or gas supply leads to transient fluid flow characteristics (Khadilkar et al., 1999; Lange et al., 2004; Ayude et al., 2007), which have been reported to increase the reactor performance compared with the steady state flow behaviour (Haure et al., 1989; Lange et al., 1994; Castellari and Haure, 1995; Lange et al., 2004; Tukac et al., 2007).
Heap leaching is another system in which the unsaturated flow behaviour of the liquid through a bed of particles is a crucial aspect of the performance of the system, though they have significant differences compared to trickle bed reactors in terms of the scale and flow rates used (Roman and Bhappu, 1993). This mineral processing technique is used for extraction of base and precious metals from low grade ores by running a leaching solution through an unsaturated bed of ore particles. In heaps, irrigation strategies with alternating solution application periods followed by much longer rest periods has been demonstrated to have the potential to increase the heap performance (Bartlett, 1992).
In this paper the transient variations in the liquid content as the liquid addition rate is varied is studied. In particular the behaviour at relatively low flow rates, when the bed is in the trickle flow or low interaction regime giving droplet and rivulet flow features, is studied. Packed beds consisting of non-porous glass beads as well as slightly porous (approximately 5% porosity) ore particles (a copper ore) are studied in order to ascertain how porosity of the particles affects the behaviour.
Most previous studies in both leaching columns and trickle bed reactors have concentrated on the steady state relationship between the liquid addition rate and liquid holdup as a function of various bed and operating parameters (eg. Yusuf, 1984; Fu and Tan, 1996; Nemec et al., 2001; de Andrade Lima, 2006). While there have been some previous studies into the transient behaviour of these systems (Standish, 1968; Bartlett, 1992; Tukac et al., 2007; Liu et al., 2008, Liu et al., 2009), the descriptions of the behaviour has typically been qualitative in nature, while the aim of this paper is to develop and validate a model that can describe the transient behaviour of these systems while including the effects of both porosity and the hysteresis observed in these systems.
2. Experimental design
In this study the liquid holdup measurements were performed gravimetrically using a high precision load cell. The gravimetric measurements were compared to an independent measurement based on the volume of drained liquid to obtain uncertainty in the measured holdup values and to verify that the load cell was able to measure the relatively small changes in liquid holdup needed in this work (see Ilankoon and Neethling (2012), for the method and results). It was found out that both methods give virtually identical results and thus providing conﬁdence in the load cell based measurements (Ilankoon and Neethling, 2012, 2013).
The column used is Perspex and has an internal diameter of 243mm. 3 different column heights were used in the study, namely 300, 500 and 800mm. A detailed description of the experimental setup including photos can be found in Ilankoon (2012), Ilankoon and Neethling (2012, 2013).
Mono-dispersed glass spheres of 10 mm and 14 mm were used for the model non-porous system whereas the slightly porous particle system consisted of 8-11.2 mm copper ore particles (average water accessible porosity of 5%) collected from Kennecott Utah Bingham Canyon Mine. The ore particle properties are described in more detail in Ilankoon and Neethling (2013). The experimentally determined average voidage values for the non-porous and porous system were about 40% and 35% respectively. For the ore system this is the external voidage excluding the porosity of the particles, which was about 5%. 
Using a novel liquid distributor that allowed even liquid addition over the entire bed surface even at the very low flow rates used (Ilankoon, 2012; Ilankoon and Neethling, 2012), the applied liquid flow rates were 1.26, 2.52, 5.04, 10.08 and 20.16 L/h and the corresponding superficial flow are within the range of 0.0075-0.12 mm/s. Deionised water was used as the liquid for all the experiments in this work.
3. Transients during initial liquid addition
The packed column, which was initially dry, was suspended via a load cell to gravimetrically measure the weight of liquid within the column. In addition, a measuring beaker was kept on top a high precision electronic balance in order to continuously measure the drained liquid weight (see Figure 1). These independent measures of the liquid behaviour within the column were obtained every second until steady state was reached in order to obtain the wetting front movement. Steady state was indicated by a constant load cell reading over a number of minutes. In addition, the wetting of the columns was filmed through the Perspex walls of the column.
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Figure 1: Experimental setup to measure wetting front movement in the model system.

The liquid within the packed bed moves under the influence of both gravitational and capillary/dispersive effects. If the flow is completely dominated by gravity, a sharp wetting front can be expected, while capillary/dispersive will act to spread out the wetting front. The reason why gravity sharpens the front is that the gravity driven flow rate increases with increasing liquid content. This means that, excluding the capillary and dispersive effects, any liquid ahead of the front will be travelling slower than the front and will thus be caught up by the front.
If the gravity effect is strong enough, then the sharpening effect of gravity and the spreading effect of capillarity and other dispersive phenomena will be able to reach an equilibrium that will manifest itself as a standing wave, or soliton, moving through the bed. 
Assuming that the particle bed is uniform in its properties in both the vertical and horizontal directions, once established, the shape and velocity of a soliton moving through the bed should be independent of the position of the soliton within the bed. The existence of a soliton moving through the bed can thus be investigated by examining the liquid flow out of the system as a function of time for different bed heights.
If the liquid is moving through the system as a wetting front there will be an initial time period in which liquid does not drain out of the packed bed followed by a rapid transition region towards a uniform drainage rate (linear increase in drained liquid). If there is a standing wave then, in different column heights, the breakthrough time would change, but the shape of the transition region would be the same.
Figures 2a (10mm glass spheres) and 3a (14mm glass spheres) show the variation of the drained liquid weight as a function of the time (time = 0 indicates initial liquid addition) since the start of the liquid addition into the bed. All these experiments were carried out with a superficial liquid velocity of 0.0075 mm/s (1.26 L/h liquid flow rate). The liquid holdup curves for column lengths of 300 mm, 500 mm and 800 mm are shown and the breakthrough time increases with the packed bed height and decreases with the particle size for the same packed bed height. The average gradient of each line after the transition regions in Figures 2a and 3a is 1.19 L/h, which is similar to the input liquid flow rate suggesting that the transition to steady state after the passing of the wetting front is indeed very rapid. The subtle differences in the final slopes are mainly due to small variations in the input liquid flow rate between experiments. The slight fluctuations in the flow are likely to be due to the effect of the peristaltic pump.
In Figures 2b and 3b, it is shown that when the initial liquid holdup curves are shifted onto one another for different column lengths, the transitions are very similar and all very rapid. The shift is achieved by adding a time shift onto the data for the shorter columns. Since, while nominally the same, the flow out of each column is subtly different, the time is shifted by  ( = length of the column,  is the input liquid velocity) where the subscript 1 refers to the 800 mm column and 2 refers to the column being shifted.
All these results indicate that the liquid motion through the bed during the initial wetting takes the form of wetting front, with all the results being consistent with the wetting front taking the form of a solitary wave.


a)

b)
Figure 2: Drained weight of water for 10 mm particles in different column lengths for a superficial velocity of 0.0075 mm/s. a) as a function of time b) as a function of time shifted relative to 800 mm column (time shifting method is described in the text).
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Figure 3: Drained weight of water for 14 mm particles in different column lengths for a superficial velocity of 0.0075 mm/s. a) as a function of time b) as a function of time shifted relative to 800 mm column (time shifting method is described in the text).

4. Model for Inter-Particle Liquid Flow
To describe unsaturated flow through a packed bed of non-porous particles, a theoretically based model has been formulated which includes the effect of liquid holdup hysteresis. The following section gives a brief description of this model, though more details can be found in Ilankoon and Neethling (2012).
The two liquid holdups that are important in describing the behaviour of this system are the external liquid holdup at steady state, , and the external residual liquid holdup, , of the system. Definitions of different liquid holdup values are given by de Klerk (2003). The static (truly immobile) and the residual liquid content are not necessarily the same thing since the residual liquid pocket that remains once the liquid has drained could have been involved in the flow.
It was found that rivulet flow behaviour was the dominant liquid flow feature through the particles at low superficial liquid velocities and it can be assumed that the residual liquid holdup consists of the remnants of these rivulets. It can thus be assumed that the residual liquid holdup is proportional to number of rivulets per cross-sectional area ().
		(1)
where  is the average cross-sectional area of the residual liquid in a rivulet.
This average residual area will actually consist of a string of liquid droplets held between particles by capillarity. The size of these residual liquid connections will depend on Bond number, contact angle and particle properties only, and thus  is likely to be virtually independent of the flow rate within the system (Ilankoon and Neethling, 2012, 2013).
A relative velocity, , (which is proportional to average flow per rivulet, , where  is the superficial liquid velocity) and a relative holdup, , (which is proportional to liquid holdup per rivulet, ) are defined as follows:
			(2)
			(3)
The theoretical inter-particle flow model was developed between the relative velocity () and the relative holdup () assuming that the cross-sectional shape of the rivulet is reasonably constant (Ilankoon and Neethling, 2012). Full details of this derivation can be found in Ilankoon (2012) including detailed information about the dimensionless drag coefficient and the average cross-sectional area of the residual liquid.
		(4)
				where, 
where  is dimensionless drag coefficient,  is density and  is viscosity of the liquid.
The model gives a squared relationship between  and  for the non-porous system, which was indeed found experimentally (see Figure 4). The proportionality  is a function of both particle size and size distribution. While these systems exhibit quite strong hysteresis, there is no hysteresis in the relationship shown in Figure 4. This is because the hysteresis takes the form of changes in the number of flow paths as liquid flow is increased and thus the rescaling of both the velocity and the holdup by the residual liquid content collapses the data and accounts for the hysteresis.

Figure 4: The relationship between the relative flow rate () and the additional liquid content of that rivulet () for both model glass bead and slightly porous ore particle systems (after Ilankoon and Neethling, 2013). The line is for a power law exponent of 2, to which all the data is very close to parallel indicating that the theoretical model form is applicable.

5. Drainage behaviour of the porous versus non-porous system
The model described in the previous section was initially developed based on a non-porous glass bead system, but has been shown to be applicable to systems with porous particles when suitable modifications have been made to the model. A brief description of the behaviour and model are given below, though more details can be found in Ilankoon and Neethling (2013). 
Unlike the non-porous system, where the system stops dripping and the residual is obtained after only a few minutes in a 300 mm column, the same column filled with porous particles continues to drip for many hours. In both systems there is an initial rapid decrease in the drainage rate, but in the non-porous system the flow out rapidly decreases to zero, while in the slightly porous ore particle system the decrease is not to zero but to a small and near constant flow which persists for many hours until the visible drying of the upper particles approaches the bottom of the column. It can therefore be assumed that this slow flow is associated with the drainage of the liquid within the particles, especially as this flow rate was found to be independent of the superficial liquid velocity of the system.
Within the porous system, the amount of liquid held within the pore spaces of the particles at steady state was slightly lower, but of a similar magnitude to the liquid held between the particles, but the flow associated with this internally held liquid was orders of magnitude lower. This means that to understand and model the liquid motion within the system, the contribution of the liquid around the particles needs to be separated from that within the particles.
To do this, experiments were conducted in which the particles were initially saturated in water for 3-4 days and externally dried using paper towels just before the column is packed (i.e. particles are initially saturated not the packed bed). The difference in the scale of the pores within the particles compared to that around the particles means that as long as there is liquid available in the intra-particle spaces, the particles will remain saturated or very near saturated. Any additional weight above that of these initially saturated particles is thus associated with the liquid held around the particles.
When liquid addition to the column is halted both the inter- and intra-particle liquid begins to drain (though much quicker in the case of the inter-particle liquid). Over a long time period the drainage rate from within the particles is constant. If this drainage rate from within the particles is also assumed to be constant at short times, the amount of liquid held between the particles can be estimated by adding the liquid drained from the particles back onto the measured external liquid content:
			(5)
where  is estimated external liquid holdup between the particles,  is the liquid content obtained by subtracting the initial weight of the particle bed containing saturated particles from the subsequent weight of the particle bed,  is roughly constant flow out of the column at longer times,  is length of the column and  is the drainage time (see Ilankoon and Neethling, 2013).
This flow through the particles will also eventually drain the residual liquid connections between the particles as well as the particles themselves. Since this rate is constant though, whether it is draining the stationary connections between the particles or the liquid actually within the particles, adding this liquid back onto the total will continue to provide an estimate of the liquid content at the point at which flow between the particles stopped and hence the external residual.
The system thus exhibits two residual liquid contents, a short term residual associated with the cessation in the liquid flow around the particles, , and a much longer term residual associated with the cessation of flow from within the particles. Since the flow model developed in section 4 (equation 4) is for the liquid flow around the particles, the relevant liquid holdups and residuals are the external ones. When these external liquid holdups are used the same model form as that for the non-porous particles is obtained, namely a power law relationship with an exponent of two between  and , albeit with a different pre-factor (see Ilankoon and Neethling, 2013 and Figure 4). 
6. Modelling of transient liquid drainage behaviour
6.1 The Model
The equations developed in the previous sections describe the relationship between the steady state liquid content and the liquid flux through the system. In order to model the transient behaviour of the system the change in liquid content and flux need to be related, which requires a continuity equation:
				(6)
If residual liquid holdup () is constant with respect to time and distance and if it is assumed that the only liquid holdup variations are in the vertical direction, equation 6 can be written as follows:
			(7)
In this work it will be assumed that for the liquid between the particles, gravity is the dominant force and that capillarity can be ignored. The validity of this assumption is discussed below. Making this assumption means that equation 4 can be used to describe the flux , which, when substituted into equation 7, gives the following relationship (gravity is downwards and  is positive and  is the distance from the bottom of the column, thus sign changes):
 		(8)
For the porous particles the overall flux will include a contribution from the flow within the particles, but this is assumed to be constant at the short times for which this model will be applied and thus does not contribute to the differential. The contribution of the flux within the particles to the flux out of the column is directly added on to the calculated flux, while the predicted liquid content is corrected using equation 5 in order to allow comparisons to be made with the measured results. It has also already been included within the calculation of the residual.
That the effect of capillarity on the flow around the particles will be quite a bit smaller than that of gravity for our experimental system can be demonstrated by the following analysis. The capillary pressures () will be of the following order (See Appendix A for the derivation):
 			(9)
where  is the inter-particle spacing of the system (i.e. the length scale associated with the cross-sectional size of the pore spaces between the particles, which is related to particle size and its distribution and is also a function of packing).
The resultant capillary pressure will be order of tens to hundreds of Pascals since the surface tension of water () is 0.07 N/m, particle spacing is of the order of millimetres and the liquid holdups are a few percent. Thus capillary pressure gradient over the length of the column will be order of 100-1000 Pa/m (column is tens of centimetres tall), which is significantly less than the effect of gravity, which is 10000 Pa/m (i.e. ). Thus gravity is the dominant factor in flow of liquid between the particles, with capillarity a small, though not necessarily totally insignificant factor (see below).
This first order PDE (equation 8) is solved numerically using the first order upwind method, which requires an initial condition and a top boundary condition (given that the flow is always downwards). The top boundary condition is that there is no inflow and the following initial condition holds: 
			(10)
where  is the steady state holdup associated with the solution of equation 4 at the flow rate into the column before liquid addition ceased.
6.2. Comparison with Experimental Results
Since the value  is calculated based on experimentally obtained steady and residual holdups and the known liquid flux through the system (initially dry bed of glass beads, for =0.12 mm/s, =78.5 mm/s and =0.06 mm/s, =80.8 mm/s), the following simulations are carried out with no additional fitting parameters beyond these measured values. The simulated drainage velocities obtained from the solution of equation 8 were compared to sets of experimental drainage data. Figure 5 shows this behaviour for initial superficial velocities of = 0.12 and = 0.06 mm/s for 10 mm glass beads.







Figure 5: Simulated and experimental drainage curves for different superficial velocities with 10 mm glass beads in 300 mm column (solid line is simulated, diamonds are the experimental results). Top - 0.12 mm/s, bottom - 0.06 mm/s.


Figure 6: Simulated and experimental liquid contents during the drainage for different superficial velocities with 10 mm glass beads in 300 mm column (solid line is simulated, diamonds are the experimental results). Top - 0.12 mm/s, bottom - 0.06 mm/s.

In addition, Figure 6 shows gravimetrically measured average liquid holdup values (liquid volume/reactor volume) with the simulated liquid contents for 10 mm particles at same superficial liquid velocities in Figure 5. There are high  values for the comparisons presented in Figures 5 and 6 despite the lack of any adjustable parameters beyond the inputted steady state behaviour. This gives us confidence as to the validity of the proposed form of the model.
For each set of experimental drainage curves in the ore system, the simulated drainage velocities were obtained using the numerical solution of equation 8. As stated previously, the flux due to flow through the particles, , was added onto that obtained from the simulations, which are only for the flow around the particles.
The comparison of the drainage velocity in the 300 mm ore system with 8-11.2 mm particles with the corresponding simulations are shown in Figure 7 for initial superficial velocities of 0.12 and 0.03 mm/s. Since these simulations only consider gravity, the flow out of the column is simply a function of liquid content at the bottom of the column and not gradients in this liquid content, through which capillarity would act. A good fit to the experimental results can be seen, with very high  values obtained despite the lack of adjustable fitting parameters.
In Figure 8 the simulated and experimentally obtained liquid holdup values are plotted. It can be seen that at short and long times there is good agreement between the simulated and measured liquid contents, but that at intermediate times there is a slight discrepancy between the results. It is surmised that this discrepancy is because the effect of capillarity is ignored. As there is no liquid addition into the column, the liquid content is, of course, directly related to the integral of the liquid flow out of the column. In Figure 9 simulations of the liquid content profile with height within the column are presented at a number of different time points. Note that Figure 8 plots the liquid holdup minus the holdup of the initially saturated ore particles, while Figure 9 is a simulation of the external liquid holdup. These values will differ due to the liquid lost from the pore spaces within the particles. This discrepancy can be estimated using equation 5.
Capillarity will always act down gradients of liquid content. As there is no gradient in the liquid content at the bottom of the column at short time periods, the flow out of the column during this initial period will not be influenced by capillarity. Eventually, though, the reduction in liquid content will hit the bottom of the column, accompanied by a gradient in the liquid content. Since the liquid content decreases with height in the column, the effect of capillarity would be to decrease the flow out of the column compared to the case of gravity acting along. This is consistent with what is seen in Figure 8, where the predicted liquid content (which does not include the effect of capillarity) is lower than the experimentally measured one. At higher times the gradient decreases and thus so will the influence of capillarity.



































Figure 7: Simulated and experimental drainage curves for different superficial velocities with 8-11.2 mm ore particles in 300 mm column (solid line is simulated, diamonds are the experimental results). Top - 0.12 mm/s, bottom - 0.03 mm/s.




Figure 8: Simulated and experimental liquid contents during the drainage for different superficial velocities with 8-11.2 mm ore particles in 300 mm column. Top - 0.12 mm/s, bottom - 0.03 mm/s.



Figure 9: External liquid content of 8-11.2 mm ore particles in 0.3 m column as a function of column height for the superficial velocities of: Top - 0.12 mm/s, bottom - 0.03 mm/s.

7. Conclusions
This paper has shown that the initial wetting behaviour for the packed bed is relatively simple and takes the form of a soliton or standing wave. The drying behaviour of the bed when the liquid addition is stopped is slightly more complex, with distinct differences in the behaviour of the non-porous glass bead system compared to the slightly porous ore system.
When the effect of the liquid held within the particles is separated from that held around the particles, this paper has shown that the same relatively simple model can be used to describe the behaviour of both systems, with very good agreement between the simulated and measured average liquid holdup and liquid flow rate out of the bottom of the column.
The model used assumes that, for the liquid held between the particles, the effect of gravity on the drainage is stronger than that of capillarity. The generally good correlation between the experimental and simulated results indicates that this is a reasonable assumption, though the slight discrepancy in the average liquid holdup values for the porous system at intermediate times could be due to the effect of capillarity as the discrepancy is consistent with the effect that capillarity is likely to have on the system.
These results show that the model form presented in this paper, together with the experimental procedure for obtaining the model parameters allows not only the steady state, but also transient features of the drainage in these systems to be predicted with little need for complex model calibration. This is important in industrial applications where not only the steady state behaviour, but also the transients impact performance, such as the initial wetting and final drain down behaviour in heap leaching.


Appendix A: Derivation of a relationship for the capillary pressure
The dependency of the capillary pressure on the channel size and liquid content can be estimated as follows. This estimate of the order of magnitude of the capillary force is done by assuming an idealised geometry in which the liquid is held in the corner of drainage channels between the particles.
The capillary pressure is given by:
								(A.1)
where  is the surface tension of the liquid and  is the radius of the curvature. Note that as the water is generally a wetting phase, the capillary pressure is negative as interface will curve into the liquid phase (i.e. water lower pressure than air).
								(A.2)
where  is the area of the channel between the particles occupied by liquid.
Since the total area of the channel will be proportional to the square of the particle spacing, , and the liquid holdup () is proportional to the ratio of the area occupied by liquid to the total area:
								(A.3)
Using equations A.2 and A.3:
								 (A.4)
Now the relationship for  becomes:	
 					  			(A.5)
Using equations A.1 and A.5, the relationship for the capillary pressure is:
				   				(A.6)
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Drained weight (g)



300 mm	300.5	301	301.5	302	302.5	303	303.5	304	304.5	305	305.5	306	306.5	307	307.5	308	308.5	309	309.5	310	310.5	311	311.5	312	312.5	313	313.5	314	314.5	315	315.5	316	316.5	317	317.5	318	318.5	319	319.5	320	320.5	321	321.5	322	322.5	323	323.5	324	324.5	325	325.5	326	326.5	327	327.5	328	328.5	329	329.5	330	330.5	331	331.5	332	332.5	333	333.5	334	334.5	335	335.5	336	336.5	337	337.5	338	338.5	339	339.5	340	340.5	341	341.5	342	342.5	343	343.5	344	344.5	345	345.5	346	346.5	347	347.5	348	348.5	349	349.5	350	350.5	351	351.5	352	352.5	353	353.5	354	354.5	355	355.5	356	356.5	357	357.5	358	358.5	359	359.5	360	360.5	361	361.5	362	362.5	363	363.5	364	364.5	365	365.5	366	366.5	367	367.5	368	368.5	369	369.5	370	370.5	371	371.5	372	372.5	373	373.5	374	374.5	375	375.5	376	376.5	377	377.5	378	378.5	379	379.5	380	380.5	381	381.5	382	382.5	383	383.5	384	384.5	385	385.5	386	386.5	387	387.5	388	388.5	389	389.5	390	390.5	391	391.5	392	392.5	393	393.5	394	394.5	395	395.5	396	396.5	397	397.5	398	398.5	399	399.5	400	400.5	401	401.5	402	402.5	403	403.5	404	404.5	405	405.5	406	406.5	407	407.5	408	408.5	409	409.5	410	410.5	411	411.5	412	412.5	413	413.5	414	414.5	415	415.5	416	416.5	417	417.5	418	418.5	419	419.5	420	420.5	421	421.5	422	422.5	423	423.5	424	424.5	425	425.5	426	426.5	427	427.5	428	428.5	429	429.5	430	430.5	431	431.5	432	432.5	433	433.5	434	434.5	435	435.5	436	436.5	437	437.5	438	438.5	439	439.5	440	440.5	441	441.5	442	442.5	443	443.5	444	444.5	445	445.5	446	446.5	447	447.5	448	448.5	449	449.5	450	450.5	451	451.5	452	452.5	453	453.5	454	454.5	455	455.5	456	456.5	457	457.5	458	458.5	459	459.5	460	460.5	461	461.5	462	462.5	463	463.5	464	464.5	465	465.5	466	466.5	467	467.5	468	468.5	469	469.5	470	470.5	471	471.5	472	472.5	473	473.5	474	474.5	475	475.5	476	476.5	477	477.5	478	478.5	479	479.5	480	480.5	481	481.5	482	482.5	483	483.5	484	484.5	485	485.5	486	486.5	487	487.5	488	488.5	489	489.5	490	490.5	491	491.5	492	492.5	493	493.5	494	494.5	495	495.5	496	496.5	497	497.5	498	498.5	499	499.5	500	500.5	501	501.5	502	502.5	503	503.5	504	504.5	505	505.5	506	506.5	507	507.5	508	508.5	509	509.5	510	510.5	511	511.5	512	512.5	513	513.5	514	514.5	515	515.5	516	516.5	517	517.5	518	518.5	519	519.5	520	520.5	521	521.5	522	522.5	523	523.5	524	524.5	525	525.5	526	526.5	527	527.5	528	528.5	529	529.5	530	530.5	531	531.5	532	532.5	533	533.5	534	534.5	535	535.5	536	536.5	537	537.5	538	538.5	539	539.5	540	540.5	541	541.5	542	542.5	543	543.5	544	544.5	545	545.5	546	546.5	547	547.5	548	548.5	549	549.5	550	550.5	551	551.5	552	552.5	553	553.5	554	554.5	555	555.5	556	556.5	557	557.5	558	558.5	559	559.5	560	560.5	561	561.5	562	562.5	563	563.5	564	564.5	565	565.5	566	566.5	567	567.5	568	568.5	569	569.5	570	570.5	571	571.5	572	572.5	573	573.5	574	574.5	575	575.5	576	576.5	577	577.5	578	578.5	579	579.5	580	580.5	581	581.5	582	582.5	583	583.5	584	584.5	585	585.5	586	586.5	587	587.5	588	588.5	589	589.5	590	590.5	591	591.5	592	592.5	593	593.5	594	594.5	595	595.5	596	596.5	597	597.5	598	598.5	599	599.5	600	600.5	601	601.5	602	602.5	603	603.5	604	604.5	605	605.5	606	606.5	607	607.5	608	608.5	609	609.5	610	610.5	611	611.5	612	612.5	613	613.5	614	614.5	615	615.5	616	616.5	617	617.5	618	618.5	619	619.5	620	620.5	621	621.5	622	622.5	623	623.5	624	624.5	625	625.5	626	626.5	627	627.5	628	628.5	629	629.5	630	630.5	631	631.5	632	632.5	633	633.5	634	634.5	635	635.5	636	636.5	637	637.5	638	638.5	639	639.5	640	640.5	641	641.5	642	642.5	643	643.5	644	644.5	645	645.5	646	646.5	647	647.5	648	648.5	649	649.5	650	650.5	651	651.5	652	652.5	653	653.5	654	654.5	655	655.5	656	656.5	657	657.5	658	658.5	659	659.5	660	660.5	661	661.5	662	662.5	663	663.5	664	664.5	665	665.5	666	666.5	667	667.5	668	668.5	669	669.5	670	670.5	671	671.5	672	672.5	673	673.5	674	674.5	675	675.5	676	676.5	677	677.5	678	678.5	679	679.5	680	680.5	681	681.5	682	682.5	683	683.5	684	684.5	685	685.5	686	686.5	687	687.5	688	688.5	689	689.5	690	690.5	691	691.5	692	692.5	693	693.5	694	694.5	695	695.5	696	696.5	697	697.5	698	698.5	699	699.5	700	700.5	701	701.5	702	702.5	703	703.5	704	704.5	705	705.5	706	706.5	707	707.5	708	708.5	709	709.5	710	710.5	711	711.5	712	712.5	713	713.5	714	714.5	715	715.5	716	716.5	717	717.5	718	718.5	719	719.5	720	720.5	721	721.5	722	722.5	723	723.5	724	724.5	725	725.5	726	726.5	727	727.5	728	728.5	729	729.5	730	730.5	731	731.5	732	732.5	733	733.5	734	734.5	735	735.5	736	736.5	737	737.5	738	738.5	739	739.5	740	740.5	741	741.5	742	742.5	743	743.5	744	744.5	745	745.5	746	746.5	747	747.5	748	748.5	749	749.5	750	750.5	751	751.5	752	752.5	753	753.5	754	754.5	755	755.5	756	756.5	757	757.5	758	758.5	759	759.5	760	760.5	761	761.5	762	762.5	763	763.5	764	764.5	765	765.5	766	766.5	767	767.5	768	768.5	769	769.5	770	770.5	771	771.5	772	772.5	773	773.5	774	774.5	775	775.5	776	776.5	777	777.5	778	778.5	779	779.5	780	780.5	781	781.5	782	782.5	783	783.5	784	784.5	785	785.5	786	786.5	787	787.5	788	788.5	789	789.5	790	790.5	791	791.5	792	792.5	793	793.5	794	794.5	795	795.5	796	796.5	797	797.5	798	798.5	799	799.5	800	800.5	801	801.5	802	802.5	803	803.5	804	804.5	805	805.5	806	806.5	807	807.5	808	808.5	809	809.5	810	810.5	811	811.5	812	812.5	813	813.5	814	814.5	815	815.5	816	816.5	817	817.5	818	818.5	819	819.5	820	820.5	821	821.5	822	822.5	823	823.5	824	824.5	825	825.5	826	826.5	827	827.5	828	828.5	829	829.5	830	830.5	831	831.5	832	832.5	833	833.5	834	834.5	835	835.5	836	836.5	837	837.5	838	838.5	839	839.5	840	840.5	841	841.5	842	842.5	843	843.5	844	844.5	845	845.5	846	846.5	847	847.5	848	848.5	849	849.5	850	850.5	851	851.5	852	852.5	853	853.5	854	854.5	855	855.5	856	856.5	857	857.5	858	858.5	859	859.5	860	860.5	861	861.5	862	862.5	863	863.5	864	864.5	865	865.5	866	866.5	867	867.5	868	868.5	869	869.5	870	870.5	871	871.5	872	872.5	873	873.5	874	874.5	875	875.5	876	876.5	877	877.5	878	878.5	879	879.5	880	880.5	881	881.5	882	882.5	883	883.5	884	884.5	885	885.5	886	886.5	887	887.5	888	888.5	889	889.5	890	890.5	891	891.5	892	892.5	893	893.5	894	894.5	895	895.5	896	896.5	897	897.5	898	898.5	899	899.5	900	900.5	901	901.5	902	902.5	903	903.5	904	904.5	905	905.5	906	906.5	907	907.5	908	908.5	909	909.5	910	910.5	911	911.5	912	912.5	913	913.5	914	914.5	915	915.5	916	916.5	917	917.5	918	918.5	919	919.5	920	920.5	921	921.5	922	922.5	923	923.5	924	924.5	925	925.5	926	926.5	927	927.5	928	928.5	929	929.5	930	930.5	931	931.5	932	932.5	933	933.5	934	934.5	935	935.5	936	936.5	937	937.5	938	938.5	939	939.5	940	940.5	941	941.5	942	942.5	943	943.5	944	944.5	945	945.5	946	946.5	947	947.5	948	948.5	949	949.5	950	950.5	951	951.5	952	952.5	953	953.5	954	954.5	955	955.5	956	956.5	957	957.5	958	958.5	959	959.5	960	960.5	961	961.5	962	962.5	963	963.5	964	964.5	965	965.5	966	966.5	967	967.5	968	968.5	969	969.5	970	970.5	971	971.5	972	972.5	973	973.5	974	974.5	975	975.5	976	976.5	977	977.5	978	978.5	979	979.5	980	980.5	981	981.5	982	982.5	983	983.5	984	984.5	985	985.5	986	986.5	987	987.5	988	988.5	989	989.5	990	990.5	991	991.5	992	992.5	993	993.5	994	994.5	995	995.5	996	996.5	997	997.5	998	998.5	999	999.5	1000	1000.5	1001	1001.5	1002	1002.5	1003	1003.5	1004	1004.5	1005	1005.5	1006	1006.5	1007	1007.5	1008	1008.5	1009	1009.5	1010	1010.5	1011	1011.5	1012	1012.5	1013	1013.5	1014	1014.5	1015	1015.5	1016	1016.5	1017	1017.5	1018	1018.5	1019	1019.5	1020	1020.5	1021	1021.5	1022	1022.5	1023	1023.5	1024	1024.5	1025	1025.5	1026	1026.5	1027	1027.5	1028	1028.5	1029	1029.5	1030	1030.5	1031	1031.5	1032	1032.5	1033	1033.5	1034	1034.5	1035	1035.5	1036	1036.5	1037	1037.5	1038	1038.5	1039	1039.5	1040	1040.5	1041	1041.5	1042	1042.5	1043	1043.5	1044	1044.5	1045	1045.5	1046	1046.5	1047	1047.5	1048	1048.5	1049	1049.5	1050	1050.5	1051	1051.5	1052	1052.5	1053	1053.5	1054	1054.5	1055	1055.5	1056	1056.5	1057	1057.5	1058	1058.5	1059	1059.5	1060	1060.5	1061	1061.5	1062	1062.5	1063	1063.5	1064	1064.5	1065	1065.5	1066	1066.5	1067	1067.5	1068	1068.5	1069	1069.5	1070	1070.5	1071	1071.5	1072	1072.5	1073	1073.5	1074	1074.5	1075	1075.5	1076	1076.5	1077	1077.5	1078	1078.5	1079	1079.5	1080	1080.5	1081	1081.5	1082	1082.5	1083	1083.5	1084	1084.5	1085	1085.5	1086	1086.5	1087	1087.5	1088	1088.5	1089	1089.5	1090	1090.5	1091	1091.5	1092	1092.5	1093	1093.5	1094	1094.5	1095	1095.5	1096	1096.5	1097	1097.5	1098	1098.5	1099	1099.5	1100	1100.5	1101	1101.5	1102	1102.5	1103	1103.5	1104	1104.5	1105	1105.5	1106	1106.5	1107	1107.5	1108	1108.5	1109	1109.5	1110	1110.5	1111	1111.5	1112	1112.5	1113	1113.5	1114	1114.5	1115	1115.5	1116	1116.5	1117	1117.5	1118	1118.5	1119	1119.5	1120	1120.5	1121	1121.5	1122	1122.5	1123	1123.5	1124	1124.5	1125	1125.5	1126	1126.5	1127	1127.5	1128	1128.5	1129	1129.5	1130	1130.5	1131	1131.5	1132	1132.5	1133	1133.5	1134	1134.5	1135	1135.5	1136	1136.5	1137	1137.5	1138	1138.5	1139	1139.5	1140	1140.5	1141	1141.5	1142	1142.5	1143	1143.5	1144	1144.5	1145	1145.5	1146	1146.5	1147	1147.5	1148	1148.5	1149	1149.5	1150	1150.5	1151	1151.5	1152	1152.5	1153	1153.5	1154	1154.5	1155	1155.5	1156	1156.5	1157	1157.5	1158	1158.5	1159	1159.5	1160	1160.5	1161	1161.5	1162	1162.5	1163	1163.5	1164	1164.5	1165	1165.5	1166	1166.5	1167	1167.5	1168	1168.5	1169	1169.5	1170	1170.5	1171	1171.5	1172	1172.5	1173	1173.5	1174	1174.5	1175	1175.5	1176	1176.5	1177	1177.5	1178	1178.5	1179	1179.5	1180	1180.5	1181	1181.5	1182	1182.5	1183	1183.5	1184	1184.5	1185	1185.5	1186	1186.5	1187	1187.5	1188	1188.5	1189	1189.5	1190	1190.5	1191	1191.5	1192	1192.5	1193	1193.5	1194	1194.5	1195	1195.5	1196	1196.5	1197	1197.5	1198	1198.5	1199	1199.5	1200	1200.5	1201	1201.5	1202	1202.5	1203	1203.5	1204	1204.5	1205	1205.5	1206	1206.5	1207	1207.5	1208	1208.5	1209	1209.5	1210	1210.5	1211	1211.5	1212	1212.5	1213	1213.5	1214	1214.5	1215	1215.5	1216	1216.5	1217	1217.5	1218	1218.5	1219	1219.5	1220	1220.5	1221	1221.5	1222	1222.5	1223	1223.5	1224	1224.5	1225	1225.5	1226	1226.5	1227	1227.5	1228	1228.5	1229	1229.5	1230	1230.5	1231	1231.5	1232	1232.5	1233	1233.5	1234	1234.5	1235	1235.5	1236	1236.5	1237	1237.5	1238	1238.5	1239	1239.5	1240	1240.5	1241	1241.5	1242	1242.5	1243	1243.5	1244	1244.5	1245	1245.5	1246	1246.5	1247	1247.5	1248	1248.5	1249	1249.5	1250	1250.5	1251	1251.5	1252	1252.5	1253	1253.5	1254	1254.5	1255	1255.5	1256	1256.5	1257	1257.5	1258	1258.5	1259	1259.5	1260	1260.5	1261	1261.5	1262	1262.5	1263	1263.5	1264	1264.5	1265	1265.5	1266	1266.5	1267	1267.5	1268	1268.5	1269	1269.5	1270	1270.5	1271	1271.5	1272	1272.5	1273	1273.5	1274	1274.5	1275	1275.5	1276	1276.5	1277	1277.5	1278	1278.5	1279	1279.5	1280	1280.5	1281	1281.5	1282	1282.5	1283	1283.5	1284	1284.5	1285	1285.5	1286	1286.5	1287	1287.5	1288	1288.5	1289	1289.5	1290	1290.5	1291	1291.5	1292	1292.5	1293	1293.5	1294	1294.5	1295	1295.5	1296	1296.5	1297	1297.5	1298	1298.5	1299	1299.5	1300	1300.5	1301	1301.5	1302	1302.5	1303	1303.5	1304	1304.5	1305	1305.5	1306	1306.5	1307	1307.5	1308	1308.5	1309	1309.5	1310	1310.5	1311	1311.5	1312	1312.5	1313	1313.5	1314	1314.5	1315	1315.5	1316	1316.5	1317	1317.5	1318	1318.5	1319	1319.5	1320	1320.5	1321	1321.5	1322	1322.5	1323	1323.5	1324	1324.5	1325	1325.5	1326	1326.5	1327	1327.5	1328	1328.5	1329	1329.5	1330	1330.5	1331	1331.5	1332	1332.5	1333	1333.5	1334	1334.5	1335	1335.5	1336	1336.5	1337	1337.5	1338	1338.5	1339	1339.5	1340	1340.5	1341	1341.5	1342	1342.5	1343	1343.5	1344	1344.5	1345	1345.5	1346	1346.5	1347	1347.5	1348	1348.5	1349	1349.5	1350	1350.5	1351	1351.5	1352	1352.5	1353	1353.5	1354	1354.5	1355	1355.5	1356	1356.5	1357	1357.5	1358	1358.5	1359	1359.5	1360	1360.5	1361	1361.5	1362	1362.5	1363	1363.5	1364	1364.5	1365	1365.5	1366	1366.5	1367	1367.5	1368	1368.5	1369	1369.5	1370	1370.5	1371	1371.5	1372	1372.5	1373	1373.5	1374	1374.5	1375	1375.5	1376	1376.5	1377	1377.5	1378	1378.5	1379	1379.5	1380	1380.5	1381	1381.5	1382	1382.5	1383	1383.5	1384	1384.5	1385	1385.5	1386	1386.5	1387	1387.5	1388	1388.5	1389	1389.5	1390	1390.5	1391	1391.5	1392	1392.5	1393	1393.5	1394	1394.5	1395	1395.5	1396	1396.5	1397	1397.5	1398	1398.5	1399	1399.5	1400	0	1.06	1.73	2.1800000000000002	2.4699999999999998	2.94	3.12	3.3899999999999997	3.65	3.82	4	4.2	4.42	4.5	4.5999999999999996	4.7	4.8199999999999985	4.92	5.01	5.14	5.26	5.3	5.33	5.3599999999999985	5.39	5.46	5.46	5.46	5.4700000000000024	5.4700000000000024	5.4700000000000024	5.4700000000000024	5.4700000000000024	5.4700000000000024	5.4700000000000024	5.4700000000000024	5.48	5.48	5.48	5.48	5.48	5.48	5.48	5.5	5.51	5.51	5.51	5.51	5.51	5.51	5.51	5.51	5.51	5.51	5.51	5.51	5.51	5.5	5.49	5.49	5.49	5.49	5.5	5.51	5.5	8.4600000000000026	8.44	8.5300000000000011	8.7299999999999986	8.7900000000000009	8.9	9	9.129999999999999	9.17	9.2399999999999984	9.32	9.3600000000000048	9.4	9.5400000000000009	9.5500000000000007	9.6	9.65	9.7200000000000006	9.7200000000000006	9.77	9.8700000000000028	9.89	9.94	9.99	10.07	10.09	10.15	10.28	10.27	10.31	10.44	10.629999999999999	10.729999999999999	10.96	11.02	11.15	11.219999999999999	11.33	11.38	11.44	11.52	11.57	11.719999999999999	11.719999999999999	11.76	11.83	11.870000000000006	11.92	12.05	12.05	12.129999999999999	12.17	12.25	12.26	12.33	12.44	12.44	12.47	12.52	12.62	12.639999999999999	12.729999999999999	12.76	12.84	13.11	13.47	13.77	14.129999999999999	14.51	15.15	15.55	15.99	16.579999999999988	16.95	17.43	17.73	18.309999999999999	18.670000000000005	19.059999999999999	19.420000000000002	20.439999999999987	20.309999999999999	20.8	21.22	21.57	21.93	22.5	22.73	23.2	23.419999999999987	23.97	24.23	24.64	24.87	25.39	25.57	25.9	26.18	26.459999999999987	26.830000000000005	27.04	27.36	27.54	27.79	28.06	28.310000000000031	28.47	28.630000000000031	28.830000000000005	28.959999999999987	29.12	29.34	29.47	29.6	29.779999999999987	29.85	29.979999999999986	30.2	30.279999999999987	30.439999999999987	30.62	30.7	30.8	30.959999999999987	31.279999999999987	31.32	31.43	31.55	31.69	31.779999999999987	31.91	32.01	32.200000000000003	32.270000000000003	32.449999999999996	32.65	32.800000000000004	32.870000000000005	32.97	33.130000000000003	33.28	33.4	33.54	33.720000000000013	33.849999999999994	34	34.25	34.300000000000004	34.410000000000004	34.54	34.68	34.78	34.949999999999996	35.11	35.220000000000013	35.39	35.47	35.74	35.800000000000004	35.93	36.07	36.24	36.379999999999995	36.53	36.690000000000012	36.770000000000003	36.94	37.090000000000003	37.270000000000003	37.410000000000004	37.53	37.690000000000012	37.809999999999995	37.93	38.020000000000003	38.21	38.290000000000013	38.42	38.51	38.660000000000011	38.809999999999995	38.86	38.949999999999996	39.07	39.14	39.28	39.349999999999994	39.47	39.550000000000004	39.700000000000003	39.730000000000011	39.83	39.92	40.050000000000004	40.1	40.190000000000012	40.24	40.309999999999995	40.339999999999996	40.56	40.6	40.78	40.790000000000013	40.839999999999996	40.97	41.05	41.190000000000012	41.21	41.36	41.42	41.52	41.61	41.75	41.849999999999994	41.99	42.04	42.18	42.25	42.41	42.53	42.6	42.730000000000011	42.89	42.96	43.07	43.190000000000012	43.339999999999996	43.43	43.54	43.65	43.83	43.93	44.13	44.27	44.42	44.61	44.730000000000011	44.89	45.06	45.15	45.32	45.44	45.55	45.690000000000012	45.83	45.97	46.04	46.13	46.230000000000011	46.41	46.48	46.660000000000011	46.760000000000012	46.9	46.93	47.220000000000013	47.290000000000013	47.39	47.49	47.67	47.720000000000013	47.83	47.97	48.1	48.17	48.33	48.52	48.58	48.690000000000012	48.879999999999995	48.94	49.07	49.24	49.32	49.39	49.53	49.690000000000012	49.77	49.87	49.99	50.120000000000012	50.2	50.449999999999996	50.49	50.58	50.720000000000013	50.9	50.96	51.1	51.190000000000012	51.349999999999994	51.42	51.58	51.71	51.77	51.879999999999995	52.03	52.1	52.18	52.25	52.46	52.51	52.68	52.75	52.89	52.96	53.13	53.3	53.41	53.56	53.67	53.790000000000013	53.97	54.03	54.14	54.260000000000012	54.42	54.52	54.64	54.67	54.839999999999996	54.94	55.11	55.230000000000011	55.37	55.53	55.61	55.71	55.83	55.99	56.1	56.260000000000012	56.41	56.620000000000012	56.68	56.77	56.91	57.09	57.160000000000011	57.3	57.39	57.54	57.61	57.760000000000012	57.92	57.98	58.08	58.25	58.3	58.43	58.52	58.67	58.74	58.9	59.07	59.120000000000012	59.24	59.36	59.5	59.58	59.790000000000013	59.86	59.97	60.1	60.230000000000011	60.309999999999995	60.43	60.53	60.690000000000012	60.78	60.93	61.1	61.190000000000012	61.27	61.48	61.59	61.760000000000012	61.97	62.05	62.25	62.41	62.5	62.68	62.839999999999996	62.97	63.09	63.230000000000011	63.39	63.52	63.690000000000012	63.87	63.949999999999996	64.11	64.319999999999993	64.48	64.599999999999994	64.73	64.930000000000007	65.010000000000005	65.179999999999978	65.349999999999994	65.430000000000007	65.55	65.7	65.97	66.02	66.149999999999991	66.349999999999994	66.489999999999995	66.739999999999995	67.03	67.36999999999999	67.679999999999978	68.02	68.55	68.84	69.3	69.59	70.11	70.38	70.790000000000006	71.069999999999993	71.61	71.86	72.290000000000006	72.55	73.069999999999993	73.319999999999993	73.679999999999978	73.930000000000007	74.23	74.63	74.97	75.290000000000006	75.61999999999999	76.05	76.28	76.669999999999987	76.92	77.36	77.59	77.84	78.149999999999991	78.459999999999994	78.849999999999994	79.08	79.430000000000007	79.599999999999994	79.92	80.290000000000006	80.48	80.83	81	81.27	81.63	81.81	82.02	82.25	82.42	82.679999999999978	82.85	83.09	83.22	83.38	83.6	83.76	84.03	84.179999999999978	84.440000000000026	84.58	84.76	84.990000000000023	85.210000000000022	85.42	85.57	85.83	85.97	86.2	86.35	86.53	86.75	86.86999999999999	87.16	87.27	87.440000000000026	87.64	87.77	87.960000000000022	88.07	88.240000000000023	88.36999999999999	88.63	88.7	88.84	88.960000000000022	89.11999999999999	89.2	89.36999999999999	89.54	89.63	89.740000000000023	89.86999999999999	90	90.07	90.3	90.32	90.43	90.54	90.710000000000022	90.77	90.86999999999999	91	91.16	91.23	91.36999999999999	91.52	91.61	91.72	91.9	91.960000000000022	92.08	92.19	92.34	92.410000000000025	92.56	92.73	92.79	92.89	93.03	93.169999999999987	93.23	93.32	93.58	93.59	93.69	93.81	93.960000000000022	94.03	94.14	94.27	94.43	94.490000000000023	94.61999999999999	94.710000000000022	94.83	94.9	94.97	95.07	95.32	95.33	95.42	95.54	95.73	95.79	95.95	96.03	96.23	96.27	96.36	96.490000000000023	96.64	96.83	96.89	96.990000000000023	97.11	97.26	97.33	97.440000000000026	97.55	97.710000000000022	97.79	97.9	98.03	98.240000000000023	98.4	98.48	98.55	98.7	98.86999999999999	98.93	99.04	99.169999999999987	99.31	99.35	99.43	99.54	99.66	99.740000000000023	99.79	99.93	100.19	100.23	100.32	100.44000000000032	100.6	100.64999999999999	100.66	100.66999999999999	100.95	101.04	101.16	101.28	101.43	101.51	101.61	101.69	101.83	102	102.03	102.11999999999999	102.24000000000002	102.43	102.49000000000002	102.64	102.8	102.9	102.99000000000002	103.11999999999999	103.29	103.34	103.43	103.57	103.66	103.75	103.86	103.99000000000002	104.06	104.16	104.24000000000002	104.39	104.5	104.6	104.74000000000002	104.92	104.97	105.11	105.28	105.34	105.47	105.53	105.7	105.8	105.85	106.05	106.17999999999998	106.27	106.42	106.6	106.77	106.84	106.96000000000002	107.08	107.26	107.29	107.44000000000032	107.64	107.71000000000002	107.81	108.03	108.16	108.36999999999999	108.5	108.66	108.84	108.98	109.16	109.36999999999999	109.51	109.75	109.83	110.01	110.14999999999999	110.3	110.36	110.52	110.74000000000002	110.81	110.99000000000002	111.16999999999999	111.32	111.4	111.61	111.83	111.9	112.08	112.24000000000002	112.34	112.52	112.69	112.82	113	113.16	113.28	113.45	113.53	113.71000000000002	113.83	113.94000000000032	114.13	114.27	114.4	114.55	114.74000000000002	114.82	115.01	115.19	115.27	115.38	115.61999999999999	115.77	115.85	115.98	116.08	116.26	116.36999999999999	116.52	116.7	116.8	116.97	117.17999999999998	117.27	117.36999999999999	117.47	117.64999999999999	117.75	117.93	118.08	118.17999999999998	118.36999999999999	118.46000000000002	118.61	118.86999999999999	118.99000000000002	119.16	119.39	119.57	119.71000000000002	119.92	120.05	120.26	120.36999999999999	120.52	120.73	120.8	121	121.16999999999999	121.25	121.39	121.64	121.76	121.85	121.98	122.19	122.32	122.47	122.64999999999999	122.74000000000002	122.9	123.13	123.23	123.42	123.64999999999999	123.81	124.4	124.75	125.36	125.99000000000002	126.45	126.92	127.32	127.86999999999999	128.46	128.83000000000001	129.44	129.96	130.35000000000107	130.96	131.37	131.81	132.41999999999999	132.72	133.18	133.47	133.97	134.33000000000001	134.69999999999999	135.07	135.52000000000001	135.86000000000001	136.19999999999999	136.56	136.97999999999999	137.28	137.60999999999999	137.91	138.35000000000107	138.49	138.76	139.05000000000001	139.36000000000001	139.73999999999998	139.91999999999999	140.10999999999999	140.36000000000001	140.59	140.86000000000001	141.13999999999999	141.34	141.55000000000001	141.80000000000001	142.07	142.31	142.57	142.75	143.02000000000001	143.19	143.44	143.68	143.93	144.1	144.28	144.54	144.69	144.99	145.20999999999998	145.37	145.55000000000001	145.83000000000001	145.94999999999999	146.16999999999999	146.38000000000127	146.46	146.66999999999999	146.79	146.89000000000001	147.1	147.20999999999998	147.26	147.4	147.6	147.75	147.9	148.08000000000001	148.19999999999999	148.26	148.35000000000107	148.47	148.66	148.69999999999999	148.84	148.91999999999999	149.1	149.13999999999999	149.28	149.36000000000001	149.54	149.58000000000001	149.66	149.87	149.9	150	150.1	150.26999999999998	150.33000000000001	150.44	150.55000000000001	150.70999999999998	150.76	150.88000000000127	151.01	151.19	151.26	151.44999999999999	151.54	151.68	151.76	151.9	151.97999999999999	152.13999999999999	152.33000000000001	152.39000000000001	152.5	152.60999999999999	152.78	152.84	153.01	153.07	153.15	153.26	153.44	153.5	153.6	153.72	153.9	153.94	154.04	154.13999999999999	154.33000000000001	154.37	154.47	154.66	154.69999999999999	154.80000000000001	154.91	155.06	155.13	155.22	155.34	155.47999999999999	155.56	155.68	155.76	155.93	155.99	156.13	156.19999999999999	156.37	156.46	156.58000000000001	156.65	156.80000000000001	156.86000000000001	157.04	157.15	157.19	157.22	157.37	157.47999999999999	157.58000000000001	157.75	157.82000000000087	158.06	158.09	158.20999999999998	158.34	158.5	158.58000000000001	158.70999999999998	158.79	158.94	159.04	159.16	159.34	159.39000000000001	159.5	159.72	159.73999999999998	159.84	159.94999999999999	160.12	160.16999999999999	160.28	160.39000000000001	160.57	160.60999999999999	160.70999999999998	160.83000000000001	160.99	161.06	161.25	161.32000000000087	161.41999999999999	161.54	161.72	161.76999999999998	161.88000000000127	162.01	162.18	162.23999999999998	162.38000000000127	162.47	162.63	162.85000000000107	162.9	163	163.12	163.29	163.35000000000107	163.49	163.59	163.76	163.85000000000107	163.99	164.05	164.2	164.37	164.46	164.55	164.69	164.87	164.94	165.09	165.29	165.35000000000107	165.45000000000007	165.56	165.75	165.86	165.94	166.04	166.16	166.31	166.38000000000127	166.53	166.60999999999999	166.8	166.85000000000107	166.98000000000027	167.06	167.22	167.26999999999998	167.39000000000001	167.45000000000007	167.58	167.70999999999998	167.86	168.04	168.15	168.29	168.45000000000007	168.52	168.62	168.75	168.92000000000004	168.98000000000027	169.15	169.22	169.36	169.5	169.6	169.7	169.83	170.02	170.09	170.25	170.46	170.72	170.8	171.06	171.36	171.66	171.99	172.22	172.43	172.75	173.09	173.48000000000027	173.76999999999998	174.09	174.31	174.86	175.31	175.88000000000127	176.52	176.87	177.23999999999998	177.51	177.94	178.19	178.43	178.76999999999998	179.10999999999999	179.46	179.76999999999998	180.12	180.44	180.85000000000107	181.05	181.42000000000004	181.57	181.87	182.2	182.4	182.6	182.83	183	183.17	183.39000000000001	183.72	183.83	184.07	184.33	184.6	184.99	185.13	185.34	185.59	185.78	186.02	186.32000000000087	186.52	186.69	186.92000000000004	187.08	187.26999999999998	187.49	187.79	187.89000000000001	188.1	188.32000000000087	188.47	188.67	188.9	189.17	189.28	189.49	189.7	189.81	190.02	190.23999999999998	190.35000000000107	190.62	190.76	190.93	191.14	191.22	191.42000000000004	191.64	191.72	192.03	192.17	192.3	192.55	192.7	192.9	193.12	193.22	193.44	193.56	193.75	193.89000000000001	194.04	194.23	194.47	194.56	194.70999999999998	194.97	195.03	195.20999999999998	195.42000000000004	195.51	195.70999999999998	195.9	195.99	196.19	196.39000000000001	196.46	196.63	196.83	196.92000000000004	197.12	197.3	197.41	197.68	197.83	197.95000000000007	198.10999999999999	198.29	198.43	198.58	198.79	198.92000000000004	199.16	199.23999999999998	199.42000000000004	199.59	199.75	199.95000000000007	200.2	200.29	200.52	200.63	200.76	200.96	201.05	201.2	201.36	201.45000000000007	201.62	201.76999999999998	201.85000000000107	202.04	202.04	202.13	202.23	202.44	202.51	202.64	202.70999999999998	202.89000000000001	202.94	203.1	203.23999999999998	203.35000000000107	203.42000000000004	203.56	203.60999999999999	203.76	203.83	203.98000000000027	204.04	204.14	204.25	204.36	204.43	204.46	204.52	204.57	204.64	204.82000000000087	204.84	204.97	205.15	205.28	205.37	205.43	205.55	205.62	205.79	205.83	205.94	206.05	206.10999999999999	206.23999999999998	206.3	206.47	206.6	206.67	206.76999999999998	206.88000000000127	207.03	207.18	207.19	207.29	207.4	207.54	207.62	207.72	207.84	207.97	208.08	208.19	208.31	208.34	208.52	208.64	208.81	208.86	208.96	209.08	209.2	209.26	209.4	209.55	209.65	209.76999999999998	209.86	209.91	210.09	210.15	210.41	210.45000000000007	210.57	210.68	210.85000000000107	210.9	211.01	211.13	211.31	211.35000000000107	211.45000000000007	211.57	211.75	211.76999999999998	211.84	211.98000000000027	212.16	212.26	212.39000000000001	212.5	212.62	212.70999999999998	212.85000000000107	212.97	213.07	213.22	213.3	213.43	213.5	213.56	213.88000000000127	213.88000000000127	214	214.08	214.23999999999998	214.33	214.44	214.51	214.58	214.76999999999998	214.84	215	215.07	215.23999999999998	215.3	215.49	215.59	215.7	215.79	215.94	216.03	216.17	216.35000000000107	216.41	216.51	216.63	216.83	216.87	217.06	217.12	217.22	217.33	217.51	217.57	217.70999999999998	217.76999999999998	217.94	218.03	218.12	218.20999999999998	218.35000000000107	218.46	218.57	218.67	218.78	218.91	219.04	219.13	219.2	219.3	219.51	219.58	219.67	219.76	219.92000000000004	219.97	220.06	220.18	220.39000000000001	220.47	220.63	220.76	220.88000000000127	220.96	221.07	221.19	221.28	221.36	221.48000000000027	221.63	221.75	222.10999999999999	222.39000000000001	222.75	223.3	223.67	224.12	224.43	224.94	225.31	225.68	226.04	226.48000000000027	226.83	227.23	227.6	228.01	228.31	228.62	228.96	229.35000000000107	229.68	230.01	230.35000000000107	230.79	231.05	231.41	231.67	232.12	232.36	232.69	232.89000000000001	233.2	233.58	233.78	234.1	234.25	234.53	234.91	235.02	235.25	235.49	235.67	235.88000000000127	236.12	236.34	236.51	236.68	236.9	237.05	237.23	237.45000000000007	237.73	237.82000000000087	237.94	238.09	238.29	238.43	238.67	238.81	239.06	239.18	239.29	239.4	239.55	239.63	239.76	239.89000000000001	240.08	240.13	240.31	240.46	240.53	240.72	240.76999999999998	240.92000000000004	240.98000000000027	241.13	241.20999999999998	241.3	241.43	241.58	241.63	241.72	241.83	241.98000000000027	242.04	242.17	242.25	242.4	242.51	242.62	242.69	242.86	242.91	243.07	243.2	243.26999999999998	243.38000000000127	243.5	243.69	243.73	243.83	244.04	244.07	244.16	244.26	244.43	244.52	244.60999999999999	244.73999999999998	244.89000000000001	244.97	245.10999999999999	245.2	245.36	245.42000000000004	245.58	245.69	245.78	245.89000000000001	246.06	246.13	246.29	246.42000000000004	246.53	246.63	246.75	246.9	246.97	247.13	247.26	247.32000000000087	247.47	247.62	247.70999999999998	247.81	247.95000000000007	248.1	248.16	248.32000000000087	248.44	248.55	248.63	248.79	248.86	249.01	249.13	249.23999999999998	249.26	249.43	249.60999999999999	249.68	249.86	250	250.07	250.18	250.35000000000107	250.43	250.58	250.65	250.82000000000087	250.87	251.04	251.18	251.19	251.23	251.37	251.55	251.65	251.76	251.84	252.02	252.10999999999999	252.22	252.33	252.47	252.59	252.70999999999998	252.84	252.99	253.06	253.16	253.29	253.42000000000004	253.47	253.66	253.76999999999998	253.82000000000087	253.88000000000127	253.9	254.13	254.37	254.52	254.66	254.73	254.88000000000127	255.03	255.12	255.23999999999998	255.33	255.49	255.56	255.7	255.86	255.94	256.02	256.26	256.33	256.39999999999969	256.62	256.68	256.78999999999894	256.91999999999899	257.13	257.18	257.33999999999969	257.47000000000003	257.60000000000002	257.7	257.83	257.97999999999894	258.17	258.22000000000003	258.27999999999969	258.41000000000003	258.57	258.66000000000008	258.74	258.86	259	259.07	259.22000000000003	259.38	259.47999999999894	259.57	259.76	259.81	259.89	260.01	260.19	260.25	260.33999999999969	260.47000000000003	260.68	260.82	260.94	260.97999999999894	261.22000000000003	261.31	261.47000000000003	261.62	261.83999999999969	262.13	262.45	262.74	263.05	263.41000000000003	263.95999999999964	264.28999999999894	264.7	264.92999999999893	265.45	265.77	266.13	266.39999999999969	266.94	267.19	267.58999999999969	267.87	268.39	268.57	269.02	269.20999999999964	269.64000000000038	269.95	270.27	270.60000000000002	270.89	271.33	271.45	271.76	272	272.24	272.51	272.78999999999894	272.86	273.08999999999969	273.32	273.47999999999894	273.68	273.87	273.98999999999899	274.18	274.47000000000003	274.91999999999899	275.55	275.69	276.01	276.19	276.39	276.58	276.72000000000003	276.97999999999894	277.22000000000003	277.45	277.60000000000002	277.85000000000002	278.05	278.36	278.45	278.67	278.89	278.98999999999899	279.24	279.44	279.58999999999969	279.8	279.97999999999894	280.20999999999964	280.33	280.54000000000002	280.75	280.87	281.14000000000038	281.25	281.44	281.63	281.72999999999894	281.91999999999899	282.12	282.22000000000003	282.33999999999969	282.64000000000038	282.7	282.85000000000002	282.97999999999894	283.10000000000002	283.2	283.31	283.45999999999964	283.52999999999969	283.61	283.72999999999894	283.87	283.94	284.05	284.27999999999969	284.33	284.41999999999899	284.52	284.64999999999998	284.77999999999969	284.85000000000002	284.95	285	285.17	285.22000000000003	285.36	285.41999999999899	285.57	285.64000000000038	285.81	285.95	286.02	286.14000000000038	286.20999999999964	286.41000000000003	286.44	286.55	286.66000000000008	286.8	286.87	287.02999999999969	287.08	287.20999999999964	287.22999999999894	287.27999999999969	287.39	287.44	287.61	287.66000000000008	287.78999999999894	287.81	287.91000000000003	288.01	288.02999999999969	288.14000000000038	288.26	288.35000000000002	288.45	288.62	288.66000000000008	288.75	288.87	288.91000000000003	289.06	289.10000000000002	289.16000000000008	289.27	289.41999999999899	289.48999999999899	289.69	289.7	289.78999999999894	289.88	290.05	290.12	290.2	290.31	290.47999999999894	290.54000000000002	290.64000000000038	290.75	290.89	290.92999999999893	291.02999999999969	291.13	291.37	291.37	291.47000000000003	291.58999999999969	291.7	291.74	291.82	291.92999999999893	291.95999999999964	292.01	292.18	292.19	292.28999999999894	292.39	292.42999999999893	292.58	292.58	292.62	292.72000000000003	292.77	292.89	292.89999999999969	292.94	293	293.12	293.56	293.72000000000003	293.97000000000003	294.20999999999964	294.33999999999969	294.52999999999969	294.70999999999964	294.83	295.06	295.08999999999969	295.19	295.27	295.33	295.51	295.52999999999969	295.62	295.74	295.88	295.88	295.92999999999893	296.02999999999969	296.08999999999969	296.22999999999894	296.22999999999894	296.32	296.39999999999969	296.45999999999964	296.87	297.14000000000038	297.41999999999899	297.7	297.87	298.05	298.22000000000003	298.27	298.5	298.57	298.64999999999998	298.76	298.97000000000003	298.98999999999899	299.07	299.17	299.33	299.38	299.45	299.56	299.69	299.75	299.82	299.91999999999899	299.97000000000003	300.11	300.26	300.45999999999964	300.72999999999894	301.04000000000002	301.32	301.68	301.89	302.10000000000002	302.36	302.60000000000002	302.83999999999969	303.07	303.18	303.33	303.45	303.67	303.83999999999969	304.08	304.51	304.83999999999969	305.24	305.47999999999894	305.68	306.07	306.14000000000038	306.39999999999969	306.61	306.74	306.91000000000003	307.12	307.18	307.37	307.58999999999969	307.72999999999894	307.89999999999969	308.08999999999969	308.22999999999894	308.39999999999969	308.61	308.75	308.98999999999899	309.14000000000038	309.3	309.51	309.64999999999998	309.83	310.04000000000002	310.26	310.41999999999899	310.55	310.7	310.91999999999899	311.07	311.31	311.45	311.67	311.8	311.98999999999899	312.2	312.3	312.5	312.69	312.81	313.13	313.22000000000003	313.38	313.58	313.70999999999964	313.89999999999969	314.12	314.22999999999894	314.48999999999899	314.60000000000002	314.77	314.94	315.08	315.22000000000003	315.47000000000003	315.58999999999969	315.72999999999894	316.01	316.07	316.26	316.42999999999893	316.55	316.77999999999969	316.97999999999894	317.02	317.18	317.41000000000003	317.58	317.72999999999894	317.97000000000003	318.12	318.3	318.51	318.77	318.86	318.97000000000003	319.19	319.35000000000002	319.52	319.78999999999894	319.89999999999969	320.14999999999998	320.25	320.42999999999893	320.63	320.75	320.94	321.18	321.27	321.55	321.64000000000038	321.83	322	322.12	322.32	322.54000000000002	322.63	322.87	323.01	323.19	323.38	323.5	323.68	323.87	324.01	324.19	324.39999999999969	324.60000000000002	324.7	324.83999999999969	325.02999999999969	325.20999999999964	325.38	325.44	325.72999999999894	325.89	326.08999999999969	326.27	326.39	326.58999999999969	326.81	326.89999999999969	327.08999999999969	327.25	327.41999999999899	327.66000000000008	327.78999999999894	327.97999999999894	328.17	328.31	328.44	328.67	328.8	328.95	329.16	329.3	329.47999999999894	329.68	329.84000000000032	330.04	330.19	330.34000000000032	330.55	330.67	330.85	331.05	331.19	331.39	331.55	331.71	331.9	332.04	332.2	332.41999999999899	332.54	332.8	332.9	333.08	333.26	333.36	333.56	333.76	333.85	334.04	334.31	334.38	334.57	334.72999999999894	334.84000000000032	335.04	335.28	335.35	335.53	335.75	335.86	336.05	336.22999999999894	336.36	336.54	336.71999999999969	336.86	337.19	337.22999999999894	337.36	337.58	337.71	337.84000000000032	337.98999999999899	338.17	338.31	338.63	338.67	338.88	339.07	339.12	339.34000000000032	339.52	339.66	339.84000000000032	340.09	340.16	340.37	340.56	340.71	340.88	341.09	341.18	341.52	341.58	341.78	341.95	342.06	342.28	342.46	342.57	342.89	342.96999999999969	343.09	343.3	343.44	343.62	343.78	343.94	344.08	344.31	344.45	344.6	344.78999999999894	344.91999999999899	345.08	345.28999999999894	345.37	345.56	345.71999999999969	345.88	346.06	346.22999999999894	346.32	346.48999999999899	346.71999999999969	346.81	347.12	347.22999999999894	347.4	347.46999999999969	347.62	347.78	347.96	348.19	348.34000000000032	348.61	348.71	348.89	349.11	349.25	349.4	500 mm	331.5	332	332.5	333	333.5	334	334.5	335	335.5	336	336.5	337	337.5	338	338.5	339	339.5	340	340.5	341	341.5	342	342.5	343	343.5	344	344.5	345	345.5	346	346.5	347	347.5	348	348.5	349	349.5	350	350.5	351	351.5	352	352.5	353	353.5	354	354.5	355	355.5	356	356.5	357	357.5	358	358.5	359	359.5	360	360.5	361	361.5	362	362.5	363	363.5	364	364.5	365	365.5	366	366.5	367	367.5	368	368.5	369	369.5	370	370.5	371	371.5	372	372.5	373	373.5	374	374.5	375	375.5	376	376.5	377	377.5	378	378.5	379	379.5	380	380.5	381	381.5	382	382.5	383	383.5	384	384.5	385	385.5	386	386.5	387	387.5	388	388.5	389	389.5	390	390.5	391	391.5	392	392.5	393	393.5	394	394.5	395	395.5	396	396.5	397	397.5	398	398.5	399	399.5	400	400.5	401	401.5	402	402.5	403	403.5	404	404.5	405	405.5	406	406.5	407	407.5	408	408.5	409	409.5	410	410.5	411	411.5	412	412.5	413	413.5	414	414.5	415	415.5	416	416.5	417	417.5	418	418.5	419	419.5	420	420.5	421	421.5	422	422.5	423	423.5	424	424.5	425	425.5	426	426.5	427	427.5	428	428.5	429	429.5	430	430.5	431	431.5	432	432.5	433	433.5	434	434.5	435	435.5	436	436.5	437	437.5	438	438.5	439	439.5	440	440.5	441	441.5	442	442.5	443	443.5	444	444.5	445	445.5	446	446.5	447	447.5	448	448.5	449	449.5	450	450.5	451	451.5	452	452.5	453	453.5	454	454.5	455	455.5	456	456.5	457	457.5	458	458.5	459	459.5	460	460.5	461	461.5	462	462.5	463	463.5	464	464.5	465	465.5	466	466.5	467	467.5	468	468.5	469	469.5	470	470.5	471	471.5	472	472.5	473	473.5	474	474.5	475	475.5	476	476.5	477	477.5	478	478.5	479	479.5	480	480.5	481	481.5	482	482.5	483	483.5	484	484.5	485	485.5	486	486.5	487	487.5	488	488.5	489	489.5	490	490.5	491	491.5	492	492.5	493	493.5	494	494.5	495	495.5	496	496.5	497	497.5	498	498.5	499	499.5	500	500.5	501	501.5	502	502.5	503	503.5	504	504.5	505	505.5	506	506.5	507	507.5	508	508.5	509	509.5	510	510.5	511	511.5	512	512.5	513	513.5	514	514.5	515	515.5	516	516.5	517	517.5	518	518.5	519	519.5	520	520.5	521	521.5	522	522.5	523	523.5	524	524.5	525	525.5	526	526.5	527	527.5	528	528.5	529	529.5	530	530.5	531	531.5	532	532.5	533	533.5	534	534.5	535	535.5	536	536.5	537	537.5	538	538.5	539	539.5	540	540.5	541	541.5	542	542.5	543	543.5	544	544.5	545	545.5	546	546.5	547	547.5	548	548.5	549	549.5	550	550.5	551	551.5	552	552.5	553	553.5	554	554.5	555	555.5	556	556.5	557	557.5	558	558.5	559	559.5	560	560.5	561	561.5	562	562.5	563	563.5	564	564.5	565	565.5	566	566.5	567	567.5	568	568.5	569	569.5	570	570.5	571	571.5	572	572.5	573	573.5	574	574.5	575	575.5	576	576.5	577	577.5	578	578.5	579	579.5	580	580.5	581	581.5	582	582.5	583	583.5	584	584.5	585	585.5	586	586.5	587	587.5	588	588.5	589	589.5	590	590.5	591	591.5	592	592.5	593	593.5	594	594.5	595	595.5	596	596.5	597	597.5	598	598.5	599	599.5	600	600.5	601	601.5	602	602.5	603	603.5	604	604.5	605	605.5	606	606.5	607	607.5	608	608.5	609	609.5	610	610.5	611	611.5	612	612.5	613	613.5	614	614.5	615	615.5	616	616.5	617	617.5	618	618.5	619	619.5	620	620.5	621	621.5	622	622.5	623	623.5	624	624.5	625	625.5	626	626.5	627	627.5	628	628.5	629	629.5	630	630.5	631	631.5	632	632.5	633	633.5	634	634.5	635	635.5	636	636.5	637	637.5	638	638.5	639	639.5	640	640.5	641	641.5	642	642.5	643	643.5	644	644.5	645	645.5	646	646.5	647	647.5	648	648.5	649	649.5	650	650.5	651	651.5	652	652.5	653	653.5	654	654.5	655	655.5	656	656.5	657	657.5	658	658.5	659	659.5	660	660.5	661	661.5	662	662.5	663	663.5	664	664.5	665	665.5	666	666.5	667	667.5	668	668.5	669	669.5	670	670.5	671	671.5	672	672.5	673	673.5	674	674.5	675	675.5	676	676.5	677	677.5	678	678.5	679	679.5	680	680.5	681	681.5	682	682.5	683	683.5	684	684.5	685	685.5	686	686.5	687	687.5	688	688.5	689	689.5	690	690.5	691	691.5	692	692.5	693	693.5	694	694.5	695	695.5	696	696.5	697	697.5	698	698.5	699	699.5	700	700.5	701	701.5	702	702.5	703	703.5	704	704.5	705	705.5	706	706.5	707	707.5	708	708.5	709	709.5	710	710.5	711	711.5	712	712.5	713	713.5	714	714.5	715	715.5	716	716.5	717	717.5	718	718.5	719	719.5	720	720.5	721	721.5	722	722.5	723	723.5	724	724.5	725	725.5	726	726.5	727	727.5	728	728.5	729	729.5	730	730.5	731	731.5	732	732.5	733	733.5	734	734.5	735	735.5	736	736.5	737	737.5	738	738.5	739	739.5	740	740.5	741	741.5	742	742.5	743	743.5	744	744.5	745	745.5	746	746.5	747	747.5	748	748.5	749	749.5	750	750.5	751	751.5	752	752.5	753	753.5	754	754.5	755	755.5	756	756.5	757	757.5	758	758.5	759	759.5	760	760.5	761	761.5	762	762.5	763	763.5	764	764.5	765	765.5	766	766.5	767	767.5	768	768.5	769	769.5	770	770.5	771	771.5	772	772.5	773	773.5	774	774.5	775	775.5	776	776.5	777	777.5	778	778.5	779	779.5	780	780.5	781	781.5	782	782.5	783	783.5	784	784.5	785	785.5	786	786.5	787	787.5	788	788.5	789	789.5	790	790.5	791	791.5	792	792.5	793	793.5	794	794.5	795	795.5	796	796.5	797	797.5	798	798.5	799	799.5	800	800.5	801	801.5	802	802.5	803	803.5	804	804.5	805	805.5	806	806.5	807	807.5	808	808.5	809	809.5	810	810.5	811	811.5	812	812.5	813	813.5	814	814.5	815	815.5	816	816.5	817	817.5	818	818.5	819	819.5	820	820.5	821	821.5	822	822.5	823	823.5	824	824.5	825	825.5	826	826.5	827	827.5	828	828.5	829	829.5	830	830.5	831	831.5	832	832.5	833	833.5	834	834.5	835	835.5	836	836.5	837	837.5	838	838.5	839	839.5	840	840.5	841	841.5	842	842.5	843	843.5	844	844.5	845	845.5	846	846.5	847	847.5	848	848.5	849	849.5	850	850.5	851	851.5	852	852.5	853	853.5	854	854.5	855	855.5	856	856.5	857	857.5	858	858.5	859	859.5	860	860.5	861	861.5	862	862.5	863	863.5	864	864.5	865	865.5	866	866.5	867	867.5	868	868.5	869	869.5	870	870.5	871	871.5	872	872.5	873	873.5	874	874.5	875	875.5	876	876.5	877	877.5	878	878.5	879	879.5	880	880.5	881	881.5	882	882.5	883	883.5	884	884.5	885	885.5	886	886.5	887	887.5	888	888.5	889	889.5	890	890.5	891	891.5	892	892.5	893	893.5	894	894.5	895	895.5	896	896.5	897	897.5	898	898.5	899	899.5	900	900.5	901	901.5	902	902.5	903	903.5	904	904.5	905	905.5	906	906.5	907	907.5	908	908.5	909	909.5	910	910.5	911	911.5	912	912.5	913	913.5	914	914.5	915	915.5	916	916.5	917	917.5	918	918.5	919	919.5	920	920.5	921	921.5	922	922.5	923	923.5	924	924.5	925	925.5	926	926.5	927	927.5	928	928.5	929	929.5	930	930.5	931	931.5	932	932.5	933	933.5	934	934.5	935	935.5	936	936.5	937	937.5	938	938.5	939	939.5	940	940.5	941	941.5	942	942.5	943	943.5	944	944.5	945	945.5	946	946.5	947	947.5	948	948.5	949	949.5	950	950.5	951	951.5	952	952.5	953	953.5	954	954.5	955	955.5	956	956.5	957	957.5	958	958.5	959	959.5	960	960.5	961	961.5	962	962.5	963	963.5	964	964.5	965	965.5	966	966.5	967	967.5	968	968.5	969	969.5	970	970.5	971	971.5	972	972.5	973	973.5	974	974.5	975	975.5	976	976.5	977	977.5	978	978.5	979	979.5	980	980.5	981	981.5	982	982.5	983	983.5	984	984.5	985	985.5	986	986.5	987	987.5	988	988.5	989	989.5	990	990.5	991	991.5	992	992.5	993	993.5	994	994.5	995	995.5	996	996.5	997	997.5	998	998.5	999	999.5	1000	1000.5	1001	1001.5	1002	1002.5	1003	1003.5	1004	1004.5	1005	1005.5	1006	1006.5	1007	1007.5	1008	1008.5	1009	1009.5	1010	1010.5	1011	1011.5	1012	1012.5	1013	1013.5	1014	1014.5	1015	1015.5	1016	1016.5	1017	1017.5	1018	1018.5	1019	1019.5	1020	1020.5	1021	1021.5	1022	1022.5	1023	1023.5	1024	1024.5	1025	1025.5	1026	1026.5	1027	1027.5	1028	1028.5	1029	1029.5	1030	1030.5	1031	1031.5	1032	1032.5	1033	1033.5	1034	1034.5	1035	1035.5	1036	1036.5	1037	1037.5	1038	1038.5	1039	1039.5	1040	1040.5	1041	1041.5	1042	1042.5	1043	1043.5	1044	1044.5	1045	1045.5	1046	1046.5	1047	1047.5	1048	1048.5	1049	1049.5	1050	1050.5	1051	1051.5	1052	1052.5	1053	1053.5	1054	1054.5	1055	1055.5	1056	1056.5	1057	1057.5	1058	1058.5	1059	1059.5	1060	1060.5	1061	1061.5	1062	1062.5	1063	1063.5	1064	1064.5	1065	1065.5	1066	1066.5	1067	1067.5	1068	1068.5	1069	1069.5	1070	1070.5	1071	1071.5	1072	1072.5	1073	1073.5	1074	1074.5	1075	1075.5	1076	1076.5	1077	1077.5	1078	1078.5	1079	1079.5	1080	1080.5	1081	1081.5	1082	1082.5	1083	1083.5	1084	1084.5	1085	1085.5	1086	1086.5	1087	1087.5	1088	1088.5	1089	1089.5	1090	1090.5	1091	1091.5	1092	1092.5	1093	1093.5	1094	1094.5	1095	1095.5	1096	1096.5	1097	1097.5	1098	1098.5	1099	1099.5	1100	1100.5	1101	1101.5	1102	1102.5	1103	1103.5	1104	1104.5	1105	1105.5	1106	1106.5	1107	1107.5	1108	1108.5	1109	1109.5	1110	1110.5	1111	1111.5	1112	1112.5	1113	1113.5	1114	1114.5	1115	1115.5	1116	1116.5	1117	1117.5	1118	1118.5	1119	1119.5	1120	1120.5	1121	1121.5	1122	1122.5	1123	1123.5	1124	1124.5	1125	1125.5	1126	1126.5	1127	1127.5	1128	1128.5	1129	1129.5	1130	1130.5	1131	1131.5	1132	1132.5	1133	1133.5	1134	1134.5	1135	1135.5	1136	1136.5	1137	1137.5	1138	1138.5	1139	1139.5	1140	1140.5	1141	1141.5	1142	1142.5	1143	1143.5	1144	1144.5	1145	1145.5	1146	1146.5	1147	1147.5	1148	1148.5	1149	1149.5	1150	1150.5	1151	1151.5	1152	1152.5	1153	1153.5	1154	1154.5	1155	1155.5	1156	1156.5	1157	1157.5	1158	1158.5	1159	1159.5	1160	1160.5	1161	1161.5	1162	1162.5	1163	1163.5	1164	1164.5	1165	1165.5	1166	1166.5	1167	1167.5	1168	1168.5	1169	1169.5	1170	1170.5	1171	1171.5	1172	1172.5	1173	1173.5	1174	1174.5	1175	1175.5	1176	1176.5	1177	1177.5	1178	1178.5	1179	1179.5	1180	1180.5	1181	1181.5	1182	1182.5	1183	1183.5	1184	1184.5	1185	1185.5	1186	1186.5	1187	1187.5	1188	1188.5	1189	1189.5	1190	1190.5	1191	1191.5	1192	1192.5	1193	1193.5	1194	1194.5	1195	1195.5	1196	1196.5	1197	1197.5	1198	1198.5	1199	1199.5	1200	1200.5	1201	1201.5	1202	1202.5	1203	1203.5	1204	1204.5	1205	1205.5	1206	1206.5	1207	1207.5	1208	1208.5	1209	1209.5	1210	1210.5	1211	1211.5	1212	1212.5	1213	1213.5	1214	1214.5	1215	1215.5	1216	1216.5	1217	1217.5	1218	1218.5	1219	1219.5	1220	1220.5	1221	1221.5	1222	1222.5	1223	1223.5	1224	1224.5	1225	1225.5	1226	1226.5	1227	1227.5	1228	1228.5	1229	1229.5	1230	1230.5	1231	1231.5	1232	1232.5	1233	1233.5	1234	1234.5	1235	1235.5	1236	1236.5	1237	1237.5	1238	1238.5	1239	1239.5	1240	1240.5	1241	1241.5	1242	1242.5	1243	1243.5	1244	1244.5	1245	1245.5	1246	1246.5	1247	1247.5	1248	1248.5	1249	1249.5	1250	1250.5	1251	1251.5	1252	1252.5	1253	1253.5	1254	1254.5	1255	1255.5	1256	1256.5	1257	1257.5	1258	1258.5	1259	1259.5	1260	1260.5	1261	1261.5	1262	1262.5	1263	1263.5	1264	1264.5	1265	1265.5	1266	1266.5	1267	1267.5	1268	1268.5	1269	1269.5	1270	1270.5	1271	1271.5	1272	1272.5	1273	1273.5	1274	1274.5	1275	1275.5	1276	1276.5	1277	1277.5	1278	1278.5	1279	1279.5	1280	1280.5	1281	1281.5	1282	1282.5	1283	1283.5	1284	1284.5	1285	1285.5	1286	1286.5	1287	1287.5	1288	1288.5	1289	1289.5	1290	1290.5	1291	1291.5	1292	1292.5	1293	1293.5	1294	1294.5	1295	1295.5	1296	1296.5	1297	1297.5	1298	1298.5	1299	1299.5	1300	1300.5	1301	1301.5	1302	1302.5	1303	1303.5	1304	1304.5	1305	1305.5	1306	1306.5	1307	1307.5	1308	1308.5	1309	1309.5	1310	1310.5	1311	1311.5	1312	1312.5	1313	1313.5	1314	1314.5	1315	1315.5	1316	1316.5	1317	1317.5	1318	1318.5	1319	1319.5	1320	1320.5	1321	1321.5	1322	1322.5	1323	1323.5	1324	1324.5	1325	1325.5	1326	1326.5	1327	1327.5	1328	1328.5	1329	1329.5	1330	1330.5	1331	1331.5	1332	1332.5	1333	1333.5	1334	1334.5	1335	1335.5	1336	1336.5	1337	1337.5	1338	1338.5	1339	1339.5	1340	1340.5	1341	1341.5	1342	1342.5	1343	1343.5	1344	1344.5	1345	1345.5	1346	1346.5	1347	1347.5	1348	1348.5	1349	1349.5	1350	1350.5	1351	1351.5	1352	1352.5	1353	1353.5	1354	1354.5	1355	1355.5	1356	1356.5	1357	1357.5	1358	1358.5	1359	1359.5	1360	1360.5	1361	1361.5	1362	1362.5	1363	1363.5	1364	1364.5	1365	1365.5	1366	1366.5	1367	1367.5	1368	1368.5	1369	1369.5	1370	1370.5	1371	1371.5	1372	1372.5	1373	1373.5	1374	1374.5	1375	1375.5	1376	1376.5	1377	1377.5	1378	1378.5	1379	1379.5	1380	1380.5	1381	1381.5	1382	1382.5	1383	1383.5	1384	1384.5	1385	1385.5	1386	1386.5	1387	1387.5	1388	1388.5	1389	1389.5	1390	1390.5	1391	1391.5	1392	1392.5	1393	1393.5	1394	1394.5	1395	1395.5	1396	1396.5	1397	1397.5	1398	1398.5	1399	1399.5	1400	0	1.6800000000000141	2.68	3.64	4.4400000000000004	5.01	5.46	5.9300000000000024	6.1599999999999975	6.46	6.87	6.96	7.1499999999999995	7.34	7.45	7.6499999999999995	7.73	7.91	7.96	8.02	8.08	8.120000000000001	8.129999999999999	8.2100000000000009	8.33	8.32	8.34	8.4	8.4700000000000006	8.51	8.51	8.5300000000000011	8.59	8.7299999999999986	8.7200000000000006	8.7200000000000006	8.75	8.8600000000000048	8.8800000000000008	8.92	9.0400000000000009	9.07	9.1399999999999988	9.2299999999999986	9.26	9.3600000000000048	9.41	9.4500000000000028	9.5	9.58	9.6399999999999988	9.77	9.77	9.81	9.92	9.9600000000000026	10.01	10.15	10.15	10.220000000000001	10.3	10.31	10.360000000000024	10.47	10.54	10.49	10.52	10.53	10.639999999999999	10.709999999999999	10.84	10.96	11.08	11.27	11.370000000000006	11.6	11.77	12.09	13.139999999999999	13.78	14.04	14.32	14.61	14.870000000000006	15.12	15.360000000000024	15.41	15.51	15.62	15.77	15.81	15.88	15.99	16.03	16.14	16.190000000000001	16.25	16.36	16.439999999999987	16.62	16.670000000000005	16.739999999999988	16.86	17.03	17.18	17.3	17.38	17.510000000000005	17.54	17.62	17.690000000000001	17.779999999999987	17.829999999999988	17.979999999999986	18.100000000000001	18.130000000000031	18.21	18.27	18.399999999999999	18.459999999999987	18.479999999999986	18.59	18.75	18.84	18.89	19	19.190000000000001	19.34	19.420000000000002	19.579999999999988	19.75	19.760000000000002	19.760000000000002	19.88	20.079999999999988	20.16	20.22	20.239999999999988	20.32	20.49	20.55	20.69	20.79	20.82	21.05	21.25	21.330000000000005	21.49	21.71	21.79	21.959999999999987	22.18	22.25	22.610000000000031	22.79	22.97	23.19	23.279999999999987	23.49	23.71	23.810000000000031	24.1	24.18	24.330000000000005	24.5	24.610000000000031	24.72	24.84	25.02	25.08	25.18	25.279999999999987	25.459999999999987	25.64	25.66	25.71	25.89	26.04	26.110000000000031	26.22	26.36	26.51	26.55	26.68	26.75	26.88	26.91	27.01	27.36	27.51	27.67	27.88	27.95	28.110000000000031	28.27	28.38	28.49	28.64	28.87	28.95	29.04	29.150000000000031	29.25	29.34	29.38	29.54	29.59	29.74	29.810000000000031	29.97	30.03	30.17	30.24	30.55	30.66	30.72	30.88	31.09	31.19	31.34	31.53	31.650000000000031	31.79	31.87	32.07	32.14	32.300000000000004	32.43	32.53	32.64	32.770000000000003	32.89	32.96	33.04	33.160000000000011	33.32	33.370000000000005	33.449999999999996	33.54	33.74	33.790000000000013	33.849999999999994	33.9	34	34.050000000000004	34.18	34.270000000000003	34.36	34.49	34.6	34.67	34.800000000000004	35.08	35.36	35.44	35.64	35.89	36.04	36.25	36.449999999999996	36.67	36.770000000000003	36.86	36.99	37.21	37.339999999999996	37.590000000000003	37.720000000000013	37.839999999999996	38.090000000000003	38.190000000000012	38.379999999999995	38.57	38.660000000000011	38.75	38.97	39.120000000000012	39.24	39.379999999999995	39.56	39.65	39.800000000000004	39.849999999999994	39.96	40.050000000000004	40.15	40.230000000000011	40.25	40.410000000000004	40.47	40.720000000000013	40.97	41.2	41.339999999999996	41.52	41.74	42.68	43.09	43.49	44.01	44.42	44.7	45.01	45.33	45.730000000000011	45.97	46.25	46.42	46.87	47.2	47.5	47.78	47.97	48.290000000000013	48.56	48.660000000000011	48.839999999999996	49.05	49.160000000000011	49.36	49.55	49.63	49.71	49.87	50.09	50.17	50.32	50.47	50.6	50.74	50.879999999999995	51.04	51.17	51.43	51.620000000000012	51.83	52.09	52.21	52.4	52.620000000000012	52.730000000000011	53.02	53.17	53.32	53.5	53.59	53.82	54.03	54.11	54.309999999999995	54.48	54.54	54.720000000000013	54.94	55.02	55.190000000000012	55.379999999999995	55.48	55.660000000000011	55.89	55.94	56.03	56.14	56.18	56.41	56.660000000000011	56.879999999999995	57	57.28	57.379999999999995	57.61	57.879999999999995	58.1	58.339999999999996	58.59	58.660000000000011	58.8	58.93	59.11	59.21	59.339999999999996	59.49	59.54	59.620000000000012	59.71	59.77	59.89	59.93	60	60.11	60.14	60.309999999999995	60.33	60.53	60.53	60.63	60.690000000000012	60.730000000000011	60.75	60.75	60.78	60.93	60.99	61.03	61.07	61.15	61.21	61.37	61.379999999999995	61.42	61.46	61.54	61.61	61.74	61.8	61.97	62.11	62.190000000000012	62.28	62.41	62.6	62.879999999999995	63.04	63.290000000000013	63.44	63.65	63.89	64	64.260000000000005	64.349999999999994	64.52	64.66	64.75	64.86	64.989999999999995	65.13	65.22	65.31	65.42	65.59	65.61	65.69	65.72	65.73	65.930000000000007	66.11	66.23	66.36999999999999	66.63	66.77	66.930000000000007	67.13	67.239999999999995	67.459999999999994	67.540000000000006	67.72	67.86	67.95	68.13	68.290000000000006	68.36999999999999	68.47	68.59	68.75	68.790000000000006	68.84	68.959999999999994	69.010000000000005	69.040000000000006	69.08	69.23	69.400000000000006	69.510000000000005	69.599999999999994	69.78	69.959999999999994	70.14	70.39	70.510000000000005	70.649999999999991	70.84	70.940000000000026	71.09	71.22	71.33	71.48	71.53	71.66	71.77	71.849999999999994	71.89	72.010000000000005	72.16	72.45	72.53	72.709999999999994	72.910000000000025	73.05	73.38	73.790000000000006	74	74.28	74.53	74.849999999999994	75.22	75.36999999999999	75.56	75.81	76.06	76.33	76.58	76.7	76.930000000000007	77.23	77.56	77.92	78.099999999999994	78.33	78.58	78.83	79.11	79.36	79.569999999999993	79.89	80.08	80.319999999999993	80.55	80.81	80.959999999999994	81.38	81.58	81.81	82.169999999999987	82.31	82.57	82.83	83	83.29	83.55	83.69	83.82	84.06	84.179999999999978	84.36999999999999	84.56	84.679999999999978	84.83	85.1	85.240000000000023	85.39	85.59	85.740000000000023	85.910000000000025	86.11999999999999	86.22	86.47	86.52	86.64	86.78	86.990000000000023	87.13	87.27	87.47	87.83	87.95	88.13	88.3	88.47	88.679999999999978	88.76	88.97	89.11999999999999	89.32	89.51	89.77	89.86	90.05	90.25	90.36	90.84	91.08	91.4	91.58	91.86	92.25	92.410000000000025	92.649999999999991	92.9	93.06	93.27	93.490000000000023	93.73	93.83	94.02	94.19	94.29	94.48	94.61999999999999	94.740000000000023	94.82	94.98	95.25	95.33	95.45	95.57	95.740000000000023	95.81	96.04	96.32	96.47	96.679999999999978	96.75	96.960000000000022	97.2	97.32	97.460000000000022	97.7	98.06	98.13	98.33	98.56	98.7	98.89	99.14	99.36	99.460000000000022	99.61	99.75	99.88	100	100.13	100.32	100.45	100.61	100.85	100.9	101.02	101.13	101.29	101.41000000000012	101.63	101.83	101.93	102.09	102.26	102.34	102.48	102.56	102.71000000000002	102.8	102.85	102.94000000000032	103.09	103.16	103.25	103.36	103.51	103.55	103.63	103.73	103.76	103.86	103.91000000000012	103.93	103.98	104.11999999999999	104.36999999999999	104.4	104.48	104.73	104.86999999999999	105.08	105.16	105.29	105.39	105.56	105.81	105.86	105.94000000000032	106.08	106.2	106.24000000000002	106.41000000000012	106.49000000000002	106.58	106.64999999999999	106.81	106.86	106.99000000000002	107.06	107.2	107.23	107.39	107.41000000000012	107.46000000000002	107.7	107.77	107.86	107.98	108.14	108.2	108.43	108.66	108.73	108.86	109.05	109.2	109.27	109.43	109.6	109.66999999999999	109.8	109.92	110.05	110.11	110.26	110.39	110.46000000000002	110.51	110.63	110.67999999999998	110.8	110.84	110.86999999999999	110.93	111.1	111.11999999999999	111.16	111.25	111.31	111.55	111.73	111.92	112.14999999999999	112.35	112.45	112.56	112.7	112.9	113.01	113.16999999999999	113.29	113.36999999999999	113.48	113.6	113.91000000000012	113.96000000000002	114.14999999999999	114.26	114.41000000000012	114.46000000000002	114.59	114.66999999999999	114.79	114.9	115	115.03	115.17999999999998	115.21000000000002	115.24000000000002	115.36999999999999	115.43	115.52	115.61	115.71000000000002	115.9	115.9	115.98	116.01	116.09	116.22	116.25	116.38	116.73	116.96000000000002	117.25	117.6	117.95	118.25	118.73	119.03	119.38	119.66999999999999	120.11	120.36	120.69	120.91000000000012	121.56	121.99000000000002	122.36	122.66999999999999	123.06	123.35	123.64999999999999	123.95	124.22	124.6	124.76	125	125.25	125.55	125.91000000000012	126.14999999999999	126.42	126.66	126.83	127.09	127.31	127.58	127.73	127.92	128.10999999999999	128.22999999999999	128.36000000000001	128.60999999999999	128.73999999999998	129.01	129.1	129.18	129.39000000000001	129.53	129.66	129.82000000000087	130.02000000000001	130.15	130.39000000000001	130.49	130.58000000000001	130.68	130.82000000000087	130.91999999999999	131	131.1	131.30000000000001	131.49	131.69999999999999	131.94	132.15	132.26	132.51	132.70999999999998	132.94999999999999	133.07	133.31	133.39000000000001	133.58000000000001	133.76999999999998	133.85000000000107	134.03	134.20999999999998	134.32000000000087	134.53	134.73999999999998	134.79	134.88000000000127	135.03	135.18	135.22	135.35000000000107	135.44	135.57	135.63	135.69	135.87	136.02000000000001	136.15	136.36000000000001	136.46	136.55000000000001	136.66999999999999	136.79	136.85000000000107	136.91999999999999	137.16	137.32000000000087	137.52000000000001	137.72	137.94	138.08000000000001	138.35000000000107	138.5	138.63999999999999	138.78	138.97	139.07	139.19	139.25	139.46	139.53	139.63999999999999	139.73999999999998	139.87	139.94999999999999	140.06	140.31	140.43	140.47999999999999	140.58000000000001	140.80000000000001	140.87	140.96	141.1	141.22	141.35000000000107	141.51	141.56	141.62	141.72	141.76999999999998	141.91	141.94	142.04	142.13	142.19	142.32000000000087	142.34	142.38000000000127	142.51	142.63999999999999	142.72	142.79	142.86000000000001	142.91999999999999	143.03	143.08000000000001	143.32000000000087	143.37	143.44999999999999	143.56	143.72999999999999	143.76999999999998	143.85000000000107	143.96	144.1	144.16999999999999	144.28	144.4	144.53	144.57	144.69	144.83000000000001	144.99	145.06	145.19	145.26999999999998	145.43	145.55000000000001	145.66999999999999	145.81	145.9	145.97999999999999	146.09	146.22	146.29	146.36000000000001	146.68	146.69999999999999	146.72999999999999	147.02000000000001	147.06	147.10999999999999	147.26999999999998	147.41	147.51	147.57	147.69	147.83000000000001	147.89000000000001	147.97999999999999	148.12	148.32000000000087	148.39000000000001	148.47	148.62	148.83000000000001	149.07	149.36000000000001	149.6	149.69999999999999	150.31	150.6	151.02000000000001	151.23999999999998	151.44	151.69999999999999	151.94999999999999	152.19	152.43	152.52000000000001	152.62	152.75	152.88000000000127	153.02000000000001	153.25	153.44999999999999	153.72999999999999	154.02000000000001	154.29	154.58000000000001	154.86000000000001	155.26999999999998	155.53	155.79	156.06	156.34	156.70999999999998	156.94	157.20999999999998	157.46	157.79	158.22	158.41	158.79	158.97	159.26	159.66	159.87	160.07	160.41	160.78	161.13	161.30000000000001	161.60999999999999	161.78	162.04	162.29	162.54	162.66	162.83000000000001	163.03	163.18	163.47999999999999	163.63	163.87	163.94	164.04	164.3	164.44	164.68	164.93	165.2	165.34	165.5	165.67	165.78	165.97	166.16	166.23999999999998	166.32000000000087	166.42000000000004	166.57	166.66	166.84	166.87	166.95000000000007	167.04	167.16	167.22	167.26	167.31	167.33	167.38000000000127	167.43	167.56	167.57	167.67	167.81	167.83	167.86	167.95000000000007	168.07	168.22	168.38000000000127	168.44	168.54	168.64	168.75	168.83	168.99	169.05	169.26	169.4	169.52	169.56	169.60999999999999	169.68	169.92000000000004	170.03	170.20999999999998	170.52	170.63	170.72	170.83	170.98000000000027	171.07	171.17	171.45000000000007	171.56	171.76	171.96	172.07	172.13	172.23	172.45000000000007	172.56	172.70999999999998	172.91	172.98000000000027	173.08	173.19	173.31	173.38000000000127	173.51	173.57	173.65	173.75	173.9	173.96	174.06	174.17	174.36	174.44	174.53	174.62	174.79	174.88000000000127	175.10999999999999	175.26	175.4	175.54	175.72	175.87	176.19	176.31	176.58	176.66	176.8	177.01	177.14	177.26999999999998	177.4	177.56	177.65	177.79	177.87	178.02	178.07	178.19	178.26	178.37	178.44	178.55	178.6	178.63	178.76	178.91	179.09	179.35000000000107	179.73	180.01	180.44	180.68	181.16	181.38000000000127	181.70999999999998	182.01	182.33	182.72	182.83	183.20999999999998	183.4	183.7	184.09	184.25	184.46	184.70999999999998	184.96	185.20999999999998	185.58	185.81	186.07	186.23999999999998	186.54	187.1	187.45000000000007	187.76	188.07	188.47	188.67	188.88000000000127	189.09	189.4	189.64	189.95000000000007	190.08	190.26999999999998	190.54	190.70999999999998	190.84	191.08	191.35000000000107	191.49	191.65	191.8	191.9	192.10999999999999	192.3	192.38000000000127	192.57	192.84	192.93	193.10999999999999	193.29	193.4	193.6	193.9	194.16	194.3	194.51	194.73	194.85000000000107	195.06	195.26999999999998	195.4	195.63	195.72	195.9	196.08	196.17	196.35000000000107	196.41	196.60999999999999	196.73	196.88000000000127	197.22	197.37	197.65	197.79	197.98000000000027	198.20999999999998	198.33	198.6	198.73999999999998	199.05	199.23	199.4	199.63	199.79	200.06	200.23999999999998	200.45000000000007	200.57	200.78	200.97	201.09	201.29	201.51	201.63	201.79	201.99	202.09	202.23999999999998	202.4	202.49	202.63	202.73	202.87	202.99	203.02	203.08	203.16	203.22	203.33	203.42000000000004	203.63	203.8	203.91	204.03	204.18	204.35000000000107	204.52	204.58	204.70999999999998	204.78	204.95000000000007	205.02	205.19	205.38000000000127	205.47	205.55	205.68	205.78	205.89000000000001	206.18	206.28	206.43	206.64	206.7	206.79	207.07	207.22	207.3	207.56	207.67	207.8	207.87	208.07	208.13	208.20999999999998	208.43	208.46	208.47	208.5	208.65	208.83	208.87	208.93	209.03	209.09	209.22	209.26	209.34	209.39000000000001	209.44	209.59	209.72	209.67	209.70999999999998	209.86	210.03	210.1	210.3	210.5	210.65	210.81	211.06	211.2	211.37	211.49	211.52	211.63	211.76	211.89000000000001	212.03	212.18	212.23	212.34	212.41	212.49	212.55	212.63	212.82000000000087	212.88000000000127	212.95000000000007	213.02	213.08	213.26999999999998	213.38000000000127	213.54	213.7	213.75	213.82000000000087	213.93	214.12	214.19	214.34	214.42000000000004	214.49	214.59	214.8	214.88000000000127	215.04	215.19	215.34	215.47	215.59	215.63	215.88000000000127	215.89000000000001	215.91	215.97	216.08	216.23	216.29	216.5	216.62	216.70999999999998	216.88000000000127	217.13	217.33	217.47	217.65	217.83	217.92000000000004	218.1	218.23	218.35000000000107	218.41	218.55	218.70999999999998	218.92000000000004	218.96	219.07	219.2	219.39000000000001	219.49	219.63	219.82000000000087	219.89000000000001	220.07	220.36	220.47	220.67	221	221.96	222.67	223.09	223.69	224.32000000000087	224.85000000000107	225.29	225.78	226.01	226.29	226.7	226.89000000000001	227.23999999999998	227.41	227.69	228.04	228.17	228.3	228.54	228.66	228.79	228.93	229.10999999999999	229.17	229.31	229.53	229.72	229.8	229.95000000000007	230.25	230.5	230.70999999999998	230.94	231.1	231.32000000000087	231.51	231.60999999999999	231.8	232.01	232.15	232.4	232.48000000000027	232.65	232.81	232.92000000000004	233.10999999999999	233.3	233.43	233.55	233.67	233.89000000000001	233.96	234.12	234.19	234.34	234.42000000000004	234.51	234.54	234.73	234.79	235	235.2	235.29	235.5	235.60999999999999	235.72	235.78	235.91	235.96	236.13	236.18	236.39000000000001	236.45000000000007	236.53	236.64	236.69	236.79	236.85000000000107	236.95000000000007	237.04	237.08	237.2	237.23999999999998	237.32000000000087	237.41	237.44	237.64	237.7	237.84	237.94	238.09	238.16	238.4	238.67	239.06	239.19	239.45000000000007	239.73	239.99	240.22	240.44	240.56	240.76	240.97	241.04	241.22	241.37	241.48000000000027	241.58	241.7	241.81	241.87	241.92000000000004	241.97	242.25	242.26999999999998	242.37	242.49	242.68	242.73999999999998	242.87	243.1	243.17	243.29	243.42000000000004	243.54	243.6	243.76999999999998	243.76999999999998	243.84	243.95000000000007	244.01	244.13	244.16	244.22	244.34	244.49	244.54	244.58	244.65	244.73	244.79	244.92000000000004	244.93	245.03	245.29	245.34	245.42000000000004	245.53	245.73999999999998	245.82000000000087	245.91	246.01	246.17	246.2	246.25	246.36	246.42000000000004	246.55	246.57	246.59	246.67	246.73999999999998	246.84	246.92000000000004	246.99	247.03	247.13	247.17	247.26999999999998	247.33	247.39000000000001	247.68	247.91	248.03	248.23	248.51	248.82000000000087	249.34	250.38000000000127	251.59	252.54	253.37	253.8	254.33	254.75	255.19	255.49	255.76999999999998	255.96	256.27	256.52	256.64000000000038	256.86	257.08999999999969	257.20999999999964	257.39	257.60000000000002	257.69	257.97999999999894	258.06	258.27	258.55	258.68	258.97000000000003	259.12	259.45	259.61	259.78999999999894	260	260.16000000000008	260.45	260.58999999999969	260.77999999999969	260.87	260.97999999999894	261.22000000000003	261.39	261.52999999999969	261.76	261.88	261.98999999999899	262.24	262.32	262.48999999999899	262.69	262.78999999999894	262.95999999999964	263.12	263.22999999999894	263.35000000000002	263.66000000000008	263.89	264.02	264.3	264.42999999999893	264.67	264.89999999999969	265.14999999999998	265.26	265.38	265.58999999999969	265.72999999999894	265.86	266	266.18	266.3	266.44	266.66000000000008	266.74	266.85000000000002	266.97999999999894	267.18	267.27	267.44	267.5	267.66000000000008	267.72000000000003	267.91999999999899	268.11	268.42999999999893	268.57	268.81	268.98999999999899	269.22999999999894	269.45999999999964	269.7	269.83	269.95	270.08999999999969	270.3	270.52999999999969	270.77999999999969	271.05	271.14999999999998	271.27999999999969	271.41000000000003	271.64000000000038	271.76	271.94	272.13	272.24	272.38	272.56	272.61	272.77999999999969	272.97000000000003	273.02999999999969	273.14000000000038	273.44	273.61	273.89	274	274.22999999999894	274.45	274.52999999999969	274.77999999999969	275.3	275.48999999999899	275.75	276.06	276.37	276.72000000000003	276.87	277.14000000000038	277.33	277.45999999999964	277.72999999999894	277.95	278.2	278.3	278.42999999999893	278.57	278.74	278.82	279	279.17	279.26	279.41999999999899	279.5	279.92999999999893	280	280.20999999999964	280.39999999999969	280.52999999999969	280.74	280.91999999999899	280.98999999999899	281.18	281.32	281.36	281.52999999999969	281.74	281.81	281.97000000000003	282.14000000000038	282.26	282.45	282.62	282.70999999999964	282.81	282.95	283.10000000000002	283.18	283.33	283.44	283.55	283.66000000000008	283.98999999999899	284.14999999999998	284.27	284.42999999999893	284.64000000000038	284.72000000000003	284.91999999999899	285.11	285.2	285.39999999999969	285.45	285.69	285.72000000000003	285.78999999999894	285.91000000000003	286.04000000000002	286.18	286.45	286.64000000000038	286.72999999999894	287.01	287.06	287.24	287.45999999999964	287.56	287.66000000000008	287.77	287.97999999999894	288.06	288.25	288.63	288.75	288.91999999999899	289.13	289.28999999999894	289.47000000000003	289.68	289.85000000000002	290.04000000000002	290.16000000000008	290.3	290.48999999999899	290.57	290.72000000000003	290.81	290.95999999999964	291.01	291.18	291.36	291.41999999999899	291.57	291.64000000000038	291.76	291.83999999999969	292.01	292.12	292.27999999999969	292.54000000000002	292.81	293.07	293.14999999999998	293.25	293.45	293.58	293.76	293.97000000000003	294.08999999999969	294.35000000000002	294.42999999999893	294.55	294.7	294.91999999999899	295.02999999999969	295.17	295.35000000000002	295.44	295.63	295.82	295.89999999999969	296.06	296.2	296.31	296.41000000000003	296.54000000000002	296.7	296.77999999999969	296.97999999999894	297.32	297.42999999999893	297.66000000000008	297.87	298.02999999999969	298.20999999999964	298.41000000000003	298.54000000000002	298.77	298.87	299.05	299.26	299.33999999999969	299.47999999999894	299.68	299.77999999999969	299.89999999999969	300.27999999999969	300.41000000000003	300.69	300.95999999999964	301.13	301.45	301.70999999999964	301.77999999999969	301.92999999999893	302.14999999999998	302.26	302.44	302.60000000000002	302.70999999999964	303.04000000000002	303.14000000000038	303.37	303.63	303.8	304	304.24	304.45	304.58	304.74	304.95	305.06	305.20999999999964	305.41000000000003	305.48999999999899	305.64999999999998	305.85000000000002	305.94	306.02999999999969	306.14999999999998	306.33999999999969	306.47000000000003	306.63	306.81	306.87	307.02	307.08	307.36	307.47000000000003	307.68	307.92999999999893	308.02999999999969	308.22999999999894	308.42999999999893	308.52999999999969	308.77999999999969	308.91000000000003	309.08	309.24	309.35000000000002	309.47000000000003	309.61	309.83	309.89	310.05	310.33	310.35000000000002	310.41999999999899	310.55	310.72000000000003	310.8	310.95	311.12	311.20999999999964	311.32	311.45	311.63	311.78999999999894	311.97999999999894	312.13	312.33	312.42999999999893	312.60000000000002	312.77	312.89999999999969	313.01	313.16000000000008	313.33999999999969	313.45999999999964	313.58	313.77999999999969	313.86	314.05	314.22999999999894	314.31	314.39	314.52	314.72000000000003	314.91999999999899	315.02	315.18	315.39	315.51	315.64999999999998	315.83	315.98999999999899	316.3	316.44	316.64999999999998	316.83	316.98999999999899	317.24	317.38	317.56	317.74	317.87	318.01	318.2	318.32	318.47999999999894	318.64999999999998	318.75	318.91000000000003	319.06	319.18	319.27	319.39	319.55	319.64000000000038	319.82	319.89999999999969	320.07	320.12	320.19	320.45999999999964	320.77	321.04000000000002	321.5	322.05	322.28999999999894	322.64000000000038	322.82	323.10000000000002	323.45999999999964	323.60000000000002	323.83	324.06	324.17	324.37	324.57	324.66000000000008	324.91999999999899	325.01	325.12	325.24	325.36	325.44	325.52	325.62	325.77999999999969	325.85000000000002	325.94	326.04000000000002	326.18	326.27	326.37	326.52	326.66000000000008	326.78999999999894	326.86	327.02999999999969	327.13	327.22999999999894	327.27	327.39999999999969	327.45	327.60000000000002	327.68	327.7	327.82	327.94	328.03	328.06	328.12	328.21999999999969	328.27	328.42999999999893	328.48999999999899	328.69	328.77	328.86	328.97999999999894	329.11	329.19	329.39	329.56	329.67	329.83	329.92999999999893	330.09	330.21999999999969	330.31	330.41999999999899	330.47999999999894	330.62	330.67	330.76	330.86	330.95	331.03	331.1	331.17	331.2	331.36	331.42999999999893	331.46999999999969	331.46	331.46	331.46999999999969	331.64000000000038	331.8	331.91999999999899	332	332.18	332.4	332.42999999999893	332.53	332.63	332.69	332.82	332.88	333.02	333.17	333.28	333.38	333.53	333.71999999999969	333.78999999999894	334.01	334.11	334.25	334.44	334.7	334.98999999999899	335.26	335.42999999999893	335.65000000000032	335.86	335.96	336.17	336.38	336.52	336.86	336.97999999999894	337.17	337.32	337.36	337.65000000000032	337.8	337.92999999999893	338.07	338.34000000000032	338.37	338.47999999999894	338.58	338.74	338.81	338.89	338.98999999999899	339.12	339.18	339.24	339.31	339.41999999999899	339.54	339.57	339.67	339.78999999999894	800 mm	440	440.5	441	441.5	442	442.5	443	443.5	444	444.5	445	445.5	446	446.5	447	447.5	448	448.5	449	449.5	450	450.5	451	451.5	452	452.5	453	453.5	454	454.5	455	455.5	456	456.5	457	457.5	458	458.5	459	459.5	460	460.5	461	461.5	462	462.5	463	463.5	464	464.5	465	465.5	466	466.5	467	467.5	468	468.5	469	469.5	470	470.5	471	471.5	472	472.5	473	473.5	474	474.5	475	475.5	476	476.5	477	477.5	478	478.5	479	479.5	480	480.5	481	481.5	482	482.5	483	483.5	484	484.5	485	485.5	486	486.5	487	487.5	488	488.5	489	489.5	490	490.5	491	491.5	492	492.5	493	493.5	494	494.5	495	495.5	496	496.5	497	497.5	498	498.5	499	499.5	500	500.5	501	501.5	502	502.5	503	503.5	504	504.5	505	505.5	506	506.5	507	507.5	508	508.5	509	509.5	510	510.5	511	511.5	512	512.5	513	513.5	514	514.5	515	515.5	516	516.5	517	517.5	518	518.5	519	519.5	520	520.5	521	521.5	522	522.5	523	523.5	524	524.5	525	525.5	526	526.5	527	527.5	528	528.5	529	529.5	530	530.5	531	531.5	532	532.5	533	533.5	534	534.5	535	535.5	536	536.5	537	537.5	538	538.5	539	539.5	540	540.5	541	541.5	542	542.5	543	543.5	544	544.5	545	545.5	546	546.5	547	547.5	548	548.5	549	549.5	550	550.5	551	551.5	552	552.5	553	553.5	554	554.5	555	555.5	556	556.5	557	557.5	558	558.5	559	559.5	560	560.5	561	561.5	562	562.5	563	563.5	564	564.5	565	565.5	566	566.5	567	567.5	568	568.5	569	569.5	570	570.5	571	571.5	572	572.5	573	573.5	574	574.5	575	575.5	576	576.5	577	577.5	578	578.5	579	579.5	580	580.5	581	581.5	582	582.5	583	583.5	584	584.5	585	585.5	586	586.5	587	587.5	588	588.5	589	589.5	590	590.5	591	591.5	592	592.5	593	593.5	594	594.5	595	595.5	596	596.5	597	597.5	598	598.5	599	599.5	600	600.5	601	601.5	602	602.5	603	603.5	604	604.5	605	605.5	606	606.5	607	607.5	608	608.5	609	609.5	610	610.5	611	611.5	612	612.5	613	613.5	614	614.5	615	615.5	616	616.5	617	617.5	618	618.5	619	619.5	620	620.5	621	621.5	622	622.5	623	623.5	624	624.5	625	625.5	626	626.5	627	627.5	628	628.5	629	629.5	630	630.5	631	631.5	632	632.5	633	633.5	634	634.5	635	635.5	636	636.5	637	637.5	638	638.5	639	639.5	640	640.5	641	641.5	642	642.5	643	643.5	644	644.5	645	645.5	646	646.5	647	647.5	648	648.5	649	649.5	650	650.5	651	651.5	652	652.5	653	653.5	654	654.5	655	655.5	656	656.5	657	657.5	658	658.5	659	659.5	660	660.5	661	661.5	662	662.5	663	663.5	664	664.5	665	665.5	666	666.5	667	667.5	668	668.5	669	669.5	670	670.5	671	671.5	672	672.5	673	673.5	674	674.5	675	675.5	676	676.5	677	677.5	678	678.5	679	679.5	680	680.5	681	681.5	682	682.5	683	683.5	684	684.5	685	685.5	686	686.5	687	687.5	688	688.5	689	689.5	690	690.5	691	691.5	692	692.5	693	693.5	694	694.5	695	695.5	696	696.5	697	697.5	698	698.5	699	699.5	700	700.5	701	701.5	702	702.5	703	703.5	704	704.5	705	705.5	706	706.5	707	707.5	708	708.5	709	709.5	710	710.5	711	711.5	712	712.5	713	713.5	714	714.5	715	715.5	716	716.5	717	717.5	718	718.5	719	719.5	720	720.5	721	721.5	722	722.5	723	723.5	724	724.5	725	725.5	726	726.5	727	727.5	728	728.5	729	729.5	730	730.5	731	731.5	732	732.5	733	733.5	734	734.5	735	735.5	736	736.5	737	737.5	738	738.5	739	739.5	740	740.5	741	741.5	742	742.5	743	743.5	744	744.5	745	745.5	746	746.5	747	747.5	748	748.5	749	749.5	750	750.5	751	751.5	752	752.5	753	753.5	754	754.5	755	755.5	756	756.5	757	757.5	758	758.5	759	759.5	760	760.5	761	761.5	762	762.5	763	763.5	764	764.5	765	765.5	766	766.5	767	767.5	768	768.5	769	769.5	770	770.5	771	771.5	772	772.5	773	773.5	774	774.5	775	775.5	776	776.5	777	777.5	778	778.5	779	779.5	780	780.5	781	781.5	782	782.5	783	783.5	784	784.5	785	785.5	786	786.5	787	787.5	788	788.5	789	789.5	790	790.5	791	791.5	792	792.5	793	793.5	794	794.5	795	795.5	796	796.5	797	797.5	798	798.5	799	799.5	800	800.5	801	801.5	802	802.5	803	803.5	804	804.5	805	805.5	806	806.5	807	807.5	808	808.5	809	809.5	810	810.5	811	811.5	812	812.5	813	813.5	814	814.5	815	815.5	816	816.5	817	817.5	818	818.5	819	819.5	820	820.5	821	821.5	822	822.5	823	823.5	824	824.5	825	825.5	826	826.5	827	827.5	828	828.5	829	829.5	830	830.5	831	831.5	832	832.5	833	833.5	834	834.5	835	835.5	836	836.5	837	837.5	838	838.5	839	839.5	840	840.5	841	841.5	842	842.5	843	843.5	844	844.5	845	845.5	846	846.5	847	847.5	848	848.5	849	849.5	850	850.5	851	851.5	852	852.5	853	853.5	854	854.5	855	855.5	856	856.5	857	857.5	858	858.5	859	859.5	860	860.5	861	861.5	862	862.5	863	863.5	864	864.5	865	865.5	866	866.5	867	867.5	868	868.5	869	869.5	870	870.5	871	871.5	872	872.5	873	873.5	874	874.5	875	875.5	876	876.5	877	877.5	878	878.5	879	879.5	880	880.5	881	881.5	882	882.5	883	883.5	884	884.5	885	885.5	886	886.5	887	887.5	888	888.5	889	889.5	890	890.5	891	891.5	892	892.5	893	893.5	894	894.5	895	895.5	896	896.5	897	897.5	898	898.5	899	899.5	900	900.5	901	901.5	902	902.5	903	903.5	904	904.5	905	905.5	906	906.5	907	907.5	908	908.5	909	909.5	910	910.5	911	911.5	912	912.5	913	913.5	914	914.5	915	915.5	916	916.5	917	917.5	918	918.5	919	919.5	920	920.5	921	921.5	922	922.5	923	923.5	924	924.5	925	925.5	926	926.5	927	927.5	928	928.5	929	929.5	930	930.5	931	931.5	932	932.5	933	933.5	934	934.5	935	935.5	936	936.5	937	937.5	938	938.5	939	939.5	940	940.5	941	941.5	942	942.5	943	943.5	944	944.5	945	945.5	946	946.5	947	947.5	948	948.5	949	949.5	950	950.5	951	951.5	952	952.5	953	953.5	954	954.5	955	955.5	956	956.5	957	957.5	958	958.5	959	959.5	960	960.5	961	961.5	962	962.5	963	963.5	964	964.5	965	965.5	966	966.5	967	967.5	968	968.5	969	969.5	970	970.5	971	971.5	972	972.5	973	973.5	974	974.5	975	975.5	976	976.5	977	977.5	978	978.5	979	979.5	980	980.5	981	981.5	982	982.5	983	983.5	984	984.5	985	985.5	986	986.5	987	987.5	988	988.5	989	989.5	990	990.5	991	991.5	992	992.5	993	993.5	994	994.5	995	995.5	996	996.5	997	997.5	998	998.5	999	999.5	1000	1000.5	1001	1001.5	1002	1002.5	1003	1003.5	1004	1004.5	1005	1005.5	1006	1006.5	1007	1007.5	1008	1008.5	1009	1009.5	1010	1010.5	1011	1011.5	1012	1012.5	1013	1013.5	1014	1014.5	1015	1015.5	1016	1016.5	1017	1017.5	1018	1018.5	1019	1019.5	1020	1020.5	1021	1021.5	1022	1022.5	1023	1023.5	1024	1024.5	1025	1025.5	1026	1026.5	1027	1027.5	1028	1028.5	1029	1029.5	1030	1030.5	1031	1031.5	1032	1032.5	1033	1033.5	1034	1034.5	1035	1035.5	1036	1036.5	1037	1037.5	1038	1038.5	1039	1039.5	1040	1040.5	1041	1041.5	1042	1042.5	1043	1043.5	1044	1044.5	1045	1045.5	1046	1046.5	1047	1047.5	1048	1048.5	1049	1049.5	1050	1050.5	1051	1051.5	1052	1052.5	1053	1053.5	1054	1054.5	1055	1055.5	1056	1056.5	1057	1057.5	1058	1058.5	1059	1059.5	1060	1060.5	1061	1061.5	1062	1062.5	1063	1063.5	1064	1064.5	1065	1065.5	1066	1066.5	1067	1067.5	1068	1068.5	1069	1069.5	1070	1070.5	1071	1071.5	1072	1072.5	1073	1073.5	1074	1074.5	1075	1075.5	1076	1076.5	1077	1077.5	1078	1078.5	1079	1079.5	1080	1080.5	1081	1081.5	1082	1082.5	1083	1083.5	1084	1084.5	1085	1085.5	1086	1086.5	1087	1087.5	1088	1088.5	1089	1089.5	1090	1090.5	1091	1091.5	1092	1092.5	1093	1093.5	1094	1094.5	1095	1095.5	1096	1096.5	1097	1097.5	1098	1098.5	1099	1099.5	1100	1100.5	1101	1101.5	1102	1102.5	1103	1103.5	1104	1104.5	1105	1105.5	1106	1106.5	1107	1107.5	1108	1108.5	1109	1109.5	1110	1110.5	1111	1111.5	1112	1112.5	1113	1113.5	1114	1114.5	1115	1115.5	1116	1116.5	1117	1117.5	1118	1118.5	1119	1119.5	1120	1120.5	1121	1121.5	1122	1122.5	1123	1123.5	1124	1124.5	1125	1125.5	1126	1126.5	1127	1127.5	1128	1128.5	1129	1129.5	1130	1130.5	1131	1131.5	1132	1132.5	1133	1133.5	1134	1134.5	1135	1135.5	1136	1136.5	1137	1137.5	1138	1138.5	1139	1139.5	1140	1140.5	1141	1141.5	1142	1142.5	1143	1143.5	1144	1144.5	1145	1145.5	1146	1146.5	1147	1147.5	1148	1148.5	1149	1149.5	1150	1150.5	1151	1151.5	1152	1152.5	1153	1153.5	1154	1154.5	1155	1155.5	1156	1156.5	1157	1157.5	1158	1158.5	1159	1159.5	1160	1160.5	1161	1161.5	1162	1162.5	1163	1163.5	1164	1164.5	1165	1165.5	1166	1166.5	1167	1167.5	1168	1168.5	1169	1169.5	1170	1170.5	1171	1171.5	1172	1172.5	1173	1173.5	1174	1174.5	1175	1175.5	1176	1176.5	1177	1177.5	1178	1178.5	1179	1179.5	1180	1180.5	1181	1181.5	1182	1182.5	1183	1183.5	1184	1184.5	1185	1185.5	1186	1186.5	1187	1187.5	1188	1188.5	1189	1189.5	1190	1190.5	1191	1191.5	1192	1192.5	1193	1193.5	1194	1194.5	1195	1195.5	1196	1196.5	1197	1197.5	1198	1198.5	1199	1199.5	1200	1200.5	1201	1201.5	1202	1202.5	1203	1203.5	1204	1204.5	1205	1205.5	1206	1206.5	1207	1207.5	1208	1208.5	1209	1209.5	1210	1210.5	1211	1211.5	1212	1212.5	1213	1213.5	1214	1214.5	1215	1215.5	1216	1216.5	1217	1217.5	1218	1218.5	1219	1219.5	1220	1220.5	1221	1221.5	1222	1222.5	1223	1223.5	1224	1224.5	1225	1225.5	1226	1226.5	1227	1227.5	1228	1228.5	1229	1229.5	1230	1230.5	1231	1231.5	1232	1232.5	1233	1233.5	1234	1234.5	1235	1235.5	1236	1236.5	1237	1237.5	1238	1238.5	1239	1239.5	1240	1240.5	1241	1241.5	1242	1242.5	1243	1243.5	1244	1244.5	1245	1245.5	1246	1246.5	1247	1247.5	1248	1248.5	1249	1249.5	1250	1250.5	1251	1251.5	1252	1252.5	1253	1253.5	1254	1254.5	1255	1255.5	1256	1256.5	1257	1257.5	1258	1258.5	1259	1259.5	1260	1260.5	1261	1261.5	1262	1262.5	1263	1263.5	1264	1264.5	1265	1265.5	1266	1266.5	1267	1267.5	1268	1268.5	1269	1269.5	1270	1270.5	1271	1271.5	1272	1272.5	1273	1273.5	1274	1274.5	1275	1275.5	1276	1276.5	1277	1277.5	1278	1278.5	1279	1279.5	1280	1280.5	1281	1281.5	1282	1282.5	1283	1283.5	1284	1284.5	1285	1285.5	1286	1286.5	1287	1287.5	1288	1288.5	1289	1289.5	1290	1290.5	1291	1291.5	1292	1292.5	1293	1293.5	1294	1294.5	1295	1295.5	1296	1296.5	1297	1297.5	1298	1298.5	1299	1299.5	1300	1300.5	1301	1301.5	1302	1302.5	1303	1303.5	1304	1304.5	1305	1305.5	1306	1306.5	1307	1307.5	1308	1308.5	1309	1309.5	1310	1310.5	1311	1311.5	1312	1312.5	1313	1313.5	1314	1314.5	1315	1315.5	1316	1316.5	1317	1317.5	1318	1318.5	1319	1319.5	1320	1320.5	1321	1321.5	1322	1322.5	1323	1323.5	1324	1324.5	1325	1325.5	1326	1326.5	1327	1327.5	1328	1328.5	1329	1329.5	1330	1330.5	1331	1331.5	1332	1332.5	1333	1333.5	1334	1334.5	1335	1335.5	1336	1336.5	1337	1337.5	1338	1338.5	1339	1339.5	1340	1340.5	1341	1341.5	1342	1342.5	1343	1343.5	1344	1344.5	1345	1345.5	1346	1346.5	1347	1347.5	1348	1348.5	1349	1349.5	1350	1350.5	1351	1351.5	1352	1352.5	1353	1353.5	1354	1354.5	1355	1355.5	1356	1356.5	1357	1357.5	1358	1358.5	1359	1359.5	1360	1360.5	1361	1361.5	1362	1362.5	1363	1363.5	1364	1364.5	1365	1365.5	1366	1366.5	1367	1367.5	1368	1368.5	1369	1369.5	1370	1370.5	1371	1371.5	1372	1372.5	1373	1373.5	1374	1374.5	1375	1375.5	1376	1376.5	1377	1377.5	1378	1378.5	1379	1379.5	1380	1380.5	1381	1381.5	1382	1382.5	1383	1383.5	1384	1384.5	1385	1385.5	1386	1386.5	1387	1387.5	1388	1388.5	1389	1389.5	1390	1390.5	1391	1391.5	1392	1392.5	1393	1393.5	1394	1394.5	1395	1395.5	1396	1396.5	1397	1397.5	1398	1398.5	1399	1399.5	1400	0	0.97000000000000064	1.46	1.6800000000000141	1.84	1.8800000000000001	1.9600000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.9700000000000166	1.980000000000018	1.980000000000018	1.980000000000018	1.980000000000018	1.9900000000000186	1.9900000000000186	1.9900000000000186	1.9900000000000186	1.9900000000000186	1.9900000000000186	1.9900000000000186	1.9900000000000186	1.980000000000018	1.980000000000018	1.980000000000018	1.980000000000018	1.9700000000000166	1.9700000000000166	1.980000000000018	1.9900000000000186	1.9900000000000186	1.980000000000018	1.9700000000000166	1.9600000000000166	1.9600000000000166	1.9600000000000166	1.9600000000000166	1.9600000000000166	1.9600000000000166	1.9700000000000166	1.9700000000000166	2.98	3.6	3.72	3.8899999999999997	3.9099999999999997	4	4.04	4.04	4.04	4.04	4.04	4.04	4.04	4.05	4.05	4.05	4.05	4.05	4.05	4.05	4.04	4.04	4.0199999999999996	3.98	3.96	3.96	3.9699999999999998	3.98	4.0199999999999996	4.04	4.04	4.04	4.04	4.04	4.04	4.04	4.1599999999999975	5.09	5.48	5.76	5.9	6.06	6.17	6.2700000000000014	6.28	6.35	6.42	6.4700000000000024	6.5	6.6499999999999995	6.67	6.67	6.67	6.6899999999999995	6.72	6.8199999999999985	7.05	7.1599999999999975	7.38	7.48	7.6599999999999975	7.9	8.0500000000000007	8.2100000000000009	8.3700000000000028	8.5	8.81	8.8800000000000008	8.98	9.11	9.31	9.39	9.5500000000000007	9.61	9.7800000000000011	9.93	10.02	10.17	10.220000000000001	10.27	10.33	10.59	10.57	10.66	10.739999999999998	10.77	10.96	11.01	11.07	11.19	11.29	11.33	11.370000000000006	11.44	11.53	11.53	11.57	11.69	11.739999999999998	11.739999999999998	11.81	11.860000000000024	11.91	11.96	11.96	12.06	12.06	12.08	12.16	12.15	12.25	12.28	12.38	12.42	12.49	12.59	12.709999999999999	12.79	12.89	12.97	13.16	13.17	13.219999999999999	13.32	13.4	13.58	13.7	13.69	13.78	13.89	13.92	14.09	14.12	14.2	14.3	14.39	14.42	14.46	14.58	14.639999999999999	14.81	14.84	14.93	15.04	15.16	15.229999999999999	15.3	15.47	15.55	15.61	15.729999999999999	15.78	15.84	15.94	16.079999999999988	16.16	16.22	16.32	16.41	16.479999999999986	16.55	16.670000000000005	16.739999999999988	16.86	16.91	17	17.110000000000031	17.23	17.23	17.329999999999988	17.43	17.54	17.579999999999988	17.670000000000005	17.779999999999987	17.829999999999988	17.899999999999999	17.97	18.130000000000031	18.22	18.27	18.43	18.53	18.57	18.610000000000031	18.649999999999999	18.779999999999987	18.809999999999999	18.95	19.03	19.149999999999999	19.25	19.38	19.420000000000002	19.5	19.62	19.77	19.82	19.939999999999987	19.979999999999986	20.100000000000001	20.16	20.25	20.37	20.41	20.51	20.59	20.67	20.759999999999987	20.89	20.919999999999987	21.01	21.09	21.150000000000031	21.3	21.35	21.47	21.7	21.74	21.84	21.939999999999987	21.99	22.12	22.18	22.259999999999987	22.35	22.53	22.57	22.68	22.779999999999987	22.85	23.03	23.05	23.130000000000031	23.2	23.25	23.41	23.43	23.52	23.6	23.64	23.9	23.88	23.93	24.04	24.09	24.2	24.279999999999987	24.39	24.459999999999987	24.610000000000031	24.68	24.82	24.9	25.05	25.08	25.16	25.21	25.27	25.47	25.89	26.41	27.67	28.279999999999987	28.8	29.53	29.97	30.41	30.959999999999987	31.27	31.53	31.85	32.130000000000003	32.51	32.660000000000011	32.94	33.260000000000012	33.550000000000004	33.949999999999996	34.130000000000003	34.32	34.56	34.720000000000013	34.86	35.090000000000003	35.220000000000013	35.46	35.590000000000003	35.74	35.89	35.97	36.06	36.17	36.309999999999995	36.379999999999995	36.520000000000003	36.67	36.770000000000003	36.870000000000005	37.050000000000004	37.160000000000011	37.290000000000013	37.36	37.5	37.590000000000003	37.760000000000012	37.9	37.980000000000004	38.11	38.18	38.32	38.339999999999996	38.42	38.53	38.760000000000012	38.809999999999995	38.910000000000004	39.03	39.200000000000003	39.309999999999995	39.46	39.64	39.730000000000011	39.839999999999996	40.06	40.220000000000013	40.290000000000013	40.39	40.5	40.65	40.71	40.790000000000013	40.9	40.99	41.01	41.13	41.13	41.21	41.24	41.379999999999995	41.42	41.5	41.55	41.660000000000011	41.82	41.86	41.92	42	42.2	42.36	42.4	42.49	42.6	42.720000000000013	42.790000000000013	42.879999999999995	42.99	43.15	43.21	43.260000000000012	43.41	43.56	43.6	43.7	43.86	44.15	44.24	44.32	44.65	44.83	45.01	45.25	45.54	45.68	45.849999999999994	46	46.15	46.449999999999996	46.59	46.89	46.98	47.21	47.39	47.71	48.04	48.36	48.65	48.949999999999996	49.120000000000012	49.47	49.720000000000013	49.91	50.190000000000012	50.349999999999994	50.620000000000012	50.83	51.120000000000012	51.24	51.36	51.61	51.730000000000011	51.949999999999996	52.190000000000012	52.44	52.57	52.67	52.92	53.07	53.27	53.47	53.58	53.8	53.92	54.160000000000011	54.32	54.47	54.57	54.74	54.96	55.11	55.379999999999995	55.54	55.77	55.91	56.04	56.37	56.449999999999996	56.74	56.89	57.03	57.230000000000011	57.309999999999995	57.5	57.7	57.790000000000013	57.949999999999996	58.120000000000012	58.32	58.51	58.620000000000012	58.790000000000013	58.879999999999995	59.02	59.220000000000013	59.32	59.51	59.730000000000011	59.849999999999994	60.04	60.09	60.27	60.339999999999996	60.51	60.690000000000012	60.78	60.89	61.04	61.230000000000011	61.449999999999996	61.58	61.720000000000013	61.949999999999996	62.08	62.37	62.5	62.730000000000011	62.790000000000013	62.97	63.220000000000013	63.37	63.5	63.71	63.790000000000013	64.099999999999994	64.19	64.31	64.45	64.63	64.69	64.849999999999994	65	65.099999999999994	65.2	65.33	65.540000000000006	65.739999999999995	65.89	66.14	66.27	66.459999999999994	66.63	66.77	66.900000000000006	67.19	67.23	67.38	67.59	67.72	67.89	67.989999999999995	68.16	68.27	68.440000000000026	68.63	68.739999999999995	68.86999999999999	69.02	69.11999999999999	69.28	69.400000000000006	69.52	69.61	69.739999999999995	69.95	70.14	70.25	70.36	70.489999999999995	70.679999999999978	70.81	70.98	71.19	71.33	71.59	71.649999999999991	71.73	71.88	72.08	72.22	72.349999999999994	72.55	72.61999999999999	72.81	73.02	73.069999999999993	73.179999999999978	73.38	73.5	73.59	73.739999999999995	73.940000000000026	74.05	74.19	74.31	74.5	74.52	74.599999999999994	74.739999999999995	74.940000000000026	75	75.11999999999999	75.290000000000006	75.39	75.52	75.669999999999987	75.819999999999993	76.02	76.11999999999999	76.290000000000006	76.5	76.61999999999999	76.819999999999993	77.02	77.16	77.400000000000006	77.489999999999995	77.61999999999999	77.709999999999994	77.849999999999994	77.98	78.11	78.260000000000005	78.34	78.53	78.66	78.73	78.760000000000005	79.010000000000005	79.11999999999999	79.22	79.36	79.430000000000007	79.61999999999999	79.709999999999994	79.86999999999999	79.92	80.099999999999994	80.290000000000006	80.36999999999999	80.59	80.669999999999987	80.819999999999993	81.040000000000006	81.16	81.25	81.55	81.7	81.81	82.04	82.169999999999987	82.33	82.51	82.64	82.78	82.95	83.01	83.19	83.45	83.55	83.63	83.78	83.97	84.06	84.25	84.43	84.56	84.7	84.88	84.98	85.149999999999991	85.33	85.42	85.59	85.77	85.9	86.07	86.29	86.38	86.55	86.61	86.77	86.88	87	87.13	87.3	87.36	87.52	87.72	87.88	88.01	88.14	88.33	88.42	88.6	88.77	88.92	89.11	89.32	89.410000000000025	89.490000000000023	89.72	89.83	89.960000000000022	90.11999999999999	90.31	90.42	90.56	90.8	90.86999999999999	91.02	91.23	91.32	91.440000000000026	91.57	91.740000000000023	91.88	92.03	92.25	92.33	92.4	92.6	92.69	92.77	92.940000000000026	93.16	93.27	93.440000000000026	93.61999999999999	93.72	93.89	94.03	94.13	94.31	94.460000000000022	94.55	94.7	94.93	94.98	95.2	95.26	95.440000000000026	95.61999999999999	95.7	95.89	96.05	96.149999999999991	96.35	96.52	96.669999999999987	96.740000000000023	96.93	97.11999999999999	97.210000000000022	97.36999999999999	97.47	97.64	97.75	97.93	98.13	98.2	98.34	98.48	98.63	98.77	98.92	99.11	99.240000000000023	99.38	99.59	99.679999999999978	99.8	99.98	100.06	100.23	100.45	100.53	100.67999999999998	100.76	101.06	101.1	101.22	101.35	101.54	101.66	101.79	101.96000000000002	102.06	102.25	102.33	102.59	102.66	102.81	103.02	103.09	103.16999999999999	103.43	103.53	103.64	103.78	104	104.11	104.27	104.39	104.49000000000002	104.6	104.76	104.94000000000032	105.06	105.19	105.4	105.55	105.66	105.8	105.97	106.04	106.19	106.38	106.48	106.59	106.72	106.9	107.02	107.11	107.26	107.33	107.5	107.61	107.78	107.92	108.02	108.19	108.36	108.6	108.64	108.75	108.89	109.11	109.26	109.43	109.61999999999999	109.77	110	110.14	110.26	110.47	110.57	110.74000000000002	110.89	110.99000000000002	111.17999999999998	111.25	111.42	111.52	111.67999999999998	111.82	111.89	112	112.14	112.29	112.38	112.54	112.67999999999998	112.75	112.83	112.96000000000002	113.13	113.19	113.34	113.49000000000002	113.58	113.66999999999999	113.81	114.01	114.14999999999999	114.31	114.49000000000002	114.64	114.76	114.88	115.04	115.11	115.28	115.39	115.56	115.63	115.79	115.94000000000032	116.04	116.16999999999999	116.24000000000002	116.39	116.57	116.64	116.75	116.88	117.06	117.13	117.33	117.52	117.69	117.81	117.93	118.13	118.19	118.3	118.57	118.69	118.93	119.14999999999999	119.42	119.69	119.8	120.04	120.27	120.55	120.74000000000002	120.89	121.04	121.17999999999998	121.41000000000012	121.6	121.69	122	122.08	122.17999999999998	122.3	122.47	122.54	122.75	122.93	123.03	123.21000000000002	123.27	123.56	123.58	123.74000000000002	123.83	124	124.06	124.25	124.43	124.58	124.76	125	125.07	125.26	125.44000000000032	125.53	125.71000000000002	125.89	125.98	126.16	126.31	126.47	126.57	126.69	126.84	126.98	127.09	127.22	127.4	127.47	127.66	127.82	127.97	128.04	128.16999999999999	128.35000000000107	128.43	128.53	128.66	128.76999999999998	128.85000000000107	129.04	129.19999999999999	129.47	129.56	129.75	129.91	130.02000000000001	130.15	130.30000000000001	130.47999999999999	130.62	130.76999999999998	131.01	131.06	131.16999999999999	131.29	131.44	131.56	131.69999999999999	131.85000000000107	131.94	132.07	132.15	132.33000000000001	132.51	132.56	132.69	132.80000000000001	132.85000000000107	133.05000000000001	133.1	133.28	133.44	133.53	133.72999999999999	133.94	134.1	134.35000000000107	134.60999999999999	134.72999999999999	134.93	135.15	135.39000000000001	135.58000000000001	135.69	135.85000000000107	136.05000000000001	136.19999999999999	136.35000000000107	136.56	136.69	136.87	137.02000000000001	137.16	137.35000000000107	137.41999999999999	137.55000000000001	137.75	137.86000000000001	137.97999999999999	138.15	138.39000000000001	138.43	138.58000000000001	138.68	138.83000000000001	138.96	139.12	139.31	139.46	139.72999999999999	139.84	140.01	140.12	140.30000000000001	140.43	140.56	140.76	140.85000000000107	141.05000000000001	141.26999999999998	141.34	141.46	141.58000000000001	141.69999999999999	141.81	142	142.04	142.22999999999999	142.31	142.49	142.54	142.76	142.9	142.94	143.07	143.26999999999998	143.34	143.55000000000001	143.63999999999999	143.79	144	144.23999999999998	144.32000000000087	144.49	144.68	144.75	144.86000000000001	145.12	145.22999999999999	145.35000000000107	145.52000000000001	145.75	145.79	145.89000000000001	146.1	146.19	146.30000000000001	146.43	146.57	146.65	146.84	146.9	147.08000000000001	147.28	147.32000000000087	147.4	147.57	147.72999999999999	147.78	147.94999999999999	148.16999999999999	148.37	148.69	148.84	149.04	149.28	149.41999999999999	149.69999999999999	149.86000000000001	150.10999999999999	150.18	150.39000000000001	150.62	150.70999999999998	150.91999999999999	151.15	151.29	151.51	151.60999999999999	151.76999999999998	151.97999999999999	152.10999999999999	152.23999999999998	152.29	152.53	152.66	152.91	153.02000000000001	153.13999999999999	153.26999999999998	153.46	153.55000000000001	153.69999999999999	153.91	154.06	154.39000000000001	154.47	154.69	154.88000000000127	154.99	155.19	155.37	155.47999999999999	155.76	155.87	156.05000000000001	156.22	156.32000000000087	156.44	156.57	156.78	156.9	157.06	157.23999999999998	157.37	157.52000000000001	157.66	157.76	157.94	158.1	158.19999999999999	158.33000000000001	158.47	158.58000000000001	158.82000000000087	158.86000000000001	158.97	159.18	159.30000000000001	159.53	159.73999999999998	159.84	160.09	160.23999999999998	160.41	160.57	160.72	160.85000000000107	161.01	161.19	161.31	161.57	161.66	161.84	162	162.10999999999999	162.23999999999998	162.36000000000001	162.53	162.62	162.81	162.97	163.13999999999999	163.26	163.39000000000001	163.51	163.63	163.73999999999998	164	164.16	164.47	164.60999999999999	164.86	165.1	165.23999999999998	165.57	165.69	165.94	166.07	166.23999999999998	166.45000000000007	166.59	166.73999999999998	166.96	167.2	167.33	167.43	167.57	167.76	167.88000000000127	168.03	168.18	168.29	168.48000000000027	168.60999999999999	168.76	168.89000000000001	169.03	169.17	169.26	169.44	169.6	169.7	169.91	170.18	170.29	170.42000000000004	170.63	170.73999999999998	170.91	171.12	171.20999999999998	171.43	171.57	171.7	171.87	172.07	172.18	172.34	172.52	172.60999999999999	172.67	172.84	173.07	173.15	173.26	173.37	173.55	173.62	173.78	173.97	174.06	174.22	174.38000000000127	174.6	174.68	174.86	175.05	175.15	175.35000000000107	175.56	175.67	175.81	176.06	176.20999999999998	176.35000000000107	176.60999999999999	176.78	176.94	177.16	177.39000000000001	177.54	177.7	177.89000000000001	178.01	178.23	178.43	178.54	178.81	178.89000000000001	179	179.13	179.34	179.45000000000007	179.60999999999999	179.76	179.86	180.02	180.17	180.34	180.47	180.64	180.83	180.96	181.14	181.33	181.47	181.73	181.83	182.01	182.15	182.28	182.41	182.53	182.73999999999998	182.81	182.99	183.15	183.28	183.35000000000107	183.49	183.67	183.73	183.85000000000107	183.99	184.14	184.25	184.4	184.59	184.65	184.78	184.92000000000004	185.07	185.29	185.46	185.78	185.91	186.18	186.34	186.51	186.69	186.84	187.10999999999999	187.26	187.53	187.6	187.76	187.95000000000007	188.04	188.17	188.3	188.5	188.56	188.73999999999998	188.9	189.05	189.15	189.3	189.49	189.54	189.64	189.84	189.93	190.06	190.18	190.37	190.59	190.65	190.75	190.89000000000001	191.07	191.23	191.4	191.6	191.73	191.85000000000107	192.10999999999999	192.15	192.3	192.54	192.65	192.85000000000107	193.06	193.17	193.43	193.56	193.70999999999998	193.85000000000107	193.96	194.19	194.37	194.44	194.6	194.79	194.95000000000007	195.02	195.17	195.32000000000087	195.45000000000007	195.55	195.7	195.93	196.12	196.33	196.41	196.5	196.65	196.89000000000001	197.05	197.18	197.4	197.46	197.73999999999998	197.84	197.93	198.13	198.26999999999998	198.4	198.49	198.69	198.75	198.9	199.01	199.23	199.3	199.39000000000001	199.52	199.65	199.73	199.87	200.05	200.18	200.39000000000001	200.7	200.82000000000087	201.04	201.25	201.41	201.62	201.82000000000087	201.92000000000004	202.15	202.3	202.46	202.67	202.81	202.97	203.13	203.25	203.39000000000001	203.59	203.70999999999998	203.79	204.01	204.14	204.23999999999998	204.37	204.56	204.63	204.8	204.95000000000007	205.10999999999999	205.18	205.28	205.36	205.53	205.60999999999999	205.73	206	206.09	206.26999999999998	206.53	206.62	206.70999999999998	206.86	207.09	207.19	207.34	207.55	207.65	207.82000000000087	208.05	208.12	208.26	208.42000000000004	208.5	208.63	208.86	208.99	209.17	209.39000000000001	209.51	209.62	209.75	209.92000000000004	210.02	210.17	210.31	210.41	210.51	210.64	210.82000000000087	210.99	211.1	211.26999999999998	211.45000000000007	211.56	211.7	211.83	212.02	212.14	212.26	212.41	212.59	212.63	212.73	212.84	212.99	213.06	213.15	213.28	213.42000000000004	213.55	213.76	213.91	214.06	214.14	214.26999999999998	214.42000000000004	214.51	214.60999999999999	214.73999999999998	214.94	215.08	215.26	215.59	215.73	215.89000000000001	216.08	216.23999999999998	216.4	216.58	216.69	216.91	217.09	217.22	217.37	217.55	217.64	217.76	217.83	218.03	218.09	218.18	218.38000000000127	218.45000000000007	218.68	218.78	219	219.19	219.28	219.5	219.67	219.76999999999998	219.92000000000004	220.02	220.18	220.31	220.45000000000007	220.60999999999999	220.73	220.87	221.05	221.2	221.39000000000001	221.60999999999999	221.79	221.93	222.10999999999999	222.2	222.35000000000107	222.55	222.69	222.86	223.06	223.10999999999999	223.29	223.47	223.55	223.7	223.84	223.98000000000027	224.12	224.54	224.67	224.85000000000107	225.02	225.16	225.31	225.54	225.65	225.92000000000004	226.07	226.25	226.45000000000007	226.6	226.78	226.95000000000007	227.09	227.36	227.38000000000127	227.5	227.62	227.8	227.87	228.04	228.10999999999999	228.23	228.36	228.51	228.68	228.72	228.89000000000001	229	229.09	229.19	229.35000000000107	229.48000000000027	229.64	229.73999999999998	229.86	229.93	230.06	230.20999999999998	230.31	230.48000000000027	230.60999999999999	230.75	230.94	231.05	231.20999999999998	231.4	231.49	231.64	231.84	231.95000000000007	232.03	232.13	232.26999999999998	232.37	232.48000000000027	232.56	232.62	232.81	233.1	233.34	233.43	233.63	233.82000000000087	233.92000000000004	234.12	234.33	234.41	234.59	234.73999999999998	234.83	235.01	235.15	235.22	235.33	235.52	235.66	235.79	235.94	236.1	236.23	236.35000000000107	236.47	236.6	236.81	236.94	237.02	237.09	237.29	237.43	237.57	237.86	237.99	238.12	238.28	238.38000000000127	238.48000000000027	238.62	238.78	238.85000000000107	239.08	239.39000000000001	239.47	239.58	239.73	239.88000000000127	239.99	240.13	240.29	240.35000000000107	240.45000000000007	240.7	240.79	240.98000000000027	241.1	241.42000000000004	241.55	241.78	242.02	242.26	242.36	242.53	242.63	242.8	242.93	243.08	243.54	243.76999999999998	243.98000000000027	244.2	244.33	244.55	244.76	245.04	245.18	245.29	245.4	245.58	245.72	245.93	246.06	246.18	246.3	246.42000000000004	246.63	246.7	246.84	247.02	247.1	247.34	247.53	247.62	247.82000000000087	248.01	248.10999999999999	248.22	248.44	248.56	248.76	248.92000000000004	249.03	249.13	249.23999999999998	249.49	249.56	249.70999999999998	249.88000000000127	249.93	249.99	250.17	250.29	250.36	250.53	250.58	250.73999999999998	250.78	250.96	251.01	251.20999999999998	251.22	251.32000000000087	251.46	251.63	251.73	251.88000000000127	252.05	252.13	252.52	252.52	252.72	252.97	253.18	253.37	253.64	253.76999999999998	253.89000000000001	254.03	254.26	254.39000000000001	254.51	254.72	254.78	254.94	255.09	255.28	255.31	255.45000000000007	255.65	255.70999999999998	255.81	255.93	256.07	256.13	256.22000000000003	256.35000000000002	256.55	256.61	256.86	256.92999999999893	257.08	257.22000000000003	257.33999999999969	257.44	257.58	257.77999999999969	257.95	258.25	258.28999999999894	258.39	258.51	258.72999999999894	258.95999999999964	259.27	259.41999999999899	259.60000000000002	259.77	259.95	260.06	260.27	260.47000000000003	260.58	260.76	260.97000000000003	261.10000000000002	261.22999999999894	261.39999999999969	261.47999999999894	261.64999999999998	261.89	261.97000000000003	262.38	262.62	262.83	263.07	263.22000000000003	263.38	263.61	263.82	263.95999999999964	264.13	264.41999999999899	264.51	264.70999999999964	264.89999999999969	265	265.3	265.38	265.58	265.77	265.86	265.95	266.08999999999969	266.25	266.32	266.48999999999899	266.66000000000008	266.87	266.87	266.95999999999964	267.07	267.27	267.3	267.39999999999969	267.51	267.76	267.88	268.02999999999969	268.27	268.32	268.45	268.52999999999969	268.67	268.76	268.94	269.11	269.18	269.39999999999969	269.68	269.85000000000002	270.08	270.31	270.44	270.66000000000008	270.85000000000002	270.95999999999964	271.18	271.31	271.42999999999893	271.51	271.68	271.82	272.18	272.31	272.47000000000003	272.64999999999998	272.77	273.02	273.18	273.41999999999899	273.67	273.89999999999969	Time (s)

Drained weight (g)
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Drained weight (g)



2 mm beads (300 mm)	0.14814814534971721	0.19333333004668621	0.27710842947813319	0.35227272216871541	0.47567566911906323	0.34408601678807088	0.25396825054168976	0.1711229923189086	0.11170212614443532	8.5938839507737846E-4	1.5468991140613461E-3	2.7956008131251905E-3	5.2735197202708464E-3	1.0033940231587948E-2	4.9899971585521475E-3	2.455395427758301E-3	1.2408281705330341E-3	6.1711401038964367E-4	2 mm beads (500 mm)	0.13080169074398637	0.19140625403749476	0.26865672183114381	0.34892087008697187	0.46853147737787304	0.32876712936761704	0.28321678856422278	0.19860627551383025	0.15034965318843632	8.3645398873017827E-4	1.5487468358891801E-3	2.9587999224862452E-3	5.7047365370617451E-3	1.1090326968122175E-2	5.4312217665281213E-3	2.7725817420306063E-3	1.3814605891438443E-3	6.9314543550764367E-4	10 mm beads (300 mm)	9.9099099456170264E-2	0.16393442676699294	0.22388059768321117	0.34306569443233093	0.47260274102083832	0.3333333342222175	0.23225806511555103	0.15822784850181651	0.19745222980239258	1.0452021256303649E-3	1.9019251788078445E-3	3.4632070409915195E-3	6.7747407804750462E-3	1.2714239544630081E-2	6.1875965779345787E-3	2.9939983439044252E-3	1.4685751369697601E-3	7.3896455937884223E-4	10 mm beads (500 mm)	0.18705036536410846	0.23611111799767492	0.28666667469329532	0.31395349603838762	0.45054946094672993	0.28421053259832829	0.20512820954634187	0.18652850146853428	0.12820513096644434	1.4261841496558975E-3	2.7533277304747309E-3	5.2863892363439521E-3	9.2204463094384768E-3	1.7427656737314362E-2	8.3469303239717772E-3	4.0664532324505304E-3	2.0542963225514852E-3	1.0166133081126326E-3	14 mm beads (300 mm)	0.13402061468801574	0.23076922455621249	0.26229507594732743	0.27464788190832001	0.33742330708724499	0.23529411377163206	0.16091953764038094	0.13529411541865988	0.13690475962304569	1.1960560018344044E-3	2.231104469295201E-3	3.803850257842726E-3	6.5361934219284965E-3	1.1388214334622103E-2	5.4596439348717591E-3	2.6670674404586452E-3	1.3649109837179211E-3	6.9057996186473324E-4	14 mm beads (500 mm)	0.10000000192304316	0.14864865115960091	0.20238095539252141	0.25257732284246481	0.36915888281730425	0.23478261124763211	0.17796610358014858	0.11111111225424541	9.4650206735069395E-2	1.5249199586499281E-3	2.6789134346058572E-3	4.7199903276711032E-3	8.1748285924464776E-3	1.4821651822660481E-2	6.8952901901556188E-3	3.3599931002066051E-3	1.6316015872567921E-3	8.1580079362840701E-4	18 mm beads (300 mm)	0.11403509032005599	0.17073171092606243	0.1986301405235138	0.23976608551687212	0.30526316207201482	0.22110553052700421	0.16097561179771458	0.11428571570067562	0.11004784825899061	1.017696826078082E-3	1.8864624061674148E-3	3.1785599340535715E-3	5.4277163644864141E-3	9.7698894412211208E-3	4.6640175695557284E-3	2.2637548682601896E-3	1.1049279710790521E-3	5.5510735392428929E-4	18 mm beads (500 mm)	0.1666666667658685	0.16666666675086006	0.20370370379800895	0.23076923086781126	0.33716475108700505	0.24363636372496791	0.17525773201900041	0.11904761908812556	9.1216216247023349E-2	1.1799975650606841E-3	2.0024201102254151E-3	3.6711035352587512E-3	6.7774219110056134E-3	1.2152618598507071E-2	5.7669699166337934E-3	2.7249428299700646E-3	1.348568645439653E-3	6.6972834756475993E-4	4-8 mm ore	0.17054491179128684	0.25407421485249732	0.34870930749611923	0.48347714773373485	0.66668293516195654	0.50049327462167703	0.36707206050560576	0.26752660131780737	0.20810886775661738	1.5569398862627206E-4	3.0232610923967829E-4	5.9566642057315455E-4	1.206724373443445E-3	2.4844169437682603E-3	1.2248721328554661E-3	5.941368959282309E-4	2.9630760302531202E-4	1.4903868508847769E-4	8-11.2 mm ore	0.2050698290801567	0.30145929339479816	0.34058268362742494	0.41728468308112782	0.55568499534012761	0.43564976593916194	0.35445046951467657	0.27740300766731241	0.20672647224334484	2.1763001115683082E-4	4.4718849311091538E-4	8.7602702753857248E-4	1.6888186422318984E-3	3.4108020760666951E-3	1.6890970128131321E-3	8.4706171119358067E-4	4.215099936381393E-4	2.1201077818975973E-4	11.2-13.2 mm ore	0.24585527943721774	0.3374459559211484	0.36707545905370031	0.48845257675434506	0.59581595679230737	0.49426983255556611	0.33508949900195895	0.27635299533115038	0.20481015989994344	2.2640018771534067E-4	4.5025378117187698E-4	8.5841507978541695E-4	1.7556564995282477E-3	3.5029110058273716E-3	1.7580661296401903E-3	8.3833043100617832E-4	4.2116360296439462E-4	2.1072036949000016E-4	13.2-16 mm ore	0.24817485754990876	0.3071987342885068	0.42852709053827232	0.45959309394498032	0.6235382559303706	0.47272429868325638	0.41365090052186881	0.30225538693722248	0.19877863846886834	2.851065526324207E-4	5.6294573247205894E-4	1.1358754275666441E-3	2.0765611083194292E-3	4.2797417964143929E-3	2.0952428554296336E-3	1.0780396563431682E-3	5.3698613216522444E-4	2.6249574156051011E-4	16-20 mm ore	0.3241627488537559	0.40716234256205097	0.42494020802037258	0.59992165202310566	0.75270323267418993	0.64144360558212665	0.49676025917927208	0.38819698354649734	0.30146474395376727	3.7173565490364546E-4	7.434713098072892E-4	1.424914310770113E-3	2.8673719171009616E-3	5.741169677480837E-3	2.9305118271947006E-3	1.4560949410786501E-3	7.3179085904180108E-4	3.6361040072299992E-4	20-26.5 mm	0.38009888751543935	0.45678739693761117	0.56229367015932463	0.65692656006795458	0.76134547223552484	0.62187692518319071	0.5275437008148709	0.38680891035966436	0.29719804134938188	4.9479554993312911E-4	9.429672553496291E-4	1.8385628242671142E-3	3.6250933059768938E-3	7.1216997410062134E-3	3.5072262842547812E-3	1.7841447449919053E-3	8.5945163692091565E-4	4.3557083775400953E-4	26.5-31.5 mm ore	0.4594103392567373	0.53896612492650176	0.69053325344525707	0.73333944449537936	0.82676460050144884	0.73250762547383663	0.66177176312503394	0.50610494920295235	0.41172106824930582	6.4667140532450489E-4	1.2540892105608221E-3	2.5582718587317068E-3	4.6967704451989414E-3	9.1789804347315249E-3	4.7358414628597134E-3	2.4588285241709676E-3	1.1938919933514613E-3	5.9390148352509863E-4	31.5-37.5 mm ore	0.30263838592856324	0.53791692018370552	0.61501185689239646	0.66712941539408921	0.88239949351059743	0.73358558942659791	0.51076083661712512	0.41144220518805291	0.3148307879649111	6.0242062834772931E-4	1.3526224108922841E-3	2.6413588659775509E-3	5.0293712924099534E-3	1.032143529240098E-2	5.2129739003455274E-3	2.4708558721350132E-3	1.2413858859089263E-3	6.2037801427066623E-4	37.5-45 mm ore	0.60588901472244461	0.66455696202522407	0.89986468200275538	0.88375796178261445	1.0509554140114701	0.97608274078802348	0.69485591166182992	0.52961579509012413	0.42844651705050174	1.204481942044951E-3	2.2437923097588792E-3	4.6773505455802774E-3	7.9032939318229578E-3	1.5806587863642703E-2	8.2499616405334389E-3	4.0101820004206064E-3	1.986366831317388E-3	1.0074503215342242E-3	Vs* = K(θ*-1)^2	9.6000000000000002E-2	0.11520000000000002	0.13824000000000145	0.16588800000000001	0.19906560000000001	0.23887871999999988	0.28665446400000238	0.34398535679999998	0.41278242816000038	0.4953389137920059	0.5944066965503999	0.71328803586047984	0.85594564303258802	1.02713477163908	1.232561725966909	1.8432000000000184E-4	2.6542080000000005E-4	3.8220595200000009E-4	5.5037657088000862E-4	7.9254226206720987E-4	1.1412608573767701E-3	1.6434156346225679E-3	2.3665185138564658E-3	3.4077866599533523E-3	4.9072127903328679E-3	7.0663864180791833E-3	1.0175596442034023E-2	1.4652858876528993E-2	2.1100116782201802E-2	3.0384168166370611E-2	θ*-1

vs* (m/s)
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Drainage velocity (mm/s)
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Drainage velocity (mm/s)
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Liquid holdup
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Liquid holdup
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Drainage velocity (mm/s)


Experimental drainage	0	15	30	45	60	75	90	105	120	135	150	165	180	195	210	225	240	255	270	285	300	315	330	345	360	375	390	405	420	435	450	465	480	495	510	525	540	555	570	585	600	615	630	645	660	675	690	705	720	735	750	765	780	795	810	825	840	855	870	885	900	930	960	990	1020	1050	1080	1110	1140	1170	1200	1230	1260	1290	1320	1350	1380	1410	1440	1470	1500	1530	1560	1590	1620	1650	1680	1710	1740	1770	1800	1860	1920	1980	2040	2100	2160	2220	2280	2340	2400	3.0185424752048187E-2	2.9810106796176881E-2	2.7217923596506852E-2	2.2033557197166292E-2	1.6849190797843683E-2	1.2960915998333501E-2	1.1664824398503389E-2	9.0726411988324047E-3	7.7765495990020648E-3	6.4804579991715834E-3	5.1843663993314517E-3	6.4804579991714134E-3	5.1843663993314517E-3	3.8882747995010796E-3	3.8882747995009352E-3	3.8882747995010796E-3	3.8882747995009352E-3	3.8882747995010796E-3	3.8882747995009352E-3	2.5921831996704447E-3	2.5921831996612837E-3	2.5921831996701668E-3	3.8882747995010796E-3	2.5921831996704447E-3	2.5921831996611466E-3	2.5921831996703081E-3	2.5921831996704447E-3	2.5921831996611466E-3	1.2960915998398721E-3	2.5921831996611466E-3	1.2960915998397361E-3	2.5921831996611466E-3	1.2960915998305761E-3	2.5921831996704447E-3	1.2960915998304345E-3	1.2960915998398721E-3	2.5921831996611466E-3	2.5921831996704447E-3	1.2960915998304345E-3	1.2960915998398721E-3	2.5921831996611466E-3	1.2960915998397361E-3	2.5921831996611466E-3	1.2960915998398721E-3	1.2960915998305761E-3	1.2960915998305761E-3	1.2960915998397361E-3	1.2960915998307375E-3	1.2960915998304345E-3	1.2960915998398721E-3	1.2960915998305761E-3	2.5921831996703081E-3	1.2960915998307375E-3	1.2960915998304345E-3	1.2960915998398721E-3	1.2960915998305761E-3	1.2960915998305761E-3	1.2960915998397361E-3	1.2960915998307375E-3	1.2960915998304345E-3	2.5921831996704447E-3	1.2960915998351541E-3	1.2960915998305761E-3	1.2960915998352449E-3	1.2960915998351541E-3	1.2960915998305761E-3	1.2960915998352449E-3	6.4804579991530129E-4	1.2960915998352449E-3	1.2960915998351541E-3	6.4804579991530129E-4	6.4804579991530129E-4	6.4804579991987966E-4	1.2960915998305761E-3	6.480457999199484E-4	1.2960915998305761E-3	6.4804579991987966E-4	6.4804579991537437E-4	1.2960915998305761E-3	1.2960915998351541E-3	1.2960915998352449E-3	6.4804579991530129E-4	6.4804579991530129E-4	1.2960915998351541E-3	1.2960915998352449E-3	6.4804579991530129E-4	6.4804579991530129E-4	1.2960915998351541E-3	6.4804579991537437E-4	6.4804579991987966E-4	6.4804579991530129E-4	6.4804579991762431E-4	9.7206869987524563E-4	6.4804579991530129E-4	6.4804579991758864E-4	6.4804579991762431E-4	9.7206869987525744E-4	6.4804579991530129E-4	6.4804579991758864E-4	9.7206869987524563E-4	6.4804579991762431E-4	Fitted data	0	2.0884999999999998	4.1769999999999996	6.2653999999999996	8.3539000000000048	10.442	12.531000000000001	14.619	16.707999999999988	18.795999999999989	20.885000000000002	22.972999999999889	25.061999999999987	27.150000000000031	29.239000000000001	31.327000000000005	33.416000000000004	35.504000000000005	37.593000000000011	39.681000000000004	41.77	43.857999999999997	45.947000000000003	48.035000000000011	50.124000000000002	52.212000000000003	54.3	56.389000000000003	58.477000000000004	60.566000000000003	62.654000000000003	64.742999999999995	66.831000000000003	68.92	71.007999999999996	73.096999999999994	75.185000000000002	77.274000000000001	79.361999999999995	81.450999999999993	83.539000000000001	85.627999999999986	87.715999999999994	89.804999999999993	91.893000000000001	93.982000000000014	96.07	98.158999999999978	100.25	102.34	104.42	106.51	108.6	110.69	112.78	114.86999999999999	116.95	119.04	121.13	123.22	125.31	127.4	129.49	131.57	133.66	135.75	137.84	139.93	142.02000000000001	144.10999999999999	146.19	148.28	150.37	152.46	154.55000000000001	156.63999999999999	158.72	160.81	162.9	164.99	167.08	169.17	171.26	173.34	175.43	177.52	179.60999999999999	181.7	183.79	185.87	187.96	190.05	192.14	194.23	196.32000000000087	198.41	200.49	202.58	204.67	206.76	208.85000000000107	210.94	213.02	215.10999999999999	217.2	219.29	221.38000000000127	223.47	225.56	227.64	229.73	231.82000000000087	233.91	236	238.09	240.18	242.26	244.35000000000107	246.44	248.53	250.62	252.70999999999998	254.79	256.88	258.97000000000003	261.06	263.14999999999998	265.24	267.33	269.41000000000003	271.5	273.58999999999969	275.68	277.77	279.86	281.94	284.02999999999969	286.12	288.20999999999964	290.3	292.39	294.47999999999894	296.56	298.64999999999998	300.74	302.83	304.91999999999899	307.01	309.10000000000002	311.18	313.27	315.36	317.45	319.54000000000002	321.63	323.70999999999964	325.8	327.89	329.97999999999894	332.07	334.16	336.25	338.33	340.41999999999899	342.51	344.6	346.69	348.78	350.86	352.95	355.04	357.13	359.21999999999969	361.31	363.4	365.47999999999894	367.57	369.66	371.75	373.84000000000032	375.92999999999893	378.01	380.1	382.19	384.28	386.37	388.46	390.55	392.63	394.71999999999969	396.81	398.9	400.98999999999899	403.08	405.17	407.25	409.34000000000032	411.42999999999893	413.52	415.61	417.7	419.78	421.87	423.96	426.05	428.14000000000038	430.22999999999894	432.32	434.4	436.48999999999899	438.58	440.67	442.76	444.85	446.92999999999893	449.02	451.11	453.2	455.28999999999894	457.38	459.46999999999969	461.55	463.64000000000038	465.72999999999894	467.82	469.90999999999963	472	474.08	476.17	478.26	480.35	482.44	484.53	486.62	488.7	490.78999999999894	492.88	494.96999999999969	497.06	499.15000000000032	501.24	503.32	505.40999999999963	507.5	509.59	511.68	513.77000000000055	515.84999999999798	517.93999999999949	520.03	522.12	524.21	526.29999999999995	528.39	530.47	532.55999999999949	534.65	536.74	538.82999999999947	540.91999999999996	543	545.09	547.17999999999995	549.27000000000055	551.35999999999797	553.44999999999948	555.54	557.62	559.71	561.79999999999995	563.89	565.98	568.07000000000005	570.16	572.24	574.32999999999947	576.41999999999996	578.51	580.6	582.69000000000005	584.77000000000055	586.85999999999797	588.94999999999948	591.04	593.13	595.22	597.30999999999949	599.39	601.48	603.57000000000005	605.66	607.75	609.83999999999946	611.91999999999996	614.01	616.1	618.19000000000005	620.28000000000054	622.37	624.45999999999947	626.54	628.63	630.72	632.80999999999949	634.9	636.99	639.07000000000005	641.16	643.25	645.33999999999946	647.42999999999938	649.52	651.61	653.69000000000005	655.78000000000054	657.87	659.95999999999947	662.05	664.14	666.23	668.31	670.4	672.49	674.58	676.67000000000053	678.76	680.83999999999946	682.93	685.02	687.11	689.2	691.29000000000053	693.38	695.45999999999947	697.55	699.64	701.73	703.81999999999948	705.91	707.99	710.08	712.17000000000053	714.26	716.34999999999798	718.43999999999949	720.53	722.61	724.7	726.79000000000053	728.88	730.97	733.06	735.15	737.23	739.31999999999948	741.41	743.5	745.59	747.68000000000052	749.76	751.84999999999798	753.93999999999949	756.03	758.12	760.21	762.3	764.38	766.47	768.56	770.65	772.74	774.82999999999947	776.91	779	781.09	783.18000000000052	785.27000000000055	787.35999999999797	789.44999999999948	791.53	793.62	795.71	797.8	799.89	801.98	804.06	806.15	808.24	810.32999999999947	812.42	814.51	816.6	818.68000000000052	820.77000000000055	822.85999999999797	824.94999999999948	827.04	829.13	831.22	833.3	835.39	837.48	839.57	841.66	843.75	845.82999999999947	847.92	850.01	852.1	854.19	856.28000000000054	858.37	860.44999999999948	862.54	864.63	866.72	868.81	870.9	872.98	875.07	877.16	879.25	881.33999999999946	883.43	885.52	887.6	889.69	891.78000000000054	893.87	895.95999999999947	898.05	900.13	902.22	904.31	906.4	908.49	910.58	912.67000000000053	914.75	916.83999999999946	918.93	921.02	923.11	925.2	927.29000000000053	929.37	931.45999999999947	933.55	935.64	937.73	939.81999999999948	941.9	943.99	946.08	948.17000000000053	950.26	952.34999999999798	954.43999999999949	956.52	958.61	960.7	962.79000000000053	964.88	966.97	969.05	971.14	973.23	975.31999999999948	977.41	979.5	981.59	983.67000000000053	985.76	987.84999999999798	989.93999999999949	992.03	994.12	996.21	998.29000000000053	1000.4	1002.5	1004.6	1006.6	1008.7	1010.8	1012.9	1015	1017.1	1019.2	1021.3	1023.4	1025.4000000000001	1027.5	1029.5999999999999	1031.7	1033.8	1035.9000000000001	1038	1040.0999999999999	1042.2	1044.2	1046.3	1048.4000000000001	1050.5	1052.5999999999999	1054.7	1056.8	1058.9000000000001	1060.9000000000001	1063	1065.0999999999999	1067.2	1069.3	1071.4000000000001	1073.5	1075.5999999999999	1077.7	1079.7	1081.8	1083.9000000000001	1086	1088.0999999999999	1090.2	1092.3	1094.4000000000001	1096.5	1098.5	1100.5999999999999	1102.7	1104.8	1106.9000000000001	1109	1111.0999999999999	1113.2	1115.2	1117.3	1119.4000000000001	1121.5	1123.5999999999999	1125.7	1127.8	1129.9000000000001	1132	1134	1136.0999999999999	1138.2	1140.3	1142.4000000000001	1144.5	1146.5999999999999	1148.7	1150.8	1152.8	1154.9000000000001	1157	1159.0999999999999	1161.2	1163.3	1165.4000000000001	1167.5	1169.5	1171.5999999999999	1173.7	1175.8	1177.9000000000001	1180	1182.0999999999999	1184.2	1186.3	1188.3	1190.4000000000001	1192.5	1194.5999999999999	1196.7	1198.8	1200.9000000000001	1203	1205.0999999999999	1207.0999999999999	1209.2	1211.3	1213.4000000000001	1215.5	1217.5999999999999	1219.7	1221.8	1223.8	1225.9000000000001	1228	1230.0999999999999	1232.2	1234.3	1236.4000000000001	1238.5	1240.5999999999999	1242.5999999999999	1244.7	1246.8	1248.9000000000001	1251	1253.0999999999999	1255.2	1257.3	1259.4000000000001	1261.4000000000001	1263.5	1265.5999999999999	1267.7	1269.8	1271.9000000000001	1274	1276.0999999999999	1278.0999999999999	1280.2	1282.3	1284.4000000000001	1286.5	1288.5999999999999	1290.7	1292.8	1294.9000000000001	1296.9000000000001	1299	1301.0999999999999	1303.2	1305.3	1307.4000000000001	1309.5	1311.6	1313.7	1315.7	1317.8	1319.9	1322	1324.1	1326.2	1328.3	1330.4	1332.5	1334.5	1336.6	1338.7	1340.8	1342.9	1345	1347.1	1349.2	1351.2	1353.3	1355.4	1357.5	1359.6	1361.7	1363.8	1365.9	1368	1370	1372.1	1374.2	1376.3	1378.4	1380.5	1382.6	1384.7	1386.8	1388.8	1390.9	1393	1395.1	1397.2	1399.3	1401.4	1403.5	1405.5	1407.6	1409.7	1411.8	1413.9	1416	1418.1	1420.2	1422.3	1424.3	1426.4	1428.5	1430.6	1432.7	1434.8	1436.9	1439	1441.1	1443.1	1445.2	1447.3	1449.4	1451.5	1453.6	1455.7	1457.8	1459.8	1461.9	1464	1466.1	1468.2	1470.3	1472.4	1474.5	1476.6	1478.6	1480.7	1482.8	1484.9	1487	1489.1	1491.2	1493.3	1495.4	1497.4	1499.5	1501.6	1503.7	1505.8	1507.9	1510	1512.1	1514.1	1516.2	1518.3	1520.4	1522.5	1524.6	1526.7	1528.8	1530.9	1532.9	1535	1537.1	1539.2	1541.3	1543.4	1545.5	1547.6	1549.7	1551.7	1553.8	1555.9	1558	1560.1	1562.2	1564.3	1566.4	1568.4	1570.5	1572.6	1574.7	1576.8	1578.9	1581	1583.1	1585.2	1587.2	1589.3	1591.4	1593.5	1595.6	1597.7	1599.8	1601.9	1604	1606	1608.1	1610.2	1612.3	1614.4	1616.5	1618.6	1620.7	1622.7	1624.8	1626.9	1629	1631.1	1633.2	1635.3	1637.4	1639.5	1641.5	1643.6	1645.7	1647.8	1649.9	1652	1654.1	1656.2	1658.3	1660.3	1662.4	1664.5	1666.6	1668.7	1670.8	1672.9	1675	1677	1679.1	1681.2	1683.3	1685.4	1687.5	1689.6	1691.7	1693.8	1695.8	1697.9	1700	1702.1	1704.2	1706.3	1708.4	1710.5	1712.6	1714.6	1716.7	1718.8	1720.9	1723	1725.1	1727.2	1729.3	1731.4	1733.4	1735.5	1737.6	1739.7	1741.8	1743.9	1746	1748.1	1750.1	1752.2	1754.3	1756.4	1758.5	1760.6	1762.7	1764.8	1766.9	1768.9	1771	1773.1	1775.2	1777.3	1779.4	1781.5	1783.6	1785.7	1787.7	1789.8	1791.9	1794	1796.1	1798.2	1800.3	1802.4	1804.4	1806.5	1808.6	1810.7	1812.8	1814.9	1817	1819.1	1821.2	1823.2	1825.3	1827.4	1829.5	1831.6	1833.7	1835.8	1837.9	1840	1842	1844.1	1846.2	1848.3	1850.4	1852.5	1854.6	1856.7	1858.7	1860.8	1862.9	1865	1867.1	1869.2	1871.3	1873.4	1875.5	1877.5	1879.6	1881.7	1883.8	1885.9	1888	1890.1	1892.2	1894.3	1896.3	1898.4	1900.5	1902.6	1904.7	1906.8	1908.9	1911	1913	1915.1	1917.2	1919.3	1921.4	1923.5	1925.6	1927.7	1929.8	1931.8	1933.9	1936	1938.1	1940.2	1942.3	1944.4	1946.5	1948.6	1950.6	1952.7	1954.8	1956.9	1959	1961.1	1963.2	1965.3	1967.3	1969.4	1971.5	1973.6	1975.7	1977.8	1979.9	1982	1984.1	1986.1	1988.2	1990.3	1992.4	1994.5	1996.6	1998.7	2000.8	2002.9	2004.9	2007	2009.1	2011.2	2013.3	2015.4	2017.5	2019.6	2021.6	2023.7	2025.8	2027.9	2030	2032.1	2034.2	2036.3	2038.4	2040.4	2042.5	2044.6	2046.7	2048.8000000000002	2050.9	2053	2055.1	2057.1999999999998	2059.1999999999998	2061.3000000000002	2063.4	2065.5	2067.6	2069.6999999999998	2071.8000000000002	2073.9	2075.9	2078	2080.1	2082.1999999999998	2084.3000000000002	2086.4	2088.5	2090.6	2092.6999999999998	2094.6999999999998	2096.8000000000002	2098.9	2101	2103.1	2105.1999999999998	2107.3000000000002	2109.4	2111.5	2113.5	2115.6	2117.6999999999998	2119.8000000000002	2121.9	2124	2126.1	2128.1999999999998	2130.1999999999998	2132.3000000000002	2134.4	2136.5	2138.6	2140.6999999999998	2142.8000000000002	2144.9	2147	2149	2151.1	2153.1999999999998	2155.3000000000002	2157.4	2159.5	2161.6	2163.6999999999998	2165.8000000000002	2167.8000000000002	2169.9	2172	2174.1	2176.1999999999998	2178.3000000000002	2180.4	2182.5	2184.6	2186.6	2188.6999999999998	2190.8000000000002	2192.9	2195	2197.1	2199.1999999999998	2201.3000000000002	2203.3000000000002	2205.4	2207.5	2209.6	2211.6999999999998	2213.8000000000002	2215.9	2218	2220.1	2222.1	2224.1999999999998	2226.3000000000002	2228.4	2230.5	2232.6	2234.6999999999998	2236.8000000000002	2238.9	2240.9	2243	2245.1	2247.1999999999998	2249.3000000000002	2251.4	2253.5	2255.6	2257.6	2259.6999999999998	2261.8000000000002	2263.9	2266	2268.1	2270.1999999999998	2272.3000000000002	2274.4	2276.4	2278.5	2280.6	2282.6999999999998	2284.8000000000002	2286.9	2289	2291.1	2293.1999999999998	2295.1999999999998	2297.3000000000002	2299.4	2301.5	2303.6	2305.6999999999998	2307.8000000000002	2309.9	2311.9	2314	2316.1	2318.1999999999998	2320.3000000000002	2322.4	2324.5	2326.6	2328.6999999999998	2330.6999999999998	2332.8000000000002	2334.9	2337	2339.1	2341.1999999999998	2343.3000000000002	2345.4	2347.5	2349.5	2351.6	2353.6999999999998	2355.8000000000002	2357.9	2360	2362.1	2364.1999999999998	2366.1999999999998	2368.3000000000002	2370.4	2372.5	2374.6	2376.6999999999998	2378.8000000000002	2380.9	2383	2385	2387.1	2389.1999999999998	2391.3000000000002	2393.4	2395.5	2397.6	2399.6999999999998	2401.8000000000002	3.0185424752048187E-2	3.018500000000001E-2	3.018500000000001E-2	3.018500000000001E-2	3.018500000000001E-2	3.018500000000001E-2	3.018500000000001E-2	3.018500000000001E-2	3.018500000000001E-2	3.018500000000001E-2	3.018500000000001E-2	3.0180000000000002E-2	3.0165000000000001E-2	3.0127999999999999E-2	3.0052000000000002E-2	2.9921999999999997E-2	2.9719000000000002E-2	2.9433000000000518E-2	2.9056999999999999E-2	2.8591000000000002E-2	2.8041000000000052E-2	2.741700000000049E-2	2.6731000000000452E-2	2.5996999999999989E-2	2.5228E-2	2.4438000000000001E-2	2.3638000000000006E-2	2.2836000000000495E-2	2.2042000000000016E-2	2.1260999999999999E-2	2.0498000000000002E-2	1.9757000000000021E-2	1.9040000000000289E-2	1.8348000000000003E-2	1.7683000000000001E-2	1.7045999999999999E-2	1.6435000000000005E-2	1.5851000000000001E-2	1.5293000000000001E-2	1.4759999999999916E-2	1.4251999999999996E-2	1.3767999999999999E-2	1.3306000000000005E-2	1.2865000000000001E-2	1.2444999999999998E-2	1.2045E-2	1.1663000000000227E-2	1.1297999999999999E-2	1.0950000000000001E-2	1.0617999999999994E-2	1.0302E-2	9.9987000000000027E-3	9.7094000000000208E-3	9.4328000000000068E-3	9.1682000000000013E-3	8.9151000000000247E-3	8.6727000000000228E-3	8.4406000000000047E-3	8.2182000000000002E-3	8.0049000000000006E-3	7.8004000000000033E-3	7.6042000000000123E-3	7.4158000000000114E-3	7.2349000000000024E-3	7.0611000000000024E-3	6.8940000000000034E-3	6.7333000000001529E-3	6.5787000000001178E-3	6.4298000000000124E-3	6.2865000000000134E-3	6.1485000000000003E-3	6.0155E-3	5.8872000000000134E-3	5.7635000000000004E-3	5.6441E-3	5.5288999999999998E-3	5.4177000000000114E-3	5.3102000000000114E-3	5.2063000000001133E-3	5.1060000000000003E-3	5.0088999999999993E-3	4.9150000000000114E-3	4.8240999999999996E-3	4.7361000000000963E-3	4.6509999999999998E-3	4.5684000000000002E-3	4.4885000000000124E-3	4.4110000000000963E-3	4.3359000000000002E-3	4.2629999999999986E-3	4.1923000000000004E-3	4.1237000000000001E-3	4.0570999999999992E-3	3.9925000000000056E-3	3.9296999999999995E-3	3.8687000000000595E-3	3.8094000000000001E-3	3.7518000000000052E-3	3.6958000000000052E-3	3.6413000000000699E-3	3.5883000000000755E-3	3.5366999999999998E-3	3.4866000000000012E-3	3.4377000000000092E-3	3.3902000000000012E-3	3.3438000000000092E-3	3.2987000000000623E-3	3.2547000000000595E-3	3.2119000000000292E-3	3.1701000000000567E-3	3.1294000000000092E-3	3.0897000000000541E-3	3.0510000000000012E-3	3.0132000000000002E-3	2.9763000000000012E-3	2.9403000000000506E-3	2.9052000000000001E-3	2.8709000000000052E-3	2.8374000000000012E-3	2.8046999999999998E-3	2.7727000000000012E-3	2.7415000000000638E-3	2.7110000000000012E-3	2.6812000000000012E-3	2.6521000000000092E-3	2.6236000000000484E-3	2.5956999999999998E-3	2.5684000000000423E-3	2.5418000000000012E-3	2.5157000000000001E-3	2.4902000000000001E-3	2.4652000000000012E-3	2.4407000000000092E-3	2.4167999999999998E-3	2.3934E-3	2.3704000000000004E-3	2.3479000000000052E-3	2.3259000000000001E-3	2.3044000000000012E-3	2.2832000000000637E-3	2.2625000000000292E-3	2.2422000000000002E-3	2.2223000000000212E-3	2.2028000000000052E-3	2.1837000000000692E-3	2.1650000000000011E-3	2.1466000000000002E-3	2.1286000000000052E-3	2.1109000000000002E-3	2.0934999999999999E-3	2.0764999999999998E-3	2.0598000000000001E-3	2.0434000000000012E-3	2.0273000000000578E-3	2.0115000000000011E-3	1.9959999999999999E-3	1.9807000000000353E-3	1.9658000000000123E-3	1.9511000000000315E-3	1.936700000000034E-3	1.9225000000000336E-3	1.9086000000000328E-3	1.8949000000000285E-3	1.8814000000000229E-3	1.8682000000000325E-3	1.8552000000000225E-3	1.8425000000000268E-3	1.8299000000000021E-3	1.8175999999999999E-3	1.8055000000000061E-3	1.7936000000000041E-3	1.7819000000000001E-3	1.7703000000000228E-3	1.7589999999999999E-3	1.7478000000000001E-3	1.7369000000000041E-3	1.7261000000000227E-3	1.7155E-3	1.7049999999999999E-3	1.6947000000000309E-3	1.6846000000000306E-3	1.6746000000000308E-3	1.6648000000000279E-3	1.6552000000000235E-3	1.6456999999999999E-3	1.6363000000000297E-3	1.6271000000000217E-3	1.6181000000000301E-3	1.6091000000000041E-3	1.6003000000000265E-3	1.5916999999999999E-3	1.5831000000000061E-3	1.5747000000000211E-3	1.5664000000000231E-3	1.5583000000000226E-3	1.5502000000000226E-3	1.5423000000000231E-3	1.5345000000000061E-3	1.5268000000000061E-3	1.5192000000000001E-3	1.5117000000000021E-3	1.5043999999999999E-3	1.4971000000000001E-3	1.4898999999999978E-3	1.4829000000000001E-3	1.4758999999999998E-3	1.4691000000000001E-3	1.4622999999999999E-3	1.4556E-3	1.449E-3	1.4425000000000041E-3	1.4361000000000061E-3	1.4298E-3	1.4235999999999958E-3	1.4173999999999999E-3	1.4112999999999999E-3	1.4054E-3	1.3994999999999999E-3	1.3936000000000061E-3	1.3879000000000001E-3	1.3822000000000265E-3	1.3766000000000242E-3	1.3711000000000081E-3	1.3656000000000041E-3	1.3602000000000254E-3	1.3549000000000041E-3	1.3496000000000001E-3	1.3443999999999999E-3	1.3393000000000001E-3	1.3343000000000218E-3	1.3292999999999998E-3	1.3243000000000141E-3	1.3194999999999999E-3	1.3147000000000041E-3	1.3098999999999999E-3	1.3052000000000001E-3	1.3006000000000061E-3	1.2960000000000217E-3	1.2915000000000001E-3	1.2869999999999999E-3	1.2826000000000061E-3	1.2782000000000021E-3	1.2738999999999999E-3	1.2697000000000001E-3	1.2654999999999999E-3	1.2613000000000001E-3	1.2572E-3	1.2530999999999998E-3	1.2490999999999999E-3	1.2451999999999999E-3	1.2412E-3	1.2374E-3	1.2335E-3	1.2297E-3	1.2260000000000001E-3	1.2222999999999999E-3	1.2186E-3	1.2149999999999999E-3	1.2114000000000001E-3	1.2078999999999998E-3	1.2044000000000041E-3	1.2009E-3	1.1975000000000041E-3	1.1941000000000306E-3	1.1908000000000233E-3	1.1875000000000021E-3	1.184200000000028E-3	1.1810000000000021E-3	1.1777999999999999E-3	1.1746000000000232E-3	1.1715000000000041E-3	1.1684000000000251E-3	1.1653000000000021E-3	1.1623000000000256E-3	1.1593000000000061E-3	1.1563000000000239E-3	1.1533000000000001E-3	1.1504000000000236E-3	1.1476000000000001E-3	1.1447000000000041E-3	1.1418999999999999E-3	1.1391000000000001E-3	1.1363000000000228E-3	1.1336000000000041E-3	1.1309000000000041E-3	1.1282000000000241E-3	1.1256E-3	1.1229000000000041E-3	1.1203000000000222E-3	1.1178000000000021E-3	1.1152000000000041E-3	1.1126999999999999E-3	1.1102000000000221E-3	1.1077000000000001E-3	1.1053E-3	1.1029000000000021E-3	1.1005000000000001E-3	1.0981000000000061E-3	1.0957E-3	1.0934E-3	1.0911000000000041E-3	1.0888000000000041E-3	1.0866000000000061E-3	1.0843000000000061E-3	1.0821000000000081E-3	1.0799E-3	1.0777E-3	1.0755999999999999E-3	1.0734000000000021E-3	1.0713000000000001E-3	1.0692000000000021E-3	1.0670999999999999E-3	1.0651E-3	1.0631000000000041E-3	1.0610000000000001E-3	1.059E-3	1.0571000000000001E-3	1.0551E-3	1.0531000000000021E-3	1.0512000000000021E-3	1.0493E-3	1.0474E-3	1.0455E-3	1.0437000000000001E-3	1.0417999999999998E-3	1.0399999999999958E-3	1.0382000000000021E-3	1.0364000000000061E-3	1.0346000000000001E-3	1.0329E-3	1.0310999999999999E-3	1.0294E-3	1.0276999999999999E-3	1.0260000000000041E-3	1.0243000000000001E-3	1.0226E-3	1.021E-3	1.0192999999999999E-3	1.0177000000000001E-3	1.0161000000000061E-3	1.0145000000000041E-3	1.0129000000000021E-3	1.0112999999999999E-3	1.0098000000000002E-3	1.0081999999999999E-3	1.0067000000000001E-3	1.0051999999999978E-3	1.0036999999999978E-3	1.0022000000000021E-3	1.0007E-3	9.9922000000000248E-4	9.9776000000000747E-4	9.9632000000001776E-4	9.9488000000000007E-4	9.9346000000000026E-4	9.9205000000001297E-4	9.9066000000001798E-4	9.8927000000002775E-4	9.8789000000000277E-4	9.8653000000002624E-4	9.8518000000001778E-4	9.8384000000000297E-4	9.8250000000001266E-4	9.8118000000000098E-4	9.7987000000000031E-4	9.7857000000000868E-4	9.7729000000000067E-4	9.7601000000000068E-4	9.7474000000000042E-4	9.734800000000002E-4	9.7223000000000025E-4	9.7099000000000046E-4	9.6976000000000245E-4	9.6854000000002607E-4	9.6733000000000225E-4	9.6613000000000027E-4	9.6494000000000267E-4	9.6376000000000025E-4	9.6259000000000264E-4	9.6142000000000026E-4	9.6027000000001566E-4	9.5912000000000026E-4	9.5799000000001565E-4	9.5686000000001065E-4	9.5574000000002489E-4	9.5463000000000026E-4	9.5353000000000028E-4	9.5243000000000042E-4	9.5134000000002034E-4	9.5027000000001748E-4	9.492000000000209E-4	9.4814000000001267E-4	9.4708000000001268E-4	9.4604000000002991E-4	9.4500000000002286E-4	9.4397000000001228E-4	9.4294000000002393E-4	9.4193000000000228E-4	9.4092000000001066E-4	9.3992000000001248E-4	9.3893000000001728E-4	9.37940000000034E-4	9.3696000000003234E-4	9.3599000000002736E-4	9.3503000000001268E-4	9.3407000000000266E-4	9.3312000000000006E-4	9.3217000000000245E-4	9.3124000000003237E-4	9.3031000000001567E-4	9.2938000000000027E-4	9.2846000000000063E-4	9.275500000000223E-4	9.2665000000001268E-4	9.2575000000001228E-4	9.2486000000000001E-4	9.2398000000000024E-4	9.2310000000000005E-4	9.2222000000000061E-4	9.2136000000000225E-4	9.2050000000000248E-4	9.1964000000001247E-4	9.1879000000000006E-4	9.1795000000002088E-4	9.1711000000000028E-4	9.1628000000001746E-4	9.1546000000000747E-4	9.1464000000000248E-4	9.138200000000003E-4	9.1302000000000028E-4	9.1221000000000227E-4	9.1142000000000003E-4	9.1062000000000066E-4	9.0984000000000247E-4	9.0905000000001247E-4	9.0828000000001748E-4	9.0751000000001978E-4	9.0674000000002196E-4	9.0598000000001748E-4	9.0523000000001727E-4	9.0448000000000026E-4	9.0373000000000005E-4	9.0299000000000065E-4	9.0225000000002055E-4	9.0152000000000266E-4	9.0080000000000043E-4	9.0008000000000264E-4	8.9936000000000768E-4	8.9865000000002426E-4	8.979400000000301E-4	8.9724000000003274E-4	8.9654000000003646E-4	8.9585000000001747E-4	8.9516000000001267E-4	8.9447000000000062E-4	8.9379000000000043E-4	8.9312000000000061E-4	8.9245000000000567E-4	8.9178000000000065E-4	8.9112000000000024E-4	8.9046000000001066E-4	8.8980000000000244E-4	8.8915000000001248E-4	8.8851000000002463E-4	8.8787000000001227E-4	8.8723000000001748E-4	8.8659000000002822E-4	8.8596000000003272E-4	8.8534000000003467E-4	8.8472000000000041E-4	8.8410000000000008E-4	8.8348000000000224E-4	8.8287000000000066E-4	8.8227000000001767E-4	8.8167000000001266E-4	8.8107000000001265E-4	8.8047000000000765E-4	8.7988000000000042E-4	8.7929000000000045E-4	8.7871000000000043E-4	8.781300000000004E-4	8.7755000000002022E-4	8.7697000000001065E-4	8.7640000000000027E-4	8.7584000000000565E-4	8.7527000000001728E-4	8.7471000000000001E-4	8.7416000000000002E-4	8.7360000000000042E-4	8.7305000000000043E-4	8.7251000000000028E-4	8.7196000000000246E-4	8.7142000000000014E-4	8.7089000000000003E-4	8.7035000000000248E-4	8.6982000000000032E-4	8.6930000000000048E-4	8.6877000000000048E-4	8.6825000000001267E-4	8.6773000000000026E-4	8.6722000000000567E-4	8.6671000000000046E-4	8.6620000000001748E-4	8.6569000000000728E-4	8.6519000000000027E-4	8.6469000000000042E-4	8.6419000000000014E-4	8.6370000000000001E-4	8.6320000000000244E-4	8.627200000000002E-4	8.6223000000000061E-4	8.6175000000000064E-4	8.6127000000001065E-4	8.6079000000000006E-4	8.6031000000000063E-4	8.5984000000000245E-4	8.5937000000000068E-4	8.5891000000000266E-4	8.5844000000001228E-4	8.5798000000001067E-4	8.5752000000000766E-4	8.5707000000001228E-4	8.5661000000001068E-4	8.5616000000000728E-4	8.5571000000000247E-4	8.5527000000002525E-4	8.5482000000000017E-4	8.5438000000000061E-4	8.5394000000000268E-4	8.5351000000000068E-4	8.5307000000000048E-4	8.5264000000001246E-4	8.5221000000000266E-4	8.5179000000000027E-4	8.5136000000000727E-4	8.5094000000001768E-4	8.5052000000000727E-4	8.5011000000000028E-4	8.4969000000000266E-4	8.4928000000001746E-4	8.4887000000000048E-4	8.4846000000000248E-4	8.4805000000002053E-4	8.476500000000254E-4	8.4725000000003038E-4	8.4685000000001248E-4	8.4645000000001767E-4	8.4606000000002238E-4	8.4566000000002714E-4	8.4527000000002967E-4	8.4488E-4	8.4450000000000248E-4	8.4411000000000024E-4	8.4373000000000022E-4	8.4335000000000746E-4	8.4297000000000267E-4	8.4259000000000764E-4	8.4222000000000246E-4	8.4185000000000228E-4	8.4148000000000046E-4	8.4111000000000027E-4	8.4074000000001266E-4	8.4038000000000764E-4	8.4001000000000247E-4	8.3965000000002358E-4	8.3929000000001748E-4	8.3894000000003007E-4	8.3858000000002484E-4	8.3823000000001727E-4	8.3788000000000265E-4	8.3753000000002078E-4	8.3718000000000746E-4	8.3683000000000065E-4	8.3649000000000267E-4	8.3615000000002268E-4	8.3580000000001067E-4	8.3547000000001989E-4	8.3513000000000727E-4	8.3479000000000062E-4	8.3446000000000225E-4	8.341300000000002E-4	8.3380000000000043E-4	8.3347000000000065E-4	8.3314000000000727E-4	8.3281000000000023E-4	8.3249000000000062E-4	8.3217000000000067E-4	8.3185000000000247E-4	8.3153000000001228E-4	8.3121000000001266E-4	8.3089000000000047E-4	8.3058000000002345E-4	8.302700000000254E-4	8.2996000000000068E-4	8.2965000000000068E-4	8.2934000000000068E-4	8.2903000000000002E-4	8.2873000000000018E-4	8.2842000000000018E-4	8.2812000000000001E-4	8.2782000000000016E-4	8.2752000000000227E-4	8.2722000000000047E-4	8.2693000000000046E-4	8.2663000000000007E-4	8.2634000000001567E-4	8.2605000000000764E-4	8.2576000000000264E-4	8.2547000000000046E-4	8.2518000000000044E-4	8.2489000000000011E-4	8.2461000000000025E-4	8.2432000000000002E-4	8.2404000000000006E-4	8.2376000000000042E-4	8.2348000000000002E-4	8.2320000000000028E-4	8.2293000000000025E-4	8.2265000000000224E-4	8.2238000000000005E-4	8.221000000000002E-4	8.2182999999999996E-4	8.2156000000000264E-4	8.2129000000000045E-4	8.2103000000000005E-4	8.2076000000000046E-4	8.2049E-4	8.2023000000000024E-4	8.1997000000000244E-4	8.1971000000000008E-4	8.1945000000000065E-4	8.1919000000000024E-4	8.1893000000000027E-4	8.1867000000000246E-4	8.1842000000000004E-4	8.1816000000000028E-4	8.1791000000000264E-4	8.1766000000000748E-4	8.1741000000000062E-4	8.1716000000000048E-4	8.1691000000000727E-4	8.1666000000000767E-4	8.1642000000000043E-4	8.1617000000000224E-4	8.1593000000000247E-4	8.1569000000000747E-4	8.1544000000001264E-4	8.1520000000001765E-4	8.1496000000000064E-4	8.1473000000000016E-4	8.1449000000000018E-4	8.1425000000000247E-4	8.1402000000000015E-4	8.1378000000000006E-4	8.1355000000000728E-4	8.1332000000000008E-4	8.1309000000000004E-4	8.1286000000000043E-4	8.1263000000000006E-4	8.1240000000000001E-4	8.1217000000000008E-4	8.1195000000000746E-4	8.1172000000000004E-4	8.1150000000000265E-4	8.1128000000000244E-4	8.1106000000000244E-4	8.1083000000000001E-4	8.1061000000000045E-4	8.1040000000000062E-4	8.1018000000000041E-4	8.0996000000000767E-4	8.0975000000000068E-4	8.0953000000000264E-4	8.0932000000000063E-4	8.0910000000000042E-4	8.0889000000000004E-4	8.0868000000000248E-4	8.0847000000000048E-4	8.0826000000001267E-4	8.0805000000001566E-4	8.0784000000000248E-4	8.0764000000002373E-4	8.0743000000000026E-4	8.0723000000000264E-4	8.0702000000000226E-4	8.0682000000000041E-4	8.0662000000000247E-4	8.0642000000000062E-4	8.0622000000000766E-4	8.0602000000000245E-4	8.0582000000000028E-4	8.0562000000000765E-4	8.0542000000000048E-4	8.0523000000000768E-4	8.0503000000000226E-4	8.0484000000000024E-4	8.0464000000000566E-4	8.0445000000000028E-4	8.0426000000000228E-4	8.0407000000000026E-4	8.038800000000002E-4	8.0369000000000024E-4	8.0350000000000245E-4	8.0331000000000044E-4	8.0312000000000005E-4	8.0293000000000042E-4	8.0275000000000225E-4	8.0256000000001248E-4	8.0238000000000065E-4	8.0220000000000248E-4	8.0201000000000024E-4	8.0183000000000001E-4	8.0165000000000748E-4	8.0147000000000063E-4	8.0129000000000246E-4	8.0111000000000028E-4	8.0093000000000048E-4	8.0076000000000246E-4	8.0058000000001264E-4	8.0040000000000026E-4	8.0023000000000247E-4	8.0005000000000766E-4	7.9988000000001593E-4	7.9971000000000534E-4	7.9953000000001736E-4	7.9936000000002151E-4	7.9919000000001753E-4	7.9902000000002071E-4	7.9885000000001673E-4	7.9868000000002013E-4	7.985100000000155E-4	7.9835000000001775E-4	7.9818000000002071E-4	7.9801000000001728E-4	7.9785000000001812E-4	7.9768000000002184E-4	7.975200000000229E-4	7.973600000000245E-4	7.9719000000002095E-4	7.9703000000002201E-4	7.9687000000001592E-4	7.9671000000000949E-4	7.9655000000000134E-4	7.9639000000001194E-4	7.9623000000001419E-4	7.9607000000001611E-4	7.9591000000001804E-4	7.9576000000001774E-4	7.9560000000001901E-4	7.9544000000000934E-4	7.9529000000000134E-4	7.9513000000002137E-4	7.9498000000002074E-4	7.9483000000002033E-4	7.9467000000002204E-4	7.9452000000002109E-4	7.9437000000002079E-4	7.9422000000002038E-4	7.9407000000001975E-4	7.9392000000002628E-4	7.9377000000001926E-4	7.9362000000002513E-4	7.9347000000001757E-4	7.9332000000002442E-4	7.9318000000002233E-4	7.9303000000002159E-4	7.9289000000001071E-4	7.9274000000000933E-4	7.9260000000001677E-4	7.9245000000000032E-4	7.9231000000001253E-4	7.9216000000002047E-4	7.9202000000001859E-4	7.9188000000001541E-4	7.9174000000001201E-4	7.9160000000001859E-4	7.9146000000001563E-4	7.9132000000002101E-4	7.9118000000001892E-4	7.9104000000001563E-4	7.9090000000002101E-4	7.9076000000001859E-4	7.9063000000002164E-4	7.9049000000000133E-4	7.9035000000001626E-4	7.9022000000001985E-4	7.9008000000001775E-4	7.8995000000001169E-4	7.8981000000000114E-4	7.8968000000001221E-4	7.8955000000000138E-4	7.8940999999999994E-4	7.8928000000000104E-4	7.89150000000012E-4	7.8902000000001526E-4	7.8889000000001062E-4	7.8876000000001421E-4	7.8863000000001726E-4	7.8850000000000534E-4	7.8837000000001652E-4	7.882400000000109E-4	7.8812000000002083E-4	7.8799000000001607E-4	7.8786000000001912E-4	7.8773000000001425E-4	7.8761000000001583E-4	7.8748000000000533E-4	7.8736000000002003E-4	7.8723000000001527E-4	7.8711000000001685E-4	7.8699000000000434E-4	7.8686000000001259E-4	7.8674000000000083E-4	7.8662000000001564E-4	7.8649999999999998E-4	7.8638000000000124E-4	7.8625000000000038E-4	7.8613000000001421E-4	7.8601000000000094E-4	7.8589000000000024E-4	7.8578000000000014E-4	7.8566000000001657E-4	7.8554000000000124E-4	7.8542000000000932E-4	7.853000000000121E-4	7.8519000000001112E-4	7.8507000000000934E-4	7.8495000000001374E-4	7.8484000000001244E-4	7.8472000000001435E-4	7.8461000000001294E-4	7.8449000000000021E-4	7.8438000000001366E-4	7.8426000000001524E-4	7.8415000000001361E-4	7.8404000000001231E-4	7.8393000000002023E-4	7.8381000000000934E-4	7.8370000000001173E-4	7.8359000000000534E-4	7.8348000000000133E-4	7.8337000000001792E-4	7.8326000000001727E-4	7.831500000000163E-4	7.8304000000001522E-4	7.8293000000001359E-4	7.8281999999999994E-4	7.8271000000000037E-4	7.8261000000000194E-4	7.8249999999999999E-4	7.8239000000000032E-4	7.8228000000000021E-4	7.8218000000000124E-4	7.8207000000001035E-4	7.8197000000001539E-4	7.8186000000001442E-4	7.8176000000000124E-4	7.8165000000001024E-4	7.8155000000000032E-4	7.8144000000000022E-4	7.8134000000000124E-4	7.8124000000000184E-4	7.811300000000155E-4	7.8103000000001273E-4	7.8093000000001756E-4	7.8083000000001479E-4	7.8073000000001137E-4	7.8063000000001728E-4	7.8053000000001364E-4	7.8042000000001191E-4	7.8032000000001858E-4	7.8023000000000534E-4	7.801300000000183E-4	7.8003000000001466E-4	7.7993000000002003E-4	7.7983000000001682E-4	7.7973000000001341E-4	7.796300000000191E-4	7.7954000000001323E-4	7.7944000000000114E-4	7.7934000000001583E-4	7.7925000000000834E-4	7.7915000000001566E-4	7.7906000000001901E-4	7.7896000000002275E-4	7.7887000000001851E-4	7.7877000000001531E-4	7.7868000000001791E-4	7.7858000000001503E-4	7.784900000000096E-4	7.7839000000001464E-4	7.78300000000018E-4	7.7821000000001224E-4	7.7812000000002308E-4	7.7802000000002074E-4	7.7793000000002312E-4	7.7784000000001834E-4	7.7775000000001302E-4	7.7766000000002375E-4	7.775700000000194E-4	7.7748000000001365E-4	7.7739000000001657E-4	7.7730000000001982E-4	7.772100000000145E-4	7.7712000000002457E-4	7.7703000000002044E-4	7.7694000000001545E-4	7.7685000000000124E-4	7.7675999999999993E-4	7.7668000000001352E-4	7.7659000000000538E-4	7.7650000000001123E-4	7.7642000000001192E-4	7.7633000000001517E-4	7.7624000000000594E-4	7.761600000000191E-4	7.7607000000001335E-4	7.7599000000001502E-4	7.7590000000001816E-4	7.7581000000000134E-4	7.7573000000001266E-4	7.7565000000001389E-4	7.7556000000001703E-4	7.7548000000000113E-4	7.7539000000000134E-4	7.7531000000001299E-4	7.7523000000001389E-4	7.7514000000001725E-4	7.7506000000001837E-4	7.7498000000001917E-4	7.7490000000002008E-4	7.7482000000002023E-4	7.7473000000001524E-4	7.7465000000001593E-4	7.7457000000001727E-4	7.7449000000000593E-4	7.7441000000000434E-4	7.7433000000001946E-4	7.7425000000001137E-4	7.7417000000002041E-4	7.7409000000001253E-4	7.740100000000142E-4	7.7393000000002281E-4	7.7386000000002138E-4	7.7378000000001459E-4	7.7370000000001517E-4	7.7362000000002367E-4	7.7354000000001753E-4	7.7347000000001535E-4	7.7339000000001626E-4	7.7331000000001749E-4	7.7323000000001872E-4	7.731600000000238E-4	7.7308000000001756E-4	7.7301000000001602E-4	7.7293000000001682E-4	7.7285000000000114E-4	7.7278000000000112E-4	7.7270000000000539E-4	7.7263000000001622E-4	7.7255000000000184E-4	7.7248000000000084E-4	7.7241000000000039E-4	7.7233000000001464E-4	7.7226000000001299E-4	7.7218000000001433E-4	7.7211000000001302E-4	7.7204000000001137E-4	7.7197000000001894E-4	7.7189000000000532E-4	7.7182000000001756E-4	7.7175000000000193E-4	7.7168000000001579E-4	7.7161000000001425E-4	7.7153000000001494E-4	7.7146000000001319E-4	7.7139000000001133E-4	7.7132000000001857E-4	7.7125000000000034E-4	7.7118000000001659E-4	7.7111000000001494E-4	7.7104000000001341E-4	7.7097000000002065E-4	7.7090000000001912E-4	7.7083000000001758E-4	7.7076000000001691E-4	7.7069000000001494E-4	7.7062000000002143E-4	7.7056000000001853E-4	7.7049000000000193E-4	7.7042000000001611E-4	7.7035000000001447E-4	7.7028000000000534E-4	7.7022000000001849E-4	7.7015000000001685E-4	7.7008000000001531E-4	7.7001000000001378E-4	7.6995000000000123E-4	7.6988000000000024E-4	7.6982000000001339E-4	7.6975000000000003E-4	7.6968000000000533E-4	7.6962000000001609E-4	7.6955000000000003E-4	7.6949000000000017E-4	7.6942000000000124E-4	7.6936000000001384E-4	7.6929000000000038E-4	7.6923000000000193E-4	7.6916000000001655E-4	7.6910000000001246E-4	7.6903000000001114E-4	7.6897000000001605E-4	7.689100000000124E-4	7.6884000000000533E-4	7.6878000000000103E-4	7.6872000000001168E-4	7.6865000000001112E-4	7.6859000000000139E-4	7.6853000000000934E-4	7.6847000000000113E-4	7.684100000000003E-4	7.6834000000001177E-4	7.6828000000000139E-4	7.6822000000001335E-4	7.6816000000001804E-4	7.6810000000001439E-4	7.6804000000000932E-4	7.6798000000001673E-4	7.6791000000001443E-4	7.6785000000000134E-4	7.6779000000000094E-4	7.6773000000001192E-4	7.6767000000001716E-4	7.6761000000001361E-4	7.6755000000000594E-4	7.6749000000000023E-4	7.6743000000000134E-4	7.6738000000001335E-4	7.6732000000001826E-4	7.6726000000001482E-4	7.6720000000000932E-4	7.6714000000001673E-4	7.6708000000001253E-4	7.6702000000001798E-4	7.6697000000001134E-4	7.6691000000000183E-4	7.6685000000000002E-4	7.6679000000000016E-4	7.6674000000000002E-4	7.6668000000000114E-4	7.6662000000001299E-4	7.665599999999999E-4	7.6651000000000019E-4	7.6645000000000001E-4	7.6640000000000009E-4	7.6634000000000023E-4	7.6627999999999993E-4	7.6623000000000023E-4	7.661700000000111E-4	7.6612000000001389E-4	7.6606000000000124E-4	7.6601000000000002E-4	7.6595000000000114E-4	7.6590000000001195E-4	7.6584000000000114E-4	7.6579000000000003E-4	7.6573000000000103E-4	7.6568000000000133E-4	7.6562000000001556E-4	7.6557000000000122E-4	7.6551000000000039E-4	7.6545999999999993E-4	7.6541000000000001E-4	7.6535000000000014E-4	7.6530000000000434E-4	7.652500000000002E-4	7.6519000000000034E-4	7.6514000000001137E-4	7.6509000000000039E-4	7.6504000000000123E-4	7.6498000000001308E-4	7.6493000000001673E-4	7.6488000000000532E-4	7.6483000000001245E-4	7.6478000000000104E-4	7.6472000000001137E-4	7.6467000000001503E-4	7.6462000000001727E-4	7.6457000000000933E-4	7.6452000000001429E-4	7.6447000000000103E-4	7.6441999999999992E-4	7.6437000000001323E-4	7.6431000000000133E-4	7.6426000000001226E-4	7.6421000000000084E-4	7.6416000000001827E-4	7.6411000000000534E-4	7.6406000000001464E-4	7.6401000000000539E-4	7.6396000000001989E-4	7.6391000000001423E-4	7.6387000000001479E-4	7.6382000000001682E-4	7.6377000000001126E-4	7.6372000000001329E-4	7.6367000000001728E-4	7.6362000000001942E-4	7.6357000000001321E-4	7.6352000000001643E-4	7.6348000000000138E-4	7.6343000000001068E-4	7.6338000000001325E-4	7.6333000000001594E-4	7.6328000000000994E-4	7.6324000000000834E-4	7.6319000000001297E-4	7.6314000000001631E-4	7.6309000000000034E-4	7.6305000000000134E-4	7.6300000000001323E-4	7.6295000000000139E-4	7.6291000000000032E-4	7.6286000000001027E-4	7.6280999999999994E-4	7.6277000000000029E-4	7.6272000000000113E-4	7.6267000000000533E-4	7.6263000000000134E-4	7.6258000000000012E-4	7.6254000000000003E-4	7.6249E-4	7.6244000000000008E-4	7.624000000000001E-4	7.6235000000000029E-4	7.6231000000000031E-4	7.6226000000000104E-4	7.6221999999999998E-4	7.621700000000109E-4	7.6213000000001124E-4	7.6207999999999994E-4	7.6204000000000094E-4	7.6199000000000123E-4	7.619500000000096E-4	7.6191000000000594E-4	7.6186000000001187E-4	7.6182000000001222E-4	7.6177000000000102E-4	7.6173000000000093E-4	7.6169000000000139E-4	Time (s)

Drainage velocity (mm/s)
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Liquid holdup


Holdup minus holdup of saturated particles - Experimental	0	15	30	45	60	75	90	105	120	135	150	165	180	195	210	225	240	255	270	285	300	315	330	345	360	375	390	405	420	435	450	465	480	495	510	525	540	555	570	585	600	615	630	645	660	675	690	705	720	735	750	765	780	795	810	825	840	855	870	885	900	930	960	990	1020	1050	1080	1110	1140	1170	1200	1230	1260	1290	1320	1350	1380	1410	1440	1470	1500	1530	1560	1590	1620	1650	1680	1710	1740	1770	1800	1860	1920	1980	2040	2100	2160	2220	2280	2340	2400	5.2737967197229278E-2	5.124746185742042E-2	4.9886565677595064E-2	4.8784887817736808E-2	4.794242827784459E-2	4.7294382477927915E-2	4.6711141258002783E-2	4.6257509198061146E-2	4.58686817181111E-2	4.5544658818152485E-2	4.5285440498185892E-2	4.4961417598227381E-2	4.4702199278260787E-2	4.4507785538285723E-2	4.4313371798310713E-2	4.4118958058335662E-2	4.3924544318360563E-2	4.3730130578385526E-2	4.3535716838410503E-2	4.3406107678426974E-2	4.3276498518443902E-2	4.3146889358460387E-2	4.2952475618485357E-2	4.2822866458501835E-2	4.2693257298518791E-2	4.2563648138535283E-2	4.2434038978551733E-2	4.230442981856871E-2	4.2239625238576696E-2	4.2110016078593639E-2	4.2045211498601645E-2	4.1915602338618574E-2	4.1850797758627073E-2	4.1721188598643502E-2	4.1656384018651987E-2	4.1591579438660008E-2	4.146197027867695E-2	4.1332361118693449E-2	4.1267556538701906E-2	4.1202751958709913E-2	4.1073142798726842E-2	4.1008338218734869E-2	4.0878729058751812E-2	4.0813924478759832E-2	4.0749119898768289E-2	4.0684315318776761E-2	4.0619510738784767E-2	4.0554706158793266E-2	4.0489901578801724E-2	4.0425096998809723E-2	4.0360292418818215E-2	4.02306832588347E-2	4.016587867884313E-2	4.0101074098851622E-2	4.0036269518859628E-2	3.99714649388681E-2	3.9906660358876571E-2	3.9841855778884598E-2	3.9777051198893049E-2	3.9712246618901541E-2	3.9582637458918012E-2	3.9453028298934489E-2	3.9323419138951425E-2	3.919380997896791E-2	3.9064200818984401E-2	3.8934591659001344E-2	3.8804982499017815E-2	3.87401779190263E-2	3.8610568759042764E-2	3.8480959599059249E-2	3.8416155019067734E-2	3.8351350439076191E-2	3.8286545859084205E-2	3.8156936699101147E-2	3.8092132119109168E-2	3.7962522959126097E-2	3.7897718379134131E-2	3.7832913799142588E-2	3.7703304639159538E-2	3.7573695479176022E-2	3.7444086319192479E-2	3.7379281739200951E-2	3.7314477159209436E-2	3.7184867999225921E-2	3.7055258839242391E-2	3.6990454259250842E-2	3.6925649679259348E-2	3.6796040519275826E-2	3.673123593928429E-2	3.6666431359292283E-2	3.6601626779300782E-2	3.6472017619317267E-2	3.6277603879342209E-2	3.6147994719359158E-2	3.6018385559375636E-2	3.58887763993921E-2	3.5694362659417063E-2	3.5564753499433992E-2	3.5435144339450476E-2	3.5240730599475446E-2	3.511112143949191E-2	Simulated	0	2.0884999999999998	4.1769999999999996	6.2653999999999996	8.3539000000000048	10.442	12.531000000000001	14.619	16.707999999999991	18.795999999999992	20.885000000000002	22.972999999999988	25.061999999999994	27.150000000000006	29.239000000000001	31.327000000000005	33.416000000000004	35.504000000000005	37.593000000000011	39.681000000000004	41.77	43.857999999999997	45.947000000000003	48.035000000000011	50.124000000000002	52.212000000000003	54.3	56.389000000000003	58.477000000000004	60.566000000000003	62.654000000000003	64.742999999999995	66.831000000000003	68.92	71.007999999999996	73.096999999999994	75.185000000000002	77.274000000000001	79.361999999999995	81.450999999999993	83.539000000000001	85.627999999999986	87.715999999999994	89.804999999999993	91.893000000000001	93.982000000000014	96.07	98.158999999999978	100.25	102.34	104.42	106.51	108.6	110.69	112.78	114.86999999999999	116.95	119.04	121.13	123.22	125.31	127.4	129.49	131.57	133.66	135.75	137.84	139.93	142.02000000000001	144.10999999999999	146.19	148.28	150.37	152.46	154.55000000000001	156.63999999999999	158.72	160.81	162.9	164.99	167.08	169.17	171.26	173.34	175.43	177.52	179.60999999999999	181.7	183.79	185.87	187.96	190.05	192.14	194.23	196.32000000000005	198.41	200.49	202.58	204.67	206.76	208.85000000000005	210.94	213.02	215.10999999999999	217.2	219.29	221.38000000000005	223.47	225.56	227.64	229.73	231.82000000000005	233.91	236	238.09	240.18	242.26	244.35000000000005	246.44	248.53	250.62	252.70999999999998	254.79	256.88	258.97000000000003	261.06	263.14999999999998	265.24	267.33	269.41000000000003	271.5	273.58999999999986	275.68	277.77	279.86	281.94	284.02999999999986	286.12	288.20999999999987	290.3	292.39	294.4799999999999	296.56	298.64999999999998	300.74	302.83	304.9199999999999	307.01	309.10000000000002	311.18	313.27	315.36	317.45	319.54000000000002	321.63	323.70999999999987	325.8	327.89	329.9799999999999	332.07	334.16	336.25	338.33	340.4199999999999	342.51	344.6	346.69	348.78	350.86	352.95	355.04	357.13	359.21999999999991	361.31	363.4	365.4799999999999	367.57	369.66	371.75	373.84000000000009	375.92999999999989	378.01	380.1	382.19	384.28	386.37	388.46	390.55	392.63	394.71999999999991	396.81	398.9	400.9899999999999	403.08	405.17	407.25	409.34000000000009	411.42999999999989	413.52	415.61	417.7	419.78	421.87	423.96	426.05	428.1400000000001	430.2299999999999	432.32	434.4	436.4899999999999	438.58	440.67	442.76	444.85	446.92999999999989	449.02	451.11	453.2	455.28999999999991	457.38	459.46999999999991	461.55	463.6400000000001	465.7299999999999	467.82	469.90999999999991	472	474.08	476.17	478.26	480.35	482.44	484.53	486.62	488.7	490.78999999999991	492.88	494.96999999999991	497.06	499.15000000000009	501.24	503.32	505.40999999999991	507.5	509.59	511.68	513.77000000000021	515.8499999999998	517.93999999999983	520.03	522.12	524.21	526.29999999999995	528.39	530.47	532.55999999999972	534.65	536.74	538.82999999999981	540.91999999999996	543	545.09	547.17999999999995	549.27000000000021	551.35999999999979	553.44999999999982	555.54	557.62	559.71	561.79999999999995	563.89	565.98	568.07000000000005	570.16	572.24	574.32999999999981	576.41999999999996	578.51	580.6	582.69000000000005	584.77000000000021	586.85999999999979	588.94999999999982	591.04	593.13	595.22	597.30999999999972	599.39	601.48	603.57000000000005	605.66	607.75	609.8399999999998	611.91999999999996	614.01	616.1	618.19000000000005	620.2800000000002	622.37	624.45999999999981	626.54	628.63	630.72	632.80999999999972	634.9	636.99	639.07000000000005	641.16	643.25	645.3399999999998	647.42999999999972	649.52	651.61	653.69000000000005	655.7800000000002	657.87	659.95999999999981	662.05	664.14	666.23	668.31	670.4	672.49	674.58	676.67000000000019	678.76	680.8399999999998	682.93	685.02	687.11	689.2	691.29000000000019	693.38	695.45999999999981	697.55	699.64	701.73	703.81999999999982	705.91	707.99	710.08	712.17000000000019	714.26	716.3499999999998	718.43999999999983	720.53	722.61	724.7	726.79000000000019	728.88	730.97	733.06	735.15	737.23	739.31999999999982	741.41	743.5	745.59	747.68000000000018	749.76	751.8499999999998	753.93999999999983	756.03	758.12	760.21	762.3	764.38	766.47	768.56	770.65	772.74	774.82999999999981	776.91	779	781.09	783.18000000000018	785.27000000000021	787.35999999999979	789.44999999999982	791.53	793.62	795.71	797.8	799.89	801.98	804.06	806.15	808.24	810.32999999999981	812.42	814.51	816.6	818.68000000000018	820.77000000000021	822.85999999999979	824.94999999999982	827.04	829.13	831.22	833.3	835.39	837.48	839.57	841.66	843.75	845.82999999999981	847.92	850.01	852.1	854.19	856.2800000000002	858.37	860.44999999999982	862.54	864.63	866.72	868.81	870.9	872.98	875.07	877.16	879.25	881.3399999999998	883.43	885.52	887.6	889.69	891.7800000000002	893.87	895.95999999999981	898.05	900.13	902.22	904.31	906.4	908.49	910.58	912.67000000000019	914.75	916.8399999999998	918.93	921.02	923.11	925.2	927.29000000000019	929.37	931.45999999999981	933.55	935.64	937.73	939.81999999999982	941.9	943.99	946.08	948.17000000000019	950.26	952.3499999999998	954.43999999999983	956.52	958.61	960.7	962.79000000000019	964.88	966.97	969.05	971.14	973.23	975.31999999999982	977.41	979.5	981.59	983.67000000000019	985.76	987.8499999999998	989.93999999999983	992.03	994.12	996.21	998.29000000000019	1000.4	1002.5	1004.6	1006.6	1008.7	1010.8	1012.9	1015	1017.1	1019.2	1021.3	1023.4	1025.4000000000001	1027.5	1029.5999999999999	1031.7	1033.8	1035.9000000000001	1038	1040.0999999999999	1042.2	1044.2	1046.3	1048.4000000000001	1050.5	1052.5999999999999	1054.7	1056.8	1058.9000000000001	1060.9000000000001	1063	1065.0999999999999	1067.2	1069.3	1071.4000000000001	1073.5	1075.5999999999999	1077.7	1079.7	1081.8	1083.9000000000001	1086	1088.0999999999999	1090.2	1092.3	1094.4000000000001	1096.5	1098.5	1100.5999999999999	1102.7	1104.8	1106.9000000000001	1109	1111.0999999999999	1113.2	1115.2	1117.3	1119.4000000000001	1121.5	1123.5999999999999	1125.7	1127.8	1129.9000000000001	1132	1134	1136.0999999999999	1138.2	1140.3	1142.4000000000001	1144.5	1146.5999999999999	1148.7	1150.8	1152.8	1154.9000000000001	1157	1159.0999999999999	1161.2	1163.3	1165.4000000000001	1167.5	1169.5	1171.5999999999999	1173.7	1175.8	1177.9000000000001	1180	1182.0999999999999	1184.2	1186.3	1188.3	1190.4000000000001	1192.5	1194.5999999999999	1196.7	1198.8	1200.9000000000001	1203	1205.0999999999999	1207.0999999999999	1209.2	1211.3	1213.4000000000001	1215.5	1217.5999999999999	1219.7	1221.8	1223.8	1225.9000000000001	1228	1230.0999999999999	1232.2	1234.3	1236.4000000000001	1238.5	1240.5999999999999	1242.5999999999999	1244.7	1246.8	1248.9000000000001	1251	1253.0999999999999	1255.2	1257.3	1259.4000000000001	1261.4000000000001	1263.5	1265.5999999999999	1267.7	1269.8	1271.9000000000001	1274	1276.0999999999999	1278.0999999999999	1280.2	1282.3	1284.4000000000001	1286.5	1288.5999999999999	1290.7	1292.8	1294.9000000000001	1296.9000000000001	1299	1301.0999999999999	1303.2	1305.3	1307.4000000000001	1309.5	1311.6	1313.7	1315.7	1317.8	1319.9	1322	1324.1	1326.2	1328.3	1330.4	1332.5	1334.5	1336.6	1338.7	1340.8	1342.9	1345	1347.1	1349.2	1351.2	1353.3	1355.4	1357.5	1359.6	1361.7	1363.8	1365.9	1368	1370	1372.1	1374.2	1376.3	1378.4	1380.5	1382.6	1384.7	1386.8	1388.8	1390.9	1393	1395.1	1397.2	1399.3	1401.4	1403.5	1405.5	1407.6	1409.7	1411.8	1413.9	1416	1418.1	1420.2	1422.3	1424.3	1426.4	1428.5	1430.6	1432.7	1434.8	1436.9	1439	1441.1	1443.1	1445.2	1447.3	1449.4	1451.5	1453.6	1455.7	1457.8	1459.8	1461.9	1464	1466.1	1468.2	1470.3	1472.4	1474.5	1476.6	1478.6	1480.7	1482.8	1484.9	1487	1489.1	1491.2	1493.3	1495.4	1497.4	1499.5	1501.6	1503.7	1505.8	1507.9	1510	1512.1	1514.1	1516.2	1518.3	1520.4	1522.5	1524.6	1526.7	1528.8	1530.9	1532.9	1535	1537.1	1539.2	1541.3	1543.4	1545.5	1547.6	1549.7	1551.7	1553.8	1555.9	1558	1560.1	1562.2	1564.3	1566.4	1568.4	1570.5	1572.6	1574.7	1576.8	1578.9	1581	1583.1	1585.2	1587.2	1589.3	1591.4	1593.5	1595.6	1597.7	1599.8	1601.9	1604	1606	1608.1	1610.2	1612.3	1614.4	1616.5	1618.6	1620.7	1622.7	1624.8	1626.9	1629	1631.1	1633.2	1635.3	1637.4	1639.5	1641.5	1643.6	1645.7	1647.8	1649.9	1652	1654.1	1656.2	1658.3	1660.3	1662.4	1664.5	1666.6	1668.7	1670.8	1672.9	1675	1677	1679.1	1681.2	1683.3	1685.4	1687.5	1689.6	1691.7	1693.8	1695.8	1697.9	1700	1702.1	1704.2	1706.3	1708.4	1710.5	1712.6	1714.6	1716.7	1718.8	1720.9	1723	1725.1	1727.2	1729.3	1731.4	1733.4	1735.5	1737.6	1739.7	1741.8	1743.9	1746	1748.1	1750.1	1752.2	1754.3	1756.4	1758.5	1760.6	1762.7	1764.8	1766.9	1768.9	1771	1773.1	1775.2	1777.3	1779.4	1781.5	1783.6	1785.7	1787.7	1789.8	1791.9	1794	1796.1	1798.2	1800.3	1802.4	1804.4	1806.5	1808.6	1810.7	1812.8	1814.9	1817	1819.1	1821.2	1823.2	1825.3	1827.4	1829.5	1831.6	1833.7	1835.8	1837.9	1840	1842	1844.1	1846.2	1848.3	1850.4	1852.5	1854.6	1856.7	1858.7	1860.8	1862.9	1865	1867.1	1869.2	1871.3	1873.4	1875.5	1877.5	1879.6	1881.7	1883.8	1885.9	1888	1890.1	1892.2	1894.3	1896.3	1898.4	1900.5	1902.6	1904.7	1906.8	1908.9	1911	1913	1915.1	1917.2	1919.3	1921.4	1923.5	1925.6	1927.7	1929.8	1931.8	1933.9	1936	1938.1	1940.2	1942.3	1944.4	1946.5	1948.6	1950.6	1952.7	1954.8	1956.9	1959	1961.1	1963.2	1965.3	1967.3	1969.4	1971.5	1973.6	1975.7	1977.8	1979.9	1982	1984.1	1986.1	1988.2	1990.3	1992.4	1994.5	1996.6	1998.7	2000.8	2002.9	2004.9	2007	2009.1	2011.2	2013.3	2015.4	2017.5	2019.6	2021.6	2023.7	2025.8	2027.9	2030	2032.1	2034.2	2036.3	2038.4	2040.4	2042.5	2044.6	2046.7	2048.8000000000002	2050.9	2053	2055.1	2057.1999999999998	2059.1999999999998	2061.3000000000002	2063.4	2065.5	2067.6	2069.6999999999998	2071.8000000000002	2073.9	2075.9	2078	2080.1	2082.1999999999998	2084.3000000000002	2086.4	2088.5	2090.6	2092.6999999999998	2094.6999999999998	2096.8000000000002	2098.9	2101	2103.1	2105.1999999999998	2107.3000000000002	2109.4	2111.5	2113.5	2115.6	2117.6999999999998	2119.8000000000002	2121.9	2124	2126.1	2128.1999999999998	2130.1999999999998	2132.3000000000002	2134.4	2136.5	2138.6	2140.6999999999998	2142.8000000000002	2144.9	2147	2149	2151.1	2153.1999999999998	2155.3000000000002	2157.4	2159.5	2161.6	2163.6999999999998	2165.8000000000002	2167.8000000000002	2169.9	2172	2174.1	2176.1999999999998	2178.3000000000002	2180.4	2182.5	2184.6	2186.6	2188.6999999999998	2190.8000000000002	2192.9	2195	2197.1	2199.1999999999998	2201.3000000000002	2203.3000000000002	2205.4	2207.5	2209.6	2211.6999999999998	2213.8000000000002	2215.9	2218	2220.1	2222.1	2224.1999999999998	2226.3000000000002	2228.4	2230.5	2232.6	2234.6999999999998	2236.8000000000002	2238.9	2240.9	2243	2245.1	2247.1999999999998	2249.3000000000002	2251.4	2253.5	2255.6	2257.6	2259.6999999999998	2261.8000000000002	2263.9	2266	2268.1	2270.1999999999998	2272.3000000000002	2274.4	2276.4	2278.5	2280.6	2282.6999999999998	2284.8000000000002	2286.9	2289	2291.1	2293.1999999999998	2295.1999999999998	2297.3000000000002	2299.4	2301.5	2303.6	2305.6999999999998	2307.8000000000002	2309.9	2311.9	2314	2316.1	2318.1999999999998	2320.3000000000002	2322.4	2324.5	2326.6	2328.6999999999998	2330.6999999999998	2332.8000000000002	2334.9	2337	2339.1	2341.1999999999998	2343.3000000000002	2345.4	2347.5	2349.5	2351.6	2353.6999999999998	2355.8000000000002	2357.9	2360	2362.1	2364.1999999999998	2366.1999999999998	2368.3000000000002	2370.4	2372.5	2374.6	2376.6999999999998	2378.8000000000002	2380.9	2383	2385	2387.1	2389.1999999999998	2391.3000000000002	2393.4	2395.5	2397.6	2399.6999999999998	2401.8000000000002	5.2737967197229278E-2	5.2528000000000012E-2	5.2318000000000024E-2	5.2108000000000002E-2	5.189700000000002E-2	5.1686999999999997E-2	5.1477000000000002E-2	5.1267E-2	5.1057000000000012E-2	5.0847000000000003E-2	5.0637000000000001E-2	5.0425999999999999E-2	5.0215999999999997E-2	5.0006000000000016E-2	4.9797000000000036E-2	4.958700000000002E-2	4.9379000000000013E-2	4.9172000000000014E-2	4.8967000000000004E-2	4.8765000000000003E-2	4.8565999999999998E-2	4.8370999999999997E-2	4.8180000000000001E-2	4.7994000000000016E-2	4.7813000000000029E-2	4.7637000000000013E-2	4.7467000000000023E-2	4.7303000000000019E-2	4.7143999999999998E-2	4.6989999999999997E-2	4.6842000000000002E-2	4.6698999999999997E-2	4.6561999999999999E-2	4.6428999999999998E-2	4.6302000000000017E-2	4.6177999999999997E-2	4.6059999999999997E-2	4.5945E-2	4.5835000000000001E-2	4.5729000000000013E-2	4.5626E-2	4.5527000000000012E-2	4.5431000000000013E-2	4.5338000000000017E-2	4.5248999999999984E-2	4.5162000000000022E-2	4.5078E-2	4.4997000000000023E-2	4.491800000000002E-2	4.4842000000000021E-2	4.476800000000003E-2	4.469600000000002E-2	4.4627000000000014E-2	4.4559000000000001E-2	4.4493000000000026E-2	4.4430000000000011E-2	4.4368000000000019E-2	4.430700000000002E-2	4.4247999999999996E-2	4.4191000000000015E-2	4.4136000000000022E-2	4.4081000000000016E-2	4.4028000000000012E-2	4.3977000000000002E-2	4.3926000000000014E-2	4.3876999999999999E-2	4.3829E-2	4.3782000000000022E-2	4.3736000000000011E-2	4.3692000000000016E-2	4.3647999999999985E-2	4.3604999999999998E-2	4.3563000000000004E-2	4.3521999999999984E-2	4.3482000000000014E-2	4.3443000000000002E-2	4.3404000000000012E-2	4.3367000000000017E-2	4.3330000000000014E-2	4.3293000000000012E-2	4.3257999999999998E-2	4.3222999999999998E-2	4.3188999999999998E-2	4.3154999999999999E-2	4.3122000000000001E-2	4.3090000000000003E-2	4.3057999999999999E-2	4.3027000000000003E-2	4.299600000000002E-2	4.2966000000000011E-2	4.2936000000000016E-2	4.2907000000000015E-2	4.2878000000000013E-2	4.2849999999999999E-2	4.2821999999999999E-2	4.2795000000000021E-2	4.2768000000000021E-2	4.2742000000000016E-2	4.2715000000000017E-2	4.2689999999999999E-2	4.2664000000000014E-2	4.2639000000000003E-2	4.2615E-2	4.2590000000000017E-2	4.2567000000000015E-2	4.2543000000000004E-2	4.2520000000000002E-2	4.2497000000000021E-2	4.2474000000000012E-2	4.2452000000000011E-2	4.2430000000000016E-2	4.2408000000000015E-2	4.2386000000000021E-2	4.2365000000000021E-2	4.2344000000000014E-2	4.232300000000002E-2	4.2303000000000021E-2	4.2283000000000001E-2	4.2263000000000016E-2	4.2243000000000003E-2	4.2223000000000004E-2	4.2203999999999998E-2	4.2185E-2	4.2166000000000016E-2	4.2147000000000004E-2	4.2129E-2	4.2111000000000003E-2	4.2093000000000019E-2	4.2075000000000001E-2	4.2057000000000004E-2	4.2040000000000001E-2	4.2021999999999997E-2	4.2005000000000001E-2	4.1987999999999998E-2	4.1970999999999987E-2	4.1954999999999999E-2	4.1938000000000003E-2	4.1922000000000001E-2	4.1905999999999985E-2	4.1889999999999997E-2	4.1874000000000001E-2	4.1857999999999999E-2	4.1841999999999983E-2	4.1827000000000003E-2	4.1811000000000001E-2	4.1796000000000021E-2	4.1780999999999999E-2	4.1766000000000018E-2	4.1751000000000003E-2	4.1737000000000003E-2	4.1722000000000016E-2	4.1708000000000002E-2	4.1693000000000001E-2	4.167899999999998E-2	4.1664999999999987E-2	4.1650999999999987E-2	4.1637E-2	4.1623E-2	4.1610000000000001E-2	4.1596000000000015E-2	4.1583000000000002E-2	4.1569000000000002E-2	4.1556000000000003E-2	4.1542999999999997E-2	4.1529999999999984E-2	4.1517000000000012E-2	4.1503999999999999E-2	4.1491E-2	4.1477999999999987E-2	4.1465000000000002E-2	4.1453000000000004E-2	4.1439999999999998E-2	4.1428E-2	4.1416000000000015E-2	4.1403000000000002E-2	4.1391000000000004E-2	4.1378999999999999E-2	4.1367000000000015E-2	4.1355000000000003E-2	4.1342999999999998E-2	4.1332000000000015E-2	4.1320000000000003E-2	4.1308000000000004E-2	4.1297E-2	4.1284999999999995E-2	4.1273999999999984E-2	4.1262E-2	4.1250999999999996E-2	4.1239999999999985E-2	4.1227999999999987E-2	4.1217000000000004E-2	4.1206E-2	4.1195000000000002E-2	4.1183999999999998E-2	4.1172999999999987E-2	4.1161999999999997E-2	4.1152000000000001E-2	4.1140999999999983E-2	4.113E-2	4.1119999999999997E-2	4.1108999999999986E-2	4.1099000000000004E-2	4.1088E-2	4.1077999999999996E-2	4.1067000000000013E-2	4.1057000000000003E-2	4.1047E-2	4.1036000000000003E-2	4.1026E-2	4.1015999999999997E-2	4.1006000000000015E-2	4.0996000000000019E-2	4.0986000000000015E-2	4.0975999999999985E-2	4.0966000000000016E-2	4.0955999999999999E-2	4.0946000000000003E-2	4.0937000000000015E-2	4.0927000000000012E-2	4.0917000000000016E-2	4.0908E-2	4.0898000000000018E-2	4.0888000000000015E-2	4.0878999999999999E-2	4.0869000000000003E-2	4.0860000000000014E-2	4.0849999999999997E-2	4.0840999999999995E-2	4.0832000000000021E-2	4.0821999999999997E-2	4.0813000000000016E-2	4.0804000000000014E-2	4.0795000000000019E-2	4.0785000000000002E-2	4.0776000000000014E-2	4.0767000000000019E-2	4.0758000000000003E-2	4.0749E-2	4.0740000000000012E-2	4.0731000000000003E-2	4.0722000000000015E-2	4.071300000000002E-2	4.0704000000000004E-2	4.0695000000000002E-2	4.0686000000000014E-2	4.0677999999999999E-2	4.0668999999999997E-2	4.0660000000000002E-2	4.0651E-2	4.0642999999999999E-2	4.0634000000000003E-2	4.0624999999999988E-2	4.0617000000000014E-2	4.0607999999999998E-2	4.0599999999999997E-2	4.0591000000000002E-2	4.0583000000000015E-2	4.0573999999999999E-2	4.0565999999999998E-2	4.0557000000000003E-2	4.0548999999999995E-2	4.054E-2	4.0531999999999999E-2	4.0523999999999998E-2	4.0515000000000002E-2	4.0507000000000001E-2	4.0499000000000014E-2	4.0491000000000013E-2	4.0481999999999997E-2	4.0474000000000003E-2	4.0466000000000023E-2	4.0458000000000001E-2	4.0450000000000014E-2	4.0441999999999999E-2	4.0434000000000012E-2	4.0425000000000003E-2	4.0417000000000015E-2	4.0409E-2	4.0400999999999999E-2	4.0393000000000019E-2	4.0385000000000004E-2	4.0377000000000003E-2	4.0370000000000003E-2	4.036200000000003E-2	4.0354000000000015E-2	4.0346000000000014E-2	4.0338000000000013E-2	4.0329999999999998E-2	4.0321999999999997E-2	4.0315000000000017E-2	4.0307000000000016E-2	4.0299000000000001E-2	4.0291E-2	4.0284E-2	4.0275999999999985E-2	4.0267999999999998E-2	4.0259999999999983E-2	4.0253000000000004E-2	4.0244999999999996E-2	4.0237000000000002E-2	4.0230000000000002E-2	4.0222000000000001E-2	4.0215000000000001E-2	4.0207E-2	4.02E-2	4.0191999999999999E-2	4.0184999999999998E-2	4.0176999999999997E-2	4.0169999999999997E-2	4.0162000000000017E-2	4.0154999999999996E-2	4.0147000000000002E-2	4.0139999999999995E-2	4.0132000000000015E-2	4.0124999999999987E-2	4.0118000000000015E-2	4.0110000000000014E-2	4.0103000000000014E-2	4.0095000000000013E-2	4.0088000000000013E-2	4.0081000000000012E-2	4.0073999999999999E-2	4.0066000000000011E-2	4.0058999999999997E-2	4.0051999999999997E-2	4.0043999999999996E-2	4.0037000000000017E-2	4.0030000000000003E-2	4.0023000000000003E-2	4.0016000000000024E-2	4.0008000000000002E-2	4.0001000000000002E-2	3.9994000000000002E-2	3.9987000000000002E-2	3.9980000000000002E-2	3.9973000000000015E-2	3.9965000000000001E-2	3.9958E-2	3.9951E-2	3.9944E-2	3.9937000000000014E-2	3.993E-2	3.9923E-2	3.9916E-2	3.9909E-2	3.9902E-2	3.9895000000000014E-2	3.9888000000000014E-2	3.9881000000000014E-2	3.9874000000000014E-2	3.9867000000000014E-2	3.986E-2	3.9853000000000006E-2	3.9846000000000006E-2	3.9838999999999999E-2	3.9832000000000006E-2	3.9824999999999999E-2	3.9817999999999999E-2	3.9812E-2	3.9805000000000014E-2	3.9798E-2	3.9791E-2	3.9784E-2	3.9777000000000014E-2	3.977E-2	3.9764000000000001E-2	3.9757000000000001E-2	3.9750000000000001E-2	3.9743000000000001E-2	3.9736E-2	3.9730000000000001E-2	3.9723000000000001E-2	3.9716000000000001E-2	3.9709000000000001E-2	3.9703000000000002E-2	3.9696000000000002E-2	3.9689000000000002E-2	3.9682000000000002E-2	3.9676000000000017E-2	3.966900000000001E-2	3.9662000000000003E-2	3.9656000000000004E-2	3.9649000000000011E-2	3.9642000000000011E-2	3.9636000000000012E-2	3.9628999999999998E-2	3.9622000000000004E-2	3.9616000000000005E-2	3.9608999999999998E-2	3.9602000000000005E-2	3.9595999999999999E-2	3.9588999999999999E-2	3.9583000000000014E-2	3.9576E-2	3.9569E-2	3.9563000000000001E-2	3.9556000000000001E-2	3.9550000000000002E-2	3.9543000000000002E-2	3.9537000000000017E-2	3.953000000000001E-2	3.9523999999999997E-2	3.9516999999999997E-2	3.9510999999999998E-2	3.9504000000000004E-2	3.9496999999999997E-2	3.9490999999999998E-2	3.9484000000000005E-2	3.9478000000000006E-2	3.9472000000000014E-2	3.9465E-2	3.9459000000000001E-2	3.9452000000000001E-2	3.9446000000000002E-2	3.9439000000000016E-2	3.9433000000000017E-2	3.9426000000000003E-2	3.9420000000000004E-2	3.9413000000000011E-2	3.9406999999999998E-2	3.9400999999999999E-2	3.9393999999999998E-2	3.9387999999999999E-2	3.9380999999999999E-2	3.9375000000000014E-2	3.9369000000000001E-2	3.9362000000000001E-2	3.9356000000000002E-2	3.9350000000000003E-2	3.934300000000001E-2	3.9336999999999997E-2	3.9329999999999997E-2	3.9323999999999998E-2	3.9317999999999999E-2	3.9310999999999999E-2	3.9305000000000014E-2	3.9299000000000001E-2	3.9292000000000001E-2	3.9286000000000001E-2	3.9280000000000002E-2	3.927400000000001E-2	3.926700000000001E-2	3.9260999999999997E-2	3.9254999999999998E-2	3.9248000000000005E-2	3.9242000000000006E-2	3.9236000000000014E-2	3.9230000000000015E-2	3.9223000000000001E-2	3.9217000000000002E-2	3.9211000000000017E-2	3.9205000000000011E-2	3.9197999999999997E-2	3.9191999999999998E-2	3.9185999999999999E-2	3.918E-2	3.9172999999999999E-2	3.9167E-2	3.9161000000000001E-2	3.9155000000000002E-2	3.914900000000001E-2	3.9142000000000003E-2	3.9136000000000004E-2	3.9129999999999998E-2	3.9123999999999999E-2	3.9118E-2	3.9111E-2	3.9105000000000001E-2	3.9099000000000002E-2	3.9093000000000017E-2	3.9087000000000011E-2	3.9081000000000012E-2	3.9074000000000012E-2	3.9067999999999999E-2	3.9061999999999999E-2	3.9056E-2	3.9050000000000001E-2	3.9044000000000002E-2	3.903800000000001E-2	3.9032000000000011E-2	3.9024999999999997E-2	3.9018999999999998E-2	3.9012999999999999E-2	3.9007000000000014E-2	3.9001000000000015E-2	3.8995000000000002E-2	3.898900000000001E-2	3.8982999999999997E-2	3.8976999999999998E-2	3.8970999999999999E-2	3.8963999999999999E-2	3.8958E-2	3.8952000000000001E-2	3.8946000000000001E-2	3.8940000000000002E-2	3.8934000000000003E-2	3.8927999999999997E-2	3.8921999999999998E-2	3.8915999999999999E-2	3.891E-2	3.8904000000000001E-2	3.8898000000000002E-2	3.889200000000001E-2	3.8886000000000004E-2	3.8880000000000005E-2	3.8874000000000006E-2	3.8868E-2	3.8862000000000001E-2	3.8856000000000002E-2	3.885000000000001E-2	3.884400000000001E-2	3.8838000000000011E-2	3.8832000000000005E-2	3.8825999999999999E-2	3.882E-2	3.8814000000000001E-2	3.8808000000000002E-2	3.880200000000001E-2	3.8795999999999997E-2	3.8789999999999998E-2	3.8783999999999999E-2	3.8778E-2	3.8772000000000001E-2	3.8765999999999995E-2	3.8760000000000003E-2	3.8753999999999997E-2	3.8747999999999998E-2	3.8741999999999999E-2	3.8736E-2	3.8730000000000001E-2	3.8724000000000001E-2	3.8717999999999995E-2	3.8712000000000003E-2	3.8705999999999997E-2	3.8700999999999999E-2	3.8695E-2	3.8689000000000001E-2	3.8683000000000002E-2	3.8677000000000017E-2	3.8671000000000011E-2	3.8664999999999998E-2	3.8658999999999999E-2	3.8653000000000014E-2	3.8647000000000015E-2	3.8641000000000002E-2	3.8635000000000017E-2	3.8629999999999998E-2	3.8623999999999999E-2	3.8618E-2	3.8612E-2	3.8606000000000001E-2	3.8600000000000002E-2	3.8594000000000003E-2	3.8587999999999997E-2	3.8582999999999999E-2	3.8577E-2	3.8571000000000001E-2	3.8565000000000002E-2	3.8559000000000003E-2	3.8552999999999997E-2	3.8546999999999998E-2	3.8540999999999999E-2	3.8536000000000001E-2	3.8530000000000002E-2	3.8524000000000003E-2	3.8517999999999997E-2	3.8511999999999998E-2	3.8505999999999999E-2	3.8501000000000001E-2	3.8495000000000001E-2	3.8489000000000002E-2	3.848300000000001E-2	3.8477000000000011E-2	3.8470999999999998E-2	3.8466E-2	3.8460000000000001E-2	3.8454000000000002E-2	3.8448000000000003E-2	3.8442000000000004E-2	3.8436000000000005E-2	3.8431000000000014E-2	3.8425000000000001E-2	3.8419000000000002E-2	3.841300000000001E-2	3.8406999999999997E-2	3.8402000000000006E-2	3.8396E-2	3.8390000000000001E-2	3.8384000000000001E-2	3.837900000000001E-2	3.8372999999999997E-2	3.8366999999999998E-2	3.8360999999999999E-2	3.8355E-2	3.8350000000000002E-2	3.8344000000000003E-2	3.8338000000000004E-2	3.8331999999999998E-2	3.8327E-2	3.8321000000000001E-2	3.8315000000000002E-2	3.8309000000000003E-2	3.8302999999999997E-2	3.8297999999999999E-2	3.8292E-2	3.8286000000000001E-2	3.8280000000000002E-2	3.8275000000000017E-2	3.8268999999999997E-2	3.8262999999999998E-2	3.8256999999999999E-2	3.8252000000000001E-2	3.8246000000000002E-2	3.824000000000001E-2	3.8234000000000011E-2	3.8228999999999999E-2	3.8223E-2	3.8217000000000001E-2	3.8212000000000003E-2	3.8206000000000004E-2	3.8199999999999998E-2	3.8193999999999999E-2	3.8189000000000001E-2	3.8183000000000002E-2	3.817700000000001E-2	3.8172000000000005E-2	3.8165999999999999E-2	3.8159999999999999E-2	3.8154E-2	3.8149000000000002E-2	3.8143000000000003E-2	3.8136999999999997E-2	3.8131999999999999E-2	3.8126E-2	3.8120000000000001E-2	3.8114000000000002E-2	3.8108999999999997E-2	3.8102999999999998E-2	3.8096999999999999E-2	3.8092000000000001E-2	3.8086000000000002E-2	3.808000000000001E-2	3.8074999999999998E-2	3.8068999999999999E-2	3.8063E-2	3.8058000000000002E-2	3.8052000000000002E-2	3.8046000000000003E-2	3.8040999999999998E-2	3.8034999999999999E-2	3.8029E-2	3.8024000000000002E-2	3.8018000000000003E-2	3.8012000000000004E-2	3.8006999999999999E-2	3.8001000000000014E-2	3.7995000000000015E-2	3.799000000000001E-2	3.7984000000000011E-2	3.7978000000000012E-2	3.7973000000000014E-2	3.7967000000000001E-2	3.7961000000000002E-2	3.7956000000000011E-2	3.7950000000000005E-2	3.7944000000000006E-2	3.7939000000000014E-2	3.7933000000000015E-2	3.7927000000000002E-2	3.7922000000000004E-2	3.7916000000000005E-2	3.7910000000000006E-2	3.7905000000000015E-2	3.7899000000000016E-2	3.7894000000000011E-2	3.7888000000000012E-2	3.7882000000000013E-2	3.7877000000000015E-2	3.7871000000000016E-2	3.7865000000000017E-2	3.7860000000000012E-2	3.7854000000000013E-2	3.7849000000000015E-2	3.7843000000000016E-2	3.7837000000000023E-2	3.7832000000000011E-2	3.7826000000000005E-2	3.7820000000000006E-2	3.7815000000000015E-2	3.7809000000000016E-2	3.7804000000000011E-2	3.7798000000000005E-2	3.7792000000000006E-2	3.7787000000000015E-2	3.7781000000000016E-2	3.7776000000000011E-2	3.7769999999999998E-2	3.7763999999999999E-2	3.7759000000000015E-2	3.7753000000000002E-2	3.7748000000000011E-2	3.7742000000000012E-2	3.7736000000000013E-2	3.7731000000000015E-2	3.7725000000000002E-2	3.7720000000000004E-2	3.7714000000000004E-2	3.7708000000000005E-2	3.7703000000000014E-2	3.7697000000000015E-2	3.7692000000000017E-2	3.7686000000000011E-2	3.7680000000000012E-2	3.7675000000000021E-2	3.7669000000000015E-2	3.766400000000001E-2	3.7658000000000011E-2	3.7653000000000013E-2	3.7647000000000014E-2	3.7641000000000015E-2	3.7636000000000017E-2	3.7630000000000011E-2	3.7624999999999999E-2	3.7619000000000014E-2	3.7614000000000002E-2	3.7608000000000016E-2	3.760200000000001E-2	3.7596999999999998E-2	3.7590999999999999E-2	3.7586000000000001E-2	3.7580000000000002E-2	3.7575000000000011E-2	3.7568999999999998E-2	3.7564E-2	3.7558000000000001E-2	3.7552000000000002E-2	3.7547000000000011E-2	3.7541000000000012E-2	3.7536000000000014E-2	3.7530000000000015E-2	3.752500000000001E-2	3.7518999999999997E-2	3.7514000000000006E-2	3.7508000000000014E-2	3.7503000000000015E-2	3.7497000000000016E-2	3.749100000000001E-2	3.7486000000000012E-2	3.7480000000000013E-2	3.7475000000000015E-2	3.7469000000000002E-2	3.7464000000000011E-2	3.7458000000000012E-2	3.7453000000000014E-2	3.7447000000000015E-2	3.7442000000000017E-2	3.7436000000000011E-2	3.7431000000000013E-2	3.7425000000000014E-2	3.7419000000000015E-2	3.7414000000000017E-2	3.7408000000000011E-2	3.7403000000000013E-2	3.7397000000000014E-2	3.7392000000000002E-2	3.738600000000001E-2	3.7381000000000011E-2	3.7375000000000012E-2	3.7370000000000014E-2	3.7364000000000001E-2	3.735900000000001E-2	3.7352999999999997E-2	3.7348000000000006E-2	3.7342000000000014E-2	3.7337000000000016E-2	3.7331000000000017E-2	3.7325999999999998E-2	3.7319999999999999E-2	3.7315000000000015E-2	3.7309000000000002E-2	3.7304000000000011E-2	3.7298000000000012E-2	3.7293000000000014E-2	3.7287000000000015E-2	3.7282000000000017E-2	3.7276000000000011E-2	3.7271000000000012E-2	3.7265000000000013E-2	3.7260000000000001E-2	3.7254000000000002E-2	3.7249000000000011E-2	3.7243000000000012E-2	3.7238000000000014E-2	3.7232000000000015E-2	3.7227000000000017E-2	3.7221000000000011E-2	3.7216000000000006E-2	3.7210000000000014E-2	3.7205000000000016E-2	3.719900000000001E-2	3.7194000000000005E-2	3.7188000000000006E-2	3.7183000000000015E-2	3.7177000000000016E-2	3.7172000000000011E-2	3.7165999999999998E-2	3.7161000000000013E-2	3.7155000000000014E-2	3.7150000000000002E-2	3.714400000000001E-2	3.7138999999999998E-2	3.7132999999999999E-2	3.7128000000000001E-2	3.7122000000000002E-2	3.7116999999999997E-2	3.7110999999999998E-2	3.7106E-2	3.7101000000000016E-2	3.7095000000000017E-2	3.7090000000000012E-2	3.7084000000000013E-2	3.7079000000000015E-2	3.7073000000000016E-2	3.7068000000000011E-2	3.7062000000000005E-2	3.7057000000000014E-2	3.7051000000000014E-2	3.7046000000000016E-2	3.704000000000001E-2	3.7035000000000012E-2	3.7028999999999999E-2	3.7024000000000001E-2	3.7019000000000017E-2	3.7013000000000011E-2	3.7008000000000006E-2	3.7002000000000014E-2	3.6997000000000002E-2	3.6991000000000017E-2	3.6986000000000005E-2	3.6980000000000006E-2	3.6975000000000015E-2	3.6969000000000002E-2	3.6964000000000004E-2	3.6958000000000005E-2	3.6953000000000014E-2	3.6948000000000002E-2	3.694200000000001E-2	3.6937000000000011E-2	3.6931000000000012E-2	3.6926E-2	3.6920000000000001E-2	3.691500000000001E-2	3.6908999999999997E-2	3.6904000000000006E-2	3.6899000000000015E-2	3.6893000000000016E-2	3.6888000000000011E-2	3.6882000000000012E-2	3.6877000000000014E-2	3.6871000000000015E-2	3.686600000000001E-2	3.6860000000000011E-2	3.6854999999999999E-2	3.6850000000000015E-2	3.6844000000000016E-2	3.6839000000000011E-2	3.6833000000000012E-2	3.6828E-2	3.6822000000000001E-2	3.6817000000000016E-2	3.6812000000000011E-2	3.6806000000000012E-2	3.6801000000000014E-2	3.6795000000000001E-2	3.679000000000001E-2	3.6784000000000004E-2	3.6778999999999999E-2	3.6774000000000001E-2	3.6768000000000002E-2	3.6762999999999997E-2	3.6756999999999998E-2	3.6752E-2	3.6746000000000001E-2	3.6741000000000017E-2	3.6736000000000012E-2	3.6729999999999999E-2	3.6725000000000001E-2	3.6719000000000002E-2	3.6714000000000004E-2	3.6708000000000005E-2	3.6703000000000006E-2	3.6698000000000001E-2	3.6692000000000002E-2	3.6687000000000011E-2	3.6681000000000012E-2	3.6676000000000014E-2	3.6671000000000016E-2	3.6665000000000017E-2	3.6660000000000005E-2	3.6654000000000006E-2	3.6649000000000015E-2	3.6643000000000016E-2	3.6638000000000011E-2	3.6633000000000013E-2	3.6627000000000014E-2	3.6622000000000002E-2	3.661600000000001E-2	3.6611000000000012E-2	3.6606000000000014E-2	3.6600000000000014E-2	3.6595000000000009E-2	3.658900000000001E-2	3.6584000000000005E-2	3.6579000000000014E-2	3.6573000000000015E-2	3.6568000000000003E-2	3.6562000000000004E-2	3.6556999999999999E-2	3.6552000000000001E-2	3.6546000000000002E-2	3.6541000000000011E-2	3.6535000000000012E-2	3.6530000000000014E-2	3.6525000000000002E-2	3.651900000000001E-2	3.6514000000000005E-2	3.6508000000000006E-2	3.6503000000000015E-2	3.649800000000001E-2	3.6492000000000011E-2	3.6487000000000012E-2	3.6481000000000013E-2	3.6476000000000015E-2	3.6471000000000017E-2	3.6464999999999997E-2	3.6460000000000006E-2	3.6454000000000014E-2	3.6449000000000016E-2	3.6444000000000011E-2	3.6438000000000012E-2	3.6433000000000014E-2	3.6427000000000015E-2	3.642200000000001E-2	3.6416999999999998E-2	3.6410999999999999E-2	3.6406000000000015E-2	3.6401000000000017E-2	3.6394999999999997E-2	3.6389999999999999E-2	3.6384E-2	3.6379000000000015E-2	3.637400000000001E-2	3.6367999999999998E-2	3.6362999999999999E-2	3.6357E-2	3.6352000000000002E-2	3.6346999999999997E-2	3.6340999999999998E-2	3.6336E-2	3.6331000000000016E-2	3.632500000000001E-2	3.6319999999999998E-2	3.6313999999999999E-2	3.6309000000000001E-2	3.630400000000001E-2	3.6298000000000011E-2	3.6292999999999999E-2	3.6288000000000015E-2	3.6282000000000002E-2	3.6277000000000011E-2	3.6271000000000012E-2	3.6266E-2	3.6261000000000002E-2	3.6255000000000016E-2	3.6250000000000011E-2	3.6244999999999999E-2	3.6239000000000014E-2	3.6234000000000002E-2	3.6228000000000003E-2	3.6222999999999998E-2	3.6218E-2	3.6212000000000001E-2	3.6207000000000017E-2	3.6202000000000012E-2	3.6195999999999999E-2	3.6191000000000001E-2	3.6185000000000002E-2	3.6180000000000004E-2	3.6174999999999999E-2	3.6169E-2	3.6164000000000002E-2	3.6158999999999997E-2	3.6152999999999998E-2	3.6148E-2	3.6143000000000002E-2	3.6137000000000002E-2	3.6132000000000011E-2	3.6126999999999999E-2	3.6121E-2	3.6116000000000002E-2	3.6110000000000003E-2	3.6104999999999998E-2	3.61E-2	3.6094000000000001E-2	3.6089000000000017E-2	3.6084000000000012E-2	3.6078000000000013E-2	3.6073000000000015E-2	3.6068000000000003E-2	3.6062000000000004E-2	3.6056999999999999E-2	3.6052000000000001E-2	3.6046000000000002E-2	3.6041000000000011E-2	3.6035000000000011E-2	3.6030000000000013E-2	3.6025000000000001E-2	3.6019000000000002E-2	3.6014000000000004E-2	3.6008999999999999E-2	3.6003000000000014E-2	3.5998000000000002E-2	3.5992999999999997E-2	3.5986999999999998E-2	3.5982E-2	3.5977000000000002E-2	3.5971000000000017E-2	3.5965999999999998E-2	3.5961E-2	3.5955000000000001E-2	3.5950000000000003E-2	3.5944999999999998E-2	3.5938999999999999E-2	3.5934000000000001E-2	3.5928000000000002E-2	3.5922999999999997E-2	3.5917999999999999E-2	3.5911999999999999E-2	3.5907000000000001E-2	3.5902000000000003E-2	3.5896000000000004E-2	3.5890999999999999E-2	3.5886000000000001E-2	3.5880000000000002E-2	3.5875000000000011E-2	3.5869999999999999E-2	3.5864E-2	3.5859000000000002E-2	3.5854000000000011E-2	3.5848000000000005E-2	3.5843000000000014E-2	3.5838000000000002E-2	3.5832000000000017E-2	3.5826999999999998E-2	3.5822E-2	3.5816000000000001E-2	3.5811000000000016E-2	3.5806000000000011E-2	3.5799999999999998E-2	3.5795E-2	3.5790000000000002E-2	3.5784000000000003E-2	3.5778999999999998E-2	3.5774E-2	3.5768000000000001E-2	3.5763000000000003E-2	3.5757999999999998E-2	3.5751999999999999E-2	3.5747000000000001E-2	3.574200000000001E-2	3.5736000000000004E-2	3.5730999999999999E-2	3.5726000000000001E-2	3.5720000000000002E-2	3.5714999999999997E-2	3.5709999999999999E-2	3.5704E-2	3.5699000000000002E-2	3.569400000000001E-2	3.5688000000000011E-2	3.5682999999999999E-2	3.5678000000000001E-2	3.5672000000000002E-2	3.5666999999999997E-2	3.5661999999999999E-2	3.5656E-2	3.5651000000000002E-2	3.5646000000000011E-2	3.5640000000000012E-2	3.5635000000000014E-2	3.5630000000000016E-2	3.5624999999999997E-2	3.5618999999999998E-2	3.5614E-2	3.5609000000000016E-2	3.5603000000000017E-2	3.5597999999999998E-2	3.5593E-2	3.5587000000000001E-2	3.5582000000000009E-2	3.5576999999999998E-2	3.5570999999999998E-2	3.5566E-2	3.5561000000000002E-2	3.555500000000001E-2	3.5549999999999998E-2	3.5545000000000014E-2	3.5539000000000001E-2	3.553400000000001E-2	3.5528999999999998E-2	3.5522999999999999E-2	3.5518000000000001E-2	3.551300000000001E-2	3.5507999999999998E-2	3.5501999999999999E-2	3.5497000000000015E-2	3.549200000000001E-2	3.5486000000000011E-2	3.5480999999999999E-2	3.5476000000000014E-2	3.5470000000000015E-2	3.546500000000001E-2	3.5460000000000005E-2	3.5453999999999999E-2	3.5449000000000015E-2	3.544400000000001E-2	3.5438000000000011E-2	3.5433000000000013E-2	3.5428000000000001E-2	3.542300000000001E-2	3.5416999999999997E-2	3.5412000000000006E-2	3.5407000000000015E-2	3.5401000000000016E-2	3.5395999999999997E-2	3.5390999999999999E-2	3.5385000000000014E-2	3.5380000000000002E-2	3.5375000000000011E-2	3.5368999999999998E-2	3.5364E-2	3.5359000000000002E-2	3.5354000000000003E-2	3.5348000000000004E-2	3.5342999999999999E-2	3.5338000000000001E-2	3.5332000000000002E-2	3.5326999999999997E-2	3.5321999999999999E-2	3.5316E-2	3.5311000000000002E-2	Time (s)

Liquid holdup
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External liquid holdup
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External liquid holdup



300 mm	349	349.5	350	350.5	351	351.5	352	352.5	353	353.5	354	354.5	355	355.5	356	356.5	357	357.5	358	358.5	359	359.5	360	360.5	361	361.5	362	362.5	363	363.5	364	364.5	365	365.5	366	366.5	367	367.5	368	368.5	369	369.5	370	370.5	371	371.5	372	372.5	373	373.5	374	374.5	375	375.5	376	376.5	377	377.5	378	378.5	379	379.5	380	380.5	381	381.5	382	382.5	383	383.5	384	384.5	385	385.5	386	386.5	387	387.5	388	388.5	389	389.5	390	390.5	391	391.5	392	392.5	393	393.5	394	394.5	395	395.5	396	396.5	397	397.5	398	398.5	399	399.5	400	400.5	401	401.5	402	402.5	403	403.5	404	404.5	405	405.5	406	406.5	407	407.5	408	408.5	409	409.5	410	410.5	411	411.5	412	412.5	413	413.5	414	414.5	415	415.5	416	416.5	417	417.5	418	418.5	419	419.5	420	420.5	421	421.5	422	422.5	423	423.5	424	424.5	425	425.5	426	426.5	427	427.5	428	428.5	429	429.5	430	430.5	431	431.5	432	432.5	433	433.5	434	434.5	435	435.5	436	436.5	437	437.5	438	438.5	439	439.5	440	440.5	441	441.5	442	442.5	443	443.5	444	444.5	445	445.5	446	446.5	447	447.5	448	448.5	449	449.5	450	450.5	451	451.5	452	452.5	453	453.5	454	454.5	455	455.5	456	456.5	457	457.5	458	458.5	459	459.5	460	460.5	461	461.5	462	462.5	463	463.5	464	464.5	465	465.5	466	466.5	467	467.5	468	468.5	469	469.5	470	470.5	471	471.5	472	472.5	473	473.5	474	474.5	475	475.5	476	476.5	477	477.5	478	478.5	479	479.5	480	480.5	481	481.5	482	482.5	483	483.5	484	484.5	485	485.5	486	486.5	487	487.5	488	488.5	489	489.5	490	490.5	491	491.5	492	492.5	493	493.5	494	494.5	495	495.5	496	496.5	497	497.5	498	498.5	499	499.5	500	500.5	501	501.5	502	502.5	503	503.5	504	504.5	505	505.5	506	506.5	507	507.5	508	508.5	509	509.5	510	510.5	511	511.5	512	512.5	513	513.5	514	514.5	515	515.5	516	516.5	517	517.5	518	518.5	519	519.5	520	520.5	521	521.5	522	522.5	523	523.5	524	524.5	525	525.5	526	526.5	527	527.5	528	528.5	529	529.5	530	530.5	531	531.5	532	532.5	533	533.5	534	534.5	535	535.5	536	536.5	537	537.5	538	538.5	539	539.5	540	540.5	541	541.5	542	542.5	543	543.5	544	544.5	545	545.5	546	546.5	547	547.5	548	548.5	549	549.5	550	550.5	551	551.5	552	552.5	553	553.5	554	554.5	555	555.5	556	556.5	557	557.5	558	558.5	559	559.5	560	560.5	561	561.5	562	562.5	563	563.5	564	564.5	565	565.5	566	566.5	567	567.5	568	568.5	569	569.5	570	570.5	571	571.5	572	572.5	573	573.5	574	574.5	575	575.5	576	576.5	577	577.5	578	578.5	579	579.5	580	580.5	581	581.5	582	582.5	583	583.5	584	584.5	585	585.5	586	586.5	587	587.5	588	588.5	589	589.5	590	590.5	591	591.5	592	592.5	593	593.5	594	594.5	595	595.5	596	596.5	597	597.5	598	598.5	599	599.5	600	600.5	601	601.5	602	602.5	603	603.5	604	604.5	605	605.5	606	606.5	607	607.5	608	608.5	609	609.5	610	610.5	611	611.5	612	612.5	613	613.5	614	614.5	615	615.5	616	616.5	617	617.5	618	618.5	619	619.5	620	620.5	621	621.5	622	622.5	623	623.5	624	624.5	625	625.5	626	626.5	627	627.5	628	628.5	629	629.5	630	630.5	631	631.5	632	632.5	633	633.5	634	634.5	635	635.5	636	636.5	637	637.5	638	638.5	639	639.5	640	640.5	641	641.5	642	642.5	643	643.5	644	644.5	645	645.5	646	646.5	647	647.5	648	648.5	649	649.5	650	650.5	651	651.5	652	652.5	653	653.5	654	654.5	655	655.5	656	656.5	657	657.5	658	658.5	659	659.5	660	660.5	661	661.5	662	662.5	663	663.5	664	664.5	665	665.5	666	666.5	667	667.5	668	668.5	669	669.5	670	670.5	671	671.5	672	672.5	673	673.5	674	674.5	675	675.5	676	676.5	677	677.5	678	678.5	679	679.5	680	680.5	681	681.5	682	682.5	683	683.5	684	684.5	685	685.5	686	686.5	687	687.5	688	688.5	689	689.5	690	690.5	691	691.5	692	692.5	693	693.5	694	694.5	695	695.5	696	696.5	697	697.5	698	698.5	699	699.5	700	700.5	701	701.5	702	702.5	703	703.5	704	704.5	705	705.5	706	706.5	707	707.5	708	708.5	709	709.5	710	710.5	711	711.5	712	712.5	713	713.5	714	714.5	715	715.5	716	716.5	717	717.5	718	718.5	719	719.5	720	720.5	721	721.5	722	722.5	723	723.5	724	724.5	725	725.5	726	726.5	727	727.5	728	728.5	729	729.5	730	730.5	731	731.5	732	732.5	733	733.5	734	734.5	735	735.5	736	736.5	737	737.5	738	738.5	739	739.5	740	740.5	741	741.5	742	742.5	743	743.5	744	744.5	745	745.5	746	746.5	747	747.5	748	748.5	749	749.5	750	750.5	751	751.5	752	752.5	753	753.5	754	754.5	755	755.5	756	756.5	757	757.5	758	758.5	759	759.5	760	760.5	761	761.5	762	762.5	763	763.5	764	764.5	765	765.5	766	766.5	767	767.5	768	768.5	769	769.5	770	770.5	771	771.5	772	772.5	773	773.5	774	774.5	775	775.5	776	776.5	777	777.5	778	778.5	779	779.5	780	780.5	781	781.5	782	782.5	783	783.5	784	784.5	785	785.5	786	786.5	787	787.5	788	788.5	789	789.5	790	790.5	791	791.5	792	792.5	793	793.5	794	794.5	795	795.5	796	796.5	797	797.5	798	798.5	799	799.5	800	800.5	801	801.5	802	802.5	803	803.5	804	804.5	805	805.5	806	806.5	807	807.5	808	808.5	809	809.5	810	810.5	811	811.5	812	812.5	813	813.5	814	814.5	815	815.5	816	816.5	817	817.5	818	818.5	819	819.5	820	820.5	821	821.5	822	822.5	823	823.5	824	824.5	825	825.5	826	826.5	827	827.5	828	828.5	829	829.5	830	830.5	831	831.5	832	832.5	833	833.5	834	834.5	835	835.5	836	836.5	837	837.5	838	838.5	839	839.5	840	840.5	841	841.5	842	842.5	843	843.5	844	844.5	845	845.5	846	846.5	847	847.5	848	848.5	849	849.5	850	850.5	851	851.5	852	852.5	853	853.5	854	854.5	855	855.5	856	856.5	857	857.5	858	858.5	859	859.5	860	860.5	861	861.5	862	862.5	863	863.5	864	864.5	865	865.5	866	866.5	867	867.5	868	868.5	869	869.5	870	870.5	871	871.5	872	872.5	873	873.5	874	874.5	875	875.5	876	876.5	877	877.5	878	878.5	879	879.5	880	880.5	881	881.5	882	882.5	883	883.5	884	884.5	885	885.5	886	886.5	887	887.5	888	888.5	889	889.5	890	890.5	891	891.5	892	892.5	893	893.5	894	894.5	895	895.5	896	896.5	897	897.5	898	898.5	899	899.5	900	900.5	901	901.5	902	902.5	903	903.5	904	904.5	905	905.5	906	906.5	907	907.5	908	908.5	909	909.5	910	910.5	911	911.5	912	912.5	913	913.5	914	914.5	915	915.5	916	916.5	917	917.5	918	918.5	919	919.5	920	920.5	921	921.5	922	922.5	923	923.5	924	924.5	925	925.5	926	926.5	927	927.5	928	928.5	929	929.5	930	930.5	931	931.5	932	932.5	933	933.5	934	934.5	935	935.5	936	936.5	937	937.5	938	938.5	939	939.5	940	940.5	941	941.5	942	942.5	943	943.5	944	944.5	945	945.5	946	946.5	947	947.5	948	948.5	949	949.5	950	950.5	951	951.5	952	952.5	953	953.5	954	954.5	955	955.5	956	956.5	957	957.5	958	958.5	959	959.5	960	960.5	961	961.5	962	962.5	963	963.5	964	964.5	965	965.5	966	966.5	967	967.5	968	968.5	969	969.5	970	970.5	971	971.5	972	972.5	973	973.5	974	974.5	975	975.5	976	976.5	977	977.5	978	978.5	979	979.5	980	980.5	981	981.5	982	982.5	983	983.5	984	984.5	985	985.5	986	986.5	987	987.5	988	988.5	989	989.5	990	990.5	991	991.5	992	992.5	993	993.5	994	994.5	995	995.5	996	996.5	997	997.5	998	998.5	999	999.5	1000	1000.5	1001	1001.5	1002	1002.5	1003	1003.5	1004	1004.5	1005	1005.5	1006	1006.5	1007	1007.5	1008	1008.5	1009	1009.5	1010	1010.5	1011	1011.5	1012	1012.5	1013	1013.5	1014	1014.5	1015	1015.5	1016	1016.5	1017	1017.5	1018	1018.5	1019	1019.5	1020	1020.5	1021	1021.5	1022	1022.5	1023	1023.5	1024	1024.5	1025	1025.5	1026	1026.5	1027	1027.5	1028	1028.5	1029	1029.5	1030	1030.5	1031	1031.5	1032	1032.5	1033	1033.5	1034	1034.5	1035	1035.5	1036	1036.5	1037	1037.5	1038	1038.5	1039	1039.5	1040	1040.5	1041	1041.5	1042	1042.5	1043	1043.5	1044	1044.5	1045	1045.5	1046	1046.5	1047	1047.5	1048	1048.5	1049	1049.5	1050	1050.5	1051	1051.5	1052	1052.5	1053	1053.5	1054	1054.5	1055	1055.5	1056	1056.5	1057	1057.5	1058	1058.5	1059	1059.5	1060	1060.5	1061	1061.5	1062	1062.5	1063	1063.5	1064	1064.5	1065	1065.5	1066	1066.5	1067	1067.5	1068	1068.5	1069	1069.5	1070	1070.5	1071	1071.5	1072	1072.5	1073	1073.5	1074	1074.5	1075	1075.5	1076	1076.5	1077	1077.5	1078	1078.5	1079	1079.5	1080	1080.5	1081	1081.5	1082	1082.5	1083	1083.5	1084	1084.5	1085	1085.5	1086	1086.5	1087	1087.5	1088	1088.5	1089	1089.5	1090	1090.5	1091	1091.5	1092	1092.5	1093	1093.5	1094	1094.5	1095	1095.5	1096	1096.5	1097	1097.5	1098	1098.5	1099	1099.5	1100	1100.5	1101	1101.5	1102	1102.5	1103	1103.5	1104	1104.5	1105	1105.5	1106	1106.5	1107	1107.5	1108	1108.5	1109	1109.5	1110	1110.5	1111	1111.5	1112	1112.5	1113	1113.5	1114	1114.5	1115	1115.5	1116	1116.5	1117	1117.5	1118	1118.5	1119	1119.5	1120	1120.5	1121	1121.5	1122	1122.5	1123	1123.5	1124	1124.5	1125	1125.5	1126	1126.5	1127	1127.5	1128	1128.5	1129	1129.5	1130	1130.5	1131	1131.5	1132	1132.5	1133	1133.5	1134	1134.5	1135	1135.5	1136	1136.5	1137	1137.5	1138	1138.5	1139	1139.5	1140	1140.5	1141	1141.5	1142	1142.5	1143	1143.5	1144	1144.5	1145	1145.5	1146	1146.5	1147	1147.5	1148	1148.5	1149	1149.5	1150	1150.5	1151	1151.5	1152	1152.5	1153	1153.5	1154	1154.5	1155	1155.5	1156	1156.5	1157	1157.5	1158	1158.5	1159	1159.5	1160	1160.5	1161	1161.5	1162	1162.5	1163	1163.5	1164	1164.5	1165	1165.5	1166	1166.5	1167	1167.5	1168	1168.5	1169	1169.5	1170	1170.5	1171	1171.5	1172	1172.5	1173	1173.5	1174	1174.5	1175	1175.5	1176	1176.5	1177	1177.5	1178	1178.5	1179	1179.5	1180	1180.5	1181	1181.5	1182	1182.5	1183	1183.5	1184	1184.5	1185	1185.5	1186	1186.5	1187	1187.5	1188	1188.5	1189	1189.5	1190	1190.5	1191	1191.5	1192	1192.5	1193	1193.5	1194	1194.5	1195	1195.5	1196	1196.5	1197	1197.5	1198	1198.5	1199	1199.5	1200	1200.5	1201	1201.5	1202	1202.5	1203	1203.5	1204	1204.5	1205	1205.5	1206	1206.5	1207	1207.5	1208	1208.5	1209	1209.5	1210	1210.5	1211	1211.5	1212	1212.5	1213	1213.5	1214	1214.5	1215	1215.5	1216	1216.5	1217	1217.5	1218	1218.5	1219	1219.5	1220	1220.5	1221	1221.5	1222	1222.5	1223	1223.5	1224	1224.5	1225	1225.5	1226	1226.5	1227	1227.5	1228	1228.5	1229	1229.5	1230	1230.5	1231	1231.5	1232	1232.5	1233	1233.5	1234	1234.5	1235	1235.5	1236	1236.5	1237	1237.5	1238	1238.5	1239	1239.5	1240	1240.5	1241	1241.5	1242	1242.5	1243	1243.5	1244	1244.5	1245	1245.5	1246	1246.5	1247	1247.5	1248	1248.5	1249	1249.5	1250	1250.5	1251	1251.5	1252	1252.5	1253	1253.5	1254	1254.5	1255	1255.5	1256	1256.5	1257	1257.5	1258	1258.5	1259	1259.5	1260	1260.5	1261	1261.5	1262	1262.5	1263	1263.5	1264	1264.5	1265	1265.5	1266	1266.5	1267	1267.5	1268	1268.5	1269	1269.5	1270	1270.5	1271	1271.5	1272	1272.5	1273	1273.5	1274	1274.5	1275	1275.5	1276	1276.5	1277	1277.5	1278	1278.5	1279	1279.5	1280	1280.5	1281	1281.5	1282	1282.5	1283	1283.5	1284	1284.5	1285	1285.5	1286	1286.5	1287	1287.5	1288	1288.5	1289	1289.5	1290	1290.5	1291	1291.5	1292	1292.5	1293	1293.5	1294	1294.5	1295	1295.5	1296	1296.5	1297	1297.5	1298	1298.5	1299	1299.5	1300	1300.5	1301	1301.5	1302	1302.5	1303	1303.5	1304	1304.5	1305	1305.5	1306	1306.5	1307	1307.5	1308	1308.5	1309	1309.5	1310	1310.5	1311	1311.5	1312	1312.5	1313	1313.5	1314	1314.5	1315	1315.5	1316	1316.5	1317	1317.5	1318	1318.5	1319	1319.5	1320	1320.5	1321	1321.5	1322	1322.5	1323	1323.5	1324	1324.5	1325	1325.5	1326	1326.5	1327	1327.5	1328	1328.5	1329	1329.5	1330	1330.5	1331	1331.5	1332	1332.5	1333	1333.5	1334	1334.5	1335	1335.5	1336	1336.5	1337	1337.5	1338	1338.5	1339	1339.5	1340	1340.5	1341	1341.5	1342	1342.5	1343	1343.5	1344	1344.5	1345	1345.5	1346	1346.5	1347	1347.5	1348	1348.5	1349	1349.5	1350	1350.5	1351	1351.5	1352	1352.5	1353	1353.5	1354	1354.5	1355	1355.5	1356	1356.5	1357	1357.5	1358	1358.5	1359	1359.5	1360	1360.5	1361	1361.5	1362	1362.5	1363	1363.5	1364	1364.5	1365	1365.5	1366	1366.5	1367	1367.5	1368	1368.5	1369	1369.5	1370	1370.5	1371	1371.5	1372	1372.5	1373	1373.5	1374	1374.5	1375	1375.5	1376	1376.5	1377	1377.5	1378	1378.5	1379	1379.5	1380	1380.5	1381	1381.5	1382	1382.5	1383	1383.5	1384	1384.5	1385	1385.5	1386	1386.5	1387	1387.5	1388	1388.5	1389	1389.5	1390	1390.5	1391	1391.5	1392	1392.5	1393	1393.5	1394	1394.5	1395	1395.5	1396	1396.5	1397	1397.5	1398	1398.5	1399	1399.5	1400	1400.5	1401	1401.5	1402	1402.5	1403	1403.5	1404	1404.5	1405	1405.5	1406	1406.5	1407	1407.5	1408	1408.5	1409	1409.5	1410	1410.5	1411	1411.5	1412	1412.5	1413	1413.5	1414	1414.5	1415	1415.5	1416	1416.5	1417	1417.5	1418	1418.5	1419	1419.5	1420	1420.5	1421	1421.5	1422	1422.5	1423	1423.5	1424	1424.5	1425	1425.5	1426	1426.5	1427	1427.5	1428	1428.5	1429	1429.5	1430	1430.5	1431	1431.5	1432	1432.5	1433	1433.5	1434	1434.5	1435	1435.5	1436	1436.5	1437	1437.5	1438	1438.5	1439	1439.5	1440	1440.5	1441	1441.5	1442	1442.5	1443	1443.5	1444	1444.5	1445	1445.5	1446	1446.5	1447	1447.5	1448	1448.5	1449	1449.5	1450	1450.5	1451	1451.5	1452	1452.5	1453	1453.5	1454	1454.5	1455	1455.5	1456	1456.5	1457	1457.5	1458	1458.5	1459	1459.5	1460	1460.5	1461	1461.5	1462	1462.5	1463	1463.5	1464	1464.5	1465	1465.5	1466	1466.5	1467	1467.5	1468	1468.5	1469	1469.5	1470	1470.5	1471	1471.5	1472	1472.5	1473	1473.5	1474	1474.5	1475	1475.5	1476	1476.5	1477	1477.5	1478	1478.5	1479	1479.5	1480	1480.5	1481	1481.5	1482	1482.5	1483	1483.5	1484	1484.5	1485	1485.5	1486	1486.5	1487	1487.5	1488	1488.5	1489	1489.5	1490	1490.5	1491	1491.5	1492	1492.5	1493	1493.5	1494	1494.5	1495	1495.5	1496	1496.5	1497	1497.5	1498	1498.5	1499	1499.5	1500	0	1.08	1.33	1.52	1.58	1.6700000000000021	1.74	1.81	1.980000000000018	2.0099999999999998	2.19	2.23	2.4099999999999997	2.4699999999999998	2.66	2.8	2.94	3.17	3.24	3.4	3.57	3.69	3.8	3.94	4.18	4.2300000000000004	4.38	4.46	4.6399999999999997	4.7	4.87	4.9800000000000004	5.08	5.18	5.3	5.41	5.42	5.52	5.6599999999999975	5.81	5.83	5.96	6.03	6.1599999999999975	6.21	6.33	6.38	6.56	6.6099999999999985	6.64	6.78	6.8199999999999985	6.9300000000000024	6.9300000000000024	7.01	7.1	7.17	7.18	7.31	7.3	7.31	7.38	7.42	7.44	7.51	7.52	7.6199999999999966	7.6199999999999966	7.67	7.73	7.8199999999999985	7.84	7.94	7.95	7.9700000000000024	8.0500000000000007	8.11	8.1399999999999988	8.16	8.2399999999999984	8.3600000000000048	8.3600000000000048	8.3700000000000028	8.43	8.51	8.5500000000000007	8.6399999999999988	8.65	8.69	8.76	8.8500000000000068	8.8600000000000048	8.94	8.98	9.0500000000000007	9.129999999999999	9.15	9.2000000000000011	9.3500000000000068	9.3500000000000068	9.3800000000000008	9.44	9.5500000000000007	9.56	9.6	9.7299999999999986	9.7399999999999984	9.76	9.81	9.8000000000000007	9.82	9.9700000000000006	9.98	10.07	10.06	10.120000000000001	10.239999999999998	10.44	10.68	10.81	10.93	11.17	11.29	11.47	11.58	11.77	11.88	12.03	12.209999999999999	12.29	12.43	12.57	12.66	12.75	12.850000000000026	13	13.08	13.19	13.31	13.44	13.5	13.6	13.719999999999999	13.850000000000026	13.93	14.01	14.139999999999999	14.28	14.34	14.46	14.54	14.69	14.739999999999998	14.84	14.94	15.08	15.1	15.2	15.3	15.450000000000006	15.47	15.51	15.67	15.81	15.89	15.950000000000006	16.110000000000031	16.14	16.22	16.309999999999999	16.37	16.5	16.559999999999999	16.7	16.760000000000002	16.93	16.95	17.04	17.149999999999999	17.260000000000002	17.34	17.41	17.489999999999789	17.55	17.690000000000001	17.690000000000001	17.77	17.850000000000001	17.87	17.920000000000002	18.059999999999999	18.07	18.149999999999999	18.170000000000005	18.27	18.29	18.36	18.479999999999986	18.489999999999789	18.610000000000031	18.71	18.88	18.93	19.059999999999999	19.149999999999999	19.29	19.350000000000001	19.5	19.670000000000005	19.829999999999988	19.84	19.93	20.04	20.2	20.260000000000002	20.350000000000001	20.47	20.6	20.69	20.86	20.99	21.12	21.21	21.4	21.439999999999987	21.52	21.74	21.84	21.95	22.05	22.25	22.39	22.56	22.67	22.8	22.88	23.02	23.18	23.25	23.36	23.47	23.6	23.67	23.8	24.02	24.130000000000031	24.36	24.43	24.5	24.630000000000031	24.8	24.939999999999987	25.09	25.27	25.34	25.45	25.58	25.85	25.89	26.01	26.150000000000031	26.36	26.47	26.610000000000031	26.8	26.87	27.05	27.19	27.310000000000031	27.39	27.479999999999986	27.59	27.73	27.779999999999987	27.93	27.99	28.1	28.16	28.35	28.57	28.84	28.959999999999987	29.1	29.35	29.47	29.68	29.9	30.02	30.3	30.41	30.62	30.85	30.99	31.2	31.43	31.69	31.82	32.020000000000003	32.24	32.36	32.57	32.790000000000013	32.879999999999995	33.17	33.300000000000004	33.47	33.68	33.809999999999995	33.99	34.190000000000012	34.290000000000013	34.54	34.64	34.82	35.01	35.120000000000012	35.32	35.480000000000004	35.550000000000004	35.65	35.790000000000013	36.090000000000003	36.14	36.309999999999995	36.49	36.58	36.65	36.800000000000004	37	37.130000000000003	37.300000000000004	37.47	37.56	37.74	37.82	37.980000000000004	38.1	38.270000000000003	38.46	38.57	38.75	38.97	39.090000000000003	39.230000000000011	39.43	39.56	39.74	39.949999999999996	40.07	40.33	40.43	40.65	40.849999999999994	40.99	41.17	41.39	41.53	41.78	41.94	42.2	42.349999999999994	42.57	42.809999999999995	42.92	43.18	43.309999999999995	43.44	43.65	43.839999999999996	44.05	44.27	44.56	44.67	44.87	45.1	45.230000000000011	45.42	45.65	45.9	46.04	46.230000000000011	46.44	46.52	46.75	46.96	47.11	47.36	47.53	47.7	47.92	48.04	48.24	48.42	48.55	48.86	48.96	49.17	49.39	49.54	49.75	49.94	50.02	50.339999999999996	50.43	50.64	50.82	50.96	50.98	51.33	51.52	51.790000000000013	51.9	52.01	52.230000000000011	52.27	52.55	52.75	52.86	53.13	53.27	53.44	53.65	53.790000000000013	53.97	54.18	54.3	54.52	54.68	54.96	55.13	55.349999999999994	55.59	55.8	55.96	56.190000000000012	56.43	56.64	56.93	57.33	57.349999999999994	57.720000000000013	57.87	58.07	58.32	58.57	58.75	59.04	59.15	59.41	59.660000000000011	59.879999999999995	60.02	60.25	60.47	60.660000000000011	60.839999999999996	61.05	61.24	61.41	61.64	61.809999999999995	61.98	62.230000000000011	62.41	62.67	62.8	62.94	63.18	63.32	63.52	63.61	63.86	64.08	64.2	64.38	64.58	64.69	64.849999999999994	65.099999999999994	65.22	65.510000000000005	65.66	65.86	66.08	66.169999999999987	66.410000000000025	66.63	66.77	67.02	67.22	67.410000000000025	67.55	67.75	67.959999999999994	68.11	68.31	68.400000000000006	68.61	68.819999999999993	68.910000000000025	69.14	69.349999999999994	69.61999999999999	69.72	69.819999999999993	69.97	70.169999999999987	70.31	70.48	70.679999999999978	70.83	71.069999999999993	71.16	71.349999999999994	71.540000000000006	71.64	71.84	72.06	72.149999999999991	72.47	72.540000000000006	72.66	72.8	73	73.14	73.31	73.48	73.61999999999999	73.77	73.98	74.08	74.22	74.430000000000007	74.510000000000005	74.75	74.92	75.010000000000005	75.209999999999994	75.410000000000025	75.53	75.679999999999978	75.86	75.989999999999995	76.16	76.349999999999994	76.489999999999995	76.81	76.86999999999999	76.989999999999995	77.13	77.319999999999993	77.440000000000026	77.59	77.760000000000005	77.84	77.989999999999995	78.179999999999978	78.39	78.53	78.7	78.86999999999999	79	79.16	79.36999999999999	79.510000000000005	79.73	79.89	80.03	80.13	80.319999999999993	80.430000000000007	80.599999999999994	80.81	80.930000000000007	81.08	81.260000000000005	81.36999999999999	81.540000000000006	81.679999999999978	81.78	82.01	82.2	82.29	82.48	82.64	82.78	82.89	82.940000000000026	83.179999999999978	83.29	83.440000000000026	83.63	83.710000000000022	83.9	84.07	84.22	84.33	84.460000000000022	84.63	84.710000000000022	84.88	85.1	85.19	85.36	85.57	85.72	85.81	85.98	86.16	86.3	86.45	86.64	86.77	87.06	87.149999999999991	87.27	87.5	87.64	87.84	88.07	88.169999999999987	88.5	88.61	88.78	89.02	89.16	89.36999999999999	89.56	89.679999999999978	89.960000000000022	90.1	90.26	90.47	90.6	90.910000000000025	91.06	91.36	91.52	91.77	91.92	92.13	92.36999999999999	92.5	92.76	92.910000000000025	93.08	93.31	93.5	93.75	93.86	94.149999999999991	94.34	94.52	94.7	94.79	95.01	95.240000000000023	95.38	95.66	95.81	96.08	96.2	96.32	96.58	96.7	96.89	97.11	97.3	97.53	97.649999999999991	97.84	98.03	98.169999999999987	98.45	98.55	98.78	99.01	99.179999999999978	99.38	99.6	99.84	99.960000000000022	100.11	100.3	100.4	100.57	100.79	100.86999999999999	101.06	101.35	101.52	101.61999999999999	101.82	101.89	102.07	102.28	102.38	102.59	102.83	102.92	103.13	103.31	103.44000000000032	103.61	103.79	103.89	104.09	104.28	104.39	104.5	104.64999999999999	104.78	104.99000000000002	105.17999999999998	105.26	105.35	105.51	105.66999999999999	105.83	105.95	106.08	106.23	106.3	106.49000000000002	106.64999999999999	106.77	106.96000000000002	107.14	107.27	107.38	107.55	107.73	107.86	108.02	108.2	108.28	108.49000000000002	108.67999999999998	108.82	108.96000000000002	109.13	109.23	109.4	109.59	109.69	109.85	110.03	110.19	110.29	110.44000000000032	110.61999999999999	110.72	110.92	111.1	111.17999999999998	111.35	111.52	111.69	111.78	111.93	112.11	112.2	112.38	112.53	112.64999999999999	112.77	112.9	113.11999999999999	113.22	113.38	113.54	113.64999999999999	113.77	113.91000000000012	114.09	114.21000000000002	114.36999999999999	114.64999999999999	114.73	114.91000000000012	115.11999999999999	115.2	115.33	115.56	115.7	115.89	116.13	116.26	116.55	116.7	116.9	117.11	117.24000000000002	117.54	117.66	117.85	118.06	118.21000000000002	118.36999999999999	118.58	118.86	119.01	119.22	119.48	119.64	119.84	120.1	120.32	120.54	120.8	120.93	121.14999999999999	121.39	121.55	121.74000000000002	121.86999999999999	122.06	122.23	122.38	122.6	122.71000000000002	122.94000000000032	123.16999999999999	123.22	123.42	123.63	123.82	124.09	124.21000000000002	124.47	124.53	124.72	124.92	125.03	125.2	125.45	125.55	125.75	125.93	126.05	126.2	126.4	126.52	126.67999999999998	126.88	127.01	127.29	127.36	127.46000000000002	127.67999999999998	127.8	127.94000000000032	128.08000000000001	128.26	128.39000000000001	128.54	128.72999999999999	128.82000000000087	129	129.18	129.26999999999998	129.47999999999999	129.69999999999999	129.80000000000001	129.96	130.13999999999999	130.25	130.41	130.59	130.66999999999999	130.86000000000001	131.03	131.13	131.31	131.47999999999999	131.6	131.72	131.85000000000107	132.03	132.09	132.28	132.43	132.51	132.69999999999999	132.86000000000001	133.03	133.12	133.25	133.37	133.56	133.69	133.83000000000001	133.96	134	134.22	134.4	134.60999999999999	134.73999999999998	134.87	135.05000000000001	135.15	135.32000000000087	135.49	135.63	135.76	135.89000000000001	136.01	136.16	136.25	136.41	136.6	136.72	136.83000000000001	136.97	137.16	137.28	137.53	137.66999999999999	137.79	137.91	138.1	138.20999999999998	138.38000000000127	138.57	138.66999999999999	138.85000000000107	139.04	139.13	139.22999999999999	139.47	139.54	139.66999999999999	139.94999999999999	140.06	140.26999999999998	140.49	140.63	140.80000000000001	141	141.16999999999999	141.44999999999999	141.6	141.88000000000127	142.03	142.16999999999999	142.43	142.6	142.80000000000001	143.06	143.32000000000087	143.47999999999999	143.73999999999998	143.9	144.04	144.33000000000001	144.44	144.73999999999998	144.87	145.03	145.26	145.41	145.66	145.81	145.94	146.16999999999999	146.31	146.47999999999999	146.65	146.86000000000001	147.08000000000001	147.19999999999999	147.46	147.56	147.75	147.93	148.06	148.13999999999999	148.31	148.55000000000001	148.76	148.94999999999999	149.07	149.25	149.46	149.58000000000001	149.73999999999998	149.93	150.08000000000001	150.34	150.46	150.66	150.86000000000001	150.96	151.16	151.35000000000107	151.44999999999999	151.65	151.84	151.9	152.06	152.26999999999998	152.35000000000107	152.54	152.72	152.81	153.02000000000001	153.19999999999999	153.32000000000087	153.46	153.65	153.80000000000001	153.94	154.13	154.19999999999999	154.32000000000087	154.65	154.72	154.89000000000001	154.97	155.16999999999999	155.28	155.44	155.60999999999999	155.66999999999999	155.83000000000001	156.06	156.19999999999999	156.26999999999998	156.46	156.63	156.70999999999998	156.88000000000127	157.05000000000001	157.16	157.33000000000001	157.5	157.66	157.73999999999998	157.89000000000001	158.05000000000001	158.15	158.26999999999998	158.41	158.58000000000001	158.66	158.83000000000001	159	159.13999999999999	159.22999999999999	159.33000000000001	159.47	159.60999999999999	159.69999999999999	159.86000000000001	160.04	160.16	160.30000000000001	160.43	160.66999999999999	160.76999999999998	160.99	161.16999999999999	161.26	161.41999999999999	161.60999999999999	161.70999999999998	161.89000000000001	162.1	162.20999999999998	162.34	162.47999999999999	162.69	162.80000000000001	162.96	163.15	163.26999999999998	163.44	163.65	163.76	163.9	164.1	164.23999999999998	164.42000000000004	164.63	164.78	165.04	165.18	165.36	165.58	165.75	166.05	166.18	166.46	166.62	166.87	167.03	167.26	167.51	167.72	167.85000000000107	168.05	168.26999999999998	168.38000000000127	168.59	168.78	168.88000000000127	169.20999999999998	169.26999999999998	169.46	169.62	169.76999999999998	169.91	170.17	170.35000000000107	170.64	170.70999999999998	170.91	171.13	171.26999999999998	171.44	171.64	171.76999999999998	172	172.14	172.3	172.5	172.6	172.82000000000087	173.04	173.15	173.44	173.52	173.69	173.9	174	174.19	174.38000000000127	174.5	174.69	174.89000000000001	175.02	175.17	175.35000000000107	175.45000000000007	175.64	175.83	175.93	176.1	176.18	176.36	176.46	176.63	176.79	176.88000000000127	177.1	177.31	177.42000000000004	177.56	177.78	177.87	178.05	178.23	178.35000000000107	178.54	178.62	178.83	178.94	179.2	179.31	179.43	179.57	179.75	179.88000000000127	180.04	180.23	180.36	180.5	180.7	180.79	180.89000000000001	181.04	181.23	181.36	181.52	181.70999999999998	181.79	181.96	182.17	182.26999999999998	182.36	182.49	182.66	182.78	182.94	183.14	183.26	183.43	183.68	183.76	183.94	184.12	184.23999999999998	184.44	184.64	184.76999999999998	184.94	185.13	185.25	185.4	185.58	185.69	185.87	186.05	186.17	186.33	186.58	186.65	186.83	186.99	187.09	187.20999999999998	187.34	187.49	187.53	187.72	187.92000000000004	188.10999999999999	188.23999999999998	188.39000000000001	188.57	188.70999999999998	188.91	189.10999999999999	189.23999999999998	189.52	189.6	189.76999999999998	189.98000000000027	190.10999999999999	190.33	190.54	190.66	190.95000000000007	191.08	191.25	191.47	191.62	191.81	192.04	192.34	192.46	192.66	192.75	192.92000000000004	193.04	193.29	193.45000000000007	193.55	193.87	193.98000000000027	194.16	194.37	194.49	194.69	194.89000000000001	194.99	195.26999999999998	195.38000000000127	195.57	195.75	195.86	196.02	196.2	196.3	196.42000000000004	196.68	196.82000000000087	196.95000000000007	197.1	197.28	197.41	197.57	197.76999999999998	197.9	198.17	198.26	198.38000000000127	198.5	198.68	198.76	198.94	199.16	199.25	199.45000000000007	199.65	199.73999999999998	199.91	200.06	200.18	200.29	200.43	200.60999999999999	200.73	200.88000000000127	201.07	201.20999999999998	201.33	201.46	201.65	201.76999999999998	201.95000000000007	202.14	202.25	202.42000000000004	202.65	202.72	202.89000000000001	203.08	203.16	203.34	203.51	203.62	203.75	203.97	204.15	204.26999999999998	204.43	204.62	204.70999999999998	204.92000000000004	205.12	205.25	205.51	205.58	205.73	205.9	206.04	206.16	206.39000000000001	206.52	206.64	206.79	207	207.08	207.26	207.44	207.52	207.67	207.85000000000107	207.97	208.09	208.23999999999998	208.48000000000027	208.56	208.73999999999998	208.92000000000004	209	209.19	209.4	209.5	209.69	209.92000000000004	210.03	210.23	210.43	210.59	210.76999999999998	211	211.3	211.4	211.62	211.85000000000107	211.96	212.19	212.4	212.64	212.78	212.89000000000001	213.15	213.28	213.52	213.76	214	214.13	214.34	214.52	214.66	214.86	215.08	215.22	215.51	215.6	215.8	216.01	216.13	216.33	216.57	216.89000000000001	216.99	217.13	217.28	217.5	217.7	217.81	218.03	218.26999999999998	218.42000000000004	218.62	218.83	218.94	219.17	219.4	219.5	219.76999999999998	219.91	220.07	220.28	220.43	220.66	220.81	221.08	221.19	221.35000000000107	221.54	221.67	221.86	222.05	222.18	222.36	222.56	222.69	222.84	223.02	223.15	223.31	223.51	223.59	223.78	224	224.09	224.23999999999998	224.42000000000004	224.54	224.66	224.83	225.01	225.14	225.28	225.5	225.60999999999999	225.76	225.95000000000007	226.04	226.2	226.39000000000001	226.48000000000027	226.6	226.75	226.95000000000007	227.03	227.19	227.35000000000107	227.45000000000007	227.55	227.69	227.87	227.95000000000007	228.14	228.35000000000107	228.48000000000027	228.6	228.73999999999998	228.91	229	229.18	229.38000000000127	229.46	229.62	229.73999999999998	229.96	230.06	230.22	230.36	230.49	230.62	230.78	230.98000000000027	231.10999999999999	231.26	231.46	231.59	231.73999999999998	231.95000000000007	232.07	232.23999999999998	232.44	232.56	232.82000000000087	232.92000000000004	233.04	233.18	233.37	233.48000000000027	233.64	233.84	233.91	234.1	234.31	234.39000000000001	234.5	234.63	234.82000000000087	234.94	235.1	235.3	235.43	235.6	235.82000000000087	235.95000000000007	236.10999999999999	236.32000000000087	236.47	236.73	236.87	237.07	237.23999999999998	237.42000000000004	237.63	237.75	237.97	238.20999999999998	238.33	238.59	238.72	238.88000000000127	239.10999999999999	239.26999999999998	239.53	239.68	239.95000000000007	240.09	240.25	240.47	240.62	240.86	241.02	241.3	241.41	241.59	241.8	241.92000000000004	242.13	242.34	242.45000000000007	242.72	242.85000000000107	243.03	243.22	243.36	243.54	243.73999999999998	243.91	244.16	244.25	244.41	244.60999999999999	244.75	244.96	245.19	245.48000000000027	245.57	245.75	245.95000000000007	246.09	246.31	246.52	246.62	246.89000000000001	246.99	247.17	247.36	247.44	247.6	247.78	247.94	248.13	248.35000000000107	248.49	248.65	248.86	249.01	249.18	249.38000000000127	249.51	249.76	249.88000000000127	250.02	250.18	250.28	250.51	250.72	250.84	251.15	251.23	251.41	251.60999999999999	251.72	251.93	252.13	252.23999999999998	252.43	252.6	252.73	252.87	253.07	253.13	253.32000000000087	253.5	253.6	253.78	254.02	254.1	254.20999999999998	254.35000000000107	254.55	254.66	254.82000000000087	254.99	255.12	255.28	255.49	255.59	255.69	255.83	256.01	256.13	256.27	256.45	256.52	256.68	256.83999999999969	257.02999999999969	257.11	257.25	257.37	257.54000000000002	257.64000000000038	257.78999999999894	257.97999999999894	258.08999999999969	258.24	258.45	258.54000000000002	258.64999999999998	258.77	258.97000000000003	259.02999999999969	259.22000000000003	259.41999999999899	259.5	259.69	259.89	260.02	260.19	260.37	260.47999999999894	260.68	260.86	260.92999999999893	260.97999999999894	261.13	261.33999999999969	261.5	261.62	261.78999999999894	261.94	262.08	262.22999999999894	262.39	262.48999999999899	262.7	262.95	263.05	263.14000000000038	263.26	263.45	263.56	263.69	263.85000000000002	263.94	264.06	264.19	264.35000000000002	264.51	264.58	264.72999999999894	264.94	265.02	265.12	265.25	265.42999999999893	265.52999999999969	265.69	265.97000000000003	266.05	266.22999999999894	266.36	266.47999999999894	266.66000000000008	266.89	267.02	267.20999999999964	267.47999999999894	267.63	267.8	268.02	268.20999999999964	268.45	268.60000000000002	268.87	268.97000000000003	269.18	269.42999999999893	269.58999999999969	269.82	270.02999999999969	270.31	270.5	270.74	270.87	271.11	271.35000000000002	271.58	271.72000000000003	271.92999999999893	272.16000000000008	272.28999999999894	272.48999999999899	272.70999999999964	272.95999999999964	273.06	273.17	273.39	273.55	273.75	274	274.11	274.35000000000002	274.5	274.68	274.87	274.98999999999899	275.14000000000038	275.37	275.52	275.78999999999894	275.89999999999969	276.08999999999969	276.28999999999894	276.41999999999899	276.58	276.78999999999894	276.92999999999893	277.2	277.27	277.45	277.64999999999998	277.75	277.92999999999893	278.10000000000002	278.22000000000003	278.41999999999899	278.58999999999969	278.69	278.89	279.05	279.16000000000008	279.35000000000002	279.54000000000002	279.64000000000038	279.85000000000002	280.08999999999969	280.16000000000008	280.33	280.52999999999969	280.64000000000038	280.83999999999969	281.02999999999969	281.14999999999998	281.33999999999969	281.54000000000002	281.64999999999998	281.82	282.02	282.10000000000002	282.28999999999894	282.48999999999899	282.62	282.95	283.01	283.11	283.25	283.45999999999964	283.58999999999969	283.70999999999964	283.91999999999899	284.02999999999969	284.17	284.42999999999893	284.56	284.72000000000003	284.89	284.98999999999899	285.13	285.24	285.45999999999964	285.58999999999969	285.74	285.92999999999893	286.05	286.18	286.38	286.48999999999899	286.64999999999998	286.83999999999969	286.91999999999899	287.11	287.27999999999969	287.41999999999899	287.52999999999969	287.66000000000008	287.85000000000002	287.97000000000003	288.14000000000038	288.32	288.44	288.60000000000002	288.78999999999894	288.91999999999899	289.07	289.24	289.33999999999969	289.51	289.69	289.77999999999969	289.94	290.10000000000002	290.28999999999894	290.37	290.52999999999969	290.7	290.78999999999894	290.91000000000003	291.14000000000038	291.27	291.47000000000003	291.70999999999964	291.8	291.98999999999899	292.22000000000003	292.33	292.52	292.68	292.83	293.12	293.22999999999894	293.45	293.68	293.77999999999969	293.97000000000003	294.17	294.27	294.58	294.69	294.89999999999969	295.13	295.25	295.47000000000003	295.68	295.82	296.07	296.24	296.5	296.62	296.81	297.05	297.31	297.47000000000003	297.60000000000002	297.86	298.02	298.22999999999894	298.45	298.57	298.85000000000002	299	299.27999999999969	299.41000000000003	299.63	299.87	299.97999999999894	300.27	300.39999999999969	300.56	300.77999999999969	300.92999999999893	301.10000000000002	301.3	301.44	301.64000000000038	301.77999999999969	301.94	302.14999999999998	302.3	302.47000000000003	302.68	302.81	303.01	303.13	303.3	303.48999999999899	303.58999999999969	303.77999999999969	303.97000000000003	304.07	304.26	304.39	304.54000000000002	304.72999999999894	304.81	304.95999999999964	305.04000000000002	305.25	305.45999999999964	305.54000000000002	305.76	305.98999999999899	306.08	306.25	306.39999999999969	306.45	306.63	306.78999999999894	306.87	307.05	307.26	307.45	307.47999999999894	307.60000000000002	307.72999999999894	307.89	308.01	308.19	308.39	308.5	308.67	308.87	308.97000000000003	309.14000000000038	309.31	309.41999999999899	309.58999999999969	309.77	309.89999999999969	310.07	310.27	310.39999999999969	310.56	310.72000000000003	310.83999999999969	310.97000000000003	311.12	311.3	311.41999999999899	311.57	311.77999999999969	311.91000000000003	312.05	312.22999999999894	312.33	312.51	312.69	312.78999999999894	312.95	313.05	313.27999999999969	313.39	313.51	313.69	313.8	313.95999999999964	314.14999999999998	314.24	314.44	314.70999999999964	314.77999999999969	314.89999999999969	315.04000000000002	315.28999999999894	315.44	315.60000000000002	315.83	316.08	316.20999999999964	316.42999999999893	316.67	316.81	317	317.22000000000003	317.47999999999894	317.64000000000038	317.83	318.08	318.22999999999894	318.41000000000003	318.64000000000038	318.86	319.05	319.20999999999964	319.41000000000003	319.5	319.76	319.95999999999964	320.10000000000002	320.35000000000002	320.56	320.77999999999969	320.87	321.06	321.16000000000008	321.32	321.64999999999998	321.81	321.92999999999893	322.16000000000008	322.28999999999894	322.5	322.69	322.83	322.95999999999964	323.20999999999964	323.33	323.51	323.72999999999894	323.88	324.12	324.25	324.52999999999969	324.63	324.83	325.02999999999969	325.14000000000038	325.33999999999969	325.55	325.67	325.87	326.08	326.3	326.45999999999964	326.62	326.76	326.91000000000003	327.11	327.24	327.51	327.58999999999969	327.78	327.96999999999969	328.08	328.3	328.5	328.6	328.86	329.03	329.2	329.40999999999963	329.51	329.72999999999894	329.96	330.04	330.3	330.44	330.6	330.8	330.91999999999899	331.1	331.3	331.4	331.66	331.78999999999894	331.96999999999969	332.15000000000032	332.28	332.48999999999899	332.7	332.78999999999894	332.96999999999969	333.15000000000032	333.27	333.44	333.64000000000038	333.78	333.94	334.12	334.24	334.5	334.6	334.71	334.85	335.05	335.17	335.32	335.51	335.59	335.78	336.01	336.1	336.27	336.44	336.54	336.71	336.86	336.97999999999894	337.1	337.22999999999894	337.52	337.59	337.78999999999894	337.95	338.08	338.21	338.35	338.53	338.66	338.8	339.01	339.09	339.24	339.41999999999899	339.52	339.69	339.76	339.96	340.07	340.22999999999894	340.5	340.53	340.64000000000038	340.77	340.94	341.06	341.21	341.40999999999963	341.46999999999969	341.65000000000032	341.84000000000032	341.95	342.08	342.22999999999894	342.40999999999963	342.47999999999894	342.65000000000032	342.8	342.90999999999963	343.02	343.18	343.44	343.52	343.62	343.76	343.92999999999893	344.05	344.2	344.4	344.46999999999969	344.66	344.85	344.96	345.12	345.27	345.46	345.58	345.76	345.95	346.06	346.34000000000032	346.46	346.64000000000038	346.74	346.94	347.05	347.21	347.41999999999899	347.54	347.71999999999969	347.94	348.08	348.24	348.45	348.6	348.86	348.96999999999969	349.26	349.39	349.56	349.76	349.9	350.13	350.33	350.42999999999893	350.67	350.85	351.03	351.25	351.39	351.57	351.77	351.94	352.18	352.31	352.46999999999969	352.68	352.83	353.07	353.21	353.54	353.62	353.82	354.03	354.14000000000038	354.35	354.57	354.71999999999969	354.94	355.1	355.27	355.45	355.58	355.76	355.96	356.06	356.39	356.54	356.71	356.92999999999893	357.08	357.24	357.46	357.61	357.85	357.98999999999899	358.25	358.38	358.58	358.78999999999894	358.9	359.19	359.27	359.38	359.53	359.74	359.86	360.02	360.21	360.34000000000032	360.48999999999899	360.68	360.78999999999894	360.92999999999893	361.12	361.19	361.37	361.56	361.63	361.71999999999969	361.96999999999969	362.13	362.27	362.4	362.62	362.78	362.95	363.13	363.21999999999969	363.38	363.6	363.72999999999894	363.89	364.08	364.19	364.33	364.51	364.59	364.71999999999969	364.86	365.13	365.25	365.39	365.57	365.7	365.86	366.04	366.11	500 mm	390.5	391	391.5	392	392.5	393	393.5	394	394.5	395	395.5	396	396.5	397	397.5	398	398.5	399	399.5	400	400.5	401	401.5	402	402.5	403	403.5	404	404.5	405	405.5	406	406.5	407	407.5	408	408.5	409	409.5	410	410.5	411	411.5	412	412.5	413	413.5	414	414.5	415	415.5	416	416.5	417	417.5	418	418.5	419	419.5	420	420.5	421	421.5	422	422.5	423	423.5	424	424.5	425	425.5	426	426.5	427	427.5	428	428.5	429	429.5	430	430.5	431	431.5	432	432.5	433	433.5	434	434.5	435	435.5	436	436.5	437	437.5	438	438.5	439	439.5	440	440.5	441	441.5	442	442.5	443	443.5	444	444.5	445	445.5	446	446.5	447	447.5	448	448.5	449	449.5	450	450.5	451	451.5	452	452.5	453	453.5	454	454.5	455	455.5	456	456.5	457	457.5	458	458.5	459	459.5	460	460.5	461	461.5	462	462.5	463	463.5	464	464.5	465	465.5	466	466.5	467	467.5	468	468.5	469	469.5	470	470.5	471	471.5	472	472.5	473	473.5	474	474.5	475	475.5	476	476.5	477	477.5	478	478.5	479	479.5	480	480.5	481	481.5	482	482.5	483	483.5	484	484.5	485	485.5	486	486.5	487	487.5	488	488.5	489	489.5	490	490.5	491	491.5	492	492.5	493	493.5	494	494.5	495	495.5	496	496.5	497	497.5	498	498.5	499	499.5	500	500.5	501	501.5	502	502.5	503	503.5	504	504.5	505	505.5	506	506.5	507	507.5	508	508.5	509	509.5	510	510.5	511	511.5	512	512.5	513	513.5	514	514.5	515	515.5	516	516.5	517	517.5	518	518.5	519	519.5	520	520.5	521	521.5	522	522.5	523	523.5	524	524.5	525	525.5	526	526.5	527	527.5	528	528.5	529	529.5	530	530.5	531	531.5	532	532.5	533	533.5	534	534.5	535	535.5	536	536.5	537	537.5	538	538.5	539	539.5	540	540.5	541	541.5	542	542.5	543	543.5	544	544.5	545	545.5	546	546.5	547	547.5	548	548.5	549	549.5	550	550.5	551	551.5	552	552.5	553	553.5	554	554.5	555	555.5	556	556.5	557	557.5	558	558.5	559	559.5	560	560.5	561	561.5	562	562.5	563	563.5	564	564.5	565	565.5	566	566.5	567	567.5	568	568.5	569	569.5	570	570.5	571	571.5	572	572.5	573	573.5	574	574.5	575	575.5	576	576.5	577	577.5	578	578.5	579	579.5	580	580.5	581	581.5	582	582.5	583	583.5	584	584.5	585	585.5	586	586.5	587	587.5	588	588.5	589	589.5	590	590.5	591	591.5	592	592.5	593	593.5	594	594.5	595	595.5	596	596.5	597	597.5	598	598.5	599	599.5	600	600.5	601	601.5	602	602.5	603	603.5	604	604.5	605	605.5	606	606.5	607	607.5	608	608.5	609	609.5	610	610.5	611	611.5	612	612.5	613	613.5	614	614.5	615	615.5	616	616.5	617	617.5	618	618.5	619	619.5	620	620.5	621	621.5	622	622.5	623	623.5	624	624.5	625	625.5	626	626.5	627	627.5	628	628.5	629	629.5	630	630.5	631	631.5	632	632.5	633	633.5	634	634.5	635	635.5	636	636.5	637	637.5	638	638.5	639	639.5	640	640.5	641	641.5	642	642.5	643	643.5	644	644.5	645	645.5	646	646.5	647	647.5	648	648.5	649	649.5	650	650.5	651	651.5	652	652.5	653	653.5	654	654.5	655	655.5	656	656.5	657	657.5	658	658.5	659	659.5	660	660.5	661	661.5	662	662.5	663	663.5	664	664.5	665	665.5	666	666.5	667	667.5	668	668.5	669	669.5	670	670.5	671	671.5	672	672.5	673	673.5	674	674.5	675	675.5	676	676.5	677	677.5	678	678.5	679	679.5	680	680.5	681	681.5	682	682.5	683	683.5	684	684.5	685	685.5	686	686.5	687	687.5	688	688.5	689	689.5	690	690.5	691	691.5	692	692.5	693	693.5	694	694.5	695	695.5	696	696.5	697	697.5	698	698.5	699	699.5	700	700.5	701	701.5	702	702.5	703	703.5	704	704.5	705	705.5	706	706.5	707	707.5	708	708.5	709	709.5	710	710.5	711	711.5	712	712.5	713	713.5	714	714.5	715	715.5	716	716.5	717	717.5	718	718.5	719	719.5	720	720.5	721	721.5	722	722.5	723	723.5	724	724.5	725	725.5	726	726.5	727	727.5	728	728.5	729	729.5	730	730.5	731	731.5	732	732.5	733	733.5	734	734.5	735	735.5	736	736.5	737	737.5	738	738.5	739	739.5	740	740.5	741	741.5	742	742.5	743	743.5	744	744.5	745	745.5	746	746.5	747	747.5	748	748.5	749	749.5	750	750.5	751	751.5	752	752.5	753	753.5	754	754.5	755	755.5	756	756.5	757	757.5	758	758.5	759	759.5	760	760.5	761	761.5	762	762.5	763	763.5	764	764.5	765	765.5	766	766.5	767	767.5	768	768.5	769	769.5	770	770.5	771	771.5	772	772.5	773	773.5	774	774.5	775	775.5	776	776.5	777	777.5	778	778.5	779	779.5	780	780.5	781	781.5	782	782.5	783	783.5	784	784.5	785	785.5	786	786.5	787	787.5	788	788.5	789	789.5	790	790.5	791	791.5	792	792.5	793	793.5	794	794.5	795	795.5	796	796.5	797	797.5	798	798.5	799	799.5	800	800.5	801	801.5	802	802.5	803	803.5	804	804.5	805	805.5	806	806.5	807	807.5	808	808.5	809	809.5	810	810.5	811	811.5	812	812.5	813	813.5	814	814.5	815	815.5	816	816.5	817	817.5	818	818.5	819	819.5	820	820.5	821	821.5	822	822.5	823	823.5	824	824.5	825	825.5	826	826.5	827	827.5	828	828.5	829	829.5	830	830.5	831	831.5	832	832.5	833	833.5	834	834.5	835	835.5	836	836.5	837	837.5	838	838.5	839	839.5	840	840.5	841	841.5	842	842.5	843	843.5	844	844.5	845	845.5	846	846.5	847	847.5	848	848.5	849	849.5	850	850.5	851	851.5	852	852.5	853	853.5	854	854.5	855	855.5	856	856.5	857	857.5	858	858.5	859	859.5	860	860.5	861	861.5	862	862.5	863	863.5	864	864.5	865	865.5	866	866.5	867	867.5	868	868.5	869	869.5	870	870.5	871	871.5	872	872.5	873	873.5	874	874.5	875	875.5	876	876.5	877	877.5	878	878.5	879	879.5	880	880.5	881	881.5	882	882.5	883	883.5	884	884.5	885	885.5	886	886.5	887	887.5	888	888.5	889	889.5	890	890.5	891	891.5	892	892.5	893	893.5	894	894.5	895	895.5	896	896.5	897	897.5	898	898.5	899	899.5	900	900.5	901	901.5	902	902.5	903	903.5	904	904.5	905	905.5	906	906.5	907	907.5	908	908.5	909	909.5	910	910.5	911	911.5	912	912.5	913	913.5	914	914.5	915	915.5	916	916.5	917	917.5	918	918.5	919	919.5	920	920.5	921	921.5	922	922.5	923	923.5	924	924.5	925	925.5	926	926.5	927	927.5	928	928.5	929	929.5	930	930.5	931	931.5	932	932.5	933	933.5	934	934.5	935	935.5	936	936.5	937	937.5	938	938.5	939	939.5	940	940.5	941	941.5	942	942.5	943	943.5	944	944.5	945	945.5	946	946.5	947	947.5	948	948.5	949	949.5	950	950.5	951	951.5	952	952.5	953	953.5	954	954.5	955	955.5	956	956.5	957	957.5	958	958.5	959	959.5	960	960.5	961	961.5	962	962.5	963	963.5	964	964.5	965	965.5	966	966.5	967	967.5	968	968.5	969	969.5	970	970.5	971	971.5	972	972.5	973	973.5	974	974.5	975	975.5	976	976.5	977	977.5	978	978.5	979	979.5	980	980.5	981	981.5	982	982.5	983	983.5	984	984.5	985	985.5	986	986.5	987	987.5	988	988.5	989	989.5	990	990.5	991	991.5	992	992.5	993	993.5	994	994.5	995	995.5	996	996.5	997	997.5	998	998.5	999	999.5	1000	1000.5	1001	1001.5	1002	1002.5	1003	1003.5	1004	1004.5	1005	1005.5	1006	1006.5	1007	1007.5	1008	1008.5	1009	1009.5	1010	1010.5	1011	1011.5	1012	1012.5	1013	1013.5	1014	1014.5	1015	1015.5	1016	1016.5	1017	1017.5	1018	1018.5	1019	1019.5	1020	1020.5	1021	1021.5	1022	1022.5	1023	1023.5	1024	1024.5	1025	1025.5	1026	1026.5	1027	1027.5	1028	1028.5	1029	1029.5	1030	1030.5	1031	1031.5	1032	1032.5	1033	1033.5	1034	1034.5	1035	1035.5	1036	1036.5	1037	1037.5	1038	1038.5	1039	1039.5	1040	1040.5	1041	1041.5	1042	1042.5	1043	1043.5	1044	1044.5	1045	1045.5	1046	1046.5	1047	1047.5	1048	1048.5	1049	1049.5	1050	1050.5	1051	1051.5	1052	1052.5	1053	1053.5	1054	1054.5	1055	1055.5	1056	1056.5	1057	1057.5	1058	1058.5	1059	1059.5	1060	1060.5	1061	1061.5	1062	1062.5	1063	1063.5	1064	1064.5	1065	1065.5	1066	1066.5	1067	1067.5	1068	1068.5	1069	1069.5	1070	1070.5	1071	1071.5	1072	1072.5	1073	1073.5	1074	1074.5	1075	1075.5	1076	1076.5	1077	1077.5	1078	1078.5	1079	1079.5	1080	1080.5	1081	1081.5	1082	1082.5	1083	1083.5	1084	1084.5	1085	1085.5	1086	1086.5	1087	1087.5	1088	1088.5	1089	1089.5	1090	1090.5	1091	1091.5	1092	1092.5	1093	1093.5	1094	1094.5	1095	1095.5	1096	1096.5	1097	1097.5	1098	1098.5	1099	1099.5	1100	1100.5	1101	1101.5	1102	1102.5	1103	1103.5	1104	1104.5	1105	1105.5	1106	1106.5	1107	1107.5	1108	1108.5	1109	1109.5	1110	1110.5	1111	1111.5	1112	1112.5	1113	1113.5	1114	1114.5	1115	1115.5	1116	1116.5	1117	1117.5	1118	1118.5	1119	1119.5	1120	1120.5	1121	1121.5	1122	1122.5	1123	1123.5	1124	1124.5	1125	1125.5	1126	1126.5	1127	1127.5	1128	1128.5	1129	1129.5	1130	1130.5	1131	1131.5	1132	1132.5	1133	1133.5	1134	1134.5	1135	1135.5	1136	1136.5	1137	1137.5	1138	1138.5	1139	1139.5	1140	1140.5	1141	1141.5	1142	1142.5	1143	1143.5	1144	1144.5	1145	1145.5	1146	1146.5	1147	1147.5	1148	1148.5	1149	1149.5	1150	1150.5	1151	1151.5	1152	1152.5	1153	1153.5	1154	1154.5	1155	1155.5	1156	1156.5	1157	1157.5	1158	1158.5	1159	1159.5	1160	1160.5	1161	1161.5	1162	1162.5	1163	1163.5	1164	1164.5	1165	1165.5	1166	1166.5	1167	1167.5	1168	1168.5	1169	1169.5	1170	1170.5	1171	1171.5	1172	1172.5	1173	1173.5	1174	1174.5	1175	1175.5	1176	1176.5	1177	1177.5	1178	1178.5	1179	1179.5	1180	1180.5	1181	1181.5	1182	1182.5	1183	1183.5	1184	1184.5	1185	1185.5	1186	1186.5	1187	1187.5	1188	1188.5	1189	1189.5	1190	1190.5	1191	1191.5	1192	1192.5	1193	1193.5	1194	1194.5	1195	1195.5	1196	1196.5	1197	1197.5	1198	1198.5	1199	1199.5	1200	1200.5	1201	1201.5	1202	1202.5	1203	1203.5	1204	1204.5	1205	1205.5	1206	1206.5	1207	1207.5	1208	1208.5	1209	1209.5	1210	1210.5	1211	1211.5	1212	1212.5	1213	1213.5	1214	1214.5	1215	1215.5	1216	1216.5	1217	1217.5	1218	1218.5	1219	1219.5	1220	1220.5	1221	1221.5	1222	1222.5	1223	1223.5	1224	1224.5	1225	1225.5	1226	1226.5	1227	1227.5	1228	1228.5	1229	1229.5	1230	1230.5	1231	1231.5	1232	1232.5	1233	1233.5	1234	1234.5	1235	1235.5	1236	1236.5	1237	1237.5	1238	1238.5	1239	1239.5	1240	1240.5	1241	1241.5	1242	1242.5	1243	1243.5	1244	1244.5	1245	1245.5	1246	1246.5	1247	1247.5	1248	1248.5	1249	1249.5	1250	1250.5	1251	1251.5	1252	1252.5	1253	1253.5	1254	1254.5	1255	1255.5	1256	1256.5	1257	1257.5	1258	1258.5	1259	1259.5	1260	1260.5	1261	1261.5	1262	1262.5	1263	1263.5	1264	1264.5	1265	1265.5	1266	1266.5	1267	1267.5	1268	1268.5	1269	1269.5	1270	1270.5	1271	1271.5	1272	1272.5	1273	1273.5	1274	1274.5	1275	1275.5	1276	1276.5	1277	1277.5	1278	1278.5	1279	1279.5	1280	1280.5	1281	1281.5	1282	1282.5	1283	1283.5	1284	1284.5	1285	1285.5	1286	1286.5	1287	1287.5	1288	1288.5	1289	1289.5	1290	1290.5	1291	1291.5	1292	1292.5	1293	1293.5	1294	1294.5	1295	1295.5	1296	1296.5	1297	1297.5	1298	1298.5	1299	1299.5	1300	1300.5	1301	1301.5	1302	1302.5	1303	1303.5	1304	1304.5	1305	1305.5	1306	1306.5	1307	1307.5	1308	1308.5	1309	1309.5	1310	1310.5	1311	1311.5	1312	1312.5	1313	1313.5	1314	1314.5	1315	1315.5	1316	1316.5	1317	1317.5	1318	1318.5	1319	1319.5	1320	1320.5	1321	1321.5	1322	1322.5	1323	1323.5	1324	1324.5	1325	1325.5	1326	1326.5	1327	1327.5	1328	1328.5	1329	1329.5	1330	1330.5	1331	1331.5	1332	1332.5	1333	1333.5	1334	1334.5	1335	1335.5	1336	1336.5	1337	1337.5	1338	1338.5	1339	1339.5	1340	1340.5	1341	1341.5	1342	1342.5	1343	1343.5	1344	1344.5	1345	1345.5	1346	1346.5	1347	1347.5	1348	1348.5	1349	1349.5	1350	1350.5	1351	1351.5	1352	1352.5	1353	1353.5	1354	1354.5	1355	1355.5	1356	1356.5	1357	1357.5	1358	1358.5	1359	1359.5	1360	1360.5	1361	1361.5	1362	1362.5	1363	1363.5	1364	1364.5	1365	1365.5	1366	1366.5	1367	1367.5	1368	1368.5	1369	1369.5	1370	1370.5	1371	1371.5	1372	1372.5	1373	1373.5	1374	1374.5	1375	1375.5	1376	1376.5	1377	1377.5	1378	1378.5	1379	1379.5	1380	1380.5	1381	1381.5	1382	1382.5	1383	1383.5	1384	1384.5	1385	1385.5	1386	1386.5	1387	1387.5	1388	1388.5	1389	1389.5	1390	1390.5	1391	1391.5	1392	1392.5	1393	1393.5	1394	1394.5	1395	1395.5	1396	1396.5	1397	1397.5	1398	1398.5	1399	1399.5	1400	0	1.52	1.75	1.8900000000000001	2.06	2.12	2.21	2.42	2.58	3.24	3.58	3.8699999999999997	4.13	4.4000000000000004	4.6199999999999966	4.7699999999999996	4.9300000000000024	5.08	5.1499999999999995	5.25	5.3599999999999985	5.48	5.51	5.55	5.6199999999999966	5.74	5.8199999999999985	5.8599999999999985	5.9	5.9700000000000024	6.05	6.09	6.23	6.28	6.33	6.35	6.45	6.64	6.67	6.73	6.81	6.83	6.87	7.06	7.21	7.17	7.21	7.28	7.3599999999999985	7.4	7.55	7.55	7.59	7.6899999999999995	7.72	7.72	7.72	7.78	7.8599999999999985	7.96	7.95	7.98	8.1	8.129999999999999	8.16	8.2900000000000009	8.33	8.39	8.4600000000000026	8.51	8.61	8.69	8.7100000000000009	8.83	8.91	9.06	9.09	9.16	9.18	9.26	9.3000000000000007	9.43	9.4700000000000006	9.4700000000000006	9.4700000000000006	9.59	9.6399999999999988	9.7800000000000011	9.8000000000000007	9.82	9.83	9.93	9.91	10.130000000000001	10.18	10.19	10.25	10.32	10.33	10.360000000000024	10.41	10.48	10.55	10.54	10.57	10.61	10.68	10.7	10.739999999999998	10.79	10.81	10.84	10.91	10.89	10.89	10.91	11.16	11.239999999999998	11.49	11.870000000000006	12.04	12.26	12.52	12.68	12.91	13.05	13.1	13.31	13.450000000000006	13.54	13.68	13.81	13.89	14.04	14.16	14.31	14.46	14.68	14.81	14.97	15.04	15.19	15.25	15.43	15.48	15.54	15.56	15.68	15.8	15.860000000000024	16.059999999999999	16.279999999999987	16.36	16.66	16.809999999999999	17.03	17.309999999999999	17.610000000000031	17.959999999999987	18.130000000000031	18.39	18.649999999999999	18.93	19.350000000000001	19.510000000000005	19.72	19.95	20.09	20.34	20.59	20.79	20.9	21.12	21.330000000000005	21.43	21.67	21.86	21.99	22.259999999999987	22.32	22.419999999999987	22.650000000000031	22.82	23.03	23.12	23.34	23.610000000000031	23.73	23.93	24.09	24.17	24.21	24.279999999999987	24.52	24.610000000000031	24.72	24.82	24.959999999999987	25.01	25.05	25.17	25.37	25.479999999999986	25.66	25.72	25.95	26.110000000000031	26.259999999999987	26.43	26.49	26.650000000000031	26.72	26.9	26.95	26.979999999999986	27.12	27.1	27.110000000000031	27.37	27.39	27.45	27.56	27.67	27.71	27.73	27.79	27.84	27.91	28.04	28.110000000000031	28.17	28.25	28.29	28.419999999999987	28.49	28.55	28.650000000000031	28.69	28.72	28.77	28.85	28.9	28.979999999999986	29.08	29.27	29.47	29.56	29.66	29.72	29.75	29.979999999999986	30.03	30.130000000000031	30.24	30.39	30.41	30.47	30.6	30.77	30.79	30.830000000000005	30.89	31	31.12	31.14	31.72	32.39	32.97	33.17	33.520000000000003	33.67	33.849999999999994	33.96	34.01	34.14	34.230000000000011	34.339999999999996	34.42	34.620000000000012	34.65	34.720000000000013	34.800000000000004	34.82	34.86	34.910000000000004	34.980000000000004	35.120000000000012	35.190000000000012	35.300000000000004	35.51	35.78	35.800000000000004	35.9	36.130000000000003	36.21	36.300000000000004	36.449999999999996	36.53	36.6	36.64	36.720000000000013	36.800000000000004	36.870000000000005	37.020000000000003	37.11	37.260000000000012	37.49	37.520000000000003	37.61	37.74	37.910000000000004	37.949999999999996	38.04	38.1	38.160000000000011	38.260000000000012	38.339999999999996	38.5	38.71	38.82	38.980000000000004	39.11	39.18	39.339999999999996	39.49	39.57	39.67	39.770000000000003	39.980000000000004	40.04	40.120000000000012	40.21	40.260000000000012	40.379999999999995	40.449999999999996	40.51	40.590000000000003	40.760000000000012	40.92	40.99	41.15	41.27	41.39	41.46	41.56	41.620000000000012	41.78	41.839999999999996	41.99	42.14	42.25	42.36	42.55	42.64	42.809999999999995	42.98	43.08	43.18	43.39	43.52	43.63	43.75	43.93	44.08	44.120000000000012	44.220000000000013	44.32	44.47	44.55	44.660000000000011	44.78	45	45.14	45.3	45.56	45.71	45.91	46.14	46.290000000000013	46.53	46.68	46.98	47.05	47.230000000000011	47.449999999999996	47.53	47.68	47.86	47.949999999999996	48.04	48.190000000000012	48.36	48.52	48.59	48.730000000000011	48.8	48.97	49.09	49.24	49.4	49.47	49.63	49.77	49.89	50.05	50.17	50.309999999999995	50.449999999999996	50.56	51.61	51.949999999999996	52.21	52.46	52.6	52.77	52.949999999999996	53.06	53.21	53.37	53.44	53.6	53.8	53.879999999999995	54	54.260000000000012	54.379999999999995	54.77	54.879999999999995	55.17	55.4	55.7	55.96	56.24	56.44	56.690000000000012	56.809999999999995	57.05	57.28	57.52	57.690000000000012	57.9	58.15	58.290000000000013	58.53	58.75	58.98	59.1	59.3	59.449999999999996	59.55	59.67	59.809999999999995	59.949999999999996	59.97	60.14	60.3	60.37	60.449999999999996	60.55	60.730000000000011	60.74	60.790000000000013	60.82	60.93	61.160000000000011	61.33	61.47	61.64	61.71	61.849999999999994	61.949999999999996	62.160000000000011	62.13	62.21	62.309999999999995	62.41	62.46	62.54	62.620000000000012	62.7	62.87	62.94	63.02	63.13	63.25	63.32	63.4	63.5	63.63	63.64	63.71	63.790000000000013	63.87	63.96	64.179999999999978	64.34	64.510000000000005	64.75	64.900000000000006	65.05	65.349999999999994	65.61	65.739999999999995	66.010000000000005	66.169999999999987	66.430000000000007	66.66	66.84	66.95	67.06	67.27	67.39	67.53	67.679999999999978	67.83	67.97	68.14	68.349999999999994	68.489999999999995	68.63	68.8	68.95	69.08	69.239999999999995	69.34	69.5	69.649999999999991	69.86999999999999	69.910000000000025	70.02	70.14	70.239999999999995	70.31	70.47	70.66	70.739999999999995	70.84	71.11	71.38	71.45	71.64	71.83	71.930000000000007	72.099999999999994	72.31	72.39	72.5	72.61999999999999	72.790000000000006	72.88	72.959999999999994	73.040000000000006	73.16	73.31	73.38	73.540000000000006	73.679999999999978	73.739999999999995	73.84	73.989999999999995	74.179999999999978	74.36999999999999	74.53	74.599999999999994	74.709999999999994	74.930000000000007	75.069999999999993	75.2	75.36	75.410000000000025	75.489999999999995	75.739999999999995	75.8	75.83	76.010000000000005	76.06	76.11	76.36999999999999	76.52	76.790000000000006	77.03	77.260000000000005	77.39	77.69	78	78.430000000000007	78.61999999999999	78.86999999999999	79.14	79.31	79.5	79.73	79.97	80.11	80.260000000000005	80.47	80.61	80.78	80.97	81.099999999999994	81.319999999999993	81.45	81.61	81.7	81.900000000000006	82	82.14	82.31	82.440000000000026	82.57	82.740000000000023	82.95	83.08	83.210000000000022	83.4	83.48	83.669999999999987	83.86	83.940000000000026	84.11	84.36	84.57	84.82	85.07	85.23	85.43	85.649999999999991	85.86999999999999	86	86.179999999999978	86.25	86.45	86.58	86.740000000000023	86.93	87.04	87.19	87.43	87.48	87.56	87.72	87.940000000000026	88.149999999999991	88.23	88.45	88.53	88.8	88.9	88.98	89.11	89.29	89.42	89.59	89.77	89.85	90.01	90.240000000000023	90.29	90.47	90.66	90.75	90.89	91	91.16	91.28	91.39	91.58	91.73	91.81	91.98	92.11	92.179999999999978	92.2	92.36	92.56	92.63	92.86	93.09	93.32	93.54	93.75	93.89	94.07	94.179999999999978	94.35	94.42	94.73	94.84	94.97	95.11999999999999	95.3	95.42	95.6	95.79	95.93	96.09	96.3	96.45	96.6	96.75	96.79	96.93	97.02	97.169999999999987	97.25	97.39	97.56	97.669999999999987	97.940000000000026	97.97	98.09	98.2	98.36999999999999	98.48	98.63	98.79	98.86999999999999	98.990000000000023	99.11	99.27	99.43	99.51	99.61	99.72	99.910000000000025	99.98	100.14	100.31	100.4	100.66	100.97	101.2	101.48	101.67999999999998	101.99000000000002	102.31	102.49000000000002	102.76	102.95	103.26	103.66	103.85	104.05	104.31	104.55	104.81	105.08	105.22	105.42	105.66	105.84	106.16999999999999	106.4	106.55	106.74000000000002	106.95	107.1	107.3	107.5	107.61	107.78	107.97	108.03	108.2	108.35	108.36999999999999	108.48	108.66999999999999	108.78	108.9	109.02	109.16	109.27	109.36	109.66999999999999	109.81	110.04	110.17999999999998	110.38	110.6	110.73	111	111.06	111.16	111.28	111.44000000000032	111.54	111.71000000000002	111.77	111.96000000000002	112.06	112.17999999999998	112.4	112.51	112.55	112.61	112.82	112.86999999999999	112.92	113.07	113.26	113.34	113.55	113.9	114.07	114.2	114.38	114.52	114.73	114.93	115.05	115.16999999999999	115.28	115.41000000000012	115.53	115.91000000000012	116.05	116.3	116.55	116.76	116.86999999999999	116.99000000000002	117.17999999999998	117.28	117.51	117.72	117.82	118.09	118.21000000000002	118.34	118.56	118.74000000000002	118.96000000000002	119.16	119.25	119.6	119.71000000000002	119.91000000000012	120.13	120.28	120.48	120.72	120.96000000000002	121.1	121.28	121.39	121.56	121.67999999999998	121.83	121.96000000000002	122.01	122.11999999999999	122.27	122.39	122.46000000000002	122.7	122.77	122.85	122.96000000000002	123.08	123.16999999999999	123.23	123.36	123.54	123.66	123.84	124.03	124.23	124.36	124.53	124.73	124.88	125.08	125.28	125.42	125.55	125.7	125.76	125.86999999999999	125.94000000000032	126.04	126.14	126.25	126.4	126.59	126.72	126.86	127.04	127.17999999999998	127.24000000000002	127.33	127.41000000000012	127.45	127.61	127.61999999999999	127.7	127.81	127.95	128.02000000000001	128.13999999999999	128.26	128.44999999999999	128.53	128.66	128.73999999999998	128.82000000000087	128.91	129.01	129.08000000000001	129.22	129.30000000000001	129.49	129.60999999999999	129.76	129.97	130.04	130.26	130.53	130.68	130.83000000000001	131.05000000000001	131.19	131.53	131.65	131.94999999999999	132.16999999999999	132.41999999999999	132.59	132.94999999999999	133.22	133.32000000000087	133.56	133.81	133.99	134.31	134.60999999999999	134.79	135.04	135.15	135.38000000000127	135.68	135.9	136.08000000000001	136.23999999999998	136.4	136.58000000000001	136.80000000000001	136.99	137.13	137.44	137.53	137.72999999999999	137.9	137.99	138.1	138.22999999999999	138.4	138.46	138.6	138.69	138.83000000000001	138.88000000000127	138.96	139.16	139.19	139.30000000000001	139.41	139.53	139.62	139.80000000000001	140.09	140.28	140.62	140.79	141.09	141.25	141.51	141.73999999999998	141.97	142.05000000000001	142.22999999999999	142.4	142.51	142.66999999999999	142.75	142.94999999999999	143.03	143.16	143.35000000000107	143.52000000000001	143.55000000000001	143.65	143.87	143.96	144.07	144.22	144.36000000000001	144.43	144.6	144.76999999999998	144.84	144.99	145.01	145.07	145.22999999999999	145.38000000000127	145.47	145.54	145.66999999999999	145.86000000000001	145.96	146.06	146.13	146.28	146.34	146.57	146.62	146.83000000000001	147.08000000000001	147.26	147.47999999999999	147.86000000000001	148.03	148.26	148.54	148.81	149.16	149.31	149.54	149.82000000000087	150.03	150.36000000000001	150.6	150.76999999999998	150.96	151.19999999999999	151.44	151.66999999999999	151.78	152.10999999999999	152.25	152.53	152.69	152.9	152.97999999999999	153.16	153.32000000000087	153.52000000000001	153.63	153.72999999999999	153.78	153.97999999999999	154.05000000000001	154.13	154.23999999999998	154.37	154.41	154.51	154.60999999999999	154.85000000000107	155.07	155.26	155.5	155.72	155.80000000000001	156.05000000000001	156.30000000000001	156.6	156.80000000000001	156.96	157.13999999999999	157.22999999999999	157.38000000000127	157.44999999999999	157.63	157.69999999999999	157.89000000000001	158.06	158.19999999999999	158.22	158.30000000000001	158.4	158.57	158.66	158.79	158.93	159.10999999999999	159.22	159.36000000000001	159.51	159.75	159.76999999999998	159.88000000000127	160	160.16	160.26999999999998	160.41	160.6	160.66999999999999	160.78	160.91	161.09	161.22	161.33000000000001	161.47	161.6	161.72	161.99	162.23999999999998	162.55000000000001	162.63	162.80000000000001	163.04	163.15	163.36000000000001	163.6	163.69999999999999	163.94	164.07	164.20999999999998	164.4	164.5	164.68	164.84	164.93	165.09	165.19	165.37	165.47	165.54	165.7	165.84	165.91	166	166.10999999999999	166.28	166.34	166.52	166.59	166.75	166.82000000000087	167.02	167.1	167.22	167.29	167.34	167.54	167.64	167.76	167.81	167.97	168.10999999999999	168.42000000000004	168.65	168.76	168.95000000000007	169.15	169.31	169.5	169.65	169.78	170.08	170.18	170.36	170.59	170.9	171.26	171.43	171.69	171.97	172.16	172.5	172.76999999999998	172.95000000000007	173.15	173.4	173.56	173.83	173.98000000000027	174.23999999999998	174.45000000000007	174.57	174.8	174.93	175.23	175.37	175.63	175.75	175.92000000000004	176.1	176.16	176.38000000000127	176.6	176.67	176.83	176.98000000000027	177.08	177.14	177.31	177.49	177.57	177.69	177.9	178.01	178.42000000000004	178.54	178.8	179.09	179.36	179.60999999999999	179.85000000000107	180	180.16	180.38000000000127	180.52	180.69	180.89000000000001	181.02	181.20999999999998	181.29	181.42000000000004	181.60999999999999	181.67	181.76999999999998	181.91	182.04	182.12	182.3	182.41	182.49	182.57	182.83	182.88000000000127	182.98000000000027	183.05	183.23	183.34	183.43	183.53	183.70999999999998	183.78	183.88000000000127	184	184.13	184.2	184.41	184.51	184.6	184.81	184.92000000000004	185.03	185.17	185.35000000000107	185.46	185.60999999999999	185.81	185.92000000000004	186.05	186.19	186.38000000000127	186.46	186.70999999999998	187.20999999999998	187.51	187.87	188.06	188.38000000000127	188.78	188.99	189.31	189.53	189.76999999999998	190.15	190.33	190.51	190.79	191	191.26999999999998	191.54	191.75	191.94	192.16	192.3	192.48000000000027	192.68	192.82000000000087	193.08	193.16	193.3	193.39000000000001	193.57	193.66	193.82000000000087	193.97	194.06	194.17	194.29	194.47	194.53	194.68	194.73	194.83	194.96	195.12	195.16	195.25	195.37	195.57	195.72	195.89000000000001	196.23	196.32000000000087	196.47	196.62	196.79	196.93	197.08	197.26999999999998	197.37	197.5	197.66	197.73999999999998	197.83	197.95000000000007	198.08	198.14	198.23999999999998	198.33	198.45000000000007	198.55	198.63	198.73999999999998	198.86	198.94	199.02	199.10999999999999	199.16	199.33	199.38000000000127	199.53	199.56	199.66	199.78	199.95000000000007	200	200.08	200.2	200.35000000000107	200.39000000000001	200.41	200.54	200.73999999999998	200.8	200.96	201.04	201.22	201.29	201.36	201.49	201.69	201.95000000000007	202.2	202.52	202.7	202.91	203.17	203.34	203.66	203.97	204.15	204.35000000000107	204.6	204.84	204.95000000000007	205.17	205.42000000000004	205.53	205.76999999999998	206	206.16	206.33	206.56	206.78	206.9	207.08	207.29	207.41	207.65	207.88000000000127	208.14	208.29	208.5	208.72	208.83	209.04	209.26999999999998	209.54	209.68	209.81	209.95000000000007	210.14	210.3	210.46	210.64	210.76	210.9	211.16	211.16	211.26999999999998	211.47	211.52	211.5	211.69	211.78	211.9	212.04	212.23999999999998	212.3	212.38000000000127	212.5	212.76999999999998	212.76999999999998	212.88000000000127	213.01	213.17	213.23999999999998	213.41	213.59	213.68	213.76999999999998	213.88000000000127	214.05	214.12	214.25	214.33	214.51	214.67	214.76	214.86	214.97	215.16	215.20999999999998	215.34	215.42000000000004	215.57	215.66	215.9	215.93	216.04	216.12	216.15	216.32000000000087	216.39000000000001	216.57	216.73	216.84	217.02	217.23	217.51	217.83	218.2	218.42000000000004	218.8	219.09	219.38000000000127	219.68	219.92000000000004	220.15	220.44	220.63	220.81	221.06	221.16	221.4	221.60999999999999	221.86	221.98000000000027	222.16	222.23	222.45000000000007	222.59	222.72	222.91	222.99	223.1	223.23	223.43	223.48000000000027	223.7	223.94	224.1	224.28	224.5	224.64	224.84	224.98000000000027	225.12	225.32000000000087	225.47	225.64	225.85000000000107	225.99	226.29	226.46	226.60999999999999	226.76999999999998	226.86	227.1	227.32000000000087	227.45000000000007	227.58	227.76	227.8	227.86	228.01	228.16	228.28	228.45000000000007	228.66	228.72	228.89000000000001	229.03	229.15	229.26999999999998	229.39000000000001	229.55	229.65	229.76	229.86	230.1	230.18	230.28	230.41	230.65	230.70999999999998	230.81	230.92000000000004	231.09	231.16	231.34	231.4	231.56	231.68	231.82000000000087	231.96	232.16	232.22	232.31	232.42000000000004	232.65	233.02	233.45000000000007	233.7	234.08	234.33	234.64	234.98000000000027	235.22	235.48000000000027	235.64	235.94	236.31	236.48000000000027	236.67	236.9	237.13	237.39000000000001	237.53	237.76	237.92000000000004	238.15	238.29	238.46	238.65	238.79	238.92000000000004	239.14	239.25	239.39000000000001	239.54	239.63	239.81	240	240.05	240.15	240.26999999999998	240.43	240.7	240.75	240.84	241.07	241.13	241.36	241.6	241.78	242.06	242.22	242.4	242.59	242.70999999999998	242.84	243.02	243.12	243.35000000000107	243.54	243.57	243.73999999999998	243.93	243.97	244.06	244.22	244.33	244.45000000000007	244.58	244.7	244.83	244.92000000000004	245.04	245.15	245.28	245.42000000000004	245.49	245.59	245.73	245.84	245.92000000000004	246.1	246.28	246.41	246.62	246.76	246.89000000000001	247.14	247.32000000000087	247.7	247.95000000000007	248.09	248.38000000000127	248.51	248.73999999999998	249.07	249.31	249.47	249.70999999999998	249.86	250.1	250.41	250.78	251.1	251.4	251.66	251.97	252.18	252.26999999999998	252.44	252.68	252.83	252.98000000000027	253.18	253.29	253.55	253.60999999999999	253.70999999999998	253.84	254.01	254.14	254.29	254.44	254.53	254.62	254.75	254.91	255.09	255.14	255.23999999999998	255.34	255.47	255.55	255.65	255.75	255.88000000000127	255.95000000000007	256.05	256.17	256.33	256.47000000000003	256.74	256.89999999999969	257.06	257.26	257.39	257.52999999999969	257.74	257.81	257.95	258.04000000000002	258.17	258.27999999999969	258.37	258.52	258.70999999999964	258.78999999999894	258.89	259.02	259.14000000000038	259.20999999999964	259.28999999999894	259.39	259.57	259.63	259.74	259.89999999999969	259.95999999999964	260.10000000000002	260.25	260.33999999999969	260.38	260.52999999999969	260.76	260.89	261.04000000000002	261.24	261.35000000000002	261.54000000000002	261.91000000000003	262.08	262.28999999999894	262.70999999999964	262.83	263.07	263.32	263.51	263.8	264.04000000000002	264.18	264.39	264.62	264.76	264.95999999999964	265.17	265.41000000000003	265.5	265.61	265.75	265.89999999999969	265.97999999999894	266.16000000000008	266.35000000000002	266.42999999999893	266.58999999999969	266.77	266.95999999999964	267.07	267.22000000000003	267.41000000000003	267.52	267.72999999999894	267.8	267.91999999999899	267.98999999999899	268.17	268.36	268.56	268.58999999999969	268.78999999999894	269.08	269.33	269.57	269.82	269.94	270.07	270.27999999999969	270.45	270.64000000000038	270.87	270.98999999999899	271.24	271.33	271.44	271.57	271.72999999999894	271.78999999999894	271.89	272.01	272.20999999999964	272.27	272.35000000000002	272.47999999999894	272.61	272.68	272.89999999999969	273	273.11	273.19	273.36	273.39999999999969	273.60000000000002	273.74	273.86	273.97000000000003	274.08999999999969	274.28999999999894	274.36	274.52999999999969	274.63	274.76	274.91000000000003	274.98999999999899	275.14999999999998	275.33	275.45999999999964	275.68	275.95	276.02999999999969	276.22999999999894	276.42999999999893	276.55	276.77	276.98999999999899	277.11	277.35000000000002	277.47999999999894	277.63	277.81	277.89	278.02999999999969	278.18	278.26	278.37	278.51	278.72000000000003	278.91000000000003	279.10000000000002	279.35000000000002	279.60000000000002	279.87	280.18	280.47999999999894	280.74	281	281.14999999999998	281.51	281.83999999999969	282.01	282.28999999999894	282.45999999999964	282.69	283.01	283.25	283.39999999999969	283.67	283.8	284.02999999999969	284.3	284.51	284.69	284.83999999999969	284.92999999999893	285.13	285.27	285.39	285.61	285.72999999999894	285.85000000000002	286.04000000000002	286.11	286.19	286.31	286.5	286.57	286.75	286.87	286.97000000000003	287.06	287.20999999999964	287.35000000000002	287.41000000000003	287.57	287.67	287.77999999999969	287.85000000000002	288	288.05	288.13	288.20999999999964	288.28999999999894	288.47000000000003	288.57	288.7	288.81	288.88	288.95999999999964	289.05	289.2	289.24	289.44	289.54000000000002	289.72000000000003	290.02999999999969	290.2	290.36	290.56	290.74	290.91000000000003	291.02999999999969	291.24	291.33	291.41999999999899	291.64000000000038	291.77	291.87	292.12	292.33999999999969	292.47999999999894	292.8	292.92999999999893	293.19	293.61	293.81	294.19	294.39	294.8	295.10000000000002	295.36	295.67	295.88	296.25	296.45999999999964	296.70999999999964	296.98999999999899	297.17	297.36	297.61	297.81	298	298.39999999999969	298.66000000000008	299.14999999999998	299.37	299.56	299.83999999999969	300.05	300.33999999999969	300.54000000000002	300.64000000000038	300.76	301.02999999999969	301.14999999999998	301.32	301.56	301.64999999999998	301.75	301.97000000000003	302.06	302.19	302.27999999999969	302.42999999999893	302.42999999999893	302.52	302.64000000000038	302.8	302.85000000000002	302.91999999999899	303.08	303.22000000000003	303.26	303.41000000000003	303.47000000000003	303.64999999999998	303.75	303.77999999999969	303.86	303.95999999999964	304.08999999999969	304.16000000000008	304.17	304.14999999999998	304.27999999999969	304.45999999999964	304.44	304.56	304.64000000000038	304.77	304.85000000000002	304.91999999999899	305.02999999999969	305.14000000000038	305.24	305.33	305.45999999999964	305.58	305.69	305.83	306.11	306.24	306.41999999999899	306.69	306.81	307.06	307.19	307.36	307.56	307.64000000000038	307.78999999999894	307.94	308.06	308.18	308.32	308.45999999999964	308.64999999999998	308.78999999999894	308.97000000000003	309.26	309.51	309.88	310.06	310.33	310.61	310.8	311.13	800 mm	486	486.5	487	487.5	488	488.5	489	489.5	490	490.5	491	491.5	492	492.5	493	493.5	494	494.5	495	495.5	496	496.5	497	497.5	498	498.5	499	499.5	500	500.5	501	501.5	502	502.5	503	503.5	504	504.5	505	505.5	506	506.5	507	507.5	508	508.5	509	509.5	510	510.5	511	511.5	512	512.5	513	513.5	514	514.5	515	515.5	516	516.5	517	517.5	518	518.5	519	519.5	520	520.5	521	521.5	522	522.5	523	523.5	524	524.5	525	525.5	526	526.5	527	527.5	528	528.5	529	529.5	530	530.5	531	531.5	532	532.5	533	533.5	534	534.5	535	535.5	536	536.5	537	537.5	538	538.5	539	539.5	540	540.5	541	541.5	542	542.5	543	543.5	544	544.5	545	545.5	546	546.5	547	547.5	548	548.5	549	549.5	550	550.5	551	551.5	552	552.5	553	553.5	554	554.5	555	555.5	556	556.5	557	557.5	558	558.5	559	559.5	560	560.5	561	561.5	562	562.5	563	563.5	564	564.5	565	565.5	566	566.5	567	567.5	568	568.5	569	569.5	570	570.5	571	571.5	572	572.5	573	573.5	574	574.5	575	575.5	576	576.5	577	577.5	578	578.5	579	579.5	580	580.5	581	581.5	582	582.5	583	583.5	584	584.5	585	585.5	586	586.5	587	587.5	588	588.5	589	589.5	590	590.5	591	591.5	592	592.5	593	593.5	594	594.5	595	595.5	596	596.5	597	597.5	598	598.5	599	599.5	600	600.5	601	601.5	602	602.5	603	603.5	604	604.5	605	605.5	606	606.5	607	607.5	608	608.5	609	609.5	610	610.5	611	611.5	612	612.5	613	613.5	614	614.5	615	615.5	616	616.5	617	617.5	618	618.5	619	619.5	620	620.5	621	621.5	622	622.5	623	623.5	624	624.5	625	625.5	626	626.5	627	627.5	628	628.5	629	629.5	630	630.5	631	631.5	632	632.5	633	633.5	634	634.5	635	635.5	636	636.5	637	637.5	638	638.5	639	639.5	640	640.5	641	641.5	642	642.5	643	643.5	644	644.5	645	645.5	646	646.5	647	647.5	648	648.5	649	649.5	650	650.5	651	651.5	652	652.5	653	653.5	654	654.5	655	655.5	656	656.5	657	657.5	658	658.5	659	659.5	660	660.5	661	661.5	662	662.5	663	663.5	664	664.5	665	665.5	666	666.5	667	667.5	668	668.5	669	669.5	670	670.5	671	671.5	672	672.5	673	673.5	674	674.5	675	675.5	676	676.5	677	677.5	678	678.5	679	679.5	680	680.5	681	681.5	682	682.5	683	683.5	684	684.5	685	685.5	686	686.5	687	687.5	688	688.5	689	689.5	690	690.5	691	691.5	692	692.5	693	693.5	694	694.5	695	695.5	696	696.5	697	697.5	698	698.5	699	699.5	700	700.5	701	701.5	702	702.5	703	703.5	704	704.5	705	705.5	706	706.5	707	707.5	708	708.5	709	709.5	710	710.5	711	711.5	712	712.5	713	713.5	714	714.5	715	715.5	716	716.5	717	717.5	718	718.5	719	719.5	720	720.5	721	721.5	722	722.5	723	723.5	724	724.5	725	725.5	726	726.5	727	727.5	728	728.5	729	729.5	730	730.5	731	731.5	732	732.5	733	733.5	734	734.5	735	735.5	736	736.5	737	737.5	738	738.5	739	739.5	740	740.5	741	741.5	742	742.5	743	743.5	744	744.5	745	745.5	746	746.5	747	747.5	748	748.5	749	749.5	750	750.5	751	751.5	752	752.5	753	753.5	754	754.5	755	755.5	756	756.5	757	757.5	758	758.5	759	759.5	760	760.5	761	761.5	762	762.5	763	763.5	764	764.5	765	765.5	766	766.5	767	767.5	768	768.5	769	769.5	770	770.5	771	771.5	772	772.5	773	773.5	774	774.5	775	775.5	776	776.5	777	777.5	778	778.5	779	779.5	780	780.5	781	781.5	782	782.5	783	783.5	784	784.5	785	785.5	786	786.5	787	787.5	788	788.5	789	789.5	790	790.5	791	791.5	792	792.5	793	793.5	794	794.5	795	795.5	796	796.5	797	797.5	798	798.5	799	799.5	800	800.5	801	801.5	802	802.5	803	803.5	804	804.5	805	805.5	806	806.5	807	807.5	808	808.5	809	809.5	810	810.5	811	811.5	812	812.5	813	813.5	814	814.5	815	815.5	816	816.5	817	817.5	818	818.5	819	819.5	820	820.5	821	821.5	822	822.5	823	823.5	824	824.5	825	825.5	826	826.5	827	827.5	828	828.5	829	829.5	830	830.5	831	831.5	832	832.5	833	833.5	834	834.5	835	835.5	836	836.5	837	837.5	838	838.5	839	839.5	840	840.5	841	841.5	842	842.5	843	843.5	844	844.5	845	845.5	846	846.5	847	847.5	848	848.5	849	849.5	850	850.5	851	851.5	852	852.5	853	853.5	854	854.5	855	855.5	856	856.5	857	857.5	858	858.5	859	859.5	860	860.5	861	861.5	862	862.5	863	863.5	864	864.5	865	865.5	866	866.5	867	867.5	868	868.5	869	869.5	870	870.5	871	871.5	872	872.5	873	873.5	874	874.5	875	875.5	876	876.5	877	877.5	878	878.5	879	879.5	880	880.5	881	881.5	882	882.5	883	883.5	884	884.5	885	885.5	886	886.5	887	887.5	888	888.5	889	889.5	890	890.5	891	891.5	892	892.5	893	893.5	894	894.5	895	895.5	896	896.5	897	897.5	898	898.5	899	899.5	900	900.5	901	901.5	902	902.5	903	903.5	904	904.5	905	905.5	906	906.5	907	907.5	908	908.5	909	909.5	910	910.5	911	911.5	912	912.5	913	913.5	914	914.5	915	915.5	916	916.5	917	917.5	918	918.5	919	919.5	920	920.5	921	921.5	922	922.5	923	923.5	924	924.5	925	925.5	926	926.5	927	927.5	928	928.5	929	929.5	930	930.5	931	931.5	932	932.5	933	933.5	934	934.5	935	935.5	936	936.5	937	937.5	938	938.5	939	939.5	940	940.5	941	941.5	942	942.5	943	943.5	944	944.5	945	945.5	946	946.5	947	947.5	948	948.5	949	949.5	950	950.5	951	951.5	952	952.5	953	953.5	954	954.5	955	955.5	956	956.5	957	957.5	958	958.5	959	959.5	960	960.5	961	961.5	962	962.5	963	963.5	964	964.5	965	965.5	966	966.5	967	967.5	968	968.5	969	969.5	970	970.5	971	971.5	972	972.5	973	973.5	974	974.5	975	975.5	976	976.5	977	977.5	978	978.5	979	979.5	980	980.5	981	981.5	982	982.5	983	983.5	984	984.5	985	985.5	986	986.5	987	987.5	988	988.5	989	989.5	990	990.5	991	991.5	992	992.5	993	993.5	994	994.5	995	995.5	996	996.5	997	997.5	998	998.5	999	999.5	1000	1000.5	1001	1001.5	1002	1002.5	1003	1003.5	1004	1004.5	1005	1005.5	1006	1006.5	1007	1007.5	1008	1008.5	1009	1009.5	1010	1010.5	1011	1011.5	1012	1012.5	1013	1013.5	1014	1014.5	1015	1015.5	1016	1016.5	1017	1017.5	1018	1018.5	1019	1019.5	1020	1020.5	1021	1021.5	1022	1022.5	1023	1023.5	1024	1024.5	1025	1025.5	1026	1026.5	1027	1027.5	1028	1028.5	1029	1029.5	1030	1030.5	1031	1031.5	1032	1032.5	1033	1033.5	1034	1034.5	1035	1035.5	1036	1036.5	1037	1037.5	1038	1038.5	1039	1039.5	1040	1040.5	1041	1041.5	1042	1042.5	1043	1043.5	1044	1044.5	1045	1045.5	1046	1046.5	1047	1047.5	1048	1048.5	1049	1049.5	1050	1050.5	1051	1051.5	1052	1052.5	1053	1053.5	1054	1054.5	1055	1055.5	1056	1056.5	1057	1057.5	1058	1058.5	1059	1059.5	1060	1060.5	1061	1061.5	1062	1062.5	1063	1063.5	1064	1064.5	1065	1065.5	1066	1066.5	1067	1067.5	1068	1068.5	1069	1069.5	1070	1070.5	1071	1071.5	1072	1072.5	1073	1073.5	1074	1074.5	1075	1075.5	1076	1076.5	1077	1077.5	1078	1078.5	1079	1079.5	1080	1080.5	1081	1081.5	1082	1082.5	1083	1083.5	1084	1084.5	1085	1085.5	1086	1086.5	1087	1087.5	1088	1088.5	1089	1089.5	1090	1090.5	1091	1091.5	1092	1092.5	1093	1093.5	1094	1094.5	1095	1095.5	1096	1096.5	1097	1097.5	1098	1098.5	1099	1099.5	1100	1100.5	1101	1101.5	1102	1102.5	1103	1103.5	1104	1104.5	1105	1105.5	1106	1106.5	1107	1107.5	1108	1108.5	1109	1109.5	1110	1110.5	1111	1111.5	1112	1112.5	1113	1113.5	1114	1114.5	1115	1115.5	1116	1116.5	1117	1117.5	1118	1118.5	1119	1119.5	1120	1120.5	1121	1121.5	1122	1122.5	1123	1123.5	1124	1124.5	1125	1125.5	1126	1126.5	1127	1127.5	1128	1128.5	1129	1129.5	1130	1130.5	1131	1131.5	1132	1132.5	1133	1133.5	1134	1134.5	1135	1135.5	1136	1136.5	1137	1137.5	1138	1138.5	1139	1139.5	1140	1140.5	1141	1141.5	1142	1142.5	1143	1143.5	1144	1144.5	1145	1145.5	1146	1146.5	1147	1147.5	1148	1148.5	1149	1149.5	1150	1150.5	1151	1151.5	1152	1152.5	1153	1153.5	1154	1154.5	1155	1155.5	1156	1156.5	1157	1157.5	1158	1158.5	1159	1159.5	1160	1160.5	1161	1161.5	1162	1162.5	1163	1163.5	1164	1164.5	1165	1165.5	1166	1166.5	1167	1167.5	1168	1168.5	1169	1169.5	1170	1170.5	1171	1171.5	1172	1172.5	1173	1173.5	1174	1174.5	1175	1175.5	1176	1176.5	1177	1177.5	1178	1178.5	1179	1179.5	1180	1180.5	1181	1181.5	1182	1182.5	1183	1183.5	1184	1184.5	1185	1185.5	1186	1186.5	1187	1187.5	1188	1188.5	1189	1189.5	1190	1190.5	1191	1191.5	1192	1192.5	1193	1193.5	1194	1194.5	1195	1195.5	1196	1196.5	1197	1197.5	1198	1198.5	1199	1199.5	1200	1200.5	1201	1201.5	1202	1202.5	1203	1203.5	1204	1204.5	1205	1205.5	1206	1206.5	1207	1207.5	1208	1208.5	1209	1209.5	1210	1210.5	1211	1211.5	1212	1212.5	1213	1213.5	1214	1214.5	1215	1215.5	1216	1216.5	1217	1217.5	1218	1218.5	1219	1219.5	1220	1220.5	1221	1221.5	1222	1222.5	1223	1223.5	1224	1224.5	1225	1225.5	1226	1226.5	1227	1227.5	1228	1228.5	1229	1229.5	1230	1230.5	1231	1231.5	1232	1232.5	1233	1233.5	1234	1234.5	1235	1235.5	1236	1236.5	1237	1237.5	1238	1238.5	1239	1239.5	1240	1240.5	1241	1241.5	1242	1242.5	1243	1243.5	1244	1244.5	1245	1245.5	1246	1246.5	1247	1247.5	1248	1248.5	1249	1249.5	1250	1250.5	1251	1251.5	1252	1252.5	1253	1253.5	1254	1254.5	1255	1255.5	1256	1256.5	1257	1257.5	1258	1258.5	1259	1259.5	1260	1260.5	1261	1261.5	1262	1262.5	1263	1263.5	1264	1264.5	1265	1265.5	1266	1266.5	1267	1267.5	1268	1268.5	1269	1269.5	1270	1270.5	1271	1271.5	1272	1272.5	1273	1273.5	1274	1274.5	1275	1275.5	1276	1276.5	1277	1277.5	1278	1278.5	1279	1279.5	1280	1280.5	1281	1281.5	1282	1282.5	1283	1283.5	1284	1284.5	1285	1285.5	1286	1286.5	1287	1287.5	1288	1288.5	1289	1289.5	1290	1290.5	1291	1291.5	1292	1292.5	1293	1293.5	1294	1294.5	1295	1295.5	1296	1296.5	1297	1297.5	1298	1298.5	1299	1299.5	1300	1300.5	1301	1301.5	1302	1302.5	1303	1303.5	1304	1304.5	1305	1305.5	1306	1306.5	1307	1307.5	1308	1308.5	1309	1309.5	1310	1310.5	1311	1311.5	1312	1312.5	1313	1313.5	1314	1314.5	1315	1315.5	1316	1316.5	1317	1317.5	1318	1318.5	1319	1319.5	1320	1320.5	1321	1321.5	1322	1322.5	1323	1323.5	1324	1324.5	1325	1325.5	1326	1326.5	1327	1327.5	1328	1328.5	1329	1329.5	1330	1330.5	1331	1331.5	1332	1332.5	1333	1333.5	1334	1334.5	1335	1335.5	1336	1336.5	1337	1337.5	1338	1338.5	1339	1339.5	1340	1340.5	1341	1341.5	1342	1342.5	1343	1343.5	1344	1344.5	1345	1345.5	1346	1346.5	1347	1347.5	1348	1348.5	1349	1349.5	1350	1350.5	1351	1351.5	1352	1352.5	1353	1353.5	1354	1354.5	1355	1355.5	1356	1356.5	1357	1357.5	1358	1358.5	1359	1359.5	1360	1360.5	1361	1361.5	1362	1362.5	1363	1363.5	1364	1364.5	1365	1365.5	1366	1366.5	1367	1367.5	1368	1368.5	1369	1369.5	1370	1370.5	1371	1371.5	1372	1372.5	1373	1373.5	1374	1374.5	1375	1375.5	1376	1376.5	1377	1377.5	1378	1378.5	1379	1379.5	1380	1380.5	1381	1381.5	1382	1382.5	1383	1383.5	1384	1384.5	1385	1385.5	1386	1386.5	1387	1387.5	1388	1388.5	1389	1389.5	1390	1390.5	1391	1391.5	1392	1392.5	1393	1393.5	1394	1394.5	1395	1395.5	1396	1396.5	1397	1397.5	1398	1398.5	1399	1399.5	1400	0	0.91	1.54	1.57	1.73	1.77	1.8800000000000001	1.9100000000000001	2	2.04	2.11	2.12	2.1	2.09	2.1	2.21	2.2200000000000002	2.2000000000000002	2.2000000000000002	2.2000000000000002	2.19	2.19	2.2200000000000002	2.2400000000000002	2.25	2.25	2.2599999999999998	2.2599999999999998	2.2599999999999998	2.2400000000000002	2.2200000000000002	2.2000000000000002	2.21	2.21	2.21	2.2000000000000002	2.19	2.56	3.25	3.4299999999999997	3.57	3.7	3.73	3.73	3.74	3.8	3.79	3.7800000000000002	3.7800000000000002	3.79	3.8	3.8099999999999987	3.86	3.8699999999999997	3.86	3.8299999999999987	3.8	3.8	3.8	3.8099999999999987	3.8099999999999987	3.8099999999999987	3.8099999999999987	3.8	3.7800000000000002	3.77	3.7800000000000002	3.7800000000000002	3.7800000000000002	3.7800000000000002	3.79	3.8299999999999987	3.8499999999999988	3.84	3.84	3.84	3.84	3.84	3.8499999999999988	3.8499999999999988	3.84	3.84	3.84	3.84	3.84	3.8299999999999987	3.72	3.71	4.8599999999999985	5.1599999999999975	5.2700000000000014	5.38	5.44	5.7	6	6.57	7.1	7.41	7.57	7.89	7.99	8.0300000000000011	8.11	8.2100000000000009	8.2000000000000011	8.2100000000000009	8.2800000000000011	8.2900000000000009	8.44	8.43	8.42	8.42	8.42	8.42	8.42	8.43	8.43	8.4500000000000028	8.5500000000000007	8.56	8.56	8.56	8.56	8.56	8.56	8.56	8.56	8.56	8.56	8.5500000000000007	8.5500000000000007	8.5500000000000007	8.5500000000000007	8.5500000000000007	8.5500000000000007	8.5500000000000007	8.5500000000000007	8.5400000000000009	8.52	8.5	8.5	8.5	8.5	8.5	9.6	10.050000000000002	10.79	11.39	11.68	12.07	12.25	12.729999999999999	13.03	13.32	13.53	13.639999999999999	13.78	13.82	13.870000000000006	13.88	13.88	13.88	13.88	13.93	13.950000000000006	13.950000000000006	13.92	13.88	13.870000000000006	13.88	13.9	13.91	13.950000000000006	13.98	13.98	13.98	13.98	13.98	13.96	13.92	13.92	15.03	15.82	16.190000000000001	16.32	16.510000000000005	16.579999999999988	16.7	16.77	16.809999999999999	16.82	16.93	16.979999999999986	17.04	17.07	17.12	17.12	17.12	17.12	17.12	17.149999999999999	17.170000000000005	17.2	17.2	17.2	18.07	18.53	18.95	19.03	19.27	19.47	19.54	19.649999999999999	19.77	19.899999999999999	20	19.989999999999789	20.010000000000005	20.03	20.07	20.100000000000001	20.100000000000001	20.130000000000031	20.14	20.14	20.170000000000005	20.18	20.170000000000005	20.170000000000005	20.18	20.170000000000005	20.16	20.149999999999999	20.149999999999999	20.149999999999999	20.14	20.12	20.130000000000031	20.130000000000031	20.130000000000031	20.130000000000031	20.14	21.37	22.19	22.68	23.29	23.62	24.02	24.19	24.479999999999986	24.69	24.89	25.05	25.150000000000031	25.21	25.39	25.45	25.45	25.54	25.630000000000031	25.73	25.8	25.810000000000031	25.89	25.97	26	26.02	26.07	26.2	26.19	26.259999999999987	26.29	26.36	26.39	26.459999999999987	26.54	27.29	27.79	28.12	28.37	28.62	28.939999999999987	29.02	29.23	29.38	29.47	29.610000000000031	29.66	29.779999999999987	29.830000000000005	29.88	29.97	30	30.130000000000031	30.110000000000031	30.16	30.19	30.259999999999987	30.3	30.36	30.49	30.53	30.830000000000005	31.04	31.150000000000031	31.37	31.56	31.71	32.11	32.410000000000004	32.630000000000003	32.9	33.020000000000003	33.24	33.480000000000004	33.74	33.849999999999994	33.980000000000004	34.090000000000003	34.28	34.39	34.57	34.730000000000011	34.75	34.82	34.949999999999996	35.06	35.08	35.160000000000011	35.25	35.290000000000013	35.42	35.44	35.480000000000004	35.480000000000004	35.58	35.590000000000003	35.67	35.75	35.78	35.790000000000013	35.82	35.96	36.08	36.220000000000013	36.260000000000012	36.33	36.44	36.61	36.64	36.690000000000012	37.18	37.630000000000003	37.9	38.18	38.309999999999995	38.46	38.56	38.800000000000004	39.160000000000011	39.370000000000005	39.520000000000003	39.71	39.809999999999995	40.04	40.17	40.200000000000003	40.300000000000004	40.44	40.550000000000004	40.57	40.590000000000003	40.71	40.770000000000003	40.83	40.92	40.92	40.94	41.09	41.309999999999995	41.43	41.58	41.760000000000012	41.839999999999996	42.03	42.2	42.27	42.37	42.58	42.75	42.75	42.8	42.949999999999996	43.09	43.13	43.21	43.33	43.4	43.52	43.57	43.67	43.790000000000013	43.98	44.05	44.25	44.4	44.43	44.52	44.760000000000012	44.809999999999995	44.92	45.04	45.220000000000013	45.260000000000012	45.339999999999996	45.46	45.57	45.67	45.730000000000011	45.809999999999995	45.87	45.98	46.01	46.18	46.21	46.230000000000011	46.28	46.36	46.39	46.43	46.57	46.6	46.68	46.77	46.879999999999995	46.93	46.97	47.03	47.120000000000012	47.15	47.339999999999996	47.58	47.86	48.09	48.220000000000013	48.379999999999995	48.56	48.720000000000013	48.89	49.07	49.18	49.33	49.48	49.6	49.7	49.78	49.809999999999995	49.94	49.98	50.05	50.1	50.160000000000011	50.32	50.39	50.48	51.14	51.58	52.04	52.28	52.5	52.839999999999996	52.94	53.04	53.15	53.309999999999995	53.349999999999994	53.4	53.51	53.53	53.74	53.77	53.809999999999995	53.94	54	53.99	54.09	54.11	54.17	54.190000000000012	54.290000000000013	54.28	54.32	54.339999999999996	54.42	54.43	54.5	54.51	54.63	54.65	54.67	54.720000000000013	54.86	54.86	54.849999999999994	54.87	54.92	55.03	55.02	55.15	55.56	56.120000000000012	56.48	56.790000000000013	57.08	57.51	57.71	57.86	58.02	58.1	58.21	58.349999999999994	58.51	58.56	58.65	58.730000000000011	58.75	58.760000000000012	58.82	58.82	58.82	58.93	58.93	58.92	58.92	59.01	59.05	59.05	59.05	59.05	59.07	59.18	59.17	59.160000000000011	59.309999999999995	59.339999999999996	59.33	59.33	59.41	59.39	59.44	59.47	59.48	59.55	59.55	59.730000000000011	60.64	61.04	61.449999999999996	61.68	61.91	62.220000000000013	62.3	62.46	62.63	62.720000000000013	62.77	62.94	62.99	63.120000000000012	63.14	63.14	63.17	63.230000000000011	63.260000000000012	63.27	63.27	63.28	63.32	63.32	63.32	63.43	63.43	63.4	63.379999999999995	63.48	63.49	63.49	63.6	63.59	63.57	63.56	63.59	63.65	63.67	63.77	63.78	63.89	63.86	63.86	63.879999999999995	65.5	66.39	66.89	67.3	67.47	67.739999999999995	67.89	68.02	68.149999999999991	68.319999999999993	68.39	68.48	68.55	68.599999999999994	68.72	68.739999999999995	68.75	68.75	68.8	68.84	68.84	68.83	68.81	68.81	68.81	68.81	68.819999999999993	68.819999999999993	68.819999999999993	68.83	68.83	68.81	68.8	68.81	68.819999999999993	68.83	68.83	68.83	68.819999999999993	68.819999999999993	68.819999999999993	68.819999999999993	68.819999999999993	69.27	70.69	70.88	71.22	71.489999999999995	71.739999999999995	71.95	72.03	72.19	72.239999999999995	72.39	72.440000000000026	72.53	72.599999999999994	72.66	72.78	72.78	72.78	72.78	72.78	72.78	72.77	72.77	72.790000000000006	72.790000000000006	74.290000000000006	74.819999999999993	75.099999999999994	75.3	75.540000000000006	75.78	76.010000000000005	76.55	76.88	77.410000000000025	77.64	77.98	78.149999999999991	78.36999999999999	78.58	78.709999999999994	78.92	78.98	79.099999999999994	79.3	79.36999999999999	79.459999999999994	79.58	79.73	79.8	79.86	79.989999999999995	80.03	80.040000000000006	80.040000000000006	80.02	80.02	80.040000000000006	80.05	80.05	80.040000000000006	80.099999999999994	80.14	81.25	81.75	82.11999999999999	82.440000000000026	82.79	82.9	83.02	83.26	83.36	83.440000000000026	83.54	83.57	83.61999999999999	83.66	83.79	83.8	83.79	83.83	84.03	84.2	84.57	84.76	85	85.210000000000022	85.33	85.52	85.740000000000023	85.85	86.149999999999991	86.22	86.34	86.490000000000023	86.649999999999991	86.7	86.89	87.02	87.11	87.210000000000022	87.32	87.5	87.56	87.78	87.86	88.06	88.27	88.43	88.64	88.85	88.98	89.19	89.32	89.47	89.61999999999999	89.710000000000022	89.86999999999999	90	90.08	90.13	90.28	90.34	90.460000000000022	90.56	90.669999999999987	90.73	90.85	90.97	91.01	91.11999999999999	91.19	91.3	91.36999999999999	91.440000000000026	91.51	91.58	91.710000000000022	91.7	91.73	91.82	91.86999999999999	91.990000000000023	92.02	92.09	92.47	92.86999999999999	93.09	93.31	93.55	93.78	94	94.11999999999999	94.38	94.48	94.6	94.8	94.86999999999999	94.98	95.11999999999999	95.35	95.52	95.82	95.990000000000023	96.149999999999991	96.36	96.47	96.63	96.83	96.9	97.05	97.14	97.36999999999999	97.4	97.490000000000023	97.6	97.76	97.81	97.86	97.98	98.169999999999987	98.28	98.48	98.66	98.9	98.97	99.16	99.32	99.440000000000026	99.55	99.66	99.84	99.93	100.14	100.38	100.48	100.57	100.78	100.88	101.06	101.16999999999999	101.35	101.42	101.58	101.76	101.91000000000012	101.93	102.04	102.11	102.28	102.34	102.43	102.47	102.58	102.81	102.95	103.14	103.45	103.56	103.78	104	104.11	104.3	104.47	104.56	104.72	104.93	105.05	105.25	105.5	105.61999999999999	105.85	106.07	106.16999999999999	106.4	106.52	106.66	106.81	106.86	107.03	107.24000000000002	107.35	107.58	107.75	107.93	108.06	108.23	108.43	108.51	108.67999999999998	108.85	108.93	109.05	109.14	109.29	109.36	109.48	109.55	109.61999999999999	109.7	109.86999999999999	109.94000000000032	110.02	110.1	110.14	110.16999999999999	110.27	110.35	110.72	111.31	111.74000000000002	112.07	112.36999999999999	112.61999999999999	112.89	113.03	113.28	113.4	113.53	113.71000000000002	113.91000000000012	114.04	114.3	114.46000000000002	114.57	114.73	114.81	114.85	114.97	115.01	115.05	115.24000000000002	115.27	115.39	115.48	115.5	115.61	115.67999999999998	115.8	115.85	116	116.04	116.03	116.04	116.19	116.3	116.32	116.69	116.81	117.16999999999999	117.35	117.53	117.75	117.99000000000002	118.09	118.25	118.39	118.51	118.61999999999999	118.73	118.86	118.95	119.04	119.13	119.28	119.39	119.49000000000002	119.7	119.82	119.96000000000002	120.14999999999999	120.25	120.42	120.61	120.66999999999999	120.81	120.9	121.04	121.04	121.1	121.33	121.33	121.41000000000012	121.54	121.91000000000012	122.59	122.96000000000002	123.32	123.67999999999998	124.11	124.39	124.67999999999998	124.88	125.22	125.48	125.57	125.77	125.96000000000002	126.07	126.21000000000002	126.29	126.49000000000002	126.56	126.64	126.77	126.86	126.89	126.98	127.09	127.28	127.64	127.96000000000002	128.26	128.57	128.82000000000087	129.02000000000001	129.22999999999999	129.32000000000087	129.41999999999999	129.57	129.81	129.93	130.22	130.36000000000001	130.47	130.75	130.89000000000001	131.07	131.19	131.32000000000087	131.44	131.58000000000001	131.73999999999998	131.79	131.94	131.97999999999999	132.1	132.18	132.20999999999998	132.29	132.4	132.54	132.57	132.62	132.65	132.73999999999998	132.76999999999998	132.89000000000001	132.91999999999999	133	133.12	133.23999999999998	133.25	133.30000000000001	133.44	133.89000000000001	134.68	135.39000000000001	136	136.25	136.46	136.75	136.94999999999999	137.19	137.41	137.5	137.56	137.72	137.88000000000127	137.91	137.96	138.13999999999999	138.15	138.22	138.22	138.26	138.32000000000087	138.46	138.76	139.16999999999999	139.35000000000107	139.57	139.83000000000001	140.05000000000001	140.30000000000001	140.41	140.63	140.76	140.91	141.08000000000001	141.16	141.30000000000001	141.49	141.62	141.83000000000001	142.10999999999999	142.32000000000087	142.54	142.81	143.04	143.30000000000001	143.53	143.63999999999999	143.85000000000107	144.06	144.16999999999999	144.37	144.57	144.68	144.84	145.02000000000001	145.07	145.16	145.26999999999998	145.4	145.5	145.59	145.68	145.72999999999999	145.89000000000001	145.94	146.07	146.13999999999999	146.22999999999999	146.29	146.35000000000107	146.44	146.49	146.53	146.56	146.69	146.68	146.81	146.89000000000001	147	147.06	147.12	147.30000000000001	147.31	147.37	147.44999999999999	147.52000000000001	147.60999999999999	147.66999999999999	147.76	147.87	147.91	148.03	148.12	149.08000000000001	149.66	150.02000000000001	150.39000000000001	150.82000000000087	151.09	151.31	151.41999999999999	151.63	151.81	151.9	152.04	152.10999999999999	152.36000000000001	152.37	152.41999999999999	152.47999999999999	152.56	152.60999999999999	152.72	152.75	152.88000000000127	152.94999999999999	153.06	153.09	153.18	153.26	153.28	153.32000000000087	153.41999999999999	153.47	153.49	153.55000000000001	153.63999999999999	153.66999999999999	153.70999999999998	153.86000000000001	153.88000000000127	153.9	154.02000000000001	154.08000000000001	154.30000000000001	154.73999999999998	154.99	155.30000000000001	155.44999999999999	155.70999999999998	155.99	156.35000000000107	156.66999999999999	156.96	157.13999999999999	157.47999999999999	157.69	157.79	157.97999999999999	158.16	158.20999999999998	158.33000000000001	158.43	158.58000000000001	158.65	158.72999999999999	158.83000000000001	158.88000000000127	158.97	159.02000000000001	159.1	159.19	159.22	159.32000000000087	159.39000000000001	159.44	159.51	159.88000000000127	160.26	160.59	160.83000000000001	161.16	161.38000000000127	161.51	161.66	161.97999999999999	162.26	162.59	162.69	162.87	163.06	163.16	163.28	163.41	163.57	163.59	163.76999999999998	163.85000000000107	164.02	164.07	164.3	164.32000000000087	164.41	164.5	164.67	164.73	164.78	164.92000000000004	164.97	165.13	165.15	165.20999999999998	165.32000000000087	165.43	165.5	165.9	166.32000000000087	166.72	166.95000000000007	167.28	167.64	167.82000000000087	168.05	168.23	168.37	168.62	168.72	168.83	169.03	169.1	169.19	169.34	169.5	169.53	169.6	169.7	169.83	169.9	169.97	170.04	170.1	170.25	170.26999999999998	170.32000000000087	170.45000000000007	170.5	170.55	170.69	170.7	170.76	170.86	170.92000000000004	171.06	171.31	171.69	172.09	172.42000000000004	172.8	172.95000000000007	173.2	173.5	173.82000000000087	174.22	174.41	174.6	174.83	174.98000000000027	175.22	175.35000000000107	175.47	175.66	175.73999999999998	175.82000000000087	175.93	176.06	176.12	176.25	176.32000000000087	176.45000000000007	176.47	176.55	176.67	176.78	176.81	176.87	176.97	177.01	177.05	177.15	177.18	177.3	177.42000000000004	177.45000000000007	177.47	177.59	177.6	177.95000000000007	178.23	178.65	178.91	179.16	179.47	179.58	179.73999999999998	179.99	180.07	180.25	180.48000000000027	180.75	180.96	181.16	181.33	181.5	181.67	181.76	181.96	182.03	182.2	182.3	182.44	182.46	182.58	182.67	182.70999999999998	182.85000000000107	182.9	182.98000000000027	183.07	183.20999999999998	183.31	183.36	183.44	183.51	183.60999999999999	183.67	183.8	183.85000000000107	184	184.04	184.06	184.19	184.23	184.28	184.67	184.95000000000007	185.32000000000087	185.5	185.79	186.16	186.26	186.43	186.55	186.72	186.83	186.95000000000007	187.15	187.20999999999998	187.31	187.44	187.58	187.60999999999999	187.79	187.9	188.02	188.14	188.28	188.4	188.56	188.73	188.96	189.20999999999998	189.36	189.53	189.72	189.86	190.01	190.18	190.28	190.47	190.67	190.70999999999998	190.83	190.91	191.12	191.18	191.26	191.38000000000127	191.62	191.78	191.94	192.19	192.32000000000087	192.5	192.69	192.82000000000087	192.97	193.19	193.34	193.56	193.67	193.87	194.05	194.23	194.42000000000004	194.59	194.66	194.8	194.98000000000027	195.13	195.20999999999998	195.32000000000087	195.48000000000027	195.55	195.72	195.94	196.05	196.22	196.51	196.59	196.78	196.98000000000027	197.15	197.39000000000001	197.63	197.9	198.05	198.25	198.5	198.73	198.96	199.07	199.32000000000087	199.44	199.59	199.65	199.86	200	200.14	200.28	200.36	200.54	200.60999999999999	200.78	200.92000000000004	201	201.08	201.26999999999998	201.36	201.45000000000007	201.58	201.76	201.86	202.10999999999999	202.41	202.56	202.73999999999998	202.97	203.10999999999999	203.26	203.47	203.62	203.81	203.89000000000001	204.07	204.23	204.28	204.49	204.66	204.72	204.9	205.07	205.14	205.26	205.32000000000087	205.44	205.52	205.65	205.78	205.87	205.91	206.14	206.26999999999998	206.41	206.7	206.85000000000107	207.03	207.2	207.31	207.5	207.58	207.78	207.88000000000127	208.07	208.23999999999998	208.36	208.51	208.69	208.72	208.73999999999998	208.98000000000027	209.08	209.12	209.29	209.48000000000027	209.54	209.84	209.93	210.17	210.45000000000007	210.7	211.01	211.3	211.53	211.78	211.95000000000007	212.20999999999998	212.47	212.69	212.92000000000004	213.19	213.36	213.55	213.76999999999998	214.06	214.10999999999999	214.26999999999998	214.49	214.56	214.64	214.87	214.96	215.06	215.23999999999998	215.35000000000107	215.58	215.60999999999999	215.66	215.78	215.94	216.05	216.15	216.26999999999998	216.38000000000127	216.44	216.63	216.79	216.86	217.14	217.23	217.45000000000007	217.70999999999998	217.96	218.20999999999998	218.45000000000007	218.53	218.73999999999998	218.94	219.06	219.19	219.32000000000087	219.5	219.64	220.01	220.16	220.38000000000127	220.63	220.73999999999998	220.91	221.12	221.25	221.49	221.6	221.73999999999998	221.94	222.05	222.18	222.23999999999998	222.39000000000001	222.46	222.62	222.78	222.94	223.07	223.23999999999998	223.44	223.59	223.8	223.96	224.12	224.37	224.46	224.58	224.7	224.86	224.95000000000007	225.14	225.20999999999998	225.31	225.36	225.58	225.76	225.96	226.12	226.31	226.52	226.67	226.95000000000007	227.09	227.2	227.39000000000001	227.5	227.60999999999999	227.81	227.87	227.99	228.2	228.31	228.45000000000007	228.59	228.72	228.88000000000127	229.01	229.17	229.34	229.41	229.52	229.65	229.82000000000087	229.89000000000001	230.04	230.19	230.28	230.32000000000087	230.44	230.6	230.73999999999998	230.94	231.23999999999998	231.63	231.86	232.1	232.33	232.45000000000007	232.65	232.84	232.96	233.2	233.26	233.37	233.53	233.7	233.81	233.92000000000004	234.07	234.16	234.23999999999998	234.33	234.75	234.96	235.3	235.49	235.76	235.97	236.04	236.34	236.42000000000004	236.6	236.81	236.87	236.96	237.07	237.23999999999998	237.29	237.38000000000127	237.51	237.65	237.70999999999998	237.76999999999998	237.88000000000127	238	238.01	238.05	238.17	238.23	238.35000000000107	238.38000000000127	238.46	238.56	238.6	238.70999999999998	238.70999999999998	239.13	239.34	239.67	239.82000000000087	239.97	240.16	240.25	240.42000000000004	240.59	240.65	240.76999999999998	240.96	241.16	241.26	241.47	241.69	241.78	241.96	242.1	242.19	242.28	242.36	242.42000000000004	242.58	242.6	242.8	242.82000000000087	242.8	242.82000000000087	242.92000000000004	243.09	243.10999999999999	243.16	243.20999999999998	243.28	243.32000000000087	243.47	243.54	243.96	244.28	244.48000000000027	244.7	244.95000000000007	245.1	245.23999999999998	245.47	245.53	245.73	245.81	246	246.22	246.23	246.33	246.43	246.6	246.64	246.7	246.78	246.83	246.85000000000107	246.87	247.02	247.05	247.15	247.29	247.42000000000004	247.48000000000027	247.55	247.72	247.85000000000107	247.99	249.1	250.07	250.45000000000007	250.85000000000107	251.25	251.44	251.64	251.85000000000107	252.06	252.3	252.37	252.42000000000004	252.47	252.57	252.73	252.89000000000001	252.91	253.01	Time (s)
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