Supporting Information

Hypercrosslinked PolyHIPEs as Precursors to Designable, Hierarchically Porous Carbon Foams.

Robert T. Woodward*, Arthur Jobbe-Duval, Sofia Marchesini, David B. Anthony, Camille Petit and Alexander Bismarck

Figure S1 N2 uptake isotherms for polyHIPEs containing varying ratios of styrene:divinylbenzene.

Figure S2 Photograph of HCLHIPEs. From left-right, HCL(ST98-DVB2)HIPE, HCL(ST90-DVB10)HIPE, HCL(ST80-DVB20)HIPE, HCL(ST50-DVB50)HIPE and HCL(DVB100)HIPE.

Figure S3 Nitrogen sorption isotherms of  HCLHIPEs, a) HCL(ST98-DVB2)HIPE, b) HCL(ST90-DVB10)HIPE, c) HCL(ST80-DVB20)HIPE, d) HCL(ST50-DVB50)HIPE and e) HCL(DVB100)HIPE.

Figure S4 Pore size distributions of HCLHIPEs.

Figure S5 Scanning electron micrographs of hypercrosslinked samples  a) HCL(ST98-DVB2)HIPE, b) HCL(ST90-DVB10)HIPE, c) HCL(ST80-DVB20)HIPE, d) HCL(ST50-DVB50)HIPE and e) HCL(DVB100)HIPE. Scale bars represent 5 μm.

Figure S6 XPS surveys of a) HCL(DVB)HIPE and b) a carboHIPE derived from a HCL(DVB)HIPE.

Figure S7 Scanning electron micrographs of carbonized polyHIPE samples a) poly(ST50-co-DVB50)HIPE and b) poly(DVB)HIPE, in which the emulsion-templated macropores were destroyed. Scale bars represent 20 μm.

Table S1 Volume changes for all materials after both hypercrosslinking and carbonization of hypercrosslinked materials.

|  | Volume change after hypercrosslinking (%)a | Volume change after carbonization (%)a | Volume change after carbonization (%)b |
| --- | --- | --- | --- |
| poly(ST98-DVB2)HIPE | +33 | -42 | -57 |
| poly(ST90-DVB10)HIPE | +32 | -53 | -65 |
| poly(ST80-DVB20)HIPE | +25 | -71 | -77 |
| poly(ST50-DVB50)HIPE | +7 | -78 | -80 |
| poly(DVB)HIPE | -1 | -77 | -77 |
| aRelative to the volume of the initial polyHIPE. bRelative to the volume of the HCLHIPE |  |  |  |

Table S2 CHN analysis of HCLHIPEs and carboHIPEs showing increased carbon content post-carbonization.

|  | C (%) | H (%) | N (%) | C : H |
| --- | --- | --- | --- | --- |
| HCL(ST98-DVB2)HIPE | 75.30 | 5.77 | 0.42 | 13.1 : 1 |
| HCL(ST90-DVB10)HIPE | 79.81 | 6.25 | 0.15 | 12.8 : 1 |
| HCL(ST80-DVB20)HIPE | 82.40 | 6.58 | 0.11 | 12.5 : 1 |
| HCL(ST50-DVB50)HIPE | 81.19 | 6.69 | 0.12 | 12.1 : 1 |
| HCL(DVB)HIPE | 82.84 | 7.22 | 0.27 | 11.5 : 1 |
| carbo(ST98-DVB2)HIPE | 93.53 | 0.90 | 0.36 | 104.4 : 1 |
| carbo(ST90-DVB10)HIPE | 93.87 | 0.97 | 0.46 | 96.8 : 1 |
| carbo(ST80-DVB20)HIPE | 94.22 | 0.59 | 0.10 | 159.7 : 1 |
| carbo(ST50-DVB50)HIPE | 91.27 | 0.59 | 0.11 | 154.7 : 1 |
| carbo(DVB)HIPE | 90.85 | 0.74 | 0.37 | 122.8 : 1 |