Progress and Prospect of Anodic Oxidation for the Remediation of Per- and Polyfluoroalkyl Substances in Water and Wastewater using Diamond Electrodes

Sean T. McBeath1,5, Adrián Serrano Mora2, Fatemeh Asadi Zeidabadi3, Brooke K. Mayer4, Patrick McNamara4, Madjid Mohseni3, Michael R. Hoffmann1, Nigel J.D. Graham5

1 Linde Laboratories, California Institute of Technology, Pasadena, California, USA

2 Escuela de Ingeniería Química, Universidad de Costa Rica, San José, Costa Rica

3 Department of Chemical and Biological Engineering, University of British Columbia, Vancouver, Canada

4 Department of Civil, Construction and Environmental Engineering, Marquette University, Milwaukee, WI USA

5 Department of Civil & Environmental Engineering, Imperial College London, London, UK

ABSTRACT

While diamond electrodes are widely utilized in the field of electro-analysis and sensing, their application in the field of environmental engineering has yet to be fully realized. Many research studies have considered their potential application in water and wastewater treatment, where the in-situ electrochemical process can avoid the need for chemical additives by facilitating the oxidation of pollutants on the electrode surface or mediated by electrochemically synthesized oxidants in solution. Diamond-based electro-oxidation can effectively treat a number of organic micropollutants and is now being evaluated for the abatement of per- and polyfluoroalkyl substances (PFAS), which pose health concerns and are ubiquitous recalcitrant environmental contaminants. To move implementation of diamond-based electro-oxidation forward, the integration of modifications and co-dopants to yield more advanced electrode materials needs to be further developed and understood. The progress and current strategies associated with diamond electrode modifications for PFAS abatement, as well as future considerations are discussed.

Keywords: boron-doped diamond; electro-oxidation; wastewater; water treatment; PFAS

Introduction

Per- and polyfluoroalkyl substances (PFAS) are a wide class of synthetic chemicals, characterized by an aliphatic carbon backbone with fluorine atom substitutions on the alkyl chain. Although PFAS species have been widely manufactured for various industrial applications since the early 1950s, it was not until 2001 that definitive data, published in literature, documented their adverse health impacts and widespread contamination on a global scale [1]. PFAS are now known to be highly toxic, with many harmful health effects to humans [2–4], leading many governments across the world to impose strict health-based notification levels [5]. PFAS have an extremely wide range of applications, including as a mist suppressant agent for carcinogenic aerosols [6], aqueous film-forming foams, surfactants and lubricants [7], and are also present in various household products such as carpets, clothing and non-stick cookware [8]. PFAS are known to be chemically stable and resistant to biodegradation, as well as recalcitrant to conventional treatment processes [5,9–11], leading to the accumulation of perfluorinated compounds in the environment, wildlife and humans [11,12]. The ubiquity of PFAS in natural waters has rendered them among the most hazardous environmental contaminants and priority substances for monitoring by the European Union Directive 2013/39/EU [13].

PFAS have proven to be recalcitrant towards conventional oxidation processes like ozone [14], with much research dedicated to other treatment processes such as UV photolysis [15–20] and sonochemical degradation [21–23], amongst many others [24,25]. In environmentally relevant circumneutral pH conditions, PFAS recalcitrance can be attributed to the presence of fluorine atoms (i.e., …-CF2-CF2-…). Moreover, in advanced oxidation processes, hydroxyl radicals attack the hydrogen bonds in organics; however, this mechanism cannot proceed with PFAS given the lack of hydrogens to abstract, rendering it relatively inert to hydroxyl radical-mediated oxidation [26].

At present, electrochemical processes are being widely pursued as a viable technology for efficient remediation of PFAS due to their ability to facilitate direct oxidation at the electrode-electrolyte interface. In particular, diamond electrodes like boron-doped diamond (BDD) are receiving heightened attention due to their favorable properties for water and wastewater treatment applications [27], enabling a substantially more efficient process due to their wide potential range of water stability (-1.25-2.3 VSHE [28]). Moreover, BDD has been observed to be resistant to degradation in chemically, mechanically and thermally adverse conditions [28–33]. The use of BDD for electro-oxidation has been evaluated for a large number of organic micropollutants in recent years [34–37], which has captured the attention of many researchers for applications towards PFAS remediation. The following review describes the current state of the art and considers the future research and prospects of diamond electrodes to help address the crisis of environmental PFAS contamination.

State of the Art

The efficacy of BDD electrodes for the abatement of PFAS has been widely reported (see summary in Table 1), including investigations of the effects of typical electrochemical process variables, such as current density, supporting electrolyte type and concentration, electrolysis time, hydrodynamic conditions (flowrate/stir speed) and kinetics, amongst others [38–42]. These studies were conducted in various aqueous media, including surface water [43], ground water [44–46] and industrial wastewater [38,39,47–49]. Like BDD electro-oxidation processes targeting other organic micropollutants, its effective oxidative performance is largely attributed to its rapid charge-transfer kinetics, low background current, weak adsorption properties, chemical inertness, and wide electro-potential window [28]. In general, PFAS oxidation via BDD electro-oxidation is a mass transfer limited process, which proceeds primarily through direct oxidation at the electrode surface [50,51], rather than mediated by •OH oxidation. This has been demonstrated previously, whereby PFOS degradation was unaffected when the •OH scavenger tert-butanol was present during electrolysis [52], indicating the effectiveness of diamond electrodes for PFAS degradation in the presence of co-occurring organic scavengers in the water matrix. The mechanism of degradation via electro-oxidation is dependent on the specific PFAS species, however general pathways have been observed [53,54] (Figure 1). Due to its recalcitrance towards •OH attack, the initial decomposition of PFAS is attributed to direct oxidation [50], whereby an electron is transferred from the carboxyl or sulfonic acid group at the electrode to form a perfluorinated radical (CnF2n+1COO•/CnF2n+1SO3•) [55]. Subsequently, this radical undergoes decarboxylation or desulfonation to form a perfluoroakyl radical (CnF2n+1•), which is then susceptible to defluorination by reactions with •OH, O2 and H2O, as well as via direct oxidation [54].

Figure 1. Mechanism of PFAS degradation using electrochemical oxidation. Cycle I: O2, Cycle II: •OH, Cycle III: H2O.

Due to their recalcitrance towards •OH, electro-oxidation of PFAS is slow when compared to other organic micropollutants, like pesticides [34]. This •OH inertness is attributed to the high electronegativity of the fluorine atoms in PFAS species. Dehalogenation of PFAS by electrochemical reduction at the cathode has previously been observed [26,56–58], thereby increasing the susceptibility of products to subsequent oxidation at the anode [26]. Reductive activity at the cathode ceases once dehalogenation occurs, whereby electro-oxidation is required for any further degradation. This has also been widely reported with other halogenated chemicals [59–64].

Table 1. Experimental studies concerning the effects of operational parameters on PFAS electrochemical degradation by BDD anode.

(CD: Current density, C: Initial PFAS concentration, EC: Electrolyte concentration, t: Treatment time, P: Potential, x: Electrode gap, n: Stirrer speed, Q: Flow rate, T: Temperature)

| PFAS | Parameters investigated, unit (levels) | Experimental condition | Results | Ref. |
| --- | --- | --- | --- | --- |
| PFOA | CD, mA cm-2 (2.3, 11.85, 21.4) C, mg L-1 (1, 5.5, 10) EC (Na2SO4), g L-1 (1.5, 7.85, 14.2) t, h (1, 2.5, 4) | Factorial experiment Batch mode experiment Anode: Nb/BDD (35.05 cm2) Cathode: Nb/BDD (21.57 cm2) x: 2 cm | - CD and t were the most important factors for PFOA degradation and F- generation. - High EC had negative effect on generation of F-. But it had no significant impact on PFOA degradation. - C had slight negative effect on degradation, while it had insignificant effect on F-generation. | [38] |
| PFOA | P, V(1.5, 2, 2.5, 3, 3.5, 4) CD, mA cm-2(0.12, 0.59, 5.88, 17.64, 23.24) pH, (3, 9, 12) C, mg L-1 (20, 30, 50) | Batch mode experiments (three-electrode quartz cell) Anode: Si/BDD (8.5 cm2) Cathode: Ti sheet (8.5 cm2) Reference electrode: SCE x: 3 cm T: 32 °C EC (NaClO4): 1.4 g L-1 n: 1500 r min-1 | - PFOA decomposition was higher at acidic pH and high anodic P, CD, and C. | [50] |
| F-53B | Anode type (BDD, BDD/SnO2, BDD/PbO2, BDD/SnO2-F) F and Sn ratio (0:1, 1:1, 2:1) CD, mA cm-2 (5, 15, 20, 30) pH (3, 7, 9) C, mg L-1 (10, 20, 100) Electrolyte type (NaCl, Na2SO4, NaClO4) EC (NaCl), mol L-1 (0.5, 1, 2.5) x, cm (0.5, 1, 1.5, 2) | n: 800 r min-1 T: 40 °C Cathode: Pt sheet (2.25 cm2) Reference electrode: SCE | - BDD/SnO2-F had the highest oxidation ability for F-53B. - With increasing the ratio of F varying from 0:1 (F:Sn) to 2:1, the removal ratios of F-53 increased. - F-53B removal ratio was greater at acidic conditions, and at higher CD and C. - The effect of electrolyte on F-53B degradation was in the order of NaCl>Na2SO4> NaClO4. - A very high and very small x had negative effect on F-53B degradation. | [65] |
| PFOA PFHxS PFOS | Electrical connectors resistivity (Ti wire), Ω (7, 9) CD, mA cm-2 (1.8, 20, 27, 40) | Electrolytes: NaCl+Na2SO4 Anode: Si/BDD (78.5 cm-2) Cathode = Ti sheet (78.5 cm-2) x: 3 cm | - Increasing the CD enhanced PFAS removal. - Low resistance (7 Ω) demonstrated higher removal efficiency for all PFAS with low energy consumption. | [41] |
| PFOA | Standard CDa, mA cm-2 (1, 5, 10, 25, 50) Combined CDb, mA cm-2 (50/1, 50/5, 50/10) | Anode: Nb/BDD (105 cm-2) Cathode: Nb/BDD x: 3 mm EC (Na2SO4): 50 mM | - In standard CD, increasing the CD increased rate constant. However, the higher current was only beneficial in the first 15 min of the process. - In combined CD, 50/5 mA cm-2 combination allowed for a 37% reduction in energy usage to obtain 75% defluorination compared to using 50 mA cm-2 alone. - Combined CD of 50/5 mA cm-2 had great promise in a simulated ion exchange regeneration solution. | [40] |
| PFNA PFDA | Anode type (Ti/SnO2-Sb-Ce, Ti/SnO2-Sb/Ce-PbO2, BDD) | Cathode: Ti electrode x: 1.5 cm EC (NaClO4): 10 mmol L-1 CD: 10 mA cm-2 n: 800 r min-1 T: 25 °C | - BDD had the best performance in the degradation, defluorination and TOC removal of both PFAS compared to modified PbO2 and SnO2 electrodes. | [42] |
| PFOA | Cathode type (BDD, Pt, Zr, Stainless steel) | Q: 360 L h-1 T: 25 °C Anode: Si/BDD (63 cm2) x: 10 mm EC (Na2SO4): 3.5 mmol L-1 pH: 4 CD: 7.9 mA cm-2 | - Among all cathodes tested, Pt acted as an electrocatalyst and improved the defluorination reaction by the reduction reaction of perfluorinated carbonyl intermediates on the cathode. | [56] |

a: Standard CD means using one single CD from the beginning to the end of experiment.

b: Combined CD means using 50 mA/cm2 for the first 15 min followed by a lower CD for the rest of experiments.

While electro-reduction can increase PFAS degradation, substantial research has been dedicated recently to exploring variables to maximize electro-oxidation using diamond anodes via direct electron transfer at the electrode-solution interface. Gomez-Ruiz et al. [66] compared the effect of surface and crystalline features of two commercial BDD anodes on their electrochemical performance for perfluorooctanoic acid (PFOA) electrolysis: ultra-nanocrystalline diamond (UNCD) and microcrystalline diamond (MCD) electrodes. Results showed that MCD yielded a sharp abatement of PFOA independently of the applied current density (1-5 mA/cm2). In comparison, the UNCD anode provided significantly slower PFOA degradation kinetics. Moreover, the energy requirements for maximum PFOA degradation using the MCD anode was 37-fold lower than that of UNCD. The higher sp3 carbon content, lower boron level, and H-terminated carbon content of the MCD appeared to favor faster PFOA degradation. Alternatively, the ultra-nanocrystalline surface features and higher conductivity of the UNCD anode limited the electrochemical activity for PFOA electrolysis [66].

Pierpaoli et al. [67] compared the efficacy of two BDD electrodes with different boron contents (0.5k ppm and 10k ppm) in degrading PFOA and perfluorooctanesulfonic acid (PFOS) in landfill leachates. Although low boron-doped BDD showed a greater reduction in chemical oxygen demand, both BDDs performed similarly for the removal of PFOA and PFOS, indicating that boron-doping did not significantly affect PFAS removal efficiency. Moreover, the background current analysis showed that the recorded working potential window was 2.6 and 3.1 VAg/AgCl for 10k and 0.5k ppm electrodes, respectively. The slightly narrower potential window was due to higher carrier concentration in the higher doped electrode [67]. No clear trend regarding the effect of boron doping levels has been universally established for anodic oxidation processes for water and wastewater treatment applications. Previous research has attributed higher boron-doping concentrations to an increased number of crystallites with small diameter on the surface, and consequently a greater density of active sites, leading to better oxidation performance for azo dyes [68]. In contrast, greater oxidation and degradation of the herbicide tebuthiuron resulted using lower boron-doping (5k ppm) due to decreased incorporation of impurities in the diamond lattice during chemical vapor deposition [69].

The treatment and selectivity of multiple mixed PFAS species using BDD anodes have been an area of recent research interest. Gomez-Ruiz et al. investigated the electro-oxidation of 6:2 fluorotelomer sulfonamide alkylbetaine (6:2 FTAB) and 6:2 fluorotelomer sulfonate (6:2 FTSA), with six other short-chain perfluorocarboxylic acids (PFCAs) in industrial wastewater effluent [70]. The oxidation of the larger chain 6:2 FTAB molecule was kinetically favorable over the shorter chain 6:2 FTSA and PFCAs molecules. Similarly, the simultaneous BDD electro-oxidation of 12 PFCAs, consisting of both short (C3-C6) and long (C7-C18) chains, was investigated in a variety of water matrices (deionized water, raw surface water and wastewater treatment effluent) [71]. Once again, PFAS chain length was found to affect oxidation selectivity, whereby larger species were kinetically favored.

To enhance the primarily direct oxidation mediated process, some researchers have explored the coupling of other processes with that of diamond electrode oxidation. Two recent research studies have investigated the efficacy of BDD electro-oxidation of PFHxA [72] and GenX [73] in concentrated nanofiltration retentate. Aside from optimizing process parameters (i.e., current density, transport phenomena, reactor design, etc.) and the addition of supplemental treatment technologies like nanofiltration, other aspects related to diamond electrode materials, such as material modifiers and co-dopants, are now being explored to further increase their applicability as a viable treatment option for PFAS remediation.

Future Outlook

Doped-diamond electrodes are fabricated mainly through chemical vapor deposition or high pressure, high temperature particle production. Other methods include vacuum annealing and surface transfer doping of undoped diamond [28]. Recently, modifications to BDD have been investigated to improve the electrochemical activity (i.e., electrooxidation, electrocatalytic performance, extended solvent window) (see Table 2). Zhuo et al. (2020) utilized SnO2, PbO2 and SnO2-F as BDD modifiers to investigate the removal of F-53B, a substitute for PFOS [65]. The reported OER potentials for the modified electrodes were 2.35, 2.30 and 2.25 V vs SCE for the BDD-SnO2-F, BDD-SnO2 and BDD-PbO2, respectively. When compared to BDD, all modified electrodes exhibited improved removals of F-53B. However, BDD-SnO2-F demonstrated the greatest performance, with a removal of 95.6% after 30 min of electrolysis (30 mA cm-2, pH=3, 40 °C). In comparison, removal of 91 and 87% was achieved when using the BDD-SnO2 and BDD-PbO2 electrodes, respectively. The authors proposed that a significant level of free •OH exists in solution due to the repelling effect caused by F electronegativity on the •OH formed on the electrode surface. Consequently, this repelling effect could make more active sites available at the electrode surface to facilitate the direct oxidation of PFAS. In fact, removal of F-53B with a 2:1 F:SnO2 electrode was 1.14 and 1.21 times higher than that observed with a 1:1 and 0:1 F:SnO2 ratio, respectively.

Liu et al. (2019) observed an increase in PFOA removal when a boron and nitrogen co-doped diamond (BND) electrode was used compared to conventional BDD and nitrogen doped diamond (NDD) electrodes [74]. Although all materials showed similar morphology, oxygen evolution potential, and an identical crystal structure, PFOA reductions of 85.3 and 78.6 % were achieved with the BDD and NDD, respectively (4 mA cm-2, 0.05 M Na2SO4, pH0 = 4.8), while a reduction of 99% was achieved using BND. On average, removal of PFOA with BND electrodes was 1.3 and 1.6 times higher than those observed with BDD and NDD electrodes, respectively. The improved performance of BND over BDD and NDD was attributed to a greater electron transfer rate arising from the boron and nitrogen co-doping effect. Moreover, BND also exhibited increased kinetics for PFOA degradation via sulfate activation. Previous research concerning the co-doping of boron and nitrogen on graphene and nano-diamond demonstrated that a synergistic coupling enhanced the catalytic performance of the electrode [75–77]. Boron and nitrogen doping adjusts the electronic structure of carbon materials, which enables the formation of defect-induced active sites for electrochemical activity [76].

Table 2. Summary of recent modified and co-doped BDD PFAS oxidation research.

| PFAS | Co-dopant or Modification | OER | Reaction rate constant, k/(s-1) | Reference |
| --- | --- | --- | --- | --- |
| PFOA | Amount of boron doping (500 and 10 000 ppm) | ~2.4 V vs Ag/AgCl (500 ppm) ~2.1 V vs Ag/AgCl (10 000 ppm) | 5.55 x10-5 (j = 75 mA cm-2; 500 ppm) 2.26 x10-5 (j = 25 mA cm-2; 500 ppm) 5.67 x10-5 (j = 75 mA cm-2; 10 000 ppm) 1.78 x10-5 (j = 25 mA cm-2; 10 000 ppm) | [67] |
| PFOS |  |  | 5.85 x10-5 (j = 75 mA cm-2; 500 ppm) 4.80 x10-5 (j = 75 mA cm-2; 10 000 ppm) 2.38 x10-5 (j = 25 mA cm-2; 10 000 ppm) |  |
| PFOA | MCD | ~2.4 V | 3.52 x10-4 (j = 5 mA cm-2) 4.55 x10-4 (j = 2 mA cm-2) 4.88 x10-4 (j = 1 mA cm-2) | [66] |
|  | UNCD | ~2 V | 1.31 x10-4 (j = 20 mA cm-2) 7.29 x10-5 (j = 10 mA cm-2) 1.63 x10-5 (j = 5 mA cm-2) |  |
| PFOA | Boron-Nitrogen codoped diamond | ~2.1 V vs SCE | 9.44 x10-5 (j =0.5 mA cm-2) 1.92 x10-4 (j =1.0 mA cm-2) 3.17 x10-4 (j =2.0 mA cm-2) 5.36 x10-4 (j =3.0 mA cm-2) 6.67 x10-4 (j =4.0 mA cm-2) | [74] |
|  | Nitrogen doped diamond | ~2.2 V vs SCE | 2.81 x10-4 (j =4.0 mA cm-2) |  |
| F-53B | BDD/SnO2 | 2.25 V vs SCE | 1.07 x10-3 (30 mA cm-2) | [65] |
|  | BDD/PbO2 | 2.30 V vs SCE | 1.24 x10-3 (30 mA cm-2) |  |
|  | BDD-SnO2-F | 2.35 V vs SCE | 1.83 x10-3 (30 mA cm-2) 1.20 x10-3 (20 mA cm-2) 1.16 x10-3 (15 mA cm-2) 8.45 x10-4 (5 mA cm-2) |  |

In general, the co-oxidation and generation of chemical oxidants for water treatment applications by BDD is a promising area of research [78], and has also been investigated for enhanced PFAS degradation during electro-oxidation. The circum-neutral generation of ferrate from low concentration Fe2+ in synthetic ground water during a BDD electro-oxidation process was recently observed to significantly increase PFOS degradation [79]. Moreover, increased oxidation of PFOS was observed in chloride-containing waters due to the electrosynthesis of Cl•, as well as chlorate (ClO3-) and perchlorate (ClO4-) by-products [80]. Another study found, that by using hydrogen peroxide as a Cl- and •OH scavenger, ClO4- (an endocrine disruptor) generation could be inhibited without impairing PFOS and PFOA degradation (due to the primary pathway of direct oxidation) [81]. This process of coupling electrosynthesis and electro-oxidation is worthy of further research investigation.

Other potential areas of interest for future applications of diamond electrodes for the treatment of PFAS contaminants exist beyond the use of co-dopants, modifiers, and co-generation of electrolyte-derived oxidant species as described above. The development of porous and 3D electrodes with larger reactive surface areas more active sites [82,83] should provide for more efficient PFAS degradation. However, the use of porous diamond electrodes has yet to be pursued for PFAS remediation applications, in contrast to investigations of PFAS treatment with Ti4O7-based porous electrodes [84]. With increased active sites, however, it would be important to also investigate reactor design to maximize PFAS diffusion to the electrode surface. Moreover, integrating nanomaterials into electrodes can lead to a higher surface area, which may improve reaction rates on electrode surfaces [85]. Finally, advances in molecularly imprinted polymer (MIP) electrodes are key to enhancing the efficiency of electrochemical systems by increasing PFAS selectivity. However, to date, the majority of MIP electrode research has been directed towards the field of sensors [86,87], thus their use for PFAS degradation efficacy mostly unexplored.

Conclusion

At present, the use of BDD electrodes for water/wastewater treatment is confined to relatively small-scale applications. Cost reduction [34,88], increased oxidation selectivity and reactor design [89,90], are important challenges to address to enable their scale-up and application. Further development and application of BDD electro-oxidation technologies could assuage the challenge presented by PFAS contamination of the environment. While recent scientific and technological advances in this area have been significant, further research opportunities exist to improve process effectiveness. In particular, modifications and co-dopants for advanced electrode materials can help increase the current efficiency of the electro-oxidation process. Moreover, innovation in the area of porous electrode design may further increase the applicability of the process for PFAS treatment in water and wastewater.

Acknowledgements

This work was supported, in whole or in part, by the Bill & Melinda Gates Foundation [INV003227]. Under the grant conditions of the Foundation, a Creative Commons Attribution 4.0 Generic License has already been assigned to the Author Accepted Manuscript version that might arise from this submission.

References

[1]	J.P. Giesy, K. Kannan, Global distribution of perfluorooctane sulfonate in wildlife, Environ. Sci. Technol. (2001). https://doi.org/10.1021/es001834k.

[2]	X. Shi, Y. Du, P.K.S. Lam, R.S.S. Wu, B. Zhou, Developmental toxicity and alteration of gene expression in zebrafish embryos exposed to PFOS, Toxicol. Appl. Pharmacol. (2008). https://doi.org/10.1016/j.taap.2008.01.043.

[3]	F. Chen, C. Wei, Q. Chen, J. Zhang, L. Wang, Z. Zhou, M. Chen, Y. Liang, Internal concentrations of perfluorobutane sulfonate (PFBS) comparable to those of perfluorooctane sulfonate (PFOS) induce reproductive toxicity in Caenorhabditis elegans, Ecotoxicol. Environ. Saf. (2018). https://doi.org/10.1016/j.ecoenv.2018.04.032.

[4]	N. Yin, R. Yang, S. Liang, S. Liang, B. Hu, T. Ruan, F. Faiola, Evaluation of the early developmental neural toxicity of F-53B, as compared to PFOS, with an in vitro mouse stem cell differentiation model, Chemosphere. (2018). https://doi.org/10.1016/j.chemosphere.2018.04.011.

[5]	D. Lu, S. Sha, J. Luo, Z. Huang, X. Zhang Jackie, Treatment train approaches for the remediation of per- and polyfluoroalkyl substances (PFAS): A critical review, J. Hazard. Mater. 386 (2020) 121963. https://doi.org/10.1016/j.jhazmat.2019.121963.

[6]	M. Pilat, R. Pegnam, Particle emissions from chrome plating, Aerosol Sci. Technol. 40 (2006) 639–648. https://doi.org/10.1080/02786820600763020.

[7]	C.A. Moody, J.A. Field, Perfluorinated surfactants and the environmental implications of their use in fire-fighting foams, Environ. Sci. Technol. (2000). https://doi.org/10.1021/es991359u.

[8]	S. Fujii, C. Polprasert, S. Tanaka, N.P.H. Lien, Y. Qiu, New POPs in the water environment: Distribution, bioaccumulation and treatment of perfluorinated compounds - A review paper, J. Water Supply Res. Technol. - AQUA. (2007). https://doi.org/10.2166/aqua.2007.005.

[9]	K.H. Kucharzyk, R. Darlington, M. Benotti, R. Deeb, E. Hawley, Novel treatment technologies for PFAS compounds: A critical review, J. Environ. Manage. 204 (2017) 757–764. https://doi.org/10.1016/j.jenvman.2017.08.016.

[10]	B.N. Nzeribe, M. Crimi, S. Mededovic Thagard, T.M. Holsen, Physico-Chemical Processes for the Treatment of Per- And Polyfluoroalkyl Substances (PFAS): A review, Crit. Rev. Environ. Sci. Technol. 49 (2019) 866–915. https://doi.org/10.1080/10643389.2018.1542916.

[11]	M.F. Rahman, S. Peldszus, W.B. Anderson, Behaviour and fate of perfluoroalkyl and polyfluoroalkyl substances (PFASs) in drinking water treatment: A review, Water Res. 50 (2014) 318–340. https://doi.org/10.1016/j.watres.2013.10.045.

[12]	F. Suja, B.K. Pramanik, S.M. Zain, Contamination, bioaccumulation and toxic effects of perfluorinated chemicals (PFCs) in the water environment: A review paper, Water Sci. Technol. (2009). https://doi.org/10.2166/wst.2009.504.

[13]	L. Bu, S. Zhu, S. Zhou, Degradation of atrazine by electrochemically activated persulfate using BDD anode: Role of radicals and influencing factors, Chemosphere. 195 (2018) 236–244. https://doi.org/10.1016/j.chemosphere.2017.12.088.

[14]	A.Y.C. Lin, S.C. Panchangam, C.Y. Chang, P.K.A. Hong, H.F. Hsueh, Removal of perfluorooctanoic acid and perfluorooctane sulfonate via ozonation under alkaline condition, J. Hazard. Mater. 243 (2012) 272–277. https://doi.org/10.1016/j.jhazmat.2012.10.029.

[15]	Y. Gu, T. Liu, Q. Zhang, W. Dong, Efficient decomposition of perfluorooctanoic acid by a high photon flux UV/sulfite process: Kinetics and associated toxicity, Chem. Eng. J. 326 (2017) 1125–1133. https://doi.org/10.1016/j.cej.2017.05.156.

[16]	P. Gu, C. Zhang, Z. Sun, H. Zhang, Q. Zhou, S. Lin, J. Rong, M.R. Hoffmann, Enhanced photoreductive degradation of perfluorooctanesulfonate by UV irradiation in the presence of ethylenediaminetetraacetic acid, Chem. Eng. J. 379 (2020). https://doi.org/10.1016/j.cej.2019.122338.

[17]	X.J. Lyu, W.W. Li, P.K.S. Lam, H.Q. Yu, Insights into perfluorooctane sulfonate photodegradation in a catalyst-free aqueous solution, Sci. Rep. 5 (2015) 1–6. https://doi.org/10.1038/srep09353.

[18]	X.J. Lyu, W.W. Li, P.K.S. Lam, H.Q. Yu, Photodegradation of perfluorooctane sulfonate in environmental matrices, Sep. Purif. Technol. 151 (2015) 172–176. https://doi.org/10.1016/j.seppur.2015.07.049.

[19]	Y. Dai, X. Guo, S. Wang, L. Yin, M.R. Hoffmann, Photochemical transformation of perfluoroalkyl acid precursors in water using engineered nanomaterials, Water Res. 181 (2020) 115964. https://doi.org/10.1016/j.watres.2020.115964.

[20]	Z. Sun, C. Zhang, P. Chen, Q. Zhou, M.R. Hoffmann, Impact of humic acid on the photoreductive degradation of perfluorooctane sulfonate (PFOS) by UV/Iodide process, Water Res. 127 (2017) 50–58. https://doi.org/10.1016/j.watres.2017.10.010.

[21]	H. Cao, W. Zhang, C. Wang, Y. Liang, Sonochemical degradation of poly- and perfluoroalkyl substances – A review, Ultrason. Sonochem. 69 (2020) 105245. https://doi.org/10.1016/j.ultsonch.2020.105245.

[22]	J. Cheng, C.D. Vecitis, H. Park, B.T. Mader, M.R. Hoffmann, Sonochemical degradation of perfluorooctane sulfonate (PFOS) and perfluorooctanoate (PFOA) in groundwater: Kinetic effects of matrix inorganics, Environ. Sci. Technol. 44 (2010) 445–450. https://doi.org/10.1021/es902651g.

[23]	J. Cheng, C.D. Vecitis, H. Park, B.T. Mader, M.R. Hoffmann, Sonochemical degradation of perfluorooctane sulfonate (PFOS) and perfluorooctanoate (PFOA) in landfill groundwater: Environmental matrix effects, Environ. Sci. Technol. 42 (2008) 8057–8063. https://doi.org/10.1021/es8013858.

[24]	S. Garg, J. Wang, P. Kumar, V. Mishra, H. Arafat, R.S. Sharma, L.F. Dumée, Remediation of water from per-/poly-fluoroalkyl substances (PFAS) - Challenges and perspectives, J. Environ. Chem. Eng. 9 (2021). https://doi.org/10.1016/j.jece.2021.105784.

[25]	N. Merino, Y. Qu, R.A. Deeb, E.L. Hawley, M.R. Hoffmann, S. Mahendra, Degradation and Removal Methods for Perfluoroalkyl and Polyfluoroalkyl Substances in Water, Environ. Eng. Sci. 33 (2016) 615–649.

[26]	C.D. Vecitis, H. Park, J. Cheng, B.T. Mader, M.R. Hoffmann, Treatment technologies for aqueous perfluorooctanesulfonate (PFOS) and perfluorooctanoate (PFOA), Front. Environ. Sci. Eng. China. 3 (2009) 129–151. https://doi.org/10.1007/s11783-009-0022-7.

[27]	B.P. Chaplin, Critical review of electrochemical advanced oxidation processes for water treatment applications, Environ. Sci. Process. Impacts. 16 (2014) 1182–1203. https://doi.org/10.1039/C3EM00679D.

[28]	A. Kraft, Doped diamond: A compact review on a new, versatile electrode material, Int. J. Electrochem. Sci. 2 (2007) 355–385. https://doi.org/10.1242/jeb.00516.

[29]	G.M. Swain, The Susceptibility to Surface Corrosion in Acidic Fluoride Media: A Comparison of Diamond, HOPG, and Glassy Carbon Electrodes, J. Electrochem. Soc. 141 (1994) 3382. https://doi.org/10.1149/1.2059343.

[30]	Q. Chen, M.C. Granger, T.E. Lister, G.M. Swain, Morphological and microstructural stability of boron-doped diamond thin film electrodes in an acidic chloride medium at high anodic current densities, J. Electrochem. Soc. 144 (1997) 3806. https://doi.org/10.1149/1.1838096.

[31]	T.N. Rao, A. Fujishima, Recent advances in electrochemistry of diamond, Diam. Relat. Mater. 9 (2000) 384–389. https://doi.org/10.1016/S0925-9635(99)00234-4.

[32]	M. Fryda, T. Matthée, S. Mulcahy, A. Hampel, L. Schäfer, I. Tröster, Fabrication and application of Diachem® electrodes, Diam. Relat. Mater. 12 (2003) 1950–1956. https://doi.org/10.1016/S0925-9635(03)00261-9.

[33]	M. Panizza, G. Cerisola, Application of diamond electrodes to electrochemical processes, Electrochim. Acta. 51 (2005) 191–199. https://doi.org/10.1016/j.electacta.2005.04.023.

[34]	S.T. McBeath, D.P. Wilkinson, N.J.D. Graham, Application of Boron-Doped Diamond Electrodes for the Anodic Oxidation of Pesticide Micropollutants in a Water Treatment Process: A Critical Review, Environ. Sci. Water Res. Technol. 5 (2019) 2090–2107. https://doi.org/10.1039/C9EW00589G.

[35]	C.A. Martínez-Huitle, M. Panizza, Electrochemical oxidation of organic pollutants for wastewater treatment, Curr. Opin. Electrochem. 11 (2018) 62–71. https://doi.org/10.1016/j.coelec.2018.07.010.

[36]	A. Urtiaga, Electrochemical technologies combined with membrane filtration, Curr. Opin. Electrochem. 27 (2021) 100691. https://doi.org/10.1016/j.coelec.2021.100691.

[37]	X. Yu, M. Zhou, Y. Hu, K. Groenen Serrano, F. Yu, Recent updates on electrochemical degradation of bio-refractory organic pollutants using BDD anode: A mini review, Environ. Sci. Pollut. Res. 21 (2014) 8417–8431. https://doi.org/10.1007/s11356-014-2820-0.

[38]	J.N. Uwayezu, I. Carabante, T. Lejon, P. van Hees, P. Karlsson, P. Hollman, J. Kumpiene, Electrochemical degradation of per- and poly-fluoroalkyl substances using boron-doped diamond electrodes, J. Environ. Manage. 290 (2021) 112573. https://doi.org/10.1016/j.jenvman.2021.112573.

[39]	B. Gomez-Ruiz, S. Gómez-Lavín, N. Diban, V. Boiteux, A. Colin, X. Dauchy, A. Urtiaga, Boron doped diamond electrooxidation of 6:2 fluorotelomers and perfluorocarboxylic acids. Application to industrial wastewaters treatment, J. Electroanal. Chem. 798 (2017) 51–57. https://doi.org/10.1016/j.jelechem.2017.05.033.

[40]	M. Ensch, C.A. Rusinek, M.F. Becker, T. Schuelke, A combined current density technique for the electrochemical oxidation of perfluorooctanoic acid (PFOA) with boron-doped diamond, Water Environ. J. 35 (2021) 158–165. https://doi.org/10.1111/wej.12616.

[41]	S. Sukeesan, N. Boontanon, S.K. Boontanon, Improved electrical driving current of electrochemical treatment of Per- and Polyfluoroalkyl Substances (PFAS) in water using Boron-Doped Diamond anode, Environ. Technol. Innov. 23 (2021) 101655. https://doi.org/10.1016/j.eti.2021.101655.

[42]	H. Lin, J. Niu, J. Xu, H. Huang, D. Li, Z. Yue, C. Feng, Highly Efficient and Mild Electrochemical Mineralization of Long-Chain Perfluorocarboxylic Acids (C9−C10) by Ti/SnO2−Sb−Ce, Ti/SnO2−Sb/Ce−PbO2 and Ti/BDD Electrodes, Environ. Sci. Technol. 47 (2013) 13039–13046. https://doi.org/dx.doi.org/10.1021/es4034414.

[43]	S. Barisci, R. Suri, Electrooxidation of short and long chain perfluorocarboxylic acids using boron doped diamond electrodes, Chemosphere. 243 (2020) 125349. https://doi.org/10.1016/j.chemosphere.2019.125349.

[44]	C.E. Schaefer, S. Choyke, P.L. Ferguson, C. Andaya, A. Burant, A. Maizel, T.J. Strathmann, C.P. Higgins, Electrochemical Transformations of Perfluoroalkyl Acid (PFAA) Precursors and PFAAs in Groundwater Impacted with Aqueous Film Forming Foams, Environ. Sci. Technol. 52 (2018) 10689–10697. https://doi.org/10.1021/acs.est.8b02726.

[45]	A.M. Trautmann, H. Schell, K.R. Schmidt, K.M. Mangold, A. Tiehm, Electrochemical degradation of perfluoroalkyl and polyfluoroalkyl substances (PFASs) in groundwater, Water Sci. Technol. 71 (2015) 1569–1575. https://doi.org/10.2166/wst.2015.143.

[46]	A. Soriano, C. Schaefer, A. Urtiaga, Enhanced treatment of perfluoroalkyl acids in groundwater by membrane separation and electrochemical oxidation, Chem. Eng. J. Adv. 4 (2020) 100042. https://doi.org/10.1016/j.ceja.2020.100042.

[47]	Á. Soriano, D. Gorri, L.T. Biegler, A. Urtiaga, An optimization model for the treatment of perfluorocarboxylic acids considering membrane preconcentration and BDD electrooxidation, Water Res. 164 (2019). https://doi.org/10.1016/j.watres.2019.114954.

[48]	C. Zhang, J. Tang, C. Peng, M. Jin, Degradation of perfluorinated compounds in wastewater treatment plant effluents by electrochemical oxidation with Nano-ZnO coated electrodes, J. Mol. Liq. 221 (2016) 1145–1150. https://doi.org/10.1016/j.molliq.2016.06.093.

[49]	S. Barisci, R. Suri, Electrooxidation of short and long chain perfluorocarboxylic acids using boron doped diamond electrodes, Chemosphere. 243 (2020). https://doi.org/10.1016/j.chemosphere.2019.125349.

[50]	Q. Zhuo, S. Deng, B. Yang, J. Huang, B. Wang, T. Zhang, G. Yu, Degradation of perfluorinated compounds on a boron-doped diamond electrode, Electrochim. Acta. 77 (2012) 17–22. https://doi.org/10.1016/j.electacta.2012.04.145.

[51]	K.E. Carter, J. Farrell, Oxidative destruction of perfluorooctane sulfonate using boron-doped diamond film electrodes, Environ. Sci. Technol. 42 (2008) 6111–6115. https://doi.org/10.1021/es703273s.

[52]	C.E. Schaefer, C. Andaya, A. Burant, C.W. Condee, A. Urtiaga, T.J. Strathmann, C.P. Higgins, Electrochemical treatment of perfluorooctanoic acid and perfluorooctane sulfonate: Insights into mechanisms and application to groundwater treatment, Chem. Eng. J. 317 (2017) 424–432. https://doi.org/10.1016/j.cej.2017.02.107.

[53]	J. Radjenovic, N. Duinslaeger, S.S. Avval, B.P. Chaplin, Facing the Challenge of Poly- And Perfluoroalkyl Substances in Water: Is Electrochemical Oxidation the Answer?, Environ. Sci. Technol. 54 (2020) 14815–14829. https://doi.org/10.1021/acs.est.0c06212.

[54]	J. Niu, Y. Li, E. Shang, Z. Xu, J. Liu, Electrochemical oxidation of perfluorinated compounds in water, Chemosphere. 146 (2016) 526–538. https://doi.org/10.1016/j.chemosphere.2015.11.115.

[55]	H. Lin, J. Niu, S. Ding, L. Zhang, Electrochemical degradation of perfluorooctanoic acid (PFOA) by Ti/SnO2-Sb, Ti/SnO2-Sb/PbO2 and Ti/SnO2-Sb/MnO2 anodes, Water Res. 46 (2012) 2281–2289. https://doi.org/10.1016/j.watres.2012.01.053.

[56]	A.L. Garcia-Costa, A. Savall, J.A. Zazo, J.A. Casas, K.G. Serrano, On the role of the cathode for the electro-oxidation of perfluorooctanoic acid, Catalysts. 10 (2020) 1–14. https://doi.org/10.3390/catal10080902.

[57]	E. Mousset, K. Doudrick, A review of electrochemical reduction processes to treat oxidized contaminants in water, Curr. Opin. Electrochem. 22 (2020) 221–227. https://doi.org/10.1016/j.coelec.2020.07.008.

[58]	Y. Su, U. Rao, C.M. Khor, M.G. Jensen, L.M. Teesch, B.M. Wong, D.M. Cwiertny, D. Jassby, Potential-Driven Electron Transfer Lowers the Dissociation Energy of the C-F Bond and Facilitates Reductive Defluorination of Perfluorooctane Sulfonate (PFOS), ACS Appl. Mater. Interfaces. 11 (2019) 33913–33922. https://doi.org/10.1021/acsami.9b10449.

[59]	G.D. Sayles, G. You, M. Wang, M.J. Kupferle, DDT, DDD, and DDE dechlorination by zero-valent iron, Environ. Sci. Technol. (1997). https://doi.org/10.1021/es9701669.

[60]	H.K. Yak, B.W. Wenclawiak, I.F. Cheng, J.G. Doyle, C.M. Wai, Reductive dechlorination of polychlorinated biphenyls by zerovalent iron in subcritical water, Environ. Sci. Technol. (1999). https://doi.org/10.1021/es981066l.

[61]	C.G. Jones, J. Silverman, M. Al-Sheikhly, P. Neta, D.L. Poster, Dechlorination of Polychlorinated Biphenyls in Industrial Transformer Oil by Radiolytic and Photolytic Methods, Environ. Sci. Technol. (2003). https://doi.org/10.1021/es030412i.

[62]	D.C. Hinz, C.M. Wai, B.W. Wenclawiak, Remediation of a nonachloro biphenyl congener with zero-valent iron in subcritical water, J. Environ. Monit. (2000). https://doi.org/10.1039/a908026k.

[63]	W.X. Zhang, Nanoscale iron particles for environmental remediation: An overview, J. Nanoparticle Res. (2003). https://doi.org/10.1023/A:1025520116015.

[64]	C.B. Wang, W.X. Zhang, Synthesizing nanoscale iron particles for rapid and complete dechlorination of TCE and PCBs, Environ. Sci. Technol. (1997). https://doi.org/10.1021/es970039c.

**[65]	Q. Zhuo, J. Wang, J. Niu, B. Yang, Y. Yang, Electrochemical oxidation of perfluorooctane sulfonate (PFOS) substitute by modified boron doped diamond (BDD) anodes, Chem. Eng. J. 379 (2020) 122280. https://doi.org/10.1016/j.cej.2019.122280.

This study presents one of the first investigations focused on the use of modified BDD electrodes for the degradation of PFAS. Using SnO2, PbO2 and SnO2-F as BDD modifiers for the removal of F-53B, improved oxidation was observed using all modified electrodes due to the increase active sites on the electrode surface to facilitate the direct oxidation

**[66]	B. Gomez-Ruiz, N. Diban, A. Urtiaga, Comparison of microcrystalline and ultrananocrystalline boron doped diamond anodes: Influence on perfluorooctanoic acid electrolysis, Sep. Purif. Technol. 208 (2019) 169–177. https://doi.org/10.1016/j.seppur.2018.03.044.

Using both UNCD and MCD boron-doped diamond anodes, the authors provided one of the first comparative studies of the effect of crystalline structures on PFOA oxidation; sp3 carbon content, boron levels and H-terminated carbon content discussed.

**[67]	M. Pierpaoli, M. Szopińska, B.K. Wilk, M. Sobaszek, A. Łuczkiewicz, R. Bogdanowicz, S. Fudala-Książek, Electrochemical oxidation of PFOA and PFOS in landfill leachates at low and highly boron-doped diamond electrodes, J. Hazard. Mater. 403 (2021). https://doi.org/10.1016/j.jhazmat.2020.123606.

The boron-doping levels and its effect on PFOA and PFOS oxidation was investigated. This presents the first comprehensive study on boron concentrations in BDD electrodes, and their relative effect on PFAS degradation.

[68]	R. Bogdanowicz, A. Fabiańska, L. Golunski, M. Sobaszek, M. Gnyba, J. Ryl, K. Darowicki, T. Ossowski, S.D. Janssens, K. Haenen, E.M. Siedlecka, Influence of the boron doping level on the electrochemical oxidation of the azo dyes at Si/BDD thin film electrodes, Diam. Relat. Mater. 39 (2013) 82–88. https://doi.org/10.1016/j.diamond.2013.08.004.

[69]	S.A. Alves, T.C.R. Ferreira, N.S. Sabatini, A.C.A. Trientini, F.L. Migliorini, M.R. Baldan, N.G. Ferreira, M.R.V. Lanza, A comparative study of the electrochemical oxidation of the herbicide tebuthiuron using boron-doped diamond electrodes, Chemosphere. 88 (2012) 155–160. https://doi.org/10.1016/j.chemosphere.2012.02.042.

[70]	B. Gomez-Ruiz, S. Gómez-Lavín, N. Diban, V. Boiteux, A. Colin, X. Dauchy, A. Urtiaga, Efficient electrochemical degradation of poly- and perfluoroalkyl substances (PFASs) from the effluents of an industrial wastewater treatment plant, Chem. Eng. J. 322 (2017) 196–204. https://doi.org/10.1016/j.cej.2017.04.040.

*[71]	S. Barisci, R. Suri, Electrooxidation of short and long chain perfluorocarboxylic acids using boron doped diamond electrodes, Chemosphere. 243 (2020) 125349. https://doi.org/10.1016/j.chemosphere.2019.125349.

This study presents a thorough investigation of the BDD electro-oxidation of a mixture of 12 PFAS, both short- and long-chains species. In addition to using a variety of water matrices, it provides a comparative analysis of oxidation efficiency towards the various PFAS species

[72]	Á.S. Portilla, E.G. Cirella, A.U. Mendia, Efficient treatment of perfluorohexanoic acid by nanofiltration followed by electrochemical degradation of the NF concentrate, Water Res. 112 (2017) 147–156. https://doi.org/10.1016/j.watres.2017.01.043.

[73]	N.E. Pica, J. Funkhouser, Y. Yin, Z. Zhang, D.M. Ceres, T. Tong, J. Blotevogel, Electrochemical Oxidation of Hexafluoropropylene Oxide Dimer Acid (GenX): Mechanistic Insights and Efficient Treatment Train with Nanofiltration, Environ. Sci. Technol. 53 (2019) 12602–12609. https://doi.org/10.1021/ACS.EST.9B03171.

[74]	Y. Liu, X. Fan, X. Quan, Y. Fan, S. Chen, X. Zhao, Enhanced Perfluorooctanoic Acid Degradation by Electrochemical Activation of Sulfate Solution on B/N Codoped Diamond, Environ. Sci. Technol. 53 (2019) 5195–5201. https://doi.org/10.1021/acs.est.8b06130.

This paper presents one of the first examples of the use of modified diamond electrodes with co-dopants for the electrochemical degradation of PFAS. The research presented by the authors demonstrated the increased effect boron and nitrogen co-dopants have on the oxidation of PFAS, when compared to conventional BDD electrodes

[75]	Y. Zheng, Y. Jiao, L. Ge, M. Jaroniec, S.Z. Qiao, Two-step boron and nitrogen doping in graphene for enhanced synergistic catalysis, Angew. Chemie - Int. Ed. 52 (2013) 3110–3116. https://doi.org/10.1002/anie.201209548.

[76]	Y. Liu, Y. Zhang, K. Cheng, X. Quan, X. Fan, Y. Su, S. Chen, H. Zhao, Y. Zhang, H. Yu, M.R. Hoffmann, Selective Electrochemical Reduction of Carbon Dioxide to Ethanol on a Boron- and Nitrogen-Co-doped Nanodiamond, Angew. Chemie - Int. Ed. 56 (2017) 15607–15611. https://doi.org/10.1002/anie.201706311.

[77]	L.S. Panchakarla, K.S. Subrahmanyam, S.K. Saha, A. Govindaraj, H.R. Krishnamurthy, U. V. Waghmare, C.N.R. Rao, Synthesis, structure, and properties of boron- and nitrogen-doped graphene, Adv. Mater. 21 (2009) 4726–4730. https://doi.org/10.1002/adma.200901285.

[78]	S.T. McBeath, J.T. English, D.P. Wilkinson, N.J.D. Graham, Circumneutral electrosynthesis of ferrate oxidant: An emerging technology for small, remote and decentralised water treatment applications, Curr. Opin. Electrochem. 27 (2021) 100680. https://doi.org/10.1016/j.coelec.2020.100680.

*[79]	S.T. McBeath, N.J.D. Graham, Degradation of perfluorooctane sulfonate via in-situ electro-generated ferrate and permanganate oxidants in NOM-rich source waters, Environ. Sci. Water Res. Technol. (2021). https://doi.org/10.1039/D1EW00399B.

This study presents the first example of a simultaneous electro-oxidation and electro-generation process for the circumneutral synthesis of ferrate (Fe(VI)). The relative effect of BDD electro-oxidation, as well as the enhanced affect due to ferrate oxidation is investigated, as well as the effect of co-occurring scavengers (NOM).

[80]	L. Wang, J. Lu, L. Li, Y. Wang, Q. Huang, Effects of chloride on electrochemical degradation of perfluorooctanesulfonate by Magnéli phase Ti4O7 and boron doped diamond anodes, Water Res. 170 (2020) 115254. https://doi.org/10.1016/j.watres.2019.115254.

[81]	S. Yang, S. Fernando, T.M. Holsen, Y. Yang, Inhibition of Perchlorate Formation during the Electrochemical Oxidation of Perfluoroalkyl Acid in Groundwater, Environ. Sci. Technol. Lett. 6 (2019) 775–780. https://doi.org/10.1021/acs.estlett.9b00653.

[82]	R. Mei, Q. Wei, C. Zhu, W. Ye, B. Zhou, L. Ma, Z. Yu, K. Zhou, 3D macroporous boron-doped diamond electrode with interconnected liquid flow channels: A high-efficiency electrochemical degradation of RB-19 dye wastewater under low current, Appl. Catal. B Environ. 245 (2019) 420–427. https://doi.org/10.1016/j.apcatb.2018.12.074.

[83]	C. Hébert, E. Scorsone, M. Mermoux, P. Bergonzo, Porous diamond with high electrochemical performance, Carbon N. Y. 90 (2015) 102–109. https://doi.org/10.1016/j.carbon.2015.04.016.

[84]	G. Liu, H. Zhou, J. Teng, S. You, Electrochemical degradation of perfluorooctanoic acid by macro-porous titanium suboxide anode in the presence of sulfate, Chem. Eng. J. 371 (2019) 7–14. https://doi.org/10.1016/j.cej.2019.03.249.

[85]	M. Yence, A. Cetinkaya, G. Ozcelikay, S.I. Kaya, S.A. Ozkan, Boron-Doped Diamond Electrodes: Recent Developments and Advances in View of Electrochemical Drug Sensors, Crit. Rev. Anal. Chem. (2020). https://doi.org/10.1080/10408347.2020.1863769.

[86]	B. Feier, A. Blidar, A. Pusta, P. Carciuc, C. Cristea, Electrochemical sensor based on molecularly imprinted polymer for the detection of cefalexin, Biosensors. 9 (2019). https://doi.org/10.3390/bios9010031.

[87]	R. Kazemi, E.I. Potts, J.E. Dick, Quantifying Interferent Effects on Molecularly Imprinted Polymer Sensors for Per- A nd Polyfluoroalkyl Substances (PFAS), Anal. Chem. 92 (2020) 10597–10605. https://doi.org/10.1021/acs.analchem.0c01565.

[88]	K. Wenderich, B.A.M. Nieuweweme, G. Mul, B.T. Mei, Selective Electrochemical Oxidation of H2O to H2O2Using Boron-Doped Diamond: An Experimental and Techno-Economic Evaluation, ACS Sustain. Chem. Eng. 9 (2021) 7803–7812. https://doi.org/10.1021/acssuschemeng.1c01244.

[89]	M.A. Cataldo-Hernández, A. Bonakdarpour, J.T. English, M. Mohseni, D.P. Wilkinson, A membrane-based electrochemical flow reactor for generation of ferrates at near neutral pH conditions, React. Chem. Eng. 4 (2019) 1116–1125. https://doi.org/10.1039/c8re00306h.

[90]	S. Varigala, S. Krishnaswamy, C.P. Lohia, M. Hegarty-Craver, S. Grego, M. Luettgen, C.A. Cid, Optimal design of an electrochemical reactor for blackwater treatment, Water Environ. Res. 93 (2021) 148–158. https://doi.org/10.1002/wer.1374.